G.M. SEITMAGZIMOVA, ZH.K. DZHANMULDAYEVA

STUDY GUIDE

FOR LABORATORY WORKS ON THE DISCIPLINE

“GENERAL CHEMICAL TECHNOLOGY’’

Shymkent 2015

MINISTRY OF EDUCATION AND SCIENCE OF THE REPUBLIC OF KAZAKHSTAN

M. AUEZOV SOUTH KAZAKHSTAN STATE UNIVERSITY

G.M. Seitmagzimova, Zh.K. Dzhanmuldayeva

STUDY GUIDE

FOR LABORATORY WORKS ON THE DISCIPLINE

“GENERAL CHEMICAL TECHNOLOGY’’

for Students of Specialties

5В072000, 5В072100, 5В075300, 5В060600

Shymkent 2015

UDK 378(075.8):66

BBK 35я7

Seitmagzimova G.M., Dzhanmuldayeva Zh.K. Study Guide for Laboratory Works on the Discipline “General Chemical Technology”. - Shymkent: M. Auezov South Kazakhstan State University, 2015. - 104p.

Study guide represents a re-edition of the Study Guide for Laboratory Works on the Discipline “General Chemical Technology” edited in 2007 by authors Seitmagzimova G.M. and Dzhanmuldayeva Zh.K. It includes three newly developed laboratory works. The study guide contains theoretical bases of typical technological processes, techniques of lab carrying out, calculation of process indicators and control questions for every laboratory work defense. The study guide is composed according to the contents of the study program for basic elective discipline “General chemical technology”.

The study guide is designated for students of 5В072000, 5В072100, 5В075300, 5В060600 specialties of any form of training.

Reviewers:

Head of the Scientific-Technical Department of the private corporation “KAZNIICHIMPROJECT”, Candidate of Technical Science, Seitmagzimova L.A.

Head of the Department “Petrochemistry and Petroleum Products” of M. Auezov SKSU, Associate professor, Candidate of Technical Science Sakibayeva S.A.

Associate professor of the “Biotechnology” Department of M. Auezov SKSU, Candidate of Technical  Science , Mamitova A.D.

The study guide is recommended for print by Study-Methodical Council of M. Auezov South Kazakhstan State University (protocol #   dated from          2015).

©  M. Auezov South  Kazakhstan State University, 2015

TABLE OF CONTENTS

| PREFACE………………………………………………………………… | 4 |
| --- | --- |
| Recommendations for students to prepare for lab classes……………...... | 4 |
| Requirements for lab report completion ………………………………… | 5 |
| Goal and objectives of laboratory classes……………………………….. | 5 |
| Contents of laboratory classes ………………………………………….. | 5 |
| #1 laboratory work “Caustic soda production by electrochemical method” …………………………………………………………………. | 7 |
| #2 laboratory work “Caustification of soda solution” ……….……......... | 17 |
| #3 laboratory work “Electrochemical copper plating” …………………. | 31 |
| #4 laboratory work “Technical analysis of solid fuel” …………………. | 39 |
| #5 laboratory work “Determination of water quality indicators”………. | 46 |
| #6 laboratory work “Studying the heterogeneous process of pyrite roasting” ………………………………………………………………….. | 53 |
| #7 laboratory work “Polycondensation of phenol with formaldehyde”… | 60 |
| #8 laboratory work “Methods of corrosion testing” ……………………. | 70 |
| #9 laboratory work “Studying the filtration process for sewage purification” …………………………………………………………….. | 79 |
| #10 laboratory work “Water softening by chemical method” …………... | 85 |
| #11 laboratory work “Water softening by ion exchange method”………. | 91 |
| REFERENCES ………………………………………………………….. | 98 |

PREFACE

The base elective discipline “General Chemical Technology” has the great importance in training bachelors of specialties 5В072000 – Chemical Technology of Inorganic Substances, 5В072100 – Chemical Technology of Organic Substances, 5В075300 – Chemical Technology of Refractory Non-metallic and Silicate Materials, 5В060600 – Chemistry.

This discipline consists of a lecture course and laboratory classes. Laboratory classes are a vital part of the discipline studying. Skills of experimental and calculated analysis of technological processes are being developed; general regularities of the process behaviour are being learnt and being mastered at lab classes. On this basis optimal conditions of a process are being chosen, general indicators characterizing the technological process efficiency are being calculated.

The study guide covers the whole course content and consists of 11 labs. Each lab description includes the aim of the lab, theoretical data about a process under studying, the plant scheme and description, the technique of work and analysis carrying out, the order of calculation of technological process indicators as well as control questions and safety precautions. Students must fulfill 8 works during the academic period according to the assignment and due to the lab themes in each module given in the syllabus.

The study guide is composed in accordance with the contents of the study programs on the discipline “General chemical technology” and according to requirements of the M. Auezov SKSU procedure 7.03.2012.

RECOMMENDATIONS FOR STUDENTS TO PREPARE

TO LAB CLASSES

At the first lab class students are acquainted with safety precautions for the work in a chemical laboratory. These precautions must be strictly observed when every lab carrying out. Laboratory works are carried out by groups of 2-3 students after access getting. This access provides for knowledge of the technique of lab carrying out, the plant scheme and the technique of technological calculations. After the lab completing every student calculates required process indicators according to the assignment, makes conclusions of the process efficiency, makes up a report and defends work results.

Most of laboratory works are research ones; while these carrying out the students study the process condition influence on technological indicators and the product quality. #2 and #7 labs are virtual ones and they are performed using computing programs in the “Technological processes and apparatuses” department laboratory. Thereat all parts of the work including tests of an access and work defense are performed in the virtual form.

REGULATIONS FOR THE LAB REPORT EXECUTION

The report is being composed according to the requirements of M. Auezov SKSU procedure 7.04.2012. - “Training classes. General requirement to classes’ management, content and performance” and being executed as a manuscript or in А4 printed form.

The report includes a title, a name of the lab, work aims, the technique of experiments and analyses, the lab plant scheme, experimental data, technological calculations of process indicators and product quality and a conclusion concerning research results’ justification.

The report defense includes to prepare and to answer the control questions of knowledge of theoretical bases of the technological processes. The questions are given for every lab. Students receive the report on #2 lab in the printed form after successful virtual lab program completing.

THE GOAL AND OBJECTIVES OF LABORATORY CLASSES

The goal of laboratory classes is to solidify and to deepen knowledge of acquired theoretical knowledge in the course of experiments, to master practical skills of laboratory research performance and an analysis of lab results.

Objectives of laboratory classes:

- to master the technique and to acquire an experience of performance of technological process experimental research using up-to-date computer technologies;

- to acquire skill of exploitation of technical means and laboratory equipment;

- to form skill of experimental data treatment, work result execution and presentation;

- to develop creativities and independence at analyses of research results and formulation of conclusions of the process efficiency.

CONTENTS OF LABORATORY CLASSES

Lab classes are being kept according to the contents of a syllabus and a course program of the discipline and they cover all sections of the “General chemical technology” course.

Table 1. Themes of laboratory works

| Lab # | Num-ber of hours | Names of modules and labs | Forms and methods of the lab process | Control form |
| --- | --- | --- | --- | --- |
| Module 1. Theoretical bases of chemical technology |  |  |  |  |
| 5 | 2 | Determination of water quality indicators | Analytical | Report on the lab and defense |
| 8 | 2 | Methods of corrosion testing | Research | Report on the lab and defense |
| 10 | 2 | Water softening by chemical method | Analytical | Report on the lab and defense |
| 9 | 2 | Studying the filtration process for sewage purification | Research | Report on the lab and defense |
| 11 | 1 | Water softening by ion exchange method | Research | Report on the lab and defense |
| Module 2. Typical chemical productions |  |  |  |  |
| 1 | 2 | Caustic soda production by electrochemical method | Research | Report on the lab and defense |
| 2 | 2 | Caustification of soda solution | Virtual lab | Computing report |
| 3 | 2 | Electrochemical copper plating | Research | Report on the lab and defense |
| 4 | 2 | Technical analysis of solid fuel | Analytical | Report on the lab and defense |
| 6 | 2 | Studying the heterogeneous process of pyrite roasting | Research | Report on the lab and defense |
| 7 | 2 | Polycondensation of phenol with formaldehyde | Virtual lab | Computing report |

#1 LABORATORY WORK

CAUSTIC SODA PRODUCTION BY ELECTROCHEMICAL METHOD

1 THE AIM OF THE LAB:

1. Acquaintance with the technology of caustic soda production by electrochemical method. Studying main electrode processes of sodium chloride solution electrolysis.

2. Determination of process technological indicators: current efficiency of electrolysis products and energy utilization factor.

3. Determination of electrolysis mode parameters (duration, solution concentration, strength of current) effect on basic indicators of the process.

2 THEORETICAL INFORMATION

2.1 The concept of electrolysis, characteristics of electrochemical processes

Electrolysis is a chemical process, proceeding on electrodes when electric current passing through electrolyte solutions or melts. Electrolytes are substances which after dissolution transfer for solutions or melts ability to carry electrical current. Electrolytes are also called as secondary conductors. A water solution of sodium chloride is a typical electrolyte. When dissolving electrolytes dissociate into positive and negative particles – ions (cations and anions), which presence causes specific properties of electrolytes as compared with non-electrolytes.

Electrolytes are divided into two main groups: strong (completely dissociate into ions) and weak electrolytes. Strong electrolytes are comparatively few. They are mineral salts of alkaline and alkaline earth metals, as well as halides, perchlorates and nitrates of some transition metals. Mineral acids and alkalis are strong electrolytes in enough diluted water solutions only. More class of weak electrolytes includes majority of organic salts, acids and bases, and also many of inorganic substances forming multi-charged ions in solutions. To start the reaction in the electrolyte, it is necessary to pass constant electric current through the solution by means of electrodes. Ions, molecules and atoms donate electrons on the surface of a positive electrode (anode) and electrochemical oxidation reaction proceeds. Electron attachment takes place on a negative electrode (cathode) and electrochemical reduction reaction proceeds.

There are strict quantitative relations between time of electric current passing through electrolyte solutions or melts and quantity of electricity and the amount of formed or spent substance. They are determined by Faraday’s laws.

The first Faraday’s law says that “the amount of reacted substance during electrolysis is in direct proportion to the quantity of electricity passed through electrolyte solution or to the strength of current and to electric current passing time”. The second Faraday’s law is formulated as “when the same quantity of electricity passes through different electrolyte solutions, the substances are discharged on electrodes in amounts proportional to their electrochemical equivalents”.

The units of measurement of electricity quantity are coulombs (the quantity of electricity passed upon 1 second at 1 ampere strength of current) or ampere-hours (1 ampere-hour is equal to 3600 coulombs). The quantity of electricity necessary for one gram-equivalent of any substance formation, is constant number, called “Faraday’s number F”, and it is equal to 96500 coulombs, or 96500 amperesecond, or 26.8 amperehour.

The amount of substance discharged during 1 amperehour electricity passing is called an electrochemical equivalent of this substance. Knowing the atomic or molar mass of the substance (A) and cation valency (n), it is possible to calculate an electrochemical equivalent E:

(1.1)

An effectiveness of the electrolysis is estimated with many factors, such as strength of current, voltage, electric current density. Criteria of rational using of electric energy are current efficiency, energy utilization factor and electric energy consumption per a unit of a product.

The strength of current or load on an electrolyzer (an apparatus for electrolysis conducting) characterizes its productivity. The more strength of current is passed through an electrolyser, the more products may be obtained while the electrolyzer operation.

Factual voltage on the electrolyser is the sum of several composites:

Ufact= UТ+Uconc+Uover+I·R                                                                  (1.2)

where UТ is theoretical decomposition voltage, v;

UТ=a-eq - c-eq,                                                                                       (1.3)

where a-eq, c-eq are equilibrium potentials of anode and cathode reactions;

Uconc is concentration polarization, v;

Uconc=(a.conc -c.conc )                                                                           (1.4)

Uover is overvoltage potential on an anode and a cathode, v;

Uover=(a-c)                                                                                       (1.5)

where a, c are anode and cathode overvoltages, v;

J·R is the sum of ohmic resistances, v; i.e. voltage spent to overcome ohmic resistances of the electrolyte, a diaphragm, electrodes and current-conducting wires.

Following anode and cathode equilibrium potentials are taken in processes of sodium chloride saturated solution electrolysis with a solid cathode:

a-eq=+1,33в, c-eq= − 0,84в.

It is tended to decrease bath voltage when electrolysis due to decreasing the polarization value and ohmic composites of the voltage equilibrium, i.e. components conditioned by the process necessity. Decomposition voltage is conditioned by the nature of the reacting substance and therefore it can’t be changed.

Electric current density is a ratio of strength of current passing through the electrolyzer to the electrode surface value (a/m2). It defines the amount of a product obtained on a unit of the electrode surface, i.e. electrolyzer productivity. Therefore if electric current density increase doesn’t cause product output decrease then it is tended to work with maximal possible current densities.

Current efficiency  (%) is the ratio of the substance mass Gfact, actually obtained as a result of electrolysis, to the substance mass GT, which can be obtained according to Faradays’ laws at the same strength of current. It is described by the formula:

(1.6)

The concept of current efficiency is analogous to the concept of product output in chemical processes. Theoretical amount of a substance formed as a result of electrolysis according to Faradays’ laws can be calculated using the formula, unifying both Faradays’ laws:

GТ=   or GТ=IE                              (1.7)

where  I is strength of current, a;

is electrolysis duration, h;

A is molar mass of the substance formed as a result of electrolysis, g;

n is valency of the cation;

F is Faraday’s number, a h.

Energy utilization factor  (%) is the ratio of theoretically required amount of energy WT to the amount of energy factually spent for the electrolysis Wfact:

(1.8)

Theoretical energy consumption WT  is calculated by the formula:

(1.9)

Factual energy consumption Wfact  is calculated by the formula:

(1.10)

It depends on voltage, applied to an electrolyzer.

2.2 Electrochemical method of caustic soda production

Electrolysis of sodium chloride solution is the most typical example of an electrochemical process in water solutions. Simultaneously with main valuable product (caustic soda) hydrogen and chlorine are also obtained as at least valuable products.

Electrolysis is conducted in diaphragm electrolyzers with solid iron cathode as a mesh electrode or a perforated sheet or in baths with a mercury-pool cathode. Graphite is used as an anode. Electrolythic continuous baths with a filtration diaphragm closely fitting to a perforated steel cathode are widely used in industry. The saturated solution of sodium chloride is fed into the anode space, and then it is filtrated through a porous diaphragm due to hygroscopic pressure effect and enters to the cathode space.

Sodium chloride dissociates in water according to the scheme:

NaCl ↔ Na++Cl-                                           (1.11)

H2O ↔ H++OH-                                              (1.12)

When direct electric current passing through NaCl solution Cl- and ОН- ions on an anode, and Na+ and H+ ions on a cathode can be discharged. Oxidation-reduction process behavior is possible on the anode according to the schemes:

2OH- – 2ē  H2O+0.5O2                                       (1.13)

2Cl--2ēCl2                                                (1.14)

and on the cathode according to the schemes:

Na++ēNa                                                   (1.15)

2H++2ēH2                                                (1.16)

Equilibrium potential of ОН- ion discharge in saturated NaCl solution on the anode is +0,82v, and that of Сl- ion is +1,33v. Since oxygen overvoltage on the graphite anode is higher than that for chlorine, therefore initially Cl- ion discharges forming Сl2, but not ОН- ion. When solution concentration decreasing the chlorine discharge potential will rise. Therefore they work usually with concentrated solutions, containing 3I0-3I5 g NaCl /l.

To Na+ ion discharge on the iron cathode the electrode voltage 6.5 times more, than that for H+ ion (–2,71v for Na+, and –0,415v for H+) is required. But such bath voltage is not produced; therefore only H+ ions are discharged. Na+ ions accumulate with ОН- ions inside the solution in the cathode space, forming caustic soda:

Na++OH- ↔ NaOH                                          (1.17)

Caustic soda production by means of electrochemical method is described by the total reaction equation:

2NaCl+2H2O=Cl2+H2+2NaOH                                 (1.18)

As a result of electrolysis chlorine is deposited on an anode and hydrogen is deposited on a cathode and sodium hydroxide is formed in water solution. If there are several positive and negative ions in the electrolyte solution, theoretically only the ion with the least electrode potential is discharged on the electrode.

Together with main processes the side processes can take place. Filtering asbestos diaphragm is used for suppression of side reactions. Side processes are interactions of gaseous chlorine with solution components. Chlorine is partly dissolved in an anolyte and interacts with water and alkali forming sodium hypochlorite, chlorate and chloride according to reaction equations:

Cl2+H2O↔ HCl+HClO                                             (1.19)

HClO+NaOH ↔ NaClO+H2O                                  (1.20)

HCl+NaOH ↔ NaCl+H2O                                       (1.21)

3NaClO ↔ NaClO3+2NaCl                                      (1.22)

As a result of ОН ion discharging on the anode oxygen is formed in insignificant degree according to reaction equation (1.13) and the interaction of oxygen with anode carbon results in the secondary process:

С+O2=СO2                                                (1.23)

Side processes decrease current efficiency on main products. Significant part of electricity is spent for NaClO oxidation into NaClO3 on the cathode. To prevent or to decrease secondary processes it is necessary to provide absence of electrolysis products mixing. For this purpose a diaphragm is used, which separates anode and cathode spaces.

Most high concentration of initial electrolyte solution (saturated solution containing 3I0-3I5 g NaCl/l) promotes to current efficiency increase. The temperature increase up to 70-80С allows to reduce the bath voltage and to decrease the specific consumption of electric energy as well as to reduce side reactions due to chlorine solubility decreasing.

Electrochemical method of caustic soda production has a number of advantages over chemical method, namely: the technological process is simplified; raw materials and energy are used more completely; one can obtain simultaneously several valuable products; higher product purity degree unreachable in the chemical method of production. At the same time electrochemical processes have such essential disadvantage, as high consumption of electric energy, because this article of expenses composes a significant part in the product cost. Problems of electric energy rational usage in electrochemical productions are of primary importance.

3 THE TECHNIQUE OF LAB CARRYING OUT

3. 1 The equipment and technical means:

1. Diaphragm electrolytic plant

2. Chemical glassware

3. Titrimeter

4. Water still Liston А 1210

3.2 Laboratory plant description

The scheme of the batch laboratory plant for sodium chloride solution electrolysis is given in Fig. 1. The plant for table salt solution electrolysis consists of a diaphragm electrolytic bath 4, an alternating current rectifier 18, a rheostat 17 regulating the strength of current fed to bath electrodes, an ammeter 19, and a voltmeter 20. The electrolysis bath consists of a body counterbored of plexiglas with a cover 16. The bath cone bottom 10 is connected with a body and a cover by means of tightening columns 5. A current-carrying ring 9, a perforated iron cathode 8, a horizontal asbestos diaphragm 7 and an encapsulating rubber packing 6 are placed in the bottom. The cathode is directly adjacent to the diaphragm below. A funnel 1 for electrolyte feeding into the bath, a coal anode 2 with a horizontal disk 3 and a glass pipe 15 for chlorine outlet is fixed in holes of the body cover. Electric current is delivered to terminals 13 and 14 (cathode and anode current-conducting wires). The bath is mounted on the support 12; a volumetric cylinder 11 is placed under the bottom fitting 10. The product - sodium hydroxide solution formed in the cathode space as a result of electrolyte filtration through the diaphragm and the cathode is collected in the cylinder.

The filtration asbestos diaphragm is prepared by asbestos mass precipitation on the cathode. For that 20-30 g of asbestos is reduced and subjected to boiling in water for 15-20 minutes to form a smooth past. The formed mass is sucked by means of a vacuum pump (using a Buchner funnel and a Bunsen flask) to the perforated iron cathode. To increase the diaphragm strength it is recommended to place filter cloth of the cathode shape and then to suck the asbestos mass. The iron cathode with the diaphragm is fixed on the bath dismountable base, then the cylindrical body with the cover is set and the plant is bolted together.

1-inlet funnel, 2- carbon anode, 3-graphite disk, 4-bath, 5-column, 6-rubber packing, 7- diaphragm, 8-cathode, 9-ring, 10-bottom, 11- volumetric cylinder, 12- support, 13- cathode current wire, 14- anode current wire, 15-glass pipe, 16-cover, 17- rheostat, 18-rectifier, 19- ammeter, 20- voltmeter, 21- anode space, 22 – cathode space Fig. 1. Lab electrolytic plant scheme

3.3 The order of lab carrying out

1. Establish the table salt electrolytic plant (Fig. 1) and check the truth of electric gauges switching on.

2. Pour throw an inlet funnel sodium chloride solution of given concentration in the bath anode space for entire submersion of anode graphite disk and a half of anode rod height into the solution. Switch on the exhaust ventilation.

3. Turn on electric current and establish the given strength of current by means of the rheostat. It is necessary to maintain constant strength of current during the experiment. Note indications of voltage and strength of current.

4. Carry out the electrolysis in specified conditions for 20-30 minutes up to mode stabilization. Then 2-3 catholyte tests for analyses are consecutively sampled from the cathode space. For this purpose a volumetric cylinder graduated up to 25 ml is placed under the bottom fitting and simultaneously the gauge cock opens for cathode liquor sampling and a stop-watch starts up. In 10 minutes the cylinder is substituted by another one for the second sampling.

5. Measure the catholyte volume (V2) in the cylinder and then quantitatively replace it into a conical flask by washing over with distilled water.  If the catholyte volume is more than 10 ml, then 5 ml aliquot is sampled by a pipette for the analysis.

6. Add 2-3 drops of phenolphthalein indicator into the solution and titrate it with 0.1n hydrochloric acid solution up to solution discoloration.

7. Determine caustic soda concentration (g/l) in the catholyte CNaOH  by the formula:

CNaOH=                                            (1.24)

where V is volume of 0.1n hydrochloric acid solution, spent for the sample titration, ml;

К is correction factor for the hydrochloric acid titre;

0,004 is the amount of NaOH, corresponding to 1 ml of 0.1n HCl;

V1 is catholyte sample volume subjected to titration, ml.

4 CALCULATIONS OF TECHNOLOGICAL INDICATORS OF THE ELECTROLYSIS

Current efficiency and energy utilization factor are main criteria of energy rational usage in the electrolysis process.

1. Determine current efficiency  by the formula (1.6). For that at first the factual amount of sodium hydroxide formed as a result of electrolysis Gfact is calculated based on determined NaOH concentration in each sample of the cathode liquor:

Gfact= CNaOH V2/1000                                     (1.25)

where V2 is catholyte volume sampled into the  volumetric cylinder, ml.

Theoretical amount of NaOH is calculated by the formula (1.7) uniting both Faraday’s laws taking into account strength of current and time of electrolysis. Then current efficiency for each sample of sodium hydroxide is determined.

2. Determine energy utilization factor for each sample of the catholyte by the formula (1.8) taking into account theoretical amount of energy WT and factual amount of energy Wfact spent for the electrolysis, calculated by formulas (1.9) and (1.10). The formula (1.8) can be transformed if to substitute expressions for WT and Wfact. After simple reformation we get the dependence expressed through current efficiency value:

=     			                  (1.26)

3. Experimental data and calculated technological indicators of the electrolysis are listed in Tables 2 and 3.

Table 2. Electrolysis experimental data

| ## | Sampling time, min | Strength of current, a | Voltage, v |  | Catholyte volume subjected to titration V1, ml | Volume of sampled catholyte V2, ml | Volume of 0.1n HCl solution V, ml |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Ufact | UТ |  |  |  |

Table 3. Indicators of the electrolysis process

| Concentration of initial solution, СNaCl, % | Sample # | Catholite concentration, CNaOH, g/l | NaOH amount, g |  | Current efficiency , % | Energy utilization factor μ, % |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Gfact | GТ |  |  |

4. Based on calculation results determine the dependence of process indicators on the electrolysis time and NaOH content in the cathode liquor.

If the research lab is carried out the influence of table salt solution concentration on current efficiency and energy utilization factor is studied and then make a conclusion about optimal technological mode of the electrolysis.

- SAFETY PRECAUTIONS

1. Establish the electrolytic plant in the operating draft cupboard.

2. Check the truth of the plant assembling.

3. Switch on the exhaust ventilation before the electrolysis start.

4. Turn on electric current under completely switched off rheostat in the presence of laboratory assistant only.

5. Don’t lean over the electrolytic bath and don’t check gas exhausts in no case because of strong toxicity of emitted chlorine and other gases causing poisoning and blennosis.

6. It is categorically prohibited to set a plant near the fire in view of hydrogen emission in the cathode space.

6 CONTROL QUESTIONS

1. The electrolysis essence. The first and the second Faraday’s laws. The concept of electrochemical equivalent.

2. Basic technological indicators of electrochemical processes.

3. Cathode and anode processes in table salt solution electrolysis. The chemical scheme of the electrolysis.

4. The principle of operation of the electrolyzer with solid iron cathode and the filtration diaphragm for sodium chloride solution electrolysis.

5. The influence of technological mode parameters on electrolysis basic indicators. Choice of optimal technological mode of the electrolysis.

6. Basic types of electrolyzers used for sodium chloride solution electrolysis.

7. Advantages and disadvantages of electrochemical processes as compared with chemical ones.

#2 LABORATORY WORK

CAUSTIFICATION OF SODA SOLUTION

1 THE AIM OF THE LAB:

1. Acquaintance with the process of soda solution caustification.

2. Experimental and virtual studying the different parameters effect on caustification degree of soda solution.

3. Master skills of virtual lab carrying out on the computer program.

2 THEORETICAL INFORMATION

2.1 Chemical method of caustic soda production

Caustification of soda solution is a main stage of caustic soda production by means of lime method. In addition caustification is one of stages of cellulose production by sulphate method (with regeneration of cooking liquor), in aluminum production using wet alkaline method and others.

Caustification refers to typical heterogeneous non-catalytic processes proceeding under low temperature. This process is also used for water softening by lime-soda method. To increase sizes of particles of formed solid phase and therefore to increase the rate of slime settling the combined reagent method of water pretreatment is often used. The method consists in preliminary mixing and heating the precipitation agents, i.e. soda solution and lime milk which are injected then into water for softening. Herewith calcium carbonate precipitate is formed as a result of caustification:

Na2CO3 +Ca(OH)2 ↔ CaCO3↓ +2NaOH+Q                                        (2.1)

The same method of caustification is used for preliminary purification of sodium chloride raw brine from hardness salts in soda ash production by Solvay method.

In caustic soda production the soda solution obtained by crude sodium bicarbonate decarbonization and by soda ash dissolution, is treated with lime or lime milk forming precipitate CaCO3 according to reaction equation (2.1).

Using lime instead of lime milk in the caustification process allows using the heat of CaO slaking as an exothermic process. Thereat more concentrated caustic soda solution is formed due to partial evaporation of water from solution and removal of water entering with the lime milk. The process of soda solution caustification is a typical example of reversible heterogeneous interaction taking place in the kinetic region in liquid-solid (L-S) system. The (2.1) reaction path depends mainly on the ratio of solubility of the least soluble components Ca(OH)2 and CaCO3, i.e. on concentrations of OH- and CO32- ions in the solution.

In the process beginning the equilibrium of (2.1) reaction is displaced to the right because CaCO3 solubility is less than Ca(OH)2 solubility. For example, under 100°C Ca(OH)2 solubility in water is 0.07%, and CaCO3 solubility is only 0.00002%. In addition, there is big amount of CO32- ions in the initial solution, which decrease already low solubility of CaCO3. In the course of  caustification OH- ions are accumulated in the solution, and the number of CO32- ions decreases. Therefore CaCO3 solubility increases, and Ca(OH)2 solubility decreases. Equilibrium is established when both salts reach the same solubility.

The equilibrium constant of (2.1) reversible reaction is described in general form by the following expression:

(2.2)

Since during caustification calcium hydroxide and carbonate in solid phase are always present in the reaction mix, then values of [Ca(OH)2] and [CaCO3] are constant and they can be included in the equilibrium constant value, i.e.

(2.3)

Then the expression for equilibrium constant depending on solubility of sodium hydroxide and sodium carbonate takes the form:

(2.4)

We can see from (2.4) expression that the equilibrium in the given system is determined exceptionally by the ratio of sodium hydroxide and sodium carbonate solubility. NaOH equilibrium output called as the caustification degree is defined as the ratio of factual and theoretical amounts of the obtained product:

(2.5)

Based on this ratio one can determine following ways to increase NaOH equilibrium output.

2.2 Methods of increasing of soda solution caustification degree

The equilibrium caustification degree (i.e. the degree of Na2CO3 conversion into NaOH in equilibrium state) increases with decreasing Na2CO3 content in the initial solution. Thereat concentration of CO32- ions decreases in the equilibrium causticized solution and ratio increases, and therefore the caustification degree increases. With that water content in the causticized solution increases; it results in increasing water steam consumption for following evaporation of weak liquors. Therefore the choice of optimal soda concentration in the initial solution is determined not only by the caustification degree, but also by the concentration of obtained NaOH solution. In practice, 10-15% Na2CO3 solution (2-3 n) is used. On average the caustification degree reaches about 90%, and liquor containing 100-120 g/dm3 of NaOH is obtained. Low concentration of caustic soda in liquors sent for evaporation is the main disadvantage of the lime method.

Temperature influence on the caustification degree is also ambiguous. Temperature increasing shifts equilibrium of this reversible exothermic reaction to the left and thereby decreases the equilibrium constant and the equilibrium caustification degree as a consequence of CaCO3 solubility increase. On the other hand temperature rising increases the rate of (2.1) heterogeneous reaction taking place in the kinetic region. In addition to that temperature increase promotes to decreasing solution super saturation by CaCO3; it leads to formation of large crystals of calcium carbonate. In turn it increases the rate of sludge settling due to solution viscosity decrease. Large crystals not only are faster precipitated but and better washed out of NaOH and Na2CO3 residue with less amount of water.

That is why caustification is performed under increased temperature 80-90°C in a causticer-reactor heated with direct or indirect steam using coils in which steam circulates. Lime slaking with soda solution in a drum slaker results in formation of suspension which is fed to the causticer. Then the suspension is sent to settlers. Clarified weak caustic liquor is decanted and fed for evaporation into triple-effect vacuum-evaporator installation and then for melting and formation of solid product - flake or granular caustic soda.

Sludge, consisting mainly of CaCO3, undergoes multi-stage countercurrent washing by water and weak bypass solutions in order to extract caustic soda completely. This washing takes place in a battery of washers-decanters with stirring mechanisms, which solidify sludge in the lower part of the apparatus. Clarified solution is drained off from the upper part of the decanter and then it is sent for salts dissolution into the evaporation section. Washed sludge is separated in a drum vacuum-filter and is removed into the dump.

3 THE TECHNIQUE OF LAB CARRYING OUT

3. 1 The equipment and technical means:

1. Laboratory plant for caustification

2. Chemical glassware

3. Titrimeter

4. Water still Liston А 1210

5. Analytical balance ВЛТЭ-150

6. Vacuum-filtration plant

3.2 Laboratory plant description

The scheme of laboratory plant for soda solution caustification is shown in Fig. 2. It consists of a thermostat 1, filled with water which is heated by an electric heater 2 and is stirred with a stirring mechanism 4. A causticer 5 represents a china glass with a cover and a stirring mechanism 6 passed through the cover opening. The causticer is submerged into the water in the thermostat. Temperature in the thermostat is controlled with the control thermometer 7 and is regulated using a resistance thermometer 3 included into the automatic regulation scheme.

3.3 Calculations of lime consumption for caustification

1. To carry out the experiment, three samples of initial soda solution containing Na2CO3 in interval 5-20% are taken. It is impossible to prepare a solution with concentration higher than 22% under temperature of 20°C, because such concentration is higher than Na2CO3 solubility in water.

2. The theoretical amount of lime CaO is calculated according to reaction equation (2.1) for specified mass of initial soda solution with known concentration. In order to do this first of all Na2CO3 content in the initial solution is determined by the solution titration with 1n solution of hydrochloric acid.

3. Take 10 ml of the analyzing soda solution by a pipette and place it into the conical flask.  Add 40-50 ml of distilled water and 2-3 drops of methyl orange indicator and titrate with 1n hydrochloric acid solution until color transition into pink color. The volume of 1n HCl solution (ml) spent for titration is equivalent to the amount of Na2CO3 in the solution.

The example of calculation of soda solution composition.

Assume that 20 ml of 1n HCl solution is spent for titration of 10 ml of initial soda solution. Concentration of Na2CO3 in the solution is determined by the formula:

СNa2CO3 =                                        (2.6)

where υ is volume of 1n HCl solution spent for sample  titration, ml;

υs.s. is volume of soda solution sample subjected to titration, ml;

К is correction factor for the titre of 1n hydrochloric acid solution;

53 is g-eq of Na2CO3.

The correction factor for the titre of 1n HCl solution exactly K=0.95. Then solution concentration is СNa2CO3 =

Na2CO3 mass in given volume (V=200 ml) of initial soda solution is calculated through a ratio:

4. Consumption coefficient b (g) of CaO for each m gram of the soda solution with concentration c (%) is determined using the formula:

,                                                           (2.7)

where 56 and 106 are molar masses of CaO and Na2CO3 accordingly.

5. Then the amount of lime with 5% excess over stoichiometric amount is determined by the formula:

a =1.05 b                                                           (2.8)

Usually when caustification carrying out in lab conditions fine-divided non-slaked lime and 100 or 200 grams of soda solution samples of three different concentrations are used to determine the dependence of caustification degree on soda solution composition.

3.4 The order of lab carrying out

1. The set amount (100-200g) of initial soda solution with different concentrations is poured into china glass-causticer 5. The causticer is placed into the thermostat previously heated to the required temperature. Temperature is regulated automatically.

1-thermostat, 2-heater, 3-contact thermometer, 4,6-stirring mechanism, 5-causticer, 7-control thermometer, 8-funnel for CaO loading. Fig. 2. Scheme of the lab plant for caustification of soda solution

2. The solution is heated up to 80°C under the switched stirring mechanism inside the causticer. After 80°C reaching the fine-divided lime is added in small portions to the soda solution during 5-10 minutes.

3. After the whole amount of lime is loaded, the experiment start time is recorded. Caustification proceeds during 40 minutes. Caustification temperature is kept constant 80°C during the entire process.

4. At the experiment end the stirring mechanism and heating is switched off and the causticer is taken out of the thermostat. In order to determine the caustification degree, the suspension is filtered under vacuum of 0.06 MPa using a Bunsen flask and a Buchner funnel. The filtrate is replaced into the conical flask. The precipitate is washed by hot water, and the sludge is also filtered. Washing water is collected as well.

5. The content of NaOH and Na2CO3 is separately determined in the filtrate and the washing water, and their total amount is determined.

6. Using the obtained data the caustification degree X is determined for each experiment as the ratio of NaOH mass in the filtrate and in the precipitate to the total mass of NaOH and Na2CO3 (recalculated into NaOH) in the filtrate and the precipitate.

3.5 The technique of virtual lab carrying out

A computer version of the “Caustification of soda solution” lab includes several stages. At first students choose the language of virtual lab performance (Fig. 3). Then they should make acquaintance with theoretical bases of the process and the technique of virtual lab carrying out (Fig. 4). Then they must answer the qualification test questions:

- Reagents for caustic soda production by chemical method…

- Optimal concentration of soda solution fed for the caustification…

3. Caustification of the soda solution with lime is described by the reaction equation…

- Caustification of the soda solution with lime milk is described by the reaction equation…

- The temperature of soda solution caustification…

- Na2CO3 content in the solution is determined by the titration with…

- The slime formed in the caustification…

- Caustification degree of soda solution is determined by…

- The separation of suspension is carried out by the method of…

10. The lime input is carried out by...

Fig. 3. Interface of the virtual lab

Having chosen the correct answer, they accept it with the (OK) button and move on to the next question. Having answered 10 questions correctly out of 10 offered ones, students pass to the lab performance (“Begin work” button). In a case of even one incorrect answer students must return to the beginning of the program and to take the qualification test again.

Fig. 4. The second window of the virtual lab carrying out

Next students start the caustification process (Fig. 5): they choose soda solution mass given by the instructor (100 or 200 grams) and specify 3 different solution concentrations.

Fig. 5. Window for the first stage of the work carrying out

– caustification of soda solution

If concentrations are entered correctly, then based on these values students must calculate consumption coefficients for lime on the basis of  reaction equation (2.1). Coefficients are calculated using the stoichiometric ratio b taking into account 5% reagent excess a. Then students enter the obtained results into corresponding windows. In the case of incorrectly entered concentrations or incorrect calculation of b and a values, the mistake that needs to be corrected is pointed out after pressing the “turn on” button. When all parameters are entered correctly, the student can begin the lab.

In order to carry out the work, buttons of operational regulation of the process “lime input”, “turn off”, “temperature” and “timer” are used. If the technological mode of soda solution caustification is disturbed, the mistake is pointed out to the student as well.

If the student makes more than three mistakes, he gets an “unsatisfactory” mark and he is returned to the qualification test. If caustification is carried out properly students start (Fig. 6, 7) the process of suspension filtration and precipitate washing using buttons “turn on” and “turn off”. Obtained masses of filtrate, precipitate and washing water are shown in “work result” windows. Using total values of NaOH amount in filtrate and precipitate and Na2CO3 amount (recalculated to NaOH) in filtrate and precipitate, students have to calculate caustification degrees and enter the values into corresponding windows.

Fig. 6. Window for the second stage of the work carrying out -

suspension filtration

If the calculation is performed correctly, the program builds a graphic dependence of caustification degree on soda solution concentration based on which students make a conclusion for the work. To evaluate the student’s knowledge of theoretical bases of caustic soda production, the work defense test is provided including following 20 questions:

- The advantage of lime method of caustic soda production in comparison the electrochemical one.

- The decreasing of solution supersaturation of CaCO3 in reached by means of…

- Caustification carrying out with 5-10% lime excess using promotes to…

- The disadvantage of chemical method of caustic soda production…

- The disadvantage of electrochemical method of caustic soda production…

- Why is the caustification carried out under high temperature?

- The heterogeneous process takes place in the kinetic region if…

- How does the temperature increasing influence on the rate of the process taking place in kinetic region?

- How does caustification degree change when soda solution concentration increases?

- How does increasing the solid phase dispersion influence on the rate of the process taking place in kinetic region?

- The advantage of lime using for soda solution caustification is…

- The advantage of lime using for soda solution caustification is…

- What is the region of heterogeneous process of soda solution caustification?

- What is the disadvantage of the lime method of caustic soda production?

- What is the disadvantage of the lime method of caustic soda production?

- What influences the lower limit of Na2CO3 concentration in the solution?

- What influences the lower limit of Na2CO3 concentration in the solution?

- What influences the upper limit of Na2CO3 concentration in the solution?

- Why is the caustification carried out under high temperature?

- What stage follows after the first caustification in industrial conditions?

Fig. 7. Window for the third stage of the work carrying out

– precipitate washing

After test successful completion students get a mark: when answering 19-20 questions – “excellent”, with 2-3 incorrect answers – “good”, with 4-5 incorrect answers – “satisfactory”. If students answered less than 15 questions the work is considered as unfulfilled and it must be performed again. Summary mark for the virtual lab is given taking into account mistakes made during caustification and filtration process performance and caustification degree calculation.

3.6 The order of analyses carrying out

Filtrates and washing water are analyzed to determine the content of NaOH and Na2CO3. The method of BaCO3 precipitation is used and it is based on the following principle. The total alkalinity (NaOH+Na2CO3) is determined in one sample of testing solution by means of its titration with hydrochloric acid solution in methyl orange indicator presence.

The filtrate is separated from the slime; then filtrate volume V1 is noted and 10ml filtrate aliquot is sampled and is placed into 250 ml conical flask. Add 50 ml of water and 2-3 drops of methyl orange and titrate with 1n HCl solution up to yellow colour transition into pink colour. The amount of 1n HCl solution (ml) 1 spent for titration corresponds to the total alkalinity.

Another sample of testing solution is subjected to Na2CO3 precipitation by barium chloride to determine NaOH content by solution titration with hydrochloric acid solution in phenolphthalein indicator presence. For that 10ml filtrate sample is placed into 250 ml conical flask, then diluted with 50 ml of water and add barium chloride solution excess (30 ml of 10% BaCl2 solution). Herewith barium hydroxide and insoluble barium carbonate precipitate is formed according to reaction equations:

Na2CO3+BaCl2=2NaCl+BaCO3↓                     (2.9)

2NaOH+BaCl2↔2NaCl+Ba(OH)2                  (2.10)

After precipitation 2-3 drops of phenolphthalein is added to the sample and immediately titrate solution with 1n hydrochloric acid solution. The volume of 1n HCl (ml) 2 spent for titration corresponds to NaOH content in the sample.  NaOH и Na2CO3 content in the filtrate is calculated by formulas:

(2.11)

(2.12)

where  40 and 53 are g-equivalents of NaOH и Na2CO3 in match;

К is correction factor for 1n HCl solution titre.

Washing water is analyzed by the same method but 0.1n HCl solution is used for titration. Washing water volume V2 is measured and two samples of 20 ml are sampled to determine total alkalinity and NaOH content.

4 CALCULATIONS OF PROCESS TECHNOLOGICAL INDICATORS

Caustification degree Х is the main indicator characterizing effectiveness of caustic soda production by chemical method. It is determined by the formula (2.5), where Gfact is the factual mass of NaOH and Gtheor is the (theoretical) total mass of NaOH and Na2CO3 (in recalculation into NaOH) in the filtrate and in washing water.

The example of caustification degree calculation.

To titrate 10 ml of the filtrate 25 ml of 1n HCl solution is spent, and to titrate the same volume of the filtrate after Na2CO3 precipitation with barium chloride 21 ml of 1n HCl solution is spent. Then NaOH and Na2CO3 contents in the solution are determined by formulas (2.11) and (2.12):

The whole filtrate volume (V1=300ml) contains:

m2=

To determine the total alkalinity of washing water (sample of 20 ml volume) 22 ml of 0.1n HCl solution is spent. To determine NaOH content in washing water (sample of 20 ml volume) 18 ml of 0.1n HCl solution is spent. Then NaOH and Na2CO3 contents in washing water are determined:

The whole washing water volume (V2=200ml) contains:

m4=

Total mass of NaOH obtained as a result of caustification is m1+m3=23.94+0.72=24.66г. Mass of unused soda is m2+m4 =6.04+0.21=6.25g or in recalculation into NaOH 6.25∙80/106=4.72g. All obtained data are summarized in Tables 4 and 5.

Determine caustification degree of the soda solution:

Then the graphic dependence of caustification degree on concentration of initial soda solution is built and a conclusion is made.

Table 4. Results of filtrate analyses

| Initial solution |  |  | Volume of 1n HCl solution, ml |  | Analysis of filtrate |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Volume V, ml | Na2CO3 content |  |  |  | Volume V1, ml | Na2CO3 content |  | NaOH content |  |
|  | g/l | g | 1 | 2 |  | g/l | g | g/l | g |

Table 5. Results of washing water analyses

| Na2CO3 content in soda solution, g/l | Volume of 0.1n HCl solution, ml |  | Analysis of washing water |  |  |  |  | Caustification degree Х, % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Volume V2, ml | Na2CO3 content |  | NaOH content |  |  |
|  | 1 | 2 |  | g/l | g | g/l | g |  |

- SAFETY PRECAUTIONS

1. Check the integrity of wires, plugs, and outlets when heating and a stirrer switching on.

2. In a case of mains interruption or one phase breakdown the heating and motor engine must be immediately switched off.

3. In a case of wires or electric gauges firing it is necessary to disconnect them immediately and to extinguish with dry carbon dioxide fire extinguisher or with the asbestos cloth.

4. You must not bend over the thermostat to avoid hair twist on rotating stirrers.

5. When the work is over it is necessary to switch off electric gauges, to clean workplaces and to give them to the laboratory assistant.

6 CONTROL QUESTIONS

1. Characteristics of chemical methods of caustic soda production (lime and ferrite ones).

2. Physical-chemical bases of caustic soda production by chemical method.

3. Main technological indicators of chemical production effectiveness.

4. Choice and justification of basic parameters (concentration and temperature of soda solution) of soda solution caustification.

5. Advantages and disadvantages of chemical and electrochemical methods of caustic soda production.

6. Basic stages of caustic soda production by chemical method.

7. Determine optimal conditions of soda solution caustification based on experimental data analysis.

#3 LABORATORY WORK

ELECTROCHEMICAL COPPER PLATING

1 THE AIM OF THE LAB:

1. Practical acquaintance with processes of electrochemical metal plating.

2. Mastery the calculation technique of technological indicators of electrochemical metal plating.

3. Determination of process parameters influence on electrochemical copper plating effectiveness.

2 THEORETICAL INFORMATION

2.1 Electrochemical process essence

Electrochemical processes are processes related to electrical energy conversion into chemical one, or chemical energy conversion into electrical one. Faraday’s laws are the basis for electrochemical processes.

According to the first Faraday’s law the mass of the converted substance in any electrode process, is directly proportional to the strength of current and its passage time, i.e. it is proportional to the amount of passed electricity.

The second Faraday’s law characterizes the influence of ions’ nature. The law appoints: when the same amount of electricity passing through different electrolyte solutions the amount of each converted substance is proportional to its’ electrochemical equivalent; at that for deposition of one gram-equivalent of any substance 96500 coulombs or 26.8 ampere-hour of electricity is required. Because of side processes the amount of deposited substance is always less, than it must be deposited according to Faradays’ laws.

Basic criteria of electric energy rational using in the electrolysis process are current efficiency and energy utilization factor. Current efficiency  (%) is the ratio of a substance mass Gfact actually formed during the electrolysis, to a substance mass GT, which must be deposited by Faraday’s laws at the same electricity consumption:

(3.1)

The concept of current efficiency is analogous to the concept of product output in chemical processes. Theoretical amount of a substance can be calculated with the formula, joining both Faraday’s laws:

GТ=   or  GТ=IE                                      (3.2)

where  is electrochemical equivalent, g/ a-h;

I is strength of current, a;

is electrolysis duration, h;

A is molar mass of substance, deposited as a result of electrolysis, g;

n is valency of the cation;

F is Faraday’s number, 26,8 a-h/g-eqv.

Energy utilization factor (coefficient)  (%) is expressed as a ratio of theoretically required amount of energy  for deposition of a unit of a product to actually spent energy Wfact:

100%		                          	(3.3)

Theoretical energy consumption for a unit of a product is determined by the formula:

(3.4)

where  is theoretical voltage of the decomposition, v.

UТ=a-eq - c-eq,                                                                                       (3.5)

where a-eq, c-eq are equilibrium potentials of anode and cathode reactions.

Practical energy consumption depends on voltage, applied to an electrolizer Ufact:

(3.6)

After simple reformations we will get:

(3.7)

It is followed from this equation, that energy utilization coefficient will be the greater, the higher current efficiency and the lower the bath voltage.

  - Processes of electrochemical metal plating

Electrolysis of water solutions or melts has wide spread occurrence in industry. Electrochemical methods of production have advantages over chemical methods in some instances, namely: the technological process is simplified; raw materials and energy are used more completely; higher product purity degree. Due to these advantages electrochemical processes are used in productions of such important products as chlorine, hydrogen, oxygen, alkalis and for production of metals and metal protective coatings.

Galvanic coatings are widely used for metal protection from corrosion, which are mainly prepared by deposition on non-ferrous metal wares, by means of electrolysis of salt water solutions. In addition to that an electroplated metal can increase significantly wear resistance of the prime item, its electric conductivity and other important indicators.

Taking into account requirements to operational characteristics of metal wares the galvanic coatings can be conditionally divided into three types:

- protective-decorative galvanic coatings used to give to surfaces decorative and protective properties simultaneously;

- protective electrolytic coatings used for metal wares protection from corrosion in different aggressive mediums; They found practical application in automobile construction, aircraft, radio engineering and electronic industry and also in construction engineering;

- special-purpose galvanic coatings used to give specific  special properties to the metal surface, such as hardness, wear resistance, magnetic and dielectric properties. Special-purpose galvanic coatings can be also deposited for worn-part reclamation.

Nickel plating, chromium plating and zinc plating are most wide spread processes of electrochemical metal plating. Zinc plating is used for direct metal ware plating. Nickel plating can protect an iron ware only if there aren’t bare spots and pores on the surface; therefore the ware has to have the minimal porosity. To reduce the porosity at first a copper layer is deposited on steel and already then a nickel layer is deposited. Chromium forms also a porous surface on the iron ware, and therefore chromium is deposited on the iron surface after preliminary nickel coating. The best effect is reached at four layer coating consisting of nickel, copper, the second layer of nickel and chromium coating.

Copper plating isn’t usually used as individual electrolytic coatings neither for steel wares protection from corrosion nor for decorative purposes due to their chemical and electrochemical properties. Copper is quickly oxidized in atmospheric conditions forming oxide and basic salt deposits on the surface. It is impossible to deposit copper directly on the steel because the steel is dipped in sulphuric acid solution. Therefore it is recommended to use copper coatings as a interlayer before nickel and chromium plating; it is very important for saving the expensive and deficit nickel. Cooper plating is used as individual electrolytic coating in iron carbon cementation for protection of item separate parts unliable to cementation. This plating can be also used as basic current-carrying layer in printed-circuit board production.

Depending on the mechanism of protective action all galvanic coatings are subdivided into anode and cathode coatings. If an electrode potential of the coating metal is less (i.e. if a metal is more electronegative one) than that of protected one, then this coating will be anode one, and the coating metal is dissolved under the electrolyte action. Zinc and cadmium coatings are anode ones for the steel. Coatings with copper, chromium, nickel, tin, lead, gold and silver are cathode coatings. At the cathode coating a protecting metal ware serves as a cathode on which metal cations are discharged and deposited as thin even layer. The coating metal serves as an anode and it is dissolved in the electrolyte.

At nickel plating the metallic nickel is an anode and it is dissolved in the electrolysis process. Nickel sulphate solution containing 175-200 g/l of NiSO47H2O is used as an electrolyte; to increase solution electric conductivity the additives of 80-160 g/l of Na2SO410H2O, 20 g/l of NaCl, and 20 g/l of Н3ВО3 are injected in the electrolyte composition. During the electrolysis the following processes proceed on electrodes. Nickel or hydrogen can be discharged on the steel cathode:

Ni2++2e=Ni0                                          (3.8)

2H++2e=H2                                           (3.9)

Since equilibrium discharge potential of Ni2+ ion (φNi = – 0.23v) is less than that for H+ ion (φН2 = – 0.415v), the metallic nickel only will be deposited on the cathode. Following red-ox reactions proceed on the anode:

Ni0 –2е= Ni2+                                      (3.10)

OH-–2ē=H2O+0,5O2                                                  (3.11)

At that primary nickel anode dissolution takes place.

For copper plating the acidic electrolyte solution is used with the composition: 200-250 g/l of copper vitriol CuSO45H2O solution containing 50-70 g/l additive of sulphuric acid. Copper plates are applied for the electrolysis as an anode and nickel-plated steel as a cathode. Since copper has positive electrode potential (φCu = +0.34 v), the hydrogen reduction doesn’t take place on the cathode. Therefore Cu2+ ions are discharged on the cathode by the reaction equation:

Cu2+ +2e=Cu0                                         (3.12)

At that practically 100% current efficiency is reached.

In the process of chromium plating the iron ware is a cathode, and chromic acid solution is used as the electrolyte. Herewith Cr6+ ion is reduced up to the metallic chromium or molecular hydrogen on the iron cathode:

СrО4-2+6ē+4Н2О=Сrº+8ОН                                   (3.14)

2Н++2ē=Н2                                           (3.15)

and on the anode:

2ОН-–2ēН2О+0,5О2                                   (3.16)

Сr+3–3ēCr+6                                             (3.17)

Current efficiency for the chromium plating is very low (8-16% for Cr6+). A basic part of electric energy is spent for side processes:

СrО4+3+4ē+4Н2ОСr(ОН)2+6ОН-    (cathode process)       (3.18)

Сr+3–3ēСr+6                  (anode process)        (3.19)

Preparation of high-grade chromium deposits is available only in the presence of sulphuric acid of a certain concentration or its salts in the electrolyte solution. Sulphuric acid destructs a colloid film formed on the cathode when chromium plating.

3 THE TECHNIQUE OF LAB CARRYING OUT

3.1 The equipment and technical means:

1. Laboratory plant for electrolytic metal plating

2. Analytical balance ВЛТЭ-150

3. Dryer ШС-80

3.2. Laboratory plant description

The laboratory plant for electrolytic metal plating (Fig. 8) consists of constant-current source 1, an electrolytic bath 4 with an anode 5 and a cathode 6, a rheostat 2, a coulometer 3, a voltmeter 7, an ammeter 8 and a switch 9. All devices are put into direct current network sequentially and only the voltmeter is put into circuit in parallel. A glass blank of 0.5l capacity is used as the electrolytic bath. Two thin brass-wares or copper plates are used as anodes. They are fixed on the bath cover. The nickel plate or nickel-plated steel serves as a cathode.

1-constant-current source, 2-rheostat, 3-coulometer, 4-electrolytic bath, 5-anode, 6- cathode, 7-voltmeter, 8-ammeter, 9-switch. Fig. 8. Lab electrolytic plant scheme

3.3 The order of lab carrying out

1. The sample preparation to the electrolysis.

Uneven surface, dirt, rust, oil spots deteriorate coatings. Therefore plates subjected to electrolytic plating should be thoroughly purified. Cleaning the metal ware surface is conducted by means of mechanical and chemical treatment. The mechanical treatment is carried out using abrasive paper and a felt disk with a cleaning mixture or crocus cloth. For alkaline cleaning and for giving best wettability the wares are treated with hot alkaline solution containing 100 g/l of NaOH or with organic solution, for example, ethanol.

2. The metal ware is weighed on the analytical balance with accuracy to 0.01 g.

3. Set a laboratory plant due to the scheme (Fig. 8). Fill up the electrolytic bath with copper vitriol solution of the composition: CuSO45H2O-250 g/l, H2SO4-50 g/l. Electrolyte solution volume should provide for electrodes submersion into the solution on approximately three-quarters of plates’ height.

4. Install two copper anodes into the bath. The prepared detail is fixed at the cathode place and is submerged into the electrolyte space. Turn on the electric current and set the required strength of current by means of the rheostat. Note strength of current and voltage values of test indications.

5. The electrolysis process duration is 5-10 minutes. Turn off the electric current after copper plating completing. Then extract the plate from the bath, dry in the dryer and weigh on the analytical balance with accuracy to 0.01 g. Determine plate mass increasing and copper plating surface of the cathode plate.

6. Calculate basic indicators of the electrochemical process - plating layer thickness and current efficiency according to formula (3.1). Theoretical amount of copper is determined due to Faraday’s laws.

Conditions of the process performance can be various and they are determined by the instructor (process duration, strength of current, surface of cathode submerged part). In this case based on results of parameters’ variation students determine the dependence of electrochemical process indicators on process conditions and make a conclusion to its efficiency.

4 CALCULATIONS OF ELECTROCHEMICAL PROCESS INDICATORS

4.1 Determine plating layer thickness:

Average copper layer thickness δav (micron) is determined by the formula:

δav=,		           		(3.20)

where Gfact is change of the plate mass as a result of copper plating, g;

Gfact = G2- G1,

where G1is sample initial mass, g;

G2 is sample mass after electrolysis, g;

S is copper plating surface of the plate, cm2;

is density of the coating metal, g/cm3, Cu= 8.95 g/cm3.

4.2 Determine current efficiency:

Current efficiency   is determined by the formula (3.1). Theoretical amount of deposited copper is determined due to Faraday’s laws (according to the formula (3.2)).

Calculation results are tabulated into Table 6.

Table 6. Indicators of electrochemical copper plating

| Cathode mass, g |  | Mass of copper deposited on cathode Gfact, g | Surface of cathode submerged part, S, cm2 | Strength of current I, a | Electroly-sis duration , h | Copper layer thickness δav, micron | Current efficiency , % |
| --- | --- | --- | --- | --- | --- | --- | --- |
| before electrolysis G1 | after electrolysis G2 |  |  |  |  |  |  |

- SAFETY PRECAUTIONS

- Check the truth of the plant assembling.

2. Keep watch for isolation state of all conductors and for their correct connection.

3. It is prohibited to touch uninsulated electric wires and contacts with open skin areas.

4. It is necessary to set electrodes and to extract deposited plates from the electrolyzer under off-state plant only.

5. To work with electrolyte solutions in rubber gloves and to avoid electrolyte splash impact on skin and wear.

- When the work is over it is necessary to switch off the plant.

6 CONTROL QUESTIONS

1. Characteristic of electrolysis from the point of view of Faraday’s laws.

2. Main indicators of electric energy rational usage in processes of electrochemical metal plating.

3. Features of deposition of nickel and chromium plating.

4. Distinction of copper coatings from other types of electrochemical platings.

5. Comparative characteristics of anode and cathode coatings.

6. Electrode processes taking place during coppering and nickeling.

7. Areas of application of galvanic metal coatings.

8. Experimental determination of thickness of copper plating layer.

#4 LABORATORY WORK

TECHNICAL ANALYSIS OF SOLID FUEL

1 THE AIM OF THE LAB:

1. Acquaintance with standard methods of determination of moisture, ash and volatile matter content in solid fuel.

2. Evaluation of solid fuel quality.

2 THEORETICAL INFORMATION

2.1 General characteristics of fuel-energy resources

Fuel-energy resources are subdivided into fuel (coal, oil, natural gas, shale, peat, and biomass) and non-fuel resources (hydro power, wind power, solar power, deep earth heat, tidal and atomic energy), renewable and non-renewable ones, primary and secondary ones.

Renewable resources include all non-fuel sources besides atomic energy, as well as biomass of vegetative and animal origin. Non-renewable energy resources are those whose reserves decrease irreversibly in the course of mining. They include all fuel fossil resources and fuel of atomic energy - uranium. All above-mentioned types of energy resources are primary ones.

Secondary energy resources (SER) is energy generated when using the energetic potential of waste, target, side and intermediate products formed in chemical-technological systems. Secondary energy resources can be partially or fully utilized for production energy supply.

Fuels are natural or artificial combustible organic substances being sources of heat energy and raw materials for chemical industry. Depending on aggregate condition the fuel is subdivided into solid, liquid and gaseous one. By origination it is subdivided into natural and artificial one. Natural fuel is subdivided into solid – brown and black coal, wood, peat and shale; liquid – oil; gaseous – natural gas and accompanying gas. Artificial fuels are products of natural fuel processing, namely: solid – coke, semi-coke, peat and coal bricks, charcoal; liquid – gasoline, kerosene and other liquid products of petroleum processing, liquefied gas; gaseous - generator gas, coke gas, char gas, hydrocarbon products of petroleum processing, and hydrogen.

Energetic and technological kinds of fuel are distinguished. Energetic fuel is used for electric and heat energy generation at thermal power stations and at boiler plants. Technological fuel is directly used for technological processes performance in industrial plants and furnaces, for example, for coking and gasification of solid fuel, roasting of silicate raw materials, in processes of drying, evaporation, thermal processing, etc.

Two basic energetic characteristics of fuel are distinguished. They are heat of combustion and power capacity (intensity).

Power capacity is the amount of potential heat energy in 1 kg of solid or liquid fuel (MJ/kg) or in 1 m3 of gaseous fuel (MJ/m3). For convenience to matching fuel of different kinds the fuel consumption is compared with the consumption of so-called equivalent fuel. The equivalent fuel is assumed the fuel whose 1kg combustion results in 29.3 MJ heat emissions. In relation to the equivalent fuel the specific power capacity of coal composes on average 33.5 MJ/kg. Oil and natural gas have higher power capacity (41.9 and 46.1 MJ/kg). Hydrogen is promising clean fuel having threefold specific power capacity (120.6 MJ/kg) compared to oil.

Heat of combustion (calorific value) is heat effect of fuel combustion reaction, i.e. the amount of heat emitted after complete combustion of 1 kg of solid or liquid fuel (MJ/kg) or 1 m3 of gaseous fuel (MJ/m3) and during cooling of combustion products to standard temperature.

2.2 Chemical composition of solid fuel

Solid fuel consists of combustible organic matter and non-combustible ballast part. Main ballasting components are moisture, volatile matter and inorganic compounds. Ballasting substances decrease the combustible part content in the fuel and thereby decrease its power capacity and increase unproductive expenses on transportation. Fuel organic matter has very complex chemical composition and includes carbon, hydrogen, oxygen, nitrogen and sulphur. Sulphur is harmful volatile admixture in fuel because sulphur dioxide polluting environment is formed during it burning. Sulphur is a component of both organic and mineral part of fuel as sulphides and sulphates. Sulphate sulphur after fuel combustion remains in ash composition in the unchanged form. Technical analysis of solid fuel includes determination of such characteristics as moisture content W, ash content А, volatile matter output V, sulphur content S and calorific value Q.

External, hygroscopic and chemically bounded moisture is distinguished in coal. External moisture usually covers coal granules as a thin film and it is removed by fuel drying at temperature 70-750С up to air-dried state. Hygroscopic moisture is absorbed by coal from the environment and it depends on air relative moisture content and environmental temperature and it can be removed by fuel drying under 1050С temperature up to the fuel constant mass. Chemically bounded moisture is included in the coal composition or in the composition of mineral admixtures of coal as crystallizing water, and it is called as internal or constitutional moisture. It can be only removed by destruction of coal crystalline lattice at high temperature of fuel roasting.

Moisture content in coal varies widely (3-10% in black coal) and it reaches 30-40% in brown coal. Moisture presence in solid fuel leads to increasing heat consumption for water evaporation and to decreasing calorific value; it hinds the coal enrichment, changes the coking rate and hence coke furnace productivity.

Mineral admixtures forming ash as a result of solid fuel burning are much more harmful ballast than moisture is. Mineral part of fuel consists of carbonates, silicates, phosphates, sulphides, sulphates of metals – calcium, iron, magnesium, aluminum, potassium, sodium, etc. When solid fuel burning most of them are converted into oxides and form solid residual named as ash. Increased ash content of fuel hinds strongly their using as energetic fuel and as chemical raw materials. Combustion of coal with high ash content causes often cleaning of combustion chambers.

So-called constitutional ash chemically bounded with coal is formed from mother-of-coal; so-called carried ash formed from dust, sand and clay silted into the coal with wind and water in the process of carbon formation. Both these kinds of ash form “fixed ash”. Ash included into the coal as an interlayer and different rocks inclusions and ash entered into the coal during its mining is called “free ash”. Ash content in the fuel varies widely: 3-30% in peat, up to 50% in shale and brown coals, 0.2-30% in black coals. Anthracites are most free from ash: their ash content exceeds 5% seldom.

Volatile matters represent vapour and gaseous products formed when fuel heating without air access. Volatile matter output depends significantly on conditions of testing – temperature, heating rate, fuel piece size, constructive characteristics of equipment. Volatile matter output for different kinds of fuel varies widely: (from 6% in anthracites to 10-40% in black coal, 45-55% in brown coal и 70% in peat). Volatile matter composition includes coal tar and gases: carbon monoxide, hydrogen, ammonia, methane, benzene and also sulphur dioxide.

When solid fuel technical analysis performance its composition is usually recalculated into absolutely dry fuel. Absolutely dry fuel is the fuel obtained after sample drying at temperature 105-1100С up to constant mass. Ash content and volatile matter output recalculated into absolutely dry fuel are noted correspondingly Aс and Vс.

3 THE TECHNIQUE OF ANALYSES CARRYING OUT

3. 1 The equipment and technical means:

1. Dryer ШС-80

2. Analytical balance ВЛТЭ-150

3. Laboratory muffle electric furnace SNOL 6.7/1300

4. Desiccator

3.2 The technique of determination of solid fuel moisture content

The fuel moisture content can be determined by direct and indirect methods. When direct weight method is used (according to GOST 9516-60) a fuel sample is dried in inert gas flow (nitrogen as a rule) at the temperature 105-1100C, and emitted water vapours are absorbed by magnesium chloride or sulphuric acid. When direct volumetric method is used (according to GOST 9339-60) a coal sample is heated with toluene and water vapours emitted from the coal together with toluene are stripped and the volume of condensed water is measured. These methods give sufficiently exact results, but they are relatively complex ones.

To determine moisture content of brown and black coal, anthracites, and oil shale the indirect method is more often used (GOST 6379-59). Its essence is in solid fuel drying at the temperature 105-1100C in a dryer                                                                                                                                                                                                                                                                                                                                                                                                                                                                 up to sample constant mass. The moisture mass in the fuel is determined on mass loss after drying.

The order of analysis carrying out to determine solid fuel moisture content by the indirect method:

1. Reduce the coal in a mortar up to powdered condition.

2. Weigh one gram of fuel under investigation on the analytical balance with accuracy to 0.001g in previously weighed weighing bottle of 25-30mm height and 20-25mm diameter. The fuel depth in the weighing bottle should not to exceed 5mm.

3. Spread the sample with light shaking and dried in previously heated dryer at the temperature 105-1100C. Thereat a weighing bottle cover should be half-open. Drying duration is 90 minutes for brown coals, 120 minutes for anthracites, and 50-60 minutes for other kinds of fuel.

4. At the end of specified time the weighing bottle with fuel sample inside is taken out of the dryer. Then close tightly the weighing bottle with the cover and cool it at first for 2-3 minutes in the air and then in the desiccator to the standard temperature. After cooling the sample is weighed on the analytical balance with accuracy to 0.001g.

5. Control drying is carried out for 30 minutes under the same temperature. If mass loss is more than 0.01g, the control drying is repeated while the loss is less than 0.01g or while mass increasing starts as a result of coal oxidation. In the case of mass increasing the last but one mass is accepted for calculations.

6. Calculate the moisture content W (%) in the fuel under investigation by the formula:

W=%                                            (4.1)

where ΔG1 is coal mass change after drying, g;

ΔG1= G- G1;

G is sample mass of the fuel under investigation, g;

G1 is mass of dried fuel, g.

3.3 The technique of determination of solid fuel ash content

The standard method of determination of ash content in solid fuel (GOST 6383-52) consists in combustion of the sample of fuel under investigation and following ash residual calcination up to sample constant mass at temperature 800±25°С for anthracites, brown and black coals and at 850±25°С for shale. Using higher temperature for shale analysis is explained by significant amount of carbonates in the mineral part which decomposition requires higher temperature.

The order of analysis carrying out to determine solid fuel ash content:

1. Weigh one gram of solid fuel on the analytical balance with accuracy to 0.001g in previously weighed porcelain crucible of 25-30mm height and 30mm diameter. Place the crucible into a muffle electric furnace heated up to the temperature 800±25°С.

2. After coal burning the formed ash residual is subjected to calcination at this temperature for 1.5 hour; then the crucible is taken out of the muffle furnace using crucible tongs and cooled at first for 5 minutes in the air and then in the desiccator to the standard temperature.

3. Weigh the cooled crucible with ash inside on the analytical balance with accuracy to 0.001g.

4. To obtain more reliable results the ash residual is calcinated for 30 minutes more while mass difference between two series weightings is less than 0.01g. If the mass increases then the previous value is used for calculations.

5. Calculate the ash content of solid fuel A, (%)by the formula:

А=                                                 (4.2)

where G is sample mass of the fuel under investigation, g;

G2 is mass of ash residual, g.

6. The dry ash content Аd is recalculated by the formula:

Аd=                                                   (4.3)

3.4 The technique of determination of volatile matter content

in solid fuel

The method of determination of volatile matter output (GOST 6382-65) in coal is based on coal sample heating without air access at the temperature 800±25°С for 7 minutes and on following determination of coal mass loss.

The order of analysis carrying out to determine volatile matter content in solid fuel:

1. Weigh one gram of the coal sample with known moisture content W on the analytical balance with accuracy to 0.001g in previously calcined and weighed porcelain crucible of 25-30mm height and 30mm diameter.

2. Enclose the crucible by a cover which doesn’t block up volatile matter outlet. The volatile matter outlet from a crucible is provided with a hole in a cover.

3. Preliminary heat the muffle furnace up to the temperature 800±25°С. Place the crucible with fuel sample into the furnace such that crucible bottom is above the furnace bottom on 10-20mm. The heat-resisting support is used for that.

4. The coal is heated for 7 minutes, then the crucible enclosed by the cover is taken out of the muffle furnace using crucible tongs and cooled at first for 3-5 minutes in the air and then in the desiccator to the standard temperature.

5. Weigh the cooled crucible with solid residual inside on the analytical balance with accuracy to 0.001g. The volatile matter content Vd in the coal under investigation is calculated on fuel mass loss after heating by the formula:

Vd  =   ,                                              (4.4)

where G1 are coal weight losses after heating, g;

G is fuel sample mass, g;

ΔG3 is fuel mass change after heating, g;

ΔG3= G- G3;

G3 is fuel mass after heating, g;

W  is moisture content in the sample under investigation, %.

6.  Based of obtained results the conclusion about the fuel quality is made.

- SAFETY PRECAUTIONS

1. Check the truth of the muffle furnace and the dryer hook up into the electrical network.

2. To conduct solid fuel calcination in the muffle furnace under the switched exhaust ventilation.

3. Take hot crucibles using crucible tongs only.

4. In a case of mains interruption or one phase breakdown all electric gauges must be immediately switched off.

5. In a case of wires or electric gauges firing it is necessary to disconnect them immediately and to extinguish with dry carbon dioxide fire extinguisher or with the asbestos cloth.

6. At electric trauma it is necessary to switch off a knife switch of an electric board. At loss of consciousness it is necessary to apply artificial breathing and to call a doctor.

5 CONTROL QUESTIONS

1. Classification of fuel-energy resources.

2. General characteristic of fuel, kinds of natural and artificial fuel.

3. Main energetic characteristics of fuel.

4. Chemical composition of solid fuel. Harmful ballasting substances of coals.

5. Composition of mineral part of the solid fuel. Characteristic of fixed and free ash. Disadvantages of coals with high ash content.

6. Moisture content in the fuel. Types of moisture bonding with the solid fuel. Methods of moisture removal from fuel.

7. Chemical composition of volatile matters. Harmful volatile admixtures.

8. Methods of solid fuel processing.

9. Essence of black coal coking. Products of the coking process.

#5 LABORATORY WORK

DETERMINATION OF WATER QUALITY INDICATORS

1 THE AIM OF THE LAB:

1. Practical acquaintance with standard methods of determination of different type’s water hardness and water oxidation susceptibility.

2. Water quality assessment for different water sources.

2 THEORETICAL INFORMATION

Water is widely used in chemical industry. It is applied as raw materials and a reagent for many chemical reactions. For example, it is used for production of hydrogen, sulphuric and nitric acids, soda ash, alkali sodium as well as in reactions of hydration and hydrolysis. Water has also an application as a solvent for solid, liquid and gaseous compounds in many productions of chemical, metallurgical, food and light industries. It is often used as an absorbent for purification and washing  different gases and solid materials from admixtures. Another direction of water using is enrichment of solid raw materials by means of flotation or hydromechanical method. All above mentioned examples deal with technological aims of water application. In addition water is applied in more large scales as a heat carrier or a cooling agent. Hot reacted flows formed as a result of exothermic reactions are cooled by cold water. Water steam or heated water is used for heating the cold interacting reagents to accelerate the process or to compensate heat expenses in endothermic reactions.

Natural water is divided into three kinds distinguished on admixture content. Atmospheric water is water of rain and snow precipitations. It contains the least amount of admixtures such as dissolved gases (CO2, О2, N2, H2S) and dust.

Surface water is water of open reservoirs, rivers, lakes, seas and channels. This water contains various mineral and organic substances. Sea water contains all chemical elements of Mendeleev's Periodic Table including precious and radioactive metals. Water containing less than 1g of salts per 1kg of water is called as fresh water. If it contains from 1 to 10g per 1 kg then it is called as saltish water; if this indicator is more than 10g per 1kg then this water is called as salt water.

Underground water is water of artesian wells, sources and geysers. It is characterized with diversity of dissolved salts’ composition which depends on composition and structure of soil and mining ores through which atmospheric and surface waters are percolated. Filtrating ability of soil and mining ores predetermines high transparence of underground water and absence of organic admixtures in it.

Since water is used in large scales not only as potable or sanitary water, but and for production purposes, then there are stringent specific requirements for water quality. Water quality is determined by such characteristics as transparence, colour, flavour, total salt content, hardness, oxidation susceptibility and water acidity.

Water oxidation susceptibility is an indicator characterizing organic admixtures’ content in water. It is determined by the amount of potassium permanganate necessary for organic compound oxidation. This value for natural water can vary over a wide range from milligram fractions to tens milligrams of oxygen per 1liter of water. Surface water has higher oxidation susceptibility as compared with underground water. Maximal permissible concentration according to permanganate demand for potable water is 5-7 mg/l.

Water acidity is characterized by hydrogen ion concentration and it is determined by means of specific indicator pH. pH is one of most important indicators of water quality. Natural water acidity is close to neutral reaction (рН6.8-7.3). Acidity of recycled water depends on process nature and purpose of used water. Water is acidic one if рН value is less then 6.5 and it is alkaline water if рН value is more then 7.5.

Total salt content characterizes presence of mineral and organic impurities in water. The amount of these impurities is determined by dry residual mass (mg/l) after 1liter of water evaporation and solid residual drying up to constant mass at the temperature 110°С.

Water hardness is the main qualitative indicator in many productions. It is predetermined by calcium and magnesium salts’ presence in water. These salts cause precipitate formation on inside surfaces of steam boilers, reactors and heat exchangers. By calcium and magnesium ion content three types of water are distinguished. Soft water contains less than 3mg-eq/l of Са2+ and Mg2+ ions, temperately hard water contains 3-6 mg-eq/l of these ions and hard water contains more than 6 mg-eq/l of calcium and magnesium ions.

Three types of water hardness are distinguished. They are temporary, permanent and total hardness.

Water temporary (carbonate) hardness is predetermined by calcium and magnesium hydrocarbonates content in water. These salts are converted into non-soluble carbonates when boiling. These solid salts precipitate according to the following reaction equations:

t

Са(НСО3)2CaCO3+H2O+CO2                          (5.1)

t

2Mg(НСО3)2MgCO3 ∙ Mg(OH)2+H2O+3CO2             (5.2)

Permanent (non-carbonate) hardness is predetermined by calcium and magnesium chlorides, nitrates and sulphates content in water. These salts aren’t converted into precipitates when boiling. Total hardness is determined as the sum of temporary and permanent hardness. Usually calcium salts determine carbonate water hardness and magnesium salts determine the level of non-carbonate hardness; and their sum forms total water hardness.

The appropriate water treatment precedes water using in the production. It depends on impurities presence in water and production requirements. Technical water shouldn’t contain impurities harmful for a certain reaction, corrode the equipment and form incrustation and sludge in apparatuses and pipelines. Impurities are usually in water in dissolved and colloid form or as coarse dispersions. Basic processes of water preparation are the following ones: water clarification using settling or filtration methods, water softening, in some cases – oxidation, desalting, neutralization, degasification and disinfection. Water clarification or coagulation of colloidal admixtures is performed by Al2(SO4)3, FeSO4, NaAlO2 coagulants addition. When organic compounds or elementary phosphorus occurrence in recycling water, it is necessary to oxidize them.

Water softening consists in complete or partial removal of calcium and magnesium salts from water. Coarse water softening (about to 0.3 mg-eq/l of hardness salts) is carried out by means of soda-lime method, i.e. by addition into water the amount of lime, caustic soda or soda ash required for precipitation of calcium and magnesium carbonate or magnesium hydroxide:

Ca(HCO3)2+Ca(OH)22CaCO3+2H2O                 (5.3)

Mg(NO3)2+Ca(OH)2Ca(NO3)2+Mg(OH)2               (5.4)

CaSO4 +Na2CO3CaCO3+ Na2SO4                   (5.5)

MgSO4+Na2CO3MgCO3+Na2SO4                   (5.6)

MgCI2+2NaOHMg(OH)2+2NaCl                    (5.7)

Lime or lime milk is considered as most accessible and cheap softening agent.  Fine water softening (about to 0.03 mg-eq/l) is reached by phosphate method at tri-sodium phosphate using as the softening agent. It permits to remove water temporary and permanent hardness simultaneously; thereat insoluble calcium and magnesium phosphates are formed:

3Ca (HCO3)2+2Na3PO4Ca3 (PO4)2+6NaHCO3             (5.8)

3MgCl2+2Na3PO4Mg3(PO4)2+6NaCl               (5.9)

The most effective method of water softening and demineralization is cation exchange method. The essence of this method consists in that some solid mineral and organic substances of low solubility are capable to extract from solutions certain cations and anions as a result of them exchange into other ones contained in these solutions. Cationites and anionites are used to extract Са2+, Mg2+, Fе3+ ions from water. Sulfonated coal or high-molecular resins containing active groups with Н+, Na+, NH4+ ions are cationites; high-molecular resins containing active groups with ОН-, HCO3- и С032- ions are anionites. Ion-exchange columns with various design are used for ion exchange water softening.

Water composition, possibility of its direct using for various purposes or necessity its preparation is determined based on technical analysis results. Total water analysis includes a lot of different determinations and it takes long time. The analysis consists in determination of colour, flavour, taste, acidity; content of oxygen, hydrogen sulphide, carbon dioxide, nitrates, nitrides, fluorides, organic substances, hydrocarbonates, etc. However the total analysis conducting is unwanted in many cases; one may be limited with a part of analyses only, and determination of various types of water hardness, oxidation susceptibility and acidity has the largest value.

3 THE TECHNIQUE OF LAB CARRYING OUT

3. 1 The equipment and technical means:

1. Electric closed heater

2. Chemical glassware

3. Titrimeter

4. Water still Liston А 1210

3.2 Determination of water temporary hardness

Determination of water carbonate hardness is based on the direct colour-indicator titration by 0.1n hydrochloric acid solution.

1. Take 100ml of water (tap water or from other sources) into a volumetric cylinder and place it into a conical flask.

2. Titrate water in the presence of methyl orange indicator by 0.1n hydrochloric acid solution up to orange colour transition into pink colour. During titration the neutralization of hydrochloric acid with magnesium and calcium hydrocarbonates takes place, which determines carbonate hardness, according to the reaction equation:

Ca(HCO3)2+2HCl=CaCl2+2H2O+2CO2                      (5.10)

- Water carbonate hardness Нc (mg-eq/l) is calculated by the formula:

(5.11)

where V1 is  the volume of 0.1n HCl solution spent for titration, ml;

0.0028 is hydrochloric acid titre on CaO (the amount of CaO (mg) matching to 1ml of 0.1n HCl solution);

10000 is coefficient for measurement units recalculation;

20.04 is Са2+ ions content (mg) in 1 litre of water matching to 1 mg-eq/l of hardness salts.

3.3 Determination of water total and permanent hardness

Determination of water total and non-carbonate hardness is based on the analogous titration of excess of Na2CO3 and NaOH equal volumes mixture added to water, that didn’t enter the reaction with magnesium and calcium salts of permanent hardness.

1. Water sample from the first analysis is subjected to boiling for 5-10 minutes for carbon dioxide removal.

2. 25 ml (known excess) of Na2CO3 and NaOH equal volumes mixture is added to water and this solution is subjected to boiling for 5-10 minutes to precipitate magnesium and calcium carbonates and hydroxides formed as a result of reactions:

CaCl2+Na2CO3=CaCO3+2NaCl                         (5.12)

MgCl2+2NaOH=Mg(OH)2+2NaCl                       (5.13)

MgSO4+Na2CO3=MgCO3+Na2SO4                                   (5.14)

3. When cooling is over the solution with precipitates is placed into the 250ml volumetric flask and it is diluted with distilled water up to the mark. The flask is closed by a rubber stopper and carefully mixed.

4. The precipitate is separated by means of filtration on the funnel with a paper filter. 100 ml aliquot of the purified solution is sampled by a pipette and replaced into the conical flask for titration.

5. Titrate this sample in the presence of methyl orange indicator by 0.1n hydrochloric acid solution up to orange colour transition into pink colour.

6. Separately take 25 ml of Na2CO3 and NaOH mixture solution (without water addition) and titrate analogously by 0.1n hydrochloric acid solution.

7. Water total hardness Ht (mg-eq/l) is determined by the formula transformed similar to the formula (5.11):

Ht = 1.4(V3-2.5V2)                                         (5.15)

where V3 is volume of 0.1n HCl solution, spent for titration of 25 ml of Na2CO3 and NaOH mixture solution, ml;

V2 is volume of 0.1n HCl solution, spent for titration of excess of Na2CO3 and NaOH mixture in testing sample of water, ml;

2.5 is dilution coefficient.

8. Water permanent hardness is determined as a difference of water total and carbonate hardness:  Hn = Ht – Hc

3.4 Determination of water oxidation susceptibility

Data of water oxidation susceptibility allows to judge the amount of oxygen (as KMnO4) necessary for oxidation of organic compounds in water. Redox titration is used for this indicator determination.

1. Take 100ml of testing water by a volumetric cylinder and place it into a conical flask.

2. Add 5ml of sulphuric acid (1:3) solution and 10ml of 0.01n potassium permanganate solution to the water sample.

3. The solution is subjected to boiling for 10 minutes. Add 10ml of 0.01n oxalic acid solution to the hot solution. Excess of oxalic acid is titrated by 0.01n potassium permanganate solution up to weakly pink colour appearance.

4. Water oxidation susceptibility X is expressed in amount of oxygen in one liter of water (mg/l) and it is determined by the formula:

X=(А+В-С)∙0,01∙8∙1000V= (А+В-С)∙80100=(А+В-С)∙0,8  (5.16)

where A is volume of 0.01n KMnO4 solution, added to water for organic admixture oxidation, ml;

B is volume of 0.01n KMnO4 solution, spent for titration of oxalic acid excess, ml;

C is volume of 0.01n oxalic acid (Н2С2О4) solution, ml;

0.01 is normality of potassium permanganate solution, mole/l;

8 is equivalent of oxygen, g/mole;

V is volume of testing water sample, ml.

Based on water analyses results the conclusion about water quality is made.

- SAFETY PRECAUTIONS

1. When hydrochloric, sulphuric, oxalic acids and potassium permanganate solutions using for chemical analyses it is necessary to be extremely attentive and to avoid skin contact with solution and eye damage.

2. When solution boiling on the electric heater it is necessary to observe safety regulations when operating with electric heaters.

3. In a case of mains interruption or one phase breakdown all electric gauges must be immediately switched off.

4. In a case of wires or electric gauges firing it is necessary to disconnect them immediately and to extinguish with dry carbon dioxide fire extinguisher or with the asbestos cloth.

5. At electric trauma it is necessary to switch off a knife switch of an electric board.

- CONTROL QUESTIONS

- Water application in chemical industry.

- Comparative characteristic of natural water and its composition.

- Basic indicators of water quality.

- Water classification by hardness. Water hardness characteristic.

5. Methods of industrial water treatment. Sewage purification from mechanical and chemical admixtures.

6. The characteristic and essence of methods of water softening.

#6 LABORATORY WORK

STUDYING THE HETEROGENEOUS PROCESS OF PYRITE ROASTING

1 THE AIM OF THE LAB:

1. Practical studying the heterogeneous process of pyrite roasting.

2. Master the process control methods and SO2 output determination (sulphur burn-out degree) depending on process conditions: temperature, pyrite reduction degree, roasting time).

3. Determination of optimal technological mode of the process.

2 THEORETICAL INFORMATION

2.1 General characteristic of sulphuric acid production

Sulphuric acid is one of the most important productions of chemical industry. This production occupies the first place by output and consumption among heavy chemicals. Technical sulphuric acid can be produced by two different methods – tower and contact methods which differ in the mode of sulphur dioxide oxidation. If nitrogen oxides are used as a catalyst for SO2 oxidation, then this method is called as a tower (or nitrous) method. If this reaction takes place on a solid catalyst, for example vanadium oxide (V), then sulphuric acid is produced by a contact process. Nowadays the tower method isn’t used in chemical industry because of some disadvantages, and the contact method is widely used.

The quality of different kinds of sulphuric acids significantly differs in main component (sulphuric acid) and impurity content. According to GOST requirements the tower acid contains at least 75% of Н2SO4 and a lot of impurities, primary nitrogen oxides, whereas the contact acid contains at least 92.5% of Н2SO4 and doesn’t contain similar impurities.

Raw materials for sulphuric acid production are elementary natural sulphur and natural sulphur containing ores being a sulphur dioxide source. These are iron sulphide, non-ferrous metal sulphides (copper, zinc, lead, etc.), and hydrogen sulphide. Iron pyrite is traditionally major raw material source. Its basic component is iron disulphide. At present the share of using waste gases of non-ferrous metal production for sulphuric acid production increases significantly. These gases contain more than 5% of sulphur dioxide and some impurities.

The first stage of sulphuric acid production is raw material oxidation (for example, pyrite roasting) forming roasting gas containing sulphur dioxide. The next step is dry purification of roasting gas from cinder dust and wet washing this gas from chemical admixtures that can be catalytic poisons for vanadium oxide catalyst of sulphur dioxide oxidation. After the completion of purification and desiccation of roasting gas from sulphuric acid fog it is fed to contact oxidation into sulphur oxide (VI). This process takes place under temperature 440-6000С in a contact apparatus on 4-5 layers of a catalyst. The oxidation is performed with intermediate gas cooling between catalyst layers in order to maintain high process rate and to attain maximum SO2 oxidation degree. The final stage of the production is SO3 absorption by concentrated sulphuric acid in absorbers. If natural sulphur is used as raw materials for this production, SO2 containing gas formed after sulphur burning isn’t subjected to purification from admixtures failing this.

2.2 Physical-chemical regularities of pyrite roasting

The pyrite roasting is performed in furnaces with different construction in the air flow under atmospheric pressure. The process takes place in several stages. At first the thermal decomposition of iron disulphide FeS2 takes place forming iron sulphide FeS and a vapour sulphur:

2FeS2→2FeS+S2-Q                                           (6.1)

Sulphur evaporation begins under the temperature about 5000С and the process is accelerated essentially when the further temperature increasing. The vapour sulphur burns forming SO2; the same reaction proceeds when the elementary sulphur (as initial reagent) burning:

S2+2O2→2SO2+Q                                           (6.2)

The heat of sulphur burning is utilized for provision of endothermic reaction of FeS2 decomposition at the first step of the process. Iron sulphide burns if the temperature rises up to 8000С and it is oxidized into iron oxide (III) according to the reaction equation:

4FeS+7O2→2Fe2O3+4SO2+Q                                (6.3)

The total process of the pyrite burning is described by the reaction equation:

4FeS2+11O2→2Fe2O3+8SO2+Q                              (6.4)

Reactions of iron oxides FeO and Fe3O4 formation can also take place simultaneously. A solid residue after the roasting called as a cinder consists of iron oxides FeO, Fe3O4, Fe2O3 and it contains 0.5-2% of un-burnt out sulphur. Depending on the furnace type the roaster gas contains 7-13% of SO2, 4-11% of O2, up to 0.5% of SO3 and nitrogen.

The pyrite roasting is a typical heterogeneous process, and the total rate of the process is expressed by the formula:

( 6.5)

where is process total rate expressed as the change of obtained product amount in a unit of time;

is process rate constant, called as mass transfer coefficient;

F is interface of reacting phases, m2;

ΔС is driving force of the process, determined as a difference of gaseous reagent concentrations in the gas phase volume and on the interface.

Increasing the process driving force can be reached by increasing oxygen concentration in the gaseous phase (air) or by withdrawal of gaseous product SO2 out of the reaction zone.

The film of iron oxides is formed on the sulphide surface when roasting takes place; therefore oxygen access to the un-burnt pyrite is hindered and further sulphur burning-out slows down.  This process is usually limited by the rate of air oxygen diffusion towards the surface of non-oxidized core FeS through the layer of formed cinder and by the rate of reverse SO2 diffusion outside the pyrite core to the gaseous phase through cinder pores. This process of inside diffusion limits the total pyrite roasting rate. In this case the chemical reaction rate doesn’t effect on the process total rate.

When the burning starts, the pyrite surface is rich with sulphur and the gaseous film is the main resistance to oxygen diffusion to the surface. Further during the burning process the surface sulphur atoms burn out and the pyrite surface is covered with the film consisting of iron oxides. As the result an oxygen access to pyrite non-burnt part is complicated. At last when the thickness of iron oxide film reaches limit size for given conditions then the oxidation process stops practically.

Temperature extremely increasing (above 8500С) causes agglomeration of pyrite solid granules; hence it causes interface decrease and the process rate decrease. The flow turbulence has the great importance for the heterogeneous process rate increasing. The interface increasing is reached by the pyrite reduction and by intensive mixing of solid phase particles. However excess reduction would lead to essential agglomeration. The pyrite surface is renewed when mixing and it is released from the cinder layer. Therefore the contact of non-reacted pyrite particles and air oxygen is facilitated. Methods of mixing of roasting material particles in air are determined by the type and construction of furnaces. Presently three types of furnaces are used for sulphide raw material roasting. They are a mechanical shelf furnace, a dust roasting furnace and a fluidized-bed (“boiling layer”) furnace. The boiling layer furnace is most effective one to provide for maximal interface and conditions for intensive sulphur burn-out. Herewith the reaction heat is utilized for water steam generation. The disadvantage of these furnaces is significant cinder dust loss with the roaster gas; it predetermines further thorough cleaning this gas from admixtures.

3 THE TECHNIQUE OF LAB CARRYING OUT

3. 1. The equipment and technical means:

1. Laboratory electric tube furnace SNOL 0.2/1250

2. Chemical glassware

3. Titrimeter

4. Distiller Liston А 1210

5. Analytical balance ВЛТЭ-150

6. Water-jet pump

3.2 Laboratory plant description

Establish a laboratory plant for pyrite roasting due to the scheme (Fig. 9). The plant consists of electric tube furnace 1 with a quartz tube 2 where a lab boat 3 with a pyrite sample is placed. Temperature control and regulation is conducted automatically; temperature reading inside the tube in the roasting zone displays on the dash display 4 at the bottom of the furnace. The tube is free for air access from one side; the second side is closed down hermetically by a rubber plug 6 with a glass pipe 7, through which formed roaster gas goes into the absorption flask 8. The process is available due to the gas draw off by the water-jet pump 9.

3.3 The order of lab carrying out

1. Take 100ml of 0.1n iodine solution into a volumetric cylinder and place it into a conical flask.

2. The furnace tube is closed down hermetically by a rubber plug with a glass pipe which is connected with the absorption flask; the pipe is submerged in iodine solution.

3. Switch on electric furnace heating up.

4. Take the pyrite sample 0.4g on the analytical balance with accuracy to 0.001g and place it in the lab boat.

1-electric furnace, 2-quartz tube, 3-lab boat, 4-temperature display, 5-constant current source, 6-rubber plug, 7-glass pipe, 8-absorption flask, 9-water-jet pump Fig. 9. Scheme of the plant for pyrite roasting

5. When 5000С temperature attainment the lab boat with pyrite sample is placed into the center of the tube by means of crucible tongs. Switch on the water-jet pump and carry out roasting for 60 minutes.

6. The roaster gas containing sulphur dioxide is removed from the furnace and absorbed by 0.1n iodine solution in the absorption flask. If the iodine solution is discoloured during absorption then add more 25ml of this solution into the flask.

The gas absorption is accompanied with interaction of iodine and sulphur dioxide due to the reaction equation:

SO2+2H2O+J2=H2SO4+2HJ                                     (6.6)

7. Switch off furnace heating up when roasting completing; take out carefully the boat from the furnace tube.

8. Titrate excess of iodine by 0.1n sodium thiosulphate solution in starch indicator presence up to solution discolouration. This titration is described by the reaction equation:

J2+2Na2S2O3 = 2NaJ+Na2S4O6                                             (6.7)

9. Determine the mass of burnt-out sulphur on a basic of titrant volume spent for the titration.

4 CALCULATIONS OF TECHNOLOGICAL INDICATORS AND DETERMINATION OF PYRITE ROASTING OPTIMAL MODE

1. Calculate theoretical amount of formed sulphur dioxide GT at complete sulphur burn-out taking into account sulphur content in the pyrite:

(6.8)

where a is pyrite sample mass, g;

b is  sulphur content in pyrite;

32 and 64 are molecular masses of S and SO2 correspondently.

Calculation is carried out according to the total equation of the roasting reaction (6.4).

2. Calculate factual amount of burnt-out sulphur qs (g) based on titration results by the formula:

qs = 0.0016 (VI – VST)                                        (6.9)

where 0.0016 is titre of iodine on sulphur, matched to 1ml of 0.1n iodine solution reacted with SO2;

VI is volume of 0.1n iodine solution in the absorption falsk, ml;

VST is volume of 0.1n sodium thiosulphate solution, spent for titration of iodine excess, ml.

3. Practical amount of burnt-out sulphur Gfact in recalculation on SO2 is calculated by the formula:

(6.10)

4. Determine sulphur burn-out degree α (%) as a product output by the formula:

(6.11)

5. Fixing time of roaster gas flow to the flask one can obtain data for kinetic curve =f() generation. The research assignment can be given to study sulphur burn-out degree dependence on the roasting temperature and pyrite reduction degree. Obtained experimental data and calculation results are tabulated in the Table 7. Based on established dependences determine the optimal mode of sulphur-containing raw material roasting.

Table 7. Conditions and indicators of pyrite roasting

| N | Pyrite sample mass, g | Sulphur content in py-rite, % | Roasting tempera-ture, 0С | Roasting time, min | Volume of Na2S2O3 solution, ml | Amount of burnt-out sulphur qs, g | Factual mass of SO2 Gfact, g | Theore-tical mass of SO2, GT, g | Sulphur burn-out degree , % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |

5 SAFETY PRECAUTIONS

1. Check the set plant for tightness.

2. Sulphur dioxide is chemically toxic gas. In a case of poisoning this gas it is necessary to get out casual of a hazard area and to transport on fresh air as soon as possible. At loss of consciousness it is necessary to apply artificial breathing and to call a doctor.

3. Take hot lab boat using crucible tongs only.

4. It is prohibited to touch uninsulated electric wires or ungrounded equipment bodies with hands or metallic items.

5. In a case of burn the damaged skin to wash out by 2% soda ash solution or by potassium permanganate solution.

6 CONTROL QUESTIONS

1. Methods of sulphuric acid production.

2. Comparative characteristic of raw materials for sulphuric acid production.

3. Basic stages of sulphuric acid production.

4. How are the roasting rate and the sulphur burn-out degree determined?

5. Factors influencing on pyrite roasting rate.

6. Justification of the upper limit by temperature for the roasting process. Methods of the pyrite roasting intensification.

7. Describe a chemical scheme of iron disulphide oxidation.

8. Types of furnaces used for pyrite roasting. Advantages and disadvantages of boiling layer furnace.

#7 LABORATORY WORK

POLYCONDENSATION OF PHENOL AND FORMALDEHYDE

1 THE AIM OF THE LAB:

1. Carry out synthesis of novolacquering or resol resin through polycondensation of phenol with formaldehyde by means of both experimental and virtual methods.

2. Master skills of virtual lab carrying out on the computer program.

2 THEORETICAL INFORMATION

Natural and synthetic high-molecular organic compounds (HMC), namely cellulose, chemical fibers, plastics, rubber, lacquers, glues, films, etc. have a tremendous importance in national economy. Materials on a basis of HMC can be hard or soft, transparent for light or not, elastic and rigid, can combine high durability with low density, can be soundproof and chemically resistant ones.

HMC-polymers are a special class of organic compounds, cosisting of molecules-giants (macromolecules), formed as a result of chemical interaction of the large number of initial molecules-monomers. Tens and thousands atoms are in these compounds’ composition; a molecular mass is from several hundreds to tens of millions of carbon units.

Polymerizational and polycondensational HMC are distinguished by a production method. In both cases molecules of initial compounds must have in their structure multiple hydrocarbon bonds or non-stable cyclic grouping or functional groups =С=, С≡С-, =С=О, СН2=СНХ, x-haloid, oxi-, amino-, cyano groups etc., which are capable to react each other or with other molecules with polymer formation.

Polymerization reaction is a process of monomer molecule combination into a big polymer molecule, which has the same elementary structure, as an initial monomer has:

(7.1)

where R is a substituent.

Hereat any low-molecular side products aren’t formed, the reaction is accompanied with heat emission and it is irreversible one. Polyethylene, polyvinylchloride, polystyrene, fluoroplastic, etc. are typical polymerization HMC.

Copolymerization – is a process of mutual polymerization of two or more monomers with different chemical composition. The copolymerization process is similar to the polymerization process, however it has some features:

1. Copolymerization takes place easier between monomer molecules with a close structure;

2. Some monomers aren’t capable to form polymers, but they can be easily copolymerized with monomers of the different structure.

Polycondensation reaction is a process of HMC formation as a result of monomer molecules’ interaction between each other; herewith together with a polymer also low-molecular side products are formed (water, ammonia, carbon dioxide, alcohol etc.). Presence of these reaction products determines the process reversibility. Depending on the method and initial monomer structure the polycondensation reaction can be either reversible or irreversible one. As a rule the irreversible polycondensation proceeds with high rate and the reversible one takes place with low rate.

Since the polycondensation reaction proceeds with great amount of heat emission, i.e. it is exothermic one, then after equilibrium reaching molecular mass of final products will be more at lower temperature. Therefore for high process rate reaching at first the polycondensation would be carried out at high temperature with its decreasing when nearing to the equilibrium state for obtaining the product with big molecular mass.

Phenol-formaldehyde resins as well as polyurethane, polyamide, epoxide resins, etc. are polycondensational ones. For phenol-formaldehyde resin obtaining the equilibrium constant is К=10000, therefore the equilibrium state is shifted aside to final products, and forming water as a side product almost doesn’t  effect on polycondensation process kinetics.

The rate and the direction of polycondensation reactions, as well as obtaining compound composition and character depend on such factors as proportion of reacting substances and their properties, the number of functional groups, interface of reagents (on stirring), temperature, intensity of formed low-molecular side product removal (for equilibrium state shift to the right) and on the used catalyst kind. Herewith thermoplastic (hot-melt) or thermoreactive (heatset) resins can be formed.

Thermoplastic resins with a linear structure are melted when heating and they solidify again when cooling; they are dissolved in certain solvents. And vice versa thermoreactive resins with netting plane or space structure pass into infusible and insoluble state when heating or prolonged storing. Thermoplastic resins are known as novolacquering ones. Novolacquering resin is formed in phenol excess in an initial mix (7 moles of phenol to 6 moles of formaldehyde) and mineral acids (HCl, H3PO4, H2SO4, (COOH)2) are used as catalysts.

The reaction can be represented in general form:

nCH2O+(n+1)C6H5OH      H(-C6H3(OH)CH2-)n-C6H4OH+nH2O    (7.2)

The resin structural formula has a linear structure:

where n is polymerization degree characterizing the number of repeating elementary units which defines HMC chain length (n=4÷8).

The less molar ratio of phenol to formaldehyde is, the more molecular mass of an obtaining resin is. Polycondensation time increasing promotes to more complete phenol binding with formaldehyde and to increasing the average molecular mass of final products. Novolacquering resins are used for production of press powders, abrasive products and gas filled materials.

In formaldehyde excess (6 mole of phenol to 7 mole or more of formaldehyde) and if any alkali (NH4OH, NaOH, Ba(OH)2) or alkaline metal salt are used as catalysts the thermoreactive or resole  resins are formed. Resole resins differ from novolacquering ones in the capability to transit in infusible, insoluble state when heating above 1200С, i.e. in thermoreactive property. Three states of resole resins are distinguished depending on hardening degree:

a) resole (bakelite A) is the mixture of high-molecular products, melting when heating up to temperature 70–750С and soluble in an alcohol or in an acetone; it has a linear structure;

b) when heating up to 900С or prolonged storing the resole is converted into resitol (bakelite B) with divided structure; it is partly soluble in an alcohol and an acetone, swells significantly and it isn’t melted when heating, it is only softened and is converted into an elastic state;

c) resit (bakelite C) is the last stage of polycondensation (at higher temperature and pressure); resit  isn’t softened when heating and doesn’t swell in solvents; this process of hardening consists in binding long linear chains by across bonds:

3 THE TECHNIQUE OF LAB CARRYING OUT

3.1 The equipment and technical means:

1. Laboratory plant for resin synthesis

2. Chemical glassware

3. Analytical balance ВЛТЭ-150

4. Electric closed heater

5. Sand bath

6. Water bath

3.2 Laboratory plant description

The laboratory plant for phenol-formaldehyde resin synthesis (Fig. 10) consists of a water bath 2 with inside established reactor for the synthesis – three-neck round-bottomed flask 1 equipped with a reverse cooler 5 and a stirrer 3 geared by an electric motor 4. The cooler and the stirrer are set in the flask middle neck. A thermometer 6 is placed in one side neck of the flask; the second side neck is closed by a plug and used for reaction mix sampling during the reaction or a drop funnel is inserted in it. The plant is fixed at the stand 7; the electric closed heater 8 is used for water bath heating.

3.3 The order of novolacquering resin preparation

1. The mix of crystalline phenol and formaldehyde water solution (in the mole ratio (1.12-1.42):1) is mixed in three-neck round-bottomed flask at the room temperature up to phenol full dissolution. Reagent consumption is calculated for 10-20g of phenol.

2. Then an acidic catalyst (as HCl, H2SO4  in amount of 0.3 to 1-1.5% of phenol mass) is added to the mix into the flask. The flask is connected with a reverse cooler and it is placed into the water bath heated to 90-1000С. Carry out synthesis at constant mix stirring.

3. Perform the reaction until formed water layer stop to change in volume. To control it the reaction mix is sampled from time to time from the flask side neck and cooled.  The reaction completion is determined if stable turbidity is appeared in the mix after water evaporation from the sample and the resin cooling. If the resin doesn’t solidify the boiling should be continued.

4. It should be paid attention to intensity of the reaction proceeding. The mix is usually heated up to 90-950С. If the violent reaction takes place (usually after 20-30 minutes of heating) and the liquid starts to boil intensively then it is necessary to stop heating. And the reaction goes on some time without heating at the account of exothermic reaction heat effect with temperature increase up to 1000С.

1-three-neck flask, 2-water bath, 3-stirrer, 4-electric motor, 5-reverse cooler, 6- thermometer, 7-stand, 8-electric closed heater Fig. 10. Scheme of the plant for resin preparation

5. When the violent reaction is over then heating is continued up to the reaction completion and mix separation into two stable layers.

6. Water layer is pored out of the flask and the resin is poured into a porcelain cup for drying at temperature 130-1600С under constant stirring at the sand bath. The drying stops when solidified resin drop is easily grinded. The dried resin is weighted and its output is determined.

3.4 The order of resole resin preparation

1. The mix of crystalline phenol and 37% formaldehyde water solution (in the mole ratio (1:1.16) and 25% ammonia water solution as a catalyst (1.0-1.5% of phenol mass) is mixed in the round-bottomed flask at the room temperature up to phenol full dissolution.

2. The flask is connected with a reverse cooler. The mix is heated up to boiling temperature 90-950С in the flask under stirring at the water bath.

3. The mix is subjected to boiling for 10-15 minutes for polycondensation reaction completion. To fix the end point of a reaction the reaction mix 2-3ml is sampled from the flask by a pipette into a test tube. Determine the temperature of mix turbidity. For that cool the test tube gradually to 100С. If the mix turbidity doesn’t appear after water evaporation from the sample and the resin cooling the heating should be continued for 10-15 minutes more.

4. When the process completing the heating up is switched off and replace the mix into the porcelain cup and cool it. Upper water layer is pored out of the cup. Wash out the resin by water several times up to the neutral medium and weight the cup with resin.

5.  Determine the formed resin mass.

The obtained resole resin is a viscous mix having color from yellow to brown one. In a case of mix superheating over given temperature the resin is capable to transit into solid non-fusible and non-soluble form (resit).

3.5 The order of virtual lab carrying out

Virtual lab is created on the basis of computing program. It includes theoretical information about the process of polycondensation of phenol with formaldehyde, program description as well as control test questions for performance and defense of the work (Figures 11-14). The special methodical instruction for a computing lab contains methodical recommendations to fulfill every part of this work and plant scheme as well. This program is developed on the basis of resin synthesis mass balance.

To perform the virtual lab on novolacquering or resole resin synthesis a student has firstly to answer access control questions containing requirements for lab carrying out:

1. Initial reagents for novolacquering resin preparation.

2. Initial reagents for resole resin preparation.

3. The mole ratio of phenol to formaldehyde for novolacquering resin preparation.

4. The mole ratio of phenol to formaldehyde for resole resin preparation.

5. Temperature of phenol-formaldehyde resin synthesis.

6. Catalyst consumption for resin preparation, % of phenol mass.

7. A catalyst of resole resin synthesis.

8. What is the kind of novolacquering resin?

9. The end point of the reaction of novolacquering resin preparation is determined by…

10. What is the type of the reaction of phenol-formaldehyde resin preparation.

11. Reaction mix is heated by means of…

The student is allowed to fulfill the work after right answers all the questions. If at least one wrong answer is made it should to come back and to take an access test again. Then calculate initial reagent consumption for novolacquering or resole resin preparation: based on main reaction equation calculate mole and mass consumption of formaldehyde for 10g of phenol and put it into relevant windows.

Then it is necessary to choose a catalyst and to calculate consumption coefficients for reagents and a catalyst. If the calculation is correct the student starts to carry out polycondensation process using buttons “turn on” and “turn off”. To approximate virtual conditions to real conditions of the process the temperature dependence on the process time is provided. When maximal temperature reaching the heating is switched off and the following process is carried out to the mix cooling to 800С. If the synthesis mode is observed the obtained result is shown by the button “ready” activation – mass of formed resin and water and the structural formula of the target product.

After the work completion students should answer 20 control questions for work defense containing theoretical information about the synthesis of polycondensational resins:

1. What resin has the linear structure?

2. What structure matches to thermoplastic resins?

3. What resin isn’t thermoreactive one?

4. Bakelite B is…

5. Phenol-formaldehyde resin is formed by the reaction equation…

6. Reaction of novolacquering resin preparation.

7. Polymerizational resin is …

8. Disadvantage of polycondensational resins in comparison with polymerizational ones.

9. The process of phenol-formaldehyde resin preparation is …

10. Reactor for polycondensation performance.

11. Resit difference from other resole resins.

12. Low-molecular product formed in the course of polycondensation.

13. The catalyst of resole resin synthesis.

14. Equilibrium constant of resin synthesis shows that…

15. Temperature mode of phenol-formaldehyde resin preparation.

16. Temperature mode selection is conditioned by…

17. What factor has no affects on the polycondensation rate?

18. n(CH2 = CHR)  (– CH2 – CHR –)n is the reaction of …

19. Copolymerization – is a process of linkage of …

20. Polycondensation - is a process of linkage of …

If the student made more than 3 mistakes he would fulfill the work again. It is not required to make up a report on this lab and the computer program grades for the student’s work.

# The description of program windows

# Fig. 11. The initial program window

Fig. 12. The access test window

# Fig. 13. The program interface

The timer is turned on with the heater turning on and it shows experiment duration (minutes).

1- window showing obtained resin mass (g)

2- window showing obtained water mass (g)

3- window showing obtained resin structural formula

4- button for defense test window call; the defense test is similar to the access test

Fig. 14. The results display window

- SAFETY PRECAUTIONS

1. Check the truth of the plant assembling.

2. Establish the lab plant in the operating draft cupboard.

3. Switch on the exhaust ventilation before the synthesis start.

4. When the violent mix boiling in the flask it is necessary to stop heating the water bath.

5. Sample production mix from the flask by means of a pipette with a rubber pear and provide for excluding the reaction mix contact with a face and hands.

6. Carry out water evaporation from the resin in the porcelain cup at the sand bath under switched on exhaust ventilation only.

7. In a case of mains interruption or one phase breakdown all electric gauges must be immediately switched off.

8. In a case of wires or electric gauges firing it is necessary to disconnect them immediately and to extinguish with dry carbon dioxide fire extinguisher or with the asbestos cloth.

5 CONTROL QUESTIONS

1. Characteristic of high-molecular compounds.

2. Methods of HMC production.

3. Comparison of polymerization and polycondensation processes.

4. Synthesis of polycondensational resins, their composition and process kinetics.

5. Choice of optimal conditions of thermoplastic and thermoreactive resin production.

6. Physical and physical-chemical properties of novolacquering and resole resins.

#8 LABORATORY WORK

METHODS OF CORROSION TESTING

1 THE AIM OF THE LAB:

1. Acquaintance with methods of qualitative and quantitative assessment of metal corrosion resistance.

2. Determination of corrosion resistance of the metal under investigation.

2 THEORETICAL INFORMATION

2.1 Characteristic of corrosion processes

Requirements for constructive materials in chemical technology significantly differ of these in mechanical technology. Materials used in production of machine parts for mechanical treatment of materials, must possess mainly properties like durability, hardness and strength, i.e. only mechanical properties are taken into account. As a rule simple ferrous metals such as cast iron and steel satisfy to these requirements. In construction of apparatuses for chemical processes as well as for raw materials and products transportation and storage in chemical industry one of main requirements is material chemical resistance. Chemical resistance is so important, that for this strong decrease of material mechanical properties is often ignored. So, for example, steel is substituted by less strong, non-hard and non-elastic lead or by less thermal resistant materials or, at last, comparatively friable ceramic materials.

The metal corrosion is material destruction as a result of chemical or electrochemical interaction with corrosive medium. A metal is corrosion resistant when it resists to outer corrosive medium effect, or, by other words, if a corrosion rate is small. The less corrosion is, the higher metal corrosion resistance is. The measure of corrosion resistance is the corrosion rate in given medium and in given conditions. Corrosion rate is often expressed as mass of destructed metal converted into corrosion products in a unit of time on unit metal surface (kg/ m2∙h). The amount of destructed metal can be expressed as well by a thickness of a metal layer, converted into corrosion products in a unit of time (mm/year).

Corrosion products can be separated in solid, liquid and gaseous state. Solid products (oxides, salts) can form a continuous film on the metal surface and thus keep it from further aggressive medium effect. Artificial creating such protective films is called passivation. It is often used as one of methods of material chemical protection.

By a character of metal destruction uniform and local corrosion is distinguished. In a case of uniform corrosion corrosive destructions are comparatively uniformly spread on entire metal surface. Local (nonequal) corrosion takes place when the considerable part of metal surface is free of corrosion and the corrosion is concentrated only on separate areas as dots, spots, pits. The specific kind of local corrosion is intercrystallite one, which is characterized by that the interlayer between large granules (crystallites) or outer layers of granules with different composition than granules in their mass are subjected to corrosion. Corrosion cracks appear at simultaneous aggressive medium effect and mechanical strength. This kind of corrosion is especially dangerous, because surface appearance stays often almost invariable at strong degradation of mechanical properties.

By the character of the process itself, metal corrosion can be divided into two big classes: chemical and electrochemical corrosion.

Chemical corrosion is the process of metal direct contact with medium aggressive components. Usually red-ox process takes place, in which medium aggressive component is an oxidizer. Oxides (MemOn) and metalorganic compounds can be corrosion products. Typical chemical corrosion is metal corrosion by aggressive gases at high temperatures, for example, oxidation by air oxygen with formation of oxide film. In addition, the action of inorganic waste gases of chemical productions (SO2, NO, NO2, HF, HCl) cause chemical corrosion with metal destruction. Chemical corrosion is also observed in liquids, which are not electrolytes, for example, in anhydrous alcohols, benzene, gasoline, kerosene etc.

By destruction character the chemical corrosion is uniform one. Usually the growth of corrosion product layer on the metal surface takes place in gaseous phase, and corrosion product peeling or falling-off from metals or its dissolution is possible in liquid phase. Chemical corrosion process is subjected to regularities of heterogeneous chemical processes, i.e. a corrosion rate is expressed by the formula:

(8.1)

where Gм  is amount of corroded metal or obtained corrosion product, g;

is corrosion time;

KM is corrosion rate constant;

ΔС is corrosion driving force, expressed in grams of the aggressive component on 1m3 of medium (gas, liquid) on the boundary with metal, g/m3.

For constant corrosion driving force or for determining its average value in corrosion period this formula can be changed into the integral form:

G=KMFC         		                  	             (8.2)

Electrochemical corrosion proceeds under the action of electrolyte solutions on metals. It takes place because of thermodynamic non-stability of metals in electrolyte solutions. The surface of the metal under corrosion can be imagined as a system of micro- and macrogalvanic pairs. Such pair’s appearance is explained by presence in metals admixture granules of other metals, surface pollution with more or less electrode potential, structural non-uniformity of internal tensions and metal deformation, by difference in electrolyte concentrations boarded with metal different parts, etc. In all this cases metal different areas are distinguished in the value of electrode potentials. Areas with less electrode potential (more electronegative) become anodes in electrolytes, and more positive ones are cathodes. Accordingly anode and cathode corrosion processes take place. The anode process consists in transition of metal ions into solution (metal dissolution), for example:

Ме0Ме+2+2e                                            (8.3)

and electrons stay on the metal surface. On the cathode cations are discharged for example, hydrogen ions:

2H++2eH2                                                 (8.4)

and oxidizer reduction takes place, for example, oxygen transition into hydroxide ions:

O2+2H2O+4e4OH-                                        (8.5)

(8.4) reaction is observed in acidic solutions and (8.5) reaction takes place in neutral and alkaline solutions. Within metals the electron flow from an anode to a cathode is formed, which is called as corrosive current. As a result of electrochemical corrosion on the place of metal anode areas corrosion spots and pits appear; this corrosion is nonequal one.

Electrochemical corrosion takes place according to electrolysis laws; therefore the amount of dissolved metal can be determined by formulas:

(8.6)

(8.7)

where A is metal atomic mass;

F is Faraday’s number; 26.8 а-h/g-eq;

n is metal valency;

I is strength of current, a;

is time of electrolysis, h;

E is electrochemical equivalent, g/a∙h;

(8.8)

There are many methods of metal protection from corrosion depending on specific conditions. Most radical solution is selection of such constructive metal which would meet physical-mechanical requirements and herewith not corrode in an aggressive medium; however it is not always possible. Therefore combination of different materials is used for apparatus construction; part of materials take a mechanical load and the second serves as a protector from corrosion.

All methods of equipment preservation from aggressive component effect can be divided into following groups:

1. using corrosion resistant metals;

- using metallic protective coatings;

3. using nonmetallic inorganic materials as basic constructive materials or for metal construction protection;

4. using corrosion resistant organic nonmetallic materials as basic constructive materials or for metal construction protection;

5. chemical protection of metals by formation of protective films by interaction of the metal with medium (oxide and salt films) or by inhibitor using, or by medium composition regulation;

6. electrochemical protection by anode protector or constant current source using.

2.2 The essence of methods of metal corrosion testing

Qualitative and quantitative methods are used for metal corrosion testing. Qualitative methods don’t give full characteristic of metal resistance and therefore they are additional ones. Quantitative methods enable to determine the rate of metal corrosion in different medium.

Qualitative methods of metals corrosion resistance assessment include:

1. Visual observation; the following change is defined thereat:

a) change of metal surface appearance;

b) appearance of corrosion products, their character and spreading; color and view is registered;

c) change of corrosion medium is registered: change of solution colour is fixed.

2. Macroscopic method is the study corroded and corroding areas by means of relatively small electronic magnification.

3. Microscopic investigations enable to study local and selective character of corrosion and intercrystallite corrosion.

4. Indicated method is based on determination of location of anode and cathode parts on the surface of corroding metal through formed colored compounds by certain reagent interreaction with corrosion products.

Quantative methods enable to determine metal corrosion rate in different medium. Weight, potentiometric and hydrogen-volumetric methods are more widely used.

1. Weight method is based on determination of sample mass change as a result of corrosion testing. Depending on the nature of formed corrosion products the sample mass loss is observed when the corrosion product is removed from metal surface. If formed corrosion products stay on the metal surface then sample mass increase takes place. Mass change is generally expressed in grams per a unit of metal surface in a unit of time (g/m2∙h).  However metal corrosion rate is easier to express as metal thickness loss L (mm/year), by the formula:

(8.9)

where Km1  is sample mass change after testing, g/m2·h;

8760 is the number of hours in 1 year, h;

is metal density, g/cm3.

According to GOST-5272, 10-grade scale of metal corrosion resistance (Table 8) is used. For manufacturing apparatuses designated to the contact with aggressive medium it is necessary to use metals with the corrosion rate in this medium less than 1mm/year.

Table 8. The scale of metal corrosion resistance (iron, aluminum, copper, nickel and their alloys)

| № | Corrosion resistance group | Corrosion rate, mm/year | Corrosion resistance, grade |
| --- | --- | --- | --- |
| 1. | 1. Absolutely resistant | Less than 0.001 | 1 |
| 2. | 2. Highly resistant | from 0.001 to 0.005 | 2 |
| 3. | 3. Highly resistant | from 0.005 to 0.01 | 3 |
| 4. | 4. Resistant | from 0.01 to 0.05 | 4 |
| 5. | Resistant | from 0.05 to 0.1 | 5 |
| 6. | 5. Lower - resistant | from 0.1 to 0.5 | 6 |
| 7. | Lower - resistant | from 0.5 to 1.0 | 7 |
| 8. | 6. Low - resistant | from 1.0 to 5.0 | 8 |
| 9. | Low - resistant | from 5.0 to 10.0 | 9 |
| 10. | 7. Non - resistant | More than 10.0 | 10 |

An advantage of the weight method is simplicity and reliability of obtained data, a disadvantage is necessity to perform long-term testing (for several months).

2. Potentiometric method is based on the potential creation for a sample in the corrosion medium and strength of current measurement between work electrodes. The value of current density is used to determine the corrosion process rate. This method differs in reliability and accuracy of obtained data.

3. Hydrogen-volumetric method.

It is known that metals and alloys with negative electrode potentials including aluminum, magnesium and their alloys interact with neutral salt solutions, for example with 5% NaCl solution, and herewith they are subjected to corrosion forming hydrogen. The mass of metal passed into a solution is equivalent to the volume of emitted hydrogen. Hence this amount can be a measure of metal corrosion resistance.

Advantages of hydrogen-volumetric method are high sensibility, capability to obtain “corrosion rate – time” curve, simplicity and safety of measuring equipment; the method isn’t connected with corrosion product removal.

3 THE TECHNIQUE OF LAB CARRYING OUT

3.1 The equipment and technical means:

1. Laboratory plant for corrosion testing

2. Chemical glassware

3. Analytical balance ВЛТЭ-150

4. Dryer ШС-80

5. Water still Liston А 1210

3.2 Laboratory plant description

Experimental determination of metal corrosion resistance is carried out by weight and hydrogen-volumetric method. Hydrogen-corrosion testing plant (Fig. 15) is used to determine metal corrosion resistance. It consists of a graduated gas burette 1 fixed at the stand 2. A burette bottom part is funnel-ended; the top part is equipped with a cock 3. A rubber tube 4 with a rubber pear 5 is connected with the burette top. A testing sample 6 is hanged under the funnel, and then dips with the burette in a glass 7 with acid or salt solution. Before the test the solution is sucked into the burette from the glass up to the zero mark by means of the rubber pear. Formed hydrogen rises up to the burette and lower the solution level. Metal corrosion resistance is calculated based on the replaced hydrogen volume matched to changing number of burette divisions.

1-burette, 2-stand, 3-cock, 4-rubber pipe, 5-rubber vessel, 6-testing sample, 7-glass, 8- thermo regulator, 9-thermometer. Fig. 15. Scheme of the lab plant for corrosion testing

3.3 The order of lab carrying out

The lab essence is to determine corrosion resistance of aluminum plate in hydrochloric acid solution or magnesium alloy in sodium chloride solution.

1. Prepare the metal sample to the testing. Purify the sample surface by means of mechanical and chemical treatment using abrasive paper and defat it with alcohol, ester or gasoline.

2. Define the sample sizes and calculate the ware surface. Weigh the prepared metal ware on the analytical balance with accuracy to 0.001 g.

3. Hang the prepared sample on a hook under the burette funnel; then dip the burette into solution in the glass such the sample doesn’t touch a glass bottom and fix it with a clip on the stand.

4. Suck solution into the burette up to the zero mark by means of the rubber pear and fix this level using a cock.

5. Formed hydrogen rises up to the burette and lower the solution level. Register change of solution level every five minutes within the hour. The volume of extracted hydrogen is equal to change of solution volume in the burette.

6. After testing completing dry the metal sample in the dryer and weigh it on the analytical balance with accuracy to 0.001 g. Determine the sample mass change. Tabulate testing results into the Table 9.

The following corrosion medium is used: 5% hydrochloric acid solution for aluminum plate and 5% sodium chloride solution for magnesium alloy.

4 CALCULATIONS OF CORROSION PROCESS INDICATORS

Table 9. Results of corrosion testing

| No | Mass of ini-tial sample G1, g | Sample mass after testing G2, g | Sample mass change , g | Sample surface S, cm2 | Corrosion time , min | Hydrogen volume VH2, cm3 | Corrosion rate on hyd-rogen, cm3/cm2min |
| --- | --- | --- | --- | --- | --- | --- | --- |

Metal corrosion resistance is determined by the amount of emitted hydrogen and metal mass change after testing. Based on obtained data the following indicators of metal corrosion resistance are calculated:

1. Corrosion rate on sample mass change, g/m2·h:

(8.10)

where ΔG= G1 –G2 is metal mass change after testing, g;

S is the ware surface subjected to corrosion, m2;

is corrosion time, h.

2. Corrosion rate on hydrogen, cm3/cm2min:

(8.11)

where VH2 is volume of emitted hydrogen, cm3;

S is the ware surface subjected to corrosion, cm2;

is corrosion time, min.

Based on this value of corrosion rate the kinetic curve of corrosion КН2=f(τ) is generated.

3. Loss in metal mass on hydrogen, g/cm2min:

(8.12)

where A is metal atomic mass, g;

23.8·10-3 is volume of 1g-mole of hydrogen at temperature 17оС and pressure 0.1MPa.

4. Loss in metal thickness L, mm/year, as a result of corrosion is calculated by the formula (8.9) taking into account metal density Al =2.71 g/cm3, Mg=1.74 g/cm3.

5. Determine metal corrosion resistance due to the scale of corrosion resistance on the basis of calculated loss in metal thickness.

6. Tabulate results of corrosion indicators calculation into the table 10.

Table 10. Results of calculation of corrosion process indicators

| Indicator of corrosion process | Unit of measurement | Value |
| --- | --- | --- |
| 1 | 2 | 3 |
| 1. Corrosion rate on mass change, Кm1 | g/m2·h |  |
| 2. Average corrosion rate on hydrogen, Кн2 | cm3/cm2·min |  |
| 3. Loss in metal mass on hydrogen, Кm2 | g/cm2·min |  |
| 4. Loss in metal thickness, L | mm/year |  |
| 5. Corrosion resistance, resistance group | grade |  |

- SAFETY PRECAUTIONS

1. Be careful when hydrochloric acid solution preparation: it is necessary to pour an acid into water but not vice versa.

2. In a case of hydrochloric acid contact with skin it is necessary to wash off it by plenty amount of water, and then to neutralize it by weak soda solution.

3. Check the truth of the plant assembling before the work start. Check the integrity of wires, plugs, and outlets when heating switching on.

4. When the work is over it is necessary to switch off electric gauges, to clean workplaces and to give them to the laboratory assistant.

6 CONTROL QUESTIONS

- Concept of corrosion and metal corrosion resistance.

- General characteristic of corrosion processes. Corrosion products.

- Chemical corrosion. Rate of chemical corrosion.

- Electrochemical corrosion essence.

- Qualitative methods of determination of metal corrosion resistance.

6. Quantitative methods of determination of metal corrosion resistance. Essence of hydrogen-volumetric method.

- Methods of metal protection from corrosion.

#9 LABORATORY WORK

STUDYING THE FILTRATION PROCESS FOR SEWAGE PURIFICATION

1 THE AIM OF THE LAB:

1. Practical studying the process of suspension separation by means of filtration.

2. Determination of filtration productivity and degree of sewage purification from mechanical impurities.

2 THEORETICAL INFORMATION

2.1 Characteristic of filtration processes

Filtration refers to hydro-mechanical processes used for separation of heterogeneous systems like liquid-solid, gas-solid. These processes are used for target liquid product separation from suspension, for example in wet-process phosphoric acid production, and also for industrial sewage purification from suspended solids or for waste gases cleaning from dust. In the course of suspension separation the solid phase particles dwell on hard filtering membrane and the liquid phase passes through the layer of formed precipitate and through pores of the filtering baffle. As a result of filtration the suspension separation into solid phase – wet precipitate and liquid phase – filtrate takes place.

The suspension filtration provides for almost complete liquid decontamination from suspended solids which are deposited as a precipitate on the filtering surface or inside the filter and gradually blind the pores. Accordingly filtration with filtercake formation and filtration with baffle pores’ blinding. Filtration with filtercake formation proceeds on the filtering baffle; herewith solid particles hardly penetrate inside the baffle. In a case of filtration with baffle pores’ blinding the solid particles hold off inside pores, and a filtercake isn’t formed on the filtering surface.

The driving force of the filtration process is pressure difference on both sides of the filtering baffle. It can be created by means of three methods: by suspension feed under the increased pressure to 1.5MPa (high-pressure filter and filter press) using fluid pumps, by creation the vacuum to 0.1MPa behind the filtering baffle using vacuum pumps (vacuum filter) or due to the centrifugal force (filtering centrifuge). In addition, hydrostatic pressure of the layer of poured suspension may be used for that.

Various filtering materials are used; they are cotton, wool, and synthetic textiles, wire gauzes, porous metals, ceramics or metal-ceramics, and also bulk materials (coal, sand, gravel). Proper operation of the filter depends to a large extent on the filtering baffle properties. The filtering baffle selection is determined by porosity, chemical resistance, mechanical durability and thermal resistance and depends on filtration conditions.

Depending on filters’ purposes the production and cleaning filtration is distinguished. If the solid product or semi-product is separated as a result of filtration, for example, sodium hydrocarbonate in soda ash production, then such filtration is called as production one. If the goal of the filtration is to separate the liquid product and solid impurities, then such filtration is called as cleaning one. In particular the cleaning filtration is used for industrial sewage purification from mechanical admixtures - suspended solids of clay, sand and coal dust.

  - The rate of suspension filtration

The rate of suspension filtration depends essentially on solids’ physical properties and fineness. Suspensions are divided by solid particle size into:

- coarse suspension (particle size more than 100 microns);

- fine  suspension (particle size from 0.5 to 100 microns);

- turbidity (liquids with solid particle size from 0.1 to 0.5 microns);

- colloid solution (solid particle size less than 0.1 microns).

In practice all these kinds of suspensions occur, and mainly with different size particles, i.e. polydisperse systems. It is impossible to separate turbidities and colloid solutions by means of filtration because of high dispersion ability and low separation rate. That’s why they are separated by coagulation and flocculated collapse settling methods. Filtration is most effective method of coarse and fine suspensions separation.

The rate of suspension filtration is described by a kinetic equation of filtration, which expresses the filtrate volume separated in infinitesimal time interval from a unit of a filtering surface:

w=dVFdτ=∆Pμ(Rfc+Rfb)                                    (9.1)

where V is filtrate volume, m3;

F is filtering surface, m2;

τ is filtration time, sec;

∆Р is pressure difference on the filter, Pa;

μ is dynamic-viscosity coefficient, Pa∙с;

R= Rfc+ Rfb is filtration resistance, calculated as a sum of filtercake resistance Rfc  and filtering baffle resistance Rfb.

The kinetic equation of filtration defines factors affecting the filtration rate. The filtration rate is in direct proportion to pressure difference in front of and behind the filtering baffle and in reverse proportion to the filtering surface and to filtration resistance. According to this dependence it is expedient to filtrate the suspension in hot state, i.e. at the chemical process temperature to decrease filtrate viscosity and thereby to increase the filtration rate.

Suspension filterability depends on filtering baffle pores’ size as well. The filter can fully hold off the precipitate provided pores’ size is smaller than the size of the smallest precipitate particles. At counter this condition the filtrating liquid is turbid. At the same time the filtering material shouldn’t be too fine-pored: the denser precipitate is, the smaller material pores’ size is, the more it resists to the liquid flow and therefore the smaller filtration rate is.

The precipitate nature has a great impact on the filtration rate. As a rule amorphous and fine-cristalline precipitates are filtrated hardly, because firstly they need in fine-porous filtering materials using, and secondly they are affected to form a dense layer on the filter, which creates significant additional resistance to the liquid flow. To decrease precipitate resistance the conditions of coarse solid phase formation are selected. The key to success is slow crystallization conducting; it provides more coarse-crystalline precipitate formation.

Basic technological indicators of suspension filtration are productivity of filtration equipment, moisture content of dewatered precipitate and separated filtrate purity. The precipitate moisture content is in reverse dependence on the size of suspension dispersed phase, i.e. the larger solid phase particles are, the easier they are filtrated, washed-out of included solid phase, and the precipitate has less moisture content and therefore it is dried easier (if need). The specific productivity of filtration equipment depends mainly on the specific resistance of solid phase particles, and also on technological, hydrodynamic and physical-chemical conditions. Productivity of the filter Pf can be expressed as conditional average filtration rate which is defined as the ratio of mass or volume of filtrate or precipitate obtained from a unit of filtration surface in a unit of time; it is expressed by the formula:

Pf=GS∙τ                                               (9.2)

where G is mass of filtrate or precipitate, kg;

S is filtration surface, m2;

τ is filtration time, h.

Knowing productivity of the filter one can estimate an effectiveness of suspension separation by means of filtration and select optimal conditions of a process. Purity of obtained liquid product, for example, sewage filtrated from mechanical impurities is determined by purification degree calculated by the formula:

(9.3)

where G is mass of polluting substance in 100g of water before purification, g;

(G-Gdp) is mass of the polluting substance in 100g of water after purification, g;

Gdp is mass of dry precipitate, g.

3 THE TECHNIQUE OF LAB CARRYING OUT

3.1 The equipment and technical means:

1. Bunsen flask

2. Buchner funnel

3. Chemical glassware

4. Vacuum pump

5. Buffer capacity

6. Analytical balance ВЛТЭ-150

7. Rough balance

8. Filter cloth

9. Dryer ШС-80

3.2 Laboratory plant description

The scheme of laboratory plant for filtration process studying is imaged in Fig. 14. It represents vacuum-filtration plant including a Bunsen flask 1 hermetically connected with a Buchner funnel 4, a vacuum meter 2, cocks 3 and 6, a buffer capacity 5, hermetically connected with a vacuum pump.

1-Bunsen flask, 2-vacuum meter, 3,6-cocks, 4-Buchner funnel, 5- buffer capacity Fig. 14. Scheme of vacuum-filtration plant

3.3 The order of lab carrying out

1. Prepare water suspension of composition approximately imitating the sewage polluted with impurities of sand, clay and coal dust. Place 100ml of water into a conical flask and add a sample G of sand and clay mix weighed on the analytical balance with accuracy to 0.1g. The sample mass has to match to suspension composition with liquid to solid phase ratio L:S=10:1, 15:1 or 20:1 according to the assignment.

2. Weigh separately a Buchner funnel and a Bunsen flask on the rough balance. Take the filter cloth of a circle shape with size equal to the funnel square. Place the weighed filter cloth into the Buchner funnel to cover completely funnel’s holes. Determine the filtration surface based on the funnel diameter.

3. Set the vacuum-filtration plant (Fig. 14). Switch on the vacuum pump and by cock 6 at switched-off cock 3 set 0.05-0.06MPa vacuum of the filtration plant. The vacuum is measured by a vacuum meter.

4. Stir up the suspension and pour it in the funnel up to completely filling and simultaneously open the cock 3. Keep filtration start time with stop watch     while the first filtrate drops’ appearance. Pour out well-stirred retained suspension into the funnel and filtrate it up to complete stop of liquid drops’ separation from the funnel to the flask. Note suspension filtration time and then switch off the vacuum pump.

5. Separate the funnel and the flask on the morrow of filtration and weigh separately the funnel with filter cloth and solid phase and the flask with liquid phase on the rough balance. Determine mass of filtrate and precipitate with the filter cloth.

6. Extract the precipitate with the filter cloth from the funnel and place in the porcelain cup; then place it into a dryer and dry for 1 hour up to constant mass at temperature 105-1100C. Control drying is carried out for 30 minutes.

7. Weigh the cooled precipitate with the filter cloth and calculate mass of dry and wet precipitate. Determine precipitate moisture content W by the formula:

(9.4)

where ΔG is precipitate mass change after drying, g;

ΔG = Gwp – Gdp, g;

Gwp is mass of wet precipitate, g.

8. Calculate filtration productivity by filtrate and by wet and dry precipitate by the formula (9.2).

9. Determine purification degree of water from admixtures by the formula (9.3) taking into account that solid phase mass in water after purification can be calculated as a difference of mass of solid substance sample and mass of dry solid precipitate separated by filtration.

10. Make a conclusion of effectiveness of sewage filtration and purification from mechanical admixtures. Tabulate results of calculations in Table 11.

Table 11. Results of water suspension filtration

| Ratio of L:T in sus-pension | Mass of solid substance, g |  |  | Filtra-tion sur-face S, m2 | Precipitate moisture content W, % | Filtration productivity, kg/m2∙h |  |  | Water purify-cation α, % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | in water before purification G | wet precipi-tate on a funnel, Gwp | dry precipi-tate on a funnel, Gdp |  |  | by fil-trate Pf | by wet preci-pitate Pwp | by dry preci-pitate Pdp |  |

4 SAFETY PRECAUTIONS

1. Check the set plant for tightness.

2. In a case of mains interruption the vacuum pump and the dryer must be immediately switched off.

3. The vacuum pump must needs to be grounded.

4. It is prohibited to work at the vacuum-filtration plant without a protective cover of the Bunsen flask and the Buffer capacity.

5. Check the truth of the dryer hook up into the electrical network.

6. In a case of wires or electric gauges firing it is necessary to disconnect them immediately and to extinguish with dry carbon dioxide fire extinguisher or with the asbestos cloth.

5 CONTROL QUESTIONS

1. The concept of filtration process. Purpose and types of filtration.

2. Driving force of the filtration.

3. Methods of pressure difference creating on both sides of the filtering baffle.

4. Definition of the filtration rate. Factors influencing on the filtration rate.

5. What are components of the filtration resistance?

6. Technological indicators of suspension filtration.

7. The technique of calculation of filtration productivity and purification degree of water from mechanical admixtures.

#10 LABORATORY WORK

WATER SOFTENING BY CHEMICAL METHOD

1 THE AIM OF THE LAB:

1. Practical acquaintance with soda-lime method of water softening.

2. Determination of degree of water softening and water quality after softening.

2 THEORETICAL INFORMATION

2.1 Sewage characteristics

Industrial sewage disposal influences negatively on the environment. It causes pollution of underground and surface natural water, soil, underflooding near-by territories and destruction of natural balance of water sources. Deterioration of natural water quality caused by industrial and household sewage disposal in natural reservoirs is an urgent problem. Harmful influence of impurities in sewage appears only in a case of exceeding maximal permissible concentration (MPC) of these toxic impurities in reservoirs. Water quality in reservoirs is in direct correlation with disposed impurities’ quality and quantity.

Following kinds of sewage may be formed at modern industrial enterprises:

- water from equipment cooling, causing heat pollution of the natural water;

- water polluted with petroleum products and other toxic organic admixtures;

- water containing hardness salts and other mineral salts leading to boiler and heat exchanger incrustation formation;

- water with subacidity or superacidity, i.e. corrosion-active acidic or alkaline water;

- water containing mechanical admixtures as suspended solids – clay, sand, coal dust, precipitated hardness salts causing blockage and incrustation of equipment, such as apparatuses, pipelines, heat exchangers, and boiler-utilizers;

- steam condensate polluted with phenols and other organic substances as a result of thermal processing of coals and other solid raw materials;

- washing water from solid waste washing-out to increase maximally main liquid product output;

- absorption water from wet purification of industrial exhaust gases;

- water formed during operation of vacuum pumps, mixing barometric condensers and washing equipment, package and workplaces.

To reduce water consumption and to prevent natural reservoir pollution the wasteless discharge schemes with circulation water supply system are used in modern industrial productions. Salts and gases dissolved in water harm to water circulation system since they cause incrustation formation and metal surface destruction due to corrosion processes. To obtain closed-loop water circulation the system of water purification is provided using different methods of sewage cleaning and its components’ utilization. Depending on pollution kind, polluted substance concentration and required purification degree the various methods of sewage purification are applied.

Sewage purification degree is expressed by the generalized formula:

(10.1)

where с1 и с2 are concentrations of polluted substances in water before and after purification.

2.2 Industrial methods of sewage purification

Water applied in industrial processes must not contain harmful impurities, corrode equipment and form incrustation and insoluble sludge (as calcium and magnesium carbonates and magnesium hydroxide) in apparatuses and pipelines.

Hydromechanical, chemical, physical-chemical, physical and thermal methods of sewage purification are used in industry. Hydromechanical methods are based on difference in liquid and solid phase densities or on difference in pressures in front of and behind the filter baffle. They are settling-out and filtration. Chemical methods are used to neutralize acidic water and to soften water by some ion transition in insoluble compounds, to oxidize or to reduce toxic organic and inorganic impurities. These methods are also called as reagent methods since to separate impurities the special chemical reagents are added to water.

Flotation, extraction, electrochemical, coagulation and sorption are called physical-chemical methods. Most widely used sorption methods are adsorption and ion exchange used for sewage purification from fine, colloid and dissolved substances. Physical methods include precipitation in an electric and magnetic fields, acoustic coagulation, sewage evaporation etc. Nowadays membrane technologies (nanofiltration and reverse osmosis) are successfully used in industrial water preparation.

Water hardness (mg-eq/l) is the main qualitative indicator in majority productions. It is predetermined by soluble calcium and magnesium salts’ presence in water. Three types of water hardness are distinguished. They are temporary, permanent and total hardness.

Water temporary (carbonate) hardness is predetermined by calcium and magnesium hydrocarbonates Са(НСО3)2 and Mg(НСО3)2 content in water. These salts are converted into non-soluble carbonates when boiling. They precipitate as a dense deposit according to the reaction equations:

t

Са(НСО3)2CaCO3+H2O+CO2                     (10.2)

t

2 Mg(НСО3)2MgCO3∙Mg(OH)2+H2O+3CO2         (10.3)

Permanent (non-carbonate) hardness is predetermined by calcium and magnesium chlorides, nitrates and sulphates content in water. These salts aren’t converted into precipitates when boiling. Total hardness is determined as the sum of temporary and permanent hardness.

Water softening consists in complete or partial removal of calcium and magnesium ions Са2+ and Mg2+ from water by chemical or physical-chemical methods. Coarse water softening (about to 0.3 mg-eq/l of hardness salts) is carried out by means of reagent soda-lime method, i.e. by lime (lime milk), caustic soda or soda ash addition into water with precipitation of insoluble calcium and magnesium salts.

Water lime pretreatment is carried out at the first step. It is used to decrease the carbonate hardness and to fix СО2; herewith total salt content as well as concentration of coarse admixtures and iron compounds decrease simultaneously. Reagents for this process are slaked lime Ca(OH)2 as a water suspension – lime milk or quick lime CaO as a fine powder. The process of water lime pretreatment is described by following reaction equations:

Ca(HCO3)2+Ca(OH)22CaCO3+2H2O                     (10.4)

Mg(HCO3)2+2Ca(OH)22CaCO3+Mg(OH)2+2H2O          (10.5)

FeSO4 + Ca(OH)2 → Fe(OH)2↓ + CaSO4↓                  (10.6)

CO2 + Ca(OH)2 →CaCO3↓+ H2O                          (10.7)

At the second step water is subjected to treatment by soda ash to remove permanent hardness; thereat following reactions proceed:

MgSO4+Na2CO3MgCO3+Na2SO4                         (10.8)

MgCI2+Na2CO3MgCO3+2NaCl                           (10.9)

CaSO4+Na2CO3CaCO3+Na2SO4                         (10.10)

These processes are usually combined in industrial conditions and conducted simultaneously in the same apparatus – a clarifier. Increasing the softening temperature and stirring using accelerates processes of hardness salts’ precipitation and formed precipitate settling-out. 5-10% lime excess is usually used to provide high degree of water purification. At lime pretreatment some part of calcium transits from lime to water, therefore to calculate soda ash consumption for water softening it is necessary take into account calcium salts newly input into water and to use soda ash solution in 10-15% excess. Final water purification from the precipitate is carried out by means of filtration or settling-out.

Fine water softening (to 0.03 mg-eq/l) is reached when phosphate method using at tri-sodium phosphate action as the softening agent. It permits to remove water temporary and permanent hardness simultaneously; thereat insoluble calcium and magnesium phosphates are formed according to reaction equations:

3Ca(HCO3)2 + 2Na3PO4   Ca3(PO4)2 + 6NaHCO3                       (10.11)

3MgCl2 + 2Na3PO4   Mg3(PO4)2 + 6NaCl                       (10.12)

Solubility of calcium and magnesium phosphates is negligibly small; it provides high effectiveness of the phosphate method.

3 THE TECHNIQUE OF LAB CARRYING OUT

3. 1 The equipment and technical means:

1. Electric closed heater

2. Chemical glassware

3. Titrimeter

4. Water still Liston А 1210

5. Analytical balance ВЛТЭ-150

3.2 The order of lab carrying out

Water softening by soda-lime method

- Carry out preliminary water chemical analysis and determine temporary, permanent and total hardness according to the technique described in the #5 lab. Calculate indicators of water hardness by the formulas 10.13-10.15.

Water carbonate hardness Hc (mg-eq/l) is determined by the formula:

(10.13)

where V1 is  the volume of 0.1n HCl solution spent for titration, ml;

0.0028 is hydrochloric acid titre on CaO;

10000 is coefficient for measurement units’ recalculation;

20.04 is Са2+ ions content (mg) in 1 litre of water matching to 1 mg-eq/l of hardness salts.

The total hardness Ht (mg-eq/l) is determined by the formula:

Ht = 1.4∙(V3-2.5V2)                                  (10.14)

where V3 is volume of 0.1n HCl solution, spent for titration of 25 ml of Na2CO3 and NaOH mixture solution, ml;

V2 is volume of 0.1n HCl solution, spent for titration of excess of Na2CO3 and NaOH mixture in the testing sample of water, ml;

2.5 is dilution coefficient.

Water permanent hardness is determined as a difference of water total and carbonate hardness:

Hn = Ht – Hc                                       (10.15)

- Based on obtained results calculate the amount of lime or lime milk and soda ash for water softening. Interaction of reagents with hardness salts in water is described by reaction equations 10.4-10.10.

Consumption of slaked lime mCa(OH)2 (mg/l of water) for carbonate hardness removal is calculated by the expression:

mCa(OH)2= 1.05∙Нc ∙37                                 (10.16)

where 37 is equivalent of Ca(OH)2,

1.05 is coefficient taking into account 5% lime excess.

If dry lime is used it is necessary to recalculate into CaO, i.e. mCaO= mCa(OH)2 ∙56/74.

Consumption of soda ash mNa2CO3 (mg/l of water) for non-carbonate hardness removal is calculated by the expression:

mNa2CO3 = 1.1∙ Нn∙53                                  (10.17)

where 53 is equivalent of Na2CO3,

1.1 is coefficient taking into account 10% lime excess.

If less water volume is taken for its softening, for example 250ml instead of 1 liter, then consumption of lime and soda ash is recalculated fro given water volume, i.e. mCaO1 = mCaO ∙250/1000 и mNa2CO31 = mNa2CO3∙250/1000.

- Weigh calculated amount of lime and soda ash on the analytical balance with accuracy to 0.01g. Place 250ml of analyzed water into 500ml conical flask, heat up to the temperature 40-500С and dissolve in it consecutively reagent samples - at first lime and then soda ash. The mix is stirred for 4-5 minutes. Then settle and filtrate it on the paper filter and throw off first portions of the filtrate.

4. Analyze purified water and determine carbonate Нc1 and total Ht1 hardness by methods and formulas described in #5 lab (formulas 10.13-10.15.).

5. Calculate water softening degree by the formula:

(10.18)

6. Make a conclusion about effectiveness of water softening by reagent soda-lime method.

4 SAFETY PRECAUTIONS

1. Be careful when acid, alkalis and salt solutions preparation: avoid to contact with skin.

2. In a case of acid contact with skin it is necessary to wash off it by plenty of water or  by soda solution.

3. When water and solution boiling on the electric heater it is necessary to observe safety regulations when operating with electric heaters.

4. At electric trauma it is necessary to switch off a knife switch of an electric board.

5 CONTROL QUESTIONS

- Characteristic of industrial sewage.

- Basic indicators of water quality.

- Methods of industrial sewage purification.

- Concept of water hardness. Kinds of water hardness.

5. Chemical methods of water softening.

6. Technique of determination of water softening degree.

#11 LABORATORY WORK

WATER SOFTENING BY ION EXCHANGE METHOD

1 THE AIM OF THE LAB:

1. Practical acquaintance with ion exchange method of water softening.

2. Determination of degree of water softening and water quality after softening.

2 THEORETICAL INFORMATION

2.1 Characteristics of methods of sewage purification

Nowadays large volumes of sewage are formed in industrial productions. It contains various chemical and mechanical impurities and influences negatively on the environment causing pollution of underground and surface natural water and destruction of natural balance of water sources. To eliminate harmful influence of industrial sewage disposal, to reduce water consumption and to prevent natural reservoir pollution the wasteless discharge schemes with circulation water supply system are used in modern industrial productions.

Salts and gases dissolved in water harm to water circulation system since they cause incrustation formation and metal surface destruction due to corrosion processes. To obtain closed-loop water circulation the system of water purification is provided using different methods of sewage cleaning.

Sewage purification degree is expressed by the generalized formula:

(11.1)

where с1 и с2 are concentrations of polluted substances in water before and after purification.

Water applied in industrial processes must not contain harmful impurities, corrode equipment and form incrustation and insoluble sludge in apparatuses and pipelines. Various methods are used for industrial sewage purification depending on pollution kind, concentration of polluted substances, required purification degree and modes of impurities formation. They are hydromechanical, chemical, physical-chemical, physical and thermal methods. Hydromechanical methods are based on difference in liquid and solid phase densities or on difference in pressures in front of and behind the filter baffle. Most widely used methods of water purification from mechanical admixtures are settling-out and filtration.

Chemical methods are used to neutralize acidic water and to soften water by some ion transition in insoluble compounds, to oxidize or to reduce toxic organic and inorganic impurities. These methods are also called as reagent methods since to separate impurities the special chemical reagents are added to water. Flotation, extraction, electrochemical, coagulation and sorption are called physical-chemical methods. Coagulation of colloid impurities is used for coarse microphase formation as floccules by means of coagulating agents – iron and aluminum sulphates addition to water with following solid phase precipitation. Formed flocculated mass consisting mainly of iron and aluminum hydroxides and impurities are separated from water in settlers or in special clarifiers. Most widely used sorption methods are adsorption and ion exchange used for sewage purification from fine, colloid and dissolved substances.

2.2 Essence of ion exchange method of sewage purification

Water hardness is the main qualitative indicator of industrial sewage. It is predetermined by calcium and magnesium salts’ presence in water. To use the water circulation system it is necessary to remove hardness by water softening.  Water softening consists in complete or partial removal of dissolved calcium and magnesium salts from water by chemical or physical-chemical methods. Coarse water softening (about to 0.3 mg-eq/l of hardness salts) is carried out by means of soda-lime method, i.e. by addition of lime, caustic soda or soda ash into water with precipitation of insoluble calcium and magnesium salts.

Fine water softening (to 0.03 mg-eq/l) is reached by phosphate method at tri-sodium phosphate addition as the softening agent. It permits to remove water temporary and permanent hardness simultaneously. Nowadays a complex method of water softening and demineralization is often used in industrial water preparation. This method represents chemical and physical-chemical ion exchange methods combination.

The most effective method of water softening and demineralization is ion exchange method. The essence of this method consists in that some solid mineral and organic substances of low solubility are capable to extract from solutions certain cations and anions as a result of them exchange into other ones contained in these solutions. Cationites and anionites are used to extract Са2+, Mg2+, Fе3+ ions from water. Sulfonated coal or high-molecular resins containing active groups with Н+, Na+, NH4+ ions are cationites; high-molecular resins containing active groups with ОН-, HCO3- и С032- ions are anionites.

Cationites of H+ and Na+ forms are usually used for water softening. Na-cationites used in industrial water preparation are alumosilicates: glauconite, zeolite, permutite, etc. Sulfonated coal and synthetic resins are used as H-cationites. OH-anionites are represented by artificial resins of complex composition, for example, carbamide resins.

Ion exchange between solutions and ionites is of heterogeneous chemical reaction nature. It should be noted that impurities removed from water by ion exchange method don’t form a precipitate; such treatment doesn’t require continuous component dosing. The important characteristic of ionites is an exchange capacity showing the ionite ability to adsorb a certain number of ions in given conditions. Adsorptive capacity (exchange capacity) E (g-eq/m3 of ionite) is expressed as the amount of equivalents of calcium and magnesium cations which can be adsorbed by a unit of ionite mass or volume. So Е=1000 g-eq/m3 for sulfonated coal and Е=850 g-eq/m3 for alumosilicates.

The basis of cation softening is a reaction of exchange of sodium and hydrogen ions of cationites for Са2+ and Mg2+ ions. Exchange of sodium ions is called as Na-cationization and hydrogen ions – as H-cationization. The process of Na-cationization is described by reaction equations:

2R/Na+ + Ca2+ ↔R2/Ca2+ + 2Na+                         (11.2)

2R/Na+ + Mg2+ ↔R2/Mg2+ + 2Na+                         (11.3)

where R is complex of a matrix and a functional group which doesn’t participate in the ion exchange (it is assumed to be monovalent). The cation exchange at H-cationization proceeds according to reaction equations:

2R/H+ + Ca2+ ↔R2/Ca2+ + 2H+                                 (11.4)

2R/H+ + Mg2+ ↔R2/Mg2+ + 2H+                               (11.5)

Reactions of ion exchange are reversible ones, and when reaching the required limit of ionite exchange capacity they are regenerated by washing with sodium chloride solution or with diluted sulphuric acid. Na-cationite regeneration is carried out by 6-8% sodium chloride solution, and H-cationite regeneration is carried out by acid solutions, for example 1.0-1.5% sulphuric acid solution. NaCl application for this purpose is traditional one; it is predetermined by table salt wide-spreading and low cost. Anionites are regenerated by washing with diluted alkaline solutions, sodium carbonate or hydrocarbonate solutions, more often 4% NaOH solution.

The process of cationite regeneration with sodium chloride solution is described by following reaction equations:

R2/Ca2+ + nNa+ → 2R/Na+ + Ca2+ + (n-2) Na+               (11.6)

R2/Mg2+ + nNa+ → 2R/Na+ + Mg2+ + (n-2) Na+                  (11.7)

3 THE TECHNIQUE OF LAB CARRYING OUT

3. 1 The equipment and technical means:

1. Electric closed heater

2. Chemical glassware

3. Titrimeter

4. Water still Liston А 1210

5. Cation-exchange column

6. Analytical balance ВЛТЭ-150

3.2 Description of the plant for water softening by ion exchange method

The scheme of the lab plant for water hardness removal by ion exchange method is imaged in Fig. 15. It consists of a flask 5 for purified water collection, a loading funnel 6 and an ion exchange column 1, fixed at a stand 7. The cation-exchange column represents a separating funnel of 4-5cm diameter and 20cm height, 60-70% full of Na-cationite 2 and equipped with a cock 4 for treated water discharge. The cationite is placed on a glass fibre layer 3 in the column bottom.

1-separating funnel, 2-cationite, 3-grid, 4-cock, 5-water collecting flask, 6-loading funnel, 7-stand Fig. 15. Scheme of the lab plant for cationite water softening

3.3 The order of lab carrying out

1. Prepare ion exchange column for the work. Prepare 250-300ml of 6-8% sodium chloride solution and pass it through the column for cationite regeneration after previous experiments when exchange capacity limit reaching. The salt excess is washed-out with 300-400ml of distilled water.

2. Pass through the cationite 100-150ml of tap water of known hardness Ht (by the analyses results of #5 lab) with the outflow velocity 1 drop per second.

3. Collected softened water after the cation-exchange column is subjected to the chemical analysis to determine carbonate and total hardness Ht2 by the technique of #5 lab.

4. Calculate water softening degree by the formula:

(11.8)

5. Make a conclusion of effectiveness of water softening by ion exchange method.

4 SAFETY PRECAUTIONS

1. Be careful when acid, alkalis and salt solutions preparation: avoid to contact with skin.

2. In a case of acid contact with skin it is necessary to wash off it by plenty of water or by soda solution.

3. When water and solution boiling on the electric heater it is necessary to observe safety regulations when operating with electric heaters.

4. At electric trauma it is necessary to switch off a knife switch of an electric board.

5 CONTROL QUESTIONS

- Characteristic of industrial sewage.

- Methods of industrial sewage purification.

- Concept of water hardness. Kinds of water hardness.

4. Essence of ion exchange method of water softening. Kinds of used cationites and anionites.

- Technique of determination of water softening degree.

6. Design and the operation principle of ion exchange column.

7. Full exchange capacity, its determination.

REFERENCES

1. Лабораторный практикум по общей химической технологии. / Учебное пособие под ред. В.С. Бескова. – М.: БИНОМ. – Лаборатория знаний, 2010. – 279с.

2. Бесков В.С. Общая химическая технология. Учебник для вузов. М.: Академкнига, 2005. - 452 с.

3. Игнатенков В.И., Бесков В.С. Примеры и задачи по общей химической технологии. Учебное пособие для вузов. М.: Академкнига, 2005. - 198 с.

4. Соколов Р.С. Химическая технология. – М.: Владос, 2000, т.1, 2. – 448с., 480с.

5. Кондауров Б.П., Александров В.И., Артемов А.В. Общая химическая технология. – М.: Академия,  2005. – 336с.

6. Общая химическая технология и основы промышленной экологии // Под ред.В.И.Ксензенко. – М.: Колоc, 2003. - 328с.

7. Бесков В.С., Сафронов В.С. Общая химическая технология и основы промышленной экологии. – М.: Химия, 1999. – 472с.

8. Seitmagzimova G.M. General chemical technology. – Shymkent: M.Auezov SKSU, 2005. - 74p.

9. Seitmagzimova G.M. The technology of mineral acids.  Study guide. - Shymkent:  M.Auezov SKSU, 2007. – 68p.

Галина Мануиловна Сейтмагзимова

Жаныл Кемаладиновна Джанмулдаева

Лабораторный практикум

по дисциплине «Общая химическая технология»

для студентов специальностей

5B072000, 5B072100, 5B075300, 5B060600

всех форм обучения

Редактор Сейтмагзимова Г.М.

Подписано в печать

Формат бумаги XxY 1/16

Бумага типографская. Печать офсетная. Объем  6,25 п.л.

Тираж 100 экз. Заказ № 985.

© Издание Южно-Казахстанского государственного университета  им.М.Ауезова

Издательский центр ЮКГУ им.М.Ауезова, г.Шымкент, пр.Тауке хана, 5