Ф. 7.11-19

Dubinina E.S., Dzhumabayeva G.M.

Methodical instructions for practical classes of discipline

«PROFESSIONALLY-ORIENTED FOREIGN LANGUAGE»

Shymkent 2015 г.

Department of Education and Science of Kazakhstan Republic

M.Auezov South-Kazakhstan State University

The chair "Technology of cement, ceramics and glass"

Dubinina E.S, Dzhumabayeva G.M.

Methodical instructions for practical classes of discipline

«PROFESSIONALLY-ORIENTED FOREIGN LANGUAGE»

For students of speciality

5B075300 - Chemical technology of infusible nonmetallic and silicate materials

Shimkent, 2015

UDC 802.0

Composers: Dubinina E.S Methodical instructions for practical classes by discipline “Professionally-oriented foreign language”. – Shimkent: SKSU named after M.Auezov, 2015. – 36 р.

Methodical instructions are composed in accordance with the requirements of the curriculum and program of discipline «Professionally-oriented foreign language» and include all the necessary information to fulfill the practical training course.

Methodical instructions are intended for students of specialty: 5B075300 - Chemical technology of infusible nonmetallic and silicate materials

Reviewer: Zhakipbaev B.E. - Dr. PhD, Senior Lecturer of chair ''Technology of silicates and synthesis of minerals''

Reviewed and recommended for publication by the meeting of the department «Technology of cement, ceramics and glass » (Minutes № 10 from 19.03.15, and Methodical Committee on innovational technologies of training and Methodical provision of higher school «Сhemical engineering and biotechnology» (Minutes № 9 from 24.04.2015)

The methodical instructions are recommended to publication by Methodical Soviet of SKSU named after M.Auezov (Minutes  №_   ___201_).

© South-Kazakhstan State university named after M.Auezov, 2015

Responsible of issue Dubinina E.S

Contents

|  | Introduction | 4 |
| --- | --- | --- |
|  | Subject 1. Translation of technical-scientific literature in field of physico-chemical methods of analysis of silicate materials |  |
| 1 | X-ray analysis, qualitative x-ray analysis |  |
| 2 | Thermal methods of analysis, qualitative differential thermal analysis |  |
| 3 | Petrography of technical stone (crystal optical researches of technical stone) |  |
| 4 | Basis of patenting |  |
|  | Subject 2. Translation of technical-scientific literature in field of «Chemical technology of binders» |  |
| 5 | Technology of cement |  |
| 6 | Gypsum-based binders and wares on it base |  |
| 7 | Lime binder materials and wares on it base. Hydraulic lime |  |
| 8 | Magnesia binders |  |
|  | Subject 3. Translation of technical-scientific literature in field of «Chemical technology of ceramic and refractories» |  |
| 11 | Structure and fundamental properties of ceramic |  |
| 12 | Technology of building ceramic: wall ceramic, façade ceramic, ceramic chemically resistant wares |  |
| 13 | Technology of manufactured porous aggregate: expanded-clay aggregate and agloporite |  |
| 14 | Technology of refractories: alumina-silicate refractory |  |
| 15 | Technology of fine ceramic: household and artistic porcelain; electro technical porcelain; floor tile, façade tile, facing glazed tile; ceramic granite tile; sanitary ware; stoneware, majolica |  |
|  | Subject 4. Translation of technical-scientific literature in field of «Chemical technology of glass and glass-ceramics» |  |
| 16 | Properties of glasses, basis of glassmaking and of technology of glasswares |  |
| 17 | Technology of plate glass |  |
| 18 | Technology of hollow glass |  |
| 19 | Technology of building glass |  |
| 20 | Technology of glass-ceramics |  |
|  | Subject 5. Translation of technical-scientific literature in field of «Technology of technical crystals and precious jewel stones» |  |
| 21 | Precious jewel stones |  |
| 22 | Synthesis of technical crystals |  |
|  | Literature |  |

INTRODUCTION

In the world of science English - the main working language. More than 1,5 billion people use English as their mother language, or daily use means of communication. Still about a billion people are learning the language. 75% of all written and electronic messages sent in English. English is currently the language of international communication.

The purpose of the discipline "Foreign language in professional field" is to provide basic knowledge underlying the profession in English, the development of practical experience and skills transfer of scientific and technical literature in the field of chemical technology of infusible nonmetallic and silicate materials.

Developed methodical instructions to perform practical training on the specifics of translation of scientific and technical literature in the field of chemical technology of infusible nonmetallic and silicate materials.

In the study of the discipline the student should have knowledge of English grammar, basic translation of scientific and technical literature to be able to translate the scientific literature in the field of chemical technology of infusible nonmetallic and silicate materials.

В мире науки английский – основной рабочий язык. Более 1,5 миллиарда людей используют английский в качестве родного или ежедневно употребляемого средства общения. Еще около миллиарда людей изучают этот язык. 75% всех письменных и электронных сообщений рассылается на английском языке. Английский язык на сегодняшний день является языком международного общения.

Целью изучения дисциплины «Иностранный язык в профессиональной сфере» является обеспечение базовыми знаниями, лежащими в основе профессиональной деятельности на английском языке; развитие практического опыта и профессиональных навыков переводов научно-технической литературы в области химической технологии тугоплавких неметаллических и силикатных материалов.

Разработанные методические указания предназначены для выполнения практических занятий по особенностям перевода научно-технической литературы в области химической технологии тугоплавких неметаллических и силикатных материалов.

При изучении данной дисциплины студент должен владеть знаниями по грамматике английского языка, основам перевода научно-технической литературы; уметь переводить научно-техническую литературу в области химической технологии тугоплавких неметаллических и силикатных материалов.

1 Thematic plan of practical works

Module 1. Translation of technical-scientific literature in field of physico-chemical methods of analysis of silicate materials and chemical technology of binders

Subject 1. Translation of technical-scientific literature in field of physico-chemical methods of analysis of silicate materials

- X-ray analysis, qualitative x-ray analysis (2h)

- Thermal methods of analysis, qualitative differential thermal analysis (2h)

- Petrography of  technical stone (crystal optical researches of technical stone) (2h)

- Basis of patenting (2h)

Subject 2. Translation of technical-scientific literature in field of «Chemical technology of binders»

- Technology of cement (3h)

- Gypsum-based binders and wares on it base (2h)

- Lime binder materials and wares on it base. Hydraulic lime  (1h)

- Magnesia binders (1h)

Module 2. Translation of technical-scientific literature in field of Chemical technology of ceramic and refractories,  Chemical technology of glass and Technology of technical crystals and precious jewel stones

Subject 3. Translation of technical-scientific literature in field of «Chemical technology of ceramic and refractories»

- Structure and fundamental properties of ceramic (1h)

- Technology of building ceramic: wall ceramic, façade ceramic, ceramic chemically resistant wares (1h)

- Technology of manufactured porous aggregate: expanded-clay aggregate and agloporite (1h)

- Technology of refractories: alumina-silicate refractory (1h)

- Technology of fine ceramic: household and  и artistic porcelain; electro technical porcelain; floor tile, façade tile, facing  glazed tile; ceramic granite tile; sanitary ware; stoneware, majolica (2h)

Subject 4. Translation of technical-scientific literature in field of «Chemical technology of glass and glass-ceramics»

- Properties of glasses, basis of glassmaking and of technology of glasswares (2h)

- Technology of plate glass (2h)

- Technology of hollow glass (1h)

- Technology of building glass (1h)

- Technology of glass-ceramics (1h)

Subject 5. Translation of technical-scientific literature in field of «Technology of technical crystals and precious jewel stones»

- Precious jewel stones (1h)

- Synthesis of technical crystals (1h)

Module 1. Translation of technical-scientific literature in field of chemical technology of infusible nonmetallic and silicate materials

Subject 2. Translation of technical-scientific literature in field of physico-chemical methods of analysis of silicate materials

Practical work № 1

X-ray analysis, qualitative x-ray analysis

The aim of work: translate scientific-technical literature

Duration of work: 2 hour

- The task: translate in Russian

x-ray analysis implies various research methods which use x-ray radiation, that is, transverse electromagnetic modes with wave lengths of 10-2 - 102Å. Electrons collision is used to receive x-ray in X-rays tubes, the said electrons are accelerated by high voltage of a metal anticathode.

x-ray tubes of various configuration are used to receive X-rays. Ions or electrons moving at a high speed are used as a moving body in an X-ray tube. As a result, X-ray tubes are either of ionic type or electronic type.

X-ray radiation which appears then is divided into hard [λ>1-5 Å] depending on wave length;  continuous (independent on the nature of anticathode substance) depending on the spectral composition; there is also polychromatic radiation with a certain waves length. Continuous radiation (also "white" x-ray radiation) consists of rays having various waves lengths. Selectively absorbing filters and crystals-monochromators are used for X-rays monochromatization. When K-line anode is used, the selective filter Kβ-line. Characteristic radiation consists of rays having waves of a certain length. To produce characteristic x-ray the voltage magnitude on the tube’s electrodes must achieve a certain level which depends on anticathode metal. Usually its size varies from 30 up to 70 kV. That is, characteristic radiation appears only in those cases, when accelerated electrons possess enough energy to hit out of the anode material an electron which is in the inner shell. The atom’s electrons when moving from outer shells of greater energy into the vacant place in the inner shell emit a  quantum the energy of which is strictly certain for each element.

The idea of using x-ray radiation for researching crystalline substances is based on the fact, that its wave length is compared with the distance between normally ordered atoms in crystalline lattice which is natural diffraction lattice. The essence of x-ray methods of the analysis is to study the diffraction picture received during  reflection of X-rays by atom planes in crystalline structure.

X-raygraphic analysis is based on Woolf-Bregg’equation, connecting θ angle of incidence or reflection of X-ray onto atom plane with its wave length λ and the magnitute of inter-plane distance d:

nλ = 2d · sinӨ,

Where: n – integer (1, 2, 3, etc.), call spectrum order or reflection order;

d- inter-plane distance;

Ө - angle between the direction of rays and reflecting planes;

λ – X-rays wave length.

The reflected pencil of X-rays which can be registered, appears only in case if the said equation is observed. The rays reflected in all other directions and different angles not meeting the requirements of  Woolf-Bregg’equation, are mutually extinguished. Woolf-Bregg’equation is the main one in the x-ray analysis. It λ wave length of the used x-ray is know and Ө diffraction angle has been measured, the equation gives the opportunity to define d inter-plane distance in crystals.

There are three principally different methods of X-rays analysis with X-rays photographic registering. Two of them the method of polycrystalline powder and the  method of monocrystal rotation – use monochromatic radiation. The method of monocrystal oscillation is a variety of the method of monocrystal rotation. Besides the method of rotation and oscillation can be divided into two types, in one of them shooting is implemented on the immovable film, in the second on the film moves (the method of layer lines scanning or X-ray-goniometric method).

- The task: translate in English

Основным методом исследования структуры хорошо ограниченного кристалла являются методы вращения, колебания и развертки слоевых линий. С помощью этого метода можно индицировать рентгенограммы и определять параметры решетки. Рентгенографическое исследование монокристаллов – основной метод расшифровки их атомной структуры.

Рентгенографические методы анализа широко используются для изучения структуры, состава и свойств различных материалов, в частности цемента, фарфора и т.д. С помощью рентгеновского анализа исследуют: качественный и количественный минералогический и фазовый состав цемента, фарфора (рентгенофазовый анализ); тонкую структуру кристаллических веществ – форму, размер и тип элементарной ячейки, симметрию кристалла, координаты атомов в пространстве (рентгеноструктурный анализ); степень совершенства кристаллов и наличие в них зональных напряжений; тип твердых растворов, степень их упорядоченности и границы растворимости; размер и ориентировку частиц в дисперсных системах; внутренние микродефекты в изделиях (дефектоскопия).

- The task: translate in Russian

Defining parameters of elementary cell is necessary for other researches connected with structure and properties of sitales (glass ceramics) and sintered materials, especially: when measuring crystals of thermal expendsion coefficient in various crystallographic directions, when studying inner tensions in crystals, when definig realms and limits of phases solubility on states charts, etc.

Parameters of an elementary cell of crystals are defined by precise measurement of inter-plane distances d for a number of lines on X-raysgrams with the known reflection indexes hkl. The number of lines must be equal to the number of unknown parameters and consequently different for crystals of different symmetry. For example, for crystals cubic syngony, which have а=в=с, it is enough to measure “d” of line to define "a" and solve one equation with one unknown parameter.

Since every crystalline substance has its own set of inter-plane distances (or x-ray lines) and J intensities of corresponding lines, then x-ray phase analysis (XРhА) is based on the fact that X-raygram of heterogeneous sample is a sum of X-raygrams of individual minerals. During the quality analysis the sample’s X-raygram is compared with the standard’s X-raygram.

Qualitative X-ray phase analysis

The task of the qualitative X-ray phase analysis is to define (identify) the nature of crystalline phases which the examined material contains. The said analysis is based on the fact, that every individual crystalline compound gives a specific X-raygram with a certain sets of lines (diffraction maximums) and their intensity. Now a days scientists have reliable X-raygraphic data concerning a great number of well-known crystalline compound, their standard X-raygrams are published in various reference books or in individual papers.

The essence of the qualitative X-ray phase analysis is in comparison of experimentally defined magnitudes of inter-plane distances (d) and relative intensities (I) with standard X-raygrams. If the X-raygram of the examined sample shows diffraction maximums of  d  and I typical for the compound in question, that means the compound is present in the examined material. Naturally, the analysis is easier, if the researchers know at least approximately the chemical composition of the examined material or its mineral composition.

When the X-raygram has been received, phases identification begins with finding θ angles and corresponding inter-plane magnitudes, and relative intensity for each line. Intensity is estimated both qualitatively and quantitatively, for example by using a ten-grade or hundred-grade scale. For the analysis the most intense line on the X-raygram of examined material is chosen. If there are several such lines, then the line with the smallest “d” is chosen. Using reference standard X-raygrams the researchers select compounds with intense line with similar magnitude of d. Then 2-3 more intense lines are chosen, and if they correspond to one of the standard X-raygrams then the rest of the lines are compared. If all the lines of the standard X-raygram meet the certain lines of the examined material’s X-raygram without essential contradictions of their relative intensity, the first compound can be considered found. Then the most intense line from the left on the X-raygram is chosen and the process is repeated. The analysis goes on untill all lines are not referred to certain compounds.

- The task: translate in English

Количественный рентгенофазовый анализ

Количественный РФА основан на зависимости интенсивности дифракционного отражения от количества соответствующего минерала в смеси.

Количественный рентгенофазовый анализ, в задачу которого входит определение количественного содержания отдельных фаз в многофазовых поликристаллических материалах, основан на зависимости интенсивности дифракционных максимумов (отражений) от содержания определяемой фазы.

Используется несколько методов количественного рентгенофазового анализа многофазовых препаратов, из которых наиболее распространенным и точным для порошковых материалов считается метод внутреннего стандарта (метод подмешивания). Сущность этого метода заключается в том, что к исследуемому веществу примешивается точно известное количество эталонного вещества. Интенсивности отражений на рентгенограмме исследуемой фазы и эталонного вещества будут при этом соответственно равны.

Vocabulary

| wave lengths | длины волн |
| --- | --- |
| moving body | движущееся тело |
| flow of electrons | поток электронов |
| tungsten spiral | вольфрамовая спираль |
| anticathode substance | антикатодное вещество |
| imply | заключать в себе |
| x-ray analysis | рентгенографический анализ |
| collision | столкновение |
| X-rays tubes | рентгеновская трубка с вращающимся анодом |
| accelerate | ускорять |
| tungsten | вольфрам |
| Selectively | выборочно |
| inner shell | внутренняя электронная оболочка |
| emit | выделять |
| essence | сущность |
| lauegrams | лауэграмма |
| aperture | отверстие |
| disadvantage | помеха |
| epigrams | эпиграмма |
| Implementation | воплощение, внедрение |
| tangent | Касательный, тангенс |
| X-ray exposure | съёмка рентгенограммы |
| elementary cell | елементарная ячейка |
| microflaws | микродефекты |
| relative intensities | относительные интенсивности |
| inter-plane distances | межплоскостные расстояния |
| weakening indicator | показатель ослабления |
| reflections | отражения |
| the method of adding | метод подмешивания |
| multiphase samples | многофазовые препараты |

Task for ISW: Answer questions

- What is X-ray analysis?

- How to get x-rays?

- Which equation is the basis of X-ray analysis?

- Why use radiographic methods of analysis?

- What are the methods of X-ray diffraction?

- Why use radiographic methods of analysis?

- What is the basis of a single crystal rotation method

- What is the basis of the Laue method

- What is the basis of the method of scanning the layer lines

- What does it mean radiographic analysis by powder

- What is the method of high-temperature X-ray analysis

- What is the goal of quantitative X-ray analysis?

- On what is the quantitative X-ray analysis?

- Why use radiographic methods of analysis?

- For what purposes applied quantitative X-ray analysis

Practical work № 2

Thermal methods of analysis, qualitative differential thermal analysis (2h)

The aim of work: translate scientific-technical literature

Duration of work: 2 hour

- The task: translate in Russian

Thermoanalysis is one of the methods of physical-chemical analysis which are widely used to examine both organic and non-organic substances. Thermoanalysis  is mainly a set of two methods: differential thermal analysis (DTA) and thermal gravimetric analysis (TGA) or thermal weight.

By N.S. Kurnakov offered DTA in our country, and his followers, L.G.Berg, A.V. Nickolayev, Ye.Ya.Rode, A.I. Tsvetkov et al., improved it. As far as foreign papers are concerned, monographs by Smothers and Chang and Mccanzey (on clays thermography) are of certain interest.

The essence of the  thermoanalysis is in identifying temperatures at which physical state of a substance or its chemical composition changes.

During physical or chemical processes of the substance transformation the energy like heat can be absorbed or emitted. If the temperature of the examined substance is registered during the heating process, then, due to the changes of the temperature, we can find the temperature interval where a certain chemical transformation takes place. Each substance has its characteristic interval for transformations. For example, portlandite – Ca(OH)2 – loses hydroxide in the temperature  interval of 500-540 oC. Polymorphic transformation of   -SiO2 takes place at 573 oC, and calcite dissociation – at 975 oC.

This allows to use thermoanalysis to diagnose compounds in mixtures, ores, rocks, etc. with the help of typical only for a given substance  temperatures of dissociation, dehydration, etc.

Thermoanalysis is based on finding changes:

- energy – DTA;

- weight – thermal gravimetry;

- sample sizes – dilatometry;

- electroconductivity and viscosity.

In thermoanalysis process two, three or all four findings can be used together. But differential thermal analysis (DTA) has been used more widely.

DTA is especially efficient when it is used to define phase composition of finely dispersed substances, because it is much more difficult to study them with the help of other methods. When various building materials are examined, DTA indicates characteristic endothermal reactions, which emerge as a result of dehydration and destruction of crystalline structure and exothermal reactions, determined by new phases formation at higher temperatures. This method has been successfully used during few last decades for examining finely dispersed hydrate formations emerging during cement stone and concrete hardening, for studying transformations of the amorphous phase (glasses), for finding impurities in clays, etc.

The base of the method

Heat content changes in the substance is registered with the help of a “simple” thermocouple. But N.S. Kurnakov offered to use a differential thermocouple because the deviations on the “temperature – time” curve were insufficient in the previous case. The same heat content changes were registered on the differential curve, but the peaks were deeper, and the method sensitivity increased dramatically.

- The task: translate in English

Любая термоустановка  состоит из следующих основных узлов:

а)	нагревательного прибора с приспособлением для плавного и
равномерного нагрева исследуемого вещества;

б)	системы термопар;

в)	электроизмерительной аппаратуры для регистрации термо электродвижущая сила (э.д.с);

г)	устройства для автоматической записи кривой нагревания;

д)	вспомогательной аппаратуры - блоки, тигли, держатели термопар и т.д.

Главное требование, предъявляемое к печам для термоанализа - непрерывный и прямолинейный нагрев.

В зависимости от температуры нагревания подбирается материал термопар. Он может быть хромель-алюмелевым при нагреве до 1000°С, либо платино-платинородиевым - при нагреве свыше 1000°С.

В установках для термоанализа применяются простые и дифференциальные термопары, работающие в комплексе с электроизмерительными приборами (гальванометрами или потенциометрами).

- The task: translate in Russian

A simple thermocouple consists of 2 insulated from each other wires of the same  thickness, but of different metals. The wires’ ends are brazed with each other. The place of brazing is called “hot junctions”, the opposite ends are called “free” or “free junctions”.

A differential thermocouple consists of two thermocouples where the same wire ends are connected and also attached to the instrument, recording the change the  electromotive force in the circuit which emerges when the junctions of the thermocouples are heated. One junction of this combined thermocouple is placed in the examined substance, another one – in the inert substance.

At the same temperature of hot junctions the electromotive force emerges in the   thermocouples. This force is mutually compensated in the differential thermocouple and doesn’t cause deviations of a galvanometer’s hand or a potentiometer’s carriage. If the hot junctions have different temperature then non-compensated thermoelectric current emerges in the circuit. As the process begins the temperature of the examined substance increase or decreases in comparison with the standard. A temperature peak appears on the differential curve. It is accepted, that during endothermal processes the differential curve goes downwards from the zero line, but during exothermal processes it go upwards. The deviation amplitude from the zero line reflects the temperatures difference between the examined samples and the standard one, and is the indicator of intensity of thermal process.

Galvanometers of various systems and electronic potentiometers measure the e.m.f. that emerges in thermocouples.

Thermal effects are determination by physical and chemical transformations. Majority of effects emerging as a result of chemical transformations are accompanied with substance mass change.

The shape of diffraction curves is very much effected by the volume of sample,  substance dispersivity, the degree of its caking, heat capacity, heat conductivity, heating velocity, etc. Most often peaks shape is determined by heating velocity (under slow heating peaks are round and wide, under fast heating they are sharp) and by the amount of the used material (small amount give sharp peaks).

In the most widely used method of heating the examined substance the  temperature  increases at constant  velocity. For shooting silicate materials a sample of 2 g and heating velocity of 16-20 o/min are recommended. Thermoanalysis can be also conducted by placing the examined substance into a furnace heated to a certain temperature.

Finding the temperatures on the thermogram at which thermal effects take place is only the first stage in decoding and describing DTA curves. Complete decoding consists of defining the nature of chemical reactions or transformations in the sample during  heating.

- The task: translate in English

Процессы дегидратации, диссоциации, плавления и некоторые полиморфные превращения сопровождаются эндотермическими эффектами на кривой ДТА; реакции же образования новых соединений, полиморфные превращения, сопровождающиеся переходом неустойчивой при данной температуре модификации в устойчивую, переход из аморфного состояния в кристаллическое, кристаллизация коллоидов, обуславливают появление экзотермических эффектов.

Кроме качественного определения минеральных фаз и термопревращений в образце, кривая ДТА позволяет такие производить количественный анализ.

В ряде методов количественного анализа используется измерение площади отклонения дифференциальной кривой от нулевой линии. Поскольку эта площадь пропорциональна величине теплового эффекта и количеству термоактивного вещества, сравнивая величины отклонения на кривой чистого минерала и на кривой исследуемого вещества, можно установить количественное содержание для минерала.

5. The task:Answer the questions:

1. What is thermal methods of analysis?

2 . What is the essence of thermal analysis ?

3. What is the basis method of thermal analysis?

4. What instruments and equipment used for thermal analysis?

5. What is derivatograph? That studied by help derivatograph?

6. How do the preparation of samples for thermal analysis?

7. For what purpose are differential thermal analysis used?

Vocabulary

| Qualitative | Качественный |
| --- | --- |
| Emitted | Излученный, излучаемый |
| Finding | Определения |
| Emerge | Возникать, появляться |
| Deviation | Отклонение |
| Curve | Кривая |
| Insufficient | Незначительный, недостаточный |
| Electro conductivity | Электропроводность |
| Viscosity | Вязкость, липкость, клейкость |
| Thermocouple | Термопара |
| Differential curve | Дифференциальная кривая |
| Dramatically | Резко, ясно |
| Continuous | Непрерывный |
| Wire | Провод, проволока, трос |
| Hot junctions | Горячий спай, нагретый контакт |
| Insulated | Изолированный |
| Thickness | Толщина, плотность |
| Brazed | Спаянный, припаянный, паяный |
| Attach | Прицеплять, соединять |
| Electromotive force | Электродвижущая сила |
| Circuit | Цепь, кругооборот |
| Junction | Спай |
| Dispersivity | Дисперсность |
| Shooting | Съемка |
| Torsion balance | Торсионные весы |

Task for ISW: Read, translate and entitle the text

This method implies heating both an examined substance and a standard one with the help of the same technique. The standard substance must not undergo any changes. Usually the standard substance is alumina previously calcinated at 1100°С. Both substances - the sample and the standard – are placed in the furnace in the same metal unit which minimizes temperature gradient between them. Hot junctions of two thermocouples are inserted both in the sample and in the standard: the simple thermocouple goes (into the sample), the differential one goes both (into the standard and the sample). Temperature changes in both cases is measured, and their difference is recorded as a temperature function, which is marked on the y –coordinate, and the time is marked on the x - coordinate .

When the process is taking place in the sample, and the process is accompanied by emitting or absorption heat, its temperature becomes different from the standard’s temperature, and a current emerges in the differential thermocouple, and the galvanometer registers it.

This current causes turning of the frames in the mirror galvanometers. And the angle of the frames’ turning is proportional to the current magnitude. The light beam from the illuminator is focused on the mirrors of the galvanometers (movable light spot), and reflecting from them the beam goes through the system of mirrors which direct it into the slit of the camera and the scale of visual observation. A synchronous electrical engine rotates a drum with photopaper with the help of reduction gear and friction gear in the direction, which is perpendicular to the light signal movement. When the mirror of the galvanometer turns, it causes the movement of the light spot proportional to the temperature - its trace on the photopaper is the DTA curve in the temperature - time coordinates.

When the heat curves are registered the ends of the record of curves of heating the ends of thermocouples are connected with the register so that exothermal processes gave upward peaks on the diffraction curve, and endothermal processes gave  downwards peaks.

Polymorphic transformations of enantiotropic nature are accompanied with endothermic effect. Polymorphic transformations of monotropic nature (that is, transition of unstable modification at a given temperature into a stable one) are accompanied with exothermal effect.

A termogram was received as a result of shooting, consisting of 2 curves (simple one and a differential one) and needs shaping and decoding. For this purpose before shooting zero points for temperature and differential curves of heating are marked on the photopaper and zero lines are drawn through them. Temperature zero line corresponds to x-coordinate. Then the points responsible for the beginning of  deviation of the curve from horizontal position (the beginning of effect) and from points responsible for maximum deviation (the end of the effect) are taken from the differential curve and marked on the temperature curve; these points are transferred on the calibration ruler, specially designed for this instrument and the factual temperatures are defined within which chemical transformations take place.

Practical work № 3

Petrography of  technical stone (crystal optical researches of technical stone)

The aim of work: translate scientific-technical literature

Duration of work: 2 hour

- The task: translate in Russian

The microscopic analysis used for direct or indirect research of the most various processes. Most often it use for studying the form and the sizes of crystals; processes of growth of crystals and their destruction; identifications of minerals by measurement of their optical constants; definition of the some  crystallochemical  features of crystals structure (habit, cleavage, fissuring, zonality, availability of inclusions, porosity, etc.); phase transformations into substances; processes of diffusion, etc. At availability of an opportunity of preparation of qualitative micro preparations the microscopic analysis allows to control separate stages of any process.

The method of the light microscopic analysis is based on studying of optical properties of crystals that is connected with their structure.

As is known, all minerals in depending on an internal structure and physical properties are divided on the seven syngony: cubic, tetragonal, trigonal, hexagonal, rhombic, monoclinic and triclinic. Crystals cubic the syngonys are the most dense and their physical properties are identical in all directions. Light waves also are widespread with identical speed in all directions, i.e. these crystals optically isotropic.

Crystallographic the system, parameters of refraction, force of double refraction, axial and an optical sign are the basic characteristics of each crystal. Except for them distinguish still color, pleochroism, lengthening and extinguish minerals.

To define the specified optical characteristics of minerals it is possible by means of a polarizing microscope. Now polarizing microscopes МIN -8, МIN -9, etc. are used. They allow to receive increase from 24 up to 900 times. However at greater increases image sharpness is noticeably lost. Therefore working are increases from 160 up to 300 times. Modern microscopes allow to investigate various types of defects in crystals.

Application of microscopes demands preliminary special pre-operation of research objects. Therefore there are some methods of preparation of research objects.

preparating technique.

From all microscopic preparations the main are:

- Transparent petrographic microsection - microsection,

- Powder or immersion preparations,

- Polished microsections

- The task: translate in English

Одним из наиболее точных методов диагностики природных и искусственных минералов является изучение их оптических свойств. Эти свойства рассматриваются при помощи особого прибора — поляризационного микроскопа, применение которого позволяет увеличить образец и рассмотреть его в поляризованном свете как при параллельном, так и при сходящемся ходе лучей.

Методы петрографических исследований широко применяются при изучении различных вяжущих веществ. Особенно полезен петрографический анализ при контроле процесса производства, где он в течение 5—10 мин дает возможность установить причины изменения качества получаемой продукции. Данные петрографического анализа помогают вести контроль за режимом обжига (его равномерностью и длительностью), скоростью охлаждения, крупностью помола, обеспечивая тем самым возможность улучшения технологического процесса и выпуск цемента высокого качества. Исследование вяжущих веществ петрографическим методом производится как в проходящем, так и в отраженном свете.

Клинкер портландцемента получается обжигом до спекания (при температуре 1350—1510°С) известняка с глиной. Вместо известняка и глины могут быть использованы мергели. Качество получаемого при этом клинкера (его минеральный состав, структура) зависит главным образом от режима обжига и от скорости охлаждения.

Систематический петрографический контроль производства портландцементного клинкера сводится к определению свободной извести СаО, минерального состава клинкера и его структуры.

Vocabulary

| Methods petrographic studies | Методы петрографических исследований |
| --- | --- |
| to establish the reasons | установить причины |
| the burning mode | режим обжига |
| uniformity | равномерность |
| duration | длительность |
| the cooling rate | скорость охлаждения |
| grind size | крупность помола |
| transmitted light | проходящий свет |
| reflected light | отраженный свет |
| thin sections | шлиф |
| immersion preparations | иммерсионные препараты |
| section of crystal optics | раздел кристаллооптики |
| substantive provisions | основные положения |
| Portland cement clinker | Клинкер портландцемента |
| roasting to full sintering | обжиг до спекания |
| mineral composition | минеральный состав |
| secondary minerals | второстепенные минералы |
| magnesia (periclase) | окись магния (периклаз) |
| boils down to the determination | сводится к определению |
| fine powder | тонкий порошок |
| microscope slide | предметное стекло |
| microscope stage | столик микроскопа |
| high magnification | большое увеличение |
| power-on analyzer | включенный анализатор |
| needle crystals | игольчатые кристаллики |
| crossed nicols | скрещенные николи |
| cover glass | покровное стекло |

Task for ISW: translate in Russian

Transparent microsection represents a thin section of material under examination thickness of the 0,03 mm, tipped-in between specimen glass and microglass by means of Canada balsam.

At researches by means of a polarizing microscope microsection always it is put on  microscope little table of a by preparation glass up.

Transparent microsections are applied mainly at petrographic researches, at definition of crystals optical constants and at the description of structures of various crystal formations (rocks, refractory brick, portland cement clinker, porcelain, etc.

Powder, or immersion preparations are produced from friable formations. immersion preparations are most simple in manufacturing. For manufacturing immersion preparation from dense substance the last preliminary follows is crush up in a powder (not in a dust!).

Аншлиф, or polished microsection - a piece of the investigated material, one flank of it is polished and grind off from before high luster.

Practical work № 4

Basis of patenting

The aim of work: translate scientific-technical literature

Duration of work: 1 hour

1. The task: translate in Russian

Search and selection of the information should be carried out at the least expenses of time and with use the inter-industry and branch automated information systems.

Carrying out of patent researches with use of search in foreign patent department should be coordinated with Committee on intellectual property rights of the Ministry of Justice of Republic Kazakhstan.

Results of executed search and selection of the information are represented in the reference about search, made under the form of the obligatory supplement 3 in the volume stipulated by the retrieval schedule.

The report about patent researches is draw up at completion of researches and the ending of development of engineering object. In the intermediate stages of researches and development and in scattered instances the results of patent researches are represented by separate forms of the report on types of the works which are carried out at the given stage with registration of the title page, conclusions and the cast list.

The invention as object of the intellectual industrial property

The invention as object of the intellectual industrial property: objects of the invention, criteria of patentability, concept about attributes of invention object.

Inventions are objects invention law. The invention are new and possessing essential differences technical decision of problem in any area of a national economy, social and cultural construction or national defense, giving a positive effect.

the device, a way, substance, microbial strain, culture of cells of plants and animals, and also application of the known device, a way, substance, strain on new purpose can be objects of inventions.

The technical decision as a result of the realization is often embodied in material object – the certain machine, the machine tool station, an alloy, the technical apparatus, etc. However invention law protects not the given material object in itself, but the technical decision, therein expressed. The technical decision can be recognized by the invention if it possesses: 1) novelty; 2) amount of invention; 3) gives a positive effect. The technical decision is considered new upon condition that before date of application priority the essence of this or identical decision has not been opened in the country or abroad for indefinite set of people so, that there was possible its realization. Disclosing of essence of the decision can occur or its publication in the country or abroad, or demonstration at an exhibition, or as a result of the open application (at the industrial undertaking, in shop, on agricultural works, etc.). In all these cases there is accessible a copying of the decision that entails losses of novelty by it. Novelty is established for a moment from which the priority of the application is defined. Such moment is, as a rule, day of filing of application.

Conditions of invention patentability

Objects of patent law can be those if they answer purpose regimented law. For inventions this following:

- the result of intellectual activity should be the technical solution in any area concerning to a product or (and) to a way, except for directly specified unprotected objects;

- the result of intellectual activity should be new, have inventive level and we shall industrially applicable.

So, main principle (condition) of patentability of the decision pretend to  recognition its invention (useful model), is it subjectoability, both in a patent law in whole, and in relation immediate to the invention or the industrial sample.

The second criterion of patentability of the invention is inventive level.

The third criterion of invention patentability is industrial applicability. The invention is industrially applicable if it can be used in the industry, an agriculture, public health services and other branch of activity.

- The task: translate in English

Отчет о патентных исследований должен содержать:

- титульный лист;

- общие данные об объекте исследования;

- список исполнителей;

- содержание (перечень документов)

- основную часть;

- приложения.

Общие данные об объекте исследования должны содержать:

- наименование организации (предприятия) – исполнителя НИР или разработки;

- наименование предприятия-изготовителя;

- наименование организации (предприятия) – заказчика;

- даты начала и окончания разработки или исследования (год, месяц);

- назначение, область применения, краткое описание объекта.

Устанавливаются следующие разделы основной части отчета:

- технический уровень и тенденции развития техники;

- патентно-лицензионная ситуация;

- новизна и правовая защита;

патентная чистота объекта

Основную часть отчета выполняют в виде табличных форм.

Формы дополняют необходимым текстовым обоснованием или пояснением.

В конце каждого раздела приводят выводы и рекомендации.

В приложения к отчету о патентных исследованиях включают:

- задание на проведение патентных исследований;

- регламент поиска;

- справки о поиске; описания изобретений, аннотации документов и другие справочные материалы.

Vocabulary

| Authorship | Авторство |
| --- | --- |
| Achievable | Достижимый, достигаемый |
| Consequently | Следовательно, поэтому, в результате, таким образом |
| Deaf-mute | Глухонемой |
| Embodied | Осуществлять |
| Feasibility | Возможность |
| Interelement coupling | Связь между элементами |
| Issuance | Публикация, выдача патента |
| Indispensable | Необходимый, обязательный |
| Inter-industry | Межотраслевой |
| Lengthening | Удлинение, растяжение, продление |
| Miscalculations | Ошибка в расчетах |
| Microbial strain | Штамм микроорганизма |
| Multiclaim | Многозвенная формула |
| Nonobviousness | Неочевидность |
| Novelty | Новизна, новинка |
| Overwhelming | Подавлять |
| Pertinent | Соответственный, подходящий, применимый |
| Genus proximus | Ограничительная часть |
| Retrieval schedule | Регламент поиска |
| Scattered instances | Отдельные случаи |
| Sintering | Спекаться, спекание |
| Superinduction | Внесение |
| Single-claim formula | Однозвенная формула |

Task for ISW: translate in Russian

All technical information on invention is expounded in the description and the formula of invention.

The designation of invention should verbatim align with banner words of the formula of invention. Exception is inventions the essence which consists in application formerly known devices, methods and substances in new purpose.

The formula of invention is the composed by rule the brief verbal description which are voiced technical substance of invention. The characteristic of the invention is expressed by attributes of invention object.

In a patent practice the formula of invention is compose or in the form of one item (single-claim formula), or in the form of two and more items (multiclaim formula).

It is necessary to abide by following rules of drawing up of formula:

- the formula should begin with the name of invention specified in the application and the description;

- in the formula of invention it is necessary to specify all essential attributes of object invention abide by what scilicet sum-total of essential attributes should be necessary and sufficient for achievement of purpose of invention, that is reception of positive effect;

The formula of invention should consist, as a rule, of genus proximus including attributes, the general for declared object of the invention and the prototype (known attributes), the characteristic feature including attributes, which distinguish declared object of the invention from the prototype (that is new attributes of invention object), and the purpose of invention characterizing a positive effect; the genus proximus of invention formula also is separated from  following for it characteristic feature by expression: " differing that, with the purpose " after which the purpose of invention is underlined.

Subject 3. Translation of technical-scientific literature in field of «Chemical technology of binders»

Practical work № 5

Technology of cement

The aim of work: translate scientific-technical literature

Duration of work: 3 hour

- The task: translate in Russian

Men learned to use gypsum and lime-based binders long ago, approximately 4-3 thousand years B.C. In the Х1X th  century cement was used in construction. In 1825 the Russian engineer Yegor Cheliev published his book «Complete instruction for preparing cheap and best merthel or cement, rather strong for underwater facilities, i.e. : canals, bridges, swimming-pools, dams, cellars and plasters» for stone  and wood buildings. Being in charge of military buildings team which restored Moscow Kremlin after Napoleons raveging, Cheliev generalized builders experience in this book.

He described the method to prepare a binder using a mixture of lime-stone and clay. In the presence of water the mixture was formed into bricks, and the bricks were calcinated in furnaces at the temperature about 1100-1200 0C. After that the calculated product was ground, sieved to add gypsum. To cement in order to increase its strength and weather-resistance.

At same time, in 1824, Joseph Uspdin, an English engineer, patented a binder which he had invented and called «Portland cement». The Town of Portland gave the name to the cement» because in its vicinities so-called portland stone was mined. The binder offered by Uspdin when hardened looked like portland stone which was considered rather good building material.

The name remained, but the binder offered by Uspdin is actually a variety of roman cement but not portland cement. The composition, properties, calcinations temperature  of the binder described by Cheliev, is closer to portland cement in its present-day understanding than Uspdins  cement. Now roman cement  is used very seldom, because it has lower characteristics and it has been completely crowded out.

At the beginning binders were produced ay small enterprises and workshops located at the building sites.

The most outstanding  Soviet scientists in the field of cements, A.A. Baikov, P.A. Rebinder, V.A. Kind, V.N. Yung, P.P. Budnikov, N.A. Toropov, Yu.M. Butt, V.V. Timasgev,  B.I. Nudeiman, T.A. Atakuziev, et. аl. developed and supplemented, which knowledge concerning clinker formation binders hardening, they made up new efficient cements. The V1-th International Congress on cement chemistry, which took part in Moscow in 1974, was recognition of achievements’ of Soviet scientists.

Our cement mills in Chimkent, Sas-Tobe, Semipalatinsk, Ust-Kamenogorsk and Karaganda contribute worthily to the construction industry of Kazakhstan. Besides, cement is produced by «Monolit LTD.» in the village of Kurday of Dzhambulskaya oblast (there is one Technological lune of low capasity). In 1990 in the KazSSR more than 8mln. tons of cement were produced, including over 400.00 tons of decorative white and colored cements.

- The task: translate in English

Для повышения эффективности цементной промышленности в первую очередь необходимо переходить на сухой способ производства; увеличить выпуск смешанных цементов; шире использовать в качестве сырья и активных минеральных добавок различные отходы промышленности; внедрять помол сырья и цемента в замкнутом цикле; в помольных агрегатах нового поколения; снижать влажность сырьевого шлама; осуществлять дополнительное питание печей техногенными продуктами; разрабатывать и внедрять энерго- и ресурсосберегающие технологии.

Цементная промышленность является базовой отраслью строительного комплекса, от которой зависит состояние экономики и социальных вопросов развития Республики - строительство жилья, объектов здравоохранения, просвещения, промышленного и сельскохозяйственного производства, коммуникаций.

Важнейшими направлениями перспективного развития цементной промышленности Республики следует считать следующие:

-	техническое перевооружение и реконструкция цементных заводов с переводом их на экономичный сухой способ производства;

-	широкое внедрение ресурсо- и энергосберегающих технологий производства с вовлечением в технологический процесс отходов промышленности в качестве сырья и активных минеральных добавок, использованием разжижителей сырьевого шлама, минерализаторов обжига клинкера, интенсификаторов процесса помола цемента;

-	повышение качества цемента, оптимизация ассортимента продукции, увеличение выпуска смешанных и специальных цементов:

полное обеспечение отечественными тампонажными цементами потребностей западных нефтедобывающих регионов Республики Казахстан:

- уменьшение вредных выбросов в атмосферу, оздоровление окружающей среды, улучшение условий труда;

- подготовка и повышение квалификации специалистов цементных заводов.

Task for ISW: translate in English

- Развивалась наука о цементе.

- Цементная промышленность является базовой отраслью строительного комплекса

- После войны потребность в цементе значительно увеличилась

- Статьи по вяжущим веществам стали печататься

- В помольных агрегатах нового поколения

- Строительство жилья, объектов здравоохранения…..

- Наиболее ценное сырье – известковый мергель

- Качество клинкера зависит от его химического и минералогического состава

- Сухая строительная смесь это современный материал строительной индустрии

- При медленном схватывании цемента сильно замедляются темпы строительства

- Основными минералами клинкера являются ................, ................., ..............

- Постоянно осуществляется подготовка и повышение квалификации специалистов цементных заводов

- Тонкообломочными горными породами являются ................. ................

- Требуется предварительное их обогащение

- Глинистое сырье необходимо для производства портландцемента

- The task: translate in Russian

Our industry produces over 20 different types and kinds of cement for construction and economic activities.

Our industry produces portland cement and slag-portland cements, white and coloured cements, road  cement, oil-well cement for oil-wells and gas wells; noncontracing cements and expanding cements; sulfate-resistant, plasticized and hydrophobic cements, high-strength cement, high- early-strength cement and other special cements.  They are widely used in production of architectural and decorative pieces, for finishing buildings and facilities, for buildings hydro-power stations, sea and ocean facilities, in industrial production reinforced concrete structures, for coating roads and runways, in drilling oil and gas wells, for production of asbestos-cement wares, for building metallurgical, chemical and other heating units.

Portland cement is hydraulic binder, which is a product of fine grinding of portland cement clinker. The said clinker is produced by calcination of raw materials mixture of a proper composition till clinkering and containing dominating amount of calcium silicates. According to standard 10178-85 portland cement is a hydraulic binder produced by joint fine grinding of clinker and gypsum which hardens in water and  air. Clinker is produced by calcination till clinkering of raw materials mixture composition of which  provides Са silicates domination.

When clinker is ground some gypsum is added in the amount which is necessary to slow terms  setting and to improve  some portland cement properties. Gypsum content must not exceed 3,5 % according to SO3.. It is possible to use gypsum stone, phosphogypsum and borogypsum. It is possible to add up to  15 % of active mineral additions or granulated blast furnace slags when clinker is being ground without changing the name of  product.

Clinker is a semi-prepared product and looks like hard lumps or peas, later finely ground of portland cement powder.

According to standard 10178-85 together with portland cement there is portland cement with mineral additions. The latter unlike portland cement contains certain amount of active mineral additions: granulated blast furnace slags and electrical thermophosphorus slags – up to 20 %, additions of sedimentary origin – up to 10 %, other active mineral additions – up to 15 %.

- The task: translate in English

Портландцемент – важнейшее гидравлическое вяжущее вещество. Это основной материал современной строительной индустрии.

Согласно 10178-85, портландцемент делится по прочности на четыре марки: 300, 400, 500 и 600 в соответствии с минимальной величиной предела прочности при сжатии образцов из раствора 1:3 пластичной консистенции через 28 суток, в кгс/см2 (соответственно 30, 40, 50 и 60 МПа). Предел прочности при изгибе цементов этих марок должен быть соответственно не менее 4,5; 5,5; 6 и 6,5 МПа.

Начало схватывания портландцемента должно наступать не ранее 45 мин, а конец – не позднее 12 ч от начала затворения. Если цемент быстро схватывается, то прежде чем его успевают использовать, он уже превращается в камневидное тело. При медленном схватывании цемента сильно замедляются темпы строительства. Для замедления сроков схватывания цемента к клинкеру при помоле добавляют гипс в таком количестве, чтобы содержание SO3 в цементе находилось в пределах 1,5-3,5 %.

Важными свойствами портландцемента являются также плотность и объемная масса, водопотребность, пластичность, водоотделение, морозостойкость, выделение теплоты при твердении, сцепление со стальной арматурой, стойкость при маганизировании (сохранность свойств цемента при длительном хранении)..

Task for ISW: translate in Russian

Technological scheme of portland cement production

Portland cement production consists of a number of technological operations which can be divided into two main groups.

The first group includes operations for clinker production, the second group includes crushing together with gypsum, and in a number of cases with additions, too, that is, portland cement production.

Clinker production:  raw materials mining → crushing, grinding and blending, calcinating raw materials mixture.

Portland cement productions: clinker crushing, mineral additions preparation (crushing, drying), gypsum stone crushing, clinker grinding together with active mineral additions and gypsum, storage, packing.

- The task: translate in Russian

Cement clinker composition.

Clinker's quality depends on its chemical and mineralogical compositions. Chemical composition is characterised by various oxides contents. Mineralogical composition is characterized by quantitative ratios of the minerals which  emerge during calcination processes.

Chemical composition of clinker is more often the following (in mass percentage): СаО 62-67; SiO2 20-25; Al2О3 4-8; Fe2О3 2-5; MgО, SO3 and other 1,5-4. The major oxides - SiO2, Al2O3; Fe2O3 and CaO – interact during calcination and form clinker minerals, their ratio determines portland cement  properties.

Major clinker minerals are: alite 3CaOSiO2 (C3C), belite – β- modification of 2CaOSiO2 (β-C2S); three-calcium aluminate 3CaOAl2O3 (C3A) and calcium alumoferrites of variable composition from 8CaOAl2O3Fe2O3 up to 2CaO Fe2O3 (C8A3C – C2F).

Alite consists of three-calcium silicate, there are some impurities, included in crystalline lattice as solid solutions and isomorphic compounds. Alite is the most important mineral of portland cement clinker, the major carrier of its binding properties. It determines the possibility to achieve high strength during first hardening terms and defines strength indicator after  28-days. When alite content in clinker increases to the interval of 40 to 70 %, strength indicators grow according to linear dependence.

Belite consists of β – modification of bi-calcium Si (α, β and γ), there are some impurities, entering the crystalline lattice. Phosphorus, chromium, aluminium oxides in β-C2S stabilize this unstable modification and give a chance to keep it. The modification has hydraulic properties. During slow cooling and significant amount of bi-calcium silicate in clinker, there is a transition of β-modification which does not possess hydraulic properties. At the same time clinker crumbles to powder due to  increase of volume, determined by different densities of β- and γ-modifications (the difference is about 10 %). Belite has low strength at the first stage, but then strength indicators grow.

Three-calcium aluminate speeds up cement hardening process during first terms after mixing with water. C3A as crystalline formations is included in the composition of a transition substance.

Са alumoferrites together with aluminates and clinker glass form layers between separate grains of minerals. They are solid solutions, C4АF is found more often, uncrystallized glass is also present. Its content depends on  cooling speed and composition clinker.

The higher alite content, more difficultly calcination process, the higher the temperature. C3A  increase (and especially C3AF) facilitates clinker baking, improves covering formation. With higher C3S content, clinker grinding improves, but with higher C2S the process aggravates. It can be explained by less hardness of three-calcium silicate and its higher brittleness. Clinkers with higher alumoferrites content are ground with greater difficulty.

Choosing the production method

According to the peculiarities of preparation of raw materials mixtures, there are four methods to produce portland cement: a wet one, a dry one, a semi-wet method and a combined method.

The wet method: the raw materials mixture is ground finely in water which results in charge as water suspension - slime.

The dry method: the raw materials mixture is dried and then ground into fine powder. Dry powder mixture is calcinated. The semi-wet method is different from the dry one, because the mixture is granulated with 10 to14 % water addition and is calcinated in granular with Ш 10 to15mm.

If the combined methods is used then the raw  materials mixture is prepared like in the wet methods (slime), then it goes to the filters and dewatered up to 16-18 % of moisture and sent for calcination as semi-dried mass.

- The task: translate in English

Сырьевые материалы для производства минеральных вяжущих.

При всем разнообразии используемого сырья материалы могут быть сведены  в несколько групп:

Карбонатные породы – известняк, мел, известняк-ракушечник, мрамор, известковый туф. Все эти породы содержат в основном CaCO3 , теоретический состав которого 56% CaО и 44 % СО2. Карбонатные породы – основной вид сырья при производстве портландцемента, глиноземистого цемента и строительной воздушной извести.

Глинистые породы. Глинистым сырьем являются тонкообломочные горные породы, состоящие в основном из глинистых материалов каолинитовой, монтмориллонитовой, аллофановой групп и группы гидрослюд (иллитов).

Мергели. Переходная горная порода от известняков к глинам, применяемая при производстве портландцемента, представляет собой природную смесь из 20-50% глинисто-песчаных веществ и 50-80% мельчайших частиц углекислого кальция.

Наиболее ценное сырье – известковый мергель, содержащий примерно 75-80% CaCO3 и 20-25 % глины.

Корректирующие добавки.

Железосодержащие добавки – пиритные огарки.

Глиноземистые добавки -  маложелезистые глины, боксит.

Кремнеземистые добавки – Fe2O3 до 40 %, для кремнеземистых  Al2O3 – 30% (не менее).

Бокситы. Они являются не только корректирующей добавкой, но и основным сырьем для производства глиноземистого цемента. Бокситы представляют собой оксиды алюминия с примесями SiO2, Fe2O3, TiO2, H2O, CaO, MgO.

Активные минеральные добавки. Они предназначены для производства вяжущих веществ на основе портландцементного клинкера, а также применяются при изготовлении известково-пуццолановых, известково-шлаковых и  др. местных вяжущих. Активные минеральные добавки несколько снижают себестоимость цемента без существенного понижения его качества. Основное их назначение связать известь в нерастворимые, способные к твёрдому твердению вещества и повысить водостойкость вяжущего.

Гипсосодержащие породы. Такие породы являются сырьём для производства гипсовых вяжущих, а также применяются как добавка к цементу с целью регулирования сроков его схватывания. Применяю природный  двуводный гипс CaSO4×2H2O  и природный ангидрид CaSO4.

Vocabulary

| binding materials, binders | Вяжущие материалы |
| --- | --- |
| binding substance, binders, astringent substance | Вяжущие вещества |
| limestone | известняк |
| mixture | смесь |
| strength | прочность |
| clay | глина |
| method of preparing | метод изготовления |
| weather resistance | атмосферо-устойчивый |
| composition | состав |
| properties | свойства |
| to destroy | разрушать |
| rotary kiln | вращающаяся печь |
| a technological equipment | технологическое оборудование |
| building materials | строительные материалы |
| waste | отходы |
| granulated slag | гранулированные шлаки |
| ash | зола |
| corrective additives | корректирующие добавки |
| dry method | сухой метод |
| hardening binders | твердение вяжущих |
| To sieve | просеивать |
| sieve | сито |
| a powder | порошок |
| raw mixtures | сырьевая смесь |
| enterprises | предприятие |

Task for ISW: translate in English

- Устанавливают химический состав и подают шлам на обжиг во вращающие печи

- Обжиг клинкера является самостоятельной технологической операцией

- Помол клинкера осуществляют совместно с активными минеральными добавками

- Различают природные и искусственные активные минеральные добавки

- После дробления размер фракции уменьшается

- Приобретать способность к гидравлическому твердению

- Сырьевые материалы можно разделить на несколько основных групп

- Для окончательного домола сырьевых материалов применяют шаровые и трубные мельницы

- Влажность размалываемого сырья не должна превышать 1-2%

- При медленном схватывании цемента темпы строительства сильно замедляются

Practical work № 6

Gypsum-based binders and wares on it base

The aim of work: translate scientific-technical literature

Duration of work: 1 hour

- The task: translate in English

Гипсовыми вяжущими материалами называют тонкоизмельчённые продукты термической обработки естественных или искусственных разновидностей сульфата кальция, способныt после затворения водой схватываться, твердеть и превращаться в камень на воздухе.

Различают гипсовые вяжущие вещества низкообжиговые (полученные при температуре 140 – 1700С) и высокообжиговые (полученные при температуре 590 – 10000С). Низкообжиговые состоят в основном из полуводного гипса и быстро твердеют. К ним относятся гипсовые вяжущие марок от Г – 2 до Г – 25, используемые для строительных, формовочных и медицинских целей.

Высокообжиговые состоят преимущественно из  безводного кальция-ангидрита и медленно твердеют. К гипсовым вяжущим веществам относят также смешанные композиции, основной составляющей которой является полуводный гипс, а дополнительными – известь, цемент, молотые гранулированные доменные шлаки. В зависимости от вида дополнительной составляющей различают гипсоизвестковые, гипсоцементные, гипсошлаковые, и др. вяжущие вещества.

Гипсовые вяжущие вещества изготовляют из гипсового камня, представляющего собой в основном двуводный гипс CaSO4·2H2O. Ангидрита, состоящего главным образом из безводного гипса - CaSO4, и некоторых отходов химической промышленности, содержащих преимущественно двуводный или безводный сульфат кальция. Химически чистый двуводный  или безводный сульфат кальция. Химически чистый двуводный гипс состоит из 32,56 % СаО; 46,51 % SO3  и 20,93 % воды, а ангидрит – из 41,19 % СаО и 58,81% SO3. В природном гипсе обычно присутствуют примеси глины, песка, известняка и некоторых других веществ. Содержание CaSO4·2H2O в предварительно высушенном до постоянной массы гипсовом камне должно быть, согласно ГОСТ 4013-82, не мене 95, 90, 80 и 70 % соответственно для 1, 2, 3 и 4-го сортов.

- The task: translate in Russian

Technological process of gypsum-based binders consists of grinding gypsum  stone and the following thermal processing (dehydration).

The degree of gypsum  stone grinding is determined by the apparatus chosen for thermal processing. The material goes to shaft furnaces as pieces of 70 to 300 mm size, to rotating furnaces  - as pieces of 10 to 35mm size, to digesters - as powder.

Conventionally, sequence of main operations can be presented as the following:

- Crushing – grinding – boiling

- Crushing – drying – grinding – boiling

- Crushing – drying – grinding – boiling

- Crushing – grinding – boiling – grinding

- Crushing – drying + grinding – grinding

- Crushing – calcinations – grinding

First five sequences are used for production of building gypsum in gypsum digesters. Sequences 1 is used only for dry raw material. If moisture content of raw material exceeds 1 % it must be dried before grinding according to sequences 2. An expedient combination of these two operations in one technological apparatus in show in sequences 3. To improve the quality of the product it is desirable that semi-aquatic gypsum should be ground the second time according to sequences 4-5. Sequences 6 is used for production of both gypsum-based binders of high calcination, and gypsum-based binders of low calcination. Fine grinding  of gypsum stone and its drying are combined in the mill at the expense of heated gases (temperature 300 – 4000С).

Vocabulary

|  | high grindability | высокая размалываемость |
| --- | --- | --- |
|  | finely ground products | тонкоизмельчённые продукты |
|  | thermal processing | термическая обработка |
|  | low calcination | низкообжиговые |
|  | high calcination | высокообжиговые |
|  | waterless gypsum | безводный гипс |
|  | semi-aquatic | полу-водный гипс |
|  | calc-tuff | известковый туф |
|  | clastic limestones | обломочный известняк |
|  | harmful | вредные |
|  | harmless | безвредные |
|  | bi-aquatic gypsum | двуводный гипс |
|  | Impurities of clay | примеси глины |
|  | shell limestone | известняк-ракушечник |
|  | chalky clay | мергель |
|  | earthy-loose limestone | землисто – рыхлые известняки |
|  | gaize | опоки |
|  | tripoli | трепел |
|  | the degree of grinding | cтепень измельчения |
|  | digesters | варочные котлы |
|  | boiling | варка |

Task for ISW: translate in English:

1) Гипсовыми вяжущими материалами называют тонкоизмельченные продукты термической обработки естественных или искусственных разновидностей сульфата кальция, способные после затворения  водой схватываться, твердеть и превращаться в камень на воздухе.

2) Существует несколько теорий, объясняющих механизм твердения вяжущих веществ, в частности полуводного гипса.

3) Известно производство гипса повышенной прочности запариванием в автоклаве гипсового камня.

4) Технологический процесс производства гипсовых вяжущих состоит в измельчении гипсового камня.

5) Первые пять схем используют при производстве строительного гипса в гипсоварочных котлах.

6) Превращение пластичного теста в камневидное тело связано с образование гидратных соединений.

7) Вяжущее растворяется с образованием насыщенного раствора составляющих его соединений.

8) Известны два способа получения прочности гипса.

9) Общий цикл запаривания и сушки гипсового камня составляет 28-30 часов.

10) Титаногипс – отход при производстве титана.

11) Состоит он в основном из двуводного гипса.

12) Затем гипсовый камень подвергают сушке при закрытых крышках.

13) Превышенное количество примесей снижает.

14) Дробление-помол-варка

15) В варочные котлы в виде порошка

16) Гипсоизвестковое вяжущее

17) Перед помолом его необходимо сушить

18) Перекристаллизация коллоидных частиц в большие кристаллы и образование сростка.

19) Химически чистый двуводный гипс состоит…..

20) Выгруженный из автоклава продукт размалывают

Practical work № 7

Lime binder materials and wares on it base. Hydraulic lime

The aim of work: translate scientific-technical literature

Duration of work: 1 hour

- The task: translate in Russian

Common lime  is an air binder received by calcinating calcium-magnesian rocks – chalk, lime stones, dolomitic and marl lime stones, and dolomites containing not more than 6 % of clay and sand impurities. Thes rocks are calcinated till possibly complete  emission of carbonic acid.

According to the type of processings common lime is divided into:

- lump quicklime, which is the product of lime stone calcination and consists of mainly СаО. Lump quicklime is lump calcination lime which can contain impurities of fine particles of lime and burnt fuel ashes.

- ground quicklime  is the product of lump quicklime grinding. The product mainly consists of  СаО, too. Ground quicklime is powder produced by  grinding lump quicklime.

- hydraulic lime is fine powder, received as a result of slaking lump lime with excessive water and consisting mainly of  Са (OH) 2 .

- Lime dough is the product of plastic consistency received at slaking lump lime by surplus of water, and consisting of mainly Са (OH) 2 and waters.

Building common lime has the ability of slaking;  when it turns into powder which becomes plastic lime paste when water is exessive. Lime properties are mainly influenced mainly by such impurities (containing in limestones), as clay, magnesium carbonate, quartz, etc. They decrease in different degrees  the ability of lime of shake. Pure limestone when calcination property results in the product which slakes  completely and turns into calcium hydroxide.

The amount of water depends on lime quality, slaking method and some other factors. The richer the lime,  the more water in the limy paste. On average for slaking lime to paste 2,5 л of water is taken per 1 kg lump quicklime. If to add more water, then we have lime milk.

2. The task: translate in English

Согласно ГОСТ 1174-51 по содержанию окиси магния различают три вида строительной  воздушной извести:

- маломагнезиальная (кальциевую), содержащая не более 5% МgО;

- магнезиальная, содержащая от 5 до 20 % МgО;

- доломитовая, содержащая от 20 до 41 % МgО.

В зависимости от выхода теста, содержания непогасившихся зерен, а также суммарного содержания окиси кальция и магния известь бывает трех сортов I, II и III.

Если по различным показателям известь соответствует разным сортам, то сортность ее определяется по низшему показателю.

По признаку скорости гашения известь делится на: быстро гасящуюся – со скоростью гашения до 10 мин., средне гасящуюся – от 10 до 30 мин. и медленно гасящуюся – свыше 30 мин. За скорость гашения принимается время от момента смешивания с водой до момента достижения максимальной температуры.

В зависимости от температуры, развивающейся при гашении, известь разделяется на низкоэкзотермическую – с температурой гашения ниже 70 о и высокоэкзотермическую – с температурой гашения свыше 70 о

Сырьем для производства воздушной извести служат известково-магнезиальные карбонатные горные породы. Наиболее частыми примесями в известковых горных породах являются углекислый магний, глинистые вещества, кварц и окись железа..

Vocabulary

|  | non-slaked grains | непогасившиеся зерна |
| --- | --- | --- |
|  | сommon lime | воздушная известь |
|  | air binder | воздушное вяжущее |
|  | carbonic acid | углекислота |
|  | lime milk | известковое молоко |
|  | lump quicklime | негашеная комовая известь |
|  | raw meal | сырьевая мука |
|  | ground quicklime | негашеная молотая известь |
|  | hydraulic lime | гидравлическая известь |
|  | Lime dough | известковое тесто |
|  | slaking lump lime | гашение комовой извести |
|  | excessive water | избыток воды |
|  | magnesium carbonate | углекислый магний |
|  | slaking method | способ гашения |
|  | low exothermal | низкоэкзотермическая |
|  | high exothermal | высокоэкзотермическая |

Task for ISW: translate in Russian

Physical structure of the raw material used for quicklime production is of great importance. For example, marble-lime limestones are calcinated with great difficultlies due to their high density. If the raw material has earthly loose structure (for example, chalk), then its calcination in shaft furnaces is difficult, because the lumps such a material crumbled easily and fine pieces fill the gaps between calcinated lumps and hamper the draught. That is it is more expedient to calcinate easily crumbling raw material in rotating furnaces.

Shaft furnaces are good for calcinating lumps of pure and porous limestones of middle size (60 to 200 mm) with compression strength of 10-50 МPа. Limestones of lower compression strength abrade while moving along the shaft, increase its resistance and decrease the productivity of the furnace. Carbonate rocks with compression strength less than 2 МPа cannot be calcinated in shaft furnaces. The size of fuel lumps is also essential importance. The size must be 40 to 60 mm. The ratio of average sizes of fuel lumps  and limestone lumps is  1:2 – 1:3 during calcination shaft furnaces.

Practical work № 8

Magnesia binders

The aim of work: translate scientific-technical literature

Duration of work: 1 hour

- The task: translate in English

К магнезиальным вяжущим веществам относятся каустический магнезит и каустический доломит. Первый изготовляют из природного магнезита, а второй — из природного доломита.

Магнезит представляет собой углекислую соль магния (MgCO3). Содержание MgO в магнезите составляет 47,82%, а СО2 — 52,18%. Природный магнезит всегда содержит различные примеси, главным образом кремнезем, глину, углекислый кальций.

Доломитом называют минерал, представляющий собой двойную углекислую соль кальция и магния СаСО3·MgCO3. Теоретический состав доломита: 54,27% СаСО3, 45,73% MgCO3 или в оксидах 30,41% СаО, 21,87% MgO и 47,72% СО2.

Для производства каустического доломита желательно применять сырье с большим содержанием оксида магния.

Производство магнезиальных вяжущих веществ

Процесс производства каустического магнезита и каустического доломита состоит из обжига сырья и помола продуктов обжига. Разложение углекислого магния начинается при температуре около 673К, но протекает с достаточной скоростью лишь при 600— 650 oC. Практическая температура обжига магнезита в шахтных печах 750—800 oC, а во вращающихся — 1000 oC.

Качество каустического магнезита зависит от температуры и продолжительности обжига.

Каустический магнезит обжигают в шахтных и вращающихся печах.

После обжига магнезит размалывают в шаровых мельницах, причем если величина кусков обожженного материала значительна, то их перед помолом подвергают дроблению.

Разложение доломита происходит в интервале температур от 700 до 900 oC.

Температура обжига каустического доломита составляет 650—750 oC. Она изменяется в зависимости от состава сырья и конструкции печи.

Магнезиальные вяжущие вещества в отличие от других вяжущих затворяют не водой, а растворами хлористых и сернокислых солей. Наиболее распространенным затворителем, дающим лучшие результаты, является раствор хлористого магния MgCl2.

- The task: translate in Russian

Properties magnesia binder substances

Caustic magnesite possesses property to absorb moisture and carbonic acid from air therefore are formed Mg (OH) 2 and MgCO3.

In comparison with caustic magnesite caustic dolomite possesses smaller durability (marks: 100, 150, 200 and 300). Caustic dolomite should contain not less than 15 % oxide magnesium and no more than 2,5 % free oxide calcium, and the size of losses at incineration should be within the limits of 30—35 %.

Magnesian binder substances apply to manufacturing xylolite, fibrolite, thermally insulating materials, mortars for plastering, an artificial marble, the bases under "pure" floors, artificial millstones, grinding and lithographic stones, for production of building details and of some other products.

Vocabulary

|  | caustic magnesite | каустический магнезит |
| --- | --- | --- |
|  | carbonic salt of magnesium | углекислая соль магния |
|  | widespread rock | распространенной горной породой |
|  | double carbonic salt | двойную углекислую соль |
|  | dolomitic flour | доломитовой мукой |
|  | turn into | превратиться |
|  | Decomposition of carbonic magnesium | Разложение углекислого магния |
|  | shaft furnace | шахтная печь |
|  | ball drum | шаровая мельница |
|  | burnt material | обожженный материал |
|  | design of the furnace | конструкции печи |
|  | temper | затворять |
|  | incineration | прокаливание |
|  | xylolite | ксилолит |
|  | thermally insulating materials | термоизоляционных материал |
|  | mortar for plastering | штукатурный раствор |
|  | woody filler | древесный заполнитель |

Task for ISW: translate in English

- Магнезиальные вяжущие являются воздушными вяжущими.

- Хлористый магний значительно повышает растворимость окиси магния.

- Магнезиальные вяжущие вещества применяются главным образом в смеси с древесными заполнителями

- Mg(OH)2 может иметь две формы: стабильную и метастабильную.

- При затворении MgO водным раствором MgCl2 образуется комплексный Mg-гидроксихлорид

- Это соединение кристаллизуется в виде игл или волокон.

- На основе каустического магнезита можно получить так называемый гелевый цемент.

- Углекислый кальций повышает плотность твердеющей массы.

- Углекислый кальций способствует карбонизации извести.

- Известь может образоваться в небольшом количестве при обжиге доломита.

Subject 4. Translation of technical-scientific literature in field of «Chemical technology of ceramic and refractories»

Practical work № 9

Structure and fundamental properties of ceramic

The aim of work: translate scientific-technical literature

Duration of work: 2 hour

1. The task: translate in Russian

The making of pottery is one of the oldest of human crafts. Over the centuries different styles and techniques have developed in different parts of the world.

In the 18th century, a flourishing industry in many parts of Europe was strongly influenced by the import of fine and highly decorated ware from the Far East. Japan had learned the ceramic art from China about 400 years earlier. With the Industrial Revolution and the general change in conditions in Western Europe, production grew rapidly. At present, almost every country manufactures some ware for domestic use, and pottery is an important export from some countries. Production is now on a factory scale in many parts of the world. While the basic principles of manufacture have not changed, there has been considerable progress in the way in which manufacturing is carried out. This is particularly so in the forming or shaping of ware, in its firing and in the decoration techniques used. The increasing use of microprocessors and robots results in the introduction of high levels of automation in production areas. However, there also still exist everywhere many small-scale craft potteries.

Classification of ceramics.

- Building ceramics:  brick, stones ceramic;  tile, oven tiles; sanitary-engineering products: porcelain  and faience products (thin ceramics); ceramic tiles; expanded-clay aggregate, agloporite, pumice; ceramic pipes

2. Thin ceramics: porcelain – economic, electrotechnical, sanitary-building; ceramic tiles

3. Refractory products: fireclay, dinas, magnesital, corundum, spinelite

4. Technical ceramics

5. Thermal isolational ceramics

6. Art ceramics

Grain structure of weights.

Grain structure of mineral components  is chosen in of the expence of its influence on properties of products, and also on behavior of a material in processes of formation, drying and burning.

Used various structures ("powders") on a degree of crushing can be broken into two greater groups – coarse-grained and finely-grained. Coarse-grained consist of structures with significant or even more  fractions in the size of 0,5-1 mm and over. In finely-grained structures all particles or a great amount have the sizes less than 0,05-0,01 mm.

Coarse-grained masses are used in industry of almost all fire-proof products and in industries so-called rough building ceramics. Distinctive feature of mass from coarse-grained powders is their inability to condense intensively in burning.

Finely-grained mass is used in production of household and electro technical porcelain, some finishing building materials and practically of all kinds of technical ceramics. These productions are called finely-ceramical materials. The finely grain composition of powders facilitates processes of chemical interaction of components and condensation in burning. The products differ in volumetric changes in burning and in most cases they are concerned to the type of  sintered  (the general porosity not more than 5 – 10 %, the open porosity up to 1 – 2 %). some kinds of ceramics (for example, faience) with rather high porosity are received from finely-grained mass, but with homogeneous finely porosity  structure.

Raw materials

All the raw materials employed in technology of ceramics are divided into 4 groups:

- Clay materials

- Fluxing agents

- Filling aggregates

- Additional and auxiliary materials

2.To translate in English

- Первоначально термином «керамика» называли изделия, изготовленные из природных глин.

- С греческого «керамос» означает глина, гончарное искусство.

- Керамику можно определить как совокупность изделий, обладающих общими признаками.

- Керамические изделия изготавливают из одного либо нескольких природных или техногенных неорганических неметаллических материалов.

- Производство керамики насчитывает многие тысячи лет.

- Уникальные свойства глин – пластичность и плохая водопроницаемость.

- Керамика делится на грубую и тонкую керамику.

- Хозяйственно-бытовая керамика включает разнообразные фарфоровые, фаянсовые, майоликовые, гончарные, тонкокерамические и другие изделия.

- Техническая керамика – это изделия электротехнического назначения.

- Изделия технической керамики должны обладать точными размерами.

- Сырье для производства керамики по происхождению можно подразделить на три группы: природное, искусственное и техногенное.

- Под строением понимают взаимное расположение различных структурных элементов керамики.

- Теплофизические свойства – теплоемкость, термическое расширение и теплопроводность.

- Для производства кирпича используют легкоплавкие глины и суглинки.

- Производство строительной керамики является важной отраслью народного хозяйства.

- Керамика является диэлектриком.

- Динас, шамотные и высокоглиноземистые изделия являются огнеупорами.

- Обычно различают макроструктуру и микроструктуру.

- Макроструктура также называется текстурой.

- К основным свойствам керамики относятся – прочность, упругие свойства, ползучесть, длительная прочность, теплофизические свойства (теплоемкость, термическое расширение, теплопроводность), термические свойства (термостойкость, испаряемость, старение керамики, огнеупорность), электрофизические свойства (электрическая проводимость, диэлектрическая проницаемость, диэлектрические потери, электрическая прочность).

Vocabulary

|  | pottery, ceramic | керамика |
| --- | --- | --- |
|  | fictile art | гончарное искусство |
|  | human crafts | человеческие ремесла |
|  | moldability | пластичность |
|  | water perviousness | водопроницаемость |
|  | forming or shaping of ware | формирование или формирование изделия |
|  | craft potteries | гончарное ремесло |
|  | oven tiles | печные изразцы |
|  | sanitary-engineering products | санитарно-технические изделия |
|  | faience | фаянс |
|  | expanded-clay aggregate | керамзит |
|  | agloporite | аглопорит |
|  | pumice | пемза |
|  | economic porcelain | хозяйственный фарфор |
|  | refractory products, fire-proof products | огнеупоры, огнеупорные материалы |
|  | fireclay | шамот |
|  | coarse-grained and finely-grained | грубозернистые и тонкозернистые |
|  | household porcelain | бытовой фарфор |
|  | fluxing agent, fusing agent | плавень |
|  | filling aggregates, nonplastics | отощающие материалы |

Task for ISW: Answer the questions

- What is ceramic?

- What is “ceramic” mean?

- What kind of ceramic do you know?

- What kind of raw materials do you know?

- What kind of coarse ceramic do you know?

- What kind of fine ceramic do you know?

- List types of household ceramic.

- What properties of ceramic do you know?

- What raw materials are used in brick production?

Practical work № 10

Technology of building ceramic: wall ceramic, façade ceramic, ceramic chemically resistant wares

The aim of work: translate scientific-technical literature

Duration of work: 1 hour

1. Compose the sentences with following words

- лицевой кирпич

- черепица

- изделие

- строительный

- фасадный

- кислотостойкий

- глина

- грубая керамика

2. Find the right variant

|  | Строительная керамика |  | Drain pipe |
| --- | --- | --- | --- |
|  | Стеновая керамика |  | Building tile |
|  | Фасадная керамика |  | Expanded clay |
|  | Кровельная керамика |  | Facing tile |
|  | Канализационная труба |  | Acid-resistant ware |
|  | Дренажная труба |  | Coarse-grained structure |
|  | Керамический камень |  | Facade ceramic |
|  | Лицевой кирпич |  | Roofing tile |
|  | Черепица |  | Cellular ware |
|  | Керамические заполнители |  | Coarse ceramic |
|  | Керамзит |  | Fusible clay |
|  | Аглопорит |  | Vitrifying clay |
|  | Санитарно-технические изделия |  | Fine-grained structure |
|  | Облицовочная плитка |  | Plastic forming |
|  | Плитки для полов |  | Building ceramic |
|  | Кислотоупорные изделия |  | Fragment |
|  | Пористые изделия |  | Semidry pressing |
|  | Грубозернистое строение |  | Ceramic filling aggregates |
|  | Грубая керамика |  | Flash drier |
|  | Тонкозернистое строение |  | Floor tiles |
|  | Черепок |  | Burnt clay |
|  | Легкоплавкие глины |  | Wall ceramic |
|  | Тугоплавкие глины |  | Refractory clay |
|  | Пластическое формование |  | Maturing of mass |
|  | Полусухое прессование |  | Roof ceramic |
|  | Туннельная печь |  | Sewer-pipe drain |
|  | Распылительная сушилка |  | Agloporite |
|  | Обожженная глина |  | Loam |
|  | Суглинки |  | Infusible clay |
|  | Огнеупорная глина |  | Burning of wares |
|  | Вылеживание массы |  | Face brick |
|  | Обжиг изделий |  | Tunnel furnace |
|  | Спекающиеся глины |  | Sanitary ware |

3. Translate the following sentences into Russian

1) Ceramic tile is used in applications such as flooring and walls.

2) Tile also is a very durable and hygienic construction product.

3) Clay brick is used to build homes and commercial buildings because of its strength, durability, and beauty.

4) Brick is the only building product that will not burn, melt, rot.

5) Coated clay tiles can cut the transfer of heat by up to 70%.

6) Tile roofing is very fire resistant and also very durable, withstanding harsh weather conditions like high winds, snow, hail and even earthquakes.

7) The problems of the heat resistance of wall ceramics made of low – melting clays of various mineralogical compositions has not received due attention in the technical literature, except for a few studies.

8) Сeramic tiles are produced by adding luminescent materials (pigment).

9) Ceramics can withstand higher temperatures than quartz.

10) Ceramic Tiles are now commonly used in the household for their long durability and attractive look.

- Complete the sentences

| ceramics | brittle | thermal shock | magnetic |
| --- | --- | --- | --- |
| the microstructure | creep | keramos | dielectric loss |
| ceramics | dielectric | factors | microcracks |

1. ………….. can be defined as solid compounds that are formed by the application of heat, and sometimes heat and pressure, comprising at least two elements provided one of them is a non-metal or a nonmetallic elemental solid.

2. The shape and size of the grains, together with the presence of porosity, second phases, etc., and their distribution describe what is termed …………...

3. As a class, ………… are hard, wear-resistant, brittle, prone to thermal shock, refractory, electrically and thermally insulative, intrinsically transparent. nonmagnetic, chemically stable, and oxidation-resistant.

4. The word ceramic is derived from …………., the Greekwork for potter’s clay or ware made from clay and ﬁred, and can simply be interpreted as ‘pottery’.

5. ………….. ceramics are ferrimagnetic and are classified according to their crystal structure into spinels, hexagonal ferrites, and garnets.

6. Ceramic ……… materials are typically used in electric circuits as either capacitors or insulators.

склеянный

7. The ……… is a measure of the energy dissipated in the dielectric in unit time when an electric field acts on it.

8. Generally speaking, thermal stresses are to be avoided since they can significantly weaken a component. In extreme cases, a part can spontaneously crumble during cooling. This kind of failure is known as ……… and occurs when thermal gradients and corresponding thermal stresses exceed the strength of the part.

9. ……… is the slow and continuous deformation of a solid with time that only occurs at higher temperatures, that is, T > 0,5Tm, where Tm is the melting point in Kelvins.

10. Despite the fact that ceramics are inherently………, a variety of approaches have been used to enhance their fracture toughness and resistance to fracture.

11. The effect of temperature on the strength of ceramics depends on many ……….

Task for ISW: Compose glossary about technology of ceramics

Practical work № 11

Technology of manufactured porous aggregate: expanded-clay aggregate and agloporite

The aim of work: translate scientific-technical literature

Duration of work: 1 hour

- Answer the questions

- What kind of wall ceramic do you know?

- What is brick?

- What is roofing?

- What is loam?

- What is fragment?

2.  Translate the following sentences into English

- Свойства пористой керамики зависят от минерального состава, пористости и строения.

- Важной физической характеристикой пористых материалов являются их проницаемость.

- Важнейшим показателем пористой керамики является общая пористость.

- Первым этапом процесса изготовления пористых керамических изделий является переработка и подготовка сырья.

- Керамзитом называют искусственный пористый зернистый материал ячеистого строения.

- Керамзит получают вспучиванием глинистых пород.

- Аглопорит получают в агломерационных машинах.

- Основными сырьевыми материалами для получения аглопорита являются глины и отходы от добычи, обогащения и сжигания углей.

3. Find the mistakes

Expended clay, acid-rezistant  ware, rofing tile, refrectory clay, bunt clay, agloporite, infuseble clay, fuseble clay.

Vocabulary

| porosity | пористость |
| --- | --- |
| penetrability | проницаемость |
| void structure | пористая структура |
| bursting expansion | вспучивание |
| thermal processing | термообработка |
| filling aggregate | заполнитель |
| interstices, pores | поры |
| additive agent, addition agent, additive compound | добавка |
| ceramics. | керамика |
| raw materials processing | переработка сырья |
| raw materials preparation o | подготовка сырья |
| cellular structure | ячеистое строение |
| sintering machines | агломерационные машины |

Task for ISW: Complete the sentences

| sinterability | preparation | fire resistance | crushing | mixing |
| --- | --- | --- | --- | --- |
| fluxing agent | plastic | nonplastics | durability | burning |

- When clay absorbs water, it becomes………….

- The ……………. in dried up condition is defined by quantity of strength at bend of the dried up samples.

- A……………. is the ability of clay withstand high temperatures without melting.

- …………….  is ability clay to turn in similar  on  stone  material under influence of heats with water absorption less than 5 %.

- ………………. enter into composition of mass for decrease in temperature of burning.

- ………………. decreased plasticity of mass and therefore, decrease shrinking of wares during drying and calcination as well as prevent deformations of the wares during drying and burning.

- ………….. of raw materials must ensure that every ingredients should have the set chemical-mineralogical composition, necessary degree of purity, physical condition and moisture required for further processing.

- Preliminary rough ………….  of hard lumps is mostly implemented in jaw crushers of cone-type crushers in ceramic production.

- ………… of ingredients must provide homogeneous mixture (of charge, mass) of a certain chemical-mineralogical composition.

- The ……….is the most important process of ceramic technology which turns the semi-prepared item into finished product.

Practical work № 12

Technology of refractories: alumina-silicate refractory (1h)

The aim of work: translate scientific-technical literature

Duration of work: 1 hour

1.  Choose the right variant and explain why

1) Fire resistance is called

А) ability of clay under influence of high temperatures to turn in stone similar body with waterability less than 5 %

Б) ability of clay to save plasticity at introduction in them not plastic materials and to provide sufficient mechanical durability of mould products after drying

В) reduction of the linear sizes and volumes of wares at drying owing to removal from mass of water chutting and rapproachement of firm particles of mass

Г) ability of clay to resist, not melting, influence of high temperatures

Д) ability of clay materials in the humidified condition to accept under influence of external forces any form without abruption and cracks and to save it after the stop of external influence

2) The temperature interval of service of fire-resistant products

А)

Б)

В)

Г)

Д)

- What basic oxides are present in composition of aluminosilicate refractory material

А)  and

Б)  and

В)   and

Г)  and

Д)   and

- Name the most widely widespread refractory material?

А) magnesite

Б) corundum

В) fire-clay

Г) dinase

Д) boxite

- By what basic properties differ light weight refractory, at the expense of high porosity?

А) chemical resistance

Б) electroisolated

В) moisture conductivity

Г) characteristics of durability

Д) thermally insulating

- The mineral kaolin on fire resistance concerns to materials?

А) refractory

Б) fire-resistant

В) free-melting

Г) thermoplastic

Д) with low fire resistance

3. True or false?

- Fusible clays are used in refractory production.

- Refractories are household ceramic.

- Alumina-silicate refractory is technical ceramic.

- Faience is refer to group of refractories.

- Fireclay is refractory clay or kaolin.

- Alumina ceramic is the most widespread kind of oxide ceramic.

4. Compose the sentences with following words

- alumina ceramic

- fireclay

- aluminium oxide

- mullite ceramics

- wollastonite

Vocabulary

| refractory material, refractory brick | огнеупор |
| --- | --- |
| silicates | силикаты |
| alumosilicates | алюмосиликаты |
| refractoriness, refractory property | огнеупорность |
| technical ceramics | техническая керамика |
| phase composition | фазовый состав |
| oxide ceramic | оксидная керамика |
| pyroscope | пироскоп |
| fire-clay | шамот, шамотный |
| moisture conductivity | влагопроводность |

Task for ISW: Compose essay about technology of refractory material

Practical work № 13

Technology of fine ceramic: household and  и artistic porcelain; electro technical porcelain; floor tile, façade tile, facing  glazed tile; ceramic granite tile; sanitary ware; stoneware, majolica

The aim of work: translate scientific-technical literature

Duration of work: 2 hour

      - The task: translate in Russian

Classification of thin ceramics

To thin ceramics concern dense sinter or fine-pored wares with homogeneous structure and, as a rule, covered thin glass-like a layer – glaze. Large majority of fine ceramic products of white color. Technology production of fine ceramic wares is characterized by increased requirements to quality and uniformity of raw material, a thin grinding and enrichment raw material, more complex processes of preparation and processing of weight, formation, and also careful furnish of a surface of products depending on technical requirements.

Porcelain, semiporcelain, faience, a majolica widely use for manufacturing sanitary products and facing of walls in buildings of various purpose. Acidproof and porous thin ceramics apply in various branches of the chemical industry.

Classification of products of thin ceramics:

- Sinter, dense, very firm with a brilliant break (porcelain, stone products, technical ceramics)

- Porous (partially sintered), less firm (semiporcelain and faience).

Porcelain there is technical (high-voltage, low-voltage, sanitary products, chemical utensils, heat resisting, etc. kinds), economic and art.

Stone products: acidproof for chemical and other industries; decorative and economic, art products.

Technical ceramics: steatitic and cordierite products of different purpose on the basis of pure oxides.

Semiporcelain: housewifely, technical, sanitary-building, sanitary-and-hygienic and medical.

Faience: feldspathic (housewifely utensils, a dignity. Products, facing tiles, decorative stones and a majolica); limy (housewifely dishware, majolica); facing products on the basis of use wollastonite, talc, etc. emaciated materials.

Production of porcelain

Porcelain usually name sinter white, appearing through in a thin layer, impenetrable for liquids and gases the pottery produced from thin mix kaolin, quartz, feldspar and plastic white-burning clay.

Use clays and kaolins in plastic, liquid and powdered porcelain weights provides their high forming properties of a semi-prepared item. The high maintenance in porcelain weight more smoothly (field spars, nephelinic syenite, etc.) Enables to receive at rather low, comprehensible in industrial temperatures (1250–1400оС) products with a lot glassy phases which properties basically and define advantages of different kinds of porcelain.

Porcelain as technical material possesses number of valuable properties – high mechanical and electric durability, chemical and thermal stability. Economic porcelain differs high translucence, hygienic, durability and other exclusive decorative data.

Distinguish "firm" and "soft" porcelain; the first contains more kaolin and less feldspar, them burn at higher t (1400 – 1450 оС), than weights for soft porcelain.

There is also a "bone" porcelain (40–50 % of bone ashes), but it concedes on durability feldspathic.

Production of faience.

Faience name the white porous products covered by colorless glaze.

Classification: economic; sanitary; facing; decorative

Glazing improves characteristics of faience. The temperature of burning of faience is 1250оС.

On structure faience happens: feldspathic, firm, limy and clay.

Faience differs from porcelain greater porosity, than and the basic technical properties of these products are defined. Porous faience hydro-also is gas-permeable, at absorption of liquids quickly becomes soiled and consequently without continuous covering glaze has no neither technical, nor household application.

Schemes of production.

In production of porcelain and faience products use mass of three types: plastic (doughy), liquid and powdered.

From plastic weights form porcelain, faience and rock-ceramic houseware, produce insulators, pipes, etc. products of technical purpose.

From liquid ceramic masses with the certain fluidity and filtering ability cast products in plaster moulds.

Powdered mass apply when method of formation is pressing, for example at development of facing tiles.

More often the wet way as it is less dust release is used, gives a greater maneuverability. Crushing gives a greater degree of dispersiveness.

Nonplastic materials                                            plastic materials

coarse crushing                                                  crushing

intermediate crushing                                      dissolution

wet milling

Mixing

sieving

magnetic separation

partial dehydration

knead (vacuumizing)

molding

Figure 1 –  Wet method of preparation of mass

Nonplastic materials                                          plastic materials

coarse crushing                                                   crushing

dry milling                                                          drying

separation                                                        dry milling

Mixing

Humidifying

Formation

Drying

bisque firing

porcelain enameling

glost firing

decoration

decorating firing

Figure 2 – Production fine ceramic wares in the dry way of preparation of mass

2. Answer the questions

- What is the expended clay?

- What is the agloporite?

- What is the drying in technology of ceramics?

- What is the firing in technology of ceramics?

3. Choose the right variant and explain why

1. The differs between faience and porcelain

А) Specific weight

Б) Gas impermeability

В) Large porosity

Г) High temperature of burn

Д) Heat conductivity

2. To thin ceramics are related to

А) Porcelain and faience wares, ceramic tiles

Б) Brick and ceramic stones

В) Porcelain and faience wares, expanded clay

Г) Tile, expanded clay, faience wares

Д) Ceramic tiles, acid-resistant brick, porcelain

3. For what purpose the porcelain wares are exposed to first burn?

А) For decrease of water absorption and heat resistance

Б) For increase of heat resistance and fire resistance of a ceramic wares

В) For decrease of porosity and water absorption

Г) For increase of plasticity and binding ability

Д) For increase of durability of wares before operation of  glazing or application the decor

4. Feldspar is entered in composition of porcelain mass as

А) Fire-resistant admixture

Б) Fluxing agent

В) Solid ingredient

Г) Abrasive material

Д) Mineralizer

5. The household porcelain wares refer to group

А) Building ceramics

Б) Wall ceramics

В)Acid-resistant ceramic

Г) Thin ceramics

Д) Art ceramics

6. The pressure filtering of slips by preparation of porcelain mass is carried out with the purpose:

А) Decrease of humidity

Б) Removals of soluble salts

В) Increase of humidity

Г) Decrease of plasticity

Д) Removals of large grain inclusions

4. Translate into English. Retell the text

Утельный обжиг при температуре 850-900 °С производят при изготовлении фарфоровой посуды. При этом получают полуфабрикат, не обладающий еще никакими признаками фарфора. Для фаянса первичный обжиг является основным. Данный обжиг формирует структуру и свойства. Максимальная температура может быть различной в зависимости от состава шихты и исходного сырья. Температура не превышает 1200-1250 °С. Вторичный (политой) обжиг применительно к фарфору является основным. В результате образуется плотноспекшаяся структура. При этом происходит также разлив глазури.

5. Complete the sentences using these words

Kaolin, white-burning, feldspar, quartz sand, ceramic, glaze, burning, household, porcelain, mass, clay, furnace, tunnel, wares.

Vocabulary

| white-burning | беложгущийся |
| --- | --- |
| household porcelain | хозяйственный фарфор |
| decorative porcelain | художественный фарфор |
| electrotechnical porcelain | электротехнический фарфор |
| insulator | изолятор |
| ceramic glaze | глазурь |
| ceramic granite tile | керамогранит |
| sanitary ware | санитарные изделия |
| sanitary porcelain | санитарно-технический фарфор |
| majolica | майолика |
| humidifying | увлажнение |
| knead | промин (проминать) |
| molding | формование |
| glaze | глазурь |
| bisquit firing | утельный обжиг, бисквитный обжиг |
| glost firing | политой обжиг |

Task for ISW: Translate into English

- Кроме керамических материалов студенты изучают цемент

- В соответствии с рабочим планом мы должны изучать «Химическую технологию керамики и огнеупоров»

- В отличие от цемента гипс имеет белый цвет

- С целью получения практических знаний,  мы проходим практику на заводах.

- Чтобы выступать на конференциях, студент должен заниматься научной работой

- Преподаватель заболел, поэтому студенты ушли рано.

- Вместе с алмазами, они нашли золото

- С другой стороны актуальной темой является производство цемента из нетрадиционных материалов.

- Он занимается исследованием цемента, однако его дипломная работа связана с керамикой.

- Чтобы определить какой это минерал, студенты должны определить его основные физические свойства.

Subject 5. Translation of technical-scientific literature in field of «Chemical technology of glass and glass-ceramics»

Practical work № 14

Properties of glasses, basis of glassmaking and of technology of glasswares

The aim of work: translate scientific-technical literature

Duration of work: 2 hour

      - The task: translate in Russian

Glassy state

Substances in solid state at usual temperature and pressure can have crystal or amorphous structure. In the nature crystal solid substances are most widespread, for structure which geometrically strict order an arrangement of particles (atoms, ions) in three-dimensional space is characteristic. The crystal condition is stable and is characterized by low internal energy, solid crystal substances have the precise geometrical forms, the certain melting temperature, etc.

Glass-like condition of substance represents an amorphous version of  solid condition (for inorganic substances; for organic substances – resinous condition).

Glass-like condition is metastable, i.e. is characterized by surplus of internal energy.

According to laws of chemical thermodynamics transition of substances from glassy state in crystal should to be carried out spontaneously, however high viscosity of solid substances not allow to pass spontaneously from glassy in a crystal state.

Types of raw materials.

All the raw materials applied to melting of glass, depending on their purpose can be classified on main and auxiliary.

To the main things raw carry materials by means of which into structure glass batch enter glasses necessary for a given kind acid and the basic oxides, glasses forming a basis and properties defining it.

Auxiliary materials contain compounds which are entered into glass for a variation of properties of glass and acceleration of its melting. The substances creating the regenerative or oxidizing environment in glass batchе concern to them, liquid melt and the surrounding oven atmosphere, accelerating processes glass formation and decolouration glass mass, and also painting has flown down. These are dyes, oxidizers, reducers and accelerators. Such classification of raw materials has, certainly, conditional character. Sometimes the same material carries out not one of the listed functions, and two or more. Raw materials as share on natural and (limestone, chalk-stone, dolomite, quartz, field spares, pegmatites, etc.) synthetic (soda, potash, dyes)

Glassmaking.

Thermal process as a result of which the mix of diverse components forms homogeneous liquid melt, are called glassmaking.

Loose or granulated batchу heat up in bathing or other furnaces therefore it turns in liquid glass mass, undergoing the complex physical and chemical interactions of components occuring during a significant temperature interval. For this reason it is impossible also for process of reception of glass to apply the term of "fusion" as components batch melt at various temperatures, form, finally, a special condition of substance liquid meltе – glass. This special condition of glass is emphasized, in particular, and that it does not have melting point – similarly to other compounds and simple substances, it has only « an interval of a softening ».

Distinguish five stages of glassmaking: silicate-formation, glass formation, clarification (decontamination), homogenization (averaging), chilling (cooling).

Silicate-formation. At this stage silicates and other intermediate compounds, arise liquid phase due to fusion eutectic mixes and salts are formed. Arisen in batchе silicates not reacted components together with a liquid phase form by the end of a stage dense fritted mass. For glasses of usual structure the first stage comes to the end at 650-11500С.

Glass formation. Formed at the first stage sinter with rise in temperature melt, reactions silicate-formation come to the end, there is a mutual dissolution of silicates. In liquid meltе silicates there is rather slow, gradual dissolution of superfluous quartz making the main maintenance of this stage. By the end of a stage appears transparent not homogeneous on structure liquid melt, including it is a lot of bleb. For usual glasses this stage comes to the end at 1200-12500С

      - Answer the questions

- What is the glass?

- What is the melt?

- What is the glass formation?

- What the accessorial raw materials are used in glass production?

3.  Choose the right variant and explain why

1) Oxide of aluminium Al2O3 is entered into composition of glass by the following component

А) Phosphate aluminium

Б) Veined quartz

В) Quartz sand

Г) Feldspar

Д) Aluminous cement

2) Viscosity of glass is defined

А) Strength

Б) Temperature

В) Composition

Г) Density

Д) Conductivity

3) The highest meaning of viscosity is characteristic

А) Crystal glass

Б) Silicate glass

В) Flat glass

Г) Quartz glass

Д) Red glass

4) What property is considerable at glass formation?

А) Creep

Б) Reciprocal viscosity

В) Viscosity

Г) Flowability

Д) Frangibility

5) Thermal process in consequence of homogeneous fusion is formed

А) Glass formation

Б) Glass melting

В) Silicate formation

Г) Silicate melting

Д) Glass forming

6) The important technological properties of glasses

А) Viscosity, crystallisation and boundary tension

Б) Frangibility, reciprocal viscosity and transparency

В) Viscosity, transparency and optical properties

Г) Chemical stability, durability and viscosity

Д) Viscosity, crystallisation and durability

- Translate into English.

1) Приготовление шихты – одна из важнейших технологических операций в производстве стекла.

2) Стекловарение - это термический процесс, в результате которого образуется однородная стекломасса.

3) Стекольная шихта содержит около 18 % газов.

4) Для производства стекол используют горшковые печи.

5) Отжиг стекла – дополнительная тепловая обработка.

6) Теплофизические свойства стекол – теплопроводность, теплоемкость, термостойкость.

7) К группе механических свойств стекол относятся плотность, твердость, хрупкость.

5. Find the mistakes: sinthering; glass bath; liqud melt; oxsides; silikate formaition; quarts glass; ckemical stability

6. Complete the sentences using these words:

- raw materials; apply, purpose, classify, auxiliary depending on, main, glass.

- substances; crystal; structure; usual temperature; have; amorphous; pressure; solid state.

Vocabulary

| glass | стекло |
| --- | --- |
| amorphous substance | аморфное вещество |
| liquid melt | расплав |
| glass formation | стеклообразование |
| glassmaking | стекловарение |
| viscosity | вязкость |
| glass mass | стекломасса |
| glass batch | шихта |
| burn-in, flashing | отжиг |
| vitrification, sintering | спекание |
| glass rolling | прокат |
| press forming | прессование |
| devitrification | кристаллизация стекла |
| auxiliary raw material | вспомогательные сырьевые материалы |
| colorant, coloring agent, dyes, pigment | красители |
| opacifier | глушители |
| refining agent | осветлители |
| fritted mass | спёкшаяся масса |

Task for ISW: Translate into English

- Важнейшими стадиями варки стекла являются силикатообразование, стеклообразование, дегазация (осветление), гомогенизация и студка стекломассы

- При  высоких температурах завершаются реакции силикатообразования, происходит взаимное растворение остатков кремнезема и силикатов

- Вторая стадия варки стекла – стеклообразование

- Стеклообразование протекает в 8-9 раз медленнее, чем силикатообразование

- Третья стадия варки стекла – осветление (дегазация)

- Четвертая стадия варки стекла называется гомогенизацией.

- Разделение варки стекла на отдельные этапы является условным.

- Формование стекла – основная и важнейшая после стекловарения технологическая стадия

Practical work № 15

Technology of plate glass

The aim of work: translate scientific-technical literature

Duration of work: 2 hour

- The task: translate in Russian

Methods of formation of glass

Existing versions of technological ways of formation of glass subdivide by character of external influence on glass-mass, to a kind of products made from glass and a principle of interaction glass masses with forming bodies and devices.

The basic most widespread ways of formation – stretching, rolling, float-method, pressing, blowing, press-blow forming.

In technology of plat glass production are used the following ways of formation: – stretching, rolling, float-method, pressing.

Stretching glass masses  is made continuously under action unilateral the directed stretching efforts created by the exhaust mechanism. The principle of the given method consists in gradual procrastination of a portion initial continuously replenishing and feeding process glass masses (bulbs) in a product of the set configuration (a sheet, a pipe, fibres). Distinguish vertical and horizontal stretching, and by the form unit of formation – debiteuse and nondebiteuse.

Vertical stretching formation: flat (or corrugated) sheet glass thickness from 0,8 up to 15 m, pipes thick-walled and tubes with Ø 2– 30 mm, fiber glasses.

In the horizontal method: flat sheet glass thickness 0,4– 20 mm, glass tubes with Ø 2– 50 mm

rolling glass masses it is made periodically or continuously under action (accordingly) one -or bilaterial) the efforts created rotating rolls.

The given method is very widely widespread at development of the "crude" sheet glass intended for the further grinding and polishing, and also in production for construction of the figured, reinforced or wavy sheet glass, profile glass and a tape of glass punched at hire with the purpose of reception of a carpet -mosaic tile and a facing film.

Float-method of formation of a tape of glass is carried out in the closed bath on a surface of the fused metal (tin) by free flowing glass masses (a bath merged in the beginning on a tray from the furnace) and movements on liquid meltу metal of a floating tape which thus, being gradually cooled and hardening, is continuously delayed from a bath by rotating rollers of the conveyor located from other end of a bath. For prevention of oxidation of tin in a bath at heats and damage of a surface of glass in a bath create the isolated inert environment (a mix of nitrogen with hydrogen).

Float-method allows to develop sheet glass in the big range of thickness – from 2 up to 30 mm with width of a tape up to 40000мм

Pressing glass masses concerns to cyclic methods of formation of piece products and is made for one reception in metal (usually pig-iron) form under action unilaterally the directed compressing efforts created by a punch at its movement from a drive press

Pressing is rather widespread, mechanized, as is a simple, reliable method of formation of various assortment of continuous (massive) or hollow products with precisely adjustable sizes: in diameter 10 -650 mm, in height 10350 mm, thickness 350 mm and weight 0,0215 kg. Building blocks, tiles, screens of kinescopes, insulators, utensils, empties concern to them, products lighting glasses (caps) and so on.

Production of  plate glass

To sheet types of glasses are the glasses developed in the form of flat sheets which thickness in relation to length and width is rather insignificant.

On method of production distinguish sheet glass: drawn glass received vertical stretching tapes of glass from glass masses; rolling developed by hire glass masses in a tape rolling; polished, produced by a method of thermal polishing.

On method of application sheet glass there are shares: window, polished, technical, safety glass  (including tempered, multilayered and reinforced).

The basic technological scheme of production of sheet glass has no essential differences from other types and includes following technological operations: preliminary preparation of components batch, preparation batch, melting of glass masses, formation of a tape of glass, burn-in tapes, additional processing (mechanical, chemical, etc.).

- Retell the text

The glass, produced in the form of flat sheets are referred to a sheet glass types. According to a method for producing flat glass are distinguished: drawn glass obtained by vertical drawing a glass ribbon from glass mass; rolled glass generated by rolling glass mass in glass ribbon and polished, producible by the method of thermal polishing.

According to the method of application flat glass is divided into window, polished, technical, safety glass.

Schematic flow sheet of flat glass comprises the following steps: preconditioning components of the charge, batch preparation, glass mass melting, forming the glass ribbon, flashing, additional processing (mechanical, chemical, etc.)

The glass mass melting for sheet glass production is carried out in glass furnaces.

- Find the mistakes

- The plate glass is use for biulding.

- The plate glass divided into window, glazing plate glas, teshnical, polished glass.

- The plate glasses are a glass in the form of flet glass with a smal thickness.

- The glass meltin is carried in glass-melting furnase.

- Translate the following sentences

- К важнейшим свойствам стекла можно отнести плотность, прочность, твердость, хрупкость, теплопроводность, термическую устойчивость, оптические свойства.

- Для строительства изготовляют следующие виды стекла: листовое, оконное, армированное, узорчатое и др.

- В строительстве используют исключительно силикатное стекло, основным компонентом которого является диоксид кремния (кремнезем).

- Кремнезем при охлаждении расплава способен образовывать стекло, как и некоторые другие оксиды; их называют стеклообразующими оксидами.

- Основным сырьем для изготовления стекла являются кварцевый песок, известняк, сода и сульфат натрия.

- Благодаря введению в шихту оксида кальция в виде известняка или доломита стекло становится нерастворимым в воде.

- Глинозем, вводимый в шихту в виде каолина и полевого шпата, повышает механическую прочность, а также термическую и химическую стойкость стекла.

- В специальные стекла, например, оптическое, лабораторное, вводят оксиды свинца, бария и цинка.

Vocabulary

| thermal stability | термическую устойчивость |
| --- | --- |
| optical properties | оптические свойства |
| plate glass | листовое стекло |
| window glass | оконное стекло |
| ferroglass | армированное стекло |
| figured glass | узорчатое стекло |
| silicate glass | силикатное стекло |
| debiteuse and nondebiteuse stretching | лодочное и безлодочное вытягивание |
| silicium dioxide | диоксид кремния |
| glass-forming oxide | стеклообразующие оксиды |
| insoluble | нерастворимый |
| plumbous oxide | оксид свинца |
| flashing | отжиг стекла |
| drawn glass | вытянутое стекло |

Task for ISW:  Choose the right variant and explain why

1. What is it the glassy state?

А) State of viscous flow

Б) Crystalline state

В) Amorphous variety of the solid state

Г) Brittle state

Д) Geometric strict order of the location of the particles

2. Indicate simple composition of glass?

А) Calcium silicate

Б) Magnesium oxide

В) Aluminium oxide

Г) Sodium silicate

Д) Silicon oxide

3. What wares get by vertical pulling?

А) Dishes, tubes

Б) Sheet glass, heavy-wall pipe

В) Container glass, rippled glass

Г) Insulators, sheet glass

Д) Fiberglass, blocks

4. What furnace is used in glassmaking?

А) Box furnace

Б) Rotary furnace

В) Tunnel furnace

Г) Bath furnace

Д) Shaft furnace

5. Raw materials for entering of silicon in sheet glass composition

А) Tripoli

Б) Rock crystal

В) Agate, jasper, firestone

Г) Quartz sands

Д) Opal, diatomite

Practical work № 16

Technology of hollow glass (1h)

The aim of work: translate scientific-technical literature

Duration of work: 1 hour

- The task: translate in Russian

Production of hollow glass

This group glasswares is united with presence of an internal cavity that defines specificity of a choice of structure of glass and a method of formation of a product though they are very various to destination and to scopes. This glass is container, high-quality, chemico-laboratory and medical.

Container glass Tare name the glass developed in the form of products of various capacity, intended for packaging, storages, transportations of various liquid, pastelike and solid products.

Classify glass container on the size of a forge, color of glass and purpose. It can be with internal diameter of a neck up to 30 mm (narrow-necked) and with above 30 mm (wide-mouthed). To the first, most widespread group narrow-necked container, bottles for flood and storages of food liquids concern; to the second – pharmaceutical utensils, to the third – utensils for perfumery production. Of glass container are made great demands enough and on mechanical durability, especially on resistance to internal hydrostatic pressure and squashing under loading, and also thermal stability.

For production of container glasses use traditional raw materials. By production semi-white and green glasswares usually apply unenriched sand, the maintenance of return fight reach 40 %. In batchу for the painted glasses in addition enter oxides manganese and chlorine

High-quality glass

To high-quality glass carry an extensive class glasswares, the developed and crystal, colorless and painted glasses. The assortment of products from high-quality glass is extremely various, there are: tableware, utensils for wine and drinks, art-decorative products.

Glass masses for high-quality glasses should be melting and clarified at the high temperatures, have well greater temperature area of formation (to be "long"), to possess ability to machining and to have high chemical and thermal stability. First of all these requirements concern to crystal lead-bearing glasses. Besides crystal glasses should possess a high parameter of refraction and raised light transmission.

Into compositions of color glasses enters various dyes as which apply oxides heavy metals (Со2О3, Мn2О3, Cr2O3 and оther), oxides rare-earth elements, and also compounds of gold, silver, copper, sulphurous compounds of zinc, cadmium and est.

Development of products of high-quality utensils is carried out as a method of manual blowing (a product on legs, vases of a complex configuration, souvenir products), and the mechanized methods.

Chemico-laboratory glass

From chemico-laboratory glass produce the products used in a laboratory practice, and also in various areas of the industry (chemical, food, etc.): chemical utensils, laboratory and industrial devices.

In conformity with purpose to chemico-laboratory glass show 3 basic requirements: high chemical stability in relation to various reagents; high thermal stability; ability to processing on a glass-blowing torch (it is low crystallization ability in a corresponding interval of temperatures).

- Find the right variant, complete the sentences and translate it

| The plate glass is | such as optical, laboratory is introduced oxides of lead, barium and zinc |
| --- | --- |
| Batch preparation is | chemical, container, household, laboratory, medical glass |
| Container glass is | divided into window, glazing plate glass, technical, polished glass |
| Wide-mouthed glass are used | quartz sand, feldspars, limestone, dolomite |
| Glassmaking is | glass for packing, keeping, transportation different liquid, pastelike and solid products |
| The raw materials for production glass are | for keeping liquid, semiliquid and solid product |
| In a special glass | the one of most important working operation in glass production |
| Uncleaned sand is used | the additional heat processing necessary for stress relieving in glass |
| The glass must be | in the manufacture of green glass wares |
| Burn-in of glass is | thermal process as a result of which the mix of diverse components forms homogeneous liquid melt |

Vocabulary

|  | internal cavity | внутренняя полость |
| --- | --- | --- |
|  | container glass | тарное стекло |
|  | narrow-necked | узкогорлый |
|  | wide-mouthed | широкогорлый |
|  | pharmaceutical utensils | фармацевтическая приборы |
|  | unenriched sand | необогащённый песок |
|  | high-quality glass | высококачественное стекло |
|  | batch preparation | приготовление шихты |

Task for ISW: Choose the right variant and explain why

1. Raw materials for entering of silicon in sheet glass composition

А) Tripoli

Б) Rock crystal

В) Agate, jasper, firestone

Г) Quartz sands

Д) Opal, diatomite

2. Indicate stages of glass melting

А) Silicate formation, melting, refinement, homogeneous

Б) Glass formation, refinement, homogeneous and hydration

В) Silicate formation, glass formation, refinement, homogenizing and chilling

Г) Homogeneous, vitrification, refinement, diffluence and chilling

Д) Torrefaction, melting, glass formation, c refinement and chilling

3. The requirements to glass container

А) Low mechanical durability, chemical stability, thermal stability

Б) High mechanical durability, chemical stability and electroconductivity

В) Chemical stability, thermal stability, water requirement

Г) Water absorption, surface of products should be smooth, without wrinkle-frees

Д) Sufficient mechanical durability, chemical stability, thermal stability

4. Pigment, opacifiers, refining agent, oxidants and desoxidants are

А) Primary materials

Б) Main materials

В) Basic materials

Г) Accessorial materials

Д) Processed materials

5. By method of application plate glass to divide

А) Chemical glass, polished glass, container glass

Б) Optical glass, art glass, wired glass

В) Container glass, polished glass, chemical glass

Г) Window glass, polished glass, wired glass

Д) Medical glass, optical glass, wired glass

Practical work № 17

Technology of building glass

The aim of work: translate scientific-technical literature

Duration of work: 1 hour

- The task: translate in Russian

Production of architecturally-building glass

Architecturally-building has flown down includes wide assortment of products various by the form and to purpose: special glass sheet, decorative glass; constructive building elements from glass (blocks, profile glass, double-glazed windows and so forth); facing glass (color carpet-mosaic tiles, stemalite, etc.); heat-and sound-proof materials (cellular glass, etc.). Depending on a kind of products the structure of glass, a mode of melting glass masses, methods of formation can essentially vary, etc.

The glasses passing ultra-violet beams (uviol), its possesses the raised transparency in ultra-violet biological area of a spectrum (at lengths of waves 380 – 240 nanometers). Them are made on the basis of quartz glass, and also silicate, borosilicate, the phosphatic glasses which are not containing impurity of compounds, absorbing Тх-beams (oxides iron, chrome, vanadium and др). These glasses are applied for glass fixing medical establishments, incubators, hotbeds, etc.

Heat-shielding glass possesses ability partially or completely to absorb or reflect thermal (infra-red) beams with length of a wave from 700 nanometers and more. Thus its remains transparent for apparent color. Produce it on the basis of industrial glass by colouring in bulk by oxide iron (0,4 – 1,5 %) or drawings on a surface oxides metal and nonmetallic film.

Glasses for sun-protection are reduced to a necessary level of receipt of thermal beams, a solar spectrum, possessing in too time high enough transmission visible visibility of a solar spectrum.

Glasses with translucent mirror coverings are one of the most demanded materials forming shape of modern city. Its are used both in internal partitions and when viewing premises from streets is undesirable.

Glazing plate glass represents colorless transparent sheet glass with smooth planes of greater sizes. Its are made in accord with traditional technology basically in the method of thermal polishing. Thickness of a plate glasses 6– 12 mm, The area of glass sheet 4– 12 м2, for it high values of mechanical durability are necessary. Its are applied for glass cover internal and external show-windows and apertures in shops, restaurants, the airports, etc.

Sheet decorative glass includes wide group of the products differing as on structure, and methods of additional processing of a glass sheet: color glasses, figured glasses, tone glasses and glasses with translucent mirror coverings.

- Translate the following sentences into Russian

1. Building glass, wares from the glass, glasses applied to a glass fixing of light apertures, facing and furnish of walls, ladders, other parts of buildings.

2. The heat- and sound insulation materials are relative to building glass (a foam glass and fibrous glass) and glass pipes

3. Building glass is divided into the sheet glass pane, polished, glazing plate glass, armored glass, figured, color and others.

4. Marblite is rolled opacified color building glass for facing of walls of internal premises of industrial and public buildings

5. Figured building glass has on the one hand a wavy surface, what intends for light dispersion

3. Find the right variant

| 1 | Container glass |  | Стеклообразование |
| --- | --- | --- | --- |
| 2 | Refining agent |  | Полое стекло |
| 3 | Glassmaking |  | Широкогорлый |
| 4 | Crucible furnace |  | Необогащённый песок |
| 5 | Isotropy |  | Сортовое стекло |
| 6 | Opacification |  | Хрупкость |
| 7 | Hollow glass |  | Осветлители |
| 8 | Accessorial raw materials |  | Вспомогательные сырьевые материалы |
| 9 | Household glass |  | Изотропность |
| 10 | Frangibility |  | Глушение стекла |
| 11 | Bath furnace |  | Стекольный бой |
| 12 | Wide-mouthed |  | Стекловарение |
| 13 | Glass formation |  | Тарное стекло |
| 14 | Uncleaned sand |  | Горшковые печи |
| 15 | Cullet |  | Ванная печь |

4. Compose the sentences with following phrase

- Optical properties of glass

- Mechanical properties

- Hardness

- Drawn glass

- Rolled glass

Vocabulary

| 1 | Architecturally-building glass | Архитектурно-строительное cтекло |
| --- | --- | --- |
| 2 | double-glazed windows | стеклопакет |
| 3 | mosaic tiles | мозаичная плитка |
| 4 | cellular glass | пеностекло |
| 5 | glass fixing | остекление |
| 6 | apparent color | видимый цвет |
| 7 | glazing plate glass | витринное стекло |
| 8 | translucent mirror | полупрозрачное зеркальное |
| 9 | thermal polishing | термическая полировка |
| 10 | figured glass | узорчатое стекло |
| 11 | fibrous glass, fibered glass | стекловата |
| 12 | glass pane, window glass | оконное стекло |
| 13 | armored glass | армированное стекло |
| 14 | opacified glass | глушеное стекло |
| 15 | wavy surface | рифлёная поверхность |

Task for ISW: Complete the sentences

| rolling | scheme | structure | container | accessorial |
| --- | --- | --- | --- | --- |
| compositions | glass-like | burn-in | fused | glassmaking |

- Substances in solid state at usual temperature and pressure can have crystal or amorphous ………...

- Thermal process as a result of which the mix of diverse components forms homogeneous liquid melt, are called …………...

- ………. condition of substance represents an amorphous version of solid condition.

- ……….. glass masses it is made periodically or continuously under action (accordingly) one -or bilaterial) the efforts created rotating rolls.

- Float-method of formation of a tape of glass is carried out in the closed bath on a surface of the ………… metal (tin).

- The basic technological ……….. of production of sheet glass has no essential differences from other types and includes following technological operations: preliminary preparation of components batch, preparation batch, melting glass masses, formation of a tape of glass, burn-in tapes, additional processing (mechanical, chemical, etc.)..

- Into …………….. of color glasses enters various dyes as which apply oxides heavy metals (Со2О3, Мn2О3, Cr2O3 and оther), oxides rare-earth elements, and also compounds of gold, silver, copper, sulphurous compounds of zinc, cadmium and est.

- ……….. of glass is the additional heat processing necessary for stress relieving in glass.

- …………… glass is glass for packing, keeping, transportation different liquid, pastelike and solid products.

- Pigment, opacifiers, refining agent, oxidants and desoxidants are ……………..materials.

Practical work № 18

Technology of glass-ceramics

The aim of work: translate scientific-technical text

Duration of work: 1 hour

- The task: translate in Russian

Theoretical bases of glass production

Polycrystalline glass name the artificial polycrystalline material received by crystallization of glass of the corresponding chemical compound and possessing higher in comparison with this glass physical and chemical properties. Glass-ceramics consist of set more or less fine crystals connected among themselves by an intercrystal layer.

Two conditions are necessary for transformation of glass into polycrystalline glass: first, glass should have the necessary chemical compound and, secondly, process of crystallization of such glass should be carried out on a special method. The first condition provides formation of such crystal phases (cordierite, spodumene, wollastonite, etc.) which define properties of glass-ceramics. The second condition concerns, basically, to a mode of thermal processing initial glass at its transformation into polycrystalline glass. Thermal processing allows to form germs of crystallization in glass and to provide their transformation into microcrystals with transition of glass in more or less crystallize a condition.

Glass-ceramics consist from crystal and residual glassy phases. The size of crystals, as a rule, less 1 microns, and their concentration can vary in significant limits (20-90 % on volume).

There is a number of the polycrystalline materials received by methods of ceramic technology, for example: mullite, dinas, magnesite, etc. These materials usually are received from ready crystal powders which during thermal processing conglomerate and recrystallize.

Glass-ceramics, as a rule, are received from liquid melts, stiffening in glassy form and capable at repeated heating to allocate the certain crystal phases. In some cases glass-ceramics are received by means of the powder method similar with applied in ceramics, however at reception glass-ceramics are applied not crystal, and glassy powders which at heating crystallize and conglomerate in a monolithic material of a polycrystalline structure.

Spontaneous crystallization is defined by the nature of glass, its aspiration to pass from metastable – an amorphous condition in steady crystal.

For realization of process of transformation of glass in glass-ceramics it is necessary to form all over again in glass the centers of crystallization, and then on these centers to grow up crystals of the greater or smaller size. The centers of crystallization can arise spontaneously or to appear as a result of entering extraneous particles from the outside. The first mechanism has received the name homogeneous, the second – heterogeneous nucleation. Germs name: the center of crystallization, a kernel, a priming and so forth

To explain process nucleation on the heterogeneous mechanism it is simple – the alien particle is brought from the outside and becomes a germ during crystallization of glass.

- Translate the following sentences into English

  - Ситаллом называют искусственный поликристаллический материал, полученный кристаллизацией стекла.

  - Ситаллы состоят из множества более или менее мелких кристаллов.

  - Ситаллы состоят из кристаллической и остаточной стекловидной фаз.

  - Ситаллы получают из расплавов.

  - Катализаторами в технологии ситаллов называют вещества, инициирующие процесс зарождения центров кристаллизации.

  - Катализатор кристаллизации стекла выступает в роли ускорителя и в роли участника процесса.

  - Технические ситаллы отличаются плотной и развитой кристаллической структурой.

  - Для производства шлакоситаллов варят шихту, состоящую из доменного шлака, кварцевого песка, глины, сульфата натрия и катализаторов кристаллизации.

  - Для производства ситаллов используют технологию стекольного производства.

  - Варка стекломассы при производстве ситаллов осуществляется в различных стекловаренных печах.

  - Для получения ситаллов необходимо выбрать соответствующий состав стекла.

  - Оптимальная термическая обработка является самым важным элементом технологии ситаллов.

  - Температура варки стекломассы и длительность зависят от состава стекла.

  - Для обеспечения высокой степени гомогенности стекла при необходимости применяют различные приемы перемешивания.

Vocabulary

| 1 | glass-ceramics | ситаллы |
| --- | --- | --- |
| 2 | crystallization of glass | кристаллизация стекла |
| 3 | intercrystal layer | межкристаллическая прослойка |
| 4 | germs of crystallization | зародыши кристаллизации |
| 5 | residual glassy phase | остаточная стекловидная фаза |
| 6 | monolithic material | монолитный материал |
| 7 | extraneous particles | посторонние частицы |
| 8 | heterogeneous nucleation | гетерогенное зародышеобразование |
| 9 | kernel | ядро |
| 10 | a priming | затравка |

Task for ISW: Choose the right variant and explain why

1. The methods of glass-ceramics forming

А) Drawing, blowing, pressing

Б) Plastic forming, dry-pressing, stone casting

В) Slip casting, modeling, drawing

Г) Blowing, stone casting, slip casting

Д) Pressing, plastic forming, modeling

2. What is difference between glas-ceramics and glasses?

А) formation methods

Б) amorphous condition and chemical composition

В) crystal structure

Г) modes of burn of glass

Д) lower physical and chemical properties

3. The sizes of crystals in sytalls:

А) from 3 to 7 microns

Б) more than 1 microns

В) from 1 to 5 microns

Г) less than 1 microns

Д) more than 0,8 microns

4. At thermal processing into glass ceramic are formed minerals of

А) Trydimite and cristobolite

Б) Mullite and quartz

В) Alite and cordierite

Г) Belite and mullite

Д) Trydimite and alite

5. Catalysts in technology sytalls are named:

А) substances accelerating process of melting sytalls

Б) substances accelerating crystallisation reaction

В) substances accelerating homogenization reaction

Г) substances initiating process of opacification of glasses

Д) substances initiating process of nucleation of the centres of crystallisation

6. For flashing large-sized sytalls it is necessary to observe:

А) fast refrigerating conditions

Б) slow refrigerating conditions

В) slow heating of wares

Г) fast heating of wares

Д) slow temperature rise

7. Duration stage  burn-in of glass depends on:

А) composition of glass

Б) temperature of  burn-in

В) method of  burn-in

Г)  thicknesses of ware

Д) time of burn-in

Subject 6. Translation of technical-scientific literature in field of «Technology of technical crystals and precious jewel stones

Practical work № 19

Precious jewel stones

The aim of work: translate scientific-technical literature

Duration of work: 1 hour

- The task: translate in Russian and retell

The term "precious stones" can be used heavenly wide.

Considered a precious stone, that is, has a certain value, if it has a number of attributes: beauty, durability, rarity, traditional use and compact.

The science of gems divides them into two types: inorganic and organic origin.

Inorganic: strong mineral of natural origin with a constant chemical structure. Most gemstones are inorganic, but of the thousands of minerals extracted from the depths of our planet, only about twenty were awarded the title "jewel" - for their rarity, beauty, durability and strength.

DIAMOND - a mineral, native element, sometimes it forms aggregates and aggregates, among which are distinguished: the board, the ballas, carbonado. Usually colorless or pale colored in shades of yellow, brown, gray, green, pink, rarely black. Diamond - the hardest of natural materials. Mining: India, Brazil, South Africa. In subsequent years, diamonds have been found in South-West Africa, today Namibia, the Congo Basin and Taganike, current Tanzania, but also - in Venezuela, on the island of Borneo and in British Guiana.

RUBIN - transparent, gem-quality corundum bright red, dark red or purple-red color, color creates an admixture of chromium resistant. Rubies mined from alluvial deposits formed during the destruction rubin-bearing magnesian skarns (Burma) and plagioclasites (Tanzania). Rubin is now synthesized in large scale.

SAPPHIRE. The raw material for sapphire is corundum - colorless aluminum oxide. High quality sapphires are mined in Burma (Myanmar), Thailand and Tanzania, and dark blue stones with a metallic sheen found in Montana (USA).

EMERALD is a type of beryl - silicate of aluminum and beryllium. His emerald green color due to ions of chromium. Most of the known deposits of emeralds were in the area of Upper Egypt, near the Red Sea, found in South America. One of the most known deposits were found in the mountain Zabara.

2.Translate the following sentences into English

- Топаз кристаллизуется в ромбической сингонии и имеет идеальную для драгоценного камня твердость

- Существует множество химических форм граната.

- Цвет граната зависит от элементов, попавших в его кристаллическую решетку в процессе формирования

- Камни, образование которых связано с жизнедеятельностью организма, называются органическими

- Характерные свойства органических камней: невысокая твердость, химическая нестойкость, иногда способность гореть.

- К органическим камням, имеющим ювелирное значение, относятся: жемчуг, янтарь, коралл, гагат.

- Жемчуг представляет собой твердые образования карбоната кальция.

- Янтарь — окаменелая ископаемая смола хвойных деревьев.

- Гагат– органогенный камень, являющийся плотной разновидностью каменного (бурого) угля.

- Коралл - это внешний скелет крошечных морских организмов коралловых полипов, состоящий из карбоната кальция, окиси железа и органического вещества

Vocabulary

| 1 | jewel stones, gemstones, precious stones | драгоценные камни |
| --- | --- | --- |
| 2 | board | борт |
| 3 | ballas | баллас |
| 4 | carbonado | карбонадо |
| 5 | mining | добыча |
| 6 | gem-quality | ювелирное качество |
| 7 | alluvial deposits (placer) | россыпи |
| 8 | emerald | изумруд |
| 9 | garnet | гранат |
| 10 | pearls | жемчуг |
| 11 | amber | янтарь |
| 12 | jet, gagate | гагат |

Task for ISW: Compose the sentences with following phrase

- optical properties of

- strong pleochroism

- precious jewel stones

- microcrystalline variety

- technical crystals

Practical work № 20

Synthesis of technical crystals

The aim of work: translate scientific-technical literature

Duration of work: 1 hour

1.The task: translate in Russian

Synthetic Crystal (also, man-made crystal) is any of the crystals grown artificially either in the laboratory or in industry. Of the total number of synthetic crystals, approximately 10,000 are inorganic substances, and some of these do not occur in nature. Organic synthetic crystals, however, are far more numerous, numbering in the hundreds of thousands; these crystals are of various compositions and, in general, do not occur in nature. On the other hand, of the 3,000 crystals that make up the variety of natural minerals, it has been possible to grow only a few hundred, of which only 20–30 are of practical importance (see Table 1). This low number is explained by the complexity of the crystallization processes and the technical difficulties involved in precise maintenance of the conditions necessary for the growth of single crystals.

The first attempts to synthesize crystals were made in the 16th and 17th centuries; they consisted of the recrystallization of water-soluble crystalline substances encountered in crystalline form in nature (sulfates, halides). Later, knowledge of the composition of natural minerals brought attempts to synthesize minerals from powders using roasting techniques. The first small synthetic crystals were obtained by this method. In the early 20th century, E. S. Fedorov and G. V. Vul’f studied the synthesis of crystals, investigated the conditions of crystallization of water-soluble compounds, and improved the crystallization apparatus. Subsequently, A. V. Shubnikov worked out general principles for the formation of crystals from aqueous solutions (seignette salt, potassium dihydrogen phosphate) and melts (single-component and multicomponent systems). Under his direction, the first factory for the synthesis of crystals was set up.

Synthetic crystals of quartz are obtained under hydrothermal conditions. Small crystals (seeds) of various crystallographic directions are cut from natural quartz crystals. Although quartz is very common in nature, supply does not meet the demands of technology. Furthermore, natural quartz contains many impurities. Synthetic crystals of quartz of up to 15 kg are grown in autoclaves over a period of many months; the growth period for high-purity crystals (large flawless quartz crystals used in optical devices) can reach several years.

Synthetic diamond crystals were obtained in the 1950’s from graphite powder mixed with Ni. The mixture was pressed into small (2–3 cm) disks, which were then heated to 2000°-3000°C at pressures of 100,000–200,000 atmospheres. Under these conditions, graphite is converted into diamond. The size of synthetic crystals of diamond is of the order of tenths of a millimeter, although under special conditions it is possible to obtain crystals of up to 2–3 mm. The diamond industry in the USSR was established mainly to meet the requirements of drilling technology. Synthetic crystals of diamond able to compete with the natural diamonds used in jewelry have so far been obtained in only small quantities.

Synthetic crystals of iron garnets and emeralds are grown under laboratory conditions from solutions of the melts. However, these methods have not yet been developed industrially. Studies are currently under way on the industrial production of synthetic gemstones from yttrium aluminum garnets (garnetites) and zirconium and hafnium dioxides (flanites). These synthetic crystals have a wide range of colors and resemble emeralds, topazes, and diamonds because of their high light refraction.

Vocabulary

| 1 | attempts to synthesize crystals | попытки синтеза кристаллов |
| --- | --- | --- |
| 2 | the growth of single crystals | рост монокристаллов |
| 3 | recrystallization | перекристаллизация |
| 4 | roasting techniques | техника обжига |
| 5 | water-soluble compounds | водорастворимые соединения |
| 6 | seignette salt | сегнетова соль |
| 7 | autoclaves | автоклавы, пропарочные котлы |
| 8 | large flawless quartz crystals | большие безупречные кристаллы кварца |
| 9 | yttrium aluminum garnets | алюминиево-иттриевый гранат |
| 10 | garnetite | гранатит |

Task for ISW: Compose the sentences with following phrase

- synthetic crystals

- high light refraction

- organic synthetic crystals

- high-purity crystals

- technical crystals

Literature

- Ковчур С.Г. и др. Англо-русский словарь по химии и технологии силикатов. –М.: Издательство «Русский язык», 1986. -293с.

- Yessimov B.O., Adyrbayeva T.A., Dubinina H.S. Crystallography and mineralogy. Course of lectures for students of specialties 5V072000 – Chemical technology of inorganic substances, 5V075300 - Chemical technology of infusible nonmetallic and silicate materials. –Shymkent: M.Auezov SKSU Publishing center, 2012. -277р.

- Макеева М.Н. и др. Технический перевод в повседневной жизни. Учебное пособие. –Тамбов: Издательско-полиграфический центр Тамбовского государственного технического университета, 2004. -160с.

- Yessimov B.O., Adyrbaeva T.A., Dubinina E.S., Kurbanbaev M.E., Musaev R.A. Crystallography and mineralogy (Part 1. Geometric crystallography. Physical and chemical properties of crystals). Учебное пособие. Шымкент: ЮКГУ, 2008. -60с.

- Yessimov B.O., Adyrbaeva T.A., Dubinina E.S., Kurbanbaev M.E., Musaev R.A. Crystallography and mineralogy (Part 2. Mineralogy). Учебное пособие. Шымкент: ЮКГУ, 2008. -130с.

- Рябцева Н.К. Научная речь на английском языке. Руководство по научному изложению. Словарь оборотов и сочетаемости общенаучной лексики: Новый словарь-справочник активного типа (на английском языке). –М.: Флинта: Наука, 1999. -600с.

Dubinina E.S., Dzhumabayeva G.M.

Methodical instructions for practical classes of discipline

«PROFESSIONALLY-ORIENTED FOREIGN LANGUAGE»

It is signed in a press 25.06.2014

Format of a paper 60×84

Paper typographical. A press offset. Volume 1,5 п.л.

Circulation 20 copy the Order 3188

The edition of the M.Auezov South-Kazakhstan state university.

Publishing center ЮКГУ M.Auezova, Shymkent, пр. Тауке-khan, 5