F.7.03-03

Jumabayeva G.M., Kulmakhanova A.Sh.

METHODICAL INSTRUCTIONS

for laboratory work discipline

«Chemistry of silicate materials»

Shymkent, 2018

MINISTRY OF EDUCATION AND SCIENCE OF THE REPUBLIC OF KAZAKHSTAN

M.Auezov South Kazakhstan State University

High school «Chemical Engineering and Biotechnology»

Chair «Technology of cement, ceramics and glass»

Jumabayeva G.M., Kulmakhanova A.Sh.

METHODICAL INSTRUCTIONS

for laboratory work discipline

«Chemistry of silicate materials»

for students of specialty 5B075300 "Chemical technology of infusible nonmetallic and silicate materials"

Shymkent, 2018

UDC

Authors: Jumabayeva G. M., Kulmakhanova A.Sh.

Methodical instructions for laboratory work  discipline «Chemistry of silicate materials» for students of specialty  5B075300- "Chemical technology of infusible nonmetallic and silicate materials" – Shymkent: M.Auezov  SKSU, 2018.-60 р.

Methodical instructions  are made in accordance with the requirements of the curriculum and program of discipline "Chemistry of silicate materials" and includes all the necessary information for the implementation of the laboratory classes of the course.

The methodical provides and objective; recommendations to students for preparation for classes; theme of laboratory works; a brief theoretical information, reagents, equipment, instruments and technical means; the progress and processing of the obtained results; the order of registration of reports and their protection; control issues; safety rules; list of recommended literature.

Reviewers:Dubinina E. S. Candidate of Technical Sciences, Associate Professor Chair «Technology of cement, ceramics and glass»

Considered and recommended to the printing by the meeting of the Chair «Technology of cement, ceramics and glass» (minutes № __ from date «__»___ 2018), Methodical committee on the innovative technologies of training and methodological support of high school «Chemical Engineering and Biotechnology», (minutes №__ from date «__» ____ 2018).

It is recommended for the publication of methodical advice of M.Auezov SKSU (minutes №__ from date «__»  ____2018).

© M.Auezov South Kazakhstan State University

Responsible for issue  Kulmakhanova A.Sh.

CONTENT

|  |  | page |
| --- | --- | --- |
|  | Introduction | 6 |
|  | The criteria for the evaluation of students in laboratory work | 9 |
| 1 | Analysis of raw materials for production of silicate materials | 10 |
| 2 | Determination of density and volume mass of the material | 15 |
| 3 | Determination of moisture and fineness of grinding material | 22 |
| 4 | Determination of ductility and conduct ability of clay raw materials | 27 |
| 5 | Determination of charge composition of glass: control of glass charge | 32 |
| 6 | Laboratory glass melting | 39 |
| 7 | Determination of the properties of air building lime | 43 |
| 8 | Determination of the normal thicness and timing of setting binders materials | 51 |
| 9 | Determination of air, fire and general shrinkage of ceramic products | 56 |

Introduction

To obtain high-quality building materials and binders, to reduce energy consumption and improve resources seregenti technological processes of producing inorganic binders it is necessary to study the regularities of chemistry of building materials and binders.

In the discipline "Chemistry of silicate materials" considered the applied aspects of chemistry, solid dispersions (limestone, clay, ceramics, dry mortar, cement); the principles and fundamental laws and regulations of the chemistry of building materials and binders. The regularities of the interaction of disperse systems are examined in the sections on electro-kinetic and structural-mechanical phenomena. Discusses the stability and rheological properties of the construction dispersions and binders

The discipline "Chemistry of silicate materials" is a required component of the disciplines of bachelor of 5В075300 specialty – "Chemical technology of infusible nonmetallic and silicate materials".

The course content aims to study the current state and prospects of development of the chemistry of construction materials in Kazakhstan and abroad. The study of the problems facing the chemistry of silicate materials and ways of their solution.

The purpose of studying of discipline "Chemistry of silicate materials" consists in the formation of bachelors skills describe the physical and chemical processes; the ability to explain the nature of the processes occurring during the production of construction materials; skills of planning and organization of technological processes.

The main tasks of the discipline include the use of acquired in the process of studying knowledge, to solve ecological and economic problems facing the silicate industry specifically for each company.

Development and retrofitting of enterprises with modern silicate products, allowed us to repurpose existing production of the latest high quality materials which have long enjoyed huge demand in the market. The production of silicate materials was developed thanks to tax incentives for activities of enterprises, mechanisms for providing long-term Finance, the ability to attract foreign investment, and most importantly - the creation of a modern, civilized construction market.

Kazakhstan is rich in natural opportunities for the development of asbestos-processing, ceramic, porcelain, clay, cement, building industry, and the development of the production of lime, paints and insulating materials.

Chemistry of silicates

Chemistry of silicates – a section of physical chemistry that involves the study of the physical and chemical building, structure, composition, and chemical properties of substances based on silicon, combined with oxygen and other elements 90% component of the earth's crust. The main objective of this science is the study of substances most common in nature and, accordingly — in practice. Last predefines the following survey: or a work based on the study of silicate analogs of various minerals, either absolutely new substances, according to the different qualities superior to any existing in nature — the creation of such important materials as cement, ceramics, glass, refractories, enamels, coatings, dyes, used in construction, metallurgy, chemical, optical, radio and electrical, aviation, medical, aerospace and other industries.

In nature, silicates are presented in the form of minerals, comprise the majority of rocks that form the main part of the crust. Chemistry of silicates conducts basic research for a broad class of chemical compounds.

Silicates

Silicates, salts of silicic acid. The role of cations in silicates play mostly. elements of the 2nd, 3rd and 4th the periodic system. In nature is widely represented in the form of minerals, part of most rocks, composing the bulk of the earth's crust (75% of its total mass), upper and lower mantle. The main minerals of the crust-polevo spotovyj aluminosilicates (55%, see feldspar), of various classes of ortho, meta and dimethacrylate (15%), quartz (12%, see Silicon dioxide), mica (3%). Silicates make up the minefield. Foundation soil: quartz sand, primary and metamorphosed shales, clay, etc. sedimentary rocks. Meet in the lunar soil - clinopyroxene basalts, Nickel-iron and stone meteorites-olivines, pyroxenes, plagioclases, quartz, etc.

The Si atoms in silica oxide anions isomorphically substituted (see below) atoms Al, B, Be etc., in accordance with what distinguish alumino-, Boro and other silicates.

Silicate industry

Silicate industry is the production of ceramics, glass, cement from natural compounds of silicon.

Silicon is a leading modern semiconductor material, which is widely used in electronics, electrical for manufacturing integrated circuits, diodes, transistors, photocells, etc. Technical silicon – alloying component (alloying element increases the strength, corrosion durability of steel, reduce the danger of brittle fracture) in the production of steel (e.g., transformer steel) and nonferrous metallurgy (silicon bronze).

Ceramics

Brick, tile, earthenware, crockery — all ceramics. Raw material for the production of pottery are clay and mineral supplements. Clay consists of the mineral kaolinite (Al2O3*2SiO2*2H2O). The process is as follows:

- Preparation of raw materials

- Forming

- Drying

- Firing

Preparing raw clay is mixed with water (it turns a pasty), then, given form, and in the end the product is dried and fired (after that the product becomes solid).

Ceramic production developed in three areas: building ceramics, ceramics for home, technical ceramics.

Glass

The composition of ordinary window glass is usually expressed by the formula Na2O*CaO*6SiO2. Glass is obtained by sintering a pure silica sand, soda ash and limestone in special furnaces(at t 1500oC):

SiO2 + Na2CO3 = Na2SiO3 + CO2↑

SiO2 + CaCO3 = CaSiO3 + CO2↑ Window glass

Na2SiO3 + CaSiO3 + 4SiO2 = Na2O*CaO*6SiO2

Cement

Raw materials for cement production are clay and limestone. When sintering the decomposition of limestone and the formation of silicates and aluminum alloy. The main chemical process in cement production - sintering at t = 1200 - 1300 оС   of a mixture of clay with limestone, leading to the formation of silicates and aluminates of calcium:

Al2O3 * 2SiO2 * 2H2O = Al2O3 * 2SiO2 + 2H2 O

CaCO3 = CaO + CO2

CaO + SiO2 = CaSiO3

3CaO + Al2O3 = 3CaO * Al2O3

Properties

Materials and products should have good characteristics and qualities.

A property is a characteristic of the material, manifested in the process of its handling, application or use.

Quality — the totality of material properties that lead to its ability to satisfy certain requirements in accordance with its purpose.

Properties of building materials and products to qualify into four main groups: physical, mechanical, chemical, technological, etc.

To chemical include the ability of materials to resist the action of chemically aggressive environment, causing them metabolic reactions leading to the destruction of the materials change their original properties: solubility, corrosion resistance, resistance to rotting, hardening.

Physical properties: the average, apparent, true and relative density; porosity, humidity, water-yielding capacity, thermal conductivity.

Mechanical properties: ultimate strength in compression, tension, bending, shear, elasticity, plasticity, stiffness, hardness.

Technological properties: workability, heat resistance, melting, speed of solidification and drying.

The criteria for the evaluation of students in laboratory work

Knowledge, skills and competencies of students at all types of control are determined by estimates score-rating letter system, which are directly proportional to the ratio.

The rating of "excellent" correspond to the grades A, having the digital equivalent of 4.0, and the percentage of 95-100% and A-having the digital equivalent of 3.67 and the percentage of 90-94%.

This assessment is placed in the case if student showed full assimilation of the program material and did not allow any errors, inaccuracies, timely and properly completed in class, showed thus original thinking, is timely and without any mistakes handed in all assignments, completed homework, independently used additional scientific literature when studying discipline, was able to independently be systematized program material.

The "good" match rating B+ having a digital equivalent of 3.33 and the percentage of 85-89%, In having the digital equivalent of 30 and the percentage of 80-84% and having the digital equivalent of 2.67 percent and content of 75-79%.

This assessment is placed in the case, if the student has mastered the program material is not lower than 75% and not made serious mistakes in the answer, in a timely manner completed all assignments and turned them without basic remarks, correctly executed and promptly passed homework without basic remarks, used additional literature according to instructions of the teacher, made unprincipled inaccuracies or fundamental errors corrected by the student, managed to organize the program material with the help of a teacher.

The rating "satisfactory" match rating C+ having a digital equivalent of 2.33 and the percentage of 70-74%, C, having the digital equivalent of 2.0 and the percentage of 65-69%, C-having a digital equivalent of 1.67 and the percentage of 60-64 %, D + with the digital equivalent of 1.33 and the percentage of 55 - 59% D with the equivalent of 1.0 and the percentage of 50-54%,

This assessment is placed in the case, if the student has mastered the program material is not less than 50%, when performing control and laboratory work, homework needed help teachers, upon delivery of the

The rating "unsatisfactory" rating corresponds to ), having a digital equivalent of 0 and percentage of 0-49%. This assessment is put in case the student found gaps in knowledge of the basic material provided by the program, not mastered more than half of the program discipline, the responses made fundamental errors, did not fulfill specific tasks stipulated forms of current, intermediate and final control, has not worked for all the basic literature provided by the program.

Laboratory work №1

Theme lessons: Analysis of raw materials for production of silicate materials

The purpose of lessons:

1. The macroscopic study and description of clay raw materials;

2. Determination of content of coarse inclusions.

Running time of work – 1 hours

Brief theoretical information

Macroscopic characterization is based on the gross examination of a sample of clay with a magnifying glass (visual) or with the naked eye. Thus note the following information:

Color (dry and moist), structure, texture. the presence of limestone and its distribution (boiling 10% HCl). the content of other impurities (mica, quartz, gypsum,pyrite and organic inclusions).

Color. The color of the clays is varied and changes depending on the mineral composition of the main mass of clay. Impurities series of compounds even in small quantities causes a change in the primary color of clay. Coloring are finely dispersed hydroxides and iron oxides, organic matter and less oxides of titanium and manganese. Hydroxides and oxides of iron stained clay in various shades of yellow, red and purple oxides, titanium - gray, manganese black and brown. Often there are heterogeneous clay color mottled due to uneven distribution in mass clay coloured components.

Structure and texture

The nature of the structure part (grains) mineral rocks are called structure and their mutual arrangement texture.

According to the structure distinguish clay fine-disperse, coarse, distressing, and various-grained sand.

Fine-grained clay, which consist mostly of particles less than 0.001 mm when the rolling of the mass as the molding moisture give solid long cords with a thickness of less than 0.5 cm. When rolling the damp clay in the hands of individual particles it does not oxosalts, and when cut with a knife not hear a characteristic crunch and on the site of the incision smooth surface. When considering a magnifying glass clay is a homogeneous mass: a flake or fracture very smooth, for compacted clays.

Coarse clay with the rolling give a more fine-grained cords.When you wet clay in the hands, and when cut with a knife sensitivity the impurity particles larger than clay (clay say that "crunches"). A magnifying glass sometimes shows rare small grains of mineral impurities, kink breed - rough.

Aleurolite clay when rolling the moist give you a short cord. When cutting with a knife clay much crunches. A magnifying glass shows individual large particles of minerals that can be easily separated, if slightly to clean up the clay, removing the clay and silt particles. The fracture of rocks rugged.

Sandy clay with the rolling even more short and thick, quickly tearing the cords. Sharply felt the presence of particles of more than 0.01 mm. the fracture of rocks uneven, grainy.

The texture of shale is divided into three main types:

- Random (undirected) - lumpy and dense.

For erratic texture particles are without any orientation. This texture is typical for the coarse and less fine-grained rocks. It can be loose, lumpy, etc.

- Micrologica (oriented).

When wet layered texture of the particles are oriented as if in layers. The nature and arrangement of layers are distinguished texture horizontally layered, lisowice-layered and complex, determined by the combination of the first three varieties of layered textures.

- Fluidized (tangled) - type slate.

Fluid texture is not widely practiced and is the result of a secondary violation of the layered texture.

Equipment, tools and technical means:

- Oilcloth (steel, plywood sheet or a sheet of heavy paper)

- Wooden hammer ("mallet")

3.Cup for the preparation of clay dough

- Knife

- Technical laboratory scales with weights

- Drying oven with thermostatic control, ensuring the heating temperature up to 105-110 °C (lamp light or infrared radiation an output of 500 watts with internal specular reflector)

- The desiccator

- Cup for evaporation

- A set of sieves with meshes № 0,5; 1: 2; 3; 4; 5.

- Capacity for soaking clay

- Measuring length of at least 100 mm

- Binocular magnifier.

- Microscope MIN-8, or MIN-10

- Hydrochloric acid by the GOST 3118-77. diluted 1:10

- Wooden paddle for stirring the suspension

- Lens graduated

The order of performance of works in the audience:

Make the inspection of test samples with the naked eye or with a magnifying glass. When you do this, pay attention to the color and shade in a dry condition and texture. Then the clay is spread a thin layer on the area of 1 m2, large clods break with a wooden hammer (mallet) to pieces no larger than 2-3 cm and the clay is divided by two diagonals into four equal triangles. Select a sample of two opposite triangles, thoroughly mixed, spread in a thin layer and re-divide the diagonals into 4 triangles. Operation be repeated several times to obtain average samples of the raw materials in the quantity required for research. The remaining clay is also considered to be average.

To define the structure of composite samples of clay raw materials (100-200g) preparing a mass of molding moisture content, rolled out the cords, cut with a knife - the cut (break) viewed through a magnifying glass.

The color and shade in the wet state is determined by examination of the mass, prepared for structure determination, artificial irrigation of a part of composite samples, usually water, or in the process of determining the content of coarse inclusions. Mineral impurities and inclusions determined visually. 	Quantitative determination of the content of coarse inclusions (greater than 0.5 mm) in accordance with the requirements of GOST 21216.4-93 produce a wet method using a sieve with the hole diameter of 0.5 mm.

From the average of the sample clay raw material is taken a sample weighing 0.5 kg of clay with undisturbed texture in a container to soak, and poured water in volume, exceeding by 3-4 times the volume of the raw clay. The resulting suspension was stirred and allowed to stand for 1h for swelling. If the clay slurry did not dissolve in 1 hour, leave it in the water for at least 24h. Quantitative determination of the content of coarse inclusions (greater than 0.5 mm) in accordance with the requirements of GOST 21216.4-93 produce a wet method using a sieve with the hole diameter of 0.5 mm.

The sieve with the residue of hurt under a stream of water, pre-adjusting it so that it was not sprinkling. The residue is washed until then while the water passed through the mesh becomes transparent. The rest sieve with mesh № 0.5 of wash water from rinse in a clean, previously dried and weighed dish and dried to constant weight in a drying chamber or under an infrared lamp at a temperature of 105-110 C, cooled and weighed. In the dried residue determine the total number of inclusions and their material composition.

Residue on the sieve № 0.5 weight more than 5% of the sample is sifted through a set of sieves with meshes № 0,5; 1; 2; 3; 4; 5 and balances on each sieve is weighed.

Next, each residue visually determine the presence of inclusions, their material composition and grain size.

Quartz, calcite, gypsum is determined by the hardness, luster and cleavage. Pyrite, marcasite, siderite, and iron hydroxides is determined by color, metallic luster and a brownish halo in natural state or after acid etching. Residues determined by color and appearance.

Calcium carbonates is determined by the release of carbon dioxide upon treatment with hydrochloric acid.

The grain size is measured with a metal ruler with a length of 100 mm or graduated lens. You can define the natural composition of the grains under a binocular magnifying glass or microscope.

The order of registration reports and their protection:

Mass fraction of coarse-grained inclusions (X) on each sieve in percentage calculated by the formula (1.1.):

X- (m1 – m2) 100/ m (1-4)                                                                            (1.1)

where: m1 - mass of the Cup with a dry residue, g;

m2- is the mass of the Cup, g;

m- is the mass of the original sample.

The discrepancy between the results of two parallel determinations should not exceed 2% when the content of coarse inclusions more than 10% and 1% when the content is less than 10%. If the discrepancy between the results of two parallel measurements exceeds the specified value, determining.

Research results are issued in table 1.

Table 1 – Macroscopic description of clay raw materials.

The determination coarse inclusions

| Name of raw materials | Color |  | Structure | Texture | Classification clay content of coarse inclusions |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | In the dry state. | In the wet state |  |  | The number of inclusions | The size of the inclusions | In appearance of the inclusions |

Control questions:

- What are the data compiled by the macroscopic characteristics of clay raw materials?

- Structure and texture, variety and methods of determining?

- What three main clay is subdivided into clayey texture of the rocks?

- What impurities and inclusions may be contained in the clay raw materials?

- Classification of the glial content of coarse inclusions?

Safety requirements

- Before the start of classes, the laboratory should be prepared to: prepare the workplace, necessary equipment, raw materials, special clothing (gowns, gloves, goggles).

- Special caution should be observed when working with electric furnaces.

- When performing work with the glass to avoid getting it into eyes, wear protective glasses.

- In the laboratory it is prohibited to:

-Smoking and eating;

- to be outsiders;

-to leave unattended laboratory instruments.

- 5 minutes before the end of the lessons students should gather all tools and instruments and pass them to the duty assistant. General safety requirements for training, laboratory work established in GOST 12.4.113.-82

List of used literature:

Main literature

- Бикбау М.Я. Нанотехнологии в производстве цемента. – М., 2008. –   761с.

- Таймасов Б.Т. Химическая технология вяжущих материалов: Учебник. – Шымкент: ЮКГУ им. М.Ауэзова, 2014. – 444с.

- Маневич В.Е. и др. Сырьевые материалы, шихта и стекловарение. –М.: РИФ «Стройматериалы», 2008. -224с.

- Сулименко Л.М. Общая технология силикатов. Учебник. - М.: ИНФРА, 2010. – 336 с.

Additional literature

- Классен В.К., Борисов И.Н., Мануйлов В.Е. Техногенные материалы   в производстве цемента / Монография – Белгород: Изд-во БГТУ, 2008. – 126 с.

- Бишимбаев В.К., Есимов Б.О., Адырбаева Т.А., Руснак В.В., Егоров Ю.В. Минерально-сырьевая и технологическая база Южно-Казахстанского кластера строительных и силикатных материалов. Монография. –Алматы: Раритет, 2009. -266с.

- Дворкин Л.И., Дворкин О.Л. Строительные материалы из отходов промышленности. – Ростов н/Д: Феникс, 2007. – 368с.

Laboratory work №2

Theme lessons: Determination of density and volume mass of the material

The purpose of lessons: familiarization with the Methods and materials of construction to assess the quality and mass density the desire to determine the amount of practical formation.

Running time of work – 2 hours

Brief theoretical information

Density 1

We say that density is mass per unit volume of a substance. An important property of binders is the density. Because the basis of its quality materials. Given a reference and densities of the investigated substances.

In the following examples you can see the density and properties of the binders that are linked.

Construction gypsum, depending on the heat treatment conditions, can be obtained in the form of  - hemihydrate (α–and β it is possible to cartilaginous state–in the form of cartilaginous. (p of the apparatus by the atmosphere of communion.b.) α-CaSO4 • 0,5H2O in the form of large crystals and tightly produced 2,72-2,75 g/cm3 density. Crystals -hemihydrate smaller and more defective. The density of β-СаЅО4 + O,5H2O – 2,62-of 2.66 g/cm3. Due to these peculiarities of the structure -hemihydrate, called high-strength gypsum, has a lower water requirement (30-40%), which provides a higher mechanical strength after hydration, in contrast to -hemihydrate, water requirement of which 50-70%.

The quality of caustic magnesite (MgO), obtained by calcination of the original carbonate at 700-800 оС by the reaction MgCO3 = MgO + CO2 largely depends on the quality of firing, changing the density of MgO.

Burned evenly caustic magnesit of 3.1-3.4 g/cm3 density. In the case of caustic density unbaked fully magnesit 3.1 g/см3 below, in connection with the peculiarities of some of the original numbers. Because it is MgCO3 density of 2.9-3.1 g/cm3, equal.

As burnout and underburning reduces the hydration ability of caustic magnesite.

The density of quicklime is in the range of 3.1-3.3 g/cm3.

It mainly depends on the firing temperature, the presence of impurities, incomplete combustion and burnout. The density value is below 3.1 g/cm3, evidence of underburning, i.e. the content of a certain number of initial CaCO3 with a density of 2.6 to 2.8 g/cm3. When burnout is influenced by sintering, recrystallization and the introduction of impurities Fe, Mn, Ca etc. into the lattice of Cao lime compacted to a density of 3.4 g/cm3 and the speed of hydration can be reduced several times.

As a result of various chemical additives and admixtures, as well as in connection with portlandcement phase composition, density of 3.1-3.2 g/cm3 to floating.

A higher density value are cements with a high content С4АF (=3,77 г/см3), and weighted backfill cements and cements for protection against ionizing radiation. The density of these cements is enhanced by heavy additives such as Fe2O3 (=5,24 г/см3 ),  BaSO4 ( =4,5 г/см3 ).

Slag and pozzolana Portland cement are characterized by a low density (2.7 to 2.9 g/cm3) due to the content of light additives, which =2,3-2,6 г/см3 (silica clay, diatomite, diatomaceous earth, etc.).

Bulk

Volume weight per unit volume of a substance is called mass, which in a particular case.

Distinguish mass of compacted volume, and to 2 selects. Loose materials (sand, stone flake) bulk density, without taking into account their places, and between units, is called the volumetric mass of manual work.

A lot of material bulk density weight. Only dense materials (glass, steel, concrete and liquid materials), the density and volume weight.

Practical sense very large masses of building materials. Given its stability in the preparation construction. Also, carrying and placing materials.

The bulk of construction materials obtained by roasting their level of maturity. Since the property of viscosity. The temperature and duration of annealing among the substances, mass, in turn, has a big impact on volume. The dependence of bulk density with temperature for burning lime, as specified below. 	 850-900 0С  -  1,4 – 1,6 g/см3;

1100- 1200 0С  -  1,5 – 2,5 g/см3;

1500 0С  -  3,43 g/см3.

Evaluate the quality of the clinker burning away portlandcement clinker liters weight. It is 1200 g/l up to 1750 g/l can vary up to. Low volume weight (weight l), is equal to 1200 -1400 g/l, evidence of either underburning, or about education in a furnace fine dust the clinker is of lower quality.

The liter weight of clinker above 1700 g/l is a sign of burnout clinker, associated with overheating of the lining, premature refractory wear and excessive fuel consumption. The optimal litre weight of clinker is set empirically at the factory and is in the range of 1450-1650 g/l.

Bulk volume weight of Portland cement is in the range of 900-1100 kg/m3, and the compacted 1400-1700 kg/m3 . Often in calculations of storage tanks make an average bulk weight of the cement 1200 kg/m3, while the volumetric dosage of the material for making the concrete mix is accepted body mass of 1300 kg/m3.

Bulk weight depends on the fineness of grinding. The finer the grind, the less the volume weight of the material.

As a result of prolonged storage of powdered materials become compressed, compacted and bulk density increases.

Table 2 shows the values of density and bulk density of some building materials.

Table 2 – density and volume weight of some building materials

| Material | Density, g/cm3 | Volumetric weight, kg/m3 |  |
| --- | --- | --- | --- |
|  |  | in loose condition | in a Packed |
| Construction gypsum is highly durable Construction gypsum is common Natural gypsum (СаSO4 * 2H2O) Anhydride (CaSO4) Magnesite (МgCO3) Caustic magnesite (MgO) Limestone Lime, quicklime lump Lime pushonka Portland cement Pozzolanic cement Portland slag cement Flask Diatomaceous earth Diatomite | 2,72-2,75 2,62-2,66 2,2-2,4 2,9-3,1 2,9-3,0 3,1-3,4 2.6-2.7 3,1-3,3 2,08-2,23 3,1-3,2 2,7-2,9 2,7-2,9 2,3-2,6 2,3-2,6 2,3-2,6 | 800-1100 1200-1400 2400-2800 800 400-450 900-1100 900-1100 1400 1400 850 750 | 1250-1450 1200 1400-1700 1300-1500 2200 |

Cement weight in calculating the average volume of intermediate tanks, it adopts the separately – 1200 kg/m3. In the preparation of the slurry volume of concrete, and at a dose of 1300 kg/m3, bulk density is taken to be equal.

The mass of the crushed material in contact with the intermediate age. The crushed material is narrower than less bulk. As a result, after compliance with a long captaincy powders, the bulk density will increase and destroy them.

Equipment, tools and technical means:

For determining the density Le Chatelier tool.

- The spatula, funnel Gasoline or kerosene

- A device for determining bulk density

- Test material

The order of performance of works in the audience:

1 Determination of the density of the material

To determine the average density of the used instrument Le Chatelier-Congo, which is a glass flask (Fig.1.1); the neck above and below the extensions applied 2 features, the volume between which is equal to 20 cm3.

The device is placed in a glass vessel with water to the calibration part of it was submerged in water. To avoid floating, the flask attached to a special tripod. The device is pre-check. At definition time, you must make sure that as the first and the second samples the water temperature in the vessel were the same and corresponded to the temperature of calibration of the instrument.

The device filled with gasoline or other inert material to the fluid, and the fluid level is set at the lower meniscus.

The test material is pre-dried, weighed on a technical balance in the amount of 100 g and poured through a funnel in small portions until the fluid level reaches 20 cm3 of division or any other division within the graduated part of the instrument. Then the remaining sample is weighed to the nearest 0.01 and the difference between results 1 and 2 weighings determine the mass of powder, poured into the flask

The average density of the tested material is obtained by dividing the mass is poured into a flask of powder to its volume, as the arithmetic average from two definitions, and the divergence of outcomes should not exceed 0.02 g.

The results of determination of density of record in the following form:

The name of the material ......................................................

Liquid ....................................................................

Linkage U1..................................................................

The remainder of the sample U2 ....................................................

The mass of the powder immersed in liquid U1- U2=...............

The volume of displaced fluid WA ..................................cm3

The average density .............................g/cm3

Determination of density

Volume weight material in a loose state is determined by the device of the funnel Le Chatelier-Congo. The device consists of an inverted truncated cone, which passes into a tube with a valve. Inside the truncated cone is located a sieve with holes of 2 mm diameter, preventing the tube from falling into it larger particles. The cone relies on a three-legged stand. Under the tube is placed a cone-liter container. The distance between the upper edge of the vessel with the valve is 50 mm (Fig.1.2). In the funnel of the device in the closed latch poured about 2 liters of dried material, and then open the valve and place the powder on a sieve, fill the liter container. When the vessel is filled with some excess, the valve closed, and the excess powder is cut with a metal or wooden ruler flush with the edges of the vessel. Should avoid shocks, contributing to the seal material. Then a container of material is weighed.

To determine the bulk density of material in compacted condition, liter vessel misleading uniform shocks. As the sedimentation of material in the vessel, its complement. When the volume becomes constant, the volumetric weight is determined as described above.

The notation is similar as in the determination of the density of the material.

Fig 1.1.The device Le Chatelier for                Fig 1.2.Funnel to determine the volumetric weight                                                          determining the specific gravity

Control questions

1. What is the density of the material?

2. What is the bulk of the material?

3. What is density of gypsum in different binders?

4. What is the impact on the density, the temperature, the lime burning?

Safety requirements

- Before the start of classes, the laboratory should be prepared to: prepare the workplace, necessary equipment, raw materials, special clothing (gowns, gloves, goggles).

- Special caution should be observed when working with electric furnaces.

- When performing work with the glass to avoid getting it into eyes, wear protective glasses.

- In the laboratory it is prohibited to:

- Smoking and eating;

- to be outsiders;

-to leave unattended laboratory instruments.

- 5 minutes before the end of the lessons students should gather all tools and instruments and pass them to the duty assistant. General safety requirements for training, laboratory work established in GOST 12.4.113.-82

List of used literature:

Main literature

- Бикбау М.Я. Нанотехнологии в производстве цемента. – М., 2008. –761с.

- Таймасов Б.Т. Химическая технология вяжущих материалов: Учебник. – Шымкент: ЮКГУ им. М.Ауэзова, 2014. – 444с.

- Маневич В.Е. и др. Сырьевые материалы, шихта и стекловарение. –М.: РИФ «Стройматериалы», 2008. -224с.

- Сулименко Л.М. Общая технология силикатов. Учебник. - М.: ИНФРА, 2010. – 336 с.

Additional literature

5 Классен В.К., Борисов И.Н., Мануйлов В.Е. Техногенные материалы

в производстве цемента / Монография – Белгород: Изд-во БГТУ, 2008. – 126 с.

- Бишимбаев В.К., Есимов Б.О., Адырбаева Т.А., Руснак В.В., Егоров

Ю.В. Минерально-сырьевая и технологическая база Южно-Казахстанского кластера строительных и силикатных материалов. Монография. –Алматы: Раритет, 2009. -266с.

- Дворкин Л.И., Дворкин О.Л. Строительные материалы из отходов

промышленности. – Ростов н/Д: Феникс, 2007. – 368с.

Laboratory work №3

Theme lessons: Determination of moisture and fineness of grinding material

The purpose of lessons:  To master the methodology for determining the moisture content and fineness of grinding raw slurry and to study the influence of the fineness of grinding of slime on the processes of mineral formation.

Running time of work – 2 hours

Brief theoretical information

The raw slurry is a dispersed system in which the limestone, clayey and correcting component serve as the dispersed phase, and the dispersion medium is water. A solid phase is a polydisperse material whose particle size varies from 3 to 200 μm.

The most coarsely dispersed are the grains of limestone, quartz, feldspars, and highly dispersed - clay minerals, aluminum and iron hydroxides. The total solids content in slimes varies from 65 to 50%. Such sludge can be considered as a colloidal system. Like any colloidal system, slimes are characterized by certain structural and mechanical properties - viscosity, ultimate shear stress and coagulation ability.

The fluidity and stability of such systems are determined by the concentration of the solid phase, its specific surface, the energy state of the surface of solid particles, and the formation of solvate shells on their surfaces. Since for the production process water is not just a ballast, but also a component that requires large heat costs for its removal, it is necessary to obtain a raw slurry with a minimum moisture content. The minimum moisture content is determined by the necessary transportable capacity of the slurry, in which the sludge will not cover the mill, it can flow along the inclined planes by gravity (in the ditch) and be pumped by slurry centrifugal pumps.

With increasing humidity, the distance between structural elements in the sludge increases, the Van der Waals forces are weakened and the mud becomes more mobile. The flow / moisture ratio with the minimum amount of water is associated with the fineness of grinding the solid particles. The greater the specific surface area of ​​raw materials, the more water is required to ensure the necessary flow. The fluidity / humidity ratio is also affected by the mineralogical nature of the raw materials, the amount of water-soluble salts and humic acids, and the clay constituents present. The water demand of raw sludge is determined mainly by the dispersion of clay and chalk in clay-chalk mixtures, as well as by the density (porosity) of the limestone component, since it is associated with a specific surface including internal pores.

The properties of slurries based on hard limestone are determined by the clay component, since clays are a more dispersed material than limestone. Clay is a heterogeneous material and often contains a large amount of quartz sand. Sludge based on unclaimed clays (fatty) always have higher humidity (based on limestone - up to 44%, based on chalk - up to 50%).

The fineness of grinding of raw sludge, in addition to fluidity, has a significant influence on the rate of binding of lime with acidic oxides, and on the clinker formation processes both at the stage of solid-phase reactions and at the stage of liquid-phase sintering. It has been established that in uncoated cement raw mixes, in comparison with fine dispersions, unbound lime remains much more often in clinkers. Coarse milling affects the structure of the clinker, while in it there are alternating accumulations of minerals. With coarse grinding of raw sludge, some of the large-sized grains do not have time to completely react in the firing process and remain in the clinker in a free state. Only the grains of components having a size of less than 120 μm are sufficiently reactive. In practice, however, industrial slurries contain up to 10% or more particles of more than 120 μm, which in some cases is one of the reasons for the slow absorption of lime.

The permissible fineness of grinding the raw material to ensure normal sinterability is largely determined by its mineralogical nature.

Particular attention should be given to the fineness of grinding of quartz and limestone, since it is these two components, being difficult to grind, form the basis of coarse fractions of raw mixtures. Clayey components are highly dispersed from nature, their specific surface reaches 300 m2 / g, so the formation of coarse aggregates is practically impossible. However, the use of dense clay shales as a clay component, some highly silicified particles of the latter may not be sufficiently finely ground.

The positive effect of increased fineness of grinding of the slurry on the reactivity of the mixture is explained by the following reasons

- an increase in the surface energy of the particles due to the breaking of chemical bonds and an increase in the fraction of weakly bound ions;

- an increase in the number of defects in crystals;

- an increase in the total area of contact between the particles;

- Reducing the thickness of the reaction product layer on the grains of acidic components;

- acceleration of dissolution of particles in the melt;

- increasing the degree of homogeneity of the raw meal composition

- increase in the density of particle packing.

Establishing the optimal and technically achievable granulometric composition of all components of the feed mixture that would ensure the highest rate of CaO binding and the lowest power consumption for grinding raw materials is a difficult task. Therefore, at each enterprise, this problem is approached individually, by studying the reactivity of raw components. Different researchers give different information about the expedient fineness of grinding of slime. Most of them note that the fineness of grinding the factory raw mixtures, determined by the residue on the screen № 008, should be from 5 to 15%. Some, in particular Kravchenko I. V., Dolbilov G. I., found that when firing in modern high-performance furnaces, the fineness of grinding can be higher (up to 20%). Since at high fineness of grinding in such furnaces, solid-phase reactions and formed C2S, as well as CaO, are accelerated. they succeed in recrystallizing and their dissolution in the melt is slowed down. Studies carried out at the SKSU at the Chair Technology of cement, ceramics and glass confirm these assumptions and, moreover, establish that under certain conditions it is possible to burn raw slurries with the residue on a sieve № 008 to 30-35% safely in rotary kilns.

Equipment, tools and technical means:

1. Wet sludge.

2. Dry sludge.

3. Porcelain bowls.

4. Technical scales.

5. Glass beakers.

6. Spoon, spatula, calipers.

7. Laboratory drying cabinet.

8. Set of sieves

9. Weights

The order of performance of works in the audience:

The procedure for determining the moisture content and fineness of the grinding of the sludge is to bring the sludge to a complete loss of flowability by settling and subsequent evaporation of the excess water content (at a temperature of no more than 800 0C), during the drying process, the sludge must be mixed.

To determine the moisture content of the sludge, 100 grams of wet sludge is weighed. The sample is transferred to a drying cabinet for complete removal of water, for an hour at 800 ° C. Each determination is made twice. If there is more than one difference in the measurement results, a third determination is made, after obtaining a number of values for the slurry, one is chosen which has a large convergence.

- Determination of moisture (W1) of the original slurry (%)

(3.1.)

Where:W1-is the moisture content of the slurry,%;

Рsh - suspension of sludge, g;

Pс - dry sludge weight, g.

To determine the fineness of grinding:

- 50 g of averaged slurry with known moisture are weighed on technical scales to within 0.1 g

- We carefully wash the sample with a stream of water from the water pipe

- to №008 sieve, and wash the sediment until absolutely pure water hadrained off.

- The sieve with the residue is dried at a temperature of 100-1100 ° C. The

dried residue is screened onto a sheet of white paper (sieving is considered complete if no more than 0.05 g of residue passes through the sieve for 1 minute). The residue remaining on the sieve №008 is poured onto the pan and weighed.

- The fineness of the grind is expressed in% of the residue on a sieve and is calculated by the formula:

Тp=Р1*100/Р0(100-W)                                                                              (3.2.)

where:Р1-the rest on a sieve № 008 in grams;

P0- is the sample of wet sludge, g;

W- slurry humidity,%.

- The rest of the sieve No. 008 after weighing is transferred to a No. 02

sieve, screened and the remaining residue on sieve  №02 is weighed. The fineness of grinding on №02 sieve is expressed in% and is calculated by formula №02

Note: With the addition of a wet slurry of 50 g, formula 2 takes the following form:

Тp = 2Р1 / (100-W)                                                                                     (3.3.)

Control questions

- Purpose of the work.

- Economic feasibility of determining the fineness of grinding of sludge.

- Influence of fineness of grinding of raw sludge on the processes of clinker formation.

- Influence of fineness of grinding of limestone component on lime assimilation.

- Influence of fineness of grinding of a clay component on the assimilation of lime.

- Indicate the main causes of deterioration of reactivity of raw sludge with coarse grinding.

- At what fineness of grind, the enlarged raw mixes do not degrade the reactivity of the feedstock and why?

- How is the moisture content of raw sludge determined and for what?

- How is the fineness of the grinding cut determined?

Safety requirements

- Before the start of classes, the laboratory should be prepared to: prepare the workplace, necessary equipment, raw materials, special clothing (gowns, gloves, goggles).

- Special caution should be observed when working with electric furnaces.

- When performing work with the glass to avoid getting it into eyes, wear protective glasses.

- In the laboratory it is prohibited to:

- Smoking and eating;

- to be outsiders;

- to leave unattended laboratory instruments.

- 5 minutes before the end of the lessons students should gather all tools and instruments and pass them to the duty assistant.

- General safety requirements for training, laboratory work established in GOST 12.4.113.-82

List of used literature:

Main literature

- Бикбау М.Я. Нанотехнологии в производстве цемента. – М., 2008. –761с.

- Таймасов Б.Т. Химическая технология вяжущих материалов: Учебник. – Шымкент: ЮКГУ им. М.Ауэзова, 2014. – 444с.

- Маневич В.Е. и др. Сырьевые материалы, шихта и стекловарение. –М.: РИФ «Стройматериалы», 2008. -224с.

- Сулименко Л.М. Общая технология силикатов. Учебник. - М.: ИНФРА, 2010. – 336 с.

Additional literature

- Классен В.К., Борисов И.Н., Мануйлов В.Е. Техногенные материалы в производстве цемента / Монография – Белгород: Изд-во БГТУ, 2008. – 126 с.

- Бишимбаев В.К., Есимов Б.О., Адырбаева Т.А., Руснак В.В., Егоров Ю.В. Минерально-сырьевая и технологическая база Южно-Казахстанского кластера строительных и силикатных материалов. Монография. –Алматы: Раритет, 2009. -266с.

- Дворкин Л.И., Дворкин О.Л. Строительные материалы из отходов промышленности. – Ростов н/Д: Феникс, 2007. – 368с.

Laboratory work №4

Theme lessons: Determination of ductility and conduct ability of clay raw materials

The purpose of lessons: Qualitative determination of plasticity of clay raw materials.

Running time of work – 2 hours

Brief theoretical information

The plasticity of clays is the ability of a clay dough under pressure to change shape (deform) without the formation of cracks and discontinuities and to preserve this shape after the load is removed.

Plastic properties of clays are characterized by one and the same clay, depending on the content of the water. The transition of clay from one consistency to another takes place at certain values of humidity, which are called the limits of plasticity:

- Moisture content (% by mass) at which the clay passes from the plastic

state to the fluid, is called the upper limit of plasticity, or the lower boundary of yield (W2).

- Moisture content (% by mass) in which clay does not stick to hands and

the metal, called the normal working consistency or limit stickiness (adhesion)

- Moisture content (% by mass) at which the clay passes from the plastic

state to the fragile (not rolled into threads), is called the lower limit of plasticity, or limit of rolling (W2).

The difference between the upper and lower limits of plasticity is the plasticity characteristics of clays and is called the plasticity number

P = W1 – W2                                                                                                (4.1)

where: W1 is the moisture content of clay (mass) to a lower limit of the   flowage,%;

W2 - moisture content of clay (mass) on the border of rolling, %.

Depending on the plasticity of clay raw materials according to the classification GOST 9169-75 is divided into five groups (table 3).

Table 3- Classification of clays according to the number of plasticity (GOST 9169-75)

| The name of the group of clay raw materials | The number of plasticity |
| --- | --- |
| Highly The average plastic Moderately plastic Little plastic Non-plastic | Over 25 Over 15 to 25 Over 7 to 15 More than 3 to 7 Do not give plastic test |

Determination of plasticity of clay raw materials produced by two methods:

- The definition of the upper limit of plasticity on the device Vasiliev and

lower limit of elasticities the Granin rolling (GOST 21216-93).

- Determination of upper plastic limit using cone beam and lower limit of

plasticity, the value for the maximum molecular moisture capacity (according to the method of A. F. Lebedev).

Equipment, tools and technical means:

- Laboratory scales

- Drying wardrobe, providing a heating temperature of 105-110°C or lamp infrared radiation with a power of 500W with internal mirror reflector.

- Desiccator

- The sieve № 05

- Cup porcelain

- Porcelain mortar with pestle

- Crucibles porcelain

- Cups or boxy for weighing

- Spatula with tip

10.Device design Vasilyev

The order of performance of works in the audience:

1. The definiton of the upper limit of plasticity on the device vasiliev and the lower limit of plasticity at the border of rolling  (GOST 21216.1-93).

The method is based on determining the difference between the humidity of the clay mass, corresponding to the lower border of the yield strength and the limit of rolling.

Device A. Vasiliev (figure 4.1.) represents a basic unit 1 with base plate 2 in the upper part of the frame is free to move the stem 3 mounted thereon the disc 4 on which is mounted a porcelain Cup 5 with a diameter of 95 mm, weight 58 - 60 g. In the lower part of the rod is fixed focus. The rod at the desired height is fixed by screw 1,2.

Figure 4.1. - Device A. Vasiliev                     Figure 4.2. - Distribution of clay dough in the Cup:

Definition of lower boundary fluidity:

Take 60 grams of dried to air-dried clay, crushed in a porcelain mortar and sifted through a sieve with the hole diameter 0.5 mm, was placed in the Cup, where with continuous stirring distilled water is added until a homogeneous dough (more liquid than in the normal operating condition).

The dough is spread evenly on the bottom of the Cup with a layer thickness of 10 mm and with a spatula cut into equal parts so that the gap between them had top width to 2.5...3 mm and on the bottom of the Cup - 1 mm (figure 4.2.). The Cup is mounted on the disk, and a rod fixed with screws in such a position that he was at a distance of 75 mm from the base plate of the device. After this stem with the Cup allowed to freely fall and strike the base plate. Weight in the Cup is shaken, the gap between the two parts is reduced. Shake produce three times. The yield strength is reached, if both halves of the mass after the third strike at the bottom of the cups are connected for 10...15 mm. If after the third shaking of the mass at the bottom of the Cup is not connected, it is necessary to add water (0.5 to 1 cm ). thoroughly stir the whole mass, and a re-definition of the lower boundary of the flow. If parts of the mass are connected after the first or second on shaking, the humidity of the mass above the yield limit and the weight should be added 0.5 to 1 g air-dry sieved clay, thoroughly mixed, and to repeat the experience.

Definition produced until then, until you reach the desired consistency of the mass.

After finishing the test, take the sample weight of 25g. placed in a previously dried to constant mass and weighed the Cup with the lid open, and dried in a drying cabinet at a temperature of 105 to 110"C. Then the Cup is removed, close lid, cooled in a desiccator and weighed. Drying is repeated until the constant weight. The obtained value of moisture, expressed as a percentage, sets the lower limit of fluidity.

The definition of the boundaries of the rolling.

Remaining after determining the lower border of the yield mass transfer on flat glass, linoleum, or glossy sheet of paper and hand rolled into a rope with a diameter of about 3 mm. If in this thickness  retains viscosity and plasticity, it is collected into a ball, add the tin. mix thoroughly and re-rolled to the specified diameter. Highly plastic mass is pre-rolled on a plaster plate to the loss of viscoelastic properties. Rolling lead, gently pressing down the harness, preventing simple skating on the plate. Rolling lead so far. while the wiring with a diameter of about 3 mm will begin to divide the transverse cracks into pieces with a length of 3...10 mm. The resultant lumps of clay (at least 10 g) is collected in pre-dried to constant weight and weighed Cup or boxe and determine the percentage moisture content by the above method. The resulting moisture value (in %) sets the limit of rolling.

Technological calculations

Moisture content (W) in percent is calculated according to the formulas:

1. For the upper limit of plasticity, or the lower boundary fluidity:

W1= ( m1– m2) 100/ m2                                                                                 (4.2.)

where: m1 - mass of wet sediment;

m2 - weight of sample dried at a temperature of 105...110 °C.

2.For the lower plastic limit, or border rolling:

W2 = ( m3 – m4) 100/ m4                                                                               (4.3)

where: m3- is the mass of wet sample, g,

m4 - mass of sample dried at a temperature of 105...110 °C.

The number to the plasticity (P) in percent is expressed by the difference between the upper and lower limits calculated by the formula:

P = W1 - W2                                                                                                  (4.4.)

Admissible divergence between results of two parallel measurements of the number of plasticity must not exceed the values shown in table 4.

Table 4 - Valid value

| The number of plasticity, % | Allowable difference, % |
| --- | --- |
| Up to 15 | 2 |
| Over 15 to 25 | 3 |
| Over 25 | 4 |

If the discrepancy between the results of parallel measurements exceeds the specified value, the determination is repeated. The final result of the analysis taking the arithmetic average of the results of two parallel measurements.

All the results are recorded in table 5.

Table 5- the result of the analysis

| Name of raw materials | Number buxa | Weight, g |  |  |  |  |  |  |  |  |  | Humidity,% |  |  |  | Pure plasticity P=W1-W2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Dry buxa |  |  | Box covered |  |  | sample |  |  |  | W1 |  | W2 |  |  |
|  |  |  |  |  | Wet | Dry |  | Wet |  | Dry |  |  |  |  |  |  |
| The upper limit of plasticity |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| The lower limit of plasticity |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

Control questions

- What does the concept tie "the plasticity of clays", what determines the number of plasticity?

- What are the methods of determining plasticity know?

- Classification of clays for plasticity.

- What state takes the clay depending on the amount of water?

- How to explain the mechanism of transformation of the clay; plastic dough?

Safety requirements

- Before the start of classes, the laboratory should be prepared to: prepare the workplace, necessary equipment, raw materials, special clothing (gowns, gloves, goggles).

- Special caution should be observed when working with electric furnaces.

- When performing work with the glass to avoid getting it into eyes, wear protective glasses.

- In the laboratory it is prohibited to:

- Smoking and eating;

- to be outsiders;

-to leave unattended laboratory instruments.

- 5 minutes before the end of the lessons students should gather all tools and instruments and pass them to the duty assistant. General safety requirements for training, laboratory work established in GOST 12.4.113.-82

List of used literature:

Main literature

  - Бикбау М.Я. Нанотехнологии в производстве цемента. – М., 2008. –   761с.

  - Таймасов Б.Т. Химическая технология вяжущих материалов: Учебник. – Шымкент: ЮКГУ им. М.Ауэзова, 2014. – 444с.

  - Маневич В.Е. и др. Сырьевые материалы, шихта и стекловарение. –М.: РИФ «Стройматериалы», 2008. -224с.4. Сулименко Л.М. Общая технология силикатов. Учебник. - М.: ИНФРА, 2010. – 336 с.

Additional literature

- Классен В.К., Борисов И.Н., Мануйлов В.Е. Техногенные материалы   в производстве цемента / Монография – Белгород: Изд-во БГТУ, 2008. – 126 с.

- Бишимбаев В.К., Есимов Б.О., Адырбаева Т.А., Руснак В.В., Егоров Ю.В. Минерально-сырьевая и технологическая база Южно-Казахстанского кластера строительных и силикатных материалов. Монография. –Алматы: Раритет, 2009. -266с.

- Дворкин Л.И., Дворкин О.Л. Строительные материалы из отходов промышленности. – Ростов н/Д: Феникс, 2007. – 368с.

Laboratory work № 5

Theme lessons: Determination of charge composition of glass: control of glass charge

The purpose of lessons: The calculation of the glass batch of high quality raw materials.

Running time of work – 1 hour

Brief theoretical information

Batch is a homogeneous mixture previously prepared and weighed according to the calculated (specified) the recipe of raw materials.

In the calculation of the glass batch accept that glass pass oxides and fluorides, and the moisture and gases evaporate. The calculation of the charge can be carried out on 100 mass. glass or h. on 100 mass. hour. quartz sand. More common the first method, as it facilitates further computations.

Initial data for calculation of the charge are:

- specified chemical composition glass, wt. %;

- chemical compositions of selected raw materials, mass. %;

- correction coefficients for the volatilization of glass components during boiling

Given the chemical composition of the glass to result in 100 wt. %. It should not include components that fall into the glass as an unwanted impurity in raw materials (Fe2O3, Cr2O3, etc.) or components that fall from the atmosphere furnace (SO3). This composition is called project glass.

Chemical compositions of raw materials are taken from the regulatory documents with regard to the type of glass for which the calculation of the charge and distance of transportation of raw materials, if the calculation is done for a particular company. The chemical composition of each raw material should be presented in the form of oxides or fluorides, turning into glass, so the data of normative documents should be pre-treated. The main substances of raw materials of complex compounds (Na2CO3, KNO3, H3BO3, Na2BO4, 10H2O and Ba(NO)2, etc.), recalculated to oxides, in accordance with stoichiometry of chemical reactions. Water and gases are removed in the melting process, are not included in the composition of the raw materials. Complex oxides (PbO2, Pb3O4), and metals (Al, Na, Pb) and cations (Fe3+, Zn2+) are converted into oxides, which are formed in the glass during melting Contained in the raw materials of NaCl result from the volatilization and decomposition of water vapor when melting pass into glass oxide Na2O, the amount of which is 10 times less by weight of the initial amount of NaCl. The sum of the components in the chemical composition of raw materials according to regulatory documents always below 100 wt. % as it does not include loss on ignition, volatile substances and many small impurities.

Some components of the glass much or much disappear in the melting process. To compensate for losses and ensure the desired chemical composition of the glass corresponding raw materials are injected into the charge increased (in accordance with the correction factors) amounts (table 6).

Table 6 – Correction factors for the volatilization of glass components when boiling in the fiery furnaces

| Glass components | The value of the correction factor |
| --- | --- |
| Na2O (when administered through the soda) | 1,032 |
| Na2O (with the introduction of a sulfate) | 1,05 |
| K2O | 1,12 |
| ZnO | 1,04 |
| PbO | 1,14 |
| P2O5 (flat glass) | 1,075 |
| B2O3 (when the content in the glass up to 7 wt. %) | 1,11 |
| B2O3(when the content in the glass is more than 7 wt. %) | 1,15 |
| Na2SiF6 and 3NaF AlF3 | 1,30 |
| F (with other components for normal glass) | 1,30 |
| F (with other components for refractory glasses) | 1,50 |
| Se | 1,90 |

To high-quality raw materials can be classified as high grade quartz sand, dolomite, limestone, as well as most technical of raw materials. With rare exceptions (dolomite, calcium borate) they are designed to penetrate glass of any one of the specified oxide, whose content in them is high, and the other impurity oxides contained in small quantities.

Dolomite and calcium borate intended for insertion respectively in the glass of oxides of magnesium and boron, but at the same time they are introduced about the same weight amount of calcium oxide. If the quartz sand contains a significant amount of admixture of aluminum oxide, it can be calculated like material, which we introduce two specified oxide of aluminium and silicon.

Batch of high quality raw materials used in the manufacture of optical and crystal glass, profiled glass, technical glass, laboratory synthesis of glasses.

The calculation of the charge on 100 mass. hour. glass is produced by formula

СМj III = Окi CT ·Кi ·100 / Окi SM                                                                 (5.1.)

where: СМj III - amount of raw material in the mixture, wt. h. on 100 wt. h glass;

Окi ST- is a specific oxide content in the glass, wt. %;

Кi -is the correction coefficient for the volatilization of oxide when cooking;

Окi SM - the contents of the specified oxide in the raw material wt. %.

With the introduction of one of the oxide glass by two different commodities (for example. K2O is introduced into lead crystal potash, and nitrate) establish in advance what amount of oxide introduced from each of the two raw materials.

The amount of dolomite, calcium borate and quartz determined on the basis of the specified content in the glass of those oxides, for the introduction which they are intended, i.e., MgO, B2O3 and SiO2. Then calculate how much you enter with these materials, respectively, of the oxides CaO, CaO and Al2O3. By difference between the specified content of oxides in the glass and entered from the specified raw materials establish new target content of Cao and Al2O3. Based on the new given content of oxides in the glass according to the expression (1) determine the quantity of raw materials (limestone, technical alumina) required for the introductions of the remainder of the oxides of calcium and aluminum.

Further calculations are performed in the following sequence According to the calculated quantities of each raw material in the charge СМj III calculates the quantity of all oxides including the impurity that go into each glass raw material. Calculations performed by the formula

OKij ST = СМj III · Окij SM  / Кi · 100                                                             (5.2.)

where: OKij ST - the number of oxides that go into a glass from each of the j-th raw material sequentially;

Окij SM - oxides successively in each raw material, wt. %.

Then create a pivot table and summarize the calculated values for each specified impurity, and the oxide. This produces the so-called calculated chemical composition in which the sum of the components is more than 100 massa.hour due to the occurrence of impurity in the glass of oxides of the raw materials Calculated chemical composition of the glass recalculated to 100 wt. % get the so-called theoretical part of the glass Because the burden calculation is carried out on 100 wt. h, glass, the report adjusts the number of raw materials.

The results of the calculation of the charge determine important from a technological point of view, the indicators of output glass during the glass formation and waste charges.

The output of the glass batch, a quantity of glass, which is obtained from 100 mass. hour. part of the charge. Frenzy charge - the quantity of gaseous components of the charge, retreating when cooking 100 mass. hour.part of the charge.

Sample.To calculate the composition of the batch for crystal glass the following chemical composition, wt. %:

| № | SiO2 | Al2O3 | PbO | K2O | Na2O | Σ |
| --- | --- | --- | --- | --- | --- | --- |
| 0 | 62,0 | 0,9 | 19,5 | 14,6 | 3,0 | 100 |
| 1 | 61,0 | 1,8 | 18,6 | 14,6 | 4,0 | 100 |
| 2 | 64,0 | 1,0 | 18,0 | 14,1 | 2,9 | 100 |
| 3 | 63,0 | 0,5 | 19,5 | 14,1 | 2,9 | 100 |
| 4 | 62,0 | 1,0 | 20,0 | 13,5 | 3,5 | 100 |
| 5 | 62,1 | 0,8 | 19,5 | 14,6 | 3,0 | 100 |
| 6 | 65,0 | 1,0 | 17,0 | 14,1 | 2,9 | 100 |
| 7 | 66,0 | 1,0 | 16,0 | 14,1 | 2,9 | 100 |
| 8 | 64,0 | 2,0 | 17,0 | 14,1 | 2,9 | 100 |
| 9 | 65,0 | 1,0 | 17,0 | 14,9 | 2,1 | 100 |
| 10 | 65,9 | 1,0 | 17,0 | 14,1 | 2,0 | 100 |
| 11 | 65,1 | 1,0 | 17,0 | 14,0 | 2,9 | 100 |

Potash glass to enter in 8.0, and the nitrate of 6.6 wt % of potassium oxide.

Chemical composition of raw materials after necessary preliminary recalculations are presented in table 7.

Table 7 – Chemical composition of raw materials

| Raw materials | The content of oxides, mass.% |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | SiO2 | Al2O3 | PbO | K2O | Na2O | Fe2O3 |
| Quartz sand | 98,5 | 0,6 | - | - | 0,3 | 0,03 |
| Alumina | - | 98,9 | - | - | 0,4 | 0,03 |
| Lead minium | - | - | 97,0 | - | - | 0,003 |
| Potash | - | - | - | 66,8 | 0,3 | 0,001 |
| Nitrate potassium | - | - | - | 46,5 | - | 0,005 |
| Nitrate technical | - | - | - | - | 57,6 | 0,005 |

Consistently first determine the amount of each raw material in the mixture according to the expression (1).

The amount of quartz sand in the mixture, wt. h:

СМkv.p. III = 62,0·100 / 98,5 = 62,94

The calculated amount of quartz sand in the glass is introduced aluminium

oxide,

wt. h:OKAl2O3st  =  62,94 · 0,6 / 100 = 0,38

Therefore, using the alumina in the glass it is necessary to introduce aluminum oxide, wt. h:

0,90 – 0,38 = 0,52

Then the amount of alumina in the mixture amount, wt. h:\

СМ. =  0,52 · 100 / 98,9 = 0,53

The amount of red lead in the charge, mass. hour:

СМ =  19,5 · 1,14 · 100 / 97,0 = 22,92

The amount of potash in the mixture, mass. hour:

СМ =  8,0 · 1,12 · 100 / 66,8 = 13,41

The amount of potassium nitrate in the mixture, mass. hour:

СМ =  6,6 · 1,12 · 100 / 46,5 = 15,90

The amount of soda technical in the charge, mass. hour:

СМ =  3,0 · 1,0,32 · 100 / 57,6 = 5,37

Next, determine the number of oxides that go into each glass raw material.

With quartz sand in the glass passes, wt.CH.:

OK SiO2 СT  =  62,94 · 98,5 / 100 = 62,00

OKAl2O3 CT  =  62,94 · 0,6 / 100 = 0,38

OK Na2O CT  =  62,94 · 0,3 / 1,032·100 = 0,18

OK Fe2O3 CT  =  62,94 · 0,03 / 100 = 0,019

With alumina in the glass goes, wt.CH.:

OKAl2O3 CT  =  0,53 · 98,9 / 100 = 0,52

OK Na2O CT  =  0,53 · 0,4 / 100 = 0,002

OK Fe2O3 CT  =  0,53 · 0,03 / 100 = 0,0002

With lead red lead goes in the glass, wt.CH.:

OK PbO CT  =  22,92 · 97,0 / 1,14·100 = 19,50

OK Fe2O3 CT  =  22,92 · 0,003 / 100 = 0,0007

With potash in the glass goes, wt.CH.:

OK К2O CT  =  13,41 · 66,8 / 1,12·100 = 8,00

OK Na2O CT  =  13,41 · 0,3 / 1,032·100 = 0,04

OK Fe2O3 CT  =  13,41 · 0,001 / 100 = 0,0001

With potassium nitrate in the glass goes, wt.CH.:

OK К2O CT  =  15,90 · 46,5 / 1,12·100 = 6,60

OK Fe2O3 CT  =  15,90 · 0,005 / 100 = 0,0008

Soda technical in the glass goes, wt.CH.:

OK Na2O CT  =  5,37 · 57,6 / 1,032·100 = 3,00

OK Fe2O3 CT  =  5,37 · 0,005 / 100 = 0,0003

Then make free table 8, and determine the calculated composition of the glass.

Table 8 – Summary table of calculation of the charge

| Raw materials | The content of oxides, mass.% |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | SiO2 | Al2O3 | PbO | K2O | Na2O | Fe2O3 |
| Quartz sand | 62,0 | 0,38 | - | - | 0,18 | 0,019 |
| Alumina | - | 0,52 | - | - | 0,002 | 0,0002 |
| Lead minium | - | - | 19,50 | - | - | 0,0007 |
| Potash | - | - | - | 8,0 | 0,04 | 0,0001 |
| Nitrate potassium | - | - | - | 6,60 | - | 0,0008 |
| Nitrate technical | - | - | - | - | 3,00 | 0,0003 |
| The estimated glass composition | 62,0 | 0,90 | 19,50 | 14,60 | 3,22 | 0,0211 |
| The amount of oxides in the calculated glass composition, wt.h. |  |  |  |  |  | 100,2411 |

The sum of the components in the calculated composition of the glass was above 100 by entering in the glass of sodium oxide from silica sand, industrial alumina and potash, and the impurities of oxide of iron from all raw materials. The theoretical composition of the glass obtained by resampling the estimated composition of 100 wt. % compare the specified (design), the calculated and theoretical formulations (table 9).

Table 9 – Chemical composition of glass

| Oxide | The contents in the glass composition |  |  |
| --- | --- | --- | --- |
|  | given | the estimated | theoretical |
| SiO2 | 62,0 | 62,0 | 61,85 |
| Al2O3 | 0,9 | 0,9 | 0,90 |
| PbO | 19,5 | 19,5 | 19,45 |
| K2O | 14,6 | 14,6 | 14,57 |
| Na2O | 3,0 | 3,22 | 3,21 |
| Fe2O3 | - | 0,0211 | 0,02 |
| Σ | 100,0 wt.%. | 100,2411 wt.h | 100,0 wt.% |

Considering the theoretical composition of the glass produced from selected raw materials, acceptable, adjust the charge composition.

Quartz sand 62,94•100 / 100,2411 = 62,79

Alumina 0,53•100 / 100,2411 = 0,53

Lead minium 22,02 •100 / 100,2411 = 22,86

Potash 13,41•100 / 100,2411 = 13,38

Nitrate potassium 15,90•100 / 100,2411 = of 15.86

Soda technical 5,37•100 / 100,2411 = 5,35

Thus, 100 mass.h. glass is produced from 120,77 wt.h. of the charge.

Output of glass (OG) in the glass formation, %

OG = 1002 / 120,77 = 82,8

Frenzy charge (FCh), %

FCh = 100 - 82,8 = 17,2

Control questions

1.Used raw materials ?

2. Chemical composition of raw materials

Safety requirements

- Before the start of classes, the laboratory should be prepared to: prepare the workplace, necessary equipment, raw materials, special clothing (gowns, gloves, goggles).

- Special caution should be observed when working with electric furnaces.

- When performing work with the glass to avoid getting it into eyes, wear protective glasses.

- In the laboratory it is prohibited to:

-Smoking and eating;

-to be outsiders;

-to leave unattended laboratory instruments.

- minutes before the end of the lessons students should gather all tools and instruments and pass them to the duty assistant. General safety requirements for training, laboratory work established in GOST 12.4.113.-82

List of used literature:

Main literature

- Бикбау М.Я. Нанотехнологии в производстве цемента. – М., 2008. –   761с.

- Таймасов Б.Т. Химическая технология вяжущих материалов: Учебник. – Шымкент: ЮКГУ им. М.Ауэзова, 2014. – 444с.

- Маневич В.Е. и др. Сырьевые материалы, шихта и стекловарение. –М.: РИФ «Стройматериалы», 2008. -224с.

- Сулименко Л.М. Общая технология силикатов. Учебник. - М.: ИНФРА, 2010. – 336 с.

Additional literature

- Классен В.К., Борисов И.Н., Мануйлов В.Е. Техногенные материалы   в производстве цемента / Монография – Белгород: Изд-во БГТУ, 2008. – 126 с.

- Бишимбаев В.К., Есимов Б.О., Адырбаева Т.А., Руснак В.В., Егоров Ю.В. Минерально-сырьевая и технологическая база Южно-Казахстанского кластера строительных и силикатных материалов. Монография. –Алматы: Раритет, 2009. -266с.

- Дворкин Л.И., Дворкин О.Л. Строительные материалы из отходов промышленности. – Ростов н/Д: Феникс, 2007. – 368с.

Laboratory work № 6

Theme lessons: Laboratory glass melting

The purpose of lessons: melting glass.

Running time of work – 3 hours

Brief theoretical information

In the laboratory different chemical composition and properties of glass are boiled in the crucible of a small capacity from 50 to 200 ml.

The great value has the correct calculation of the charge, accurate metering and careful mixing of the components of the charge, the reasonable choice of the conditions and observance of the mode of boiling.

The correct choice of crucible material depends on the glass composition and mode of melting. Glass, which does not impose special requirements on the impurity content and melting temperature which does not exceed 1450-1500°C, melting in chamotte crucibles. For melting glass containing significant amounts of oxides of boron, lead, barium, alkali metals and fluoride, used corundum crucibles, 97% consisting of A12O3. Platinum crucibles are used for melting glass, in which the presence of impurities impurities due to dissolution of the crucible material. In recent years, also used glass crucible, glass melting in this case are in a special atmosphere.

In the laboratory most often use electric resistance furnace with silicon carbide heaters allowing the temperature of 1350-1500 0C.

Equipment, tools and technical means:

- Сrucibles

- Electric furnace

- the components of the charge

The order of performance of works in the audience:

The charge loaded into the crucible before installing them into the oven. Typically, a crucible is filled half their volume, given the propensity of the mixture to foaming. To fill up in the crucible in the process of melting (once or twice) produce pre- melting with the briquettes of the charge.

When loading the crucibles in the oven make the scheme of their arrangement. This scheme is required to extract the crucibles after the end of melting  in order. At the same time in the furnace for melting glass you can set a different number of crucibles depending on the size of the furnace bottom and the crucible.

Before melting  glass set heat mode in which it is necessary to provide a rate of temperature rise, maximum temperature and duration of exposure, and the cooling furnace. Usually the thermal regime present in the form of a graph in the coordinates "temperature – time" (figure 6.1). Depending on the chemical composition of the glass temperature chart melting can vary greatly.

Figure 6.1. Temperature melting glass

When you select the heat mode melting of glass are guided by practical experience or calculation method of installing the corresponding characteristic temperatures.

The end of cooking set by visual inspection of the sample of glass is taken to a steel rod. Glass is considered welded if the sample does not contain particles of the charge, it is homogeneous and it has only individual (seldom located) large gas bubbles.

Maintenance of temperature control is usually on display. The temperature recorded in the laboratory log every 30 minutes.

Glass is formed, typically by casting. You need to have a metal table and the appropriate forms. In the laboratory a simple molded product in the form of tiles, etc. Glass moulds directly from the crucible, for which it is removed from the furnace and support the special forceps. When there is no need to produce glassware, crucibles can stay in the oven and cool along with it. If necessary, the glass can be granulated by pouring into a vessel with water with a volume of 2-3 liters.

Developed products must be subjected to annealing. The temperature of annealing can be determined by calculation. Glass is annealed in a muffle furnace. If the crucibles remain after cooking in the oven, the cooling furnace is combined with annealing. The quality of annealing is necessary to check with the help of a polariscope or polarimeter.

Developed and annealed glass is subjected to a thorough visual inspection to assess the melting properties. Especially convenient to do it on the glass left to cool in the crucibles together with the furnace. To do this, the crucible with the glass should be cut into two pieces of silicon carbide or a diamond wheel. The obtained glass cut ground and polished, after which it was visually inspected. Determine the number particles mark the sites of their accumulations, count the number of bubbles in the glass, also noting the location of their clusters, set the color of the glass and other features. At the same time study the degree of corrosion of the walls of the crucible. Usually the largest erosion is observed at the level of the surface of the glass.

If necessary, give the characteristic of the degree of homogeneity of glass by determining the temperature interval of the bundle of the glass powder when the centrifugation or dispersion of refractive indices.

Control questions

1.What is glass melting?

2. How to load the Charge in the crucible before installing them into the oven

Safety requirements

1. Before the start of classes, the laboratory should be prepared to: prepare the workplace, necessary equipment, raw materials, special clothing (gowns, gloves, goggles).

2. Special caution should be observed when working with electric furnaces.

3. When performing work with the glass to avoid getting it into eyes, wear protective glasses.

4. In the laboratory it is prohibited to:

-Smoking and eating;

- to be outsiders;

-to leave unattended laboratory instruments.

5. 5 minutes before the end of the lessons students should gather all tools and instruments and pass them to the duty assistant.

General safety requirements for training, laboratory work established in GOST 12.4.113.-82

List of used literature:

Main literature

- Бикбау М.Я. Нанотехнологии в производстве цемента. – М., 2008. –   761с.

- Таймасов Б.Т. Химическая технология вяжущих материалов: Учебник. – Шымкент: ЮКГУ им. М.Ауэзова, 2014. – 444с.

- Маневич В.Е. и др. Сырьевые материалы, шихта и стекловарение. –М.: РИФ «Стройматериалы», 2008. -224с.

- Сулименко Л.М. Общая технология силикатов. Учебник. - М.: ИНФРА, 2010. – 336 с.

Additional literature

- Классен В.К., Борисов И.Н., Мануйлов В.Е. Техногенные материалы   в производстве цемента / Монография – Белгород: Изд-во БГТУ, 2008. – 126 с.

- Бишимбаев В.К., Есимов Б.О., Адырбаева Т.А., Руснак В.В., Егоров Ю.В. Минерально-сырьевая и технологическая база Южно-Казахстанского кластера строительных и силикатных материалов. Монография. –Алматы: Раритет, 2009. -266с.

- Дворкин Л.И., Дворкин О.Л. Строительные материалы из отходов промышленности. – Ростов н/Д: Феникс, 2007. – 368с.

Laboratory work № 7

Theme lessons: Determination of the properties of air building lime

The purpose of lessons: Introduction to methods of quality assessment of lime, normalized Standards, determining the content of active oxides of calcium and magnesium content to repay grains, etc.

Running time of work – 1 hours

Brief theoretical information

Building air lime is called the product obtained from lime and lime-magnesia rocks by firing them up to possible the complete removal of carbon dioxide and consisting mainly of calcium oxide.

Building lime is produced by firing limestone or chalk. It is used for the preparation of masonry and gypsum solutions, porous and dense silicate concrete, mixed binders, for the manufacture of sand-lime brick production and construction work. Building lime consists mainly of calcium oxide. The calcination of limestone is done in shaft or rotary kilns at the temperature of 1000...1100 °C.

Under the terms of the hardening building lime is divided into:

a) air lime, ensuring the hardening of mortars and concretes and the preservation of their strength in the air conditions; .

b) hydraulic lime, which provides the hardening of mortars and concretes, saving their strength both in air and under water.

The following types of air lime:

a) lime quicklime whom;

b) ground slaked lime;

in) hydrated lime (hydrated);

d) lime putty.

Slaked lime lump is a mixture of pieces of various sizes. In chemical composition it consists entirely of CaO and MgO with a predominant content of CaО.

Slaked lime, grinded - powder-like product of fine grinding of lump lime. Lime crushed with no additives or jointly, with any active mineral additives (granulated blast furnace slag or fuel from pulverized fuel combustion, pozzolana volcanic or sedimentary origin, etc.). Active mineral additives increase the water-resistance of mortars and concretes and increase their strength.

Hydrated lime is a finely dispersed dry powder obtained damping lump or ground burnt lime a liquid or vaporous water, i.e. such amount which is necessary for the transition of CaO into Ca(OH)2. Hydrated lime consists of Ca(OH)2 and Mg(OH)2.

Lime dough is produced by slaking lump lime or ground lime with plenty of water, providing a transition of CaO and MgO hydrates to Ca(OH)2 and Mg(OH)2 and the formation of plastic doughy mass. Depending on the plasticities of the resulting product distinguish fat and lean lime.

Depending on the content of magnesium oxide are: calcium citrate with MgO content up to 5 %; magnesia, in which the amount of MgO is 5 to 20 % and dolomite with MgO content of 20...40 %.

According to GOST 9179-77 building air lime is divided into three classes: 1, 2, 3. Air the lime should meet the requirements specified in table 10.

Table 10 - Technical requirements for building air lime

| Indicators | 1st grade | 2 grade | 3 grade |
| --- | --- | --- | --- |
| The content of active Cao+MgO in terms of dry substance, % not less: - at any lime without additives | 90 | 80 | 70 |
| in lime with additives | 65 | 55 | - |
| The content of active MgO %: | 5 | 5 | 5 |
| The content of CO2,%, not more: | 3 | 5 | 7 |
| The contents inslaked grains, %, not more: | 7 | 11 | 14 |

Equipment, tools and technical means:

1. Mortar of porcelain;

2. Conical flask, capacity 250 ml; glass beads;

3. Burette, funnel;

4. hot plate;

5. Libra technical;

6. Metal container for 8...10 l;

7. The sieve №063;

8. Installation for determining the temperature and time of quenching;

9. Crucible porcelain;

10. Muffle furnace;

11. Stopwatch;

12. Analytical scale;

13. Lime construction;

14. Distilled water;

15. Hydrochloric acid according to GOST 3118-67, odnokryly solution

16. Phenolphthalein, a one percent alcohol solution.

The order of performance of works in the audience:

1 Determination of total content of active oxides of Mg and Ca.

Natural limestone or chalk contain a certain amount impurities - clay, sand, which during firing reacts with CaO to form silicates, aluminates, ferrites of calcium the following composition:

2CaO•SiO2, 2СаО•Fe203, CaO•AI2O3, 5CaO•3AI2O3 etc.

These compounds in powdered form are very slow to interact with water and, if gidratatsii lime remains in inslaked beans.When underburning lime part nepogashenija grains consist of a source of calcium carbonate. Thus, the more harmful impurities in the original carbonate and the stronger deviates the firing from optimal, the less is the content in active lime, are capable of hydration of CaO and MgO. Determination of total quantity of active Cao and MgO carried out to determine the varieties of lime according to GOST (table 10).

The sample of lime a mass of 1 g, weighed on an analytical balance, placed in a conical flask with a capacity of 250 ml and pour 150 ml of distilled water, add 3...5 glass beads or fused glass rods with a length of 5...7 mm, closed by a glass funnel or watch glass and heated for 5...7 min. to boil. The solution is cooled to a temperature of 20...30 °C, washed the walls of the flask and glass funnel (or watch glass) of boiled distilled water, add 2-3 drops of 1 % alcoholic solution of phenolphthalein and titrated with constant stirring one normal solution of hydrochloric acid until complete discoloration of the solution. Titration is considered complete if within 8 min periodic stirred the solution remains colorless.

The titration should be performed slowly by adding acid drop by drop. The content of active oxides of calcium and magnesium And in % of burnt lime is calculated by the formula:

V ·  ТСаО    · 100

А  =  -------------------------                                                                     (7.1.)

Q

where: V - volume of solution of 1N hydrochloric acid used for titration, ml;

ТСаО – titer of 1 n hydrochloric acid solution, expressed in g of CaO;

Q – weight of lime, g;

2 Determination of water of hydration

The analysis is carried out to determine the extent of hydration of lime, the rate of flow which depends on the activity of lime and time of its storage.

In the pre-calcined and weighed porcelain crucible weighed about 1 g of lime and placed for 2 hours in a muffle furnace heated to a temperature of 520±10 °C. the crucible with the charge is cooled in a sealed desiccator in the presence of moisture-absorbing substances, and then weighed. The fineness of hydrated lime is preliminarily dried at a temperature of 105...110 0C.

The content of water of hydration in percent is determined by the formula:

W=Q1Q∙100%                                                                                             (7.2.)

where Q1 -is the difference in the mass of the crucible and weighed before and after titrate, g;

Q - weight of lime, g;

3 determination of the CO2 content

The content of CO2 reflects the degree of incomplete burning of lime. The reason for underburning may be low temperature or insufficient exposure time of the material in the furnace, too much difference in the size of limestone fed to the kiln, the presence of fusible impurities. The crucible with the weighed lime, calcined at a temperature of 520±25 °C is placed in a muffle furnace, heated to a temperature of 975±25 °C for I hour. After cooling, the crucible with the charge in the desiccator, weigh produce. The CO2 content in percent is calculated by the formula:

СO2=Q2-Q3Q∙100%                                                                                    (7.3.)

where: Q - weight of lime, g (n. 2);

Q2- is the mass of sample after calcination at 520 0C, g;

Q3 -is the mass of sample after calcination at 975 0C, g;

4 Determination unslaked beans

Conducted to verify compliance with the requirements of lime GOST

9179-77.

In a metal cylindrical vessel with a capacity of 8...10 l is poured 3,5...4 liters, heated to a temperature of 85...90 0C water and pour

1 kg of lime, continuously stirring the contents until the end of intensive evaporation (boiling). The resulting dough cover with lid and allowed to stand 2 hours, then dilute with cold water to the consistency of milk of lime and washed on the sieve № 063 weak continuous jet, lightly rubbing small pieces with a glass rod with a rubber tip. Residue on the sieve is dried at a temperature of 140...150 0 C to constant weight. Outstanding the contents of the granules in percent is calculated by the formula:

O.B.=m∙1001000                                                                                                (7.4.)

5 Determination of moisture in hydrated lime

The mass of sample 10 g was placed in a previously dried to constant weight and weighed box with lid and dried in a drying

Draing cabinet at a temperature of 105...110 0C. In the drying closet should be

bucks with soda lime for CO2 capture from air. During drying cover buxa open. After 2 hours of buxa  tight-fitting lid, remove from oven, cool in a desiccator and weighed. Repeat drying until constant mass.

Time control of drying 30 minutes Moisture lime W in % is calculated by the formula:

m  -  m1

W  =  -----------------  100  ,                                                               (7.5.)

m

where: m - weight of lime, g;

m1 - weight of sample after drying, lime,

6 Determination of degree of fineness of lime powder

The mass of sample 50 g, pre-dried at a temperature of 105 to 110 0C to constant weight, sieved through sieves with meshes №02 and 008. Screening is complete, if the control sifting in the I min through the specified sieves is not more than 0.1 g of lime. The degree of dispersion of C. D., in percent figure according to the formula:

dispersion degree=m∙10050                                                                   (7.6.)

where: m is the residue on the sieve, g;

7 Determination of ultimate strength in bending and compression

The definition of the limit urgency direct bending and compression to produce samples ravine according to GOST 310.1-76, GOST 310.4-81, with the following modifications. One part of hydraulic lime mixed with three parts normal sand, pour water in the amount of about half of the total required to obtain the solution cone 110...115 mm. the Mixed mass is then cooled to 25...30 °C, add remaining amount of water to achieve solution of the specified consistency, mixed flow 2 min and transferred to a mixer.

In the bath with hydraulic gate samples, exempt from forms, stand 5...6 days above the water and 21 days in water.

8 Definition of temperature and time of slaking lime

During the blanking take the time from adding water to the beginning of the period, when the growth temperature does not exceed 0,25 °C min. Speed damping you need to know when choosing the method of slaking lime (filling with water, immersion in water, spraying water, etc.), so that the medium temperature was optimal. Too low ambient temperature dramatically reduces the speed of quenching. If too fast the heat and lack of water the hydroxide film grains, so compacted, which prevents water from entering the grain and slaked lime may be terminated when the total of incomplete hydration of the material. So lime fill with water, whereas lime is used melanogenesis periodic immersion in water or spraying water.

The speed of slaked lime depends on the following factors:

- the quantity of impurities;

- firing temperature;

- water temperature for the slaking.

During firing clay contaminated limestone formed silicates and alyumoferritnoy calcium, which promote sintering of lime, whereby the lime is obtained in the form of a thick durable pieces with a low speed damping. The rate of lime slaking (even not containing impurities) always decreases with increasing temperature and duration of roasting. This is due to the coarsening of crystals, reduce the overall surface interaction of lime with water, and the ordering of the crystal lattice of CaO, which increases the strength of the chemical bond of the ions in the lattice of CaO, the lime slowly reacts with water.

To determine the temperature and time of slaking lime use of household thermos with a capacity of 500 ml.

The weight of lime Q – grams is calculated by the formula:

1000

Q  =  ------------   ,   г                                                         (7.7.)

А

where a is the content of active oxides of calcium and magnesium in lime %.

The mass of sample is placed in a thermos flask, pour in 25 ml of water having a temperature of 20 0C and stirred quickly polished wooden wand. The flask is stoppered with a tightly inserted thermometer at 100 0C and left alone.

The mercury bulb of the thermometer must be completely immersed in the reaction mixture. Temperature readout are reacting mixture every minute, from the moment of adding water.

The definition is considered complete if after 4 minutes the temperature does not rise more than 1 0C.

The results of the experience necessary to make a conclusion (e.g., lime, 2nd grade, srednegasjashchajasja), to select the optimal method of clearing the studied lime.

9 Determining the uniformity of the volume change of lime

The soundness of lime is determined according to GOST 310.3-76. Samples of pellets prepared from a mixture of lime Portland cement according to GOST 310-76. The weight of lime 30...40 g shut water to the consistency of the dough and cooled,temperature of 25...30 °C, then add 30 to 40 g of cement add water and mix until it forms a dough normal density. For the normal density of the test taken such consistency, in which the pistil of the device the wick is immersed in the ring, filled dough does not reach the plate 7...11 mm. The resulting dough is divided into 2 equal parts for the preparation of pellets with a thickness of 0.7...0.8 cm and a diameter of 6...7 cm.

Pellet is kept in a bath with hydraulic gate for 24±2 h. Then in place with the plate is transferred to a tank on a wire rack for steaming, located at a distance of at least 3 cm above the water level.

The water in the tank is brought to a boil which is maintained for 2 h in an hour to inspect the samples. If you show signs of uneven volume changes, the test is stopped.

Lime is considered to be conforming to the requirement of uniformity of change of volume, if the surface of the pellets does not show radical cracks reaching the edges, or mesh of fine cracks increase and education of the fragile loose structure of the bread. The data obtained are entered in table 11.

Table 11 – Test results of lime

| № | The name of the sample | to number ml, HCl | The content of active СаО и MgO, % | The contents not repaid grains, % | The contents СО2, % | Grade lime |  |
| --- | --- | --- | --- | --- | --- | --- | --- |

According to the results obtained under items 1,3,4 necessary to draw a General conclusion about the grade of lime. According to paragraph 8 necessary to draw a General conclusion about the grade of lime. In paragraph 8 it is necessary to draw the schedule of dependence of temperature from time of slaking lime.

Control questions

1. What is the construction of lime?

2. At what temperature calcined lime?

3. What types of shared lime on the hardening condition?

4. Lump lime. What is the difference between them?

5. Applications building lime?

6. What is called the activity of lime and what is the method of its determination?

7. What activity and content nepogashenija grains in lime according to GOST?

8. What are not extinguished grains on the composition and what is their effect on the activity of air-hardening lime?

9. How is the speed of slaked lime?

10. How is the content nepogashenija bean? How is the humidity of hydrated lime and what is it for guests?

11. The classification of lime on the temperature and velocity damping?

Safety requirements

- Before the start of classes, the laboratory should be prepared to: prepare the workplace, necessary equipment, raw materials, special clothing (gowns, gloves, goggles).

- Special caution should be observed when working with electric furnaces.

- When performing work with the glass to avoid getting it into eyes, wear protective glasses.

- In the laboratory it is prohibited to:

-Smoking and eating;

- to be outsiders;

-to leave unattended laboratory instruments.

- 5 minutes before the end of the lessons students should gather all tools and instruments and pass them to the duty assistant. General safety requirements for training, laboratory work established in GOST 12.4.113.-82

List of used literature:

Main literature

- Бикбау М.Я. Нанотехнологии в производстве цемента. – М., 2008. –   761с.

- Таймасов Б.Т. Химическая технология вяжущих материалов: Учебник. – Шымкент: ЮКГУ им. М.Ауэзова, 2014. – 444с.

- Маневич В.Е. и др. Сырьевые материалы, шихта и стекловарение. –М.: РИФ «Стройматериалы», 2008. -224с.

- Сулименко Л.М. Общая технология силикатов. Учебник. - М.: ИНФРА, 2010. – 336 с.

Additional literature

- Классен В.К., Борисов И.Н., Мануйлов В.Е. Техногенные материалы   в производстве цемента / Монография – Белгород: Изд-во БГТУ, 2008. – 126 с.

- Бишимбаев В.К., Есимов Б.О., Адырбаева Т.А., Руснак В.В., Егоров Ю.В. Минерально-сырьевая и технологическая база Южно-Казахстанского кластера строительных и силикатных материалов. Монография. –Алматы: Раритет, 2009. -266с.

- Дворкин Л.И., Дворкин О.Л. Строительные материалы из отходов промышленности. – Ростов н/Д: Феникс, 2007. – 368с.

Laboratory work №8

Theme lessons: Determination of the normal thicness and timing of setting binders materials

The purpose of lessons:the development of methodology for determining normal consistency and setting time of cement paste according to GOST 310.2-76 (ST SEV 3920-82).

Running time of work – 2 hours

Brief theoretical information

Water requirement of Portland cement is 24...28%, pozzolanic cements with additives active mineral additives of a sedimentary origin – diatomaceous earth, silica clay, diatomite have the normal density of 32...37%. The water demand of the cement depends on the fineness of grind, the type and amount of active mineral additives.

For complete hydration of minerals of Portland cement requires about 22% water by weight of cement. Normal density of cement paste is usually above this value. Excess mixing water that is not consumed in the chemical reaction of hydration, goes on wetting the surface of the particles, is captured into the clusters of cement particles (flocal) and remains in a free form. Free water plays a role of lubricant between the particles decreases the friction between them when mixing particles. This increases the plasticity of cement paste, improve the workability, facilitates the formation of products. On the other hand, the excess free water in the stone creates a system of pores and capillaries, which leads to an increase of porosity, decrease of strength and frost resistance. Therefore, you must always seek to reduce the water requirement of cement. The less mixing water, the less the porosity and the higher strength of cement and concrete.

The speed setting is an important property of Portland cement that determines the viability of the concrete mix. Too fast or too slow the cement setting is a major shortcoming. If the cement grasped quickly, then it will not have time to make the concrete mixture and for mold product, if grasped too slow, then slow down the pace of construction, reduced turnover forms for the precast industry.

The setting time of cement depends on the chemical and mineralogical composition of clinker, fineness of grind, the kind and amount of the active mineral and chemical admixtures, the amount of dihydrate gypsum, the temperature of the environment, the amount of mixing water. With increasing fineness of grind, temperature rise, reducing the amount of mixing water setting time of cement is accelerated.

According to the requirements of GOST 10178-85 initial setting time of cement paste should occur no earlier than 45 minutes and the end of the seizure not later than 10 hours from the start of mixing cement with water. Fine clinker is characterized by a too rapid setting of concrete (3...5 minutes). Therefore, when grinding cement in a mill to control its setting time injected 3...5% dihydrate gypsum. The beginning of the call setting the time when the cement paste during hydration loses its plasticity and begins to thicken, end of setting is when the dough has completely lost its mobility, thickened, but not yet has any strength.

Determination of the normal consistency and setting time of cement paste produced with the help of the device vetch (figure 2).

The wick device has a cylindrical metal rod 2, freely moving in the cage frame 1. To secure the rod at the desired height serves as a retainer. The rod is provided with a pointer 4 for counting moving it relative to the scale 5 that is attached to the frame. The scale has divisions of 1 mm.

In determining the normal consistency cement paste in the lower part of the shaft is inserted a metal cylinder – the pistil of Tetmajer 7.

When determining the setting time the pestle is replaced by a needle 7. The pestle should be made of stainless steel wire with a polished surface without curvature. The surface of the pistil and of the needle should be clean.

The mass of the moving parts of the device remain mutual permutation of the pistil and needles. Individual parts of the moving parts of the device are selected such that their total weight was in the range of 300g.

Ring to the device, the wick and the plate on which you install the ring should be made of stainless steel, plastic or other, does not absorb water material. The shape and size of the ring shall be as specified in the figure.

The mass of the moving parts of the device remain mutual permutation of the pistil and needles. Individual parts of the moving parts of the device are selected such that their total weight was in the range of 300g.

Ring to the device, the wick and the plate on which you install the ring should be made of stainless steel, plastic or other, does not absorb water material. The shape and size of the ring shall be as specified in the figure.

Stirrer to prepare cement paste shall meet the requirements of the relevant specifications.

In the absence of laboratory mechanical stirrer to prepare cement paste used a bowl of spherical shape, made of stainless steel.

Equipment, tools and technical means:

1. Cement

2. The device the wick with a needle and pestle;

3. The ring is to device the wick;

4. Stirrer to prepare cement paste.

5. Automatic instrument for determining the setting time.

The order of performance of works in the audience:

1 Definition of normal density.

Normal density of cement find the consistency of it, in which the pistil of the device the wick is immersed in the ring, filled dough does not reach 5...7mm to plate with ring.

Normal density of cement paste characterize the amount of mixing water expressed as a percentage of mass of cement paste.

A sample of cement paste prepared according to GOST 310.1-76.

Before starting tests, check the free fall terminal device Vika and zero the instrument reading, pestle with a plate, which is a ring. When the deviation from zero of the instrument scale accordingly move.

The ring and plate before the testing is lubricated with a thin layer of engine oil.

Manual for the preparation of cement dough weighed out 400g of cement, pour into the bowl preliminary wiped with a damp cloth. Then do the cement recess, into which is poured at one time the water in the quantity necessary to obtain a cement paste of normal consistency. The recess is filled with cement and after 30 seconds mix thoroughly, and then vigorously pound the dough with a spatula.

The duration of mixing and grinding amounts to 5 minutes after adding water.

Preparation of cement paste on the mechanical stirrer is made in accordance with the attached to the mixer instructions.

After mixing, the ring quickly filled in one step cement paste and 5...6 times shake it, tapping the plate on a firm foundation. The surface of the test align with the edges of the ring, cutting off any excess dough with a knife, rubbed with a wet cloth. Immediately after this result the pistil of the device in contact with the surface of the dough in the center of the ring and fasten the core retainer, then quickly release him and give the pestle to freely sink into the batter, after 30 sec since the release of the rod take a reading dip on the scale. The ring test, the reference should not be subjected to shocks. If there are insufficient consistency of cement paste change the amount of water, and again shut up the dough, ensuring the immersion of the pistil to the depth specified above. The amount of added water to obtain a paste of normal consistency is determined with a precision of 0.25%. The data are entered in table 12.

Table 12 – Definition of normal density cement grout

| Name of cement | Date | Number definition | Weight of cement, g | The amount of water, ml | The height of the dropping of the pistil, mm | Normal density, % |
| --- | --- | --- | --- | --- | --- | --- |

2 Determination of setting time. Before starting tests, check the free fall terminal device wick as well as the zero readings. Also check the surface cleanliness and the absence of curvature of the needle. The needle of the device is brought to contact with the surface of the cement paste of normal consistency, cooked and laid in a ring. In this position fasten the stopper rod, then release the rod, allowing the needle to freely take in the dough. At the beginning of the test until the dough is in a plastic condition, in order to avoid the strong impact of the needle on the record allowed it to hold slightly when immersed in the dough. As soon as the dough thickens enough that the risk of damage to the needle will be removed, the needle is allowed to freely fall. The time of setting is determined with the free lowering of needles.

To set the start setting of needle dipped in the dough every 5 minutes, moving the ring after every dive to ensure that the needle does not hit in the same place. After each dip the needle wipe. When determining the end setting needle dipped in dough every 15 minutes.

During the test the device must be in a shaded place where there are no drafts. It should not be exposed to shocks.

The beginning of setting of cement grout consider the time elapsed from the beginning of mixing until the moment when the needle does not reach the plates on 1...2 mm, setting the end of the think time from beginning of mixing until the needle goes down into the dough is not more than 0.5...1 mm.

Determination of setting time of cement paste on the device, automatic recording is performed in accordance with the instructions supplied with the device.

The test results are entered into the table 13  in the following form:

Table 13 – Determination of setting time of cement paste

| Name of cement | Date | Definition number | The time of mixing with water, hour, min. | The time at which the needle does not reach the end by 1-2mm, hour, min. | The time at which the needle is lowered into the dough no more than 1mm, h-min | Setting time, hours min. |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | beginning | the end |

Control questions

- What is called a normal density of cement paste?

- What factors depends on the water demand of the cement?

- What is called the beginning and the end setting time of cement?

- What factors affect the setting time of cement?

- How does the amount of mixing water on the strength and other properties of cement and concrete?

- What are the requirements of GOST on the setting time of cement?

- How works the device?

- How is the determination of normal consistency of cement paste?

- How is the determination of setting time of cement paste?

Safety requirements

- Before the start of classes, the laboratory should be prepared to: prepare the workplace, necessary equipment, raw materials, special clothing (gowns, gloves, goggles).

- Special caution should be observed when working with electric furnaces.

- When performing work with the glass to avoid getting it into eyes, wear protective glasses.

- In the laboratory it is prohibited to:

-Smoking and eating;

- to be outsiders;

-to leave unattended laboratory instruments.

- minutes before the end of the lessons students should gather all tools and instruments and pass them to the duty assistant. General safety requirements for training, laboratory work established in GOST 12.4.113.-82

List of used literature:

Main literature

- Бикбау М.Я. Нанотехнологии в производстве цемента. – М., 2008. –   761с.

- Таймасов Б.Т. Химическая технология вяжущих материалов: Учебник. – Шымкент: ЮКГУ им. М.Ауэзова, 2014. – 444с.

- Маневич В.Е. и др. Сырьевые материалы, шихта и стекловарение. –М.: РИФ «Стройматериалы», 2008. -224с.

- Сулименко Л.М. Общая технология силикатов. Учебник. - М.: ИНФРА, 2010. – 336 с.

Additional literature

- Классен В.К., Борисов И.Н., Мануйлов В.Е. Техногенные материалы   в производстве цемента / Монография – Белгород: Изд-во БГТУ, 2008. – 126 с.

- Бишимбаев В.К., Есимов Б.О., Адырбаева Т.А., Руснак В.В., Егоров Ю.В. Минерально-сырьевая и технологическая база Южно-Казахстанского кластера строительных и силикатных материалов. Монография. –Алматы: Раритет, 2009. -266с.

- Дворкин Л.И., Дворкин О.Л. Строительные материалы из отходов промышленности. – Ростов н/Д: Феникс, 2007. – 368с.

Laboratory work №9

Theme lessons: Determination of air, fire and general shrinkage of ceramic products

The purpose of lessons:Qualitative determination of firing and total shrinkage

Running time of work – 2 hours

Brief theoretical information

During dry firing clays and ceramic bodies occur deeper transformation: lose residual moisture is removed chemically bound water, clay forming minerals are decomposed, their decomposition products react with each other and with nelinistit minerals, forming a fusible eutectic, which moisten the particles partially dissolve and stick together them together. The mass becomes denser, reaching maximum density, after cooling, becomes stone-like substance. These processes are accompanied by some reduction in the size of burnt clay, called firing shrinkage.

Under firing shrinkage of the clay or ceramic mass is understood as the change in linear dimensions, which undergoes a dry crock under the influence of physico-chemical processes involved in roasting. Total shrinkage is the sum of the shrinkage of air and fire.

As firing shrinkage depends not only on the mineral and chemical composition substances, the quantitative relation between them and naginatas component, but also on the firing temperature, firing shrinkage is usually determined at different temperatures: a refractory clay feel when 900, 1000, 1100, 1200, 1250, 1300, 1350 and 1410оС; refractory – at 900, 1000, 1100, 1150, 1200, and 1250 0С; low-melting – in 850, 900, 950, 1000, 1050, 1100 and 1150 0С. The average firing shrinkage for lean clays is 1 – 2% and fat to 4% (sometimes more).

Equipment, tools and technical means:

1.Drying oven with thermostat

2.Wooden gavel or laboratory roller crusher

3.Sieve No. 1

4. Bowl for kneading the clay dough

5. Measuring vessel for water

6. Glass rod

7. Desiccator

8.Plate with a rolling pin

9. Metal form with a size of 50x50 mm.

10. A sheet of thin paper

11. A sheet of glass, plastics or plywood with equal surface

12. Caliper

13. Glass cover

The order of performance of works in the audience:

To determine the firing shrinkage of the tiles used, which was determined by air shrinkage (figure 1). This is useful because the tile is already done shrink label, but also because the samples already dried. This greatly reduces the time of determination. Tiles are usually fired in the laboratory furnace, in the absence of tiles can be burned in industrial furnaces. The firing must be carried out in air or a neutral to weakly oxidized atmosphere.

Figure 9.1. The arrangement of labels on the sample to determine shrinkage.

To determine the firing shrinkage of each particular temperature, use 3 to 4 dry tile. Near burnt samples on the same level set the working end of the thermocouple or ceramic poroscopy (to control the firing temperature). The speed of temperature rise during firing in electric kilns should average 100о/hour. For brick and tile clays it is recommended that this mode of firing:

from room temperature to 150 ° C .......60 min.

from 150 to 500 ° C ..................................30 min.

from 500 to 650оС ..................................45 min.

from 650 to 1000 ° C .................................75 min.

Ends roasting the extract for 60 min at the final temperature. Cool the samples in a closed oven for several hours, then removed from the furnace, inspect (defective samples do not take into account), and a caliper with an accuracy of 0.1 mm measure the distance between the shrinkage marks.

Processing of the results

- The value of firing shrinkage is calculated according to the formula:

Lfiring shrinkage =( l1 – l2)·100/ l1 ,                                                                      (9.1)

where: l1 – distance between the labels of the dry sample, in mm;

l2– the distance between the marks annealed sample, in mm;

- Complete shrinkage is determined by the formula:

L Full shrinkage =(lо – l2)·100/ lо ,				                                                (9.2)

where : lо -is the distance between the marks fresh molded sample in mm;

l2 – the distance between the marks annealed sample, in mm;

L Full shrinkage -the tile is baked correctly and is not distorted, both measurements on each tile must match.

The relationship between these three quantities is expressed by the formula:

L firing shrinkage = L Full shrinkage – L air shrinkage			                                               (9.3)

where : L firing shrinkage - fire shrinkage,  %;

L Full shrinkage - total shrinkage,  %;

L air shrinkage – air shrinkage

Fire shrinkage, if necessary, are calculated as the difference between total and air shrinkage.

The result of the determination is recorded in table 14.

According to the obtained average data can be used to build a graph of shrinkage against temperature of roasting, lay the abscissa shows temperature and the y - axis the shrinkage in percent.

Table 14 - Form of record of results of the determination

| The name of the clay or ground | № tiles | The firing temperature is in the оС | The distance between the marks in mm |  |  | Shrinkage, % |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | initial, l0 | after drying, l1 | after firing, l2 | when drying | when roasting | full |

Control questions

- What is called a firing shrinkage, and why define it?

- What is called the full shrinkage?

- What happens during firing clay and ceramic masses?

- Than is accompanied by the roasting process?

- What determines the firing shrinkage of clay?

- Different firing shrinkage from the air and full of fire?

Safety requirements

- Before the start of classes, the laboratory should be prepared to: prepare the workplace, necessary equipment, raw materials, special clothing (gowns, gloves, goggles).

- Special caution should be observed when working with electric furnaces.

- When performing work with the glass to avoid getting it into eyes, wear protective glasses.

- In the laboratory it is prohibited to:

-Smoking and eating;

- to be outsiders;

-to leave unattended laboratory instruments.

- 5 minutes before the end of the lessons students should gather all tools and instruments and pass them to the duty assistant. General safety requirements for training, laboratory work established in GOST 12.4.113.-82

List of used literature:

Main literature

- Бикбау М.Я. Нанотехнологии в производстве цемента. – М., 2008. –   761с.

- Таймасов Б.Т. Химическая технология вяжущих материалов: Учебник. – Шымкент: ЮКГУ им. М.Ауэзова, 2014. – 444с.

- Маневич В.Е. и др. Сырьевые материалы, шихта и стекловарение. –М.: РИФ «Стройматериалы», 2008. -224с.

- Сулименко Л.М. Общая технология силикатов. Учебник. - М.: ИНФРА, 2010. – 336 с.

Additional literature

- Классен В.К., Борисов И.Н., Мануйлов В.Е. Техногенные материалы   в производстве цемента / Монография – Белгород: Изд-во БГТУ, 2008. – 126 с.

- Бишимбаев В.К., Есимов Б.О., Адырбаева Т.А., Руснак В.В., Егоров Ю.В. Минерально-сырьевая и технологическая база Южно-Казахстанского кластера строительных и силикатных материалов. Монография. –Алматы: Раритет, 2009. -266с.

- Дворкин Л.И., Дворкин О.Л. Строительные материалы из отходов промышленности. – Ростов н/Д: Феникс, 2007. – 368с.

Jumabayeva G.M., Kulmakhanova A.Sh.

METHODICAL INSTRUCTIONS

for laboratory work by discipline

«Chemistry of silicate materials»

for students of specialty 5B075300 -"Chemical technology of infusible nonmetallic and silicate materials"

Signed in printing ___________

Paper Size _______________

Typographical paper. Offset printing. Volume 3,75 p.p.

Circulation ________ copies. Order number _______

© M.Auezov South Kazakhstan State University

Publishing centre M.Auezov South Kazakhstan State University, Shymkent, Tauke khan avenue, 5