Ф.7.03-03

A.B. Issa, A.Sh.Kydyralyeva S,.A.Sakibayeva

METHODICAL GUIDELINES

FOR LABORATORY WORKS ON THE DISCIPLINE

"CHEMISTRY AND PHYSICS OF POLYMERS"

Shymkent, 2017

MINISTRY OF EDUCATION AND SCIENCE

OF THE REPUBLIC OF KAZAKHSTAN

M. Auezov South Kazakhstan State University

"Petroleum processing and petrochemistry" department

A.B Issa, A.Sh.Kydyralyeva, S.A Sakibayeva

Methodical guidelines

for laboratory works on the discipline

"Chemistry and Physics of Polymers"

for students of the specialty

5В072100 - «Chemical technology of organic substances»

Shymkent, 2017

УДК 541.6 (075.5)

ББК 24.7 Я73

A.B Issa, A.Sh.Kydyralyeva, Sakibayeva S.A. Methodical guidelines for laboratory works on the discipline "Chemistry and physics of polymers" for students of the specialty 5B072100 - "Chemical technology of organic substances." Shymkent: M. Auezov SKSU, 2017, – 40p.

Methodical guidelines worked out in accordance with the requirements of the curriculum and program course "Chemistry and physics of polymers" and include all the necessary information to implement the laboratory course.

Each laboratory is preceded by a theoretical part, which allows a deep and detailed study of the most difficult categories of course and instill students with the skills techniques study the properties of crude oil and petroleum products.

Guidelines is made for students of the specialty 5В072100 – «Chemical technology of organic substances»

Reviewers:

O.K.Beisenbayev –professor of the department “Petroleum processing and petrochemistry ”, M.Auezov SKSU.

N.O.Dzhakipbekova-     professor of the department “Chemistry and basics of chemical technology”, M.Auezov SKSU

The guideline were considered and recommended to print by the «Petroleum processing and petrochemistry" department meeting

(Minutes №3, 24.10, 2017)

And by Committee on innovative teaching technologies and methodical maintenance of Higher School Chemical Engineering and Biotechnology

(Minutes №  ,        ,   2017)

The guideline are recommended by Methodical Council of M.Auezov SKSU

(Minutes № ___ , _______ , 2017)

Responsible for issue Issa A.B

©M.Auezov South Kazakhstan State University, 2017

INTRODUCTION

The purpose of  laboratory practical work is studying of the main regularities of radical polymerization, polycondensation, process of swelling and dissolution of polymers. Before performance of laboratory practical work students are introduced with monomers, the main ways of carrying out reactions of polymerization and polycondensation, regularities of swelling of polymers. Before each work the student has to study the content of work, the device of the equipment or the device, to execute necessary calculations and to study safety regulations.

After the conversation with the teacher, from which it follows that the student clearly, clearly represents the purpose and objectives of the work, learned the methodology for its implementation, familiarized himself with the device, he is allowed to work independently. On work progress the report in the laboratory journal is made out, and the corresponding conclusions then the student is allowed to protection are given.

1 GENERAL PROVISIONS CHAIN POLYMERIZATION

In general terms, the formation of a polymer represented by the scheme:

Where М – monomer molecule;

– monomer unit;

n – degree of polymerization.

Polymers are macromolecules of the mixture differing from each other in degree of polymerization, i.e. polydisperse polymers. Therefore, polymers introduced the concept of “average molecular weight "or" average degree of polymerization”, respectively MM and DP, which are statistical value. Furthermore, this characteristic of the polymer was introduced as a molecular weight distribution (MWD).

MM and MWD are essential molecular characteristics that determine the physical and technical properties of polymers, for example, their ability to rubbery deformation.

There are several methods of determining an average molecular weight of the polymer, and the MWD polydispersity measure being defined as the ratio of weight average MW  to number average, t.е. . Polydispersion than the polymer, the broader the MWD. For many polymers, it is within 1.5-2.0. Obtain polymers having narrow MWD (1.0-1.5).

Polymerization - a process for producing polymers by joining monomer molecules using force main valences due to the rupture of double bonds or disclosure unstable cycles:С=С, С=S, С=N, С  С	С  С

\       /

О	        О  О

The main signs of polymerization:

1. Monomer molecule contains multiple bonds or unstable cycle;
2 . Process proceeds without isolation of significant amounts of by- products;
1. The polymer and the monomer are one and the same elemental composition;

2. The reaction is essentially irreversible.

Polymerization of unsaturated monomers proceeds mainly by the laws of chain reactions, and polymerization of cyclic monomers often develops as a stepwise process.

A characteristic feature of the polymerization reaction is a chain mechanism and kinetics of the process. Chain mechanism is represented as a closed reaction sequence consisting of three stages:

Initiation stage - the formation of the active site:

- Developmental stage of the reaction chain - molecular chain growth:

и т.д.

- Stage open circuit, leading to the formation of the macromolecule:

These steps are independent of each other and vary the speed and thermal effects. Chain mechanism of the polymerization reaction is characterized by the following features: 1) the monomer concentration changes gradually during the reaction, and 2) the macromolecule formed immediately (high growth rate) and the molecular weight varies little during the process, and 3) the reaction mixture contains only the monomer and polymer, the number of growing chains is about 6.10 % 4 ) increasing the reaction time increases the yield only.

Active centers of chain polymerization can be free radicals or ions. Depending on the type of the active center of the growing distinguished radical or ionic polymerization.

Reaction of active centers can be expressed by the following scheme:

2 RADICAL POLYMERIZATION

Radical chain polymerization is one of the most common methods for the synthesis of polymers. The polymerization process consists of three stages: 
1. The emergence of free radicals (initiation);

2. Growth kinetic chain;

3. Cessation of growth of macroradicals.

Free radical arises as a result of the homolytic rupture of chemical bonds and is an atom or group of atoms containing an unpaired electron.

  - Initiation

Initiation of radical polymerization is in education primary active radical of the monomer or initiator. Free radicals may be formed under the influence of heat (thermal polymerization), by the action of light (photochemical polymerization), the monomer by irradiation of high energy particles (radiation curing), and also by decomposition of special substances - initiators (chemical initiation). Chemical initiation is the most common method of initiation.

2.1.1 Chemical initiation

Initiators can be used peroxides, hydroperoxides, persulfates, azo and diazo compounds, redox systems.

Initiation of benzoyl peroxide can be represented by the scheme: 
a) thermal decomposition of peroxide to form primary radicals:

б) Interconnection of primary radicals with monomer molecule:

Initiating dinitrile azo iso-butyric acid:

The thermal decomposition of the initiator of the activation energy of the initiation stage is in the range 85-126 kJ/mol. This value can be significantly reduced to 50-84 kJ/mol using the redox system (initiator-oxidant). Used as the reducing metal salts of variable valence. Using a redox system allows to significantly reduce the temperature of polymerization. For example, decomposition of the benzoyl peroxide with salts of 2-valent iron x occurs at a temperature of 700C:

The redox system used for example in the preparation of emulsion polymerization rubbers.

2.2 Growth kinetic chain

With each act of joining one electron -monomer molecule bond valence forms -bond with an unpaired electron of the free radical and the second electron is unpaired and thereby saved the radical nature of the growing chain.

Reaction of polymer chain growth proceeds at a high speed, and characterized by low activation energy (17-42 kJ/mol). Growth rate of reaction depends both on the reactivity of the monomer, and the activity of growing macroradical. With an average MM typical elastomers chain growth process takes less than a second. During this time attached to a molecular chain of monomer molecules up to 10000.

In the presence of the substituent in the molecule are various types of monomer units join:

(«tail to tail»)

(«head to tail»)

(«head to head»)

More probable is the structure of a "head to tail." In the polymerization, for example, divinyl activation energy in the chain a 1,4 polybutadiene is 28.8 kJ/mol, and in position 1,2 - 31,6 kJ/mol:

(link 1,2)

2.3 Termination of growth Macroradicals

Cessation of growth occurs by Macroradicals chain termination and transfer of the kinetic chain.

2.3.1 Open circuit

Open circuit can occur in two ways: by recombination and disproportionation of polymer radicals.

Recombination:

Disproportionation:

Thus, the process that leads to the saturation of the final link macroradical valence and not accompanied by the formation of new radicals called chain termination. The activation energy of the reaction of chain termination is within 4,2-16,8 kJ/mol (open circuit may occur as a result of accession to the macroradicals decay products of the initiator (open on the initiator) or inhibitor (open to the inhibitor).

2.3.2 Transfer of kinetic chain

Cessation of growth of macroradicals by transferring the kinetic chain is homolytic isolation atom or group of atoms of the molecule, faced with macroradical and then became the new radical (chain transfer) with simultaneous conversion macroradical in saturated macromolecule (open circuit).

Passing through the polymer chain:

Chain transfer to monomer:

Chain transfer to solvent:

Chain transfer reactions leading to the polymer, usually in the formation of branched polymers, and the transmission chain on the monomer and the solvent - to decrease the molecular weight of the polymer.

During the polymerization reaction of diene monomers chain transfer can cause separation of the hydrogen atom as well as rupture of the double bond in a macromolecule:

With increasing conversion reaction macromolecule through the chain transfer becomes more likely, and one and the same macromolecule can participate in several reaction transmitting, acquiring new laterals that eventually accompanied by several molecules of the compound to form microgels.

2.4 Inhibitors and retarders

To prevent spontaneous polymerization of the monomers during storage and transportation use inhibitors - a substance easily reactive with the chain transfer free radical:

To prevent spontaneous polymerization of the monomers during storage and transportation use inhibitors - a substance easily reactive with the chain transfer free radical:

2.5 Regulators molecular weight

Substances which readily undergo chain transfer, but do not appreciably alter the rate of polymerization, molecular weight regulators are called. Use of regulators commonly used in emulsion polymerization of rubbers, e.g., butadiene-styrene. As regulators used diproksid di-isopropyl xanthate disulfide and tert-dodecyl mercaptan:

Action diproksid associated with the collapse of a disulfide bond:

chain growth

The use of polymerization regulators produces styrene butadiene rubbers with a molecular weight that provides a high flexibility of these rubbers.

2.6 Kinetics of radical polymerization

The total reaction rate of chain radical polymerization is a sum of its three stages:

,

where 	 - the overall rate of polymerization;

- accordingly the rate of reactions initiation, propagation and termination.

Initiation rate is determined by the decay rate of the initiator:

,

where 	 - reaction rate constant of initiation;

- initiator concentration

The rate of conversion of the monomer determines the growth rate:

где   	 - concentration Macroradicals

- monomer concentration,

Кр - a constant growth rate.

The rate of disappearance of the active centers (open circuit) depends on the rate break:

.

After a certain period of time (fixed period) equilibrium is established:

,

hence .

Macroradicals concentration can be expressed:

Converting all these expressions, we obtain the general kinetic equation radical polymerization:

;

In the stationary period monomer concentration [M] can be considered constant:

.			.

Takim obrazom, skorost' radikal'noy polimerizatsii chasto proportsional'na kontsentratsii initsiatora v stepeni ½. Eti zakonomernosti khorosho soblyudayutsya v sluchaye polimerizatsii, naprimer, stirola v prisutstvii perekisi benzoila (PB) i dinitrila azoizomaslyanoy kisloty (DAK) pri dostatochno malykh kontsentratsiyakh stirola.

Возможно, вы имели в виду: Концентрацию макро радикалов можно выразить:

Thus, the rate of radical polymerization initiator is often proportional to the degree of concentration of ½. These patterns are well-respected in the case of polymerization, for example, styrene in the presence of benzoyl peroxide (BP) and dinitrile azoizomaslyanoy acid (AIBN) at sufficiently low concentrations of styrene.

The average degree of polymerization is:

.

Thus, the average degree of radical polymerization is inversely proportional to the square root of the concentration of initiator.

2.7 Effect of polymerization conditions on the rate and properties of polymers

The polymerization conditions do not change the basic laws, however, affect the reaction rate and the molecular weight of the polymer.

1. Temperature - its influence is evident at all stages of the polymerization. With increasing temperature increases the overall growth rate and chain termination. Since the highest activation energy for the initiation stage, the increase in temperature increases the rate of formation of active centers. From the general equation that the higher the concentration of active sites, the higher the overall reaction rate

, but the higher the rate of termination

, wherein the concentration of radicals is included in the rate equation of the second degree of breakage, however increasing the speed up to breakage. Consequently, the polymer will decrease the MM.

2. The concentration of the initiator - its effect due to the change in the amount of free radicals. The higher the initiator concentration , the more active centers , and therefore higher and the rate of polymerization. The molecular weight is lowered.

3.Concentration monomer - leads to an increase in the polymerization rate and polymer molecular weight.

4. Pressure - the order of several atmospheres does not affect the polymerization process. High (3000-5000 atm or higher) and accelerates the rate of increase is not accompanied with the decrease in polymer molecular weight.

2.8 Heteropolymerization

The polymers obtained by co polymerization (heteropolymerization) of two or more monomers are called joint polymers or heteropolymers.

Macromolecules heteropolymers comprise residues of all present in the initial reaction mixture of monomers.

In the polymerization in the monomer mixture in the chain growth of molecules participating monomers are present. Composition macromolecule determined activity monomers, reactivity in the heteropolymerization process which depends on the structure of the monomer.
Several activities of the monomers in the heteropolymerization reaction coincide with the activity in the homopolymerization reactions: etc.
Radicals of these monomers are arranged in a series of activities in the reverse order. The most studied binary heteropolymerization, which involves two monomers. Initiation of monomers M1 and M2 takes place separately, and the initial radical formed two types:

Radicals attached to the initial molecule both one and the other monomer, i.e. may leak 4 chain growth reactions:

1)

2)

3)

4)

Among the most common monomers, styrene is most easily enter into the copolymerization reaction. This is explained by the increased resistance due to the radical styrene conjugation with the phenyl substituent. Monomers forming the radicals unstable less actively participate in the heteropolymerization reaction.

The ratio of the reaction rate constant with "their" monomer to the rate constant with the "alien" called monomer reactivity ratios or relative activity of the monomer.

An important determinant of the heteropolymer composition is the degree of polymerization of the monomer molecules. Particularly easy to polymerize monomers of opposite polarity.

Heteropolymerization reaction accompanied by the formation of homopolymers, the amount of which is determined by the activity of their monomers and reaction conditions.

Heteropolymerization method can control the composition of units of macromolecules to produce heteropolymers network structure.

2.9 Technology laboratory work in ampoules

Polymerization in mass (in the solvent) in sealed ampoules allows the greatest amount of study monomers and does not require complicated equipment. Heating is performed by means of ampoules thermostatic liquid (preferably water).

Loaded into a vial initiator weighed on an analytical balance. First weigh the empty vial, then the vial with the initiator. Then graduated pipette of charged amount of the monomer required.

If the polymerization is carried out in a solvent, it is immersed at first in the initiator and the monomer, and then - the solvent. Sealing vials requires caution, as this is possible flash monomer vapor or solvent. Before sealing the contents of vials should be cooled with cold water. After cooling and sealing the ampoule is agitated until complete dissolution of the initiator and a homogeneous solution was placed in a heated thermostat to the desired temperature. After the required time of the ampoule is removed from the oven and cooled rapidly.

Depending on the conditions of copolymerization, the polymer may be a liquid of various viscosities or a rubbery solid.

To isolate the contents of the opened ampoule polymer is dissolved in a suitable solvent and then the solution was poured dropwise with stirring at 5-10 fold volume of the precipitant. As wasp drivers use liquid immiscible with the solvent and monomer. If the content of the ampoule is a liquid the polymer can be precipitated without addition of solvent.

Concentration of the solution, providing optimum deposition conditions selected empirically. When you right-boron concentration of the polymer, solvent and precipitant polymer was isolated in the form of particulate or fibrous precipitate. In some cases, good results are obtained by precipitation of the polymer solution, to which a precipitant is added, until turbidity nonvanishing ing. Below are some solvents precipitators and constants for the polymers obtained (Table 1).

Table 1. Solvents and polymers of various precipitants

| polymer | solvents | precipitators |
| --- | --- | --- |
| polystyrene | and chlorinated aromatic hydrocarbons (benzene, toluene, carbon tetrachloride, etc.) | Lower alcohols, aliphatic hydrocarbons (benzene, petroleum ether, hexane, heptane, etc.) |
| Polymethyl- methacrylate | and chlorinated aromatic hydrocarbons (benzene, toluene, carbon tetrachloride, etc.) | Lower alcohols, aliphatic hydrocarbons (benzene, petroleum ether, hexane, heptane, etc.) |
| polyesters | lower alcohols, ketones, aromatic hydrocarbons, esters, | Water, aliphatic hydrocarbons, |
| formaldehyde resin | acetone, methyl and ethyl alcohols | Petroleum ether, water |

Laboratory work №1

Polymerization of styrene in weight

Objective:	familiar with laboratory techniques block polymerization of styrene under the influence of initiators. Master the technique of re-precipitation of the polymer and the determination of the molecular weight of the viscometric method. To investigate patterns of styrene mass polymerization, namely, the influence of a reaction rate, temperature, type and amount of initiator on the rate, yield and molecular weight of the polymer.

Styrene Polymerization in the mass can be carried out without heating the initiator as well as in its presence. In the polymerization process the monomer in the medium (liquid phase polymerization), it is difficult to remove heat generated during the reaction, particularly at the final stage where the viscosity increases sharply reaction medium. The larger size of the mass, the more difficult to maintain the desired temperature of the reaction. Each layer of the monomer, polymerizing under different conditions, different from the rest of average molecular weight and molecular weight distribution (MWD). To avoid this, the block polymerization is carried out at a low speed and in a small volume.

The polymerization forms a monolithic solid polymer mass (unit), which has the shape of the vessel in which the polymerization was carried out.

In the polymers obtained by block polymerization, there are no by-products, however it is most translucent and most high dielectric properties.

Block method, the transparent organic glass of styrene and methyl acrylate, as well as rubber natriybutadienovy SKB.

TASK

1. Conduct polymerization of the monomer in the conditions of one of the following options:

1.1. Low 70,80,1000 C PB or the amount of initiator AIBN 0.5 wt.% (Based on monomer), the duration 3h;

1.2. Temperature 800C, the number of initiators or PB DAK 0.3, 0.5, 0.7 wt.% (Monomer), the duration of 3h;

1.3. Temperature 800C; PB or the amount of initiator AIBN 0.5 wt.% (Based on monomer), respectively, to each tube, the duration 3h;

1.4. Temperature 800C, the number of initiators or PB DAK 0.5 wt.% (Monomer), the duration of 2,3,4 hrs

2. Each ampoule determines:

1.1. The yield of polymer in or %;

1.2. The polymerization rate in % /hr or %/min and a mol/(l∙s);

1.3. The molecular weight of the polymer viscometer method.

2. The results obtained are tabulated and graphed 2 according to the polymerization rate and molecular weight of the test factor.

3. Draw conclusions about the impact of the investigated factors on the process of polymerization of the monomer.

Example of calculation. Carried out the polymerization of styrene (molecular weight - 104, 14;  = 0,903) in mass at 700°C for 4 h with the initiator AIBN (MW-164).

In vial loaded styrene or 4 g  mol/l and 0.02 g of AIBN, or   wt.% of styrene

or	 mol/g.

The polymer yield was 1.6 g or .

The polymerization rate is:

%/ч		or	 %/мин

or

| Reagents: | Apparatus: |
| --- | --- |
| Styrene, 9d Benzoyl peroxide or AIBN - on orders Benzene, toluene or dichloroethane, 80-100 mL Ethanol (hydrolysis) or petroleum ether 400-600 ml | ampoules Microburet emk.5 ml Conical flask cap. 50-100 mL dropping funnel Ml glass emk.250 small funnel Petri dish |

Table 2. Form recording results

| Loading |  |  |  |  |  | Exit polymer |  | The polymerization rate |  | Characterization of polymer |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| monomer |  |  | initiator |  |  |  |  |  |  |  |  |
| g | mol | mol / l | g | % | mol / l | g | % | % / min |  | [] | MW |
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 |

Carrying out experience

In three vials loaded in the job specified amount of initiator and 3 g of styrene. The sealed ampoule is placed after dissolving the initiator in a thermostat at a predetermined temperature and maintained the required time. Upon completion of polymerization chilled vials opened, the polymer is dissolved in an aromatic or chlorinated hydrocarbon Scoma and precipitated in petroleum ether or alcohol, checking fullness of deposition.

The polymer was washed precipitant is filtered and dried in a pre-weighed Petri dish, first in air and then in an oven at 60 to 700C and vacuum - oven at 30 – 400C to constant weight.

QUESTIONS

to laboratory work №1

1. What is the initiator?

2. Write scheme homolytic decomposition of benzoyl peroxide, acid dinitrile azoizomaslyanoy, isopropylbenzene hydroperoxide.

3. Initiation methods.

4. Write a mechanism for the polymerization of styrene.

5. Provide examples of chain transfer to the monomer, initiator, resin.

6. Why radical polymerization rate increase is usually accompanied by a decrease in the molecular weight? In some cases, this is not observed?

7. For what purpose is held reprecipitation of the polymer?

8. Do the MM and MMP on the properties of polymers and their applications?

Laboratory work №2

Polystyrene reprecipitation. Preparation of solutions for viscometry.

Apparatus:   viscometer, thermostat, a device for installation viscometer, graduated pipette 5 ml by dividing the 0.2 ml stopwatch.

Viscometers - used Ostwald capillary viscometers Ubbelohde and diameter of 0.6-0.9 mm. To determine the viscosity of the solution of volatile compounds liquids recommended viscometers cranes with a system allowing to make the re-determination of viscosity in a closed system to eliminate evaporation of the solvent (Fig. 3).

1 - a reservoir, 2, 3, 4 - tubes 5, 7 - mark 6, 8 - beads. Figure 3. Ostwald viscometer (a) and with a suspended level Ubbelohde (b and c).

When using an Ostwald viscometer must be poured into the viscometer Vat strictly equal amount of solution (solvent) to its level in the ball was always the same. In Ref use only clean viscometer.

Thermostat. When measuring the viscosity necessary to maintain a constant temperature with an accuracy of  0,010. To measure the viscosity at low temperatures ( 15-200 C), the thermostat can be filled with water. As the thermostat can be used by a small beaker.

Preparation of the polymer. Before examining the polymer need Dimo - cleaned from impurities reprecipitation and dried to constant- mass in a vacuum enclosure. For reprecipitation the polymer is dissolved in a test tube if it is viscous, or in flat-bottomed flask , if Dy solid.

Ratio of polymer - solvent 1:3 or 1:5. To accelerate the dissolution flask can be heated in a water bath. Then, the glass with the polymer solution by glass rod to make a five to tenfold volume, the amount of precipitant. 30-40 min after exposure test for completeness of precipitation by adding 2-3 drops of precipitant.

In the case of the disappearing dregs reintroduced portion precipitant. The precipitate was separated from the precipitant dried in a drying oven at 50 – 600C to constant weight. The drying time depends on the kind and amount of sample.

Preparation of the polymer solution. To determine the molecular weight of polystyrene viscometer is recommended to use as a solvent toluene or benzene.

Preparation of 1% solution: 0.5 g of polymer is weighed with an accuracy of 0,001 g was placed in a 70 ml Erlenmeyer flask with ground stopper, and 49.5 g of solvent poured. Withstand polymer to completely dissolve at room temperature. Preparation of the solutions of 0.5, 0.25, 0.125% concentration, is carried out by sequential dilution of a 1% solution of the pure solvent.

For this purpose, a portion of 1% concentration, 15 ml, poured amount of solvent equal to slightly agitated solution, to align its concentration (bulb to be closed due to the volatility of the solvents). Then, 15 ml were taken again and the solution is diluted with 15 ml of solvent, etc. 
For preparation of a solution of 0.75% concentration to be 20 ml of a 1% solution, 6.6 mL to add some solvent. The polymer solution must not contain particulate matter that can clog the capillary viscometer. To remove them, the solution was filtered through a glass filter number 1 or number 2.

MEASUREMENT AND PROCESSING RESULTS

An important point in this paper is solvent and temperature control solutions prepared polymers. To this end, in an incubator set the desired temperature and vertically placed viscometer.

In broad viscometer knee through a glass filter number 1 or number 2, of pipette, pour 10-15 ml of solvent, and temperature control is carried out for 15 minutes to allow the solvent in the viscosimeter meter passed the thermostat. To reduce time-ter mostatirovaniya prepared polymer solutions, flat-bottomed flask with solutions (cork tightly fitting) pre-ter mostiruyut 15-20 minutes in an oven or a water bath. Water temperature in the oven and the water bath must be identical and are chosen depending on the type of solvent (constant K and . Appendix 1).

In this method, while another portion of each incubation solution viscometer reduced to 5 min.

Then determine the expiration time of the pure solvent. For this blower solvent injected into the narrow knee viscometer to fill the measuring ball. 
Washed three times with capillary and bulb, measure the flow time of the liquid between the upper and lower marks measuring ball. Expiration time of the liquid is measured by a stopwatch. From the same portion of the solvent is performed at least five determinations, as the final result of the arithmetic average taken. If the measurements differ by more than 0.2 s, respectively, they are discarded and increase the number of measurements.

For each concentration of the polymer solution is carried out 5 measurements, determine the mean value and the results are recorded in Table 4.

According to the table plot. Determined from the graph. Molecular weight calculated by substituting the value  in equation (1).

Example of calculation of molecular weight
To calculate the molecular weight of polystyrene of 104 to 107 in toluene at 250C under  К=1,3410-4	=0,71.

=1,4081,005+5,455=5,457.

=277000.

Table 4. The results of viscosity measurement

| Concentration | g / ml solvent - toluene | ср. | отн. | уд | уд/с. |
| --- | --- | --- | --- | --- | --- |
| 0,125% | 1,110-3 |  |  |  |  |
| 0,25% | 2,210-3 |  |  |  |  |
| 0,5% | 4,310-3 |  |  |  |  |
| 0,75% | 6,510-3 |  |  |  |  |
| 1,0% | 8,810-3 |  |  |  |  |

Table 5. Constant K  and management to calculate the molecular weight

the inherent viscosity of some polymers.

| Polymer | Solvent | Temperature | Area of molecular mass | К |  |
| --- | --- | --- | --- | --- | --- |
| Polybutadiene | toluene | 25 | 7104-4105 | 1,1010-3 | 0,62 |
|  | cyclohexane | 20 | 2,3105-1,3106 | 3,610-4 | 0,70 |
| Polyisobutylene | toluene | 25 | 1,4105-3,4105 | 8,610-4 | 0,56 |
| Polyvinyl | acetone | 30 | 2,7104-1,3106 | 1,0210-4 | 0,72 |
|  | Метил.спирт | 30 | 2,7104-1,3106 | 3,1410-4 | 0,60 |
| Polyvinylchloride | cyclohexanone | 25 | 1,9104-1,5105 | 2,0410-5 | 0,56 |
| Polymethyl methacrylate | acetone | 25 | 8104-3,4106 | 7,510-5 | 0,70 |
|  | toluene | 25 | 4105-3,4106 | 7,110-5 | 0,73 |
|  | chloroform | 25 | 8104-1,4106 | 4,810-5 | 0,80 |
| Polystyrene | benzene | 20 | 1,2103-5,4106 | 1,2310-4 | 0,72 |
|  | toluene | 25 | 7104-2106 | 1,3410-4 | 0,71 |
| Polyethylene | decalin | 135 | 2,5104-6,4105 | 4,610-4 | 0,73 |
|  | octane | 95 | 5104-3,5105 | 1,110-3 | 0,57 |

QUESTIONS
to laboratory work №2

1. Give a characterization of the number average, weight-average and average molecular weight.

2. Characterize the viscometric method.

3. Define the relative, specific, intrinsic viscosities.

Laboratory work №3

Emulsion polymerization of styrene

Objective:   acquainted with laboratory methods of emulsion polymerization of styrene in the presence of an initiator.

Polymerization of the emulsion widespread production method of polymers from monomers inert to aqueous environments. The process proceeds at high speed in intensive heat sink. The polymer has a high molecular weight and narrow molecular weight distribution (MWD).

Emulsion polymerization is the cheapest method of producing polymers. 
The method of emulsion polymerization under the action of radical initiators prepared polystyrene, polymethyl methacrylate, styrene-butadiene, chloroprene, nitrile rubbers, fluororubbers, synthetic latexes, etc.

Localization process in the emulsified monomer droplets (micro-volumes) allows the allocation of the polymer (rubber) by coagulation obtain a homogeneous product with average properties.

Emulsion polymerization is suitable for insoluble or poorly soluble (less than 5%) of the monomers in water. Emulsion ready-Vyatka stirring monomer in water in the presence of limited solubility in water emulsifier, which lowers the surface tension at the boundary of the monomer-water and forms a protective shell in-circle monomer droplet. When reaching a certain concentration of emulsifier molecules in an aqueous medium to form clusters, called micelles-mye. In micelles hydrocarbon chain molecules of emulsifier directed inwards, and the hydrophilic polar groups toward the aqueous medium (Fig.1).

As salts are used as emulsifiers synthetic natural fatty acids (C12-C16), saponified rosin sodium salt sulfonates, and sulfonated alkylaromatic compounds, for example sodium diizobutilsulfonaftenat (nekal). Selection of the emulsifier is determined by the properties and the stabilizing effect on the polymerization process. Emulsifier has a significant influence on the properties of the resulting polymer.

Found that remaining after coagulation of the rubber nekal reduces the strength and stickiness of styrene-butadiene rubber and resin accelerates the aging process.

As polymerization initiators currently widely used water soluble peroxides, persulfates and redox systems. Molecular weight is regulated by means of regulators.

Thus, in the simplest system consists of emulsion monomers, water, emulsifiers, initiators and molecular weight regulators. In practice, the reaction mixture has a complex composition.

As a result of mixing the emulsion and the micelle formation of the emulsion droplets, which is a monomer and the latter is adsorbed on the surface of an emulsifier. The size of these droplets is 200-500 nm. Under the influence of emulsifier’s monomer content in the aqueous phase increases considerably as its molecules penetrate micelles, settling between the hydrocarbon chains emulsifier. This phenomenon is called solubilization. No. solubilized monomer may be up to 6% (calculated on the aqueous phase).

1 - soap micelles, 2 - soap micelles solubilized monomer; 3 - polymer-monomeric species 4 - aqueous phase; 5 – dispersing monomeric particle

Fig.1. Scheme topography emulsion polymerization (for Houwink)

According to modern concepts, emulsion polymerization takes place in the soap micelles containing dissolved monomer. Although it is not excluded the possibility of polymerization in the aqueous phase of its contribution to be very small due to the low concentration of the monomer in the aqueous phase. The free radicals initiate a reaction occur in the aqueous phase, where the dissolved initiator (persulfate, peroxide), and the formed about 1,018 radicals of 1 ml per minute.

As the polymerization monomer fresh portions come into micelles of the emulsion droplets, which are soluble in the polymer to form a polymer- particle monomer. Droplets thus act as a reservoir from which monomer flows into the reaction zone. Micelles increases and eventually converted into the synthetic latex particles in which colloidal solid particles are stabilized on their surface adsorbed electrolyte.

In industrial emulsion polymerization is often carried out in a battery of serially connected polymerizer - autoclaves with stirrers. In the process, is introduced in the molecular weight regulator, and the stopper antioxidant (stabilizer). In the latter process of autoclave ends at the same depth in the monomer conversion, which enables optimum physical and chemical properties of the polymer (elastomer).

Synthetic latex obtained by emulsion polymerization, contains particles (globules) of the polymer, partially coated with a layer of the emulsifier having an electric charge, and - positive or negative - depending on the pH. The primary method is the method of isolation of the polymer electrolyte coagulation associated with the system is initially adding electrolyte (sodium chloride, magnesium) and then acid (acetic acid or sulfuric acid). Electrolyte supplements cause coagulation, facilitating convergence of particles. Acids destroy the emulsifier (it is converted from the salt form into the free acid form), whereby the charge of the particle surface decreases and the ability to coagulate.

The polystyrene was isolated as a powder, styrene-butadiene rubbers, and many other isolated as a crumb or tape.

In addition to latex coagulation electrolytes exists a method for isolating rubber latex freeze. The advantage of this method is the possibility of obtaining pure polymers and practically pure sewage. The method is implemented on an industrial scale only for obtaining chloroprene rubbers.

TASK

1. Conduct the polymerization of styrene at 700 ° C for one of the formulations listed in Table 6 for 4-5 hours.

2. Determine the yield of the polymer (in grams and %).

3. To explain the role of each component introduced into the reaction mixture (lead structural formulas).

4. Write a reaction scheme polimeratsii styrene carried out on the corresponding recipe.

Table 3. Form recording results

| Loading |  |  |  |  |  |  |  |  | Т, 0С | Time, min | exit polymer |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| monomer |  |  | initiator |  |  | emulsifier |  |  |  |  |  |  |
| wt. h | g | mol / l | wt. h | g | mol / l | wt. h | g | mol / l |  |  | g | % |
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 |

Formulation to obtain a polystyrene emulsion

| Components | Recipe number |  |  |  |
| --- | --- | --- | --- | --- |
|  | 1 | 2 | 3 | 4 |
|  | wt. h | wt. h | wt. h | wt. h |
| styrene | 100 | 100 | 100 | 100 |
| distilled water | 160 | 180 | 180 | 180 |
| Potassium persulfate (ammonium) | 0,7 | 0,1 | 0,7 | 0,7 |
| oleic acid | 6,5 | 6,5 |  |  |
| caustic soda | 1,5 | 1,5 |  |  |
| potassium stearate | 1 | 4,5 |  |  |
| Nekal |  |  | 4,5 | 4,5 |
| dodecyl |  |  |  | 0,08 |

| Reagents: | Apparatus: |
| --- | --- |
| Styrene, 10 ml Potassium persulfate (by recipe) emulsifier nekal, dodecyl alum (alyumoammoniynye) or sodium chloride (10-15% solution), 100 mL | Apparatus for emulsion polymerization Ml glass emk.200 funnel Petridishes |

Carrying out experience

In a reaction flask a solution of the emulsifier is prepared in water 700C, dropwise with good stirring, styrene and 10-15 min. administered initiator, and dissolved in a small amount of water. Polymerization was conducted at 700C for 4-5 hours, after which the emulsion was poured into a beaker where it destroys adding a solution of alum or NaCl, dropdown fracture emulsion polymer was filtered on a Buchner funnel and washed several times with distilled water. The polymer was air dried, and then - in a thermostat at 50 – 600C. Yield was determined by the formula

,

where 	Рп – weight of the polymer, the

Рм – weight of the monomer, the

QUESTIONS

to laboratory work №3

1. Summary emulsion polymerization?

2. Appointment of emulsifiers? Cause the most common types of emulsifiers.

3. The topography of the emulsion polymerization.

4. Advantages and disadvantages of emulsion polymerization over other polymerization techniques?

5. Method for the isolation of the polymer in emulsion polymerization.

6. What is synthetic latex?

7. Which polymers and elastomers prepared by emulsion polymerization of?

Laboratory work №4

Obtaining of polyester pitches of a linear structure

Н [-OR – O – OC –  – CO - ]m OH

Table 6. Formulations for the production of polyester resins with linear structure

| Components | # Recipe number |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 |
| Adipic acid | 1 | 1, 0 | - | - | - | - | 0,05 | 0,1 | - | - | - | - | 0,9 |
| Sebacic acid | - | - | 1,0 | 1,0 | - | - | 0,95 | - 0,9 | 0,95 - | - 0,9 | 0,85 | - 0,8 | - - |
| Phthalic anhydride | - | - | - | - | 1,0 | 1,0 | - | - | 0,05 | - 0,1 | 0,15 | - 0,2 | 0,1 |
| Ethylene glycol | 1,1 | - | 1,1 | - | 1,1 | - | 1,1 - | - 1,1 | 1,1 - | - 1,1 | 1,1 - | - 1,1 | 1,1 - |
| Diethylene | - | 1,05 | - | 1,05 | - | 1,05 | - | - | - | - | - | - | - |

# REFERENCE:

# 1. Calculate the amount of reagent (in grams) in accordance with a given formulation based on 0.1 moles of glycol.

# 2. Write a polycondensation reaction scheme.

# 3. Remove the kinetics of polycondensation.

# 4. Determine the yield of the polyester (in grams and% by weight) based on the results of weighing and acid number.

# 5. Draw curves acid number, the molecular weight and amount of the released water from the duration of the polycondensation.

Form recording results

Starting the process________

Еnd of process____________

ANTEOR______________

| ## Loading |  |  |  | Overall hitch | Prod. Process | ## Yield resin |  | Kinetics of |  | ## Resin characteristics |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ## Glycol |  | ## Acid |  |  |  |  |  |  |  |  |  |  |  |
| ## mole | g | #### mole | g | g | ## hour | g | Weight% of theory | From time to experience Chala | Hitch resin in | Count - in 0, n 1. ml KOH | KCHEF | Count - in water ml. | Molek. weight |

| Reagents | Apparatus |
| --- | --- |
| # glycol, an acid anhydride, benzene-alcoholic mixture (1: 1) 100 ml. KOH 0 1N alcoholic solution of 1% phenolphthalein solution in alcohol. | three-neck flask, the stirrer, thermometer, reflux condenser, Dean-Stark trap, the flask a 50 ml conical, graduated cylinder of 25 ml, 5 ml microburette, a porcelain cup. |

# Carrying out experience

# In a reaction flask were charged device acid and glycol and the instrument after assembly, the flask was gradually (over 35 - 40 min) while stirring on an air bath heated to 185 – 1950C and polycondensation is carried out at this temperature.

# To determine the kinetics of the polycondensation of 30 min, 1 , 2 , 3, and 4 hours after obtaining a homogeneous mixture in a pre-weighed flask sampled (0,3, 0,4g up to 0,0002g), which determine the acidic number. The polycondensation was stopped when the acid number of the reaction mixture reached 30 - 40. Simultaneously with the sampling point the amount of water released in a Dean - Stark. Using the values ​​of acid number calculated molecular weight and the amount of released water.

# Heated resin is poured from the flask into a porcelain dish and analyzed.

QUESTIONS

to laboratory work №4

1. Main differences from the polycondensation reaction of the polymerization reaction.

2. The average functionality of the system and its impact on the structure of polymers.

3. Laws of equilibrium polycondensation and technological factors influence the process.

4. Adverse reactions occurring in the preparation of linear polyesters.

5. To characterize the resulting polymer, methods of preparation, processing conditions, the field of preparation.

Laboratory work №5.

Study of the kinetics of polycondensation

GENERAL PROVISIONS of POLYCONDENSATION

Polycondensation is step process of the polymers synthesis of bi-and polyfunctional compounds, in which the growth of the macromolecules occurs by a chemical interaction of functional groups of the molecules of the monomers with each other and with the n-measures, formed during the reactions, as well as molecules of n-mers each other.

Characteristic features of the mechanism of polycondensation:

1. The elemental composition of the polymer is not identical with the composition of the starting monomers.

2. Chain growth occurs at the expense of functional groups which are present not only in molecules of the monomer, but also in the intermediate reaction products.

3. The reaction is reversible and often occurs with the release of side low molecular weight products.

4. Intermediates obtained during polycondensation, stable and can be isolated at any stage of the process in any way.

5. The average molecular weight depends on the degree of conversion and high molecular weight product is present only at a high degree of conversion.

For the synthesis of polymers by polycondensation using various chemical reactions, wherein as monomers - any compound containing - OH,-COOH,-CI,-NH2, etc., functional group with not less than two (Table 1).

Currently open and study new laws polycondensation reactions: polycyclisation, polycoordination, polyrecombination, oxidative dehydropolycondensation.

Completeness or depth polycondensation, i.e its degree of completion depends on the thoroughness of the removal of low molecular weight products of the reaction medium.

Called functional monomer functional groups. According to the number of reaction centers of monomers differ:

bifunctional - glycols, dicarboxylic acids;

trifunctional - glycerol;

polyfunctional - sorbitol, mannitol.

When the polycondensation is of great importance, the average functionality of the system, which determines the structure of the resulting polymer.

Average functionality f cf. determined:

,					          (7)

where 	fА, fВ, fС - functionality of the monomers A, B and C.

NА, NВ, NС – their amount in moles.

If  fср.=1, then the polycondensation monofunctional compounds are formed only low molecular weight products.

If 1 < fср ≤2, then the polycondensation of difunctional compounds only linear polymers are formed. Example - Synthesis of polyether glycols and dicarboxylic acids (Table 1).

If f ср ≥ 2, and then three tetrafunctional monomers, and mixtures thereof with bifunctional compounds in the polycondensation to form a branched or three-dimensional products. Depending on the structure of the resulting polymer distinguish polycondensation of linear and network (three-dimensional).

In linear polycondensation involving bifunctional monomers resulting in the formation of linear polymers. For conducting mesh (three-dimensional) must use the polycondensation of monomers with three or more functional groups. In this case, a spatially cross-linked polymers.

Distinguish homopolycondensation and heteropolycondensation. Homopolycondensation called reactions that involve the least possible in this case the number of types of monomers or molecules only one monomer containing two types of functional groups.

Depending on the nature of the functional groups of the starting monomers for the polycondensation are separated and gomofunktsionalnuyu heterofunctional. Gomofunktsionalnym call process that occurs as a result of interaction between the functional groups of the same chemical nature. A typical example is the synthesis of polyesters from hydroxy acids:

n HO-(CH2)6-COOH → [H-O-(CH2)6-CO-]n  –OH + (n-1)H2O

Geteropolycondensation called molecular reactions involving monomers containing various functional groups capable of reacting with each other, for example, polyhexamethylene adipamide synthesis of hexamethylenediamine and adipic acid:

nNH2-(CH2)6-NH2+nHOOC-(CH2)4-COOH →

→H-[-NH-(CH2)6-NH-CO-(CH2)4-CO-]n-OH+(n-1)H2O

To heteropolycondensation include processes involving two or more monomers, each of which is capable of forming its own resin. Thus, according to the reaction copolycondensation, held mixed polyamide synthesis of amino acids and aminoenanthic.

By the nature of the chemical processes that underlie the polycondensation reaction distinguish equilibrium (reversible) and non-equilibrium (irreversible) polycondensation.

Equilibrium, the linear polycondensation

The main symptom of equilibrium polycondensation is its reversible, ie the establishment of equilibrium between the linear polymer products and low molecular weight substances, released during the reaction.

The equilibrium constant (K) equals the ratio of the concentration of reaction products and starting materials, or their functional groups:

, 					          (8)

where	Сп, , СRСООН,  СRОН, - concentration (molar fraction) of the polymer, water, acid and alcohol in an equilibrium state, respectively (for the synthesis of polyesters).

For reversible reaction K-values ​​are in the range from a few to several dozen.

The most common reactions are the polyesterification equilibrium polycondensation (reacting diamines with dicarboxylic acids).

The equilibrium polycondensation can occur in the presence of catalysts and in their absence. Generally, when considering a polycondensation mechanism assumed that the reactivity of functional groups is dependent on the length of a molecular chain, to which it belongs, on the viscosity of the reaction medium, which increases strongly with poly - condensation.

Speed ​​linear polycondensation measured rate of change of the concentration of one of the materials consumed in the reaction of the functional groups.

The equilibrium reaction is characterized by relatively low reaction rates [10-3 10-5 l/(mol•s)] and large values ​​of the activation energy (85  170 kJ/mol), as they may be exothermic or endothermic.

Between the degree of polycondensation (X) and depth (P) derived a mathematical relationship, the fair only when the equivalent ratio of the reacting functional groups.

The depth of the reaction (F) is the fraction of reacted functional groups.

, 			(9)

where	   - respectively the initial and final number of molecules in the reaction mixture;

fcp - the average functionality of the system;

P - the depth of the reaction.

at             or

Depth conversion expressed as

(10)

The average degree of polycondensation (X) of the resulting polymer is expressed as:

,		at  fср=2

(11)

Polycondensation degree determined by the depth of conversion and linearly related to the duration of the reaction. Since the depth of the reaction is determined by its length, the length of the macromolecule naturally increases with the time of polycondensation. When raznovesnoy polycondensation maximum achievable degree of polycondensation in the absence of adverse reactions expressed by the equation:

,

where 	К – the equilibrium constant;

- mole fraction of low molecular weight substances released during the reaction.

| However, in practice during the equilibrium polycondensation degree of polycondensation reaches the limit values ​​for a number of reasons: - Because of side processes leading to deactivation of the functional groups; - Difficulties in adhering to the strict stoichiometric ratios reactive functional groups due to the presence of impurities; - The formation in the reaction system monofunctional compounds by side reactions. When conducting heteropolycondensation involving two different monomers, the most favorable conditions are created when the monomers are taken in equivalent amounts. In this case, the most high-formed products. V.V.Korshak gave a quantitative relationship between the molecular weight of the polymer and an excess of one of the monomers expressed in mol. %. Rule Nonequivalence functional groups (usually Korshak). Excess of one of the starting materials, if it is not removed during the reaction leads to a decrease in the molecular weight of the polymer to an extent proportional to the magnitude of the excess (Figure 4). The main stage of the polycondensation process is the stage of the chain. |  |
| --- | --- |
| Excess component B mol​​% | Excess of component A, mol% |

Fig. 4. Dependence of molecular weight polycondensate

the ratio of the monomers.

It defines the major characteristics of the resulting polymer - molecular weight of the polymer composition, molecular weight distribution and other properties.

The quantity of polymer molecular weight is reduced upon administration of the monofunctional substance, which inhibits another type of functional group and the process terminates polycondensation. The molecular weight of the polymer depends on the completeness of removal of low molecular weight substances side and the depth of percolation adverse reactions. Increasing the temperature accelerates the approximation of the system to equilibrium, facilitates the removal of low molecular weight reaction products. As a result, the equilibrium shifts to the side of education higher molecular weight polymers. However, increase of temperature strongly affects the degradation of the polymer and accelerates a number of undesirable side reactions that lead to the cessation of growth of the polymer chain. Among such reactions include acidolysis, aminolysis, hydrolysis, alcoholysis, cyclization:

The hydrolysis of the polyamide.

Acidolysis of the polyester.

Aminolysis polyamide.

alcoholysis polyamide

In order to reduce unwanted processes in practice is sometimes performed first polycondensation at higher temperatures, quickly reaching equilibrium, and then to further the increase in the molecular weight of the reaction mass is cooled somewhat-su. Frequently, removal of side products without the use of excessively high temperatures, resort to purge the reaction mass of the nitrogen or the application of vacuum.

Nonequilibrium polycondensation

Nonequilibrium polycondensation a process in which the conversion of functional groups and the molecular weight is not determined by thermodynamic and kinetic factors, and does not depend on the concentration of the reactants. The value of K> 103.

For non-equilibrium polycondensation include basic processes of polymer synthesis:

- Polycondensation of phenol with aldehydes - formaldehyde resin formation.

- Interaction with the polyesterification of di-acid chlorides of carboxylic acids with diols.

- Polyamidation chlorides by reacting dicarboxylic acids with diamines; obtain ethers of glycols, the synthesis of polyurethanes, polysiloxanes, etc.

When increasing the molecular weight of the polycondensation occurs slowly and gradually, and for non-equilibrium polycondensation this increase is virtually independent of the degree of removal of low molecular weight reaction products. Similarly equilibrium polycondensation, the main stage is the process of chain growth. On termination of the chain affect the physical and chemical agents - increase the viscosity of the reaction mixtures, non-equivalent ratio of the starting materials, and the introduction of monofunctional compounds of a similar nature to regulate the molecular weight of the polymer and the possibility of formation of three-dimensional structure of precipitated. In the case of an equimolar ratio of the starting monomers, kinetic equation of the process is as follows:

,									(12)

where 	К – the reaction rate constant.

Со – initial concentration of functional groups.

Р – the degree of transformation.

For non-equilibrium polycondensation reaction is characterized by high speed (up to 103K liters/mol c) low activation energy values ​​(8.38 – 41,9 kJ/mol). These processes are strongly exothermic.

Degree of polycondensation () process is inversely proportional to the relative amount of remaining in the system of functional groups.

= 1(1-Р)	 						(13)

Molecular weight distribution polymers described by the equation:

Хn = Pn-1							(14)

## where  	Х – share polymers

Р – degree of conversion

n– polymerization degree

Features three-dimensional polycondensation

In carrying out the polycondensation in the presence of one or more compounds with the number of functional groups of more than two reaction proceeds to form the branched, in the limiting case of crosslinked polymers. Connect the polymer chains into one «infinitely large» three-dimensional molecule occur by way of cross-linking.

The formation of such particles outwardly mesh expressed that some time after the start of polycondensation, the reaction mixture is separated into two parts: insoluble and soluble sol gel. This point is called the point of gelation, and the value of P, corresponding to it, the critical degree of reaction (RCR). Gel is a single macromolecular grid in which the individual chains are linked to each other chemically so firmly that the solvent is not able to separate them from each other. It is insoluble in solvents, does not cause degradation of the polymer. After reaching the gel point number sol decreases rapidly due to its transition into the gel. As a result, the viscous reaction mass is first converted into an elastic material, and then a solid infusible and insoluble product. In this process, along with intermolecular, can walk reaction between the functional groups of a macromolecule mesh.

Experimental point of gelation is defined as the point at which the reaction mixture loses its fluidity, and the period after the gel point is called curing. Relationship between gelation and the degree of reaction is derived based on the equation of Carothers.

, 			        	        (15)

where Р –the degree of completion of the polycondensation reaction;
          f ср -  average functionality of the system;

n – degree of polymerization.

When n   critical degree of reaction to the gel point (RK) is

.

If fcp = 2, Ркр = 1, only linear polymers are formed.

If  fcp =3, degree of completion of the reaction at the gel is equal to 2/3,

If  fcp =4, Ркр.=1/2 gelation reaction proceeds to only 50%.

The most known example of non-equilibrium and three-dimensional polycondensation is the synthesis of phenolic polymers. Phenol contains three active hydrogen atoms in the ortho-and para-positions, and the highest activity of the hydrogen atom at the ortho-position. Formaldehyde - a reactive bifunctional compound by the polar carbonyl group.

ОН		  Н				Н

С    =	   0			С-  +   О-

*

*

*

Н				Н

The mechanism of the reaction of phenol with formaldehyde is dependent on the ratio of components, nature of the catalyst, the reaction conditions. An excess of phenol in acidic medium flows is formed, and non-equilibrium polycondensation thermoplastic polymer of linear structure. Initial product is phenol.

ОН                       ОН                 ОН                   ОН             ОН

*

*

*

+ СН2О       -СН2ОН+	              -СН2 - 	    -ОН

Can be reacted with phenol and phenol with each other, whereby more complex molecules are formed in which the phenolic nuclei are linked by methylene bridges.

In general synthesis novolak oligomers can be represented by the scheme:

,

где п = 4 – 8.

Novolak oligomers are mixture polimergomolov large differences in the molecular weight of the individual fractions. The average molecular weight ranges from 600 to 1300, depending on the duration of the polycondensation, and the molar ratio of phenol: formaldehyde. This thermoplastic resin is softened by heating and solidifies on cooling. When this occurs no chemical changes to the structure of the polymer.

With an excess of formaldehyde in an alkaline medium for the synthesis of the polymer takes a three-dimensional non-equilibrium polycondensation thermosetting resin and formed a branched structure. In the first step, a mixture of phenol .

| OH -CH2OH CH2OH | OH HOH2C- -CH2OH CH2OH |
| --- | --- |

At elevated temperatures, phenol condensations react with each other to form methylol derivatives polimetilenfenolov (resole oligomers).

| + | OH -CH2OH CH2OH |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | OH -CH2OH CH2OH |  |  |

Resole oligomers are mixtures of linear and branched product of general formula:

H -

where n=2-5, m=4-10.

Molecular weight from 400 up to 800 - 1000. Fusible, soluble thermoset product capable when heated structured and goes into an infusible, insoluble state.

In the synthesis process takes three stages A, B and C.

Polymer from Step A (resol) is P < RRC in the reaction mass linear macromolecules prevail. Fusible polymer, soluble, but is able to move on further heating in an insoluble state.

In stage polymer (rezitol) has PRRC. Began to form a mixture. Elastic polymer, capable of softening, but insoluble.

Polymer from Step C (resite) has P>RRC strongly crosslinked structure, the polymer is insoluble and infusible.

Methods of polycondensation

Polycondensation was carried out in various ways - in solution, melt, solid-phase interfacial phase (interfacial) and emulsions.

The polycondensation in solution - method of the process in which the monomers are in the liquid phase in the dissolved state. Thus, the resulting polymer may be completely or partially soluble or insoluble in the reaction medium. The process proceeds in mild, easily controlled conditions allows the use of monomers decompose on melting. Nature of the solvent has a significant effect on the kinetics and mechanism of the addition, the solvent serves as the catalyst is solvated-controlling agent for the initial monomers, intermediates, reaction products. The disadvantage of the process is the need to regenerate the solvent, the use of the polymer only in the form of a solution or introducing an additional isolation step of the polymer.

This method is widely used in industry for the preparation of polymers used in the production of varnishes, paints, coatings, polyurethanes, polycarbonates, polyamides, and certain types of poly-ethers. Used in equilibrium and nonequilibrium polycondensation.

The polycondensation in the melt. Carried out, if the polymer and monomers are stable at the melting temperature (2000 - 4000). In order to reduce oxidation and thermal degradation of the monomers of the polymer process is performed in an inert gas. The last step was performed under vacuum. The technological process is relatively simple, enables the use of monomers with positive reactivity. Disadvantages of the method - the need to use monomers are stable at high temperatures, the difficulty of creating and maintaining a high reaction temperature. The polycondensation in the melt can be considered as a special case of solution polycondensation, wherein the solvent is one or both of the monomers. Most often it is a reversible process. However, the melt can be carried out and irreversible polycondensation - synthesis of polyesters from acid chlorides of dicarboxylic acids and diols, the synthesis of the polyurethane diisocyanates and diols.

The polycondensation in emulsion - interfacial process under way in the presence of emulsifiers. As emulsifiers, compounds of cationic, anionic or neutral. The most common emulsifier - acid sodium salt sulfo dodecanic. Disadvantage is the difficulty of purifying the polymer emulsifier. 
When emulsion polycondensation reaction to form the polymer completely occur in volume of the organic phase. Basic laws emulsion polycondensation similar patterns melt polycondensation in solution. This method only applies to the case of irreversible exothermic polycondensation processes, namely in the preparation of polyamides from aromatic diamines and dicarboxylic acids. When interfacial polycondensation polymer formation occurs at the interface between two immiscible liquids, almost entirely in the diffusion region. Reactants are dissolved separately in two immiscible liquids, with one of the liquids is water, the other - any solvent inert to the monomers and not miscible with water. The polymer is continuously removed from the reaction zone in the form of a filament or film. The agitation increases the rate of the process, the yield of polymer and its molecular weight.

The process is carried out at ambient temperature, sometimes below. This method is most widely used for the synthesis of polyesters and polyamides of dicarboxylic acid chlorides and diols or diamines, respectively.

Polycondensation in the solid phase is conducted at a temperature less than the melting point of the monomers and a polymer of 5 – 100C. The reaction is autocatalytic reaction rate depends on the crystal monomer and increases with time.

Laboratory work №6

Kinetics and determination of depth polyesterifiation

The amount of carboxyl groups present in the polymer is characterized by an acid number.

Determination of acid value at different stages of polycondensation and measurement of the released water allows us to follow the kinetics of the process.
A) The theoretical acid value (or acid number of the initial starting reaction mixture) was calculated from the ratio of the components and their molecular weights:

,

where   М- total molar weight of the starting mixture.

Acid number is determined by titration with standard procedure soluble alkali analyte sample:

or

The solvent used alcohol, spirits - or spitrto benzene - ether mixture (1: 1), acetone, and dioxane. Alkali used in the alcohol solutions.

| Reagents | Apparatus |
| --- | --- |
| solvent, KOH or NaOH, 0.1N alcoholic or aqueous solution. Phenolphthalein, 1% alcohol solution. | microburet capacity of 5 ml dimensional cylinder capacity of 50ml, 150ml capacity conical flask |

Carrying out experience
       The flask was placed 0,3-1.0 g of the test substance, the accuracy of the weighing 0, 0002 g, was added 15 - 30 ml of solvent after dissolution of the sample is titrated with 0.1N microburette alkali solution in the presence of phenolphthalein until the pink color.

Analyze two samples in parallel control experiments with the same amount of solvent. From the results, take the mean value.
The content of carboxyl groups (in %) was calculated using the formula:

where     V1 - volume with 0.1 N alkali solution consumed to titrate sample working ml;

V2 - volume with 0.1 N alkali solution consumed to titrate the control sample, ml;

F - correction factor 0, 1N solution of alkali;

0,0045     - The number of COOH - groups corresponding to 1 ml of 0.1 N sodium exactly alkali, g;

g - Hitch substance of

Acid Number - is characterized by the amount of KOH (mg) required to neutralize the carboxyl groups contained in 1 g of the analyte.
Acid number (CN) is calculated by the formula:

,

where	0,00561 – titer 0, 1N KOH, g / mol.

B) The number of released water is measured using a Dean-Stark trap. The amount of water can be calculated from the theoretical CN and CN obtained polyester. When polyesterification per 1 mol of a dicarboxylic acid 2 mol of water is released. The amount of water (X) is released in the process of producing polyester with a specific acid value (KCHEF.) equals:

,

where: m – The number of moles of dicarboxylic acid.

B) yield polyester (N) is determined or by direct weighing (weighing flask obtained polyester and an empty flask) or the difference download components and the amount of released water (amount of water is measured or calculated).

Example of calculation: Reaction mixture: 1 mol of ethylene glycol,
  0 4 moles of maleic anhydride, 0, 3 mol of phthalic anhydride, and 0 3 mol of adipic acid (KCHEF. = 140)

Solution:
The total molecular weight

М= 62 + 98 х 0, 4 + 148 х 0, 3 + 146 х 0, 3 = 189, 4г

Theoretical acid number

.

## Complete when the polycondensation reaction should stand

## 0, 4 х 1 + 0, 3 х 1 + 0, 3 х 2 = 1, 3 моль воды

Х = 1 – (140/596)  х 18 х 1, 3 = 17, 9

N= 189, 4 – 17, 9 = 171, 5 г.

LITERATURE

- Кулезнев В.Н., Шершнев В.А. Физика и химия полимеров. М.:Высшая школа, 1988, 313с.

- Тугов И.И., Кострыкина Г.И. Физика и химия полимеров. М.:Химия, 1989, 431с.

- Догадкин Б.А., Донцов А.А., Шершев В.А. Химия эластомеров. М.:Химия, 1981, 424с.

- Кирпичников В.А., Аверко-Антонович Л.А., Аверко-Антонович Ю.О. Химия и технология синтетического каучука. Л.:Химия, 1987, 424с.

- Шур А.М. Высокомолекулярные соединения. М.:Высшая школа, 1981, 656с.

- Лосев И.П., Тростянская Е.Б. Химия синтетических полимеров. 3-е изд., М.:Химия, 1971, 616с.

- Стрепихеев А.А., Деревицкая В.А. Основы химии высокомолекулярных соединений, 3-е изд., М.:Химия, 1976, 137с.

- Практикум по высокомолекулярным соединениям /Под ред.В.А.Кабанова, М.:Химия, 1985, 224с.

- Шатейштейн Л.Н. Определение молекулярных весов полимеров.-Л.:Химия, 1964.-179с.

- Торопцева А.М., Белогородская К.В., Бондаренко В.М. Лабораторный практикум по химии и технологии высокомолекулярных соединений.-Л.:Химия, 1972.-416с.

CONTENTS

| 1 | General chain polymerization ......................... | 3 |
| --- | --- | --- |
| 2 | Radical polymerization .......................................... | 5 |
| 2.1 | Initiation ........................................................... | 5 |
| 2.1.1 | Chemical initiation ........................................... | 5 |
| 2.2 | Growth kinetic chain ................................................ | 6 |
| 2.3 | Cessation of growth Macroradicals ................................. | 7 |
| 2.3.1 | Open circuit ............................................................... | 8 |
| 2.3.2 | Transfer of kinetic chain ....................................................... | 9 |
| 2.4 | Inhibitors and retarders ......................................................... | 10 |
| 2.5 | Molecular weight regulators ........................................................ | 11 |
| 2.6 | Kinetics of radical polymerization ......................................... | 11 |
| 2.7 | Effect of polymerization conditions on the rate and properties of the polymers ...................................................................... | 13 |
| 2.8 | Copolymerization ……………………………………………… | 14 |
| 2.9 | Technology laboratory work in ampoules .................................... | 15 |
| 3 | Laboratory work №1……………………………………………... | 17 |
| 4 | Laboratory work №2……………………………………………... | 20 |
| 5 | Laboratory work №3……………………………………………... | 25 |
| 6 | Molecular weight polymers and methods definition ............................................................................... | 27 |
| 7 | Laboratory work №4……………………………………………. | 33 |
| 8 | General provisions of polycondensation………………………… | 37 |
| 9 | Laboratory work №5…………………………………………….. | 54 |
| 11 | Literature …………………………………………………......... | 60 |

Issa A.B, Kydyralyeva A.Sh, Sakibayeva S.A.

Methodical guidelines

for laboratory works on the discipline

"Chemistry and Physics of polymers"

It is passed for printing ____

Paper format 60-84  1/16

Typographic paper. Offset printing. Volume 2.

Number of printed copies      . Order  № ____

© M.Auezov South Kazakhstan State University edition

Printing-multiplying workshop of M.Auezov SKSU, Shymkent, Tauke khan avenue, 5