Ф.7.03-03

Sabirov V. Kh. Sihimbaeva M.T.

METHODICAL gUIDElineS

To PRACTICAL workS for THE discipline

“Chemicalization of technological processes of textile production”

Shymkent-2017

MINISTRY OF EDUCATION AND SCIENCE OF THE REPUBLIC OF KAZAKHSTAN

M. AUeZOV SOUTH KAZAKHSTAN STATE UNIVERSITY

HIGH SCHOOL OF TEXTILE AND FOOD ENGINEERING

Department of "Technology and Design of Textile Materials"

Sabirov V.Kh. Sihimbaeva M.T.

METHODICAL Guidelines

for PRACTICAL works on the discipline “Chemicalization of technological processes of textile production”

For students of the educational program – 5b073300 "Technology and design of textile materials"

Shymkent-2017

UDK 676, 051, 2 (083.13); 677.047.42 (07)

Compiled by: Sabirov V.Kh. Methodical guidelines for practical works on the discipline “Chemization of technological processes of textile production”. - Shymkent: M.Auezov SKSU, 2017. - p. 36.

The methodical guides are compiled based on the curricula and programs of the discipline “Chemization of technological processes of textile production” and are intended for students of the educational program 5B073300 - Technology and design of textile materials.

Theoretical propositions, methods and practical recommendations for performing laboratory work are given.

Table. 17. Illustrations 12. Bibliography: 7.

Reviewer: Dzhanpaizova V.М. - K.Chem. Sc., associate professor.

Methodical guides were considered and recommended for publication by the meeting of the department "Technology and Design of Textile Materials" (Protocol No.  _   _ "_  _" _ , 2017) and the Methodological Committee on Innovative Technologies for Teaching and Methodological Support of the Higher School "Textile and Food Engineering", Minutes No. _  _ «_  _» _ .2017

Recommended for publication by the Educational and Methodical Council of SKSU. M.Auezov, Protocol No. _ __ of "__ __" __ ____ 2018

© M. Auezov South Kazakhstan State University, 2017

Responsible for the issue Sabirov V.Kh.

Contents

Introduction

1.Calculation of Dyeing Recipe | Calculation for Dyeing ............................................................6.

2. Dyeing Recipe Calculation Formula  .........................................................................................8

3. Production Calculation of Yarn Dyeing Machine .....................................................................9

4. Dip Calculation Method Followed in Textile Dyeing Industry: ...............................................10

5. Deep Calculation Example: ......................................................................................................12

6. Yarn Dyeing Machine Production Calculation Method............................................................14

7. Calculation of Dyeing Recipe | Calculation for Dyeing ...........................................................16

8.What is Lab Dip | Objects of Lab Dips | Process Sequence of  Dip...........................................18

## 9. Dyeing Recipe Calculation Formula.........................................................................................19

10.  Chemical Formula of Common Chemicals Used in Textile Dyeing .....................................20

11. How to Calculate 0.5% Dyeing Shade in Fabric.....................................................................22

12. Calculation of Package Density in Yarn Dyeing....................................................................25

13. Dyeing Calculation in Dip.......................................................................................................28

14. Production Calculation of Yarn Dyeing Machine...................................................................29

15. Calculation of Dyeing Recipe | Calculation for Dyeing .........................................................30

16.Calculation for Deep.................................................................................................................31

17. Assessment of students knowledge of  practical subjects........................................................36

Bibliography

Introduction

Coloration of textiles is an art and less complicated than actually thought;

just needs due attention to ascertain look, quality and consistency in product. Each textile is coloured with specific colourants through its own technology. Thorough realization of basics of colouration is the basic need to achieve that.

This book is an attempt to explain basics of colouration with a match in practical application precisely but in detail.

Dyeing is a process of thorough colouration of textiles, and its success lies on type and extent of pre-treatment imparted to develop good absorbency and whiteness. Other factors, viz. pH, form of textile, type of fibre, formulation of dyeing recipe, preparation of dye solution, liquor ratio, selection of machinery, etc. too play a crucial role in the process to develop levelled shades with least effort and cost. This chapter highlights these basic concepts to be kept in mind for effective implementation of technology of dyeing.

In final chemical finishing, with its great range of desired and undesired effects, the task of a textile finisher can become demanding. He or she has to consider the compatibility of the different types of finishing products and treatments, in particular their mutual influence on the desired effects. With about 20 different types of chemical finishes and several thousand finishing agents, most of which are combined to give one-bath multipurpose finishes, chemical finishing needs a solid basis of textile chemical knowledge and technical understanding as well as some practical experience. This book aims to fulfil some of these requirements.

Theme 1. Calculation of recipe for mass dyeing

Sample 1. Formulation of instrumental dyeing recipe and maintenance of optimal dyeing conditions are also the key to produce levelled shades. The recipe for a dye–fibre system should remain unchanged to reproduce a specific hue and shade. Dyeing recipe is mostly formulated with computer colourmatching system which works on the basis of stored data of dyed textiles at different concentrations for a specific dye. The stored data also helps the dyer to know cost, fastness, etc. for each recipe. To maintain quality, stock of dyes used in the database as well as required chemicals must be adequate and dyer must remain adhered to the established recipe and

conditions; adding any foreign colour may spoil the shade. Even a dye can not be substituted with a second one having the same colour index specification as the latter does not take care of the extent of dilution of various dyes after their synthesis causing variation in share of component colour in recipe. An established recipe with dyeing conditions and the dyed sample must be well-documented for reproduction of that very shade, the so-called concept of ISO-9002.

Recipe Calculation Formula :

Dye = (Shade % * Weight of the fabric in gm )/Stock solution %.
Or, required solution = WP / C

Where , W = weight of fabric, yarn, or fiber, P = shade percentage, C = concentration of stock solution, CC = cubic centimeter . 
For auxiliaries (chemicals) the formula is as below : 
Required amount of solution (mls) = (g/l required * wt of substrate * LR ) / (10 * concentration (%) of stock soln) 
For addition of auxiliaries in solids form such as salt the formula is: 
Salt in g/l = (Required amount (%) * Sample weight * LR) / 1000 
Conversion formula from percentage to g/l is as below: 
g/l = Required amount (%) * 10 .

If alkali conc. Is given in Be. then the formula to calculate this in g/l is as follows : 
Required amount of solution (mls) = (g/l required * wt of substrate * LR) / (10 * concentration (%) of stock soln )
Or , = (Required amount (%)* wt of substrate * LR) / (Concentration (%) of stock soln) 
Or, required alkali soln in c.c. = ( g/l required * wt of substrate * LR) /  (10* conversion value from Be. to g/l of alkali )
Or, required alkali soln in c.c. = (Required amount (%) * wt of substrate * LR) /  conversion value from Be. to g/l of alkali 
Calculation: Suppose a lab deep of a fabric sample (1*1 rib) has to be formed with following dyes & chemicals: 
Dyes: 
1. Rema Blue RR = 1.122% 
2. React Red KHW = 2.014% 
3. React Yellow KHW = 1.486%

- Salt = 70%

- Soda Ash (conc.20%) = 5 g/l

- Caustic Soda (38 Be) = 1.32%

- L: R = 1:8

- Sample Wt. = 5 gm

- % Stock Soln = 1

Therefore, recipe calculation for dyes and auxiliaries in g/l will be as follows : 
For dyes: 
We know, Dye = (Shade % * Weight of the fabric in gm )/(Stock solution % )
For, 
1. Rema Blue RR = (1.122*5)/1=5.61 g/l 
2. React Red KHW = (2.014*5)/1= 10.07 g/l 
3. React Yellow KHW = (1.486*5)/1= 7.43 g/l . 
For auxiliaries : 
We know,

Salt in g/l = (Required amount (%) * Sample weight * LR)/1000 
Required Salt = (70*5*8)/1000 = 2.8 gm . 
For Soda ash(conc.20%): 
We know,

Required amount of solution (mls) = (g/l required * wt of substrate * LR)/(10 * concentration (%) of stock soln )
Required amount of soda ash in C.C. = (5*5*8)/(10*20) = 1.0 
For Caustic soda (38 Be.): 
We know, required alkali soln in c.c. = (Required amount (%) * wt of substrate * LR ) conversion value from Be. to g/l of alkali

Required caustic soda = (1.32*5*8)/441 = 0.12 c.c. 
[since 38°Be.NaOH= 441 gm NaOH 100% per 1lit NaOH soln] 
Extra Water required:
= M:L – (required water to make soln of dyes & auxiliaries) = (5*8) – [(5.61+10.07+7.43) + (1.0+0.12) ] = 40 – 24.112 = 15.77 (Salt is added in solid form) 
Equipments of Recipe Section:

- Microprocessor pH Meter (Hanna Instrument)

- Digital pipette

- Digital Weighting Meter with Glass Box (Explorer, USA)

## Sample 2. Calculation of dyeing recipe are done by the dyeing master. The whole work process are done in lap dip. Lab dip is a process by which buyers supplied swatch is matched with the varying dyes percentage in the laboratory. Lab plays an important role in shade matching & and detaching the characteristics of the dyes and chemicals are to be used in the large scale of production. So this is an important task before bulk production.

Recipe Calculation Formula: 
Required Dye = {Shade percentage (%) x Weight of the fabric in gram (gm)} / Percentage (%) of Stock solution. 
Or, 
Required solution = Fw*Sp / Cs 
Where , 
Fw = weight of fabric, yarn, or fiber 
Sp = shade percentage 
Cs = concentration of stock solution

For calculating required amount of auxiliaries (chemicals) the formula is as below : 
Required amount of solution (mls) = (Gram/liquor required x Weight of substrate x Liquor ratio ) / {10 x concentration (%) of stock solution} (cc). 
For addition of auxiliaries in solids form such as salt, soda the formula is : 
Salt in gram/ liquor = {Required amount (%) x Sample weight x Liquor Ratio} / 1000 
Conversion formula from percentage to gram/ liquor is as below : 
Gram/liquor = Required amount (%) x 10 . 
If alkali concentration is given then the formula to calculate this in gram/liquor is as follows: 
Required amount of solution (mls) = (Gram/liquor required x Weight of substrate x Liquor ratio) / (10 x concentration (%) of stock solution) Or, 
Required amount of solution (mls) = {Required amount (%) x Weight of substrate x Liquor ratio} / {Concentration (%) of stock solution} 
Example of Dyeing Calculation: 
Recipe: 
Dyes:

- Rema Blue RR = 1.122%

- React Red KHW = 2.014%

- React Yellow KHW = 1.486%

Salt = 70% 
Soda Ash (concentration.20%) = 5 gram/liter 
Caustic Soda = 1.32% 
M: L = 1:8 
Sample Weight. = 5 gram 
Stock Solution (In percentages) = 1 
Therefore, recipe calculation for dyes and auxiliaries in gram/liter will be as follows: 
For dyes: 
We know, 
Required Dye = (Shade percentage (%) x Weight of the fabric in gram (gm)/percentage (%) of Stock solution. 
Calculation of dyestuff will be, for,

- Rema Blue RR = (1.12 2x 5)/1=5.61 g/l

- React Red KHW = (2.014 x 5)/1= 10.07 g/l

- React Yellow KHW = (1.486 x 5)/1= 7.43 g/l.

For auxiliaries: 
We know, 
Salt in gram/liter = (Required amount (%) x Sample weight x Liquor Ratio) / 1000 
Required Salt = (70 x 5 x 8)/1000 = 2.8 gram. 
For Soda ash (concentration 20%) : 
We know, Required amount of solution (mls) = (Gram/liquor required x Weight of substrate x Liquor ratio ) / (10 x concentration (%) of stock solution) 
Required amount of soda ash in C.C. = (5 x 5 x 8) / (10 x 20) = 1.0 
Extra Water required: 
= M:L – (required water to make solution of dyes & auxiliaries) = (5 x 8) – [(5.61+10.07+7.43) + (1.0+0.12) ] = 40 – 24.112

## 2. Production Calculation of Yarn Dyeing Machine

Dyeing is the process of adding color to textile products like fibers, yarns, and fabrics. There are several methods of dyeing. Yarn dyeing is one of them. There are many forms of yarn dyeing. Common forms are the package form and the hanks form. Cotton yarns are mostly dyed at package form, and acrylic or wool yarn are dyed at hank form.

Figure 1. Yarn dyeing production floor

Production calculation of yarn dyeing machine is given below.

Production Calculation of Yarn Dyeing Machine is carried out by following ways.
No. of Needle = π × Machine Diameter (D) × Machine Gauge (N) = 3.1416 × 30 × 24 = 2262 
Yarn Count = 30/1 Ne 
No. of Feeder = 96 
Machine RPM = 28 
Stitch length = 3 mm 
Efficiency = 85% = 0.85 
Shift = 8 hr. = 8 × 60 = 480 min 
                             No. of Needle x No. of Feeder x Stitch length (mm) x RPM x Shift x Effi. 
Production/Shift = …………………………………………………………………..…..…………
                                                        10 x 2.54 x 36 x 30 x 840 x 2.206 
      2262 x 96 x 3 x 28 x 480 x 0.85 
= ……………………………………………………. = 146.407 Kg
    10 x 2.54 x 36 x 30 x 840 x 2.206 
Production of the machine is 146.407 Kg/Shift. 
Note: If any parameter in this calculation is changed then production capacity per shift will be changed.

## How to Calculate Dyeing Recipe in Textile Wet Processing Sector?

Dyeing Recipe Calculation:

Dyeing recipe calculation is not a tough task that we have normally seemed. The person who is engaged in textile dyeing industry has to know the dyeing recipe calculation method to dye the fabric perfectly. This article has presented an easy method for calculating dyeing recipe calculation in textile wet processing sector.

3. Dip Calculation Method Followed in Textile Wet Processing

The below equipment’s has needed to calculate the dyeing recipe in textile wet processing industry.

- Digital weighting meter with glass box (Explorer, USA),

- Digital pipette,

- Microprocessor pH meter.

Dyeing Recipe Calculation Formula:

Required amount of dye =

(Weight of the fabric in gram × Shade percentage)

=………………………………………………………………

Percentage of Stock solution

Or,

Required amount of solution,

Fw × Sp

=……………………

Cs

Where,

Fw indicates the weight of yarn, or fiber or fabric.

Sp indicates the shade percentage,

Cs indicates the concentration of stock solution.

2. Auxiliaries or Chemicals Calculation Formula:

The below formula has to follow to calculate required amount of auxiliaries or chemicals.

Required amount of solution (mls),

(Weight of substrate x Gram per liquor required x Liquor ratio)

=………..……………………………………………………………………

(Concentration percentage of stock solution× 10)

3. Additional Auxiliaries Calculation Formula:

Formula for addition of auxiliaries in solids form such as salt, soda is:

Salt in gram per liquor,

Sample weight x Liquor Ratio× required amount (%)

=………………………………………………………………………

1000

4. Percentage to Gram Conversion Calculation Formula:

Conversion formula from percentage to gram/ liquor is in the below:

Gram per liquor,

= Required amount in percentage x 10

If alkali concentration is given then the below formula has to follow for calculating this in gram per liquor:

Required amount of solution (mls),

(Weight of substrate x Gram per liquor required x Liquor ratio)

=……………………………………………………………………………….

(10 x Concentration percentage of stock solution) Or,

Required amount of solution (mls),

Weight of substrate x Liquor ratio× required amount (%)

= ……………………………………………………………………….

Concentration percentage of stock solution

Deep Calculation Example:

Recipe:

Dyes:

- Rema Blue RR = 1.122%

- React Red KHW = 2.014%

- React Yellow KHW = 1.486%

Chemicals:

Soda Ash (concentration.20%) = 5 gram/liter

Sample Weight. = 5 gram

Caustic Soda = 1.32%

Salt = 70%

Stock Solution (%) = 1

M: L = 1:8

Now, calculate the required recipe for dyes and auxiliaries or chemicals in gram per liter.

Solution:

In case of dyes,

We know,

Required amount of dye,

(Weight of the fabric in gram × Shade percentage

=……………………………………………………………………

Percentage of Stock solution

Calculation of dyestuff will be,

For,

- Rema Blue RR = (1.12 2x 5)/1=5.61 g/l

- React Yellow KHW = (1.486 x 5)/1= 7.43 g/l,

- React Red KHW = (2.014 x 5)/1= 10.07 g/l

In case of auxiliaries or chemicals,

We know,

Salt in gram per liquor,

Sample weight x Liquor Ratio× required amount (%)

=……………………………………………………………………

1000

5×8×70

=……………………….

1000

=   2.8gm

So, required amount of salt is 2.8gm

In case of Soda Ash (Concentration 20%):

Required amount of solution (mls),

(Weight of substrate x Gram per liquor required x Liquor ratio)

=……………………………………………………………………………………….

(10 x Concentration percentage of stock solution)

5×5×8

=……………………= 1 ml

10×20

So, required quantity of soda ash in c.c stands at 1.0

Extra Amount of Water Required:

= M: L – (Required amount of water to make solution of auxiliaries and dyes)

= [(5 x 8) – {(5.61+10.07+7.43) + (1.0+0.12)}] = 40 – 24.112 = 15.77

So, 15.77 amount of salt is added in solid form

- Yarn Dyeing Machine Production Calculation Method

Yarn dyeing is slightly difference from woven or knit dyeing. Yarns are dyed in package form or hank form by yarn dyeing process. Dyeing process can be vary depending on the individual procedure of a textile engineer or a dyeing master. Dyed yarns are used for making stripe knit or woven fabrics or solid dyed yarn fabric or in sweater manufacturing. Yarn dyeing starts from soft winding to packaging. Here production parameters of all section of yarn dyeing are point out below.

Production Calculation of Yarn Dyeing Machine 
No. of Needle = π × Machine Diameter (D) × Machine Gauge (N) 
= 3.1416 × 30 × 24 = 2262 
Yarn Count = 30/1 Ne 
No. of Feeder = 96 
Machine RPM = 28 
Stitch length = 3 mm 
Efficiency = 85% = 0.85 
Shift = 8 hr. = 8 × 60 = 480 min 
                               No. of Needle x No. of Feeder x Stitch length (mm) x RPM x Shift x Effi. 
Production/Shift = …………………………………………………………………..…..……
                                                        10 x 2.54 x 36 x 30 x 840 x 2.206 
      2262 x 96 x 3 x 28 x 480 x 0.85 
= …………………………………… = 146.407 Kg

10 x 2.54 x 36 x 30 x 840 x 2.206 

Production of the machine is 146.407 Kg/Shift.

Depth of shade, auxiliaries, stock solutions, & water ratios

Colour Strength is expressed as Depth of Shade. (D.O.S) which is calculated as the amount of dye as a percentage of the weight of fibre (W.O.F).  e.g 1gm dye to 100gms fibre = 1% Depth of shade.

The strength of colour does vary considerably on many dyestuffs. To determine the colour value produced by a particular amount of dye per weight of fibre you can use the following guidelines. 0.5%(D.O.S)  lighter shades, 1% D.O.S  medium shades and 2% to 4% (D.O.S) deep stronger shade.

To make calculations easier to work out we use the metric system.

Calculating Dye Quantities…fibre weight x (%D.O.S) divided by 100

Example 1. 125gms yarn dyed to 2% D.O.S.  how much dye required ?

Multiply  125gms x 2 = 250gm divide by 100 = 2.5gms dye.

Example 2. 300gms fibre dyed to 3% D.O.S. how much dye required ?

Multiply 300 gms x 3 = 900 divided by 100 = 9gms dye

Auxiliaries

|  | Light shades | Medium shades | Strong shades |
| --- | --- | --- | --- |
| Citric Acid | 1%(W.O.F) | 1.5%(W.O.F) | 2% (W.O.F) |
| Glaubers Salts | 2%(W.O.F) | 5%(W.O.F) | 10%(W.O.F) |
| Lyogen NH | 1%(W.O.F) | 1.5%(W.O.F) | 2%(W.O.F) |

Stock Solutions

This can be described as a specific amount of dye powder dissolved in a particular amount of water. Stock solutions are a great time saver as you can make a batch which you can use many times over until it runs out. It is easier to use the stock solution than to measure small quantities of dye powder every time, and when trying different D.O.S for certain colours you can easily measure the amount of stock solution for that colour. Just make sure you label & record what your solutions contain.  You can now measure small quantities easier & accurately.

Most stock solutions will last 3-6 months stored away from sunlight. Some do not last that well and their effectiveness may only be 1-2 weeks.

Calculating a 1% Stock solution

Please note: if you wish to avoid lengthy calculations, use 1% stock solutions.

1% stock solution is the total volume of stock solution required divided by 100.

Calculating 1% stock solution for 1000gm (1kg) fibre. Here, you change the measurement of weight to volume eg 1000gm to 1000mls. You would therefore add 10gms dye (1%) to 1000mls water to make the 1% stock solution.

To mix a 1% stock solution

Example 1.  500mls of stock solution… divide 500 by 100 x 1= 5gms dye.

Example 2   800ml stock solution…divide 800 by 100 x 1 = 8gms dye.

Both examples have a dye strength of 1% depth of shade. (D.O.S)

To calculate the amount of 1% stock solution required per dye lot.

Make stock solution using a 1000ml (1 litre) 1% Stock solution.

Example 1.   (W.O.F) 120gms divided by 1(% D.O.S.)= 120 mls

Example 2.   (W.O.F) 350gms divided by1=350 x 2(% D.O.S)  = 700mls.

Example 3.   (W.O.F) 55gms divided by 1= 55 x 3(% D.O.S)  = 165 mls

If you wanted to change the formula to another % of stock solution then you would simply follow the same formula .eg 2% stock solution = 20gms dye per 1000 mls water.

Albegal Set Stock Solutions

Albegal Set is measured at 1- 2% (W.O.F). 1% light shades , 2% heavy shades.

Eg to 1000mls water add 2% Albegal set =20gms. Shake mixture well every time it is used as with all stock solutions.

Water Ratios

Use a ratio of 20:1 for fibres such as wool and alpaca.

Example: 1kg (1000gms) fibre x 20 = 20litres. If this does not cover the fibre adequately then increase rate to 30:1.Bulky fibres such as silk require a water ratio between 30:1 & 40:1.

How do calculate the yarn consumption of a Yarn dyed t-shirt? Merchandising, LearashionToday we will learn how we can book the yarn for bulk dyeing. Suppose, you receive a yarn dyed t-shirt order from buyer. Details as below Style: 100% cotton, Single jersey, 160 gsm yarn dyed round neck t-shirt.

Color:  Beige/Navy (only one combo)

Quantity: 10,000 pcs (in four sizes, S, M, L & XL)

Stripe: Beige 7 cm & Navy 1.5 cm (Total 8.5 cm)

Body length: 73 cm

Sleeve length: 19.5 cm

½ Chest: 52 cm

Consumption: 2.78 kgs/dozen (considering total wastage 18%) you may use this for pricing. Normally the wastage of yarn dyed garments depends on styling.  Normal wastage for yarn dyed:

Dyeing (yarn) wastage: 6%

Knitting wastage: 3%

Wash wastage: 5%

So, you should need 116 kgs yarn to produce 100 kgs fabric But be careful, during the bulk yarn booking you should booked the yarn based on the consumption you got by using pattern & marka. Some time I saw buyer asked for match the body stripe with sleeve then the cutting wastage become more than 5%.

We know the body length is 73 cm

Where, beige color stripe is 7 cm

And Navy color stripe is 1.5 cm

Then total length of one repetition is 8.5 cm

So, we need total (73/8.5) = 8.58824 repletion to complete a body (but here we will count 9 repetition for cutting & sewing wastage.)

So, total sum of Navy stripe will be (1.5 cm X 8.58824) = 12.8824 cm

And total sum of Beige color stripe will be (7 cm X 8.58824) = 60.1177 cm

So, 12.8824 cm + 60.1177 cm = 73 cm (total body length)

Now we just calculate the percentage of each color in a body

Navy color percentage in the body will be

= (12.8824 ÷ 73) %

= 17.65 %

= (60.1177÷73) %

= 82.35 %

= 17.65 + 82.35

= 100 %

So, now if the consumption is 2.78 kg

Then

Navy color will be = 0.49067 kg ( 2.78 kg X 17.65% )

And Beige color will be = 2.28933 kg ( 2.78 kg X 82.35% )

In this above way you can booked the yarn

Calculation of Lab Dip | Working Process in Lab Dip

Dip.

Lab dip is a process by which buyers supplied swatch is matched with the varying dyes percentage in the laboratory with or without help of “DATA COLOR” .

Lab dip plays an important role in shade matching & and detaching the characteristics of the dyes and chemicals are to be used in the large scale of production. So this is an important task before bulk production.

Common Stock Solutions:

Red – 0.1%, 0.5%, 1.0%, 2.0% (very common)

Yellow – 0.1%, 0.5%, 1.0%, 2.0% (very common)

Blue – 0.1%, 0.5%, 1.0%, 2.0% (very common).

Preparation:

To prepare 0.1% Stock solution, it is necessary to mix 0.1 g dye and 100 cc water.

To prepare 0.5% Stock solution, 0.5 g dye stuff is mixed with 100 cc water.

To prepare 1.0% & 2.0% Stock solution similar procedure is followed.

To prepare 10% Stock solution of Soda ash, 10 g Soda is mixed with 100 cc water.

Depth of Shade:

0.5% to 5% shade for the goods.

Dip Calculation:
Usually following calculations are followed:

Dye Solution = (Shade % * Sample Weight) / (Stock solution %)   (cc).

Salt = (Shade % * Liquor) / 1000  (gram per liter, gpl).

Soda Solution = (Shade % * 100 * Liquor) / (1000 * Stock solution %)    (cc).

Sample Calculation for 0.5% Shade:

Sample wt. = 5 mg

Material liquor ratio = 1: 10

Total liquor (5 * 10) = 50 cc

Dye solution required = (5 * 0.5%) / 1% = 2.5 cc

Salt solution required = (50 * 25) / (20 * 10) = 6.25 cc

Soda ash solution required = (50 * 10) / (20 * 10) = 2.5 cc

Water required {50 – (2.5 + 6.25 + 2.5)} = 38.75 cc

Working Procedure in Dip:

All ingredients had been taken according to the recipe into the pot of sample dyeing machine. At a room temp the material had run then after 10 minutes started to rise the temperature at 1°C/ min. to get 60°C temperature. For performing the required dyeing temperature it took 30 minutes. The material had dyed at 60°C for 45 minutes. Then the temperature was reduced at room temperature within in 10 minutes. The fabric washed in cold water & then the material was washed in 1 gm/l soap solution (liquor ratio 1:20) at 90°C temperature for 15 minutes. Then after rapidly cold washing the material was dried & preserved. And then check the shade match with the required sample by the lighting box. Then send to buyer or merchandiser for approval.

Working Procedure of Sample Dyeing (Knit Dyeing Section):

Normally a textile dyeing mill get offer through merchandiser. Merchandising department of dyeing mill send the swatch to the central dyeing lab. Then the lab manager makes of analysis the color of swatch with the help of spectrophotometer. After shade matching three samples are submitted to the buyer or buyer agents. If sample is approved by the buyer then this sample recipe are sent to floor for bulk production. The dyeing master dyeing the sample for bulk production. Now I will give the flowchart of sample dyeing for bulk production.

(Scouring and Bleaching)

Water load in sample dyeing machine
↓
Fabric load
↓
Temperature raised in 50 *C
↓
Scouring chemical added (dosing time 10min)
↓
Temperature raised in 60 *C
↓
NaOH dosing ( dosing time 5min)
↓
Temperature raised in 70 *C
↓
Hydrogen Peroxide dosing (dosing time 10min)
↓
Temperature raised in 100-110 *C and running at 30min
↓
Cooling at 80 *C
↓
Ringe or normal wash (10min)
↓
Drain out
↓
New water load
↓
Temperature raised in 55 *C
↓
Add acid + OEM ( for destroying Hydrogen Peroxide power)
↓
pH check and obtain 4.5 by adding acetic acid
↓
Enzyme is added and run time 60 min
↓
Sample check if approved by in-charge
↓
Rinse (run time 15min)
↓
Drain out

(Dyeing)

New water load
↓
pH check and obtain 5.6 by adding acetic acid
↓
Temperature raised at 50-55 *C
↓
Dyeing auxiliaries added (leveling agent, anti creasing agent, sequestering agent etc)
↓
Salt added and running at 10-min
↓
Color is added and dosing time 30 min ( Reactive dye, Disperse dye, Acid dye etc)
↓
Running time 25 min
↓
Temperature raised at 60 *C
↓
Soda ash (dosing time 35 min)
↓
Sample cutting for checking after 10 min later
↓
If approve then rinse at 20 min
↓
New water load
↓
Add acetic acid for neutralization at 40 *C and run at 10-min
↓
Rinse at 5 min
↓
Drain out
↓
New water load
↓
Temperature raised at 90-95 *C and 10 min running
↓
Cooling at 80 *C
↓
Rinse ( for cut sample)
↓
Shade checking if approve by in-charge then
↓
Rinse and running at 15 min
↓
Drain out
↓
New water load
↓
Temperature raised at 30 *C
↓
Fixing agent added ( GG-100, ECO, CR) and dosing time 10-min
↓
Rinse ( 10-min)
↓
Drain out
↓
New water load
↓
Temperature raised at 40 *C
↓
Softener added and run time 30 min
↓
Shade matching if approve then
↓
Fabric unload

- Work in the dip

Procedure for Lab dip by the Different Dyestuff in the Laboratory:

Procedure for 100 % Cotton Fabric:

1. Calculate the recipe.
2. Weight the fabric.
3. Take the beaker keep the fabric in to the beaker.
4. Then the dyes, chemicals & required amount of water take in to the beaker by the digital pi-petting.
5. Then weight the salt by the electric balance and add in to the beaker.
6. Then the beaker set in to the lab dyeing machine for dyeing.
7. Start the program for dyeing the whole dyeing time 60 min at 60 °C temperature. (The dyeing time and temperature depends on which classes of dyes are used for dyeing.)
8. After 30 min add the then add the soda ash. By pi-petting.
9. Again run the program next 30 min at the same temperature.
10. Finished the dyeing time then the sample taken from the beaker first hot wash & then cold wash.
11. Then acid wash as for neutralization.
12. Then soaping required soap solution 10 min at 90° C temperature.
13. after the fabric again cold.
14. Then dry the lab dip and compare with the standard.

- What is Lab Dip | Objects of Lab Dips | Process Sequence of Lab Dip

A lab dip is a swatch of fabric test dyed to hit a color standard. It is a process by which buyer’s supplied swatch is matched with the varying dyes percentage in the laboratory with or without help of spectrophotometer. Lab dip plays an important role in shade matching & this is an important task before bulk production. In previous article of this author we have to learn on flow chart on dyeing lab.

Practical dip

There are different matching systems followed in Labs. They are :

Tube light matching.

Sun light matching.

Ultra Violet matching.

Sodium light matching (show room).

Object of Lab Dip:

The main objectives in lab dip are as follows:

To calculate the recipe for sample dyeing.

To compare dyed sample with swatch by light Box or Spectrometer.

To calculate revise recipe for sample dyeing.

Finally approved Lab Dip (Grade: A, B, C & D)

Process Sequence of Lab Dip:

Lab dip plays an important role in dyeing process. Bulk dyeing process completely depends on the lab dip development work. Lab dip is completely managed as the following sequence.

Lab Dip Requisition from buyer
↓
Entry in the computer
↓
First recipe is given by swatch/pan-tone number
↓
First correction
↓
Second correction
↓
Grading of sample (A, B, C, D)
↓
Yarn and knit sample send to buyer
↓
Approved by buyer
↓
Order for bulk production
↓
Production card with approved sample and recipe send to production section

Process Flow Chart/Sequence of practical

At first dyeing is performed in dyeing laboratory and then starting for bulk production. A lots of work is done in the dyeing laboratory. In the dyeing lab, lab dip or sample is developed by the dyeing master. Lab dip plays an important role in shade matching & this is an important task before bulk production.

Process Sequence of Dyeing practical:

Sample/Swatch/Panton no. / TCX no. / TPX no. from the buyer
↓
Determination of sample’s possible color combination by the help of Spectrometer or manual
↓
Dispersion by autodoser
↓
Trial dyeing of first recipe
↓
Unload
↓
Normal wash
↓
Hot wash with detergent
↓
Oven drying
↓
Ironing
↓
Shade matching in light box ( If Ok then send to buyer for approval)
↓
If not ok
↓
First correction takes from Spectrometer or manually
↓
Dispersion by auto-doser
↓
Trial dyeing of first recipe
↓
Unload
↓
Normal wash
↓
Hot wash with detergent
↓
Oven drying
↓
Ironing
↓
Shade matching in light box ( If Ok then send to buyer for approval)
↓
If not ok
↓
Second correction takes from Spectrometer or manually
↓
Dispersion by auto doser
↓
Trial dyeing of first recipe
↓
Unload
↓
Normal wash
↓
Hot wash with detergent
↓
Oven drying
↓
Ironing
↓
Shade matching in light box
↓
If ok
↓
Send for buyer’s approval
↓
Bulk production by considering the buyer’s approved sample as standard

Note: This procedure is applicable for yarn or fabric dyeing.

7. Chemical Formula of Common Chemicals Used in Textile Dyeing

Textile dyeing is a combination of some series processes such as scouring, bleaching, dyeing and after treatment which can be carried out at different stages of fiber processing in different forms like staple, yarn, fabric etc. In dyeing process lots of chemicals require. To become a successful dyeing engineer or dyeing master you should know some chemical formula which are widely used in different stages of dyeing.

Chemical Name and Their Formula:

Water = H2O

Hydrochloric Acid = HCl

Sulfuric Acid = H2SO4

Phosphoric Acid = H3PO4

Sodium Chloride (common salt) = NaCl

Sodium Carbonate = Na2CO3

Sodium Sulfate (Glauber salt) = Na2SO4

Sodium Bicarbonate = NaHCO3

Sodium Hydroxide = NaOH

Potassium Hydroxide = KOH

Sulfur Dioxide = SO2

Trisodium Phosphate = Na3PO4

Benzene = C6H6

Acetic Acid = CH3COOH

Oxalic Acid = (COOH)2

Cellulose = C6H10O5

Starch = C6H10O5

Hydroz (Sodium Hydrosulfite) = Na2S2O4

8. How to Calculate 0.5% Dyeing Shade in Fabric

Preparation:

To prepare 0.1% Stock solution, it is necessary to mix 0.1 g dye and 100 cc water.

To prepare 0.5% Stock solution, 0.5 g dye stuff is mixed with 100 cc water.

To prepare 1.0% & 2.0% Stock solution similar procedure is followed.

To prepare 10% Stock solution of Soda ash, 10 g Soda is mixed with 100 cc water.

Calculation: 
Usually following calculations are followed - 
                              Recipe % X Sample Weight 
** Dye Solution = …………………………….. (cc). 
                                   Stock solution % 
                Recipe % X Liquor) 
** Salt = …………………………….. (gram per liter, gpl). 
                         1000 
                                Recipe % X 100 X Liquor
** Soda Solution = ……………………….............. (cc). 
                                1000 X Stock solution %

Sample Calculation for 0.5% Shade 
Sample wt. = 5 mg 
Material liquor ratio = 1: 10 
Total liquor (5  10) = 50 cc 
                                        5  0.5% 
Dye solution required = ------------------- = 2.5 cc 
                                            1 % 

                                       50 X 25 
Salt solution required = ------------------- = 6.25 cc 
                                       20 X 10 

                                                50 X 10 
Soda ash solution required = ------------------- = 2.5 cc 
                                               20 X 10 

Water required = {50 - (2.5 + 6.25 + 2.5)} = 38.75 cc
Working Procedure

All ingredients had been taken according to the recipe into the pot of sample dyeing machine. At a room temp the material had run then after 10 minutes started to rise the temperature at 1°C/ min. to get 60°C temperature. For performing the required dyeing temperature it took 30 minutes. The material had dyed at 60°C for 45 minutes. Then the temperature was reduced at room temperature within in 10 minutes. The fabric washed in cold water & then the material was washed in 1 gm/l soap solution (liquor ratio 1:20) at 90°C temperature for 15 minutes. Then after rapidly cold washing the material was dried & preserved.

9. Calculation of Package Density in Yarn Dyeing

Package density has important effect on yarn dyeing. When package are too soft then liquor flowing through it will find the course of least resistance and cause channeling, which leaves some parts of the package relatively undyed or lighter. If the packages are wound too hard, a point can be reached where the flow of liquor is impeded to such an extent that poor dyeing or none may occur. In this article we will discuss on yarn package density before dyeing.

The ratio of mass and volume is called density.
Density = ρ
Mass = m
Volume = v
Here, 
m = (Bobbin weight with yarn – Bobbin weight without yarn) gm.
v = π (R12 – R22) × h 
R1 = Outer radius of the bobbin (with yarn).
R2 = Inner radius of the bobbin.. 
Say, for example, 
Outer Radius, R1=16.3/2 = 8.15 cm. 
Inner Radius, R2 = 6.96/2 =3.48 cm.
Height = 16 cm.. 
We know = πr2h. 
So, total volume, V1	= π R12h 
=3.1416 X (8.15) 2 X 16
=3339 cm3
Steel bobbin, V2= π R22h 
= 3.1416 X (3.48)2 X16.
= 609 cm3 
Original volume = (3339-609) = 2730 cm3
Package Density, ρ = m/v = (1395-235)/2730 = 0.42 gm/cm3.
Package density in soft winding for cotton must be 0.36 to 0.40 gm/cm3 and for polyester or CVC it would be higher than 0.40 gm/cm3.
We measure the package density of different bobbins in this section which are:

| Count (Ne) | Package density (gm/cm3) |
| --- | --- |
| 20s | 0. 387 |
| 24s | 0. 375 |
| 26s | 0. 382 |
| 28s | 0. 35 |
| 30s | 0. 345 |
| 34s | 0. 37 |
| 40s | 0. 378 |

For filament (Polyester):

| Count (denier) | Package density (gm/cm3) |
| --- | --- |
| 30 | 0. 44 |
| 75 | 0. 376 |
| 100 | 0. 46 |

For spun yarn:

| Count (denier) | Package density (gm/cm3) |
| --- | --- |
| 40/2 | 0. 39 |
| 50/2 | 0. 4197 |

For CVC yarn:

| Count (Ne) | Package density (gm/cm3) |
| --- | --- |
| 30s | 0. 40 |
| 26s | 0. 39 |

10. Dyeing Calculation in Lab Dip for the case with using a glauber salt, wetting agent

At the initial stage of dyeing calculation, needs to calculate the lap deep before go for bulk productions. For this a lots of work is done in the dyeing laboratory. In the dyeing lab, lab dip or sample is developed by the dyeing master. Lab dip plays an important role in shade matching & this is an important task before bulk production.

Material weight = 5.0 gm

Wetting agent = 0.5 g/l

Sequestering agent = 2.0 g/l

Antipilling agent = 1 g/k

Dyes = 1.5%

Glauber salt = 40 g/l

Soda ash = 10 g/l

M : L = 1 : 10

Stock Solution Concentration:

Wetting agent, sequestering agent and anti-pilling agent = 1.0%

Dyes = 1.0%

Salt, soda ash = 20%

Dyeing Calculation: 
1. Total amount of liquor = 5 X 10 = 50 ml 
2. Required wetting agent = [{ Total liquor (lit) X Recipe amount in gm/l} / Stock solution%] 
= [{(50 ml/1000 ml) X 0.5 g/l} / 1.0%] = 2.5 ml

3. Required sequestering agent = [{ Total liquor (lit) X Recipe amount in gm/l} / Stock solution%] = [{(50 ml/1000 ml) X 2 g/l} / 1.0%] = 10 ml 
4. Required antipilling agent = [{ Total liquor (lit) X Recipe amount in gm/l} / Stock solution%] 
= [{(50 ml/1000 ml) X 1.0 g/l} / 1.0%] 
= 5 ml 

5. Required amount of glauber salt = [{ Total liquor (lit) X Recipe amount in gm/l} / Stock solution%] 
= [{(50 ml/1000 ml) X 40 g/l} / 20%] 
= 10 ml 

6. Required amount of soda ash = [{ Total liquor (lit) X Recipe amount in gm/l} / Stock solution%] 
= [{(50 ml/1000 ml) X 10 g/l} / 20%] 
= 2.5 ml 

7. Required Dye solution = [{Material weight X recipe amount % (or shade %)} / Stock solution%] 
= {(5.0 gm X 1.5%) / 1.0%} 
= 7.5 ml 

8. Required amount of additional water = {50 – (2.5 + 10+5+7.5+10+2.5)} ml 
= (50 – 37.5) ml 
= 12.5 ml

How to Calculate Dyeing Recipe in Textile Wet Processing Sector?

Dyeing Recipe Calculation:

Dyeing recipe calculation is not a tough task that we have normally seemed. The person who is engaged in textile dyeing industry has to know the dyeing recipe calculation method to dye the fabric perfectly. This article has presented an easy method for calculating dyeing recipe calculation in textile wet processing sector.

Lab Dip Calculation Method Followed in Textile Dyeing Industry:

The below equipment’s has needed to calculate the dyeing recipe in textile wet processing industry.

Digital weighting meter with glass box (Explorer, USA),

Digital pipette,

Microprocessor pH meter.

Dyeing Recipe Calculation Formula:

The below formulas have needed to calculate lab dip in textile dyeing industry.

1. Amount of dye calculation formula:

Required amount of dye,

(Weight of the fabric in gram × Shade percentage

=………………………………………………………………

Percentage of Stock solution

Or,

Required amount of solution,

Fw × Sp

=……………………

Cs

Where,

Fw indicates the weight of yarn, or fiber or fabric.

Sp indicates the shade percentage,

Cs indicates the concentration of stock solution.

2. Auxiliaries or Chemicals Calculation Formula:

The below formula has to follow to calculate required amount of auxiliaries or chemicals.

Required amount of solution (mls),

(Weight of substrate x Gram per liquor required x Liquor ratio)

=………..……………………………………………………………………

(Concentration percentage of stock solution× 10)

3. Additional Auxiliaries Calculation Formula:

Formula for addition of auxiliaries in solids form such as salt, soda is:

Salt in gram per liquor,

Sample weight x Liquor Ratio× required amount (%)

=………………………………………………………………………

1000

4. Percentage to Gram Conversion Calculation Formula:

Conversion formula from percentage to gram/ liquor is in the below:

Gram per liquor,

= Required amount in percentage x 10

If alkali concentration is given then the below formula has to follow for calculating this in gram per liquor:

Required amount of solution (mls),

(Weight of substrate x Gram per liquor required x Liquor ratio)

=……………………………………………………………………………….

(10 x Concentration percentage of stock solution)

Or,

Required amount of solution (mls),

Weight of substrate x Liquor ratio× required amount (%)

= ……………………………………………………………………….

Concentration percentage of stock solution

Lab Deep Calculation Example:

Recipe:

Dyes:

Rema Blue RR = 1.122%

React Red KHW = 2.014%

React Yellow KHW = 1.486%

Chemicals:

Soda Ash (concentration.20%) = 5 gram/liter

Sample Weight. = 5 gram

Caustic Soda = 1.32%

Salt = 70%

Stock Solution (%) = 1

M: L = 1:8

Now, calculate the required recipe for dyes and auxiliaries or chemicals in gram per liter.

Solution:

In case of dyes,

We know,

Required amount of dye,

(Weight of the fabric in gram × Shade percentage

=……………………………………………………………………

Percentage of Stock solution

Calculation of dyestuff will be,

For,

Rema Blue RR = (1.12 2x 5)/1=5.61 g/l

React Yellow KHW = (1.486 x 5)/1= 7.43 g/l,

React Red KHW = (2.014 x 5)/1= 10.07 g/l

In case of auxiliaries or chemicals,

We know,

Salt in gram per liquor,

Sample weight x Liquor Ratio× required amount (%)

=……………………………………………………………………

1000

5×8×70

=……………………….

1000

=   2.8gm

So, required amount of salt is 2.8gm

In case of Soda Ash (Concentration 20%):

Required amount of solution (mls),

(Weight of substrate x Gram per liquor required x Liquor ratio)

=……………………………………………………………………………………….

(10 x Concentration percentage of stock solution)

5×5×8

=……………………

10×20

= 1ml

So, required quantity of soda ash in c.c stands at 1.0

Extra Amount of Water Required:

= M: L – (Required amount of water to make solution of auxiliaries and dyes)

= [(5 x 8) – {(5.61+10.07+7.43) + (1.0+0.12)}]

= 40 – 24.112

= 15.77

Depth of shade, auxiliaries, stock solutions, & water ratios

Colour Strength is expressed as Depth of Shade. (D.O.S) which is calculated as the amount of dye as a percentage of the weight of fibre (W.O.F).  e.g 1gm dye to 100gms fibre = 1% Depth of shade.

The strength of colour does vary considerably on many dyestuffs. To determine the colour value produced by a particular amount of dye per weight of fibre you can use the following guidelines. 0.5%(D.O.S)  lighter shades, 1% D.O.S  medium shades and 2% to 4% (D.O.S) deep stronger shade.

To make calculations easier to work out we use the metric system.

Calculating Dye Quantities…fibre weight x (%D.O.S) divided by 100

Example 1. 125gms yarn dyed to 2% D.O.S.  how much dye required ?

Multiply  125gms x 2 = 250gm divide by 100 = 2.5gms dye.

Example 2. 300gms fibre dyed to 3% D.O.S. how much dye required ?

Multiply 300 gms x 3 = 900 divided by 100 = 9gms dye

Auxiliaries

|  | Light shades | Medium shades | Strong shades |
| --- | --- | --- | --- |
| Citric Acid | 1%(W.O.F) | 1.5%(W.O.F) | 2% (W.O.F) |
| Glaubers Salts | 2%(W.O.F) | 5%(W.O.F) | 10%(W.O.F) |
| Lyogen NH | 1%(W.O.F) | 1.5%(W.O.F) | 2%(W.O.F) |

Stock Solutions

This can be described as a specific amount of dye powder dissolved in a particular amount of water.

Stock solutions are a great time saver as you can make a batch which you can use many times over until it runs out. It is easier to use the stock solution than to measure small quantities of dye powder every time , and when trying different D.O.S for certain colours you can easily measure the amount of stock solution for that colour. Just make sure you label & record what your solutions contain.  You can now measure small quantities easier & accurately.

Most stock solutions will last 3-6 months stored away from sunlight. Some do not last that well and their effectiveness may only be 1-2 weeks.

Calculating a 1% Stock solution

Please note: if you wish to avoid lengthy calculations, use 1% stock solutions.

1% stock solution is the total volume of stock solution required divided by 100.

Calculating 1% stock solution for 1000gm (1kg) fibre. Here, you change the measurement of weight to volume eg 1000gm to 1000mls. You would therefore add 10gms dye (1%) to 1000mls water to make the 1% stock solution.

To mix a 1% stock solution

Example 1.  500mls of stock solution… divide 500 by 100 x 1= 5gms dye.

Example 2   800ml stock solution…divide 800 by 100 x 1 = 8gms dye.

Both examples have a dye strength of 1% depth of shade. (D.O.S)

To calculate the amount of 1% stock solution required per dye lot.

Make stock solution using a 1000ml (1 litre) 1% Stock solution.

Example 1.   (W.O.F) 120gms divided by 1(% D.O.S.)= 120 mls

Example 2.   (W.O.F) 350gms divided by1=350 x 2(% D.O.S)  = 700mls.

Example 3.   (W.O.F) 55gms divided by 1= 55 x 3(% D.O.S)  = 165 mls

If you wanted to change the formula to another % of stock solution then you would simply follow the same formula .eg 2% stock solution = 20gms dye per 1000 mls water.

Albegal Set Stock Solutions

Albegal Set is measured at 1- 2% (W.O.F). 1% light shades , 2% heavy shades.

Eg to 1000mls water add 2% Albegal set =20gms. Shake mixture well every time it is used as with all stock solutions.

Water Ratios

Use a ratio of 20:1 for fibres such as wool and alpaca.

Example: 1kg (1000gms) fibre x 20 = 20litres. If this does not cover the fibre adequately then increase rate to 30:1.

Bulky fibres such as silk require a water ratio between 30:1 & 40:1.

17. 8  Dyeing lab department calculation and others

16Jan 2014

2 Comments

Calculation of Lab Dip | Working Process in Lab Dip

Lab Dip:

Lab dip is a process by which buyers supplied swatch is matched with the varying dyes percentage in the laboratory with or without help of “DATA COLOR” .

Lab dip plays an important role in shade matching & and detaching the characteristics of the dyes and chemicals are to be used in the large scale of production. So this is an important task before bulk production.

Common Stock Solutions:

Red – 0.1%, 0.5%, 1.0%, 2.0% (very common)

Yellow – 0.1%, 0.5%, 1.0%, 2.0% (very common)

Blue – 0.1%, 0.5%, 1.0%, 2.0% (very common).

Preparation:

To prepare 0.1% Stock solution, it is necessary to mix 0.1 g dye and 100 cc water.

To prepare 0.5% Stock solution, 0.5 g dye stuff is mixed with 100 cc water.

To prepare 1.0% & 2.0% Stock solution similar procedure is followed.

To prepare 10% Stock solution of Soda ash, 10 g Soda is mixed with 100 cc water.

Depth of Shade:

0.5% to 5% shade for the goods.

Lab Dip Calculation :
Usually following calculations are followed:

Dye Solution = (Shade % * Sample Weight) / (Stock solution %)   (cc).

Salt = (Shade % * Liquor) / 1000  (gram per liter, gpl).

Soda Solution = (Shade % * 100 * Liquor) / (1000 * Stock solution %)    (cc).

Sample Calculation for 0.5% Shade:

Sample wt. = 5 mg

Material liquor ratio = 1: 10

Total liquor (5 * 10) = 50 cc

Dye solution required = (5 * 0.5%) / 1% = 2.5 cc

Salt solution required = (50 * 25) / (20 * 10) = 6.25 cc

Soda ash solution required = (50 * 10) / (20 * 10) = 2.5 cc

Water required {50 – (2.5 + 6.25 + 2.5)} = 38.75 cc

Working Procedure in Lab Dip:

All ingredients had been taken according to the recipe into the pot of sample dyeing machine. At a room temp the material had run then after 10 minutes started to rise the temperature at 1°C/ min. to get 60°C temperature. For performing the required dyeing temperature it took 30 minutes. The material had dyed at 60°C for 45 minutes. Then the temperature was reduced at room temperature within in 10 minutes. The fabric washed in cold water & then the material was washed in 1 gm/l soap solution (liquor ratio 1:20) at 90°C temperature for 15 minutes. Then after rapidly cold washing the material was dried & preserved. And then check the shade match with the required sample by the lighting box. Then send to buyer or merchandiser for approval.

Working Procedure of Sample Dyeing (Knit Dyeing Section):

Normally a textile dyeing mill get offer through merchandiser. Merchandising department of dyeing mill send the swatch to the central dyeing lab. Then the lab manager analysis the color of swatch with the help of spectrophotometer. After shade matching three sample are submitted to the buyer or buyer agents. If sample is approved by the buyer then this sample recipe are sent to floor for bulk production. The dyeing master dyeing the sample for bulk production. Now I will give the flowchart of sample dyeing for bulk production.

(Scouring and Bleaching)

Water load in sample dyeing machine
↓
Fabric load
↓
Temperature raised in 50 *C
↓
Scouring chemical added (dosing time 10min)
↓
Temperature raised in 60 *C
↓
NaOH dosing ( dosing time 5min)
↓
Temperature raised in 70 *C
↓
Hydrogen Peroxide dosing (dosing time 10min)
↓
Temperature raised in 100-110 *C and running at 30min
↓
Cooling at 80 *C
↓
Ringe or normal wash (10min)
↓
Drain out
↓
New water load
↓
Temperature raised in 55 *C
↓
Add acid + OEM ( for destroying Hydrogen Peroxide power)
↓
pH check and obtain 4.5 by adding acetic acid
↓
Enzyme is added and run time 60 min
↓
Sample check if approved by in-charge
↓
Rinse (run time 15min)
↓
Drain out

(Dyeing)

New water load
↓
pH check and obtain 5.6 by adding acetic acid
↓
Temperature raised at 50-55 *C
↓
Dyeing auxiliaries added (leveling agent, anti creasing agent, sequestering agent etc)
↓
Salt added and running at 10-min
↓
Color is added and dosing time 30 min ( Reactive dye, Disperse dye, Acid dye etc)
↓
Running time 25 min
↓
Temperature raised at 60 *C
↓
Soda ash (dosing time 35 min)
↓
Sample cutting for checking after 10 min later
↓
If approve then rinse at 20 min
↓
New water load
↓
Add acetic acid for neutralization at 40 *C and run at 10-min
↓
Rinse at 5 min
↓
Drain out
↓
New water load
↓
Temperature raised at 90-95 *C and 10 min running
↓
Cooling at 80 *C
↓
Rinse ( for cut sample)
↓
Shade checking if approve by in-charge then
↓
Rinse and running at 15 min
↓
Drain out
↓
New water load
↓
Temperature raised at 30 *C
↓
Fixing agent added ( GG-100, ECO, CR) and dosing time 10-min
↓
Rinse ( 10-min)
↓
Drain out
↓
New water load
↓
Temperature raised at 40 *C
↓
Softener added and run time 30 min
↓
Shade matching if approve then
↓
Fabric unload

Calculation of Dyeing Recipe | Calculation for Dyeing Lab

Calculation for Lab Deep:

Recipe Calculation Formula :

Dye = (Shade % * Weight of the fabric in gm )/Stock solution %

Or,

Required solution = WP / C

Where ,
W = weight of fabric, yarn, or fiber
P = shade percentage
C = concentration of stock solution
CC = cubic centimeter .

For auxiliaries (chemicals) the formula is as below :

Required amount of solution (mls) = (g/l required * wt of substrate * LR ) / (10 * concentration (%) of stock soln)

For addition of auxiliaries in solids form such as salt the formula is :
Salt in g/l = (Required amount (%) * Sample weight * LR) / 1000

Conversion formula from percentage to g/l is as below :
g/l = Required amount (%) * 10 .

If alkali conc. Is given in Be. then the formula to calculate this in g/l is as follows :
Required amount of solution (mls) = (g/l required * wt of substrate * LR) / (10 * concentration (%) of stock soln )

Or ,

= (Required amount (%)* wt of substrate * LR) / (Concentration (%) of stock soln)

Or,

Required alkali soln in c.c. = ( g/l required * wt of substrate * LR) /  (10* conversion value from Be. to g/l of alkali )

Or ,

Required alkali soln in c.c. = (Required amount (%) * wt of substrate * LR) /  conversion value from Be. to g/l of alkali

Example : Suppose a lab deep of a fabric sample (1*1 rib) has to be formed with following dyes & chemicals :

Dyes:
1. Rema Blue RR = 1.122%
2. React Red KHW = 2.014%
3. React Yellow KHW = 1.486%

Salt = 70%

Soda Ash (conc.20%) = 5 g/l

Caustic Soda (38 Be) = 1.32%

L: R = 1:8

Sample Wt. = 5 gm

% Stock Soln = 1

Therefore, recipe calculation for dyes and auxiliaries in g/l will be as follows :

For dyes :
We know ,
Dye = (Shade % * Weight of the fabric in gm )/(Stock solution % )

For,
1. Rema Blue RR = (1.122*5)/1=5.61 g/l
2. React Red KHW = (2.014*5)/1= 10.07 g/l
3. React Yellow KHW = (1.486*5)/1= 7.43 g/l .

For auxiliaries :
We know ,
Salt in g/l = (Required amount (%) * Sample weight * LR) /  1000
. .   .  Required Salt = (70*5*8)/1000 = 2.8 gm .

For Soda ash(conc.20%) :
We know ,
Required amount of solution (mls) = (g/l required * wt of substrate * LR) /  (10 * concentration (%) of stock soln )
.
.   . Required amount of soda ash in C.C. = (5*5*8)/(10*20) = 1.0

For Caustic soda (38 Be.) :
We know ,
Required alkali soln in c.c. = (Required amount (%) * wt of substrate * LR )/conversion value from Be. to g/l of alkali
.
.   . Required caustic soda = (1.32*5*8)/441 = 0.12 c.c.

[since 38 °Be.NaOH= 441 gm NaOH 100% per 1lit NaOH soln]

Extra Water required :
= M:L – (required water to make soln of dyes & auxiliaries) = (5*8) – [(5.61+10.07+7.43) + (1.0+0.12) ]
= 40 – 24.112
= 15.77 (Salt is added in solid form)

Equipments of Recipe Section:

Microprocessor pH Meter (Hanna Instrument)

Digital pipette

Digital Weighting Meter with Glass Box (Explorer, USA)

Procedure for Lab dip by the Different Dyestuff in the Laboratory

Lab Dip:

Lab Dip Development means the sample which is dyed according to buyer’s requirements (similar shade and so on). Depending on lab dip development sample dyeing and bulk production dyeing planning is done.Lab work plays an important role in dyeing process. Bulk dyeing process completely depends on the lab dip development work. Lab work is completely managed as the following sequence.

Procedure for Lab dip by the Different Dyestuff in the Laboratory:

Procedure for 100 % Cotton Fabric:

1. Calculate the recipe.
2. Weight the fabric.
3. Take the beaker keep the fabric in to the beaker.
4. Then the dyes, chemicals & required amount of water take in to the beaker by the digital pi-petting.
5. Then weight the salt by the electric balance and add in to the beaker.
6. Then the beaker set in to the lab dyeing machine for dyeing.
7. Start the program for dyeing the whole dyeing time 60 min at 60 °C temperature. (The dyeing time and temperature depends on which classes of dyes are used for dyeing.)
8. After 30 min add the then add the soda ash. By pi-petting.
9. Again run the program next 30 min at the same temperature.
10. Finished the dyeing time then the sample taken from the beaker first hot wash & then cold wash.
11. Then acid wash as for neutralization.
12. Then soaping required soap solution 10 min at 90° C temperature.
13. after the fabric again cold.
14. Then dry the lab dip and compare with the standard.

What is Lab Dip | Objects of Lab Dips | Process Sequence of Lab Dip

Lab Dip:

A lab dip is a swatch of fabric test dyed to hit a color standard. It is a process by which buyer’s supplied swatch is matched with the varying dyes percentage in the laboratory with or without help of spectrophotometer. Lab dip plays an important role in shade matching & this is an important task before bulk production. In previous article of this author we have to learn on flow chart on dyeing lab.

There are different matching systems followed in Labs. They are :

Tube light matching.

Sun light matching.

Ultra Violet matching.

Sodium light matching (show room).

Object of Lab Dip:

The main objectives in lab dip are as follows:

To calculate the recipe for sample dyeing.

To compare dyed sample with swatch by light Box or Spectrometer.

To calculate revise recipe for sample dyeing.

Finally approved Lab Dip (Grade: A, B, C & D)

Process Sequence of Lab Dip:

Lab dip plays an important role in dyeing process. Bulk dyeing process completely depends on the lab dip development work. Lab dip is completely managed as the following sequence.

Lab Dip Requisition from buyer
↓
Entry in the computer
↓
First recipe is given by swatch/pan-tone number
↓
First correction
↓
Second correction
↓
Grading of sample (A, B, C, D)
↓
Yarn and knit sample send to buyer
↓
Approved by buyer
↓
Order for bulk production
↓
Production card with approved sample and recipe send to production section

Process Flow Chart/Sequence of Dyeing Lab

At first dyeing is performed in dyeing laboratory and then starting for bulk production. A lots of work is done in the dyeing laboratory. In the dyeing lab, lab dip or sample is developed by the dyeing master. Lab dip plays an important role in shade matching & this is an important task before bulk production.

Process Sequence of Dyeing Lab:

Sample/Swatch/Panton no. / TCX no. / TPX no. from the buyer
↓
Determination of sample’s possible color combination by the help of Spectrometer or manual
↓
Dispersion by autodoser
↓
Trial dyeing of first recipe
↓
Unload
↓
Normal wash
↓
Hot wash with detergent
↓
Oven drying
↓
Ironing
↓
Shade matching in light box ( If Ok then send to buyer for approval)
↓
If not ok
↓
First correction takes from Spectrometer or manually
↓
Dispersion by auto-doser
↓
Trial dyeing of first recipe
↓
Unload
↓
Normal wash
↓
Hot wash with detergent
↓
Oven drying
↓
Ironing
↓
Shade matching in light box ( If Ok then send to buyer for approval)
↓
If not ok
↓
Second correction takes from Spectrometer or manually
↓
Dispersion by auto doser
↓
Trial dyeing of first recipe
↓
Unload
↓
Normal wash
↓
Hot wash with detergent
↓
Oven drying
↓
Ironing
↓
Shade matching in light box
↓
If ok
↓
Send for buyer’s approval
↓
Bulk production by considering the buyer’s approved sample as standard

Note: This procedure is applicable for yarn or fabric dyeing.

| Assessment of students knowledge of practical subjects Evaluation by letter system | Numeral equivalent of points | %- content | Evaluation according to the traditional system | 4.5 Providing support for people with disabilities 4.5.1. Individual differentiated approach in the organization of the educational process 4.5.2. Individual differentiated approach in all kinds of activities * Note: According to the student's choice it is envisaged that all kinds of tasks can be delivered orally Criteria for assessing students' knowledge Criteria for assessing students' knowledge |
| --- | --- | --- | --- | --- |
| А | 4,0 | 95-100 | Excellent | The student demonstrates: - a deep and lasting assimilation of program material - complete, consistent, competent and logically presented answers for all types of activities; - Ability to freely cope with the tasks; - correct, well-founded decisions, - skills in the use of information from basic and additional specialized literature in the study of discipline, - the ability to self-systematize the program material; - Possession of versatile skills and methods of performing all types of tasks; - Ability to work with foreign literature and information resources of the Internet; - Timely and high-quality execution of all types of tasks. |
| А- | 3,67 | 90-94 |  | The student demonstrates: - Deep assimilation of program material; - complete, consistent and logically presented answers for all activities; - ability to cope with the tasks; - the right decisions, - skills of using special literature in the study of discipline, - the ability to self-systematize the program material; - Possession of skills and techniques for performing all types of tasks; - Timely execution of all types of tasks. |
| В+ | 3,33 | 85-89 | Good | The student demonstrates: - assimilation of program material; - complete, consistent, literate, without significant inaccuracies, an account of the answers for all kinds of tasks; - correct application of theoretical knowledge - Possession of necessary skills in the performance of applied tasks - skills in using recommended literature in the study of discipline, - skills of systematization of program material; - Possession of skills and techniques for performing all types of tasks; - Timely execution of all types of tasks. |
| В | 3,0 | 80-84 |  | The student demonstrates: - assimilation of program material; - a consistent presentation of the answers for all types of tasks with non-essential errors; - skills in applying theoretical knowledge under the guidance of a teacher; - Possession of necessary skills in performing practical tasks - skills in using recommended literature in the study of discipline, - skills of systematization of program material under the guidance of a teacher; - mastering the skills of performing all kinds of tasks; - the ability to independently correct mistakes made; - the timely execution of all types of tasks with the elimination of errors. |
| В- | 2,67 | 75-79 |  | The student demonstrates: - assimilation of program material; - Ability to present answers with non-essential errors; - skills in applying theoretical knowledge under the guidance of a teacher; - Possession of techniques in the performance of practical tasks - skills in using recommended literature under the guidance of a teacher - skills of generalization of program material under the guidance of a teacher; - the ability to correct mistakes made with the help of a teacher; - the timely execution of all types of tasks with the elimination of errors. |
| С+ | 2,33 | 70-74 | satisfactorily | The student demonstrates: - mastering of the main material; - Inadequate formulations when responding to all kinds of tasks; - violation of the sequence in the presentation of the program material; - difficulties in self-fulfillment of practical tasks; - Possession of individual techniques in the performance of practical tasks - skills in using the literature recommended by the teacher; - skills of generalization of separate sections of program material under the guidance of a teacher; - the ability to correct major mistakes made with the help of a teacher; - execution of all types of tasks with elimination of errors. |
| С | 2,0 | 65-69 |  | The student demonstrates: - mastering of the main material; - Inadequate understanding of formulations when answering all types of assignments; - lack of consistency in the presentation of the material; - difficulties in self-fulfillment of practical tasks; - Possession of separate receptions at performance of tasks - difficulty in using the literature recommended by the teacher; - difficulties in generalizing the individual sections of the material studied; - the ability to correct major mistakes made with the help of a teacher; - execution of all types of tasks with elimination of errors. |
| С- | 1,67 | 60-64 |  | The student demonstrates: - mastering of the main material; - Inadequate understanding of formulations when answering all types of assignments; - lack of consistency in the presentation of the material; - significant difficulties in the independent implementation of practical tasks; - Inadequate possession of individual methods in the performance of assignments - significant difficulties in using the literature recommended by the teacher; - significant difficulties in the generalization of individual sections of the material studied; - the ability to correct major mistakes made with the help of a teacher; - execution of all types of tasks with elimination of errors. |
| Д+ | 1,33 | 55-59 |  | The student demonstrates: - mastering of separate sections of the main material; - misunderstanding of formulations when answering all types of assignments; - lack of consistency in the presentation of the material; - significant difficulties in the independent implementation of practical tasks; - significant difficulties in the application of individual methods of performing tasks; - significant difficulties in using the literature recommended by the teacher; - significant difficulties in the generalization of individual sections of the material studied; - difficulties in correcting the mistakes made by the teacher; - untimely execution of all types of tasks with elimination of errors. |
| Д | 1,0 | 50-54 |  | The student demonstrates: - difficulties in mastering individual sections of the main material; - misunderstanding of formulations when answering all types of assignments; - lack of consistency in the presentation of the material; - significant difficulties in the independent implementation of practical tasks; - Inability to apply individual methods of performing tasks; - significant difficulties in using the literature recommended by the teacher; - Inability to generalize the individual sections of the material studied; - significant difficulties in correcting the mistakes committed by the teacher; - untimely execution of all types of tasks with elimination of errors. |
| F | 0 | 0-49 | unsatisfactory | The student demonstrates: -- not having knowledge of program material, - When performing all types of tasks, gross errors are allowed; - lack of skills in applying individual tasks; - non-fulfillment of certain types of tasks provided by the forms of current, intermediate and final control. |

References

1. Gocarneshan N. Ecological Expertise of the Textile Fabrics. New Delhi: New Age International Publisher. -2004.

2. Grosciki, Z. Watsons. Expertise of the Textile Fabrics. Universal Publishing Corporation, Mumbai.

3. Nisbeth, H. Taraporevala& Sons, Mumbai. Ecological Pollutions.

4. Klyushnik N.P. Workshop on organic synthesis. - M .: High school. 1987. p. 63-66, 74-75.

5. Laptev, NG, Bogoslovsky, B.M. Chemistry of dyes. - M .: High school. 1970. p. 118 - 184.

6. J N Chakraborty. Fundamentals and practices in colouration of textiles. New Delhi ● Cambridge ● Oxford. 2010. -414 p.

7. P. J. Hauser. Textile dyeing. Published by InTechaneza Trdine 9, 51000 Rijeka, Croatia. -392

8. J. S. Smith. Textile processing. Printing. Dyeing. Finishing. Delhi: Abhishek publications. Chandigarh

9. Мельников, Б.Н. Физико-химические основы процесса отделочного производства /Б.Н. Мельников, Т.Д. Захарова, М.Н. Кириллова. – М.: Легкая и пищевая промышленность, 1982

10. Кричевский, Г.Е. Химическая технология текстильных материалов учебник для вузов: в 3 т. – -2009, -158 p.

11. Бельцов В.М. Технологическое оборудование отделочных фабрик текстильной промышленности. - Л.: Машиностроение, 1974. -295с

Additional

1. Shababane and Blinov. Air pollutions. Mir Publishers, Moscow.

2. Marks and Robinson. Ecology of the air. Textile Institute.

3. Wynne ,A.Textiles—Motivate series, Macmillan Publications, London.

4. Ecologicale terms and definitions—Textile Institute.

5. Pollution mechanism, Volume I and II, Prof. N. N. Banerjee.

6. Robinson and Marks. Principles of weaving, Textile Institute.

7. Lord and Mohammed. Weaving conversion of yarn to fabric. Merrow Publications, London.

Electronic textbooks, TMCD, slides, video films, animated films, computer software, virtual laboratory works, presentations (numbers, full titles of modules)

1. Advances in Modern Woven Fabrics Technology. Ed. SavvasVassiliadis. InTech. JanezaTrdine 9, 51000 Rijeka, Croatia.

2. Wilson. J. Handbook of textile ecology. Principles, processes and practice. CRC Press. Boca Raton Boston New York Washington, DC. Woodhead publishing limited. Cambridge England, 2001.

3. Patanaik. A. Modeling and simulation in ecological pollutions? materialstechnicues and applications. Ed.

Nova Science Publishers, Inc. New York, 2012.

Сабиров Вахобжон Хусанович

CИХИМБАЕВА МАКПАЛ ТЕМИРБЕКОВНА

Методические указания

к практическим работам по дисциплине

химизация технологических процессов текстильного производства

("Chemicazation of technological processes of textile production”)

Подписано в печать __________________________

(число.месяц.год)

Формат бумаги XxY  1/16

Бумага типографская. Печать офсетная. Объем …2,3 п.л.

Тираж …100 экз. Заказ № …….*