Ф.7.03-03

SabirovV. Kh. Sihimbaeva M.T. Abilhaimkyzy L.

METHODICAL gUIDElineS

To PRACTICAL workS for THE discipline

“Mechanical technology of textile materials”

Shymkent-2018

MINISTRY OF EDUCATION AND SCIENCE OF THE REPUBLIC OF KAZAKHSTAN

M. AUeZOV SOUTH KAZAKHSTAN STATE UNIVERSITY

HIGH SCHOOL OF TEXTILE AND FOOD ENGINEERING

Department of "Technology and Design of Textile Materials"

SabirovV. Kh. Sihimbaeva M.T. Abilhaimkyzy L.

METHODICAL Guidelines

for  PRACTICAL works on the discipline

“Mechanical technology of textile materials”

For students of the educational program – 5b073300 "Technology and design of textile materials"

Shymkent-2018

UDK 676, 051, 2 (083.13); 677.047.42 (07)

Compiled by: Sabirov V.Kh. Sihimbaeva M.T. Abilhaimkyzy L. Methodical guidelines for practical works on the discipline “Mechanical technology of textile materials”. – Shymkent: M.Auezov SKSU, 2018. – p. 66.

The methodical guides are compiled based on the curricula and programs of the discipline “Mechanical technology of textile materials” and are intended for students of the educational program 5B073300 – Technology and design of textile materials.

Theoretical propositions, methods and practical recommendations for performing laboratory work are given.

Table. 17. Illustrations 12. Bibliography: 7.

Reviewer: Dzhanpaizova V.М. – K.Chem. Sc., associate professor.

Methodical instructions were considered and recommended for publication by the meeting of the department “Technology and Design of Textile Materials” (Protocol No.  _   _ “_  _” _ , 2017) and the Methodological Committee on Innovative Technologies for Teaching and Methodological Support of the Higher School “Textile and Food Engineering”, Minutes No. _  _ «_  _» 01.2017

Recommended for publication by the Educational and Methodical Council of SKSU. M.Auezov, Protocol No. _ __ of “__ __” __ ____ 2018

© M. Auezov South Kazakhstan State University, 2018

Responsible for the issue Sabirov V.Kh.

Contents

| Introduction…………………………………………………...….………….. Purpose and objectives of practical exercises.................................................................................................... Occupation №1. Acquaintance with the processes, the sequence of machines and semifinished products of sprinning production……………. Occupation № 2. Study of the device and operation of a crumbling-trepal plant for cotton sprinning …………………………………………………… Occupation №3. Study of tape machines cotton sprinning production. Refueling calculation and production of a tape of a given thickness……... Occupation №4. Study of a roving machine of cotton sprinning. Refueling and yarn production of a given thickness …………………………………. Occupation №5. Studying the ring sprinning machine. Refueling machine and yarn production of a given thickness …………………………………. Occupation №6. Studying the pneumomechanical sprinning machine. Drawing up the technological scheme. Refueling calculation MRP ………. Occupation №7. Study of ribbon-connecting, canvas-drawing and combing machines of cotton sprinning. Determination of the quality of carded paper and the percentage of combed fleece ……………………….. Occupation № 8. Acquaintance with the assortment of the shaped yarn and the machine of shaped torsion ……………………………………………... Occupation№9. Familiarization with the bulkhead and knotting machines Occupation № 10. Study of a weft-winding automatic machine ………… Occupation №11. The device and work of the loom. Cardboard packing and fabric production time………………………………………………….. Occupation №12. Study of a warp knitting machine with hooked needles. Acquaintance with the machine with reed needles ……………………….. Occupation № 13. Study of the round-loop machine. The development of a stocking or a sock. ………………………………………………………… Occupation №14. Study of the device and operation of a round ………… Occupation №15. Manufacture of nonwovens ......................................... | 2 7 10 12 18 23 28 30 32 35 37 39 41 43 46 54 55 57 |
| --- | --- |

Assessment of students knowledge of  practical subjects ……………………     61

Literature ………………………………………………………………………   65

Introduction

Practical classes of students on the discipline “Designing the technological and technological processes of the industry” are conducted with the aim of deeper and more detailed study of the course, instilling in students the skills of creative, independent work with educational, scientific and technical, patent, methodical literature and lecture notesIn this methodical guide, the properties of textile fibers, their modern classification, spinning systems, technological processes and modern equipment for the production of cotton yarn and their mixtures with chemical fibers, twisted and shaped yarns, as well as high-volume yarns and textured yarns are considered.

To solve the problem associated with the design of tissues, it is necessary to develop theoretical provisions that determine the main parameters of the structure of the tissue, and the methods for their design.

Practical studies provide for the consolidation of students’ theoretical information on the analysis of work and the calculation of the technological process. Subjects of students’ independent work are aimed at consolidating the studied material by independently solving issues from the most important sections of the discipline. A course project on this discipline is envisaged.

Purpose and objectives of practical exercises

Practical classes of students on the discipline “Design of the technological processes of the industry” are conducted with the aim of deeper and more detailed study of the course, inculcating the students with the skills of creative, independent work with educational, scientific and technical, patent, methodical literature and lecture notes, and also provides training in modern design processes tissues, the development of theoretical provisions that determine the main parameters of the structure of tissue, and methods for their design

Occupation №1

Lesson Topic: Acquaintance with the processes, the sequence of machines and semifinished products of sprinning production
Lesson plan:

1. Study of the raw material composition of a fiber by the type of fiber

2. Studying the nature of the finish

3. Study of the range of fabrics

4. Conclusions and a report on the work done.

Purpose and objectives of the lesson, skills, skills and competences: role and importance of the production of various types of textiles

Brief theoretical information

Four main groups of tissues are distinguished according to the kind of fibers: cotton-chateau, woolen, linen and silk. The group of silk fabrics includes fabrics produced from natural silk and from chemical yarns and yarns (artificial and synthetic).

Fabrics made from natural silk are called silk, and from chemical threads – indicating the type of fiber or thread from which they are made – viscose, acetate, capron, lavsan, etc.

In addition, for technical purposes produce fabrics of fluorine, glass, asbestos and other fibers.

- According to the fibrous composition, the tissues are divided into the following three groups:

-  homogeneous – with the base and the duck, obtained from fibers of one kind, without impurities or with the addition of not more than 10% of other types of fibers, nested to improve the spinning capacity or the supply of tissue of a certain external effect;

- non-uniform fabrics in which yarns or yarns of different systems consist of fibers of various kinds or in the basis or weft, or simultaneously in both systems twisted yarns obtained by twisting yarns or yarns of various kinds are used;

Heterogeneous and mixed fabrics are usually called by the most valuable component with the addition of the prefix “floor”, for example semi-woolen, where in one system woolen threads, and in another cotton; semi-silk, where viscose threads are based, in cotton weft yarn; lnolassan, obtained from a mixture of linen and lavsan fibers, etc.

In addition, in the process of weaving, it is possible to obtain multicolored fabrics produced from dyed yarns of different colors; apport

fabric from yarn, obtained from mixtures of color-impregnated in various colors; foundation fabrics with a surface from the tips of an additional pile foundation, cut directly on the machine after forming the fabric.

By appointment, the fabrics are divided into household, technical and special. In turn, household fabrics are divided into classes, subclasses and groups. Cotton and linen fabrics are divided into three classes: clothing, decorative and moisture absorbing. Cherstyanye and silk fabrics are divided into only two classes (clothing and decorative). In Table. 1 shows the classification of tissues into classes, subclasses and groups in accordance with state standards adopted for each

type of raw material.

- By the types of weaving, the tissues are divided into four groups:

- simple, homogeneous, smooth, without any

- patterns of the surface, developed by the main interlacing;

- • finely-speckled, interlacing which is a kind of change and complication of the main interlacing (derivatives and combined), which forms small patterns on the surface of the tissue;

- with complex interlacing, which are formed by several systems of warp and weft threads. These interlaces represent a modification of the first two groups of interlaces and can give the tissues a specific appearance, for example, double-layer fabrics, pile terry, tracery, etc.;

- large-diameter (jacquard), the pattern of which is formed by a different combination of interlacing fabrics of the first three groups.

Table 1

| Class | Subclass |  |  |  |
| --- | --- | --- | --- | --- |
|  | Cotton fabrics | Linen fabrics | Woolen fabrics | Silk fabrics |
| Decorative Moisture absorbing | Linen Dresses Suiting Coats Lining Handkerchief Shoe The sweaty Sophisticated Blankets Shoelaces Curtains Furniture Covering- Embroidered Tablecloths Track Towel | Linen (underwear) Dresses Blouse Suiting Trousers Sophisticated Applied Borting Curtains Portry Furniture Tablecloths Terraces Sunbeds Awning Bathing Searches Towel Napkin | — Dresses Suiting Coat Trousers Lining Blankets Plaid Blankets Shoe Woven Fabric Fur Blankets Blankets Furniture Tablecloths Bedspreads Track Carpet - | Linen Shirt Dresses Dress- costume Denim Conover Coats Shoe Sports Woven fur Lining Bedding Dressing gown Textile-haberdashery (tie, scarf, umbrella) Portier Curtains Curtains Furniture Checholary Track Cushions Tablecloths Napkin For pillows - |

Fabrics of the first three groups are produced on looms, equipped with a lifting mechanism (eccentric or carriage). To produce large-diameter fabrics, it is necessary to equip weaving machines with jacquard machines. Sometimes for the development of complex jacquard fabrics simultaneously with jacquard machines, remizozoemnye mechanisms are used. Recommendations for students to prepare for classes: preparation is to study the material of the practical lesson on lecture notes, textbooks and teaching aids.

Technical and tools: weaving looms АТ-100-5М

TechPerenet and types of tasks to perform in the classroom:

1. To study the main types of textile raw materials: natural and chemical fibers, chemical complex threads.

2. Analyze the waste of textile production.

List and types of homework:1Determine the characteristic of the assortment of tissue.

2. To study the options for improving the consumer properties of tissue by using new types of fibers.

Assignment for independent work of students (CDS):

1. To master the computer-aided design with the use of computers and the development of tissue.

2. Analyze the actual and calculated values ​​of the linear density of tissue.

Control questions

1. On what weaving looms produce the tissues of the first three groups?

2. What are the names of heterogeneous and mixed tissues?

3. What kinds of interlacing are used to make linen fabrics?

Reporting form: written.

Occupation № 2

Theme of the lesson: Study of the device and operation of a crumbling-trepal plant for cotton sprinning

Lesson plan:

1. Calculation of tissue density.

2. Calculation of the number of the bird.

3. Determination of the weight of the threads of the scraped base

4. Conclusions and a report on the work done.

Goals and objectives of the lesson, skills, competencies: determine the parameters of fabric finishing: shrinkage or broaching along the length, shrinkage along the width, change in the surface density of the fabric after finishing.

Brief theoretical information

After determining the main parameters of the structure of the tissue, it is necessary to compose a refueling calculation for fabrication on the machine. The following data are included in the filling calculation of the fabric.

For STB machines, the basis density in the edges should be less than or equal to the density based on the background of the same. The width of the edges for shuttle looms, as well as for pneumatic, hydraulic and pneumo-pyramidal machines is 1-1.5 cm. For fabrics produced on STB machines, the width of the edges is determined by the design of the edge-forming device and can be from 2.6 to 3, 5 cm, i.e. from 1.3 to 1.75 cm from each side of the fabric web.

In most cases, the basis density in the edges is greater than the density of

the basis of the tissue background is 1.5-2 times. If the filaments are used for filaments of greater linear density than for the background, the density in the edges may be equal to or slightly less than the background density.

For STB machines, the basis density in the edges should be less than or equal to the density based on the background; since the density of the fabric along the weft in the edges on the machines, STB is 2 times larger.

The density of the fabric in the edges must be consistent with the threading of the filaments in the reed and determined by the formula:

Where zкр and  zф — the number of threads of the edges and the background sneaking into the tooth of the reed. Number of warp threads in the edges

The total number of threads in the base

In the filling calculation, detailed refueling Fabric patterns:

a) a schematic depiction of the complete filling pattern of the weave of the fabric (interlacing, disassembly and the order of lifting of the records); while the general rapport of the weft weave on the filling figure should be the smallest multiple of the rewinding pattern for the background weft (Ru.f) and the edges (Ru.kp);

b) the type of the warp threads in the background and in the edges.

For the calculation of Burda, the number of threads trailing into the tooth

bird of the background (zf) and edges (zcr), and the number of threads trailing into the tooth

bard, should be a multiple of the total number of warp threads.

Total number of tines

Where Хф – number of burr teeth for background; - number of teeth of the reed for edges; - number of spare teeth (5 to 10 teeth are taken).

For STB machines, spare teeth are not provided. The number of the reed is determined by the formula

In addition, the number of the reed can be determined based on the density of the severe fabric, taking into account the duck ingestion:

When calculating the remission, determine:

- the width of the shaft, which is taken 1-2 cm longer than the width

refueling

where Bp- is the width of the parting of the warp threads in the gallery of remizks, cm; b) the number of haloes in the remise:

where rf- is the number of halos for the filaments of the background; rcr is the number of galevs for the filaments of the edges. C) the number of galevs on each harness

where gr.ph is the number of galevs on each branch for background threads; pr.f – the number of remotes for background threads; gr.kr – the number of galev on each branch for threads of crocks; nр.кр – number of edges of filaments; d) the density of the galev on each harness:

For STB machines, the calculation of the remission is made taking into account the sizes and number of zones that make up the frame. The width of the shaft corresponds to the working width of the machine.

The linear density of 1mg.m of severe tissue is determined

weight basis and weft in 1 pound m cloth:

where Py is the density of the stern tissue by the weft, the filaments by 1 cm; Vs is the width of the stern tissue, cm;      T0 and Tu are the linear density of the warp threads and weft, tex. If the fabric is produced from the scraped threads, the balance of the base is taken into account in the basis weight, on threads, which is taken equal to 2/3 percent of the glue and is determined by the formula

In this case, the mass of the warp threads

Recommendations for students to prepare for classes: preparation is to study the material of the practical lesson on lecture notes, textbooks and teaching aids.

Engineering and tools: weaving machines STB

List and types of tasks to perform in the classroom:

1. Explain the structure of the tissue.

2. Make a calculation of the density of the gal on each harness.

List and types of homework:

- Self-study types of weave fabrics 2.Proizvest calculation of packages and waste for transitions of weaving

Assignment for independent work of students (CDS): 1.Techniko-economic substantiation of a choice of the optimum technological plan of weaving 2. Based on the analysis of existing plans and the study of the latest technology and technology, drawing up a production plan.

Control questions

1. What weaving looms produce fabrics?

2. The density on the basis in the edges should be less than or equal to the density based on the background for STB machines?

3. Given what parameters is the calculation of the remission for STB machine tools?

Reporting form: written.

Occupation №3

Lesson Topic: Study of tape machines cotton sprinning production. Refueling calculation and production of a tape of a given thickness

Lesson plan:

1. Design the production of combed yarns with a linear density of 18.5 tex.

2.Create a plan for spinning.

3. The conclusion. Report on the work done.

Goals and objectives of the lesson, skills, skills and competencies: selection and justification of the spinning plan; plan spinning on the recommendation of the Central Scientific Research Institute of Biotechnology; spinning plan on the recommendation of Jutex.

Brief theoretical information

Selection and substantiation of the spinning plan.
To produce a combed yarn of a linear density of 18.5 tex, for weaving yarn (base) the following spinning plans are proposed.      Plan of spinning

|  | Name of the transition | Linear densities emerging Yours. Ktex (tex) | Number of additions | General exhaustЕобщ | Speed ​​of working bodies |  | КПВ | КРО | Theoretical productivity Atheor kg / hr |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | V m / min | m / min |  |  |  |
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 |
| 1 | Carding machine С-60 | 6,0-20,0 | 1 | 40-200 |  | 900 |  |  | 120 |
| 2 | Tape machine SВ-Д-15 «О»переход | 1,25-7,00 | 4-8 | 4,48-11,67 | 250-1000 |  |  |  | 300 |
| 3 | Ribbon connection machine Е-32 | 60-80 | 24 | 1,43-3,10 | 120 |  |  |  | 480 |
| 4 | Greeting machine Е-62 | 3,0-6,0 | 8 | 9-19,3 |  | 400 |  |  | 70 |
| 5 | Tape machine RSV-D-35 “I” head | 1,25-7,00 | 4-8 | 4,48-11,69 | 250-1000 |  |  |  | 300 |
| 6 | Rovnichnaya machine F-11 | 168-1475 | 1 | 4-20 |  | 840 -1500 |  |  | 7,8на 1 веретено |
| 7 | Spinning machine G-33 | 4,0-107 | 1 | 8-120 |  | 25000 |  |  | 0,67 на 1 веретено |

Spinning plan on the recommendation of the Central Scientific Research Institute of Briquettes

The recommended plan for spinning yarn 11.5-20 tex on a combed system,

produced on a ring-spinning machine with medium-fiber cotton (L = 33/34 mm)

|  | A car | Твых ktex | Еобщ | V m / min or n min-1 | Пт кг/час | КПВ | КРО |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Trepal MT | 350 | - | 9,81 | 205,8 | 0,92 | 0,935 |
| 2 | Carding | 3,5 | 100 | - | 16-18 | 0,92 | 0,955 |
| 3 | Belt «O» transition | 3,5 | 6 | 150 | 126 | 0,85 | 0,975 |
| 4 | Lento-connecting «Tekstima» 1576 | 60 | 1,05 | 72 | 259,2 | 0,75 | 0,975 |
| 5 | Combinned «Textima» 1532 | 3,5 | 68,6 | 215 | 31 | 0,86 | 0,94 |
| 6 | Band “I” transition of LNS-51-2 | 3,6 | 5,8 | 135 | 116,6 | 0,85 | 0,975 |
| 7 | The “II” transition of the LNS-51-2 | 3,6 | 6 | 135 | 116,6 | 0,85 | 0,975 |
| 8 | Rovnichnaya on 132vettenena R-192-5 | 0,6 | 6 | 1000 | 108 | 0,75 | 0,975 |
| 9 | Spinning on the open terrace P-76-5M6 | 18-20 | 33,3-30 | 12600 | 6,1-7 | 0,95 | 0,97 |

Shirokov V.P. and other reference book on cotton spinning.

Spinning plan on the recommendation of JSC “Utex”, equipped with machines firm “RIETER”

|  | A car | Your ktex | Number of additions | General exhaust Еобщ | Twist for 1 meter to / m | Number of turns m / min | Rotational speed min-1 | Theoretical productivity in kg / hour | CPV | Actual performance in kg / hour | Ugar% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 |
| 1 | Carding machine C-60 | 8,3 | 1 | 95,4 | - |  | 165 | 82,5 | 0,97 | 80,1 | 3,7 |
| 2 | Tape machine SB-D-15 “About” transition | 5,0 | 4 | 6,64 |  |  | 550 | 165 | 0,93 | 153,4 | 0,7 |
| 3 | Lento-connecting machine E-32 | 74 | 24 | 1,62 |  |  | 90 | 400 | 0,77 | 308 | 0,6 |
| 4 | Greasing machine E-62 | 5,7 | 8 | 13,2 |  |  | 385 | 66 | 0,90 | 59,4 | 17,2 |
| 5 | Tape machine RSV-D-35 “I” head | 5,135 | 6 | 6,66 |  |  | 450 | 138,5 | 0,89 | 123,5 | 0,7 |
| 6 | Rowing machine F-11 | 0,74 (740 текс) | 1 | 6,93 | 43,3 | 1100 |  | 1,129 | 0,81 | 0,915 | 1,2 |
| 7 | Spinning machine G-33 | 20 | 1 | 37,0 | 795 |  | 17500 | 0,0264 | 0,93 | 0,0246 | 3,7 |

Selection and justification of the linear density and drawing on transitions I. Carding machine C-60 linear density of the tape  1.Po technical specification     Tlen = 6.0-20.0 ktex 2.On recommendation of the Central Scientific-Research Institute   Tlen = 3.5 ktex 3. On the recommendation of “Uteks”    Tlen = 8.3 ktex

4. In the project we accept    Tlen = 8.5 ktex II. Tape machine SВ-Д-15 “О” transition Linear density, stretching and number of folds1. According to the technical specification

Tlen = 1,25-7,00 ktex

d=4-8

Еобщ=4,48-11,67

2. On the recommendation of the Central Scientific-Research Institute

Tlen =3,5 ктекс

d=6

Еобщ =6

11

3. On the recommendation of “Utex”

T Tlen  =5,0 ктекс

d=4

Еобщ =6,64

4. In the project we accept

Tlen = 5,128 ktex,

d=4,

Еобщ =6,66

III. Lento-connecting machine E-32 1. According to the technical specification     Tlen = 60-80 ktexd=24

Еобщ=1,43-3,10

у=8-25 % where y-combed strips %

2. По рекомендации ЦНИХБИ

Tлен =6 ктекс

d=18  d = 3.5/60=1.05

Еобщ =1,05

у=16-18 % (Handbook of cotton spinning с.166).

3. On the recommendation of «Utex»

Tлен =74 ktex

d=24

Еобщ =1,62

У=17-17,5%

4. In the project we accept

Tлен =74 ktex,

d=24

Еобщ =1,663

IV. Greasing machine E-62

1.Po technical specification

Tлен = 3,0-6,0 ktex

d=8

Еобщ =9-19,3

У= 8 -25 %

2. On the recommendation of the Central Scientific-Research Institute

Tлен =3,5 ktex

d=4

Еобщ =68,6

у= 16-18 %( Shiropov V.P. және т.б. «Handbook of cotton spinning» 166p)

3. По рекомендации  «ЮТЕКС»

Tлен =5,7 ktex

d=8

Еобщ =13,20

у= 17-17,5 %

4. In the project we accept

Tлен =5,8 ktex,

d=24

у=17%

The total extract is calculated for the E-62 combed machine from Rieter.

where a is the tension of the fleece (in-shell) in%, a = 8%

Tension of the fleece between the canvas rollers and feed cylinders

g is the linear density of the canvas, ktex

p – combed sheaves,%

For cotton fiber staple Lsh = 32-34mm we take p = 17-17.5%

S-length of power supply is accepted S = 5.2 mm

in-line tape density, ktex

(Instructions for the operation of the E-62 combed machine.)

We accept the general hood according to the instructions: Е общ.(GV)=13,20

Еобщ.=13,20

V. Tape machine RSV-D-35 «I» transition

1. According to the technical specification

Tлен =1,25-7,0 ktex

d=4-8

Еобщ =4,48-11,69

2. On the recommendation of the Central Scientific-Research Institute

Tлен =3,6 ktex

d=6

Еобщ =6

3. По рекомендации  «ЮТЕКС»

Tлен =5,135 ktex

d=6

Еобщ =6,66

4. In the project we accept

Tлен =5,405 ktex  ;

d=6

VI. Rovnichnaya machine F-11

- According to the technical specification

13

Tров=0,168-1,475 ktex  (168-1475 ktex  )

Еобщ =4-20

2. On the recommendation of the Central Scientific-Research Institute

Tров=0,6 ktex

Еобщ =6

3. On the recommendation of «Utex»

Tров=0,74 ktex

Еобщ =6,939

4. In the project we accept

ktex    Тр=0,744 ktex =744 ktex

VII. Ring spinning machine G-33

1. According to the technical specification   Tпря=4,0-107 ktex

Еобщ=8-120

2. On the recommendation of the Central Scientific-Research Institute

Tпря=18-20 ktex

Еобщ=33,3-30

3. In the project for a linear density of 18.5 tex yarn, we calculate the total stretch

Recommendations for students on preparation for classes: Preparation consists in studying the material of the practical lesson on lecture notes, textbooks and teaching aids.

Technical and tools: spinning

List and types of tasks to perform in the classroom:

- Selection and justification of the linear density and drawing on the transitions 2.Obosnovanie selection of equipment

List and types of homework:

1. Studying the technology of cotton production.

2. Studying the technology of woolly-weaving production.

Assignment for independent work of students (CDS):

- Selection and justification of the optimal plan for the production of yarns

on the basis of technical and economic calculations, taking into account the purpose and quality of products made from yarn.

2. Drawing up a production plan based on an analysis of existing plans and studying the latest technology and technology.

Control questions

1. What machines produce spinning processes?

2. What is the technological process of the carding machine C-60?

3.What is the linear density of the tape measured?

Reporting form: written.

Occupation №4

Theme of the lesson: Study of a roving machine of cotton sprinning. Refueling and yarn production of a given thickness

Lesson plan:

1. Calculation of linear speed and tension of threads on machines of the preparatory department

2. Calculation of the value of the bobbin rate at a time of

3. Calculation of parameters for filling looms

4. The conclusion. Report on the work done.

Goals and objectives of the lesson, skills, competencies: the right choice of process parameters for rewinding the main and weft yarn.

Brief theoretical information

Parameters of rewinding threads in bobbins.

In the technological part of the project, it is necessary to determine the technical parameters of the rewinding of the main yarn (linear speed, tension on the package) on the basis of scientifically grounded normative data and analytical calculations, and also to select the type of knotter and to justify the permissible breaking severity of the yarn when rewinding. In addition, it is necessary to bring the temperature and humidity conditions in the winding

department.

Linear speed of the thread when rewinding. It depends on the type of thread, its physical and mechanical properties and linear density, as well as on the type of equipment used. Applicability of self-winding machines allows to increase the linear speed of the thread, since the removal of the bobbins and the installation of the cartridge are auto-matched.

Threads from different fibers are rewound with the following speeds:

| Yarn and threads | Linear speed of the thread when rewinding, m / min |
| --- | --- |
| Cotton average linear density (10 to 25 tex) less than 10 and more than 25 tex Woolen combed hardware Filaments of chemical fibers (rewinding is rare) Linen average linear density more than 50 tex | 1000-1500 от 600 до 1100 600-800 400-600 400-600 600-800 400-600 |

Based on the selected linear rewinding speed and type of equipment, the rotational speed of the winding drum or spindle of the winding machine or machine is determined.

For winding machines and machines with winding brabanks, the speed of rotation is found from the formula for the linear speed of the yarn:

where D is the diameter of the winding drum, m; - coefficient of sliding between the reel and the winding drum (0,8-0,95); n – the frequency of rotation of the winding drum, min-1; hcp- the average pitch of the screw thread on the winding drum for thread direction, м.

N =

For winding machines and machines, in which the spool is rotating from the spindle, the linear speed of the thread, m / min,

where Dcp is the average winding diameter of the yarn per bobbin, m; n – frequency of spindle rotation, min-1; h-span of the yarn guide, m; pa – the frequency of rotation of the eccentric, min-1.

Location

Dcp = (Dи + Dk) /2

where Dcp is the initial diameter of the winding, m; Dk is the final diameter of the winding, m.

Thread tension when rewinding. It is one of the main parameters of the process. On the one hand, the thread tension must be

sufficient to ensure the required density of winding on the package, on the other hand, it should not degrade the physical and mechanical properties of the yarns. The thread tension during rewinding can approximately be determined from the strength of the yarn

where F is the thread tension when rewinding, Ch; Pn is the strength of the filament, Cn;

- percentage of the tension value from the strength of the yarn.

Usually, the AP ranges from 3 to 7% and less often to 10%. The latter value is set when it is necessary to ensure a high density of winding. When choosing a, it is necessary to take into account the structure of the filament and the elongation. For example, threads that have highly elastic deformations need to be rewound with the minimum possible tension so that the fabric does not shrink in the process of its operation.

The tension at the point of the cylinder farthest from the axis of the spool, (Гх) and at the top of the balloon (Г0), when winding the yarn from the spinning forging, is determined by the formulas of TsKBTM:

16

where To is the linear density of the substrate, tex; K is the empirical coefficient; β – angle of inclination of the thread to the axis of the bobbin; H – cylinder height; r is the radius of the straight pack; v is the linear velocity of the filament, cm / s.

;

where m is the mass of a unit length of the filament; - the angular velocity of the yarn at its reeling.                                 = vsinβ/r

The tension of the yarn when rewinding on machines of the M-150 type can be determined by the VT Kostitsin formula:

where F is the tension of the thread after the tensioner, Ch; FH-tension of the thread to the tensioner, c11 (1-3% of the strength of a single thread, depends on the type of thread and the condition of winding); f – coefficient of friction between the filament and porcelain sleeve-riser (0,25-0,4); a – the angle of the circumference of the strand of the tensioner (from 40 to 90 °); Wo – axial load on the brake washer, depending on the mass of the washers and braking loads, Cn; β is the angle depending on the ratio of the diameters of the riser d and the brake washer D (sinβ = d / D)

Then determine what percentage of the tension of the filament consists of the strength of the yarn:

а = F  * 100/Р.

Tension of the thread taking into account the parameters of the tensioning device (the angle between the planes of the brake washers, the radius of the washers and other

parameters) is determined by the formula

where f1-coefficient of thread bobbing about porcelain riser (0,2-0,32 depending on the type of yarn); f1-coefficient of the thread bobbing on the washer (0,2-0,4); R and – the parameters of the device; Q1 – mass of one brake disc (1.5-2 g); пш – number of cargo washers; g- weight of the cargo washer (3, 4 and 5 g); ψ is the angle between the planes of the brake washers (6-8 °).

Number of load washers to ensure thread tension at

Rewinding

nш =

When rewinding the cotton yarn, the total weight of the washers in the tensioner is set depending on the linear density of the yarn.

The change in the linear speed of the filament during rewinding is connected with the need to change the mass of the washers in the tensioning device. For example, with an increase in the linear velocity of the filament by 100-150 m / min, the total weight of the washers in the tensioning device is reduced by 7-8 g, and with a decrease in the linear velocity by the same amount, the weight of the washers is increased by 7-8 g,

17th

tion with norms.

From the properties and type of thread, the angle of crossing threads of a thread on the surface of a bobbin, the tension and the speed of rewinding, the density of the winding of the package depends;

γ = т / V,

where m is the mass of the filament on the package, r; V is the volume occupied by the thread on the bag, cm3.

Table 1 shows the approximate specific densities of winding packages (cone bobbins) of yarns and threads of some vids.

Breakage of filaments. The discontinuity in the rewinding process reduces the productivity of labor and equipment. The severity of the threads depends on many factors; the type and quality of the fiber, the linear density and quality of the threads, the linear speed of the change, the technical condition of the constructive filling line of the winding machine or machine, the structure of the spinning cob, the technological parameters of rewinding, etc. The measures for reducing the breakdown are important meaning, as with a decrease in breakage, not only the productivity of labor and equipment rises, but also the waste in the winding department decreases, the quality of the harsh tissues improves.

The discontinuity of the yarn for the transitions of the technological process in the weaving industry is established mainly on the basis of the experience of the work of the advanced enterprises. After a long study of the breakage of filaments with the optimal technological parameters of machines (linear

the speed of the thread, the spreading of the gap of the cleaner, the tension of the yarn during rewinding) and the optimum values ​​of humidity and temperature in the shops, approximate values ​​of the breakaway for yarns of various types were established. Analytic determination and prediction of the breakage of yarn from technological process transitions at various parameters of machine operation can be performed with the help of electronic computers. For example, when prerematyvaniya breakage of the yarn y0 depends on the linear speed of the yarn v, the friction force of the y thread, the thread-guiding details of the machine q, the tension of the thread F, the value of the balloon H, and other factors.

In this case, the multifactor dependence can analytically be expressed as follows:

чо = f(v,g,F,Н).

To determine the influence of each factor on y0, it is necessary to compile equations and algorithms for a computer.

Table. 1. The specific density of winding when rewinding

| Cotton carded combed twisted Woolen hardware Half-wool hardware | 83,3-15,4 15,4-5,8 15,4-5,8 50-83,3 100-333 50-83,3 100-333 | 0,40-0,42 0,42-0,43 0,41-0,440 33-0,35 0,32-0.36 0,36-0,38 0,34-0,36 |
| --- | --- | --- |
| Pure Worsted Worsted single twisted Half wool worsted single twisted Linen wet spinning dry Ocheszovaya wet spinning dry Threads viscose acetate triacetate kapron, lavsan from other chemical fibers | 19,2-41,7 15,6х2-41,6х2 19,2-41,7 15,6х2-41,6х2 16,7-290 55,5-1204 55,5-200 83-1204 - - - - | 0,36-0,38 0,40-0,42 0,39-0,42 0,44-0,46 0,52-0,55 0,48-0,52 0,46-0,48 0,43-0,46 0,7-0,8 0,6-0,65 0,7-0,8 0,55-0,65 |

Controlling the thickness of the thread. In the process of rewinding, the thread is controlled in thickness, it removes the probes, cones, incorrectly bound

knots (large size), etc. To do this, use special nategotechisteli consisting of two plates, on the basis of automatic machines, electronic nategotechisteli. The alignment of the plates of the nitrate cleaner, i.e. the size of the gap between the plates b, is established on winding machines, depending on the thickness of the rewound thread and its structure; for thin and smooth filaments b = (1.5 ... 2) d, for medium and large thickness yarns, uneven and fleecy yarns b = (2 ... 2,5) d, where d is the diameter of the yarn.

On the basic automatic machines, mainly photovoltaic and electrical cleaners with a measuring capacitor are used.

Recommendations for students on preparation for classes: preparation is to study the material of the practical lesson on lecture notes, textbooks and teaching aids.

Technical and tools: winding machine

List and types of tasks to perform in the classroom:

1.Explain the process of rewinding threads in bobbins

2. Explain the process of warping the main threads

List and types of homework:

1. Calculation of the coefficients of loading technological equipment.

2. Calculation of the production area and the layout of equipment.

Assignment for independent work of students (CDS):

1. Selecting the parameters of the base of the threads

2. Selection and substantiation of the technological process of fabric production

Control questions

1. What determines the linear speed of the thread when rewinding?

2. What does the breakage of the threads depend on?

3.What types of yarn exist? Reporting form: written.

Occupation №5

Theme of the lesson: Studying the ring sprinning machine. Refueling machine and yarn production of a given thickness

Lesson plan:

- Determination of the main parameters of the structure of the tissue

2. Calculation zapravochnyh drawings, scheduled for the production of tissues.

3. The conclusion. Report on the work done.

Goals and objectives of the lesson, skills, skills and competences: first of all, it is necessary to give a complete characterization of each fabric, i.e., to bring a set of technical indicators, by which it is possible to determine technologically the most correct and economically expedient process of pro-production; the basis of the characteristic should be the state standard that operates in a given period, analogies of tissue samples or data obtained during design; in the characteristics of the fabric indicate the name, art¬¬cule, the purpose of the fabric, the type and characteristics of the fiber used for the warp and weft threads, the characteristics of the yarn or yarn (stern, bleached, dyed, twisted, twist and its direction, tensile length, tensile load and elongation of the filament), the linear density of the filaments.

Brief theoretical information

Fabric parameters.

The linear density of the filament is characterized by the amount of mass per unit length. The unit of measurement is taken as tex-gram per kilometer. T = g/L

where T is the linear density of the filament, tex; L is the length of the filament, km; g – thread mass, g.

To determine the linear density of twisted filaments, it is necessary to know their twisting or the number of torsions per 1 m of yarn. The twisting of twisted yarns is defined as the difference between the initial length of the thread L1 and its length after twisting L2, expressed as a percentage of the original length L1 of the non-twisting yarn:У = (L1- L2) 100/L1 = α100/(250 +α),

where α is the twist coefficient.

20

α=

where Kφ is the actual number of torsions per 1 m; Tf is the actual linear density of the filament, tex.

Linear density for n-fold twisting of identical threads with allowance for twist

Т1ф = Тп-100/(100 –У),

where T is the nominal linear density of a single filament, tex; n is the number of additions in torsion; Y-yarn twisting,%

Determination of the yarn of the fabric. The processing of yarns can be taken from the state standard for fabric, according to the enterprise where this fabric is produced, according to calculations in the design of the fabric or determined according to the sample of the fabric.

When analyzing a tissue sample, the determination is determined by the formula:

warp yarns а0 = (Lо – UT  о) 100 /L0;

filament weft      ау= (Lу-LT у)100/Ly,

where L0 is the length of the straightened warp yarn removed from the fabric;

Lt.o is the length of the tissue sample along the base; LT.y is the length of the straightened weft thread taken from the tissue sample; LT. Y is the length of the tissue sample along the duck.

In addition, the working duck

aу = (В3-Bс) 100/Вз,

where B is the width of the filling of the fabric along the bird, m; All-width of severe fabric, m.

In some enterprises, in particular in cotton mills, yarn processing is determined by the formulas:

Therefore, if in the technical calculation the values of the cut-offs are used according to the data of the factory, it is necessary to establish the formulas by which they are calculated. If they are determined by the last formulas, then they must be recalculated according to the formula:

а0 =1;          оу = 1

Otherwise, the yarns of the basis of openwork, terry, pile fabrics are worked out. It is believed that for the production of 1 m of cloth, the length of the openwork or pile warp thread is 3 m at a0.b = 300%, 5 m at a0.b = 500%, etc. This calculus is caused by a special structure of the tissue.

When determining the filling width for the B3 bird of complex tissue, in the formation of which several systems of basic and weft yarns are involved, the mean value of the duck working is used:

21

where a1, ay2, aYx is the ducking of the first, second x-th system, respectively.

Width of fabric filling on a berry

В3 = Вс/(1-ау/100)

Determine the length of warp threads. The length of the base needed to produce one piece of tissue is determined by the shape

where Lc. – the length of the tissue in the piece.

If several basic thread systems, different in kind of used raw materials and linear density, as well as having different workings take part in the structure of the fabric, then it is necessary to determine the length of the basis of each system of threads necessary for the production of one piece of severe tissue.

In this case, the length of the warp threads of openwork, fleece or terry cloth is calculated by the formula

Determine the number of warp threads in the dressing. Number of background threads

nф = Ро. г (Вг – Вк),

where P0.r is the density of the finished fabric based on the base by 1 cm; Br, - width of the finished fabric, cm; Bk is the width of the edges of the tissue,

Number of threads along the base in the edges nк = Во.кBк,

где Pо.k — the density of the fabric on the basis in the edges of 1 cm.

The width of the edges for the shuttles is taken from 0.5 to 1.5% of the width of the fabric. The density of the fabric but the basis in the edges for shuttle looms is 1.5-2 times greater than the density of the fabric in the background,

P0.k = (1.5 ..2) P0 for an equal linear density of threads for the background and edges (T0 = T0.K). If we use yarns of greater linear density (T0.k> T0), then the density of the fabric along the base in the edges can be equal to the density based on the background (P0.K = P0).

The total number of warp threads in the ‘

п0 = nф + nк.

Calculation of the parameters of the dream. After determining the number of threads in the base, you need to select the method of warping and perform the calculation.

For the partion method of warping, calculate the number of filaments on the reel shaft, based on the volume of the selected creel of the back-up machine. First determine the possible number of shafts:nВ = п0/п,б.ш,

where n0 is the number of warp threads; nb.ш – the maximum number of bobbins on the creel.

If a fractional number is obtained, the nearest larger integer is taken. After this, calculate the number of warp threads on each shaft:nо.B=no/пB,

For the tape method of warping, the number of strands in the belt and the number of belts are calculated. Preliminary, proceeding from the maximum number of bobbins on the scribbler nb, the possible number of tapes is determined:

nл = п0/п,б.ш,

If a fractional number is obtained, then the nearest larger integer is taken.      Number of strands in the tape

п0.л = п0/пл.

With a multicolor base, each tape should have a whole number of rapports of color or type of threads. In the tissues of a complex structure, for which several systems of basic threads are required, which are wound on individual Navoi, the calculation of the deformation is carried out separately for each base.

Calculation of the Bird. For the calculation of a reed, the number of threads traversed in the tooth of the reed for the background zf and the edge Zk are given. Total number of tines

X=- Хф + Хк + Х3.

Where Xf, is the number of teeth for the background of the fabric; Xk- is the number of teeth for the edge of the fabric; Xa is the number of spare teeth.

The number of spare teeth for shuttle machines is taken to be from 5 to 10.

Number of teeth for the background and edge of the fabric

Хф = nф /zф; Хк = пк/zл.

Bird number, i.e., the number of tines of a reed 10 cm,

Nб = (nф   /zф + nK  /  nk) 10/В3,   или   Nб = Ро(1-ау/100)zф,

where Po is the number of warp threads per 10 cm.

The discontinuity of the main yarns when fabric is produced on a loom machine depends on many factors, one of which is the possibility of passing a knot of warp yarns through the tooth of a berd. After determining the number of the reed, it is necessary to determine the filling factor K3 by the knot of the gap between the plates of the teeth of the reed. To do this, find the value of the node on the filament, which is approximately equal to 2.25 d, and the gap between the plastins of the teeth b.

b =100/Nб – b3,

where b3 is the thickness of the tooth plate (depends on the number of the reed and is selected according to the tables

directories).

Coefficient of filling the gap between the tooth plates with a knot

К3 = =2,25 d0 /b = 0,07 С.

If K3> 1, then the passage of the node through the bird is difficult and It is necessary to change the measurement of the berd, so that K3 <1. Calculation of a remise. When calculating the remission, the width of the warp threads of the warp in galevo is determined, the number of hauls in the remise, the density of the halves. The width of the parting of the warp threads in the galleon of the visors is slightly larger than the width of the fabric stuffing along the bird:Вр = В3 + (1…2 см),

where Bp is the width of the threading of the warp threads in the gutter of the vaults,

The number of galevs in the remise

where nr.F is the number of galevs for the background threads; n.k is the number of halos for edge threads.

The number of galevs on each harness

nг.р = nг.Ф + nг.к;  nг.ф = nг.ф / np.Ф;  nг.к = nг.к /nг.к

where nr.f, n.k is the number of galleons on each release, respectively, for the threads of the background and edges;

n. φ, np. K is the number of times for the background and edge warp threads, respectively.

The density of the haloes on each harness

Рг = nг.р/Вр

The density of the gal on each harness must not exceed the permissible norms of density of the gal, namely 12-14 gaoles per 1 cm for filaments of average linear density (up to 30 tex), 8-10 gaoles per 1 cm for filaments of linear density greater than 30 tex.

Calculation of the lamellar device. When calculating the slats, a number of parameters are defined.

The width of the main threading in the lamellar device

Вл = Вр + (1 . . .2 см).

Density of lamellas on each rail

Рл = n0/(пл.РВЛ),

where n l. p is the number of lamellar slats.

The density of lamellas on each rail should not exceed for threads of different linear densities of the following data:

Linear “density of filaments,

Before 10      11—15     16—25     26—50  Over 50 tex

Number of lamellas per 1 cm         14—15      12—14      10—12       8—10	До 8

Recommendations for students on preparation for classes: Preparation consists in studying the material of the practical lesson on lecture notes, textbooks and teaching aids.

Technical and tool means: weaving machines STB

List and types of tasks to perform in the classroom:

1. Calculation of the parameter of preparation of weft to weaving.

2. Calculation of the amount of waste in the winding, rewinding, sizing,

parting and weaving shops

List and types of homework:

1. Calculation of the remise.

2. Calculation of the lamellar device.

Assignment for independent work of students (CDS): 1. Calculation of the coefficients of loading of technological equipment.  2. Calculation of the production area and equipment layout.       Control questions 1. What do I need to know to determine the linear density of twisted yarns? 2.Which formula determines the width of the filling of the fabric on the bird? 3.What kinds of tissue exist? Reporting form: written.

Occupation №6

Theme of the lesson: Studying the pneumomechanical sprinning machine. Drawing up the technological scheme. Refueling calculation MRP.

Lesson plan: 1. Determination of the weight of the roving on the coil

2. Analysis of the severity of the filament

3. Calculation of the linear density  of the roving,

4. Conclusions and a report on the work done.

Goals and objectives of the lesson, skills, skills and competences: torsion is one of the most important processes of direct production; the goal of roving is to create a product of the required minimum strength from comparatively short fibers, which will eliminate its discontinuity during transporting, as well as when winding in spinning on a spinning machine.           
Brief theoretical information

The weight of the roving on the spool has a significant effect on the efficiency of cotton spinning. The larger the mass, the longer the time it takes to form a roving machine, the less time you need to stop the machine for removing and loading the connectors during the shift, the higher the productivity of the roving, the smaller the number of rolls is in circulation in the production, the roving coil will last longer operate on the circular spinning machine, reducing the worker’s time to replace the worked coils by full and increasing the time for the spinning machine to service the circular spinning machine, i.e. increasing the productivity of her labor.          The weight G of the roving on the coil is,

G = Vγ,

where γ is the roving winding density, g / cm3; V is the volume of the roving on the coil,     cm3 (see Fig. 1):

Fig. 1. Structure of the body of the roving winding

where Dn is the diameter of the complete coil, cm; dk is the diameter of the coil, cm; Hn – total winding height, cm; H0 is the height of the cone of the winding body,

Recommended density of winding rovings for different linear densities is presented in Table. 1.

Table 1. Row winding density of different linear density

| Linear density of roving, tex | 1000 | 500 | 250 | 170 | 125 | 100 | 85 | 60 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Roving winder density, g / cm3 | 0,28 | 0,29 | 0,32 | 0,34 | 0,36 | 0,38 | 0,4 | 0,42 |

The density of the roving winding largely depends on its tension during the winding of the package, and the tension in turn is determined by the speed of the spindles. Recommended speed mode roving machines of domestic production is presented in Table 2.        Table 2. Characteristics of the winding body of the roving on the coil and the rotational speed                               spindles of leveling machines of models Р-260-3 and Р-260-5

| Model machines | Linear density rovings, tex | Diameter of the complete coil and winding height, mm | Package weight, г | Rotational frequency of spindles, min-1, when producing roving from cotton |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | medium-fiber |  | fine-grained |  |  |
|  |  |  |  | with the diameter of the spindles |  |  |  |  |
|  |  |  |  | 19 мм | 25 мм |  | 19,мм | 7.5 мм |
| Р-260-3 | 1430-589 | 166x300 | 1100 | 740-850 | 600-740 |  | - | - |
| Г-192-3 | 1430-400 | 145x250 | 800 | 840-900 | 700-800 |  | - | - |
| Р-192-3 | 400-250 | 145x250 | 900 | 900-1000 | 800-900 |  | - | - |
| Р-168-3 | 1430-211 | 130x250 | 700 | 900-1000 | 800-900 |  | - | - |
| Р-168-3 | 742-211 | 115x225 | 500 | 1000-1100 | 900-1000 |  | ~ | - |
| Р-168-3 | 211-100 | 105x200 | 400 | 1100-1200 | 1000-1100 |  | - | - |
| Р-260-5 | 1430-1000 | 155x300 | 1000-1200 | 600-700 | 700-800 |  | - | - |
| Р-192-5 | 1430-1000 | 140x250 | 850 | 600-700 | 650-800 |  |  | - |
| Р-26С-5 | 850-750 | 155x300 | 1000-1200 | 750 | 900 |  | - | - |
| Р-192-5 | 850-750 | 145x300 | 1000 | 700 | 900 |  | - | - |
| Р-260-5 | 650-500 | 155x300 | 1100-1300 | 800-850 | 1000 |  | 800-850 | 900-1000 |
| Р-192-5 | 650-500 | 140x250 | 900 | 800-900 | 1000 |  | 750-850 | 900-1000 |
| Р-192-5 | 400-286 | 140x250 | 850 | 900 | 1100 |  | 900 | 1000-1100 |
| Р-192-5 | 286-182 | 135x300 | 1150 | - | - |  | 800-900 | 1050-1200 |

Knowing the linear density of the roving produced according to the spinning plan and the model of the roving machine, the technologist chooses the optimal spindle speed taking into account the designed size of the package. The size of the roving package is selected taking into account the conditions for placing it in the feeder of the spinning machine.

Recommendations for students on preparation for classes: Preparation consists in studying the material of the practical lesson on the abstracts

lectures, textbooks and teaching aids.

Technical and tool means: roving machine

List and types of tasks to perform in the classroom:

- The maximum size of packages and the conjugate length of threads on

them.

2. Study of equipment for rewinding yarn.

List and types of homework: 1. Calculation of the rate of productivity of a roving machine 2.Selection of the value of twist roving

Assignment for independent work of students (CDS): 1. Constructive and technological features of the roving machine 2. The basis for choosing a model of a roving machine.       Control questions 1. What is the purpose of roving machines in the technological process of spinning production? 2.Why does the spinning shop depend on the progress of the whole technological process and the quality of the yarn?3. What are the basic rules for safe operation on a roving machine?

Reporting form: written.

Occupation №7

Theme of the lesson: Study of ribbon-connecting, canvas-drawing and combing machines of cotton sprinning. Determination of the quality of carded paper and the percentage of combed fleece

Lesson plan:

1. Familiarization with the construction of a stationary high-speed auto-puller of cobs on a circular spinning machine.

2. Selection of the design of the hood.

3. Calculation of the parameters of the drawing process.

4. Conclusion. Report on the work done.

Goals and objectives of the lesson, skills, skills and competencies: equipping ring spinning machines with exhaust devices; their design as the technology of spinning improves.

Brief theoretical information

On circular spinning machines it is necessary to distinguish between thinning

Product:

U = Tpd/Tn

and extracting the product in the extractor:

Е = U/Ky,

where d is the number of product additions (the number of foldable slices from rovings); Tp is the linear density of the roving, tex; Тп – linear density of a yarn, tex;    Ku – coefficient of yarn shrinkage from twisting  (Ку ≤ 1):

Ку = 1-10-2Ук.

Shrinkage shrinkage can be calculated from the form,  %:

Уk =100 = (1-Ку)100,

where l0 and l are the lengths of the corresponding sliver and yarn from it.        The shrinkage of yarn from twist can also be calculated according to the form  F. Afronchikova:

The coefficient of twist can be calculated by the formula of KI. Koritsky:

where the coefficient of twist yarn in the system, tex.

Extractor between the supply and exhaust cylinders of the traction device according to the transmission scheme:

where dvy and dpit are the cylinder diameters of the front (exit) and rear (supply) respectively; iinit-vyp – gear ratio from the rear cylinder to the front; C is the drawing constant for the kinematic scheme of the extractor; Za – the number of teeth of the replacement exhaust gear.

In the course of designing, it is recommended to be set by a general pull in the exhaust device, taking into account its technical capabilities, length

the fiber to be processed, the linear density and the expected uniformity of the yarn produced. Then determine the required linear density of the roving, using the above formulas. When choosing a general exhaust, one should take into account the fact that the thinner the strands and the longer the fiber, the more general the exhaust can be. When producing yarn from a shorter fiber on a spinning machine, the hoods are smaller, as the drawing conditions deteriorate, which can lead to a reduction in yarn quality (an increase in unevenness from stretching) and an increase in breakage. Great importance for improving the quality of yarn and reducing the severity of breakage has the issue of distributing the overall hood to a private one. Recommendations for the selection of private extracts are presented in Table. 1.

Table 1.

Recommended private extractor hoods

| Extractor type | Carded spinning system |  | Combed spinning system |  |
| --- | --- | --- | --- | --- |
|  | general exhaust | Private exhaust in the rear stretch zone | general exhaust | Private exhaust in the rear stretch zone |
| ВР-1- SPLM | 30 40 | 1,3-1,8 2,04-2,4 | 40 40 | 2,2-2,6 2,7-2,8 |
| ВР-3-45P | 30 35 40 | 1,1-1,2 1,2-1,3 1,3-1,4 | 35 40 45 | 1,2 1,4 1,4-1,8 2,0-2,5 |

When using the exhaust unit BP-1-UZM, the rear private extract is selected such that the extract in the front stretching zone does not exceed 16-19.

In accordance with the accepted private hood, recommendations are given for setting the type of clips (Table 2) and spreading in the rear zone of the extractor (Table 3) (wiring in the front zone is constant).

Table 2. Recommended clip types on the upper strap

| A type exhaust device | Mountable clips | Factory designation | Clearance, mm | Linear density of yarn, tex |
| --- | --- | --- | --- | --- |
| ВР-3-45П | blue white black | 2 3 4 | 2,5 3,3 4,3 | 11,8 and less 18,5-15,4 25 и более |

Table 3. Recommended wiring in the rear extraction zone of the exhaust

device

| A type exhaust device | Wiring, mm |  |  |  |
| --- | --- | --- | --- | --- |
|  | private hood | general exhaust |  |  |
|  |  | before 20 | 25-35 | 35-45 |
| ВР-3-45P | 1.1-1,4 2,0-3,0 | - | 51 | Lшт +(4-5) L шт+2 |
| ВР-1-UZM | до 2 2,0-2,5 2,5-3,0 | Lшт +(6-7) - - | Lшт +(4-5) Lшт +(3-4) - | Lшт +(4-5) L шт+2 L шт+2 |

Recommendations for students on preparation for classes: Preparation consists in studying the material of the practical lesson on lecture notes, textbooks and teaching aids.

Technical and tools: spinning machines      List and types of tasks to perform in the classroom: 1. Introduction to the design of the exhaust unit BP-3-45P 2. Calculating the twist of the yarn of the circular spinning method      List and types of homework:

1.Select the type of spindles and cartridges

2. Determination of the volume and mass of the full cob yarn

Assignment for independent work of students (CDS):

1. Constructive and technological features of spinning machine

2. Calculation of the required yarn breaking load

Control questions

1. What is the purpose of spinning machines in the technological process of spinning production?

2.Why from the spinning shop depends the flow of all

technological process and quality of yarn?

3. What are the basic rules for safe operation on a spinning machine?

Reporting form: written.

Occupation № 8

Theme of the lesson: Acquaintance with the assortment of the shaped yarn and the machine of shaped torsion

Lesson plan:

1. Selection of the type and diameter of the spinning ring

2. Familiarization with the design of the slider

3. Calculation of the necessary mass of the slider on the computer

4. The conclusion. Report on the work done.

Goals and objectives of the lesson, skills, skills and competencies: production program; use of mathematical methods and computers in product planning.

Brief theoretical information:

1. 
Data input:Tn; Pyrt; Zp; Cp; ZQ, CQ; пв; Dk; A; f.

2. 
Calculation of parameters: Рп = Ру.пТп

Е – 1+0,01ZQCQ

G = 1-0.01ZpCp

Kз.п(min) = E/G

Entering a value  Кз.п   ≥ Kз.п(min),

_         _

Qn = Pn/ Кз.п

Rk = 0.5Dk

r = RkA

k = 2.5 – 0.8A

B =

Ф = k(B+A/f)

_

Qx = Qn/k

_

CБ =

mБ =

3. Notation: Тп – linear density of a yarn (it is set by the designer), teks;       Rup is the minimum allowable specific breaking load of the yarn, Cn / tex (selected according to GOST for yarn);       C – quadratic unevenness for tensile strength of the yarn,% (selected in accordance with GOST for yarn); Zp and ZQ are the coefficients characterizing the limit deviations accepted in the calculation, respectively, of discontinuous load and tension 30

yarn from mathematical expectation;

C – the square unevenness of the tension of the yarn between the runner and the cartridge,% (taken in accordance with the condition 10≤Co≤50);

DK is the diameter of the ring, m (selected in accordance with the maximum permissible linear speed of the runner to 40 m / s);

RK is the radius of the ring, m;

r – radius of the cartridge, m (selected depending on the diameter of the spinning ring and the spindle structure);

A is the ratio of the radius of the cartridge to the radius of the ring A = sinα = r / R (according to the studies “Brackcr service” (France) [21] it is established that the angle α affects the tension of the yarn in Fig. 1). Recommended ratios of the diameter of the cartridge to the diameter of the ring are shown in Table 1; f is the friction coefficient of the runner on the ring; depending on the quality of the surface of the ring and the runner, the speed and type of the runner take f = 0.2-0.3; Nb is the spindle speed, min-1 (calculated in dependence on the received diameter of the ring, yarn tension between the runner and the cob, and the safety factor of the yarn); k-coefficient, taking into account the friction of the yarn about the slider (calculated by the formula 10.22); Qx is the permissible average value of the vertical composition of the yarn tension in the cylinder without regard to air resistance, Cn (calculated);

Fig. 1. Change in the ratio of the diameter of the winding coil

to the diameter of the ring

СБ – allowable centrifugal force of the runner without resistance air rotation of the balloon, Cn (calculated);      m6 – the necessary mass of the slider for the received diameter of the ring and the speed of rotation of the spindle (sought), г.

Table 1.

The recommended ratio between the diameters of the cartridge and the ring

| Assessment of the state | The ratio of the diameter of the cartridge d to the diameter of the ring DK | Angle a, degree, |
| --- | --- | --- |
| very good good normal | 0,52 0,50 0,47 | 31 30 28 |

Recommendations for students on preparation for classes: Preparation consists in studying the material of the practical lesson on lecture notes, textbooks and teaching aids.

Technical and tools: spinning machine

List and types of tasks to perform in the classroom: 1. Design of the composition of the mixture by computer 2. Study of factors influencing the yield of yarn      List and types of homework 1. Calculation of the required yarn breaking load 2. Evaluation of the quality of the mixture and its components

Assignment for independent work of students (CDS): 1. Automation of a pneumomechanical spinning machine 2. Automatic cleaning of spinning chambers

Control questions

1. What is the purpose of a computer in the technological process of spinning production? 2.Why depends on the work of the spinning shop depends the flow of all technological process and quality of yarn?

3. What are the basic rules for safe operation on a spinning machine?

Reporting form: written.

Occupation №9

Lesson Topic: Familiarization with the bulkhead and knotting machines

Yarn tension calculation Lesson plan:

1. Characteristics of runners and features of their application

2. Calculation of the maximum yarn tension

3. The conclusion. Report on the work done. Goals and objectives of the lesson, skills, skills and competences: the need differences in thinning on ring spinning machines; during the design it is recommended to be set by a general exhaust in the exhaust device; the influence of twist on physical and mechanical properties yarn.      Brief theoretical information       The tension of the yarn when winding on the cob in the “runner-cob” zone is calculated using the relationships.                                  Р =  Qσμ≈ Qxeμ

Qx = QБcosα;

К =

the coefficient K can be calculated from the formula:

K = 2,5-0,8sinγ;

sinY=r/RK,

where Р – tension of the winding of the yarn in the zone of “runner-pocheta”, Cn; QB – tension of the yarn in the balloon at the runner, Cn; Qx – the projection of the yarn tension in the cylinder on the spindle axis, Cn; α is the angle between the tangent to the balloon at the runner and the vertical axis, deg .; μ is the coefficient of friction of the yarn about the slider; - the angle of coverage of the runner with a thread, deg .; γ- is the angle between the direction of the yarn to the percha and the radius of the ring passing through the slider, deg .; SB-centrifugal force of the runner, Сн; m6 is the weight of the runner, g; V6 – speed of runner, m / s; Rk is the radius of the ring, m; r is the radius of the winding coil, m; f is the coefficient of friction of the runner on the ring

(f = 0,2—0,3).

The thread tension in the “runner-cartridge” zone can be determined according to the formula Voroshilov, Сн:

where , - angular velocity of the runner, c-1.

Taking ≈, find:

Yarn in contour motion along its longitudinal axis quickly

rotates around the axis of the spindle. In this case, the section of the thread between the thread guide and the runner is bent under the action of forces acting on the elements of this section: the centrifugal forces of air resistance, the weight of the thread, and the Coriolis force.

It can be assumed that the curve of the section of the filament describing the balloon during rotation is a sinusoid. Approximately, it is described by the equation:

where У- ordinate of the balloon (radius of rotation of the element of the section); x is the abscissa of the balloon, directed along the axis of the spindle (distance from the top of the balloon), cm; Rk is the radius of the ring, cm; h-height of the balloon, cm; a is a parameter, cm-1, equal to:

а=

m = 10-8T

where  m – weight 1 running. Cm of yarn, kg / cm; T – linear density of yarn, tex; - the angular velocity of the runner, c1; Qx – the projection of the yarn tension in the balloon at the runner on the spindle axis, Сн.

The maximum radius of the cylinder at sin (ax) = 1:

One of the reasons for the breakage of the yarn during the winding process on the cartridge of the circular spinning machine is the jamming of the runner on the ring. The kinetic energy developed by the runner at high speed and instantaneous braking is converted into a braking operation, the strength of which many times exceeds the breaking load of the yarn (F >> Ppp).

Braking force of the runner, Sn:

F = m6 аl0-1,

Where m6 — weight of the slider, g; a – negative acceleration of the runner, м/с2:

а = V6/t,

where  V6 – speed of the runner when winding, m / s; t – sluggish time of the slider, с:

t=S6/V6,

where  S6 — braking path of runner, м.

Since the braking force is much greater than the breaking load of the yarn, the yarn breaks sharply when the runner brakes abruptly.

Recommendations for students on preparation for classes: Preparation consists in studying the material of the practical lesson on lecture notes, textbooks and teaching aids.

Technical and tools: spinning machines

List and types of tasks to perform in the classroom:

1. Calculation of the thread tension in the “runner-cartridge” zone

2. Study of factors affecting the breakage of yarn

List and types of homework:

1.Increase of product outlets from raw materials without deterioration of its quality

2. Increase in CPV and the rate of productivity of machines

Assignment for independent work of students (CDS):

1. Analysis of the output of yarn from the mixture

2. Study of the influence of twist on physical and mechanical properties

yarn.

Control questions

1. What is the purpose of spinning machines in the technological process of spinning production?

2.Why from the spinning shop depends the flow of all

technological process and quality of yarn?

3. What are the basic rules for safe operation on a spinning machine?

Reporting form:

Occupation № 10

Theme of the lesson: Study of a weft-winding automatic machine

Lesson plan:

1.Calculation of the diameter of the spinning chamber

2. Calculation of the maximum permissible rotational speed of spinning chambers

3. Analysis of linear flux density of the tape in different zones

4. The conclusion. Report on the work done.

Goals and objectives of the lesson, skills, skills and competencies: determining the power consumed by the camera; A yarn of small linear density can be produced using spinning chambers of smaller diameter; the proportion of the wrapping fibers is less, the smaller the length of the fibers, the smaller the yarn forming zone in the spout of the spinning chamber.

Brief theoretical information

In the cross section of the fibrous ribbon, formed in the groove of the spinning chamber, there are mv.d fibers.

A portion of the fibrous ribbon, consisting of the fibers of the base wedge in the groove, normally curls to form the inner, rod, part of the yarn. In form, this ribbon resembles a spiral metal shaving formed when the roller is turned on a lathe.

Part of the fibers inevitably falls into the point of removal of the fibrous ribbon from the gutter, and the ends of these fibers, caught in the same bag after the removal point, are captured and carried away by the yarn. Such fibers wind in different directions onto the ballooning section of the yarn, forming the so-called , winding fibers. The proportion of such spinning fibers in the yarn is determined capture factor in the pick-up area:

kз,с = lM /(2-DK),	                                                         where  lM -  modal fiber length., мм.

In those cases where the speed of the surface of the rotating fiber ribbon is greaterthan the speed of the fibers on the inner conical surface of the chamber tothe trough, it is possible to twist the curled fibrous ribbon to the areas of these fibers, i.e. the appearance of coiled fibers in the formation zone [5, p. 94]. Their share in the yarn is determined coefficient of zahhvata in the formation zone:

Where  lф — length of the formation zone, мм.

Therefore, the total length of the coiled fibers in the number of fibers of the cross section of the yarn is equal to the total coefficient of entrainment of the fibers

The twist of the core part is equal to the nominal twist for the yarn of a given linear density

Кст = К.

Coefficient of twist of the core of the yarn:

Number of fibers in cross section and linear density:     - core part:

mст = mn (1-k); Tст = Тп(1,kз)

- casing:

moб = mпkз; Toб = Tnkз

The presence of stranded fibers in the yarn structure leads to a great unevenness in the resistance of different fibers to stretching and reduces the strength of the yarn. For this reason, when forming yarn, it is necessary to inform her of increased twist.

Recommendations for students on preparation for classes: Preparation consists in studying the material of the practical lesson on lecture notes, textbooks and teaching aids.

Technical and tools: spinning machines

List and types of tasks to perform in the classroom:

1. Determination of the proportion of the sintered fibers

2. Use of new types of raw materials

List and types of homework:

1.Designing the composition of fiber mixtures and the properties of yarn

2. Factors affecting the quality of yarn

Assignment for independent work of students (CDS):

1. Analysis of rational use of raw materials

2. The influence of fiber properties on the properties of yarn

Control questions

1. What is the formula for the twist factor of the core of the yarn:?

2.What is the technological calculation of the spinning machine?

3. What determines the proportion of the fibers?

Reporting form: written report

Occupation №11

Theme of the lesson: The device and work of the loom. Cardboard packing  and fabric production time

Lesson plan:

1. Determination of the degree of caving

2. Calculation of machine performance

3. Calculation of the time of the canvas

4. The conclusion. Report on the work done.

Goals and objectives of the lesson, skills, skills and competences: the design of the trephine machine; machine operation; technological process of the machine.            Brief theoretical information   Rotational speed of the bobbing and rolling shafts:

565  мин;

950   мин;

990  мин;

565  мин;

Linear speed of rollers 3,140,23010,467,55 м/мин

Determination of degree of caving

The degree of fiber shaking is defined as the number of strokes per unit mass (1 g) of the fiber beard

S3n/,

Where S – the degree of cadence, the number of strokes per gram of fiber beard; 3 – number of the shaft of the trepal; n – rotational speed of the trephle, min-1; - linear density of the canvas, ktex – linear speed of rolling rolls, m / min. Degree of trephination with a planned trephal at a linear density of the canvas 400 ktex

S0.985 уд/г

needles

S1,02 уд/г

Calculation of machine performance

Productivity refers to the amount of output produced by the machine per unit of time (per hour).

, for 1 hour – a canvas with a length of * 60. The weight of build-up canvases in kilograms will be equal to their length in apportrs, multiplied by the linear density of the canvas in kiloteks.d For one revolution of rolling shafts, the machine produces a canvas with a length of

Theoretical performance of the machine, кг/ч

П*60T/1000;

П7,55*60*400/1000180 кг/ч.

In fact, the machine has stops for cleaning, lubrication, removal of waste, minor repairs, which reduce the machine’s production capacity. Therefore, in order to obtain the rate of machine producibility, the theoretical productivity is multiplied by the coefficient of useful time (CPV), taking into account the specified idle time.

For the trepal machine, the CPV is 0.92-0.95, the productivity norm

НПК

Н180*0,94169,2 кг/ч.

Estimated productivity Pr takes into account planned pro¬stoy for capital and medium repair, general cleaning.

ПНК,

Where  К- coefficient of operating equipment.

Coefficient of machine use

К КК

Then

ППК,

at                  К0,95

К 0,94*0,950,893and

П180*0,893 160,7 кг/ч.

when calculating the time of the canvas

Canvas Time

tL/,                                                                                 where Lx — canvas length, м,

L16,5*1000/40041,25 м,

Where  16,5- weight of the canvas, kg; 400 – linear density of the canvas, ktex.

T41,25/7,55  5,46 mines

Recommendations for students on preparation for classes: Preparation consists in studying the material of the practical lesson on lecture notes, textbooks and teaching aids.

Technical and tools: trellis      List and types of tasks to perform in the classroom: 1. Studying the design of the treble machine T-16 2. The designation of the Trepalum Bumblebee Machine TB-3

List and types of homework:

1. The designation of the treble machine MT

2. Design and function of the Condenser of the pneumatic fiber distributor RIP-2

Assignment for independent work of students (CDS):

1. The composition of the trephining machine

2. Automated disintegration-trehpal aggregate

Control questions

1. What is the purpose of the trephine machine?

2. What are the basic rules of safe operation on the trehalnoy machine?

3. Give the formula for the theoretical performance of the trephine machine.

Reporting form: written.

Occupation №12

Theme of the lesson:

Study of a warp knitting machine with hooked needles. Acquaintance with the machine with reed needles

Lesson plan:

1. Design features of circular spinning machines

2. Choosing the length of the circular spinning machine

3. Calculation of the rope tension

4. Conclusion. Report on the work done.

Goals and objectives of the lesson, skills, abilities and competences: calculation of twist, number of tines of the torsion gear, speed of the front cylinder; calculation of drawing and number of teeth of exhaust gears; calculation of the productivity of the spinning machine and the operating time of the cob.

Brief theoretical information

The machine produces the main yarn15,4 tex from the roving 616 tex, the length of the fiber is 31/32 mm, the diameter of the ring is Dk = 44.5 mm, the hoist of the ring bar is 230 mm, the mass of the yarn on the ear is g = 90 g; the block diameter is 150 mm. Rotational frequency of the spindle when the body is ground

when you work the cob

Calculation of the twist, the number of teeth of the torsion gear, the speed of the front cylinder. According to the reference tables, depending on the linear density of the yarn and the length of the fiber, there is a twist factor

Then twist

;

Twist can also be determined by another formula

where i1 is the gear ratio from the front cylinder to the spindle; - yarn shrinkage factor (0.96); - diameter, mm, and the speed of the front cylinder,

Where  36900 – constant twist.

Number of teeth of torsion gear

Speed ​​of front cylinder

Linear speed of yarn release

Calculation of the draft and the number of teeth of the exhaust gears. The expansion between the second 2 and the rear 3 exhaust pairs

When .   .   . 53 exhaust

Where 73,82-  drawing constant in the rear zone.

Extractor between front 1 and second 2 exhaust bunks

When   . . . 80  exhaust

When  716,4 — drawing constant in the front zone.

General exhaust in the extractor

Е=

Where  52921,1 — 
constant of general drawing.

The total extract can be determined from the ratio of linear densities

Where зуб.

Private hoods

General exhaustion as a product of private

E=246·16,3=40.

Calculation of the productivity of the spinning machine and the operating time of the cob. Theoretical productivity 1000 ve

or ;

или

Theoretical productivity 1000 spindles

, или

или

Theoretical productivity of machines is greater the higher the frequency rotation of the spindles, the greater the linear density of the yarn and the smaller the twist.   The rate of production of 1000 spindles at Qt = 0.97.

H=10,2·0,97=9,9 кг/ч.

Estimated productivity at

Кр.о.=0,96.

40

Пp=10,2·0,93=9,5кг/ч,

Where  0,93 — coefficient of machine utilization(0,97·0,96=0,93).

Cob run time

Recommendations for students on preparation for classes: preparation is to study the material of the practical lesson on lecture notes, textbooks and teaching aids.

Technical and tools: spinning machines

List and types of tasks to perform in the classroom:

1. The complex effect of the length of the balloon, the diameter of the ring and the number of the runner on the speed of the spindles

2. Selection of optimal working conditions for the “ring-runner” pair

List and types of homework:

1.Construction of runners

2. Feeding belts for pneumomechanical spinning machines

Assignment for independent work of students (CDS):

1. Flow parameters of fibers in a spinning device

2. Analysis of the extraction sequence

Control questions

1. What is the purpose of spinning machines in the technological process of spinning production?

2. What are the basic rules for safe operation on a spinning machine?

3. The formula of the general drawing in the extractor

Reporting form: Written.

Occupation № 13

Theme of the lesson: Study of the round-loop machine.  The development of a stocking or a sock.

Calculation of the tissue of a given order of the phase of the structure Lesson plan:

1.Examination of designing a raincoat with a supporting surface of the main threads.

2. Determination of the height coefficient of bending waves in the fabric to obtain tissue of a given order of the phase of the structure

3. Study of the structure of the fabric produced by the twill weave (twill 3/1)

4. The conclusion. Report on the work done.

Goals and objectives of the lesson, skills, skills and competencies: to determine the coefficients of the height of the bending waves in the fabric; for fabric design

Given the order of the phase of the structure, it is necessary to know its purpose; In addition, some other parameters must be specified or selected from the working experience: the type of threads and the coefficients of changing the dimensions of their transverse

cross-sections, linear density of filaments or surface density of the fabric, which allows to determine the required linear density of filaments for obtaining tissue of a given order of the phase of the structure.

Brief theoretical information

For such a fabric, it is advisable to choose the order of the phase of the structure close to

VII. We take Φ = 6.8.

To design a raincoat, we use complex polyester yarns of equal linear density in the base and weft.

Additional parameters can be:

linear density of threads; in this case it is not difficult to design a cloth of a given order of the phase of the structure and to determine all the basic parameters;

the surface density of the fabric, on the basis of which it is possible to determine the required linear density of the filaments.

Let the surface density of lightweight raincoat

gT = 110-115 г/м2.

Fabric designing is carried out in the following order.

- Determine the height coefficients of the bending waves in the fabric

2. According to the design conditions of raincoat fabric from polyester yarns

То=Ту=Т;  Ту = Т; dо=dу и  Кd=dо/dу=1.

3. 
According to Table. 2 for polyester filaments, we choose C = 1.28.      4. Based on previous studies and work experience, we accept a change in the transverse dimensions of polyester yarns in the fabric, which assume an elliptical shape:

When the tissue is formed, the filaments within the complex are more dense and the average diameter of the filament in the tissue is reduced:

Figure 1. Location of elliptical filaments

5. Considering that the raincoat should be dense, take it

the following filling factors: 0.8.

Total factor of tissue filling

6The fabric is produced by a twill weave (twill 3/1) in which

и

7. 
The maximum density, the fabrics on the basis and the weft must be calculated through the average diameter of the yarn,

If there are long overlaps in the weave, the elliptical threads of one system are located along the bending generatrix of the filament of another system (Fig. 1). The distance between two neighboring strands AB can be determined approximately by the formula

The geometric density / 0 in this case will be determined by formula

8Determine the actual density of the fabric, taking into account the filling coefficients:

9. The linear density of the filaments is determined by the average diameter of the filaments:

10. 
We find the actual geometric density at the intersections:                                                                                   11.Определяем  уработку  нитей  основы

cutting by, we get

12. Determine the working out of the weft threads:

cutting

2dcp,  
we get

Determine the diameter of the filament, substituting all the data obtained in the formula

surface density of tissue:

Linear density of a thread

The industry produces polyester complex yarns T = 9 tex. Hence the diameter of the thread is 0.0316 • 1.28 / 9 = 0.1213 mm.   14.

Determine the density of the fabric on the basis and weft:    Po = 82.74 / 0.1213 = 682 threads per 10 cm; we take P0 = 680 threads per 10 cm.    Py = 56.83 / 0.1213 = 468 threads per 10 cm; we take Py = 470 threads per 10 cm.   15. Find the surface density of the tissue:            .

16. 
Determine the thickness of the fabric:

Recommendations for students on preparation for classes: Preparation consists in studying the material of the practical lesson on lecture notes, textbooks and teaching aids.

Technical and tools: weaving looms АТ-100-5М

List and types of tasks to perform in the classroom:

1. Selection and substantiation of the scheme of the technological process of fabric production.

2. Parameters of wiring and tying the main threads.

List and types of homework:

1. Parameters of duck preparation for weaving

2.Technical control in weaving production

Assignment for independent work of students (CDS):

1. Designing the basic properties of tissue

2. Classification of fabrics by mutual arrangement of threads

Control questions

1. What is the purpose of weaving machines in the technological process of weaving?

2.Why from the work of the weaving department depends the flow of the whole technological process and the quality of the yarn?

3. The formula for the duck yarn

Reporting form: written.

Occupation №14

Theme of the lesson:  Study of the device and operation of a round

Lesson plan:

1. Calculation of the composition of the mixture of hardware yarn for the woolen coat of the drape group

2. Study of the structure of a two-layer fabric

3. The conclusion. Report on the work done.

Goals and objectives of the lesson, skills, competencies: it is required to design a wool coat double-layer fabric with a surface density of 600 g / m2; determine C for the yarn before weaving: C = 1,13 / where is the average density of merino wool in yarn; n1- the share of merino-fiber in yarn; - the average density of the nitron in the yarn; n2 is the fraction of nitron in the yarn. C = 1,13 / 4. Conclusion and report on the work done.

Brief theoretical information  We design a two-layer fabric:

- the density ratio

Pо1/Pо2 = Kpн  = 1.  Pу1/Pу2 = Kpу = 1.

Б) 
ratio of the estimated diameters of threads to weaving

Кdо = Kdу = dh1/dh2 = dу1/dу2 = 0,93dу1;

Откуда  dо1 = 0,93dо2; dо2 = 1,075 da1.

Dу1 = 0,93dу2; dу2 = 1,075 da1.

Where dо1, dу1 – calculated diameters of warp threads and weft of the upper (first) layer; dn2, dа2 – the calculated diameters of the warp threads and the weft of the lower (second) layer.

Kd1  = dо1/dу2 = 1      dо1 = dу1

Kd2 = dо2/dу2 = 1       dо2 = dу2

The woolen yarn of the apparatus spinning method in the fabric preserves an approximately cylindrical shape. We take the coefficient of variation of the cross-section of the filaments for the upper and lower base ηο1 = ηο2 = 0.9, for the upper and lower weft ηy1 = ηy2 = 0,88;

The diameter of the filaments before weaving can be expressed in terms of the average calculated diameter of the yarn, substituting in the formula the values ​​of the diameters of the filaments expressed through the diameter of the upper base (d0l):

=

Dо1 = dу1 = dсp/1,0375 = 0,964 dсp;

Dо2 = dу2 = 1,075dh1 = 1,075∙0,964 dсp=1,037 dсp;

The diameters of threads in the fabric can be determined by taking into account the coefficients of changing the dimensions of the yarns in the fabric:

The average diameter of the yarns in the first layer of fabric

| Fig.1. Geometric model of the structure of a two-layer fabric in case of overlapping layers of twill 2/2; a – along the base; b-along duck | The average diameter of the filaments in the second layer of the fabric From the recommendations of the Central Research Institute of Wool for the fabrics of the drape group, we accept the following changes in the fabric in the finish: shrinkage of the fabric along the length Uo = 14%, shrinkage of the fabric in width Uy = 25%, weight loss in finishing βm = 15%. The fabric of the drape group is designed to design V of the order of the phase of the structure: Khol = Khy1 = 1, Ф = 5. |
| --- | --- |

Since the fabric has a large shrinkage in the finish along the length and width, we take the following factors for filling the harsh cloth: Who1 = 0.64; Knu = 0.73. For the upper and lower layers we take the weave twill 2/2, linking the layers from bottom to top, ie the lower base to the upper duck. To calculate the yarn processing in the fabric, we use a geometric model of the structure of the tissue (Fig. 1). First, we determine the working out of the first basis.

Lengths  
we define by the formulas.

Where    since the order of the phase of the structure of the fabric for the upper layer is pierced.

Delivering the values ​​of u, we obtain.

The length of the tissue within the duck rapport    Lry1 = Lm.o1 = Lmo2 = 2.674dsp + 2.079 dsp + 2.035 dsp + 1.161 dsp = 7.949sp    The length of the filament of the first base in the fabric is also determined using the mean diameter of the yarn weaving thread. To do this, we find the length of the strands of the strand bc and de: where

The length of the first warp thread

Thread on the first basis to decrease.

To determine the development of the second basis, it is necessary to establish the basic parameters of the structure of the second layer.

To determine the coefficient of filling of the tissue by the weft and the actual distances between the threads of the second duck within the framework of the rapport of weaving the fabric along the weft, the length of the fabric can be expressed as the sum of its segments:

Where

Define

Substituting all the values ​​in the formula to determine the filling factor for the second duck, we get

48

Then

The length of the half-wave bending of the filament of the second base

The length of the second warp yarn in the fabric

Second warp threads

Since the threads of the first and second bases are wound on one web, the threads of the first warp have excess length, and the threads of the second are stretched, so that the work is equalized.

To determine the development of the first duck, it is necessary to determine in advance the main parameters of the structure of the tissue by the weft. The length of the tissue within the rapport of the weave is based on the base

The length of the filament of the first weft within the bounds of the rapport of the weave is based on the base

First filament weaving

To determine the second weft, it is necessary to determine the filling factor for the weft of the second layer of tissue.

The length of the fabric within the rapport of the weave on a second basis

The obtained coefficient allows to determine the actual distances between threads:

The length of the second duck within the rapport of the weave by the base

Second filament weaving

Average duck ingestion

Determine the actual density of the fabric on the basis and the weft with the help of the average diameter of the yarn. Since, in determining the work-up, the length of the rapport of the fabric on the basis and the weft was expressed in terms of the average diameter of the yarn, the tissue density is determined using these values.

Density of the fabric on the first basis

Density of the fabric on the second basis

Density of fabric by duck

Determine the surface density, severe tissue, taking into account changes in the finish:

г/м2

We determine the linear density of threads (tex) through the average diameter of the yarn before weaving according to the general formula

The surface density of the severe tissue can be expressed in terms of the average diameter of the filament, taking into account its production in the tissue and the density of the latter:

From here

Determine the linear density of threads: for the upper layer

tex. We accept  
tex. For the bottom layer tex. We accept tex. The actual diameter of the yarn before weaving:         a) for the top layer	d о1=dу1=0,0316C

dо1=dу1=0,0316∙1,33мм

б)  для нижнеог слоя

dо2=dу2=0,0316∙1,33мм

The average diameter of the yarn before weaving

Dсp=(2∙0,343+2∙0,369)/4=0,356мм.

The actual density of severe tissue Pо1 = Pо2 = 54.39 / 0.356 = 152 threads per 10 cm Pа1 = Pа2 = 50,35 / 0,356 = 141 threads per 10 cm Total tissue density Po = 152 + 152 = 304 threads per 10 cm Ru = 141 + 141 = 282 threads per 10cm The actual density of the finished fabric Threads for 10cm Threads for 10cm

At the end of the calculation it is necessary to check the actual surface density of the severe tissue at its actual density. The work can be taken from its average values ​​for the base and weft:

г/м2

The deviation is only 0.5 g / m2 Recommendations for students on preparation for classes:

Preparation consists in studying the material of the practical lesson on lecture notes, textbooks and teaching aids.

Technical and tools: weaving looms АТ-100-5М

List and types of tasks to perform in the classroom:

1. Parameters of the continuous process of tissue formation.

2. Cleaning the weft bobbins from the backup winding and yarn remains.

List and types of homework:

1. Wet-heat treatment of weft yarn 2. Studying the structure of the AM-150-K1 winding carousel      Assignment for independent work of students (CDS): 1. Study of the design of a batch machine. 2.Technical characteristics of a band saw machine Control questions 1. What is the purpose of weaving machines in the technological process of weaving? 2. Determination of the actual density of the fabric on the basis and weft Reporting form: written.

№15 Occupation

Theme of the lesson: Manufacture of nonwovens

Lesson plan:

1.Design fabric for men’s suits.

2. Design of combined tissue

3. The conclusion. Report on the work done.

Goals and objectives of the lesson, skills, competencies:

to develop fabrics we accept for a basis and a weft a combined yarn consisting of a half wool yarn containing 70% wool and 30% viscose staple fiber twisted with viscose thread. Linear density of half-wool yarn 31.2 tex, and viscose yarn -16.67 tex.

Brief theoretical information:

This method was developed at the Weaving Department of the Moscow Textile Institute. A. N. Kosygin.

In accordance with the purpose of the fabric, warp threads must be removed to its supporting surface. Therefore, we take the VI order of the phase of tissue separation: Kһn = 0.25 and Kһa = 0.75. To obtain the fabric of the given order of the structure phase, taking into account the sufficiently high degree of filling of the fabric with fibrous material, we take the following filling coefficients for fiber yarns according to both yarn systems: on the basis of Kn0 = 0.92 and on the weft Cny = 0.86.

The warp and weft threads in the fabric are deformed, the shape of their cross section is approaching ellipse. The deformation of the weft threads is greater than that of the warp threads. On the basis of the experimental data, we take ηο, r = 1,2; ηov = 0,8; ηy, r = 1.3; ηy, в = 0.69. Geometric models of the structure of the tissue (Figure 1) are made from sections of threads with a large number of intersections. Threads in the ceilings are arranged along the generatrix of the bending wave of the opposite system of yarns, which is due to the natural properties of the wool fiber, and high filling of tissue.

To produce the fabric, we take for the warp and weft a combined a yarn consisting of a half wool yarn containing 70% wool and 30% viscose staple fiber twisted with a viscose thread. Linear density of half-wool yarn 31.2 tex, and viscose yarn -16.67 tex. The calculated linear density of the combined filament is 47.87 tex.

Figure 1. The interlacing pattern (a) and geometric patterns of the structure of the wool-laced fabric on the basis of (b) and duck (c)

The values ​​of the coefficients C for the yarn before weaving are determined by the fiber embedding fraction of each kind. For wool blend yarn 31,2 tex

C = 1.28 • 0.7 + 1.1 • 3 ≈ 1.23; for combined thread

(31,2+16,67)  С=1,23

31,2/47,87 + 1,1 16,67/47,87=1,19

In accordance with the purpose of tissue we take a combined

interlacing with longitudinal stripes: 1st band – 6 threads with twisting twill 2/1, So = +1; 2-nd strip – 3 threads, interlacing with linen weave; 3rd band – 6 threads with twill twill 2/1, Sn = -1; 4-th strip – 3 threads, intertwined with a plain weave. The rapports of the fabric are Ro = 18 and Ru = 6; tо1 = 6; tо2 = 4;

Tо.сp =   tу1 = 14; tу2 = 10;  tу сp =

Figure of the interlacing of the fabric is shown in Fig. 1, a.

The parameters of fabric finishing are taken on the basis of tissue analysis of the same structure: shrinkage of the fabric over the width of Uy -3.5%, shrinkage of the fabric along the length of Uo = 7.5%), tissue weight loss m = 6%.

Diameter of warp threads and weft on the package:

Dо.n = dу • n = dсp.n = 0.1 • 1.19 = 0.261 mm. Kd = 1.

Diameter of warp threads and weft in fabric:

The estimated diameter of the yarn in the fabric:

The heights of the wave bending of filaments in the fabric:

- the height of the bending wave of the warp threads

Һo = 0.218 • 1.25 = 0.272 mm;

b) the height of the wave of bending of the weft threads

Һy = 0.218 • 0.75 = 0.164 mm.

The maximum density of the fabric on the basis (see Fig. 1, b)

Maximum weft density by weft

нити на 10 см

The actual density of the fabric on the basis, and the weft  threads per 10 cm threads per 10 cm Trimming of the warp threads, intertwined by the motive of the binding or I twill 2/1:

Working out of warp threads weaving on the motif of linen cloth

weave:

Average processing of the main threads in the fabric where n1 is the number of threads in. apport R0, having a smaller number of intersections; n2-number of threads in the rapport R0, having a greater number of intersections duck,

55

Working out the weft threads (1, 2, 3 and 6 threads in the weave pattern):

Working out the 4th and 5th threads of the duck:

Average processing of duck threads

Surface density of severe tissue

Surface density of the finished fabric

The deviation of the calculated surface density of the finished fabric from the given one is 9 g, or 3.43%, which is quite acceptable in practical calculations during design. Then choose the equipment and the width of the fabric. The designed fabric can be worked out on the machine tool STB-2-175.

The width of the finished fabric is Br = 154 cm.

Width of severe cloth

Width of fabric filling on a berry

Recommendations for students on preparation for classes: Preparation consists in studying the material of the practical lesson on lecture notes, textbooks and teaching aids.

Technical and tools: weaving looms АТ-100-5М

List and types of tasks to perform in the classroom:

1. Parameters of the continuous process of tissue formation.

2. Determination of the design diameter of the filaments in the fabric.

List and types of homework:

1. Study of wet-heat treatment of weft yarn

2.Motal automatic revolving device AM-150-K1

Assignment for independent work of students (CDS):

1.Partionnye repeating machines

2. Belt rewinding machines

Control questions

1. What is the purpose of weaving machines in the technological process of weaving?

2. The formula for the surface density of severe tissue

3. Definitions of average weft yarn processing

Assessment of students knowledge of  laboratory subjects

| Evaluationbylettersystem | Numeral equivalentofpoints | %- content | Evaluation according to the traditional system | 4.5Providing support for people with disabilities 4.5.1. Individual differentiated approach in the organization of the educational process 4.5.2. Individual differentiated approach in all kinds of activities * Note:According to the student’s choice it is envisaged that all kinds of tasks can be delivered orally Criteria for assessing students’ knowledge Criteria for assessing students’ knowledge |
| --- | --- | --- | --- | --- |
| А | 4,0 | 95-100 | Excellent | The student demonstrates: - a deep and lasting assimilation of program material - complete, consistent, competent and logically presented answers for all types of activities; - Ability to freely cope with the tasks; - correct, well-founded decisions, - skills in the use of information from basic and additional specialized literature in the study of discipline, - the ability to self-systematize the program material; - Possession of versatile skills and methods of performing all types of tasks; - Ability to work with foreign literature and information resources of the Internet; - Timely and high-quality execution of all types of tasks. |
| А- | 3,67 | 90-94 |  | The student demonstrates: - Deep assimilation of program material; - complete, consistent and logically presented answers for all activities; - ability to cope with the tasks; - the right decisions, - skills of using special literature in the study of discipline, - the ability to self-systematize the program material; - Possession of skills and techniques for performing all types of tasks; - Timely execution of all types of tasks. |
| В+ | 3,33 | 85-89 | Good | The student demonstrates: - assimilation of program material; - complete, consistent, literate, without significant inaccuracies, an account of the answers for all kinds of tasks; - correct application of theoretical knowledge - Possession of necessary skills in the performance of applied tasks - skills in using recommended literature in the study of discipline, - skills of systematization of program material; - Possession of skills and techniques for performing all types of tasks; - Timely execution of all types of tasks. |
| В | 3,0 | 80-84 |  | The student demonstrates: - assimilation of program material; - a consistent presentation of the answers for all types of tasks with non-essential errors; - skills in applying theoretical knowledge under the guidance of a teacher; - Possession of necessary skills in performing practical tasks - skills in using recommended literature in the study of discipline, - skills of systematization of program material under the guidance of a teacher; - mastering the skills of performing all kinds of tasks; - the ability to independently correct mistakes made; - the timely execution of all types of tasks with the elimination of errors. |
| В- | 2,67 | 75-79 |  | The student demonstrates: - assimilation of program material; - Ability to present answers with non-essential errors; - skills in applying theoretical knowledge under the guidance of a teacher; - Possession of techniques in the performance of practical tasks - skills in using recommended literature under the guidance of a teacher - skills of generalization of program material under the guidance of a teacher; - the ability to correct mistakes made with the help of a teacher; - the timely execution of all types of tasks with the elimination of errors. |
| С+ | 2,33 | 70-74 | satisfactorily | The student demonstrates: - mastering of the main material; - Inadequate formulations when responding to all kinds of tasks; - violation of the sequence in the presentation of the program material; - difficulties in self-fulfillment of practical tasks; - Possession of individual techniques in the performance of practical tasks - skills in using the literature recommended by the teacher; - skills of generalization of separate sections of program material under the guidance of a teacher; - the ability to correct major mistakes made with the help of a teacher; - execution of all types of tasks with elimination of errors. |
| С | 2,0 | 65-69 |  | The student demonstrates: - mastering of the main material; - Inadequate understanding of formulations when answering all types of assignments; - lack of consistency in the presentation of the material; - difficulties in self-fulfillment of practical tasks; - Possession of separate receptions at performance of tasks - difficulty in using the literature recommended by the teacher; - difficulties in generalizing the individual sections of the material studied; - the ability to correct major mistakes made with the help of a teacher; - execution of all types of tasks with elimination of errors. |
| С- | 1,67 | 60-64 |  | The student demonstrates: - mastering of the main material; - Inadequate understanding of formulations when answering all types of assignments; - lack of consistency in the presentation of the material; - significant difficulties in the independent implementation of practical tasks; - Inadequate possession of individual methods in the performance of assignments - significant difficulties in using the literature recommended by the teacher; - significant difficulties in the generalization of individual sections of the material studied; - the ability to correct major mistakes made with the help of a teacher; - execution of all types of tasks with elimination of errors. |
| Д+ | 1,33 | 55-59 |  | The student demonstrates: - mastering of separate sections of the main material; - misunderstanding of formulations when answering all types of assignments; - lack of consistency in the presentation of the material; - significant difficulties in the independent implementation of practical tasks; - significant difficulties in the application of individual methods of performing tasks; - significant difficulties in using the literature recommended by the teacher; - significant difficulties in the generalization of individual sections of the material studied; - difficulties in correcting the mistakes made by the teacher; - untimely execution of all types of tasks with elimination of errors. |
| Д | 1,0 | 50-54 |  | The student demonstrates: - difficulties in mastering individual sections of the main material; - misunderstanding of formulations when answering all types of assignments; - lack of consistency in the presentation of the material; - significant difficulties in the independent implementation of practical tasks; - Inability to apply individual methods of performing tasks; - significant difficulties in using the literature recommended by the teacher; - Inability to generalize the individual sections of the material studied; - significant difficulties in correcting the mistakes committed by the teacher; - untimely execution of all types of tasks with elimination of errors. |
| F | 0 | 0-49 | unsatisfactory | The student demonstrates: -- not having knowledge of program material, - When performing all types of tasks, gross errors are allowed; - lack of skills in applying individual tasks; - non-fulfillment of certain types of tasks provided by the forms of current, intermediate and final control. |

List of recommended literature

Basic:

1. Designing weaving factories: a textbook for high schools. / Ed. P.V. Vlasov. – M.: Light and food industry, 2002. – 304 p.

2. Ozerov B.V. Designing the production of nonwovens. –M .: Light and food industry, 2004. – 400 p.

3. Gusev VP, Krikunova KF Technical analysis for finishing fabrics and knitwear. – M.: Light industry, 2002. – 352 p.

4. Laboratory workshop on the technology of nonwovens: a textbook for universities / Ed. G.L. Barabanov. – M.: Legprombytizdat, 2002. – 416 p.

5. Sevostyanov AG Modeling of technological processes in the textile industry. –M .: Light and food industry, 1999. -344 p.

6. Knitting equipment of knitted factories. / E. N. Kolesnikova and others – M. Legpromtizdat, 2002. – 344 p.

7. Sergeyenkov A.P. The theory of the processes of technology, the preparation of mixtures and canvas formation. – Moscow: MSTU them. A.N. Kosygina, 2004.

8. Badalov K.I. Designing of technology of cotton spinning. – Moscow: MSTU them. A.N. Kosygina, 2004.

11. Frolov VD, Bashkova GV, Bashkov A.P. Technology and equipment teks¬tilnogo production. P.1. Manufacture of yarn and yarn yarn. – Ivanovo: IGTA, 2006, -436p.

12. Damyanov G.B. and others. The structure of tissue and modern methods of its design.-M: Easy and Food Industry, 1984. -240s.

Literature:

1. Kudryavin L.A. Fundamentals of technology knitted production: a textbook for universities / LA Kudryavin, II Shalov. – M.: Legprombytizdat, 2001. – 496 p.

2. Kuznetsova L.A. Designing of knitted goods / LA Kuznetsova, ZF Kazakova, AA Kartseva. – M.: Light industry, 2002. – 264 p. 5. Gusev V.E. Raw materials for woolen and non-woven products and primary processing of wool. – M.: Light industry, 2002. – 408 p. 6.Togataev T., Қaldybayev TD, Babazhanov MA Мақта тазалау кәсіпорнын Zhobalau. – Shymkent: 2008. -76 bets.

Сабиров Вахобжон Хусанович

СИХИМБАЕВА МАКПАЛ ТЕМИРБЕКОВНА

Абилхаймкызы Лаура

Методические указания

к практичемким работам по дисциплине

МЕХАНИЧЕСКАЯ ТЕХНОЛОГИЯ ТЕКСТИЛЬНЫХ МАТЕРИАЛОВ

("Mechanical technology of textile materials”)

Подписано в печать __________________________

(число.месяц.год)

Формат бумаги XxY  1/16

Бумага типографская. Печать офсетная. Объем …4 п.л.

Тираж …100 экз. Заказ № …….*