Ф.7.03.-03

Bitanova G.A., Karataeva G.E.

METHODICAL INSTRUCTIONS

for laboratory classes on the discipline

«Metallurgy of heavy non-ferrous metals»

Shymkent,  2019

MINISTRY OF EDUCATION AND SCIENCE

REPUBLIC OF KAZAKHSTAN

SOUTH KAZAKHSTAN STATE UNIVERSITY

NAME M.AUEZOV

Higher school of chemical engineering and biotechnology

Department «Metallurgy»

METHODICAL INSTRUCTIONS

for laboratory classes on the discipline

«Metallurgy of heavy non-ferrous metals»

for students of the specialty 5B070900 - «Metallurgy»

Shymkent,  2019

UDC 378.(075.8)

Compiled by: c.t. s., assistant professor Bitanova G.A.,

c.t. s., assistant professor Karataeva G.E.

Methodical instructions for practical classes on the discipline «Metallurgy of heavy non-ferrous metals».- Shymkent: SKSU. M.Auezov, 2019.- 64p.

The methodical instructions are compiled in accordance with the requirements of the Training programme and the Modular training program of the discipline «Metallurgy of heavy non-ferrous metals» and include all the necessary information on how to carry out laboratory classes that allow in-depth and detailed study of the most complex sections of the course. The methodical instructions cover the issues of the report, the questions of control, questions and tasks for the independent work.

Methodical instructions are intended for students of the specialty 5B070900 - "Metallurgy".

Reviewer: - c.t.s., professor Shingisbayeva Zh. of the Department of “Ecology”, SKSU. M.Auezov

Considered and recommended for publication by the meeting of the Department of Metallurgy (Minutes No. _, dated ________), the Methodological Commission of the Higher School of Chemical Engineering and Biotechnology (Minutes No. __of_______)

Recommended for publication by the Educational and Methodical Council of SKSU.M.Auezov (Minutes No.___ of ___ ______)

© South Kazakhstan State University. M.Auezov, 2019

Responsible for the issue Bitanova G.A.

CONTENT

| Introduction | 6 |
| --- | --- |
| 1 The aim and tasks of the laboratory classes on the discipline «Direct iron production» | 7 |
| 2. Recommendations for students to prepare for laboratory classes | 7 |
| 3. Criteria for evaluating trainees in laboratory classes | 7 |
| Laboratory work 1, 2. Agglomerative roasting of lead concentrates. | 9 |
| Laboratory work 3, 4. Reactionary melting of lead concentrate. | 16 |
| Laboratory work 5, 6, 7. The analysis of raw materials on the content of zinc and lead. | 21 |
| Laboratory work 8, 9. Roasting of zinc concentrates. | 25 |
| Laboratory work 10, 11. Electrolytic precipitation of zinc from sulphuric acid solutions. | 35 |
| Laboratory work 12, 13. Electric melting of oxide zinc ores. | 43 |
| Laboratory work 14, 15. Melting of copper concentrates on matte. | 51 |
| Literature | 61 |

INTRODUCTION

Metallurgy is the science and technology of metals. It covers the processes of producing metals by extracting them from their ores, of the refining and purification of these ores and the working of them mechanically or alloying them to adapt them for various uses.The choice of the process depends upon the nature of the ore and the type of the metal. The metal content in the ore can vary depending upon the impurities present and chemical composition of the ore.

Non-ferrous metals are metals and alloys the main component of which is not iron but some other element such as copper, aluminium and others.

Some characteristics of non-ferrous metals are: high electric and heat conductivity, high corrosion resistance, non-magnetic qualities, light weight and easiness to fabrication. Zink, copper and lead sulphides, aluminium and tin oxides, magnesium, are the naturally occurring minerals from which these metals are extracted.

Lead is reduced easily from its ores, particularly the oxidized ores such as lead carbonate Native copper often occurs as large lumps. Though soft, it is hardened appreciably when hammered and the first fabricated metallic articles used by man for other than adornment were made of copper. the zinc of brass almost certainly came from smelting smithsonite (zinc carbonate) with charcoal and with copper. Almost the sole ore of tin is cassiterite (tin oxide).

The discipline "Metallurgy of heavy non-ferrous metals" is a component of the choice. Along with other disciplines, the course "Metallurgy of heavy non-ferrous metals" is devoted to the specialty of metallurgist-bachelor, the acquisition of knowledge to familiarize students with the processes in the field of smelting in the metallurgical industry, to teach the students the basics of the solution of the problems of cast iron in the modern metallurgy.

Independent work involves studying extra material for extra-curricular time (on textbooks, scientific journals, innovation-information technologies, the Internet), independent study of individual sections of the course.

Discipline «Metallurgy of heavy non-ferrous metals» for higher educational institutions, training specialists for the enterprises of the metallurgical industry.

The process of practical training of this discipline helps to apply English in practice, deepen and consolidate theoretical knowledge in the specialty "Metallurgy" in order to improve English in the professional field.

The training course is divided into lectures, laboratory classes, practical classes and examination.

1. The aims, objectives and place of the academic discipline in the structure of the educational program

1.1 The aim of studying the discipline is the acquisition of knowledge in the field of physicochemical properties, forms of being in nature and the use of heavy non-ferrous metals, including (lead, zinc, copper, nickel and tin); to understand in depth the theoretical foundations, technology, instrumentation of the production of heavy non-ferrous metals; evaluate and analyze the current state of metallurgical production of heavy non-ferrous metals; solve professional problems in the field of heavy non-ferrous metals, including lead, zinc, copper, nickel and tin.

1.2 Tasks of studying the subject are to master the general laws of metallurgical processes for the production of zinc, lead, copper and nickel; describe the methods of ores enrichment, production technology, methods of separation and purification of heavy non-ferrous metals; establish a link between the type of metallurgical raw materials and the method of its processing; to analyze of heavy non-ferrous metals in ores, industrial products and metallurgical production wastes.

2. Recommendations for students to prepare for classes

As a result of studying the discipline, the student must:

- to know: the theoretical foundations, technology, instrumentation of the production of heavy non-ferrous metals (lead, zinc, copper, nickel and tin); consciously recommend the optimal parameters for the process in obtaining heavy non-ferrous metals.

- be able to: professionally choose methods of conducting experiments, methods for analyzing source and end products and methods of theoretical studies; evaluate and analyze the current state of the metallurgical production of heavy non-ferrous metals;

- to possess: practical skills in the field of heavy non-ferrous metal metallurgy, including lead, zinc, copper, nickel and tin.

3. Criteria for evaluating students in laboratory classes

The knowledge, abilities, skills and competencies of students in all types of control are determined by evaluations of the rating alphabetic system, which have a directly proportional relationship.

The score "excellent" corresponds toA with a digital equivalent of 4.0 and a percentage of 95-100% and A- having a digital equivalent of 3.67 and a percentage of 90-94% correspond to an "excellent" rating.

This assessment is made if the student showed full knowledge of the material of the program and did not allow mistakes, inaccuracies, timely and correctly performed classroom assignments, simultaneously showed original thinking, fulfilled all tasks in a timely manner and made no mistakes when doing homework, independently used additional literature for studying discipline, was able to independently systematize the material of the program.

The score "good" corresponds to B + score with a digital equivalent of 3.33 and a percentage of 85-89%, B having a digital equivalent of 30 and a percentage of 80-84% and B- having a digital equivalent of 2.67 and a percentage of 75 -79%.

This assessment is made if the student hasmastered theprogram material not less than on 75% and thus did not allow gross mistakes at the answer, has in due time executed all tasks and has handed over them without fundamental remarks, correctly executed and has in due time handed over homeworks without fundamental remarks, used additional literature as instructed by the teacher, allowed unprincipled inaccuracies or fundamental mistakes, corrected by the student himself, managed to systematize the program material with the help of the teacher.

The score "satisfactory" corresponds to C + score having a digital equivalent of 2.33 and a percentage of 70-74%, C having a digital equivalent of 2.0 and a percentage of 65-69%, C- having | a digital equivalent of 1.67 and a percentage of 60-64%, D + having a digital equivalent of 1.33 and a percentage of 55 to 59% and D having an equivalent of 1.0 and a percentage of 50 to 54%.

This assessment is made if the student has mastered a program material not less than on 50%, at performance of control tasks, homework has required the help of the teacher, at delivery of translate the texts admitted inaccuracies and unprincipled errors, inaccuracies, did not show activity in research work, limited only to the educational literature specified by the teacher, experienced more difficulty in systematizing the material.

The score "unsatisfactory" corresponds to an estimate of having a digital equivalent of 0 and a percentage of 0-49%.

This assessment is made if the student has found gaps in knowledge of the basic material provided by the program, has not mastered more than half of the discipline program, in the answers he made fundamental mistakes, did not execute the separate tasks stipulated by the forms of current, intermediate and final control, did not work all the basic the literature provided by the program.

Laboratory work № 1, 2

Agglomerative roasting of lead concentrates.

The aim of laboratory work -to familiarize with the principles of agglomeration of lead sulfide concentrates the method of calculating the charge of agglomerating roasting, the course of the process, the type of materials and products of the process.

The plan of laboratory work:

1. A brief explanation of the aims and objectives of the laboratory work.

3. Issuance of initial data for calculation

4. Students carry out the necessary theoretical and technological calculations

5. Getting admission and performing laboratory work

6. Processing of the obtained results, writing conclusions

7. Protection of laboratory work

Brief process description

Agglomeration is the mostly applied agglutination method for fine-grained and dusty materials. It is a thermal-chemical process by which fine-grained ores and concentrates are turned into lump porous agglomerates. The principle of an agglomeration process lies in heating of a material on a temperature allowing the ore grains to smelt, agglutinate and sinter. The heat source is combustion of sulphur contained in the material. In order to prevent material melting as a consequence of a too high heat, it is sometimes necessary to reduce the sulphur content by pre-roasting. If the material contains no sulphur, it has to be mixed with fuel before agglomeration (coke, black oil etc.). The principle of the agglomeration process is schematically depicted in Fig. 1. The air necessary for sulphur combustion or added fuel is sucked or pressed through a glowing layer of dusty ore or concentrate lying on a belt. The batch is then inflamed by e.g. a gas burner. By the influence of hot air, the glowing zone transfers continuously through the entire layer, grains soften and smelt on their surfaces, subsequently agglutinate and their boundaries disappear. During agglomeration, exothermal reactions between gas and solid phases occur:

2 MeS + 3O2 = 2 MeO + 2SO2

MeO + SO3 = MeSO4

Requirements on agglomerate: a) sufficient porosity enabling flow of reducing gases b) high strength, resistance against crushing and abrasion c) composition corresponding to a subsequent processing (required sulphur content, slag-forming agents ensuring melting and required slag basicity) d) usage of SO2

Lead is reduced easily from its ores, particularly the oxidized ores such as lead carbonate (cerussite). The earliest method of smelting, which may have been the first metallurgical process practiced by man, was to place the ore with wood in a hole in the ground, and fire it. The lead that was produced then ran along a gutter to a second hole, where it was collected. In the case of the chief lead ore, galena (lead sulphide), roasting is carried out in an oxidizing atmosphere. At a moderate temperature lead oxide and lead sulphate are formed from the lead sulphide. With increased temperature, and assisted by the addition of a small amount of flux (e.g. quicklime), the remaining lead sulphide reacts with the two oxidized products to produce lead and the gas sulphur dioxide.

Batch: Metal-containing raw material (ore, concentrate), recycling material (waste, semi-products – dust, ash, sludge), additives influencing the agglomeration process (limestone, sand, pyritic slops), possibly fuel.

Fig. 1 - Principle of ore raw materials agglomeration.

1.1Methods of work

Laboratory work consists of three parts:

1) preparation of the mixture with a parallel study of the effect

humidity changes in the physical properties of the mixture;

2) carrying out the experiment on agglomerated roasting;

3) determining the composition of the obtained agglomerate.

To carry out the work, prepare a mixture consisting of lead concentrate (300 g), the calculated amount of fluxes and recycle sinter. The method of calculating the number of fluxes and revolving agglomerate is given below. The chemical composition of the concentrate and fluxes is given by the teacher. All components of the charge are crushed and sieved through a sieve of 3 ... 5 mm.

The mixture is thoroughly mixed and with the help of a measuring cylinder, the volume of the wet mixture is measured. Then the sample is poured into a porcelain bowl and moistened at the direction of the teacher. After moistening, the mixture is thoroughly mixed and its volume is measured again. Thus, determine the amount of the mixture at different moisture content. Moisturize the mixture and its mixing is carried out in a porcelain bowl. The mixture in the measuring cylinder should be filled up freely, without compaction, only careful alignment of the charge surface is allowed. As soon as the humidity is reached, at which the charge volume decreases, the measurements stop. Based on the data, build a graph. Along the axis of abscissas is deposited moisture, on the axis of ordinates - the volume of the charge. The optimum moisture content of the charge corresponds to its largest volume. The mixture with optimum moisture is subjected to agglomerated roasting.

The laboratory setup (fig. 1) for sintering consists of an iron welded crucible (pot) with a grate and a piston pump with a motor.

The space from the crucible bottom to the grate is an air chamber, the presence of which ensures the uniform distribution of air through the horizontal sections of the charge. The air bladder is connected with a pump by means of a pipe by a rubber hose. The pump forces air through the layer of the charge. The amount of air supplied is regulated by a clamp on a rubber hose.

Before the start of agglomeration, a fire is made of wood chips on the grate, a bed of coke pieces (size 10 ... 12 mm) weighing 100 ... 120 g is loaded and air is pumped from the pump. When coke is well flared up, proceed to download the prepared mixture. It is not necessary to load the charge immediately, but gradually over several portions so as not to extinguish the coke which has ignited and to ensure the ignition of the low layers of the charge. After loading the entire mixture, it is recommended to tamp it slightly.

crucible

charge

The end of the process is the beginning of the melting of the charge on the surface. After some cooling (before darkening), the obtained agglomerate is unloaded on a cast-iron plate, where it completely cools down. Unburnt coke pieces are manually separated from the agglomerate. The total mass of the agglomerate is determined, as well as the mass of lumpy material and fines (+5 mm and -5 mm).

air

air chamber

grate

coke

Figure 1. Installation diagram for agglomerated roasting

Calculate the total yield of sinter as a percentage of the mass of the initial charge and the yield of (+ 5 mm) sinter (as a percentage of the total mass of sinter).

When agglomeration should:

1) to fix the temperature in the layer of the mixture with the help of thermo couple with a cover;

2) determine the vertical burning rate in the charge;

3) determine the specific performance of the firing pot.

To determine the vertical burning rate (cm/s) in the charge, note the thickness of the charge layer (outside the kettle) and record the sintering time (from the start of loading the charge on red-hot coke until the end of the burning).

,                                                                                         (8)

where δ is the thickness of the charge layer, cm;

τ - time of agglomeration, s.

To determine the specific performance of the pot should measure the area of the lattice. Knowing the mass of the charge and the time of agglomeration, we determine the specific daily productivity [t / (m2-day)]:

,                                                                       (9)

where Q is the mass of the charge, t;

F — lattice section, m2;

τ - time of agglomeration, days

An average sample is taken from the ground agglomerate for analysis on total sulfur. According to the sulfur content in the charge and sinter and the yield of products, the degree of desulfurization is calculated.

1.2 The calculation of the charge agglomerated roasting

Suppose that the agglomerating roasting is subjected to a concentrate of the following composition,%: 38.6 Pb; 10.7 Zn; 10.6 Fe; 23.0 S; 4.9SiO2; 1.6 CaO; 4.2 A12O3; 6.4 other.

The calculation of the charge consists in determining the quantitative relations

materials entering the agglomerating roasting. With agglomerated roasting of lead concentrates at most plants

get self-melting sinter, i.e. in the calculation of the charge, the addition of fluxes is envisaged in such an amount that during subsequent smelting to obtain slag of the selected composition. Therefore, the calculation of the charge for agglomeration is given by the calculation of the charge for smelting.

Calculation is carried out on 100 kg of concentrate.

Pre-calculate the composition of the slag, provided that the concentrate is self-melting, i.e. when smelting without flux. In the slag will go:

iron (in terms of FeO)

55,8Fe –  71,8 FeO

10,6Fe  - x;    x= 13,6 kg;

zinc (in terms of ZnO)	
65,4Zn - 81,4ZnO

10,7Zn  -x;   x= 13,3 kg	
and completely SiO2, CaO and А12О3.

Taking the amount of FeO, ZnO, SiO2, CaO as 90% as the main slag-forming agents, we compile a table of the composition during the smelting of the concentrate without fluxes (Table 1).

Table 1 - Slag composition for flux-free smelting of concentrate

| Component | Slag composition |  |
| --- | --- | --- |
|  | кг | % |
| SiO2 | 4,9 | 13,5 |
| CaO | 1,6 | 4,3 |
| FeO | 13,6 | 36,6 |
| ZnO | 13,3 | 35,6 |
| Total | 33,4 | 90,0 |

Concentrate self-fusibility is checked according to Norton's rule.

∑ZnO + SiO2 ≤ 42%;

∑ZnO + CaO≤ 30%.

From the data table. 1 it follows that the concentrate is not self-melting and during its processing it is necessary to expend all three fluxes: quartz, limestone and iron ore to dissolve all the zinc oxide formed in the slag.

We take into account that the slag will be obtained with a content of 22% ZnO. For slagged zinc oxide we calculate the slag yield:

13,3ZnO - 22 %

х- 100 %;              х= 60,5 kg.

The ratio between the main slag-forming components with a content of 22% ZnO in the slag is taken in accordance with the condition for self-melting: 20% SiO2, 8% CaO and 40% FeO.

60.5 kg of slag will contain, kg:

SiO2- 60,5 ∙ 0,20 =12,1;

FeO - 60,5∙ 0,40 = 24,2;

СаО - 60,5 ∙ 0,08 = 4,8.

Excluding those coming from the concentrate to the slag, it is required to add with fluxes, kg:

SiO2- 12,1- 4,9 = 7,2;

FeO - 24,2 - 13,6 = 10,6;

СаО-   4,8 - 1,6  = 3,2.

Fluxes have the following composition,%:

quartz 97.0 SiO2;

1.4 SiO2 limestone and 52.4 CaO;

iron ore 13.0 SiO2; 67.0 FeO and 2.9 CaO.

We denote the number of added fluxes as follows: x - quartz, y - limestone and z-iron ore. Make a table. 2 slag formers, using which you can write the following equations:

0,97х + 0,014у + 0,13z = 7,2;

0,67z = 10,6;

0,542у + 0,029z = 3,2.

Solving the system of these equations, we find х= 5,2кг;   у= 5,2 кг;   z = 15,8 кг.

Table 2 - Slag Formers

| Material | Weight, kg | SiO2 |  | FeO |  | СаО |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | % | кг | % | кг | % | кг |
| Quartz | х | 97,0 | 0,97х | - | - | - | - |
| Limestone | у | 1,4 | 0,014 у | - | - | 52,4 | 0,524х |
| Ironore | z | 13,0 | 0,13 z | 67,0 | 0,67 | 2,9 | 0,029 z |

Firing conducts single-stage return. The amount of sulfur in the final firing mixture will be 7%. Dilution of the sulfur of the charge is necessary recycle sinter containing 1.5% sulfur.

Denoting the number of recycled sinter through x, we find

7,0 = (100 - х) ∙ 0,181 + 0,015х,

where x = 66.7 kg, i.e. for every 33.3 kg of the charge, 66.7 kg of recycle sinter will be required, which will be from the initial charge:

The amount of concentrate in the charge will be

126,2 кг - 100 кг

33,3 кг  -  х;             х = 26,4 кг.

The final composition of the batch of single-stage agglomerating firing is shown in Table 3.

Table 3 - The final composition of the charge single-stage agglomerated roasting

| Material | The final composition of the charge |  |
| --- | --- | --- |
|  | kg | % |
| Concentrate | 100,0 | 26,4 |
| Quartz | 5,2 | 1,4 |
| Limestone | 5,2 | 1,4 |
| Iron ore | 15,8 | 4,2 |
| Recycle agglomerate | 252,7 | 66,6 |
| Total | 378,9 | 100,0 |

In accordance with the above calculation, the required amount of flux and circulating agglomerate is determined for the laboratory sample of the concentrate. The necessary data for the calculation and conduct of the work are given by the teacher.

The procedure for the preparation of reports and their protection

The work report should contain:

1. A summary of the theory of agglomerated roasting and its conditions.

2. Description of equipment and methods of work. Sketch of laboratory setup.

3. The necessary calculations and the results obtained with the conclusions and conclusion.

The results of the work are given in the following form:

Set, g:

1) concentrate ___

2) limestone

3) iron ore ____

4) quartz

5) working sinter ____

6) the sulfur content in the original charge ____

Received:

1) charge moisture ____%

2) firing temperature ____ ° C

3) firing time min

4) total sinter g,% in charge ____

5) suitable agglomerate g,% in charge ____

6) the specific productivity of the pot, t / (m2-day) ____

7) the vertical burning rate of the mixture, cm / s ____

8) firing degree ____%

9) the degree of desulfurization ____%

6. Test questions

1. What is roasting of concentrates necessary for?

2. Why is it undesirable to obtain metal rods during firing?

3. What products are obtained by agglomerating roasting?

4. What is the purpose of agglomeration?

5. What is included in the charge of agglomerating roasting? The role of each component.

6. What is the main cementing agent during sintering?

7. What are the processes, and in what sequence do they take place during agglomerating roasting?

8. What is fuel during agglomerating roasting?

9. What explains the use of two-stage firing?

10. What is called the degree of roasting, desulphurisation, temperature of ignition of sulphides?

11. Will you leave sulphide sulfur in the agglomerate during roasting to further produce matte during roasting of lead-copper, lead-zinc-copper concentrates and why?

12. What is the order of the laboratory experiment?

13. What values ​​and how are you determined by laboratory experience?

Homework

1. Get acquainted with the theory of the behavior of base metals during agglomeration.

2. To study the technology and basic indicators of the agglomeration process.

Assignment to IWS

A student must prepare an ALS on the following topics:

1. To get acquainted with the thermodynamic laws in the process of sintering lead concentrates.

2. To study the kinetics of the process of agglomeration of lead concentrates.

3. To study the characteristics of raw materials.

4. Suggest basic ways to improve the process.

Laboratory work № 3, 4

Reactionary melting of lead concentrate

The aim of laboratory work - to get acquainted with the reaction method of obtaining lead, the process and its products.

The plan of laboratory work

1. Check homework

2. A brief explanation of the goals and objectives of the laboratory work.

3. Issuance of initial data for calculation

4. Students carry out the necessary theoretical and technological calculations

5. Getting admission and performing laboratory work

6. Processing of the obtained results, writing conclusions and conclusion

7. Protection of laboratory work

Brief process description

Reactions between sulphides and oxides of a same metal or of different metals occurring within ores and concentrates are highly important during production of certain NFMs (Cu, Ni, Pb). During reaction smelting, two metal compounds react together at temperatures higher than melting to produce a metal. A reaction between a sulphide and an oxide of a same metal is the mostly occurring one:

MeS + 2 MeO= 3 Me + SO2

Metal oxides are generated either by oxidation of a portion of sulphides during smelting, or by exchange reactions between Me metal sulphides and M metal oxides.

MeS + MO = MeO + MeS

The direction of a given reaction of conversion of a metal oxide to a metal sulphide can be entirely controlled if affinities of the individual metals to sulphur are known.

The smelting of lead concentrate consists of two stages: partial burning of lead concentrate, i.e. conversion of sulphides to oxides, and reaction smelting. It is called the reaction because lead is obtained as a result of reactions between the products of the process, lead sulfide and its oxides. Both stages of the process can be carried out sequentially (in reflective, short drum ovens) or at the same time (in a furnace furnace) in the same metallurgical apparatus. Depending on the apparatus used, the reaction smelting is called reflective, furnace or electrofusion. Practical use is now found in furnace smelting, electric smelting and short-drum.

If you mix in a certain proportion the lead sulfide and its oxide or lead sulfide and its sulfate, then when heated these compounds react with each other to release metallic lead and sulfur dioxide according to the following equations:

PbS + 2РЬО 3Рb + SO2 - 219,62кDj;	(11)

PbS + PbSO42Pb + 2SO2 - 407,05кDj.	(12)

If lead sulfide is roasted, then under certain conditions of the process, sulfide, oxide, lead sulfate, metallic lead, sulfur dioxide can form and interact with each other.

If lead sulfide is roasted, then under certain conditions of the process, sulfide, oxide, lead sulfate, metallic lead, sulfur dioxide can form and interact with each other.

If the ratios between sulphide, sulphate and lead oxide given in reactions (11) and (12) are strictly observed, it is theoretically possible to obtain all lead in a metallic form. In practice, however, an excess of lead oxide and sulfate is often obtained. Excess sulfate, reacting with sulfide, forms lead oxide according to the equation

PbS + 3PbSO4 = 4РbО + 4SO2 - 718,96кDj.	(13)

Reactions (11) and (12) are reversible, and their equilibrium constant is determined by the equilibrium vapor pressure of the sulfur dioxide.

The dependence of the equilibrium vapor pressure of sulfur dioxide on the temperature for the reaction (11) is given in Table. four.

Table 4-Dependence of vapor pressure on temperature for the reaction (11)

| Temperature, ° С | 692 | 755 | 800 | 847 | 870 |
| --- | --- | --- | --- | --- | --- |
| Pso2, kPa * | 0,67 | 5,07 | 13,196 | 72,52 | 110,64 |

* 1 mm Hg = 133.3 Pa.

The same relationship for reaction (12) is given in table 5.

Table 5 - Dependence of vapor pressure on temperature for the reaction (12)

| Temperature, ° С | 609 | 655 | 700 | 723 |
| --- | --- | --- | --- | --- |
| Pso2, kPa * | 3,99 | 20,66 | 56,25 | 97,97 |

At certain temperatures and pressures of sulfur dioxide, chemical equilibrium sets in, at which the reactions proceed at the same speed in both directions. With increasing temperature, the equilibrium is disturbed and the reactions go from left to right, in the direction of the formation of lead and sulfur dioxide. Thus, the temperature increase is useful for the reaction melting, since this increases the yield of metallic lead and accelerates the burning of lead sulfide. But both for firing and for the reaction itself, the charge must be maintained in a solid state. Therefore, the reaction smelting process is carried out at temperatures not higher than 850 ° C, i.e. below the melting temperature of all reaction participants (melting points for: PbS - 1135 ° С, PbSO4 –1170 ° С, РbО - 883 ° С). At higher temperatures, lead oxide melts, separation by specific gravity occurs, causing contact between the sulfide and lead oxide to be broken and lead melting down.

From tab. 6 and 7 that the temperature of 800-850 ° C is quite sufficient for these reactions to take place, since the pressure in this case exceeds 1 превышает 105 Pa (1 atm). In practice, due to the mixing of the charge and good draft, the content of sulfur dioxide anhydride in the exhaust gases rarely exceeds 4.5%, so the reactions proceed in the direction of the formation of metallic lead.

Reaction (13) begins to occur noticeably at a temperature of 550 ° C. Since the sulfur dioxide is removed from the process at the moment of its formation, then with increasing temperature, the reaction from left to right is significantly accelerated.

All the above reactions are endothermic. The heat required for endothermic reactions is obtained in the previous reactions of oxidation of lead sulfide to oxide and sulfate. In practice, a certain amount of carbonaceous fuel in the form of fine coke is added to the charge (4-10% of the mass of the charge). The increase in fuel is necessary to compensate for heat loss, as well as to obtain the temperature that ensures the process and recovery of excess lead oxide by the reactions:

PbО + С = Pb + СО;	(14)

PbО + СО = Pb + СО2.	(15)

In practice, reactions between sulfide, oxide and lead sulfate are complicated by a number of side effects.

Sulfide flotation concentrates entering the reaction smelting are almost always associated with other metal sulphides and waste rock, the amount of which dramatically affects the quality of the concentrate.

The concentrate, which is a pure lead gloss (PbS), would be an ideal raw material for the reaction process, since it contained no impurities that separated the lead sulphides from oxides, i.e. interfering with the process. From this point of view, it can be said that all impurities of the concentrate are harmful to the reaction process.

But not all impurities are equally harmful. The most harmful impurity is silicon oxide. Its harmful effect is as follows. When a significant amount of silicon oxide is contained in the concentrate, the oxides and lead sulfates formed during the reaction process will bind to silicates:

PbО + SiО2 = PbO∙SiО2;                             	(16)

PbSО4 + SiО2 = PbO∙SiО2 + SO2 + ½O2;                                               	(17)

Lead bound in silicate will not be recovered during the reaction process; it will go into a slag called gray slag. From this, the extraction of lead may be so reduced that the reaction process may be disadvantageous. Extraction of lead in this case will depend on the silica content in the feedstock. Suppose that the ore contains 5% silica, and that lead sulphatemonosilicate (2PbO ∙ SiO2) is formed during the reaction smelting. In this case, every 60 (mol. Mass of SiO2) mass parts of silica slag 414.4 (mol. Mass. Two parts of lead) mass parts of lead and 5% of silica will be transferred to gray slag:

g Pb.

When the content in the concentrate or ore 70% lead only in the gray slag would pass 50% lead, and, in addition, a significant amount of lead goes into dust and sublimates. Naturally, with 5% silica in ore or concentrate, reaction melting is inconceivable.

Lead silicates are also harmful because, because of their low melting point, they quickly melt and, wetting the reacting components of the charge, interfere with the reaction.

In connection with such negative properties of silica, its content in the incoming melting material is allowed not higher than 2%.

Other impurities present in lead concentrate also have a negative effect on the reaction smelting processes, reducing the contact of lead sulfide with its sulfate and oxide, as well as contributing to the premature melting of the charge, forming low-melting alloys. Such impurities include sulfide minerals of copper, iron, zinc, arsenic, antimony.

Since in each lead concentrate other minerals are always present in certain quantities, except for lead sulfide, to partially reduce their harmful effects and increase the refractoriness of the charge, limestone of 3-5 mm in size in an amount up to 2% of the weight of the mixture is added to it.

Based on the foregoing, rich lead ores or concentrates containing 70% of lead and above should be subjected to reaction smelting.

Method of work

For the test, 200 ... 300 g of lead concentrate and 3 ... 4% of the limestone concentrate sample taken as a thermostat are taken. The mixture is thoroughly mixed and loaded into an iron pan. The baking tray with the mixture is placed in an electric oven heated to a temperature of 600 ° C. The concentrate is oxidized vigorously at this temperature. Oxidation is carried out for 40 ... 60 minutes with continuous stirring.

After conducting a partial oxidative roasting of lead concentrate, scoop the entire hinge into one end of the pan (to the rear wall) and give the pan a slope for draining the resulting lead into the front end.

Crushed charcoal is loaded into the front end of the pan to prevent lead oxidation.

After performing all the operations, the temperature in the furnace is raised to 800 ° C. At this temperature, an energetic interaction between the oxide and lead sulfide occurs. During the course of the second period of the process (lead shedding), the charge should be mixed all the time to prevent its sintering and melting. In the process of mixing it is necessary to rake the mixture to the back wall of the tray. Separate small droplets of lead should be collected in larger ones and help them drain into the front of the pan. The experience continues until, until yAt the end of the experiment; carefully remove the residue of the mixture consisting of gray slag of unreacted particles of the charge from a baking tray. Then the baking sheet is taken out of the oven, and the lead is cast into an table, while being careful not to allow the charcoal to enter the mold. Accidentally pieces of charcoal are removed from the surface of the lead with forceps; Before casting lead, the mold is smeared with a saturated lime mortar or pulp or rubbed with chalk. The mold is dried and after that the lead is poured into it from the pan.

After cooling, the resulting melting products are weighed and determine the extraction of lead from the concentrate during the experiment.

The experience is difficult and requires a lot of attention. The results of the experiment largely depend on the actions of the experimenter.

Report content

The report on the work should contain a summary of the theory of reaction melting, a detailed description of the experience, the calculation of the yield of metallic lead and gray slag.

All performed operations are recorded in a workbook, compiled according to the following form:

| Operation | Temperature, 0С | Duration, min. | Loaded, g limestone |  | Received, g |  | Roughleadyield,% | Leadrecovery,% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | concentrate | limestone | Roughlead | остатка leftover |  |  |
| Oxidizing roasting of lead concentrate |  |  |  |  |  |  |  |  |
| Leadout |  |  |  |  |  |  |  |  |

Control questions

1. What are the stages of the reaction melting of lead concentrates?

2. At what temperatures is the reaction melting and how is this explained?

3. What is the role of coke in the reaction smelting?

4. What effect do impurities have on reaction melting?

5. What is limestone added to the mixture of the reaction smelting?

Home task:

1. To independently study the thermodynamics and kinetics of the reaction melting of lead concentrates.

2. To study the technology and the main indicators of the process of the reaction smelting of lead concentrates.

Assignment to IWS

A student must prepare an ALS on the following topics:

1. To study the characteristics of lead concentrates.

2. To familiarize with the main and auxiliary equipment of lead concentrates used in the process of the reaction smelting.

3. To propose the main ways to improve the technological process of the reaction smelting of lead concentrates.

4. Explain the processes of furnace smelting, smelting in short drum furnaces, smelting in suspension.

5. The current state of lead production in Kazakhstan and abroad.

6. Tell about new improved methods of reaction smelting of lead concentrates.

Laboratory work № 5, 6, 7

The analysis of raw materials on the content of zinc and lead.

The aim of the work is to study the methods of analysis of zinc-containing raw materials, the determination of zinc and lead by the volumetric method.

The plan of laboratory work:

1. Check homework

2. A brief explanation of the aims and objectives of the laboratory work.

3. Issuance of initial data for calculation

4. Students carry out the necessary theoretical and technological calculations

5. Getting admission and performing laboratory work

6. Processing of the obtained results, writing conclusions

7. Protection of laboratory work

Theoretical information

| Common Minerals of Zn: Zinc Oxides |  | Zinc Sulphides |  |
| --- | --- | --- | --- |
| Name | ChemicalFormula | Name | Chemical Formula |
| Zincite | ZnO | Sphalerite | ZnS |
| Franklinite |  | [ZnO(Fe, Mn)2O3] |  |
| Willemite |  | Zn2SiO4 |  |
| SmithSonite |  | ZnCO3 |  |

About 60% of lead produced world-wide is derived from ore. Lead ore is minedin many countries around the world, though three quarters of world output comesfrom only six countries: China, Australia, USA, Peru, Canada and Mexico. Smallamounts are mined in several countries in Europe, with the biggest producer

being Sweden. Total production has been at a similar level since the 1970s; new

mines open or are expanded to replace old mines. (Note: all these mines contain

at least two metals (also zinc, sometimes silver, gold and copper) so lead

extraction is not the only reason for the mining.)

The production of refined metallic lead from minerals dug out of the ground

involves a number of steps which are outlined below.

Equipment, technical and instrumental means:

Analytical Scale

Titration burettes

Conical flasks

Pipette

Chemical glasses

Electric tile

Method of work

Determination of zinc by complexometric method

The method is based on the formation of a strong complex of zinc with Trilon B at pH = 5-6. At the equivalent point, the color of the solution varies from crimson-violet, due to the complex compound of zinc with the indicator xylenol orange to yellow-lemon.

Interfering with the determination of zinc, copper, lead and iron are removed from the solution by sequential analysis. Additive in the analyzed solution of ammonium fluoride eliminates the interfering effect of aluminum, calcium and magnesium present in the solution.

Reagents:

Hydrochloric acid density of 1.19

Sulfuric acid with a density of 1.84

Nitric acid with a density of 1.4

Ammonia, 25% solution

Ammonium fluoride

Sodium thiosulfate, 10th solution

Xylenol orange indicator solution

Trilon B, titrated solution

Buffer solution, pH = 5 (500 g of ammonium acetate, 20 ml of glacial acetic acid and water up to 1 l).

The course of the analysis

A portion of the sample of 0.5 g is placed in a 200 ml conical flask, 10-20 ml of aqua regia is added and, after stopping the violent reaction, they are placed on a hot plate and boiled, evaporated to an almost dry precipitate, allowed to cool. Add 50-100 ml of distilled water, mix well and transfer into a volumetric flask of 100-200 ml. Rinse the conical flask several times with distilled water and pour into the same volumetric flask, bring to the mark (basic solution).From the main solution, take an aliquot of 50 ml, add concentrated ammonia to precipitate iron and 2 ml of excess ammonia. To boil contents of a flask to low boil, to filter in a flask on 500 ml through the compressed filter in a hot form. Rinse the precipitate 7-8 times with hot water. Put the filtrate on the electric stove and evaporate until the smell of ammonia disappears. Cool, bring the volume of the flask solution to 200 ml, pour 1 g of ammonium fluoride, add 10 ml of xylenol orange indicator solution and neutralize the excess sulfuric acid with ammonia (1: 2) until the solution turns from yellow-lemon to orange. 30 ml of a buffer solution (pH = 5-6) and 10 ml of 10% sodium thiosulfate are poured, and the solution is colored magenta-purple, titrated with vigorous stirring with Trilon B solution until the solution turns yellow-lemon color. The clarity of the color transition at the equivalent point depends on how correctly and carefully the neutralization of the solution was carried out with ammonia before adding the buffer solution.

The zinc content is calculated by the formula			,

Where V is the volume of the solution of trilon B, followed by titration;

T is the titer of the solution of trilon B in zinc, g / ml;

a - sample weight, g;

50 - aliquot part of the basic solution, ml.

200 - the volume of the volumetric flask, ml.

Determination of lead by the complexometric method

According to this method, the sample is successively decomposed with acids, the lead is separated from other elements by precipitation as sulfate, then it is dissolved in ammonium acetate and titrated with trilon B in acetate buffer solution at pH = 5.5 with xylenol orange indicator.

A distinctive feature of these products is the high content of arsenic and antimony in them, which greatly complicates the determination of the main elements.

Reagents:

Hydrochloric acid density of 1.19

Sulfuric acid with a density of 1.84

Nitric acid with a density of 1.4

Ammonium fluoride

Xylenol orange indicator

Trilon B, titrated solution (0.05 N solution)

Sodium sulfate

Potassium methyl

Ammonium acetate, 30% solution containing 3 ml of hydrochloric acid density of 1.19 to 1 liter.

The course of the analysis

A portion of the material 0.5 g is placed in a conical flask with a capacity of 250 ml, moistened with water, 15-20 ml of hydrochloric acid, 1-2 g of sodium sulfite and 1-2 g of ammonium fluoride are poured, boiled for 5-10 minutes, 5 ml of nitric acid are added and heated to complete decomposition of the sample by reaction	PbS + 2HCI = PbCI2 + H2S

CuS + 4HNO3 = Cu(NO3)2 + S + 2NO2 + 2H2O

PbSiO3 + 6HCI + 4NH4F = PbCI2 + SiF4 + 4NH4CI + 3H2O

Pb3(AsO4)2 + 12HCI + 2Na2SO3 = AsCI3 + 2Na2SO4 + 3PbCI2 + 6H2O

Pb3(SbO4)2 + 12HCI + 2Na2SO3 = SbCI3 + 2Na2SO4 + 3PbCI2 + 6H2O

Then add 7-10 ml of sulfuric acid and heat until abundant vapors of sulfuric anhydride. Cool, wash off the edges of the flask with a minimum amount of water (10 ml), and again evaporated to a thick white vapor. Add 1-2 g of potassium bromide to completely remove antimony from the sample as a compound with bromine. This operation is repeated 2 times. The reaction proceeds according to the equation:

2HSbO2 + 6KBr + 3HSO4 = 2SbBr3 + 3K2SO4 + 4H2O

50-60 ml of water are poured in, boil until soluble sulphates are completely dissolved. The solution is cooled in running water for 1 hour. The precipitate of lead sulphate is filtered through a filter with a filter paper, washed 2-3 times with cold water, acidified with sulfuric acid, then with cold water until neutral wash water (sample with methyl orange). The filter cake is transferred to a flask in which sedimentation has been carried out, 25-35 ml of ammonium acetate are added, the mixture is made up to 150 ml with water and leaching is carried out at a temperature near boiling point for 30 minutes. The volume of solution before titration should be at least 100-120 ml.

To the cooled solution add 10 ml of the xylenol orange indicator solution and titrate with the Trilon B solution until the color changes from violet-crimson to yellow.

The lead content is calculated by the formula:

where V is the volume of the solution of trilon B, followed by titration,

T is the titer of the solution of Trilon B for lead, g / ml; (0,01035)

a - linkage,

Test questions:

1. Show the main zinc reserves in the world.

2. Show top zinc minerals.

3. To tell the deposits of lead-zinc ores in the CIS.

4. Which deposits of lead-zinc ores are known in Kazakhstan.

5. Complexometric method for the determination of zinc.

6. Complexometric method for the determination of lead.

Home task:

1. Get acquainted with new ways to get zinc.

2. Examine the zinc minerals and ores.

Assignment to IWS

A student must prepare an ALS on the following topics:

1. To study the characteristics of zinc concentrate.

2. Know the features of the use of finished products (zinc).

3. To study the physico-chemical properties of zinc.

4. The current state of zinc production in Kazakhstan and abroad.

Laboratory work 8, 9.

Roasting of zinc concentrates

The aim of the work is to familiarize yourself with the roasting of sulphide zinc concentrates in a “fluidized bed” and the method of calculating the rational composition of the concentrate.

Brief theoretical information

Most of the zinc at the present time, it turns out, according to the hydrometallurgical scheme. The primary metallurgical operation is the roasting of zinc sulphide concentrate. Zinc concentrates are significantly different in composition. The content of the main components in them varies within%: 38-62 Zn; 0,7-6,0 Pb; 0,05-4,5 Cu; 0,1-0,3 Cd; 2-13 Fe; 30-34 S.

Roasting zinc concentrates is used to convert insoluble in weak solutions of sulfuric acid zinc sulphides into soluble oxides and sulphates. In general, the oxidation of sulfides during calcination can be expressed by the following main reactions:

2MeS + 3O2 = 2MeO + 2SO2;                                                                      (1)

MeS + 2O2 = MeSO4;                                                                                   (2)

MeS + O2 = Me + SO2.                                                                                 (3)

These reactions represent the final (total) result of the oxidation process and do not reveal its mechanism at all. The end result of oxidation can be judged by the magnitude of the loss of the standard isobaric potential of reactions: comparing the magnitudes of the loss of the isobaric potential for single-type reactions, it is possible to determine the relative degree of probability and the order of their realization.

The decrease in the standard isobaric potential of sulfide oxidation reactions at a given temperature depends on the dissociation pressure ratio of sulfide, sulfate, metal oxide and sulfuric anhydride. When sulphide, sulphate and metal oxide have a high dissociation pressure at a given temperature, the oxidation of sulphide proceeds to form a metal and sulfur dioxide. When sulfide and sulfate have very low dissociation pressures, then under the condition of the existence of a very strong oxide of the same metal, its sulfide will be oxidized to the sulfate state.

Sulfides of heavy non-ferrous metals can be oxidized depending on the temperature according to different schemes: at low temperatures (below 6,000 ° C and in the period) - to sulphates, and at firing temperatures (950-900 ° C) - to oxides.

Iron sulfate has a high dissociation pressure already at low temperatures. In this regard, at temperatures of 300-6000С and higher, the oxidation of iron sulfides thermodynamically proceeds to iron (II) oxide and then to iron (III) oxide. Zinc sulfate is more stable and begins to decompose at a temperature of 600-6500C. In the presence of other substances (sulfides, iron oxides and silica), the elasticity of sulfate dissociation increases dramatically.

The formation of oxides and sulfates during firing occurs according to the following final reactions:

MeS + 1,5O2 =MeO + 2SO2;                                                                        (4)

2SO2 + O2 2SO3;                                                                                      (5)

MeО + SO3MeSO4.                                                                                 (6)

The first reaction is almost irreversible, the flow of the second and third reactions is provided by the corresponding equilibrium constants. When the partial pressure of sulfuric anhydride in furnace gases is greater than the dissociation pressure of sulfate, sulfate formation will occur (sulfatizing calcination), when the partial pressure of sulfuric anhydride in furnace gases will be less than the dissociation pressure of sulfate, oxide formation will occur (oxidative calcination).

As follows from the above, sulfatizing calcination requires higher concentrations of sulfur gases in the furnace atmosphere, the process temperature should be limited to prevent thermal dissociation of sulfates, sulfatizing and oxidizing calcination requires good contact of furnace gases with the calcined material. All these conditions are best provided in the "fluidized bed" furnaces.

At low temperatures, in particular in nature, there are processes of the direct formation of metal sulfates from their sulfides by the reaction

MeS + 2SO2MeSO4.                                                                    (7)

At high temperatures, in roasting conditions in furnaces, the production of heavy non-ferrous metal sulphates by this direct reaction does not take place due to the action of a reversible reaction.

At low temperatures, in particular in nature, there are processes of the direct formation of metal sulfates from their sulfides by the reaction

3MeSO4 + MeS 4 MeO + 4SO2                                                              (8)

The equilibrium pressure of sulfur dioxide by this reaction for semi-sulfur copper reaches 0,5105Pa at a temperature of 4000C. The reactions of the interaction of sulfides and sulfates of lead and zinc also proceed vigorously.

Thus, the majority of sulphates of heavy non-ferrous metals cannot exist with their sulphides under roasting conditions in furnaces that provide contact between solid particles, and as a result of interactions they produce oxides. Proper sulfatization of the metal can be achieved only in the case when there is a small amount of sulphides in the calcined material. In other words, the formation of sulfates in the process of sulfatizing calcination ultimately occurs not by the reaction of the direct oxidation of sulfides, but by the reaction of sulfatization of the resulting oxides.

MeO + SО3MeSO4                                                                                (9)

When roasting zinc concentrate in a cinder, it is necessary to transfer part of the sulfur to the sulphate form in order to restore the sulfuric acid loss in the closed zinc production process. When zinc concentrates are roasted, zinc sulphates almost completely decompose. Sulfate sulfur is preserved in the cinder by ensuring the removal of a significant amount of fine dust (up to 40%) to gas flow and dust collecting devices, where sulphate zinc is stored at lower temperatures in gas ducts. The offset of the calcine from the furnace with the agreed dust provides in the combined product sent for leaching, the content of sulfate sulfur in the range of 2.5-3.5%.

In case of lack of oxygen in the air, when the corresponding temperatures in the roasting mixture are reached, dissociation reactions of higher sulphides take place with the formation of lower sulphides and elemental sulfur:

2FeS2 = 2FeS + S2  (10)

4CuFeS2 = 2Cu2S + 4FeS + S2                                                                   (11)

4CuS = 2Cu2S + S2                                                                                     (12)

The possibility of these processes occurring is due to the high partial pressures of sulfur vapor during dissociation, reaching, in particular, for pyrite, 15105Па already at a temperature of about 7000С. However, if the concentration of free oxygen in the furnace atmosphere is sufficient, then many sulfides, in particular pyrite, chalcopyrite and others, can begin to oxidize at temperatures below the beginning of their decomposition. The behavior of higher sulphides in this case will largely be determined not only by the presence of oxygen and the thermodynamic factors of dissociation processes, but also by the thermodynamic factors of their direct oxidation processes and, in particular, by the thermal effects of oxidation reactions and the associated sulfides.

Oxidation reactions of sulfides with oxygen are exothermic heterogeneous reactions that take place at the interface between the solid and gaseous phases, and are accompanied by the formation of an oxide or sulfate film and release of sulfur dioxide, which creates a peculiar gaseous shell around the solid part. This makes it difficult for oxygen to penetrate the reaction zone. The phenomenon of diffusion during firing is very important and often determines the speed of the process.

Fine grinding of ore and an increase in the temperature of the burning process increases its speed, but the maximum possible temperatures for conducting the process are limited by the melting temperatures of the most low-melting components of the concentrate (oxidative burning) and the dissociation of sulfates (sulfating burning).

Local overheating has a great influence on the sintering of the calcine. The temperature of the surface at which the reaction takes place, accompanied by significant heat generation, differs from the temperature of the gas stream and the environment and depends on the reaction rate, its thermal effect and the amount of heat removed from the surface. Thus, intensive heat transfer in the layer contributes to uniform temperature distribution in it, eliminates sintering of calcine due to local overheating and has a decisive influence on the performance of the firing process as a whole.

A great influence on the firing process has a gas phase composition. To speed up the oxidation of sulfides, it is desirable to supply excess air and enrich the blast with oxygen. The kiln gases are used to produce sulfuric acid; therefore, the excess air is taken as far as possible in such a way that the SO2 content of the exhaust gases is at least 4.5 ... 6%. The content of sulfur dioxide in the exhaust gases is usually within 8 ... 10%, with enrichment of the blast with oxygen - up to 14%.

In the process of roasting the concentrate, a part of zinc can interact with higher iron oxides and silicon oxide, forming ferrites and zinc silicates. The presence of both zinc compounds in the calcine is undesirable due to the fact that the former are practically insoluble in weak solutions of acids and pass into cakes, and the latter, although soluble, contaminate the solutions with colloidal silica, which increases their viscosity and reduces the rate of settling and filtration of the slurries. The formation of ferrites and zinc silicates begins at low temperatures and intensively proceeds at calcination temperatures, therefore, their reduction in the calcine can be made by properly preparing the charge with a minimum content of iron oxides and silicon to intensify the calcination process.

Roasting zinc concentrates is currently being carried out in “fluidized bed” kilns. The great advantages of this type of burning in comparison with burning in hearth furnaces are the simplicity of furnace design, good gas contact with the material, high values ​​of heat transfer coefficient in the layer, high specific productivity, the possibility of efficient use of heat from exhaust gases and their use for the production of sulfuric acid, complete mechanization and automation of the process. In these furnaces, both oxidative and sulphating roasting are equally successful.

Equipment, technical instrumental tools:

1. Electric;

2. Reactor;

3. Thermocouple;

4. Millivoltmeter;

5. Gas analyzer;

6. Blower;

7. Analytical scales;

8. Forceps;

9. Iron boat.

Methodof work

Roasting zinc concentrate is carried out in a reactor of transparent quartz. The reaction part of the reactor is inside the detachable electric furnace. The reactor has a lattice through which air is blown upwards in an amount necessary for oxidizing sulphides and creating a “fluidized bed”. A diagram of the installation for firing in a “fluidized bed” is shown in Figure 1. The temperature in the furnace is measured using a chromel-alumel thermocouple according to the readings of a millivoltmeter. Exhaust gases are fed to the gas analyzer in order to determine the released SO2. Schemes of gas analyzers are presented in Figures 1 and 2.

Figure 1. Diagram of an installation for roasting zinc concentrates in a “fluidized bed”: 1 - loading opening; 2- thermocouple; 3- reaction tube; 4- split furnace; 5- "fluidized bed"; 6-lattice; 7-crane; 8-Drexel with hydrogen peroxide

The weight of the concentrate, the firing time and the firing temperature are set by the teacher. The work is carried out in such a sequence. Turn on the furnace for heating the reactor. After the temperature inside the pipe reaches 700-8000С, the blower is turned on and the required air flow is set according to the indications of the rotameter. Then with the help of a funnel the concentrate sample is loaded, the moment of concentrate loading is the beginning of the experience. During the experience, you can open the split furnace and observe the process.

Figure 2. Installation diagram for determining SO2 in waste gases: 1-reaction vessel; 2-potentiometer; 3-unbalanced bridge; 4 test flask

At the end of the experiment, the furnace is turned off and the reactor is cooled, after which it is removed from the furnace, the candle end is poured into an iron boat and cooled, the cooled candle end is weighed, wearyed in a mortar and the total sulfur is determined in it. Using the potentiometer diagram (see Fig. 2) connected to the system with a gas analyzer, or based on the results of titration of selected samples from drexelles, the amount of released sulfur is determined and both desulphurisation results are compared (by calcine and gas).

Required calculations

The following metallurgical calculations are caused by the need to determine the rational composition of the processed concentrates, the amount of required blast, the amount and composition of the resulting gases, as well as the quality of the cinder obtained.

Calculation of the rational composition of raw concentrate

Suppose that a concentrate of the following composition is roasted%: Zn 51; Pb 2,93; Cd 0,17; Cu 0,94;  Fe 7; S 31; SiO2 4,96; А12O3 0,6; СаО 0,4; CO2 0,31; other 0,69.

According to the mineralogical study, the metals are in concentrate in the form of the following compounds: Zn in the form of ZnS; Pb - PbS; Cu — CuFeS2; Fe — FeS and FeS2; Cd - CdS; Ca - CaCO3.

In nature, there is no mineral corresponding to the formula FeS, which is isomorphically connected with ZnS in the form of marmatite.

Required to calculate the rational composition of the concentrate.

amountof ZnS:

65,4Znrequired 32 S

51,0 – x;

X=25,1kg,

ZnS = 51 + 25,1= 76,1kg.

amount of PbS:

207,2Pbrequired   32 S

2,93 – x;

X= 0,45кг,

PbS = 2,93 + 0,45= 3,38kg.

amount of CdS:

112,4 Cd требуется   32 S

0,17 – x;

X= 0,05kg,

CdS = 0,17 + 0,05= 0,22kg.

amount of CuFeS2:

63,6 Cu требуется   55,8 Fe

0,94 – x;

X= 0,88кг Fe,

63,6Curequired  64 S

0,94 – x;

X= 0,95кгS,

CuFeS2 = 0,94 + 0,88 + 0,95 = 2,72kg.

For determine the amount of FeS and FeS2, it is necessary to know the distribution of iron between these two compounds.

Sulfur remains for FeS and FeS2

31 – (25,1+0,45+0,05+0,95)=4,45kg,

of iron - 7 - 0.83 = 6.17 kg.

Denote the amount of iron in FeS through a kg, then the amount of iron in FeS2 will be (6,17 - а) kg.

The amount of sulfur in FeS:

55,8Fe – 32 S

а – x1S;

x1 = 0,573а.

The amount of sulfur in FeS2:

55,8  Fe – 64 S

(6,17-а) – x2 S;

x2 = 7,1 – 1,15а.

x1 + x2 = 4,45

or 0,573а + 7,1 -1,15а = 4,45,

from where а= 4,6.

FeS= 4,6 + 4,60,573=7,24;

FeS2 = 1,57 + 1,81 = 3,38.

The amountСаСО3:

36,1СаО – 44СО2

0,4 – х;

СаСО3 = 0,4 + 0,31 = 0,71kg

The results of the calculation of the rational composition of the concentrate are summarized in table 1.

Table 1 – Rational concentrate composition, %

| Compounds | Concentrateelements, % |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Zn | Pb | Cd | Cu | Fe | S | SiO2 | А12O3 | CaO | СО2 | Other | Total |
| ZnS | 51,0 | - | - | - | - | 25,1 | - | - | - | - | - | 76,10 |
| PbS | - | 2,93 | - | - | - | 0,45 | - | - | - | - | - | 3,38 |
| Cd | - | - | 0,17 | - | - | 0,05 | - | - | - | - | - | 0,22 |
| CuFeS2 | - | - | - | 0,94 | 0,83 | 0,95 | - | - | - | - | - | 2,72 |
| FeS | - | - | - | - | 4,6 | 2,64 | - | - | - | - | - | 7,24 |
| FeS2 | - | - | - | - | 1,57 | 1,81 | - | - | - | - | - | 3,38 |
| SiO2 | - | - | - | - | - | - | 4,96 | - | - | - | - | 4,96 |
| А12O3 | - | - | - | - | - | - | - | 0,60 | - | - | - | 0,60 |
| СаСО3 | - | - | - | - | - | - | - | - | 0,40 | 0,31 | - | 0,71 |
| Other | - | - | - | - | - | - | - | - | - | - | 0,69 | 0,69 |
| Total: | 51,0 | 2,93 | 0,17 | 0,94 | 7,00 | 31,0 | 4,96 | 0,60 | 0,40 | 0,31 | 0,69 | 100,00 |

Calculation of the required amount of air for roasting zinc concentrate

Suppose that a concentrate of the following composition is roasted, %:  Zn 50; Pb 3; Cd 0,2; Cu 1;  Fe 7; S 30; SiO2 5; А12O3 0,5; СаО 0,5;   other 2,8.

Calculation is carried out on 100g of concentrate. To simplify the calculation, we assume that in the process of burning, sulfur burns completely up to SO2. Then by reaction	S + O2 = SO2

30 g of sulfur will require 30 g of oxygen.

Zinc is oxidized to ZnO, then the oxidation of zinc will require:

50.0 ∙ 16 / 5.4 = 12.23 g ofoxygen.

A total of 30 oxygen + 12.23 = 42.23 g will be required. Since the air contains 23% of the mass. oxygen, then you can determine the required amount of air:

42,23 ∙ 100 : 23 = 183,6g.

In volumetric units, the amount of air will be:

183,6 : 1,293 = 142,0 дм3 (1,293 g/dm3 – air density). In the laboratory takes excess air 2,5:

142 ∙ 2,5 = 355l.

If you take the roasting time of 20 min, then the air flow rate will be

355 ∙ 60 : 20 = 1065 dm3/h.

10g of concentrate is taken for roasting, so the air consumption will be 107 dm3/h.

Specific air consumption per ton of concentrate is determined by the formula:

,

where Qun is the unit air flow rate, m3 / t;

Q - air flow during the experiment, dm3 / min;

- roasting time, min;

- concentrate weight, g.

For our case, the specific air flow will be

Qуд =107 ∙ 20 ∙ 103 : 60 : 10 = 3567 m3/t.

After air supply and determination of its required flow rate with the help of a rotameter (graduation is shown in Figure 3), by turning the loading spoon, the concentrate is poured into the reactor. This moment is considered the beginning of

the experience

air flow

.

Figure 3. Graduation of the rotameter

In the firing process, the exhaust gases are passed through drexel with a 2% solution of hydrogen peroxide, alternately through each of the branches (Fig. 3). The time of passing the exhaust gas through each of the branches is set by the teacher.

Calculation of the degree of desulfurization

Suppose that the sulfur content in the calcine is 2.5%, and the yield of calcination is 8 g. Then the degree of desulfurization will be equal to(10  0,3 - 8  0,025) : (10  0,3)  100 = 93,3 %.

Processing results

After passing SO2-containing gases, sulfuric acid is formed through a 2% hydrogen peroxide solution. By titrating the acid solution with alkali, we determine the amount of SO2 absorbed by the solution for a given time, calculate the SO2 content in the exhaust gases during this period of time (% vol.) And build a kinetic curve in the coordinates: [% SO2 - t (min)] . The obtained dependence is compared with the calculated value of the concentration of SO2 in gases. For this, it is necessary to sum up the amount of released SO2 (g) in each section of the kinetic curve and calculate the average SO2 concentration during the experiment for 20 minutes. Then calculate the theoretical composition of the exhaust gases.

Determination of the theoretical composition of exhaust gases

Excluding sulfide and sulfate sulfur in the candle, we can assume that all sulfur of the concentrate will be converted to SO2 during roasting.

The amount of sulfur in 10 g of concentrate - 3 g.

The number of formed SO2 g - 6 g

The amount of air fed into the kiln for 20 minutes107 20 : 60 = 35,67 l or  35,67  1,293 = 46,12 g,

including oxygen 46,12  0,23 = 10,61 gand

nitrogen 46,12  0,77 = 35,51 g.

Part of oxygen go to formation  ZnО (12,23  0,1 =1,22 г);

in the gases will be 10.61 - 3.0 - 1.22 = 6.39 g of oxygen.

The total mass of exhaust gases will be 46.12 + 3.0 - 1.22 = 47.9 g.

Table 2 shows the composition of the exhaust gases.

Table 2 - The composition of the exhaust gases

| Component | Weight | % of the mass. | Volume, dm3 | % vol. |
| --- | --- | --- | --- | --- |
| SО2 | 6,0 | 12,5 | 6 : 64 ∙ 22,4 = 2,10 | 6,0 |
| О2 | 6,39 | 13,4 | 6,39 : 32 ∙ 22,4 = 4,47 | 12,8 |
| N2 | 35,51 | 74,1 | 35,51 : 28 ∙ 22,4 = 28,4 | 81,2 |
| Total | 47,9 | 100,0 | 34,97 | 100,0 |

Determination of sulfur content in gases

After each sampling, the contents of the drexelles are transferred to a conical flask with a capacity of 250 cm3. Titration with alkali is carried out in the presence of an indicator. To do this, three drops of methyl orange are added to the flask, and the solution becomes red. Titrate the solution while gently pouring the aqueous alkali solution of known concentration until a yellow color appears. In this case, sulfuric acid is neutralized and the solution changes color. SO2 mass (g) absorbed by hydrogen peroxide:,

where TS is the alkali titer of sulfur;

VNАOH - alkali volume, followed by titration, cm3.

Report content

1. A summary of the theory of burning in a "fluidized bed" and its implementation.

2. Description of equipment and methods of work.

3. The necessary calculations and the results obtained.

Control questions

1. Why is zinc concentrate calcined?

2. By what reactions can oxidation of metal sulfides occur?

3. Under what conditions can the formation of sulfates and metal oxides occur during firing?

4. What is the metal sulphide ignition temperature?

5. What influences the performance of the sulphide roasting process?

6. What is the composition of the firing gases and how are they used?

7. What is harmful in the stub ferrites and zinc silicates?

8. In which furnaces are zinc concentrates calcined?

9. How is the laboratory experiment on firing concentrates?

Task: conduct calcination of zinc sulphide concentrates in a “fluidized bed”, determine the rational composition of the concentrate and calculate the degree of desulfurization.

Laboratory work 10, 11

Electrolytic precipitation of zinc from sulphuric acid solutions.

The aim of the laboratory work is to get acquainted with the principles of electrolytic deposition of zinc from sulphate solutions, to study the influence of some factors (current density, electrolysis duration, electrolyte composition, etc.) on technological indicators and the process.

The plan of the laboratory work:

1. Check homework

2. A brief explanation of the goals and objectives of the laboratory work.

3. Issuance of initial data for calculation

4. Students carry out the necessary theoretical and technological calculations

5. Receiving admission and performing laboratory work

6. Processing of the obtained results, writing conclusions and conclusion

7. Protection of laboratory work

Brief theoretical information

Electrolysis is one of the main operations of the hydrometallurgical method of zinc production, filtered transparent neutral zinc sulphate solution is fed to the electrolysis, containing impurities already in such quantities that can not adversely affect the zinc electrodeposition. The approximate composition of the solution entering the electrolysis is as follows: Zn - 120...170 g/dm3; Sb - 0,05...0,2 mg/dm3; Мо - 4,5...5 g/dm3; As - 0,1...0,8 mg/dm3; Cd3,5...4,5 mg/dm3; С1- 100...150 mg/dm3; Си- 0,1...0,2 mg/dm3; Fе - to50 mg/dm3; Со - 2,5...4,5 mg/dm3.

During electrolysis of zinc solutions, baths with aluminum cathodes and lead (in an alloy with 1% silver) anodes are used. The electrolyte contains an aqueous solution of zinc sulfate (50 .. .60 g / dm3), sulfuric acid (100 .. .120 g / dm3) and a small amount of impurities. At the time of inclusion in the electrical network DC zinc electrolyte bath in the first approximation represents. Electrochemical system A1 / ZnSO4, H2SO4, H2O/Pb. Since soon after switching on the bath, the aluminum cathode is covered with a layer of zinc and begins to work as zinc, we can consider the system Zn | ZnSO4, H2SO4, Н2О | Рb.

The main components of the electrolyte in solution are dissociated according to the following equations:

ZnSO4 = Zn2+ + SO42-

H2SO4 = Н+ + HSO4- = 2Н+ +SO42- ;

Н2О =  Н++ОН-.

Under the influence of a passing electric current, positively charged ions move to the electrode connected to the negative pole of the direct current source — the cathode; negatively charged ions move to the electrode with opposite charge to the anode and are discharged to them according to their position in a series of voltages and conditions electrolysis.

Processes on the cathode. During electrolysis at the cathode, the following processes are possible:

Zn2+ + 2е==Zn;

2Н+ + 2е== Н2.

As a general rule, processes involving the discharge of the most electropositive ions from an electrochemical series of metal voltages, a part of which is given below, proceed primarily at the cathode:

Na+ - -2,713; Mg2+ - -2,380; Zn 2+ - -0,763; Fe2+ - -0,441;

Cd2+ - -0,402; Ni2+ - -0,250; РЬ2+ - -0,126;

Н+ - ± 0;

Си2+_ +0,337; Hg2+ - +0,798; Ag+ - +0,799; Аи+ - +1,680.

It can be seen that zinc is a metal with a potential that is much more electronegative than hydrogen, and therefore it would be natural to expect hydrogen to be released at the cathode, and not zinc. However, the potential of hydrogen evolution varies depending on the concentration of its ions in the solution and other factors. Experiments have established that during the electrolysis of water acidified with sulfuric acid to a content of 1 g-hydrogen ion in 1 dm3, hydrogen is released on a platinized electrode at atmospheric pressure and very low current density, a voltage of 1.7 V is necessary. If a zinc plate is used as the cathode in the same electrolyte under the same conditions, then it is necessary increase the voltage to 2.45 V. The difference in voltage is 0.75 V. This additional voltage is called overvoltage of hydrogen on zinc. Due to overvoltage, the potential of hydrogen shifts to a more electronegative direction and so much that the process of discharging zinc ions becomes not only possible, but also preferential. Therefore, the amount of hydrogen overvoltage during the electrolysis of zinc solutions is trying to maintain the highest,

Hydrogen overvoltage depends on many factors:

1) the cathode material;

2) tone density;

3) electrolyte temperature;

4) the activity of hydrogen ions in solution and the concentration of salts,

being in it;

5) additives introduced into the electrolyte, etc.

Electrolytic deposition of zinc is most influenced by an increase in current density: the greater the current density, the higher the hydrogen overvoltage (at 1000 A / m2 it is 1.17) and the smoother and finer the sediment is, 350 to 500 A is almost enough m2.

Hydrogen overvoltage also increases with a decrease in temperature and acidity. The presence of impurities in the electrolyte has a large effect on the overvoltage of water, the presence of even small amounts of ions of such metals in the electrolyte, which can be released simultaneously with zinc and the overvoltage of hydrogen on which is less than on zinc, causes an increased release of hydrogen at the cathode ,

With the addition of colloids to the electrolyte, the hydrogen overpotential increases, but only to a certain limit, with a further increase in the concentration of the colloid, the overvoltage begins to decrease.

The processes at the anode. In the lead anode during the electrolysis of a zinc sulfate solution, generally speaking, the discharge of the following ions is possible:

Рb - 2е== Pb2+ (lead anodic dissolution),

2OН- - 2е== Н2О + 1/2O2 (discharge of OH-water ions),

SO42-  -2е== SОз + 1/2O2 (ion discharge SO42-),

SОз + Н2О == SO42- + 2Н+,

The reversible potentials of these processes will be expressed by the following dependencies.:

ЕPb2+ = -0,122 + 0,028·lgСPb2+ . γPb2+;

ЕOH- = 0,4 + 0,058 ·lgCOH- . γОН-;

ES042- =1,95 + 0,029·lgCso42- . γS042-.

Conditionally take the activity coefficients γPb2+ = γOH- = γSO42- = 1.

In the process of electrodeposition of zinc, the concentration of SO42- is a few r-ion / dm3, i.e. it can be roughly considered that	Eso42- ≈ 1,96В.

In acidic solutions, the concentration of OH- is equal to 10 ... 14 g-ion / dm3, therefore, the potential of the discharge of OH- will be equal to:

Еон- = 0,4 + 0,058 . lg10-14=1,21 В.

Comparing these two processes, we find that the discharge of OH- has a more negative potential than SO42-, therefore, first of all, it should discharge the OH-.

Lead discharge potential is lower than OH-, and as the lead concentration in the sulfate electrolyte is very low, the potential of its discharge. decreases even more. During electrolysis with new lead anodes, first of all, lead oxidation will take place on them, i.e. the anode will behave as soluble - PbSO4 will be formed. Since the solubility of lead in a sulphate solution is low, when the anode layer is quickly saturated with lead sulphate, which crystallizes on the surface of the anode, forming a diaphragm-like surface, while due to low electrical conductivity, lead sulphate isolates part of the anode surface. Reducing the active surface of the anode at a constant ampere load leads to an increase in the true anodic current density, resulting in an anodic potential increases and favorable conditions are created for the oxidation of divalent lead to tetravalent:

Pb2+ ~ 2е = Pb4+.

The resulting Pb (SO4)2 is easily hydrolyzed by the reaction	Pb(SO4)2 + 2Н2ОРbO2 + 2H2SO4.

Lead dioxide is deposited in the porous sulfate "diaphragm", and the lead of the anode is completely isolated from the electrolyte, as a result of which its dissolution stops. Lead dioxide has a high electrical conductivity and causes an increase in current density. As a result of lead oxidation with the formation of PbO2, the concentration of PbSO4 in the electrolyte decreases, and the Pb2 + and SO42- ions are replenished first with the anode layer due to the dissolution of the PbSO4 initially deposited on the anode. The divalent lead ions that have passed into the solution are oxidized to tetravalent and are deposited on the anode as PbO2. Ultimately, the entire surface of the anode is covered with a layer of lead dioxide, mechanical isolation of lead from the electrolyte with a layer of PbO2 makes further dissolution of lead impossible, and at the anode only the discharge of OH- becomes possible.

It has also been established that direct decomposition of water can occur at the anode:

Н2О - 2е= 2Н+ + 1/2 О2

Oxygen is released near the anode. SO42-ions along with hydrogen ions remain in solution, causing the presence of acidity of the electrolyte.

Summing up all the reactions occurring during the electrolysis of zinc, we obtain

ZnSО4 + Н2О = Zn + H2SО4 + 1/2О2.

From the total reaction of the electrolysis process, it can be seen that as the zinc is deposited on the cathode, the solution is enriched with sulfuric acid. Deposition of 65.4 g of zinc entails the formation of 98 g of sulfuric acid, i.e. for every gram of zinc 98: 65.4 = 1.5 g of sulfuric acid is formed.

In practice, the content of sulfuric acid in the electrolyte is adjusted to 120 ... 170 g / dm3 with the standard scheme, which corresponds to a deposition of at least 120: 1.5 = 80 g of zinc from each cubic decimeter. Consequently, if the electrolyte supplied to the electrolysis contains 120 g / dm3 of zinc, then in the spent electrolyte its concentration will be 120 - 80 = 40 g / dm3. Further deposition of zinc is not carried out, because in more acidic solutions, hydrogen evolution will begin.

Current output. The ratio of the amount of a substance actually obtained during electrodeposition to the amount it should have, according to the amount of electricity passed through the electrolyte, expressed as a percentage, is called the current output (BT). Current output is determined by the formula

CO = (100· P)/ а· Q, %,

where P is the amount of precipitated zinc; g,

a is the electrochemical equivalent (for zinc a = 1.219 g / A • h),

Q - the amount of electricity passed, Cl.

where 1 A • h = 3600 Cl.

The current output is always less than 100% due to the occurrence of side processes and is 88 .. .92%. The current output depends on the concentration of zinc and hydrogen ions (acidity) in the electrolyte (decreases with decreasing zinc concentration and increasing the acidity of the BT solution), cathode tone density (with increasing cathode density of the BT current increases), electrolyte temperature (with increasing VT temperature) the presence of impurities in the electrolyte and from the state of the cathode surface (in case of formation of a loose cathode sediment, the true surface increases, the current density decreases and the current efficiency also decreases).

Impurities in electrolyte affect electrolysis in different ways.

Iron significantly reduces BT. This is due to the fact that bivalent iron ions are oxidized to trivalent at the anode, and at the cathode it is restored again to bivalent. Manganese behaves similarly: at the cathode, manganese ions are reduced to bivalent, and at the anode they are oxidized to four- or heptavalent. Fourvalentmanganese in the form of MpO2 (manganese sludge) is released on the surface of the anode, protecting it from corrosion, the seven-valent gives the electrolyte pink color. Alternating oxidation at the anode and the reduction of these ions on the cathode leads to an unproductive expenditure of electrical energy.

Impurities of copper, arsenic, antimony, silver, germanium, and especially cobalt, have a dramatic effect on BT. These ions, discharging at the cathode, create separate areas in which the hydrogen overvoltage will be less than on zinc, therefore hydrogen is intensively emitted at such sites, which causes a decrease in the zinc current yield. In addition, in the presence of these impurities, cathode zinc is obtained that is highly corroded. This is explained by the fact that when impurities are released, short-circuited microgalvanic elements Co-Zp, Cu-Zp, etc. are formed on the cathode, in which zinc is the anode and the metal impurity is the cathode. During the operation of such elements at the anode, the process of dissolution of zinc (anodic process) is in progress, and at the cathode a process of hydrogen evolution occurs (cathodic process).

Metals more electronegative than zinc (aluminum, magnesium, sodium, potassium) can be present in the electrolyte without much harm to the process, as they accumulate, the resistance of the electrolyte increases, which leads to an increase in the voltage on the bath and an increase in power consumption.

The voltage during electrolysis of zinc solutions is composed of the voltage decomposition of zinc sulfate and the voltage required to overcome the resistance of the electrolyte, cathode, anode, rods, etc. It depends on the current density (with increasing current density, the voltage on the bath increases), temperature (with increasing electrolyte temperature, the voltage on the bath decreases), acidity (with increasing acidity of the electrolyte, the voltage on the bath decreases) and the distance between the electrodes (with increasing distance between the electrodes on the bath increases). Practically the voltage on the bath is 3.4 ... 3.6 V (theoretical - 2.45 V).

The energy consumption during the electrolysis of zinc solutions per 1 ton of cathode zinc is determined by the formula	А= (Q · Ев· 1000) / Р, J/t*,

whereEvis the voltage on the bath.

* 1 kW • h = 3.6 • 106 J.

Energy consumption is also dependent on a number of factors. The higher the current density, the more energy is consumed. With an increase in the acidity of the electrolyte, the consumption of energy drops to a known limit (at the same current density) and then increases again. The optimum current density and acidity of the electrolyte is chosen taking into account many factors contributing to the production of cheaper zinc. In practice, 3000 ... .3300 kW is consumed to produce 1 ton of zinc. h DC (theoretically, about 2000 kW. h is needed).

Method of work

Installation of electrolysis of zinc sulphate solution

The electrolysis plant consists of a bath for a working electrolyte with electrodes, a cooler meter, a rheostat, an ammeter, a voltmeter, and a direct current source. Before starting the experience, it is necessary to calculate the current strength on the bath.

Fig. 9. Circuit of switching on the baths (a) and the position of the cathode and the anode during electrolysis (b): 1 - rectifier; 2 - bath or bath unit; 3 - voltage regulator (rheostat); 4 - current lead tires; 5 - cathodes; 6 - anodes; 7 - intermediate tire

For do this, measure the area of ​​the submerged part of the cathode (take into account both sides of the cathode and multiply by the current density specified by the teacher. Then carefully clean the electrodes, current leads, contacts. Catholes of the cooler meter and the working bath are weighed. The electrical circuit is assembled according to Fig. 9. make sure that they are parallel and strictly vertical. After the circuit has been checked by the teacher, electrolytes are poured into the baths, the current is switched on and the electrolysis time begins. ss electrolysis takes 1 ... 2 hours. During the experiment, the electrolysis process is monitored (condition of the cathode surface, current strength, voltage, color of the solution, discharge on the electrodes, etc.). In addition, at the beginning, middle and at the end The process determines the zinc content in the electrolyte and the acidity.After the end of the electrolysis, the cathodes are removed (under current) from the baths, then the direct current source is disconnected.The cathodes are washed with water and dried in a drying cabinet at a temperature of 500 ° C. Dried cathodes are weighed.

Example of current calculation

When determining the area of ​​one cathode, it is necessary to take into account both its sides, since each cathode hangs between two anodes and current flows from two sides.

Suppose that the electrical deposition of zinc is carried out on an installation consisting of two baths (see Fig. 9). Each bath has 4 anodes and 3 cathodes. All cathodes are the same size.

The cathode width and the height of the submerged part is 40 mm. Baths are connected in series, and the electrodes in the bath - in parallel. With a given current density of DK = 300 A/m2, the area of ​​one cathode

FK = 40 • 40 • 2 = 3200 mm2;

cathode area in one bath

FK = fK • n = 3200 • 3 = 9600 mm2 = 0.0096 m2,

where n is the number of cathodes in one bath.

Current strength

I = FK • DK = 300 • 0.0096 = 2.88 A.

Based on the data obtained.current output and power consumption are calculated.

The amount of electricity passed by the mass deposited in the cooler copper is calculated by the formula

Q = (26.8 • P): 31.25,

where P is the mass of deposited copper,

The results obtained are compared with the ammeter reading.

The results of the experience are recorded in the workbook in the following form:

| Time, min | Voltage, V | Current, A | DK, А/м2 | Electrolyte composition, g / dm3 |  | Mass, g % | Q, A • hr, | W% | А, kW • h / t | Note |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | H2SО4 | Zn |  |  |  |  |  |

Determination of zinc concentration in solution

An aliquot of 2 cm3 is transferred to a flask of 0.3 dm3 and 100 ... .150 cm3 of distilled water is added to the flask and 2 cm3 of an aqueous solution of xylene orange indicator. The solution becomes yellow. Then the solution is adjusted to a raspberry color with ammonia and 15 cm3 of buffer solution with a pH of 5.4 is added. Titrate the solution with a 0.1N solution of Trilon B until the solution turns from raspberry to yellow.

Based on the analysis data, the concentration of zinc in the solution (g / dm3) is determined by the formula

CZn = (T • V \ 1000) / V2,

where T is the titer of trilon B in zinc;

V \ _ the volume of Trilon B solution titrated for titration, cm3;

V2 is the volume of the solution taken for analysis, cm3.

Determination of the acidity of the solution

Take 2 ... 5 cm3 of solution and transfer to a volumetric flask per 100 cm3. Top up with distilled water. To stir thoroughly. From a flask take 5 ... 10 cm 3 of solution, place in a titration flask, add 50 ... 100 cm3 of distilled water. Add 1-2 drops of indicator - methyl orange. The solution becomes raspberry pink in the presence of acid. Titrate this solution with a 0.1N soda solution of Na2CO3 to a bright yellow color.

Content H2SО4 = (Т·V· 1000·V2) / (V1·Vз), g/dmЗ,

where T is the titer of soda by H2SО4 (0,0049 г),

V is  amount of 0.1N Na2CO3 solution, followed by titration, cm3

V1 is the amount of solution taken for titration, cm3,

V2 is the volume of the dilution flask, cm3;

V3 - the amount of the original solution, cm3.

Report content

1. A summary of the theory of electrolytic deposition of zinc from solutions.

2. Description of equipment and methods of laboratory testing. Bath circuit

3. The results obtained with the necessary calculations and schedule.

4. Analysis of the results and conclusions.

Questions for self-control

1. What is the principle of electrolysis?

2. What processes occur on the cathode during electrolysis of zinc solutions?

3. What is hydrogen overvoltage, from what factors and how

depends on

4. What processes occur at the anode during electrolysis of zinc solutions?

5. How is the lead anode protected from dissolution?

6. What is current output, what factors and how does it depend?

7. What is the voltage on the bath during electrolysis?

zinc solutions?

8. What determines the energy consumption during the electrolysis of zinc solutions?

9. How do impurities that have a more electrically positive potential than zinc affect the electrolysis process?

10. How do impurities that have a more electronegative potential than zinc behave during electrolysis?

Laboratory work 12, 13.

Electric melting of oxide zinc ores.

The aim of the laboratory work is the acquisition of practical skills recovery smelting zinc ores in the ore-thermal furnace.

The plan of the laboratory work:

1. Check homework

2. A brief explanation of the goals and objectives of the laboratory work.

3. Issuance of initial data for calculation

4. Students carry out the necessary theoretical and technological calculations

5. Receiving admission and performing laboratory work

6. Processing of the obtained results, writing conclusions and conclusion

7. Protection of laboratory work

Brief theoretical information

In the early 1950s, in search of a process for the processing of ferrous zinc ores and concentrates, a method of smelting them in a reflective furnace with stripping of zinc and obtaining iron in the form of cast iron was tested. Zinc was extracted almost completely with simultaneous production of slag and cast iron. The success of this attempt led to the study of slag melting in electric furnaces. At the same time, a new type of condenser with spray irrigation was used to produce liquid zinc. The experiments gave positive results and in 1951 an industrial electric furnace was built for the distillation of zinc with the charge melting (sterling process).

According to the developed technology, oxidized zinc-containing materials, reducing agent and fluxes are thoroughly mixed. The size of the material does not play a noticeable role, it is important that there is good contact between the components of the charge. The chemical composition of the mixture also does not impose strict requirements. Both zinc-rich concentrates are processed, as well as poor ones, containing about 20% zinc, as much iron, as well as lead, cadmium, and copper. The charge to be smelted should not contain more than 1% of sulfur and 1% of carbon dioxide; therefore, the sulfide material is prebaked and agglomerated.

The mixed mixture is first calcined for two hours in a tubular furnace at a temperature of 850–900 ° C, volatiles from the fuel are distilled off, part of the iron trioxide is reduced to oxide, and limestone dissociates. Hot charge enters the electric furnace (Fig. 10).

At the same time load 2-3 tons of charge. Molten slag and cast iron are collected in a hearth furnace. To protect the hearth from the action of the arc, keep the iron layer constant. To prevent direct contact of the electric arc with the cast iron, a layer of slag is maintained. Excess pig iron and slag are released, and vapors of zinc, lead, cadmium and other metals, carbon oxide are sent to the condenser. The process is carried out in such a way that the bulk of the zinc contained in the mixture is reduced and distilled off until the gangue melts and the liquid slag forms. At the same time, the direct effect of the electric arc on the charge is limited. Heat is transferred to the charge by radiation. The arc is open between the electrode and the slag. The temperature of the arc reaches 3000-4000 ° C, and the temperature of the bath is maintained around 1450 ° C in order to avoid the restoration of elements of the waste rock and overheating of the furnace masonry. This is achieved by loading the charge with slopes along the entire perimeter of the furnace and it absorbs heat for endothermic reactions, as well as for heating the charge. As in the case of distillation in retorts, the main chemical reaction in an electric furnace is the interaction of zinc oxide with carbon oxide to form vapors of zinc and carbon dioxide. ZnO + CO = Zn + CO2.

Fig. 10. Ore-smelting furnace for the “Sterling” process:

1 - oven; 2 - container; 3 - electrodes; 4 - transformer;

5 - capacitor; 6 - sump; 7 - years

This reaction is reversible and in the conditions of the retort it shifts to the right due to an excess of carbon, which deoxidizes СO2 + C = 2CO.

In electric furnaces, it is impossible to allow a significant excess of carbon, as this will lead to the blockage of the furnace with coke. Therefore, the condensation conditions are worse here and carbon deficiency is compensated by increasing the temperature of the exhaust gases up to 1000 ° C, while the rapid cooling of the gases prevents the formation of a large amount of puser. An excess of carbon is also unacceptable because the components of the waste rock can recover and partially fly, which dramatically affects zinc condensation. Therefore, carbon is loaded theoretically necessary amount for the recovery of zinc, lead, cadmium and part of iron. Iron in the slag left unrestored 1.5-6.0%; this is done in order not to restore silicon, magnesium, calcium. The ratio of calcium oxide to silicon oxide in the slag is maintained close to unity. Such a slag has sufficient fluidity at the temperature of release from the furnace (1350 ° C), separates well from the iron and melts after distilling the main mass of zinc from the charge.

Theory of zinc recovery from melts

The recovery of zinc from the melts occurs by direct and two-stage reduction:

(ZnO) + C = Zn + CO

С+ CO2 = 2CO

(ZnO) + CО = Zn + CO2

(МеO) + C = Zn + CO

Despite the large number of works, there is currently no single point of view on the proportion of direct and two-stage (indirect) restoration.

The reactivity of reducing agents for their relation to ZnO in the temperature range of 850-1850K is shown in Figure 11, from which it follows that at 1700K of reducing agents, the reactivity of carbon is higher than CH4, H2, and CO.

The kinetic curves of zinc reduction from the melt with carbon monoxide (II) at 12500С are shown in Figure 11, from which it follows that within 15 minutes the degree of zinc reduction is 92%.

It follows from the figure that with an increase in FeO melt, the degree of reduction to zinc increases, and the reduction process of zinc ends at 12500С in 10 minutes. This results from the fact that the iron which is restored from zinc reacts with ZnO, reducing it to metal:

FeO + СО = Fe + СО2,        Fe + ZnO = Zn + FeO.

When reducing zinc from slag melts, it was found that CaF2, Na2O significantly accelerate the process, and Р2О5 reduces the rate of reduction. This Impact is reflected in the “apparent” activation energy (Table 9).

Table 9- Effect of Additives on E-gas () ZnO Reduction

| Temperature, 0С | Еa, kkal/mol |  |  |
| --- | --- | --- | --- |
|  | No additive | Na2O | Р2О5 |
| 1250-1270 | 20,4 | 16,7 | 27,0 |
| 1270-1300 | 16,7 | 12,7 | 22,3 |
| 1300-1330 | 16,0 | 7,3 | 17,2 |

α, %

42%FeO

35%FeO

Time, min

Figure 11. Kinetics of zinc reduction from the melt

One of the reasons that causes a change in the rate of recovery with the introduction of surface-active additives will be some change in the surface structure of the melt. With the introduction of P2O5 into the slag, redistribution of oxygen anions occurs. A strong phosphorus cation separates the oxygen anions from the Fe2 + sibotaxis and from silicate complexes. As a result, the structure of the latter is complicated, which leads to a decrease in the surface activity of iron and zinc and an increase in surface viscosity. All this taken together enhances diffusion difficulties during the migration of iron and zinc cations to the reaction boundary with the gas. On the contrary, the introduction of monovalent ions Na + and F- into the slag is accompanied by the destruction in the surface layer of the silicon-oxygen complexes. Thus, the structure of the original slag will be destroyed by the addition of Na2O and CaF2. These phenomena develop mainly in the surface layer, since all additives are superficially active.

In the case of coal-thermal reduction of melts with the same additives, the positive effect of the introduction of Na2O and CaF2 was probably enhanced due to the acceleration of the reaction of regeneration of carbon monoxide on coal.

The process of coal-thermal recovery of zinc melts can be described by the following equations: 2ZnO + C = 2Zn + CO2                                     (а),

ZnO + C = Zn + CO                                   (б),

2FeO + С = 2Fe + СО2                                                (в),           (1)

FeO + С = Fe + СО                                                     (г),

According to modern views, a coal-thermal reduction proceeds through an intermediate product is carbon monoxide, forming a new phase, as a result of which two interface surfaces are formed: gas-slag and gas-carbon. The role of carbon monoxide in this case is reduced mainly to the delivery of the reducing agent to the gas-melt surface.

The carbon-gas-slag system is not equilibrium in a real process, and the recovery rate is not, strictly speaking, a function of the initial and final state, but depends on the path traveled by the system.

Since the transfer of reactants to the interaction surface occurs with the participation of three phases (carbon, gas, slag), it can be assumed that, depending on the reduction conditions (temperature and slag composition, determining the mobility of ZnO and FeO in it, size and texture of carbon particles, hydro and aerodynamic factors), the overall speed of the process can be controlled by the speed of one or more of the following stages:

1) Diffusion of ZnO and FeO in the slag;

2) Supply of CO to the surface of the melt;

3) CO adsorption on the surface of the melt;

4) The interaction of CO with zinc oxide or ferrous oxide;

5) Removal of the reaction products (CO2, Zn, Fe) from the interaction surface;

6) Regeneration of CO2 on the surface of carbon.

With a large excess of reducing agent, when the reaction rate is determined mainly by the concentration of MeO, we get:

VFe=dCFedτ=k3(CFeO)α3,

VZn=dCZnOdτ=k4(CZnO)α4,

VZnVFe=k4k3∙(CZnO)α4(CFeO)α3,

In the diffusion recovery mode of ZnO and FeO, the relative velocity VZnVFe  can be increased by melt mixing, if α4α3.

When α3= α4 the ratio VZnVFe does not depend on the conditions of the melt mixing.

When α3 α4 the ratio  VZnVFe  increases with decreasing rate of convective transfer of MeO to the reaction surface.

In all the cases considered, the ratio  VZnVFe   VZnVFe increases with increasing temperature, if in this case k2 and k4 increase faster than k1 and k3, respectively. If the activation energy of the ZnO reduction reaction is lower than the activation energy of the FeO reduction reaction, the ratio decreases with increasing temperature.

Equipment, technical tools:

The installation diagram on which the work is carried out is shown in Figure 12. The installation consists of the OSU-80 transformer, the actual single-electrode arc furnace with a graphite crucible of the electrode moving mechanism, a device for smooth power control, instrumentation, an exhaust fan.

Figure 12. Diagram of the laboratory installation for the electric smelting of zinc ores (SKSU named after M. Auezov)

1 - furnace casing, 2 - chromo-magnesite lining, 3 - carbon-graphite hearth, 4 - graphite crucible. 5 - carbon-graphite "cushion", 6-OSU-80 transformer, 7 - terristor regulator, 8 - graphite electrode, 9 - lower conductors, 10 - 13 - controlling ammeters and voltmeters, 14 - mechanism for moving the electrode, 15 - flexible part of the short network , 16 - furnace lid, 17- disconnector.

The order of the work

Found by calculating the number of components of the mixture (zinc ore, coke and lime) are weighed and mixed in the raw material box. The total amount of the charge should not exceed 1.5 kg. Previously, within 60-80 minutes, the graphite crucible arc is heated at J = 500-600A and U = 30-40B. After the crucible is warmed up, the whole charge is loaded in portions (100-200g) every 5-7 minutes. Melting is performed within 60 minutes in the presence of the teacher and the MEP. During the smelting period, it is possible to observe the melting of the charge and the actual smelting of ferrosilicon. You can only look into the oven through safety glasses. It is possible to work at the furnace only in a dressing gown, in a coke. Hands must be protected with cloth gloves.

After the end of melting, the electrode rises. The furnace is disconnected from the transformer. The crucible is removed from the furnace after it has been cooled for 8-10 hours. Then it breaks. After cooling, the products are recovered from the crucible. Slag and metallized alloy are carefully separated from each other and weighed separately, then analyzed for zinc and iron. The degree of extraction of zinc in the gas phase is calculated by the formula:

αZn(gas)=Gore∙GZnore-Gslag∙GZn(slag)Gslag∙GZn(slag)

где  Gore, Gslag    - accordingly, the amount of ore and slag, kg,

GZn(ore), GZn(slag)   - accordingly, the zinc content in the ore and slag, %.

Required calculations

As zinc-containing ore using ore deposit Sheimorden containing: 55,6% ZnCO3; 0,9% PbCO3; 3,3% FeCO3; 1,8% ZnS; 7,5%СаСО3·MgCO3; 5,2% Al2O3;  25,7% SiO2.

The reducing agent is coke, which contains: 85,1%С; 5,1%SiO2; 2,0%СаО; 0,8%MgО; 3,8%Fe2О3; 0,8%S; 1,4%Н2О; 1,0%Al2O3.

The degree of zinc to reduce is 96-98%.

The degree of iron to reduce is - 96-98%.

The degree of silicon to reduce is - 3-6%.

The ratio of CaO/SiO2 in the charge should be equal (0,8-1,4) : 1.

- The calculation of the active carbon content in coke.

Carbon consumption for iron to reduce:

Fe2O3 + 3С = Fe + 3СО

160(Fe2O3)   - 36 (С)

3,8         -  х1,                х1=0,829kg

Carbon consumption for silicon to reduce:

SiO2 + 2С = Si + 2СО

60(SiO2)  - 24(С)

5,1   - х2,          х2=0,1kg

Carbon consumption for hydrogen reduction:

Н2О + С = Н2 + СО

18(Н2О)  - 12(С)

1,4   -  х3,    х3=0,933kg

The active carbon content in coke:

Са=85 – 0,829 -0,1 -0,933 = 83,328kg

Take Са=83,4 kg (%)

2) Calculating the amount of coke

The amount of carbon to reduce zinc from 100 kg of ore:

ZnCO3 + 2С = Zn + 3CO

113,4(ZnCO3)   - 24(С)

55,6         - х4,        х4=11,4kg

The amount of carbon to reduce iron:

FeСO3 + 2С = Fe + 3СО

104(FeСO3)   - 24(С)

3,3          - х5,    х5=0,75kg

The amount of carbon per formation СаО:

СаСО3 + С = СаО + 2СО

100(СаСО3)   - 12

7,5            -  х6,    х6=1,8kg

The amount of carbon to reduce of silicon:

SiO2 + 2С = Si + 2СО

60(SiO2)  - 24(С)

25,7   - х7,          х7=0,51kg

The required amount of carbon, taking into account 10% excess carbon:

Gc = (11,4+0,75+1,8+0,51)·1,1/ Са= 14,46·1,1/0,834=19,07kg

2) Calculating the amount of lime

The required amount of lime is calculated based on the fact that the ratio of CaO/SiO2 in the charge should be 1.0, then:

1 = GCaO(ore)+GCaO(coke)+GCaO(lime)GSiO2(ore)+GSiO2(coke)+GSiO2(lime)

GCaO(ore)=7,5∙MCaOMCaCO3=7,5∙56100=4,2kg

GCaO(coke)=19,07∙0,02=0,38kg

GSiO2ore=25,7∙0,95=24,41kg

GSiO2(coke)=19,07∙0,051∙0,95=0,92kg

Let us assume that lime contains 94% CaO and 0.7% SiO2, the rest is 5.3% - loss on ignition. That is, in lime, the SiO2 content is 0.00744 times less than СаО.

Then     GSiO2(lime)= GCaO(lime)∙0,00744

The balance equation of  basicity is then:

∆=4,2+0,38+GCaO(lime)24,41+0,92+GCaO(lime)∙0,00744

Deciding on GCaO(lime)we find that

24,41+0,92+GCaO(lime)∙0,00744= 4,2+0,38+GCaO(lime)

25,33+GCaO(lime)∙0,00744 = 5,28+GCaO(lime)

20,05= 0,99256GCaO(lime)

GCaO(lime)=20,050,99256=20,2kg

Then the amount of lime will be:

Glime= 20,2/0,94 = 21,49kg

The composition of the charge for melting:

Ore - 100kg

Coke - 19.07 kg

Lime - 21.49 kg.

The procedure for the preparation of reports and their protection

1. A summary of the theory of zinc production in ore-smelting furnaces.

2. Description of equipment and methods of laboratory testing.

3. The results obtained with the necessary calculations.

4. Analysis of the results and conclusions.

The test questions

1. The practice of processing zinc ores in electric furnaces.

2. Reactivity of reducing agents with respect to ZnO.

3. Kinetics of Zn recovery from the melt.

4. Additives that accelerate and worsen the reduction of zinc from melts.

5. Joint recovery of zinc and iron from melts.

6. Methodology for smelting.

7. Calculation of coke.

8. Calculation of lime.

Home task:

1. To get acquainted with new pyrometallurgical methods for zinc production.

2. To study the technology and the main indicators of the process of zinc production in ore-smelting furnaces.

Assignment to IWS

A student must prepare an ALS on the following topics:

1. Independently study the thermodynamics of zinc reduction.

2. Independently study the kinetics of zinc reduction.

3. Explain the patterns of zinc reduction from oxide compounds and the behavior of zinc sulfate and sulphide.

4. Familiarize yourself with the design and operation of the ore-smelting furnace.

5. To study the method of obtaining zinc and zinc oxide in electric shaft furnaces.

Laboratory work 14, 15.

Melting of copper concentrates on matte.

The aim of the laboratory work: To reproduce in the laboratory one of the options for smelting copper concentrates - smelting of cinder, smelting of concentrate, smelting with converter slag, smelting without converter slag.

Brief theoretical information

The main method of processing sulfide copper concentrates is currently melting them in reflective furnaces to matte. Melting can be carried out with pre-firing and without firing. This is determined mainly by economic considerations. Concentrate roasting is carried out to remove part of the sulfur, associated mainly with iron, so that, when smelted, matte with a higher copper content is obtained. Firing is advisable to carry out the processing of high-sulfur concentrates with low copper content or high content of zinc, arsenic and antimony.

The purpose of smelting is the transfer of copper to matte and the separation of components of waste rock and part of iron into slag. Copper matte is a complex melt consisting mainly of copper and iron sulphides with a low content of sulphides of other metals, magnetite and slag inclusions. Copper smelting slags are alloys of ferrous oxide and calcium oxide silicates with a different content of silicates of other bases, as well as a small content of magnetite and sulphides. These two main products of melting have a different specific weight and are almost mutually insoluble in each other. They form two liquid layers in the furnace, so that the slag is separated from the matte.

The composition of the charge of reflective melting includes: crude concentrate or calcine, fluxes and converter slag. Quartz and limestone are used as fluxes required to obtain the required composition of waste slag. The converter slag is poured in a furnace in order to partially extract copper from it and use it as an iron-containing flux.

The main chemical compounds present in the charge of copper smelting are sulphides and oxides, whose behavior determines the chemistry of the process.

As the mixture is heated, numerous physical and chemical transformations and interactions take place in it. At temperatures around 950-10000С, low-melting sulfides are smelted from the charge. Merging with each other, they form the matte phase, in the form of droplets penetrate the layer of molten slag and go down to the lower part of the melt.

Slag formation begins later. First, the most low-melting oxide compounds — eutectics — melt, forming a primary slag melt. This melt, interacting with more refractory oxides (SiO2, CaO, etc.), dissolves them, which leads to the completion of the slag formation process. The chemical interaction in the smelting of calcine is reduced to the reactions between the matte and slag phases, i.e. between sulphides and oxides:

2FeS + 6Fe2O3 + 7SiO2 = 7(2FeO·SiO2) + 2SO2,                                             (1)

FeS + 3Fe3O4 + 5SiO2 = 5(2FeO·SiO2) + 5O2.                                                 (2)

Higher iron oxides enter the furnace either with a candle, or with converter slag. These reactions determine the degree of desulfurization in the smelting of the calcine, which is 20-25%.

The chemistry of the process of smelting raw (unfired) concentrate includes the dissociation of higher sulphides:

FeS2 =  FeS + 1/2S2                                                   				       (3)

2CuFeS2 = Cu2S +2FeS + 1/2S2                                                    		       (4)

2CuS = Cu2S + 1/2S2                                                   		                           (5)

as well as the processes of interaction of iron sulfide and oxides, as in the smelting of calcine.

Thus, the degree of desulfurization in the smelting of raw concentrate is formed due to the processes of dissociation and interaction processes of sulfides and oxides. In this case the degree of desulfurization is 40-50%.

Slag is a waste or by-product, but the slag yield and its composition, on which the physicochemical properties (viscosity, density, surface tension, melting point) depend, determine the loss of copper with slags.

Metal losses with slags are divided into two types: electrochemical and mechanical. Electrochemical losses are due to the slagging of cuprous oxide and the partial dissolution of its sulfide in the slag melt. Their value will depend on the composition of the liquid melting products and is determined by the reaction equilibrium.:

(Cu2O) sl + [FeS]matte = [Cu2S]matte + (FeO) sl                                                     (6)

The equilibrium constant of this reaction is expressed by the equation:

К=Cu2S(FeO)Cu2O[FeS]                or          (Cu2O) = 1K·  Cu2S[FeO][FeS]

From the last expression is seen that the copper content in the slag will increase with the increase in the matte content of copper, and in the slag - the concentration of ferrous oxide. With this in mind, try not to get the matte, containing more than 30% copper. Obtaining very poor mattes is economically unprofitable due to the high cost of their further processing by the method of conversion.

Mechanical copper losses in slags are associated with incomplete lagging of the smallest particles of matte and represent a thin suspension of sulphide inclusions. Their value depends on the physicochemical properties of the matte, and mainly slag, on the duration of settling and on the state of the molten bath.

The reduction of mechanical losses in slags contributes to the intensification of mass transfer in the melt, for example, due to mixing. In this case, small inclusions will be enlarged in a collision and will settle faster in the slag melt.

A clear dependence of copper losses on the physicochemical properties of slags determines the requirements for them:

1. slag must have a sufficiently low melting point in order to become molten at the furnace temperature and be sufficiently superheated,

1. slag should have a small viscosity for better separation from the matte,

2. Slag specific weight should be small. For a good settling of the matte from the slag, the difference in their specific weights must be greater than one,

3. it is necessary to obtain slag with the lowest ability to dissolve copper sulphides,

4. slag and matte should wet each other badly,

5. slag should be cheap, i.e. obtained with a minimum consumption of fluxes.

The production of slags of the optimal composition, which satisfies the economic requirements of this metallurgical process, is achieved by adding fluxes to the mixture.

In the practice of modern reflective melting, slag containing 36-42% SiO2.

3. EQUIPMENT, TECHNICAL INSTRUMENTAL TOOLS:

In laboratory conditions, the smelting of copper concentrate is carried out in an electric furnace with saltite heaters. For work heat-resistant graphite chamfer crucibles are used. The temperature in the furnace is measured by a platinum-platinum-rhodium thermocouple with the registration of its AKP 1-03. The installation diagram is shown in Figure 1.

The mixture for smelting consists of calcine or concentrate (depending on the task), the composition of which is given by the teacher, fluxes and converter slag. The number of fluxes and converter slag is determined by metallurgical calculation.

4. DESCRIPTION OF INSTALLATION:

Figure 1 - Furnace for smelting ores and concentrates

1- electric furnace, 2 - crucible with charge, 3 - thermocouple

5. ORDER OF PERFORMANCE OF WORK

The work begins with the calculation of the charge. The composition of the concentrate, converter slag, flux and other data necessary for calculating the charge are set by the teacher. The method of calculating the charge below.

Found by metallurgical calculation of the number of components of the mixture are weighed. The mixture is thoroughly mixed and loaded into a pre-calcined graphite chamfer crucible.

The crucible with the charge with iron tongs is placed in a furnace heated to 13000С. As the mixture is heated in a crucible, one can observe the process of its melting. It is possible to look into a red-hot stove only through protective blue glasses, the work near the stove is carried on in overalls.

After the entire mass of the charge has been melted, the crucible is kept in the furnace for another 10 minutes to better settle the matte from the slag. Then the crucible is carefully removed from the furnace with forceps and cooled. You should get acquainted with some properties of the slag in the molten state. On them it is possible to judge the composition of the slag. If the slag is acidic and contains a lot of silica, then it has the ability to stretch into long threads, which is explained by the significant viscosity of such slag. The main, strongly ferruginous or calcareous, “short” slag does not possess the ability to stretch into filaments. This can be observed by gently touching the surface of the molten slag with an iron bar.

After cooling, the melting products are knocked out of the crucible (in doing so, one should try not to break it). The matte into the slag is carefully separated from each other and weighed. The results obtained are compared with the calculated ones. In the event of a significant discrepancy, the reasons for the deviation of the experimental data from the calculated ones are ascertained.

The color of the matte in the fracture varies depending on the copper content in it. The matte obtained is compared with samples having an exact chemical composition.

6. CALCULATION EXAMPLE

The calculation of the charge is carried out on 100 g of the source material (calcine, concentrate).

Melting candle. The composition of the candle: Cu-13%, Fe-44,5%, Zn-2,7%, S-13,5%, SiO2-6,0%, CaO-1,3%.

The degree of desulfurization at smelting is 23%.

Extraction of copper in matte -95%.

The sulfur content in the matte (according to Mostovich's rule) is 25%.

The composition of the fluxes: quartz -100% SiO2, limestone -56% CaO.

The composition of the converter slag: Cu-1.5%, Fe-50%, SiO2-26%.

Copper extraction from converter slag - 85%.

Melting lead to one of the slags, the compositions of which are presented in table 1.

Table 1 - The composition of the slag

| № of the slag | The composition of the slag, % |  |  |
| --- | --- | --- | --- |
|  | SiO2 | FeО | СаО |
| 1 | 34,0 | 50,0 | 6,0 |
| 2 | 34,0 | 48,0 | 8,0 |
| 3 | 35,0 | 50,0 | 5,0 |
| 4 | 35,0 | 45,0 | 10,0 |
| 5 | 36,0 | 50,0 | 4,0 |
| 6 | 36,0 | 45,0 | 9,0 |
| 7 | 37,0 | 48,0 | 5,0 |
| 8 | 37,0 | 50,0 | 3,0 |
| 9 | 38,0 | 45,0 | 7,0 |
| 10 | 38,0 | 48,0 | 6,0 |

- Melting of the cinder without converter slag

Smelting lead to slag №5 (SiO2-36%, FeО-50%, СаО-4%):

a) Determination of the composition of the matte.

The amount of matte sulfur in view of the degree of desulfurization:

13,5 *0,77 – 25%

Х – 100%

Х=41,6г.

Copper content in matte

13 *0,95 –Х

41,6 – 100%

Х=30%.

Let us assume that 40% of zinc during melting of the calcine will turn into matte. Then the zinc content in the matte will be:

2,7 *0,4 –Х

41,6 – 100%

Х=2,6%.

Copper mattes always contain oxygen in the form of dissolved magnetite. Its content in the matte depends on the copper content and is determined according to the Avetisyan table (table 2).

Table 2- Oxygen content in copper mattes

| % Cu in the matte | 10 | 20 | 30 | 40 | 45 | 50 |
| --- | --- | --- | --- | --- | --- | --- |
| % О2 in the matte | 6,54 | 5,38 | 4,21 | 3,02 | 2,49 | 1,90 |

A matte containing 30% copper contains 4.21% oxygen. The content of other components in the matte is taken 2%. The iron content in the matte is determined by the difference:

%Fe = 100 - (Cu + S + O2 + other) = 100 – (30 + 25+ 2,6 + 4,21 + 2)= 36,19%

The composition of the matte is presented in the form of a table (table 3).

Table 3 - Composition and amount of matte

| Components | Content of components |  |
| --- | --- | --- |
|  | g | % |
| Cu | 12,5 | 30,0 |
| Fe | 15,05 | 36,19 |
| S | 10,4 | 25,0 |
| Zn | 1,07 | 2,6 |
| O2 | 1,75 | 4,21 |
| other | 0,83 | 2,0 |
| Total | 41,6 | 100 |

b) Determination of the preliminary composition of the slag (without the addition of fluxes)

Iron will go to slag:     44,5 – 15,05 = 29,45g

What is in terms of FeO will be:

29,45∙7256=37,9

The main slag components of SiO2 and CaO will be transferred from the calcine to slag completely. The amount of FeO + CaO in the slag in the calculation is assumed to be 90%. Then you can find a preliminary composition of the slag (table 4).

Table 4- Preliminary Slag Composition

| Components | Composition of the slag |  |
| --- | --- | --- |
|  | г | % |
| FeО | 37,9 | 75,45 |
| SiO2 | 6,0 | 11,95 |
| СаО | 1,3 | 2,6 |
| Total | 45,2 | 90,0 |

Calculation data show that the obtained slag does not meet the requirements for the composition of the slag, in addition, its composition differs sharply from the specified.

c) Calculation of the number of fluxes

To obtain slag of a given composition, it is necessary to add fluxes: quartz and limestone. Denote the required amount of quartz X, the required amount of limestone U. After adding fluxes, the amount of slag will be:

45,2 + Х + 0,56У

To determine X and Y we compose two balance equations by SiO2:

6 + Х = 0,36· (45,2+Х+0,56У),

On the СаО:   1,3 + 0,56У = 0,04(45,2+Х+0,56У).

As a result of solving these equations, we found	Х=16,75г, У=2,2g

The composition of the charge necessary to obtain slag of the desired composition:

Cinderella - 100g

Quartz -16.75g

Limestone 2.2g

Total - 118.95g

1. Melting of cinder with converter slag

Smelting lead to slag number 2.

a) Determination of the composition of the matte. This calculation remains the same.

b) Determination of the amount of matte taking into account the extraction of copper from the converter slag.

By blowing matte onto blister copper, converter slag is obtained, which is a reverse product. The amount of converter slag can be found from the considerations that when converting all the iron of the matte passes into the converter slag.

Then, when converting 41.6g of matte, the following amount of converter slag is obtained:

15,05г Fe  –  50%

X       – 100%

Х=30,1g.

We assume that due to the extraction of copper from the converter slag, the amount of matte will increase, and its composition will not change. This is equivalent to the formation of an additional amount of matte of the same composition.

Copper to matte from converter slag:

30,1·0,015·0,85 = 0,38g.

Total copper in matte:

12,5+0,38 = 12,88g.

Total matte:

12,88-30%

х-100%

х-43g.

The amount of iron in matte

43·0,3619 = 15,6g.

The composition of the matte is presented in table 5.

Table 5 - Composition and amount of matte

|  | Content | of components |
| --- | --- | --- |
| Components | g | % |
| Cu | 12.88 | 30.0 |
| Fe | 15.6 | 36.19 |
| S | 10.75 | 25.0 |
| Zn | 1.11 | 2.6 |
| O2 | 1.80 | 4,21 |
| Other | 1,86 | 2,0 |
| Total | 43,00 | 100,0 |

c) Determination of the preliminary composition of the slag in the smelting of the calcine with converter slag without the addition of fluxes.

The next amount of iron will go to slag.

44,5+15,05-15,6=43,95 g.

In terms of iron oxide:

43,95·72/56=56,5 g.

SiO2 and CaO go to slag completely:

The amount of  SiO2 6,0+30,1·0,26=13,83 g,

The amount of CaO 1,3 g,

The sum of FeO, SiO2, CaO in the slag can be taken equal to 90%. The results of the calculation of the composition of the slag are summarized in table 6.

Table 6 - Preliminary Slag Composition

|  | Content | of components |
| --- | --- | --- |
| Components | г | % |
| Fe | 56,5 | 78,9 |
| SiO2 | 13,83 | 19,3 |
| CaO | 1,3 | 1,8 |
| Total | 71,63 | 100 |

These tables show that the slag obtained during the smelting of the cinder with converter slag without the addition of fluxes, in its composition, does not meet the requirements imposed on the slags of reflective smelting. Ferrous slag will have a large specific gravity, and have a high ability to dissolve sulfides. Copper losses will be high.

d) Calculation of the number of fluxes

Slag No. 2 has the following composition: SiO2-34%, FeO-48.0%, CaO-8%. To obtain such a slag, fluxes are needed - quartz and limestone. Pure quartz (SiO2-100%) and pure limestone (CaO-56%) are used as fluxes.

Taking the amount of quartz x, and the amount of limestone y, we get the following amount of slag:

71,63 + х + 0,56у.

Making two equations

by SiO2 13,83+х = 0,34(71,63+х+0,56у),

by CaO 1,3+0,56у  = 0,08(71,63+х+0,56у),

find x and y

х=19,27 г, у=11,57 g.

The composition of the charge:

candlestick - 100.0

converter slag - 30.1

quartz - 19.3

limestone - 11.6

Total: 161.0 g

II. Smelting raw (unfired) concentrate

When smelting raw concentrate, only such indicators as the degree of desulfurization and copper extraction into matte, which are set by the teacher, change. The calculation is carried out similarly to the previous one.

Report content

The report on the work should contain:

- the theoretical essence of the process of reflective melting,

- characteristics of the charge and smelting products,

- sketch of the reflective furnace,

- calculation of the composition of the charge,

- method of work,

- results of laboratory work and a qualitative assessment of the smelting products obtained.

7. CONTROL QUESTIONS

1. Chemistry of reflective melting.

2. Characteristics of the charge and smelting products.

3. Difference between smelting of cinder and smelting of raw concentrate.

4. Temperature regime of reflective melting.

5. Disadvantages of reflective melting.

6. The design of the reflective furnace.

7. Technical and economic indicators of the process.

8. TASK: In the laboratory to reproduce one of the options for smelting copper concentrates.

Literature

Basic:

- Газалиев А.М. Общая металлургия: уч-к. /А.М.Газалиев, В.В.Егоров, Д.К. Исин. Под ред. Акад.НАН РК А.М. Газалиева. – Алматы: Бiлiм, 2010. – 777с

- Романтеев Ю.П., Быстров В.П. Металлургия тяжелых цветных металлов. Свинец. Цинк. Кадмий.: - М.: Изд. дом МИСиС, 2010 – 575 с.

- Уткин Н.И.  Производство цветных металлов. –М.: Интермет инжиниринг. 2004.

Additional literature:

- Воскобойников В.Г., Кудрин В.А., Якушев А.М. Общая металлургия. М.: Академкнига, 2002. 786 с.

- Романтеев Ю.П. и др. Металлургия цинка и кадмия. - М.: МиСиС. 2006.

- Шевко В.М. Общая металлургия. Учебное пособие. Шымкент ЮКГУим.М.Ауезова, 2013. -357с.

- Валиев Х.Х., Романтеев Ю.П. Металлургия свинца, цинка и сопутствующих металлов. Алматы: КазНТУ, 2000. 441 с.

- Коржова Р.В. Сырьевая база и обогащение руд. М.: МиСиС. 2002. -149с.

- ШевкоВ.М.. Теоретические основы металлургических процессов.  Конспекты лекций. – Шымкент: ЮКГУ им.М.Ауэзова, 2012.-158с.

- Шевко В.М., Каратаева Г.Е.,Даулетбаева Д.А. Металлургия свинца, цинка, вольфрама и молибдена / Учебное пособие. – Шымкент.: Южно-Казахстанский государственный университет им. М.Ауэзова, 2016. - 235 с.

BITANOVA GULVIRA AZOTULAEVNA

KARATAEVA GULNARA ERGESHOVNA

METHODICAL INSTRUCTIONS

for laboratory classes on the discipline

«Metallurgy of heavy non-ferrous metals»

for students of the specialty 5B070900 - «Metallurgy»

Publishing house SKSU named after M.Auezov

Signed in the press in 2019.

Format 60x84 1/16 Offset printing. Usl.p.p. – 4,0

Circulation 100 copies. Order No.

© Edition of the South Kazakhstan State University named after M.Auezov

Publishing Center SKSU named after M.Auezov, Shymkent ave Tauke Khan 5