Ф. 7.03-20

S. Iskakova, S. Sakibayeva, A. Issa, G.Mamytova

CHEMISTRY and PHYSICS of POLYMERS

STUDY GUIDE

Shymkent, 2019

Ministry of Education and Science of the Republic of Kazakhstan

M. Auezov South Kazakhstan State University

S. Iskakova, S. Sakibayeva, G.Mamytova, A. Issa

CHEMISTRY and PHYSICS of POLYMERS

STUDY GUIDE

for students of specialty

5B072100 – Chemical technology of organic substances

Shymkent 2019

UDK66(075.8)

BBK

ISBN

S. Iskakova, S.Sakibayeva, G. Mamytova, A.Issa. Chemistry and Physics of Polymers. Study guide. Shymkent: M. Auezov SKSU. 2019. – 176 p.

Study guide «Chemistry and Physics of Polymers: selective chapters» is developed according to the Curriculum and Standard study programme of discipline “Chemistry and Physics of Polymers” for students of specialty5B072100- Chemical technology of organic substances.Study guide includes basic concepts, nomenclature of polymers, characteristics of macromolecules, mechanism of polymerization and polycondensation, polymer structure,advanced methods for identification of polymers, special topics devotedto biodegradable and smart polymers.

This study guide can be useful to master students and PhD students of speciality “6M072100 – Chemical technology of organic substances" as well as teachers and researchers in the field of Chemistry and Chemical Engineering polymers.

Reviewers: Kedelbayev B., doctor of Engineering, professor of

the Department“Biotechnology”,M. Auezov SKSU

Yeskendirov M.Z., doctor of Engineering, professor of

the Department “Chemistry”, M. Auezov SKSU

Karabayev Dz., PhD, Leading Specialist, PetroKazakhstan

Study guide is recommended for print by Study methodical Board of

M. Auezov South-Kazakhstan State University.

Minutes #	______ 2019

ISBN                                                    © M. Auezov South Kazakhstan

State University

| Contents |  |  |
| --- | --- | --- |
| Preface |  | 7 |
| Introduction Why study Polymer Chemistry? | Peculiar position of the Polymer Chemistry | 8 |
|  | New generation polymers.Biodegradable materials | 12 |
| Chapter 1 Basic concepts | 1.Basic concepts 1.1Basic terms | 17 |
|  | 1.2 Nomenclature | 20 |
| Chapter 2 Classification of polymers | 2.Classification of polymers | 23 |
|  | 2.1 Classification by origin | 23 |
|  | - Classification based on structure | 24 |
|  | 2.3 Classification based on molecular forces | 25 |
|  | 2.4 Classification based on mode of polymerization | 31 |
|  | 2.5 Classification based on variety of monomers involved in the structure | 33 |
| Chapter 3 The main characteristics of macromolecule | 3. The main characteristics of macromolecule | 39 |
|  | Introduction | 39 |
|  | 3.1 Polymer structure | 39 |
|  | 3.2 Configuration of polymer chain | 40 |
|  | 3.3 Conformation of macromolecules | 42 |
|  | 3.4 MolecularWeight | 44 |
|  | 3.5 Molecular‐weight distribution | 45 |
|  | 3.6 Features of polymers macroscopic properties | 48 |
| Chapter 4 Polymerization | 4. Polymerization | 49 |
|  | Introduction | 49 |
|  | 4.1Radical Chain-Growth Polymerization | 50 |
|  | 4.2Cationic Chain-Growth Polymerization | 56 |
|  | 4.3Anionic Chain-Growth Polymerization | 59 |
|  | 4.4Olefin Polymerization with Ziegler-Natta Catalyst | 61 |
|  | 4.5 Polymerization techniques | 71 |
| Chapter 5 Copolymerization | 5. Copolymerization | 75 |
|  | Introduction | 75 |
|  | 5.1 Types of copolymers | 75 |
|  | 5.2 Block copolymers | 76 |
|  | 5.3 Block Copolymerization | 77 |
|  | 5.4 Summary | 77 |
| Chapter 6 Polycondensation | 6. Polycondensation | 79 |
|  | Introduction | 79 |
|  | 6.1Types of polycondensation stages | 80 |
|  | 6.2Characteristics of Condensation Polymers | 82 |
|  | 6.3 Summary | 87 |
| Chapter 7 Polymer Structure (Morphology) | 7.Polymer Structure (Morphology) | 88 |
|  | Introduction | 88 |
|  | 7.1The Primary structure of Polymers | 88 |
|  | 7.2The Secondary structure of Polymers | 90 |
|  | 7.3 The tertiary structure of Polymers | 92 |
|  | 7.4 The quaternary structure of Polymers | 96 |
|  | 7.5 Summary | 97 |
| Chapter 8 Advanced methods for identification | 8. Advanced methods for identification | 100 |
|  | Introduction | 100 |
|  | 8.1 Infrared (IR) spectroscopy | 101 |
|  | 8.2 Fourier Infrared spectroscopy | 103 |
|  | 8.3 Thermogravimetric Analysis | 104 |
|  | 8.4 Differential scanning calorimetry (DSC) | 104 |
|  | 8.5 Thermomechanical Analysis (TMA) | 105 |
|  | 8.6 Nuclear Magnetic Resonance (NMR) | 105 |
|  | 8.7 Chromatography | 106 |
|  | 8.8 Mass Spectrometry (MS) | 106 |
|  | 8.9 X-Ray Fluorescence | 106 |
|  | 9.0 Microscopy | 107 |
| Chapter 9 Biopolymers Polylactic acid (PLA) | 9. Biopolymers Polylactic acid (PLA) | 107 |
|  | 9.1. Polylactic acid (PLA) | 109 |
|  | 9.1.2. History of Polylactic acid (PLA) | 110 |
|  | 9.1.3. Manufacturing of Polylactic acid | 111 |
|  | 9.1.4. Use-end of Polylactic acid | 112 |
|  | 9.1.5. Environmental Impact and Recycling | 114 |
|  | 9.1.6. Summary of Polylactic acid | 116 |
| Chapter 10 Smart Polymers | 10. Smart Polymers | 119 |
|  | Introduction | 119 |
|  | 10.1Types of “Smart polymers” | 121 |
|  | 10.2 Polymer hydrogels | 121 |
|  | 10.3Shape memory polymers | 124 |
|  | 10.4 Self-healing or restoration | 125 |
|  | 10.5 Temperature-responsive polymers | 126 |
|  | 10.6 pH-sensitive polymers | 127 |
|  | 10.7 Photo-sensitive polymers | 129 |
| Chapter 11 Recycling Plastic and Disposal | 11. Recycling Plastic and Disposal | 133 |
|  | Introduction | 133 |
|  | ## History of Recycling | 134 |
|  | ## Plastic Identification Codes | 135 |
|  | Plastic Recycling Process | 138 |
| Reference |  | 142 |
| - Appendixes |  | - 144 |
| - Appendix 1 | Clossary of Polymers | - 144 |
| - Appendix 2 | History of Plastics | - 147 |
| - Appendix 3 | Nomenclature of Polymers (rational, random) | - 155 |
| - Appendix 4 | Concept map | - 159 |
| - Appendix 5 | Uses of Plastics | - 160 |
| - Appendix 6 | Bioplastic lifecycle | - 175 |

Preface

The chemistry of high-molecular compounds develops methods for the synthesis of new, more and more complex polymer compounds, studies the mechanisms and rates of formation of macromolecules. Without knowledge of the fundamentals of the chemistry of high-molecular compounds, it is impossible to regulate and control technological processes in all branches of industry producing and consuming polymers. The presentation of the foundations of this knowledge and is devoted to the Part I of the textbook.

Synthesis of polymers is one of the stages furthertechnological processes that polymer undergoes forturning into the right product. However, to from synthesizedpolymers go to certain products, the creation of which

is the ultimate goal of production, it is necessary to solve a numbercomplex technological challenges. Solving these problems requires knowledgefundamentals of physics and physical chemistry of polymers, knowledge of their physical and physicochemical properties in a wide range of different external influences.

The study of the characteristics and specific features of the behavior of high-molecular compounds is the main task of polymer physics. The assessment of the applicability of the laws of physical chemistry, physics and mechanics to polymers is of particular importance for the correct understanding and implementation in practice of the methods of their processing into products. In particular, the study of the properties of solutions and melts of polymers and the possibility of molding articles with specified properties from them is of great importance. The above is the content of Part II of the textbook.

Thus, chemistry and physics have a directrelation to the production of polymers and therefore bachelorneed to know the basics of this science.The polymer chemistry and methods of polymer processing are set forth in given study-guide. Each topic is broken down into small chunks of information that are more manageable and easily learned.

Study-guide involves 12 tables, 8 schemes, 62 figures and 1 diagram. Bibliography lists 26 names.

| Introduction |  |
| --- | --- |
|  | WHY STUDY POLYMER CHEMISTRY? |

In recent decades, high-molecular compounds (polymers) have become firmly established in our lives. Polymers are a special kind of materials that, depending on the structure of the molecules, have the most diverse properties and are used in the most diverse spheres of life and activity of mankind: in industry and agriculture, in science and technology, in all types of transport. Modern medicine, like our everyday life, is inconceivable without the use of a wide range of polymeric materials. Plastics have no counterpart in other materials in terms of weight, ease of fabrication, efficient utilization, and economics.

We are surrounded by synthetic polymers in our daily lives. This cyclist rides on synthetic rubber tires, drinks from propylene water bottle, wears a protective Lexan halmet and goggles, and uses a lightweight nylon backpack. Figure1 illustrates several consumer products and the polymers from which they are made.

Figure1 Polymers in some common consumer products (Smith, Janish G. Organic chemistry/ Janish G. Smith. -3nd ed.- 2011)

At present, polymers occupy the 4th place in terms of the volume of materials produced and mined. The most common and produced polymers — polyethylen, polypropylene, polystyrene, polyvinyl chloride, synthetic rubber and polyethylene terephthalate — are used as construction materials, of which they make electrical insulation, rubber products, food packaging, containers for storing food and non-food products, light housings for electronics and much more.The distribution of produced and mined materials by volume is shown in Figure 2, and the volume of production and the range of basic polymers produced are shown in Figure 3

Figure 2 Place of polymers among and mined materials

Figure 3 Volume and range of world polymer production

The industrial mass-production of synthetic polymers began in the 1950s after Karl Ziegler and Julio Nutt developed catalysts that allow the incorporation of low molecular weight molecules into polymers under relatively mild conditions. At the end of the 20th century and the beginning of the 21st century, new types of polymers began to be applied in fine organic synthesis. For example, they allow the creation of biosensors that do not interfere with their wearer in their usual activities, or robotics with flexible and elastic manipulators. Thanks to polymers, three-dimensional printing became possible, and not only from polymers, but also from other materials (see: A three-dimensional printing method with metals with a record resolution was developed, “Elements”, 03/29/2018; German chemists created a polymer for 3D printing of glass products, “Elements”, 04.24.2017).

Among the polymeric materials produced by industry, leading positions are occupied by:

a) plastics and organic glasses;

b) synthetic rubbers;

c) synthetic and artificial fibers;

d) films and numerous decorative protective coatings (paints, varnishes, enamels)

Figure 4 Illustrates application ofthe plasticsin different areas of industry.

| Packaging | Building and Construction | Electrical & Electronic | Sport & Leisure |
| --- | --- | --- | --- |
| Medical & Health | Transportation | Agriculture |  |

Figure 4 Application  of the polymer use-end

What properties distinguish polymers from ordinary low-molecular compounds (LMS) and allow them to be distinguished into a special type of material?

First of all, the long length and flexibility of macromolecules give polymers the property of elasticity, i.e. abilities to large (about several hundred percent) reversible deformations.

Secondly, solid polymer bodies - plastics combine high elastic moduli, comparable in size to the elastic moduli of ordinary solids (inorganic glass, metals, and ceramics), with high tensile elongations (4 times larger, than ordinary solids). Therefore, polymer bodies are less prone to brittle fracture.

Thirdly, due to the high anisotropy of the shape of the macromolecules of polymers, they are easily oriented in a mechanical field and form fibers with high strength in the direction of orientation.

The polymers differ from low molecular weight compounds and the fact that when dissolved they first pass through the swelling stage; the viscosity of diluted (up to 1%) polymer solutions far exceeds the viscosity of solutions of low molecular weight compounds of the same concentration.

Concentrated solutions and melts of polymers, like all liquids, have elastic properties. The high molecular weights of polymers significantly broaden the spectrum of their relaxation times as compared with low molecular weight liquids. The combination of large molecular masses with high intermolecular interactions causes a number of anomalous viscous-elastic properties of polymeric liquids, which are not characteristic of low-molecular compounds. In most cases, chemical reactions of polymers differ from the corresponding reactions of low-molecular analogs. These distinctive properties of polymers allowed them to become one of the most widely used materials.

Biological polymers (biopolymers) also belong to high-molecular compounds, which possess a number of unique properties not characteristic of low-molecular compounds.

Let us name some of the most important properties of biopolymers and their functions:

- nucleic acids are able to encode, store and transmit genetic information at the molecular level, being the material substrate of heredity; for instance, DNA, which is contained in the chromosomes of the nucleus of a cell, stores all genetic information in an organism. DNA consists of two long strands of polynucleotides held together byhydrogen bonding (Figure 5)

- another class of biopolymers - muscle proteins, are able to convert chemical energy into mechanical work; this their concusive function underlies the muscle activity of proteins

- enzymes, globular proteins, have a catalytic function, they carry out all chemical reactions of metabolism, the decomposition of one and the synthesis of other substances with high speed and selectivity in nature.

Figure 5 The double helix of DNA

At the present time the structure of Amino acids, Proteins, Nucleic acides, Hormones, Vitamins and their role in the construction is the most well studied aspect.

Prospects for the development of polymer production. In recent years, the geography of the production of large-tonnage products — the main producer of synthetic plastic materials and rubbers from the developed countries of North America and Western Europe — has shifted closer to raw materials - to the regions of the Middle East and the Asia-Pacific Region. At the same time, consumer demand in developing countries is growing at faster.

- New generation polymers

The beginning of the XXI century is characterized by the revolutionary beginning of the development of nanotechnology and nanomaterials that are used in many areas of human activity: industry, defense, information sphere, radio electronics, energy, transport, biotechnology, medicine, engineering. A new class materials, in which the scale level of the size of individual components reaches the nanometer range, called "nano-composites” has widespread become(https://infuture.ru/category/news).

In the scientific publication Nanocomposite science and technology, nanocomposites are defined as multicomponent solid material, in which one of the components in one, two or three dimensions has dimensions not exceeding 100 nanometers; Also, nanocomposites are structures consisting of a plurality of repeated component layers (phases), the distance between which is measured in tens of nanometers. Although nanocomposites can be found in natural objects, for example, in the bones of living organisms, we are more interested in how artificial nano-composite materials are produced and used. The use of nanocomposites began in the middle of the last century, when they were not yet fully aware of their physical and chemical essence. The first nanocomposite materials were rheological organoclays obtained for the needs of industry and cosmetics.

Nanocomposites based on a ceramic matrix improve the optical and electrical properties of the original material (ceramic compound consisting of a mixture of oxides, nitrides, silicides, etc.).

In nanocomposites based on a metal matrix, carbon nanotubes, which increase strength and electrical conductivity, often serve as the so-called reinforcing material (nanocomponent).

Finally, polymer nanocomposites contain a polymer matrix with nanoparticles or nanofillers distributed over it, which may have a spherical, flat or fibrous structure.

It is polymer nanocomposites that have been especially in demand recently, because many different variants of nanofillers that enhance and modify the properties of polymers have been proposed. Polypropylene, polystyrene, polyamide or nylon is used as a matrix in this form of nanocomposites, and the particles of aluminum or titanium oxides, or carbon, as well as silicon nanotubes and fibers act as nanocomposites.

Polymer-based nanocomposites differ from conventional polymer composites with lower weight and greater impact resistance and wear resistance, as well as good resistance to chemical attack, which allows them to be used in military and aerospace developments. The main condition for creating a polymer nanocomposite with the required properties is full compatibility of the base material and the nanoparticles added to it, however, it is equally important for the final result to correctly distribute the nanoparticles on the polymer. Therefore, the production of nanocomposites is a high-tech industry and requires serious research in the field of nanotechnology.

The use of nanocomposite materials. Currently, most polymeric nanocomposites are made on the basis of modified montmorillonite (in other words, nanoclay, it has very pronounced sorption properties). The most popular and studied are polymeric nanocomposites based on polyamide, polypropylene, polyethylene, polystyrene, polyethylene terephthalate.

The greatest demand for composites is demonstrated by the packaging industry — 36%; significant electrical market and automotive industries occupy significant market shares.

A special place in the development of nanocomposite materials is graphene. Recently, it was found that the addition of graphene to epoxy composites leads to an increase in the stiffness and strength of the material as compared to composites containing carbon nanotubes. Graphene combines better with epoxy polymer, penetrating into the composite structure more efficiently. Graphene-based nanocom-pozites can be used in the production of aircraft components, which should remain both light and resistant to physical effects.

Scientists also hope that nanocomposites will help speed up the restoration of the structure of damaged bones, if along them establish hinges made from a polymer nanocomposite containing nanotubes that direct the growth and regeneration of bone tissue.

Nanocomposites containing particles of zirconium oxide and having excellent catalytic properties. In the automotive industry, various elements of the interior, electronic equipment, security systems, tires, and car engine modules can be made from nanocomposite materials.

- Biodegradable materials.

In recent years, due to rising oil prices and intensive environmental pollution, traditional synthetic polymers based on plastics have been replaced by so-called compostable plastics (biodegradable plastics), which allow polymeric materials to decompose under natural conditions under the influence of external and intracellular enzymes of microorganisms to practically harmless compounds without damage to the environment.

Bio-based polymers are closer to the reality of replacing conventional polymers than ever before. Nowadays, bio-based polymers are commonly found in many applications from commodity to hi-tech applications due to advancement in biotechnologies and public awareness. However, despite these advancements, there are still some drawbacks which prevent the wider commercialization of bio-based polymers in many applications. This is mainly due to performance and price when compared with their conventional counterparts, which remains a significant challenge for bio-based polymers.

Reproductive natural polymers, components of agricultural or wild plants

(starch-small, cellulose, and lignin), petrochemical products, or combined technologies can serve as a raw material base for the production of modern biopolymers.

The world's first biodegradable starch-based plastic was obtained in 1989 by the Italian industrial corporation Ferruzi Finanziaria. Currently, numerous companies in the United States, Japan, and European countries are developing new types of plastics by successively injecting starch into polymer chains. For example, as a result of the copolymerization of ethylene and vinyl acetate, ethylene vinyl acetate (EVA) is formed into which starch is introduced as a biodegradable component. The polymer obtained decomposes well under the action of enzymes of microorganisms, without contaminating the soil. The most famous synthetic product based on starch filler is Mater - Bi material from Nowamont S. p.A (Italy). The uniqueness of this synthetic product lies in its ability to absorb and transmit liquids, which makes it possible to use it in the production of "breathable films."

Polystyrene composition with natural biopolymers (starch or cellulose), used for the production of food packaging and agricultural film, has become widespread.

Polylactide is considered a promising bioplastics - biodegradable, biocompatible, thermoplastic, aliphatic polyether, a condensation product of lactic acid and renewable raw materials of biological origin. On the basis of polylactide are received porous materials, food packaging, disposable dishes, packages, various containers, as well as medical surgical threads and pins. The main producer of polylactides is the company RURAC (Netherlands).

The most promising materials of the 21st century, according to a number of scientists, are polyhydroxyalkanoates (PHA) (a copolymer of hydroxybutyrate and hydroxyvalerate), which in their physicochemical properties are similar to polyethylene and polypropylene, but are capable of biodegradation. The uniqueness of these biopolymers lies in the fact that they are made with the help of hydrogen-oxidizing microorganisms - hydrogen bacteria. Like synthetic polymers based on polypropylene and polyethylene, they are durable and thermoplastic, but unlike the above-mentioned polymers they have antioxidant properties, optical activity, piezoelectric effect, and most importantly, they are environmentally friendly polymeric materials that are decomposed in natural conditions to final products of water and carbon dioxide.

The number of innovations in the field of production of a new generation of polymer materials is growing every year. Thus, the Greensack film, made from corn grain, was recently created, thanks to which, having the same opportunity as all vegetable products, it completely decomposes in the soil.

The Italian company Convex Plastics on a similar technology has developed the material "New Greensack", obtained from corn starch. Greensack film also finds use as a wrapper for magazines, food packaging, in the fast food industry, milk packaging.

An increasing practical application for the production of environmentally friendly plastics is found in dairy acid-based polymers - polylactate, the raw material for production of which can be corn, sugarcane, potatoes. Polylactate-based products, compared to, for example, polypropylene, have a number of important chemical properties: high rigidity, transparency and gloss, as well as a great ability to retain shape after compression or torsion.

Consider the advantages and disadvantages of biopolymers. An obvious advantage of biopolymers, distinguishing them from other plastics, is their low toxicity and ability to decompose under natural conditions under the action of enzymes of microorganisms, which allows simultaneously solving the problem of waste disposal. No less important advantages due to the physicochemical properties of biopolymers are: low barrier to the transmission of oxygen and water vapor, as well as resistance to decomposition under normal conditions.

Among the disadvantages of biodegradable polymers are the following: limited opportunities for large-scale production and their high cost. Thus, polymers of a new generation (compostable plastics) undoubtedly “win” on a number of ecological properties over completely synthetic polymers, the components of which are highly toxic synthetic compounds.

Currently in Kazakhstan, the petrochemical industry is in its infancy.

In the industry, within the framework of the industrialization program, 3 projects worth a total of $ 1 billion were implemented. In particular, the bitumen plant with a design capacity of 400 thousand tons per year., A complex for the production of aromatic hydrocarbons at the Atyrau refinery, at the Pavlodar Petrochemical Plant, polypropylene production has been doubled. There are polyethylene and polypropylene production plants. A plant will be built in the South Kazakhstan region for the production of powdered polypropylene and ethyl tert-butyl and methyl tert-butyl ethers used as additives for the production of high-octane gasoline.

| Chapter 1 |  |
| --- | --- |
|  | Basic concepts |

### 1.1Basic terms

### 1.2 Nomenclature

### Basic terms

Features of the properties of polymers associated with their chain structure. It is the chain structure of polymer molecules that is their most important property, which allows them to be given the following definition:

Polymers are a special class of chemical compounds whose specific properties are determined by a large length, chain structure and flexibility of the macromolecules constituting them

### n M → [ -M- ]n

The word polymer is derived from the Greek words

poly + meros meaning “many parts.”

In turn, a macromolecule is a set of atoms or atomic groups of different or identical in composition and structure, connected by chemical bonds into a linear or branched structure of sufficiently high molecular weight;

or "Thepolymerchainmoleculeiscalledamacromolecule."

Macromoleculeisa molecule of high relative molecular mass, the structure of which essentially comprises the multiple repetition of a number of constitutional units (IUPAC nomenclature)

Polymers are called high molecular weight compounds (HMWC), the molecular weight of which is above 5000 and can reach millions.

Molecular weight of low molecular weight substances (LMW) is usually less than 500.

Between LMW and polymers are substances of average molecular weight, which relate to resins, oligomers. They can be transformed to HMWCusing polymerization or polycondensation reactions.

(fromhttp://chem21.info/info/667531/.

### According to IUPAC nomenclature, a polymer is a substance consisting of molecules characterized by multiple repetition of one or more types of atoms or groups of atoms (constitutional units) connected in an amount sufficient to manifest a complex of properties, which is almost unchanged when adding or removal of one or several constitutional units.

High-molecular weight compounds (HMWC) are substances consisting of molecules of large size, large molecular weight (from several thousand to several millions)

Monomeris a substance, each of the molecules of which can, on polymerization, contribute one or more constitutional units in the structure of the macromolecule. (IUPAC nomenclature)

Oligomeris a substance composed of oligomer molecules

(IUPAC nomenclature)

Oligomer moleculeis a molecule of intermediate relative molecular mass, the structure of which essentially comprises a small plurality of constitutional units. (IUPAC nomenclature)

Сonstitutional unitis an atom or group of atoms in a macromolecule or oligomer molecule, comprising a part of the chain together with its pendant atoms or groups of atoms, if any. (IUPAC nomenclature)

### Constitutional repeating unit “n” is the smallest molecular unit whose repetition describes a regular polymer (IUPAC nomenclature)

| ### Example: polystyrene molecule |  |  |
| --- | --- | --- |
| ### in parentheses a constitutional repeating unit is highlighted, and an ellipse is constitutional units. |  |  |
| ### In many cases, the constitutional repeating unit coincides with the monomeric unit. |  |  |
| ### Constitutional repeating unit ### of polyethylene ### ── CH2 ─ |  | ### Monomeric unit ### ── CH2 ────── CH2 ── |

Monomeric unit / mer is the largest constitutional unit contributed by a single monomer molecule to the structure of a macromolecule or oligomer molecule (IUPAC nomenclature)

Degree of polymerization, “ n” is the number of monomeric units in a macromolecule or oligomer molecule (IUPAC nomenclature)

Oligomerizationisthe process of converting a monomer or a mixture of monomers into an oligomer (IUPAC nomenclature)

Polymerizationisthe process of converting a monomer or a mixture of monomers into a polymer (IUPAC nomenclature)

### Questions for self work on.

### 1.What is the place of polymers in terms of production in modern industry?

### 2. What are the main properties of polymers that define them as a special kind of materials?

### 3. Give the definition of the following concepts: polymer, high molecular weight compound, macromolecule, constitutional unit, constitutional repeating unit.

### 4. Write an equation that determines the relationship of molecular weight and degree of polymerization.

### 5. The concept of the HMWC, oligomer and polymer

- Nomenclature of polymers

### Currently, there are 3 main types of polymers nomenclature:

- Nomenclature, based on the chemical structure of the polymer chain

### (IUPAC nomenclature)

- Nomenclature, based on the name of monomers (rational nomenclature), see Appendix 2;

- Random nomenclature, see Appendix 2

### IUPAC nomenclature, based on the chemical structure of the

### polymer chain

### According to this nomenclature it is convenient to call organic polymers consisting of one kind of Constitutional Repeating Unit (CRU) and having a linear chain.

### Formation of the name includes prefix "poly" + (name of the CRU on IUPAC nomenclature). CRU is the Constitutional Repeating Unit.

### It is necessary to identify the CRU, that is, select a fragment from the structure by repeating which it is possible to obtain the structure of the macromolecule; besides should take into account the location and orientation of this link in the chain. In Table1.1 names of polymers according to IUPAC nomenclature is given.

### Table 1.1 Names of basic polymers

| ### Structure ### of polymer chain | ### Name by IUPAC | ### Name ### by Rational Nomenclature |
| --- | --- | --- |
|  | ### Poly (methylene) | ### Polyethylene (PE) |
|  | ### Poly (1-methylethylene) | ### Polypropylene (PP) |
|  | ### Poly (1-dimethylethylene) | ### Polyisobutylene (PIB) |
|  | ### Poly (1-phenylethylene) | ### Polystyrene (PS) |
|  | ### Poly (1-chloroethylene) | ### Polyvinylchloride (PVC) |
|  | ### Poly (1-cyanoethylene) | ### Polyacrylonitryl (PAN) |
|  | ### Poly(1-acetoxyethylene) | ### Polyvinylacetate (PVA) |
|  | ### Poly (1,1-difluoroethylene) | ### Polyvinylidenefluoride (PVdF) |

### TEXT

### Table 1.2.Trademarks of polypropylene

| ### Trademark | ### Manufacturer |
| --- | --- |
| ### PP ПП | ### Tomsk Petrochemical Plant |
| ### Каплен | ### Moscow Petrochemical Plant ### Kuskovsky chemical plant |
| ### Нурален | ### Plastics (Moscow) |
| ### Филен | ### Plant of composite materials and plastics (Tomsk) |
| ### Томполен | ### Polymer compound (Tomsk) |
| ### Achieve | ### ExxonMobil |
| ### Vistamaxx | ### ExxonMobil |
| ### Novolen® | ### BASF |
| ### Marlex | ### Chevron Phillips |

| Chapter 2 |  |
| --- | --- |
|  | Classification of polymers |

There are several ways in which polymers can be characterized (Figure 2.1):

a) Classification by origin

b) Classification based on structure

c) Classification based on molecular forces

- Classification based on mode of polymerization

- Classification based on variety of monomers involved in the structure

Figure 2.1 Classification of Polymers

- Classification of Polymers based on origin

| There can be three types of origin of polymers: |  |
| --- | --- |
| Natural polymers These are obtained from nature, e.g., plant origin, animal origin etc. | - For example, Natural Rubber, Cellulose, Proteins, Sugars, Nucleic acids. |
| Biologically degradable polymers are also present, called biopolymers | ### For example, Polylactic acid (PLA) |
| Synthetic polymers | - For example, PP, PVC , |
| Semi-synthetic polymers | - For example, Rayon, Terylene |

b) Classification of Polymers based on structure

| Linear Polymers– Monomers join with each other to form long straight chains. | - Example – Poly Vinyl Chloride or PVC is a linear polymer |  |
| --- | --- | --- |
| Branched Chain Polymers– These polymers are made of branching of linear chains of monomers. They have low melting points and low densities. | - Example- Low Density Polypropylene (LDPE) |  |
| Cross-linked Polymers/Network Polymers – These polymers are formed by bi-functional and tri-functional monomers with a strong covalent bond between the various linear polymer chains. These polymers are brittle by nature. |  | - Example – Melamine Структурная формула меламин-формальдегидной смолы (упрощенная) |

c) Classification of Polymers based on molecular forces

These include:

| Thermoplastics | Thermosets (thermosetting resins) |
| --- | --- |
| Elastomers | Fibres |

Consider in detail.

| Thermomplastics consist of individual molecules with no covalent bonding between them but held together by intermolecular bonding. The polymers become soft on warming and can be molded. They can be repeatedly warmed, softened and remolded. | - Softens when exposed to heat and yelds to original state at room temperature - Do not undergo significant chemical change - Weak bond, which becomes even weaker on reheating - Thermomplastics can easily be shaped and modelled into products such as floor covering, credit cards, carpet fibres,etc. |
| --- | --- |
| A thermoplastic(sometimes written as thermo plastic) is a type of plastic made from polymer resins that becomes a homogenized liquid when heated and hard when cooled. When frozen, however, a thermoplastic becomes glass-like and subject to fracture. These characteristics, which lend the material its name, are reversible. That is, it can be reheated, reshaped, and frozen repeatedly. This quality also makes thermoplastics recyclable. There are dozens of kinds of thermoplastics, with each type varying in crystalline organization and density. Some types that are commonly produced today are polyurethane, polypropylene, polycarbonate, and acrylic. Celluloid, which is considered the first thermoplastic, made its appearance in the mid-1800s and reigned in the industry for approximately 100 years. During its peak production, it was used as a substitute for ivory. Today, it is used to make guitar picks. |  |
| Thermosetting polymers are complex networks of cross-linked polymers. Thermosetting polymers are formed by chemical reactions that occur when monomers are heated together to form a network of covalent bonds. Thermosetting polymers cannot be re-melted to form a liquid phase, because covalent bonds hold the network together. |  |
| Sometimes, thermoplastics are confused with thermosetting plastics. Although they may sound the same, they actually possess very different properties. While thermoplastics can be melted to a liquid and cooled to a solid, thermosetting plastics chemically deteriorate when subjected to heat. Ironically, however, thermosetting plastics tend to be more durable when allowed to cool than many termoplastics. |  |

| Thermosets, on the other hand, have many covalent bonds between the chains, leading to a three-dimensional structure, which can be regarded as a single molecule. They can be molded by heat and pressure, but once moulded they cannot be remolded. The most important examples include the plastics made from methanal (formaldehyde). The list of examples is given in Table 2 |  | - Solidifies or sets irrevocably when heated - The molecules of these plastics are cross linked in three dimensions and this is why they cannot be redesigned or recycled - They are useful for their durability and strength - Used predominantly in automobiles and construction applications. Other uses include adhesives, inks, and coating |
| --- | --- | --- |
| Thermosetting plastic, also known as a thermoset, is polymer material that irreversibly cures. The cure may be done through heat (generally above 200 °C (392 °F)), through a chemical reaction (two-part epoxy, for example), or irradiation such as electron beam processing. Thermoset materials are usually liquid or malleable prior to curing and designed to be molded into their final form, or used as adhesives. Others are solids like that of the molding compound used in semiconductors and integrated circuits (IC). Once hardened a thermoset resin cannot be reheated and melted back to a liquid form. According to IUPAC recommendation:A thermosetting polymer is a prepolymer in a soft solid or viscous state that changes irreversibly into an infusible, insoluble polymer network by curing. Curing can be induced by the action of heat or suitable radiation, or both. A cured thermosetting polymer is called a thermoset. |  |  |
| Elastomersare amorphous solids which, as the name suggests, are elastic. They have coiled chains which can be stretched out but spring back to their original shape when the stretching force is released. The list of examples is given in Table 2.1 | Characteristics of Elastomers are: - Elasticity - Resilience - Low permeability to air, gases, water and steam - Good electrical and thermal insulation - Good mechanical properties. Mechanicals - The ability to adhere to various fibers, metals and rigid plastics |  |

| Table 2.1 Some elastomers Polymer; Formula. Poly(buta-1.3-diene). Polyurethanes. ABS (Acrilonitrile -Butadiene - Styrene). Silicones. |
| --- |
| Fibres are thin threads which are produced by extruding a molten polymer through a die in which there are small holes.Fibres produced in this way include the polyamides (such as Nylon), the polyesters (such as Terylene) and Poly(propene). After stretching to make a fiber, the crystallite regions are aligned along the axis of the fiber, and this adds strength to it (see left – “result of stretching”) | “result of stretching” |
| Polyester Fiber Characteristics - Strong - Resistant to stretching and shrinking - Resistant to most chemicals - Quick drying - Crisp and resilient when wet or dry - Wrinkle resistant - Mildew resistant - Abrasion resistant - Retains heat-set and crease - Easily washed | - Polyamide Fiber Characteristics - Good combination of strength, toughness and hardness - High durability - Low dimensional stability heat resistant continuously up to +80-100°C and short-term at temperatures up to 150°C - Good chemical resistance - Large water absorption compared to other polyamide |
| Fibres are twisted into threads and can then be woven into cloth or imbedded in a plastic to give it much greater strength (Table 2.2). Table 2.2 Some polymers used to make fibers Polymer; Formula. Polyamide 6. Polyamide 6,6. Polyester (Terylene) formed from the dimethyl ester of 1,4-benzenedicarboxylic acid and ethane-1,2-diol. Poly(propenonitrile). Poly(ethene). Poly(propene). Poly(chloroethene). Poly(tetrafluoroethene) (PTFE). |

d) Classification of Polymers based on mode of polymerization

Synthetic polymers can be classified aschain-growth (addition polymers)or step-growth polymers (condensation polymers).

| Chain-growth polymers, also called addition polymers, are prepared by chain reactions | These compounds are formed by adding monomers to the growing end of a polymer chain. The conversion of vinyl chloride to poly(vinyl chloride) is an example of chain growth polymerization. |
| --- | --- |
| Polymerization is the joining of monomers to make polymers. |  |
| An example of a free radical polymerization in the industry is producing high-density polyethylene, polyvinylchloride, and Teflon. |  |
| Chain-growth polymerization is a chain reaction that converts an organic starting material, usually an alkene, to a polymer via a reactive intermediate—a radical, cation, or anion. |  |

Inaddition polymerization, the polymer has the same empirical formula as the monomer but a higher molecular mass (Table 2.3)

Table 2.3 Some addition polymers

| Monomer | Formula | Polymer | Trivial name | Structure |
| --- | --- | --- | --- | --- |
| Ethene |  | LDPE Low density poly(ethene) | Low density polythene |  |
| Chloro-ethene |  | Poly (chloro ethene) | Polyvinyl chlorine, PVC |  |
| Propene |  | Poly(propene) | Polypropylene |  |
| Propeno-nitrile |  | Poly(propenonitrile) | Polyacrylo-nitrile |  |
| Methyl- 2-methylpropenoate |  | Poly(methyl-2-methylpropenoate) | Polymethyl methacrylate |  |
| Phenyl-ethene |  | Poly(phenyl- ethene) | Polystyrene |  |
| Tetrafluoro- ethene |  | Poly(tetrafluoroethene) (PTFE) | Polytetrafluo-roethylenePTFE |  |

| Step-growth polymers, also called condensation polymers, are formed when monomers containing two functional groups come together and lose a small molecule such as H2O or HCl. | In this method, any two reactive molecules can combine, so the monomer is not necessarily added to the end of a growing chain. Step-growth polymerization is used to prepare polyamides and polyesters. |
| --- | --- |
| By convention, we often simplify the structure of a polymer by placing brackets around the repeating unit that forms the chain, as shown in Figure 2.2. |  |

Figure 2.2 Scheme of PET formation

Incondensation polymerization, polymerization of one or more monomers is accompanied by the elimination of small molecules (such as water or ammonia) (Table 2.4).

Table 2.4 Some condensation polymers

| Polymer | Monomer | Formula |
| --- | --- | --- |
| Polyesters |  |  |
| Polyamides |  |  |
| Phenol-methanal plastics |  |  |
| Polyurethanes |  |  |

- Classification of Polymers based on the type of monomer involved in the structure

They include:

| Homopolymer when the same monomer is repeated throughout the chain of the polymer |  |
| --- | --- |

Figure 2.3 Formation of Polyvinyl chloride (PVC)

Figure 2.4 Formation of High-density polyethylene (HDPE)

https://www.slideshare.net/Lahiru_Dilshan/polymers-106892603 Heteropolymers, or as they are more commonly known, Co-polymers.

There are several types of Co-polymer. One type is produced when two or more monomers are mixed and polymerized together. Depending on the reactivities of the monomers, they may form polymers with different arrangements of the monomer units.

| Co-polymers Alternating | ……..possess two regularly alternating monomer residues. |
| --- | --- |

Figure 2.5 Formation of Alternating co-polymer

Co-polymers are very useful as they have the properties of the constituent polymers and thus can be produced for specific purposes. For example, poly(phenylethene) (polystyrene) is brittle but when it is co-polymerized with buta-1,3-diene, the latter gives the polymer resilience and strength. Known as High Impact Polystyrene (HIPS), it can now receive impacts without damage.

Figure 2.6 High Impact Polystyrene (HIPS)

| Co-polymers Periodic | - ……. are those in which monomer residue types are arranged in a repeating sequence: [AnBm…] mbeing different from n |
| --- | --- |
| Co-polymers Block | Block copolymers are long sequences of different units of monomer |
| Co-polymers Graft; - ……the composition of the main chain is a preformed macromolecule and is compositionally or configurationally different from the side chains or branches with repeat units.. Figure 2.7 Formation of Graft co-polymer An example of Graft co-polymer is ABS. “A” is Acrylonitrile, the trivial name for propenonitrile; “B”is Butadiene; “S” is Styrene. The backbone of the polymer is formed from phenylethene (styrene) and buta-1,3-diene. Propenonitrile (acrylonitrile) is added to the system and then formed a grafted side chain onto the backbone. The nitrile is added to the double bond on the butadiene unit: |

| Statistical copolymersfollow a statistical rule in monomer arrangement |  |
| --- | --- |
|  | Chain-growth copolymer of vinyl chloride and vinyl acetateis a statistical copolymer |

| A truerandom copolymer | is a statistical copolymer, in which the probability of finding a particular type of monomer residue at a particular point in the chain and the types of surrounding monomer residue are independent of each other. |
| --- | --- |

Figure 2.8 Formation of Random co-polymer

| Figure 2.9 Formation of Random co-polymer Fibres are twisted into threads and can then be woven into cloth or imbedded in a plastic to give it much greater strength (Table 2.5). Table 2.5 Some polymers used to make fibers Polymer; Formula. Polyamide 6. Polyamide 6,6. Polyester (Terylene). Poly(propenonitrile). Poly(ethene). Poly(propene). Poly(chloroethene). Poly(tetrafluoroethene) (PTFE).. Chapter 3. characteristics of macromolecules. Introduction Polymers consist of repeat units (monomers) chemically bonded into long chains. In essence there are only two really fundamental characteristics of polymers: their chemical structure and their molar mass distribution pattern. The chemical structure (CS) of a polymer comprises: - The nature of the repeating units - The nature of the end groups - The composition of possible branches and cross links - The nature of defects in the structural sequence The molecular weight distribution (MWD) or molar mass distribution (MMD) informs about the average molecular size and describes how regular (or irregular) the molecular size is. The MMD may vary greatly, depending on the method of synthesis of thepolymer. These two fundamental characteristics, CS and MMD, determine all the properties ofthe polymer. In a direct way they determine the cohesive forces, the packing density (andpotential crystallinity) and the molecular mobility (with phase transitions). In a moreindirect way they control the morphology and the relaxation phenomena, i.e. the totalbehaviour of the polymer. - Polymer structure The polymer molecule consists of a “skeleton” (which may be a linear or branched chain or a network structure) and peripheral atoms or atom groups. Polymers of a finite size contain so-called end groups, which do not form part of the repeating structure proper. Their effect on the chemical properties cannot be neglected, but their influence on the physical properties is usually small at degrees of polymerisation as used in practice. Sometimes use is made of these end groups to increase molecular weight (telechelic polymers). Structural groups; Every polymer structure can be considered as a summation of structural groups. Monovalent; Bivalent; Trivalent; Tetravalent. In the geometrical arrangements of the atoms in a polymer chain two categories can be discerned: a. Arrangements fixed by the chemical bonding, knownas configurations; The configuration of a chain cannot be altered unless chemical bonds are broken or reformed. Examples of configurations are cis- and trans-isomers or D- and L-forms.. b. Arrangements arising from rotation about single bonds, known as conformations.. a. Configurations of polymer chains; The possible regular structure of poly-a-olefins was recognised by Natta et al. (1955), who devised a nomenclature now accepted to describe stereoregular polymers of this type. The configuration is formed in the process of synthesis and can not be broken otherwise like breaking chemical bonds.. Local isomerism (position isomerism).; It occurs because of the possibility of monomers attaching to the growing polymer chain in synthesis process in various ways:. 1 - head-tail connection (h-t) 2 - head-to-head connection (h-h) or tail-tail (t-t). The most common configuration is head-tail, due to selectivity in monomer addition reactions, for example, due to possible steric hindrance in the case ofclose location of the side groups. Isomerism resulting from the multiple opening of a multiple bond:. It is characteristic of a group of polymers having two conjugated double bonds.. Tacticity of polymers; It is the steric arrangement in macromolecules. Polymers can be isotactic, where all the chiral centers have the same configuration. ( R= phenyl, all the phenyl groups as oriented above the plane). The orderliness can also be of the type where every other chiral center has the same configuration. Such an arrangement is called syndiotactic (R = phenyl). A lack of orderliness or randomness in the steric arrangement is called atactic or heterotactic.. Stereospecific polymers can also be prepared from 1,2 disubstitued olefins. These macromolecules can be distereoisomers, or ditactic polymers. To describe the arrangement of such polymers, a threo–erythro terminology is used.. Erythrodiisotactic polymer (If we draw the carbon chain backbone in the plane of the paper, then all the R groups would find themselves on one side of the chain and all the R1 groups on the other.). All be on the same side of the chain in a Fischer or in a Newman projection.. Threodiisotactic polymer. The configuration determines the chemical structure of macromolecules.. b.Conformation of macromolecules; The conformation is the form that macromolecules acquire this configuration composition under the action of thermal motion or physical fields.. Trans zig - zag conformation (Represents an extended chain). It is possible to rotate around the bonds along the forming cone with the vertex angle 109˚28΄; motion limited, since it is difficult to turn the whole tail due to thermal movement.. When this happens partial transitions of trans conformations into convolved (gauche conformations), and an elongated chain twists and goes into the “statistical coil” conformation.. Conformation "coil" (chaotic chain); Conformation " globule " A particle densely filled with atoms forming in it macromolecule.; Conformat" spiral " (an elongated spiral). The polymer content in the coil is low (about 5%),; The polymer content is much higher than in the coil:; It is common for biopolymers and many polymers in a crystalline state.. Summary. Arrangements arising from rotation about single bonds, known as conformations. In dilute solutions the molecules are in continuous motion and assume different conformations in rapid succession (random coils). In the solid state many polymers have typical conformations, such as folded chains and helical structures. In polypeptides helical structures containing two or three chains (double and triple helices, respectively) are found. There have been a lot of quarrels in the early years of the twentieth century about the reality of what now are called polymers. It is the great merit of Staudinger (1920) to have proposed, contrary to the prevailing ideas, that rubber and other biological substances, such as starch, cellulose and proteins, are long chains of short repeating units linked by covalent bonds. He also coins the name “macromolecule”. Since then it became clear that polymer molecules are “normal” molecules and that only their chainlike nature is “different” and imposes restrictions, but also provides new properties. Conformation determines the shape of macromolecules Understanding the physical properties of a polymer (such as mechanical strength, solubility and brittleness) requires knowledge of the length of the polymer chains. Chain length is often expressed in terms of the molecular weight of the polymer chain, related to the relative molecular mass of the monomers and the number of monomers connected in the chain. However, all synthetic polymers are polydisperse in that they contain polymer chains of unequal length, and so the molecular weight is not a single value - the polymer exists as a distribution of chain lengths and molecular weights. The molecular weight of a polymer must therefore be described as some average molecular weight calculated from the molecular weights of all the chains in the sample (as MM). But the polymolecularity (polydispersity) is characterized by the molecular weight distribution (MWD) Degree of Polymerization and MolecularWeight First of all, let us discuss the degree of polymerization. The degree of polymerization (DP)-n in a polymer molecule is defined as the number of repeating units in the polymer chain. For example, −(−CH𝟐 − CH𝟐−)−n The molecular weight of a polymer molecule is the product of the degree of polymerization and the molecular weight of the repeating unit. The polymer molecules are not identical but are a mixture of many species with different degrees of polymerization, that is, with different molecular weights. Therefore, in the case of polymers we talk about the average values of molecular weights. - Molecular weight (1880) (formula weight, molecular mass). The sum of the atomic weights of all atoms in a molecule. In most non‐polymeric compounds the molecular weight is a known constant value. In high polymers, the individual molecules range widely in the number of atoms they contain, and therefore, in molecular weight. Hence an average must be used to characterize a particular sample of polymer.. The two averages most commonly used are. number‐average molecular weight (Mn) The number average molecular weight is the statistical average molecular weight of all the polymer chains in the sample, and is defined by: where Mi is the molecular weight of a chain and Ni is the number of chains of that molecular weight. Mn can be predicted by polymerization mechanisms and is measured by methods that determine the number of molecules in a sample of a given weight; for example, colligative methods such as end-group assay. If Mn is quoted for a molecular weight distribution, there are equal numbers of molecules on either side of Mn in the distribution; and weight‐average molecular weight (Mw). The weight average molecular weight is defined by: Compared to Mn, Mw takes into account the molecular weight of a chain in determining contributions to the molecular weight average. The more massive the chain, the more the chain contributes to Mw. Mw is determined by methods that are sensitive to the molecular size rather than just their number, such as light scattering techniques. If Mw is quoted for a molecular weight distribution, there is an equal weight of molecules on either side of Mw in the distribution.. Methods for determining these averages include measurements of light scattering and osmotic pressure in solutions, sedimentation in an ultracentrifuge, and depression of freezing points and vapor pressures of solutions, dilute‐solution viscosity, end‐group titration, and spectroscopy. The processing behaviour and many end-use properties of polymers are influenced not only by the average molar mass but also by the width and the shape of the MMD or MWD. The basic reason is that some properties, including tensile and impact strength, are specifically governed by the short molecules; for other properties, like solution viscosity and low shear melt flow, the influence of the middle class of the chains is predominant; yet other properties, such as melt elasticity, are highly dependent on the amount of the longest chains present. MM allows you to determine the length, size of macromolecules. - Molecular‐weight distribution. One of the chemical properties of a molecule is its molecular weight which is unique for every molecule. However, in synthetic polymer this is a bit of problem because of the nature of polymerisation reaction which produces different lengths of polymeric chains. This means synthetic polymers are polydisperse, no unique molecular weight, unlike small molecules. Therefore, the molecular weight of polymers is measured using molecular weight distribution (MWD). Figure 3.1 Figure 3.1 In MWD curve, there are three moments of molecular weight distribution which are mean-average, weight average and z-average molar mass. Mean-average molar mass, Mn, can be defined as the value obtained by weighting each molar mass by the number of molecules of that mass present in the sample. From the definition, Mn can be calculated using equation below where Niis the number of molecules with mass Mi and there are N molecules in all. Experimentally, Mn can be measured using several methods. The first method is using end-group analysis where in this technique the concentration of end-group in known concentration of polymer. This means end-group analysis depends on the functional group at the end of polymeric chain which implies the need of polymers modification. From this technique, Mn can be calculated as where Ni is the number of molecules with mass Mi and there are N molecules in all. The other methods use the fact that the polymer chains are in solution system which means the measurement is based on the colligative properties of polymer solution. The moments of MWD, especially Mn and Mw, are commonly used for the molecular weight analysis. The value of Mn is biased towards low molecular weight while Mw is biased toward high molecular weight. Those values are also used to measured how polydisperse the polymer is and this value is quoted as heterogeneity index of polydispersity index (PDI). Therefore, by definition if PDI is 1.000 this means an ideal monodisperse polymer where all the polymeric chain has the same length. If PDI is less than 1.20 it can be called near monodisperse and this value is common for living anionic polymerisation. Common value of PDI of polymerisation is around 2.00. One of the methods to plot the whole MWD curve of polymer can be done by gel permeation chromatography (GPC) which is a quick, convenient and widely used method. Figure 3.2 Figure 3.2 In this method, the molecular weight is plotted as function of elution time. The low MW polymer tends to get lost in microporous beads, so the high MWpolymer would pass the column first. This implies that the MW is inversely proportional to the elution time which means a calibration is required and this requires near-monodisperse standard. The percentages by number (or weight) of molecules of various molecular weights that comprise a given specimen of a polymer. Two samples of a given polymer having the same number‐average molecular weight Molecular‐weight distribution may perform quite differently in processing because one has a broader distribution of molecular weights than the other. Two basic groups of methods are used for measuring molecular‐weight distribution. Fractionation methods, which actually divide the specimen into portions having relatively narrow ranges of molecular weight, include: fraction precipitation and fraction solution (the two most widely used), chromatography, liquid‐liquid partition, ultra‐centrifugation, zone refining, and thermo gravimetric diffusion. After fractionation by any of these methods, the weight percent of each fraction is plotted versus the average molecular weight for that fraction to obtain a histogram of the distribution, which may be smoothed into a curve. Non‐fractionation methods include light‐scattering studies, electron microscopy, dilute‐solution viscosity, size‐exclusion chromatography, ultra‐centrifugation, and diffusion. A popular measure of the breadth of a distribution is the ratio of weight‐ average to number‐averagemolecularweight, Mw/Mn. - Features of polymers macroscopic properties The selection of polymers into a separate group of substances is due to the presence of they have a number of special properties that are a con-sequence of the large here are their macromolecules. The most important of them are: 1. The absence of gaseous aggregation state for polymers. 2. The delayed kinetics and blurriness of phase transitions (melting, crystallization). For low molecular weight species, LMWS the tempera-ture is the transition is a constant. Polymers are melted in certain nomi-nal temperature range. 3. Polymers have a highly elastic state (i.e. polymers have both solid and liquid properties). This featureis manifested in the ability of polymers to significantly reversible de-formations. The presence of high elasticity is associated with high flexi-bility and large sized macromolecules. 4. The presence of polymers specific oriented state (the possibility of orientation allows to obtain film compounds and fibrous materials). 5. Specific properties of polymer solutions. Unlike the LMWS polymer solutions have a high viscosity. The viscosity of a 1% polymer solution may exceed the viscosity of the solvent from 20 to100 times. The feature of dissolution of high-molecular weight compound is stage of swelling - the polymer absorbs volumes of solvent, embroidering his own several times. Well-known methods for the separation and purification of chemical compounds such as distillation and recrystallization are not applicable to high-molecular weight compound, as the latter decompose during distillation even in the deepest vacuum and are capable of producing of edged crystal only in special t realized difficulty conditions |
| --- |
| Chapter 4 |  |  |
|  | Polymerization |  |

| A polymer is a large organic molecule composed of repeating units—called monomers—that are covalently bonded together. The word polymer is derived from the Greek words poly + meros meaning “many parts.” | Examples of naturally-occurring polymers are silk, cotton, wood, cotton, starch, natural rubber, skin, hair and DNA. In the early 1900s, chemists began to replicate natural polymers, and create synthetic polymers, beginning with nylon which mimics silk in its strength and flexibility. |
| --- | --- |

Polymerization is chemical process in which an unsaturated hydrocarbon molecules are attached to one another due to the rupture of π-bonds and the formation of new σ- bonds.

Molecules reactive polymerizable called monomers. Macromolecular compounds formed by polymerization, called polymers. The polymer of the same monomers, called a homopolymer. The polymer derived from different monomers, called heteropolymer or copolymer.

The number of molecules connected to each other determines the degree of

polymerization. Oligomerization results in a low molecular weight polymer - oligomers dimers (n = 2), trimer (n = 3), etc. Chain polymerization is accompanied by the formation of high-molecular compounds with n more than 1000.

Most polymerization reactions of alkenes having industrial value occur by a chain mechanism and depending on the nature of the reagent; the initiation process can be free radical, cationic, anionic and ionic-coordination.

- Radical Chain-Growth Polymerization

Free radical initiation can occur through application of heat (thermal), (ultraviolet and visible) light (photochemical), (ionizing) light, redox reagents, electricity (electrochemical), etc., that is any process that creates the essential free radicals. While application of heat can rupture the pi bond in the vinyl monomer causing the formation of a two-headed free radical that can act as a free radical initiator, peroxides and dinitriles are generally employed. This is a consequence of the general bond dissociation energy trend of C ─ H˃C ─ C˃C ─ N˃O ─ O. Dinitrile or azo compounds such as 2,2′-azo-bis-isobutyronitrile (AIBN) require temperatures of about 70–800C to produce decomposition with free radical formation (see below). Peroxides such as benzoyl peroxide (BPO) require temperatures in the range of 60–1400C for decomposition and free radical formation (see below). While the dissociation bond energy for C-N is generally greater than for O-O, the formation of a stable N2 molecule is the thermodynamic driving forcedue to an entropy effect allowing dissociation to occur at typically lower temperatures.Light in the ultraviolet and visible range can disrupt selected bonds forming freeradicals.

The monomers  such as ethylene, methyl methacrylate ,vinyl acetate, styrene, tetrafluoroethylene are subject to radical polymerization. Since this can be initiated by traces of oxygen or other minor impurities, pure samples of these compounds are often "stabilized" by small amounts of radical inhibitors to avoid unwanted reaction. When radical polymerization is desired, it must be started by using a radical initiator, such as a peroxide or certain azo compounds. The formulas of some common initiators, and equations showing the formation of radical species from these initiators are presented below (Figure 4.1 a,b)

)

Figure 4.1a

# By using small amounts of initiators, a wide variety of monomers can be polymerized. One example of this radical polymerization is the conversion of styrene to polystyrene, shown in the following diagram. The first two equations illustrate the initiation process, and the last two equations are examples of chain propagation. Each monomer unit adds to the growing chain in a manner that generates the most stable radical. Since carbon radicals are stabilized by substituents of many kinds, the preference for head-to-tail regioselectivity in most addition polymerizations is understandable. Because radicals are tolerant of many functional groups and solvents (including water), radical polymerizations are widely used in the chemical industry.

Figure 4.1b

# In principle, once started a radical polymerization might be expected to continue unchecked, producing a few extremely long chain polymers. In practice, larger numbers of moderately sized chains are formed, indicating that chain-terminating reactions must be taking place. The most common termination processes are Radical Combination and Disproportionation. These reactions are illustrated by the following equations. The growing polymer chains are colored blue and red, and the hydrogen atom transferred in disproportionation is colored green. Note that in both types of termination two reactive radical sites are removed by simultaneous conversion to stable product(s). Since the concentration of radical species in a polymerization reaction is small relative to other reactants (e.g. monomers, solvents and terminated chains), the rate at which these radical-radical termination reactions occurs is very small, and most growing chains achieve moderate length before termination (Figure 4.2)

# .

# Figure 4.2

The relative importance of these terminations varies with the nature of the monomer undergoing polymerization. For acrylonitrile and styrene combination is the major process. However, methyl methacrylate and vinyl acetate are terminated chiefly by disproportionation.

Another reaction that diverts radical chain-growth polymerizations from producing linear macromolecules is called chain transfer (Figure 4.3). As the name implies, this reaction moves a carbon radical from one location to another by an intermolecular or intramolecular hydrogen atom transfer (colored green). These possibilities are demonstrated by the following equations

# Figure 4.3

# Chain transfer reactions are especially prevalent in the high pressure radical polymerization of ethylene, which is the method used to make LDPE (low density polyethylene). The 1º-radical at the end of a growing chain is converted to a more stable 2º-radical by hydrogen atom transfer. Further polymerization at the new radical site generates a side chain radical, and this may in turn lead to creation of other side chains by chain transfer reactions. As a result, the morphology of LDPE is an amorphous network of highly branched macromolecules.

# Summary

1. Peroxides, such as benzoyl peroxide, and diazo compounds, such as azobisisobutyronitrile, are readily homolytically cleaved by heat or ultraviolet light to produce free radicals, which serve as initiators for chain reaction polymerization. Each initiator has its characteristic half-life. Their decomposition into free radicals may be accelerated by heat or by reducing agents. 2. The rate of initiation of free radical chain polymerization, which is the ratecontrolling step, is proportional to the product of the concentrations of the free radical (R⋅) and the monomer.

3. The rate of propagation is proportional to the concentrations of the monomer and the macroradicals. The additional stability of the macroradical with the functional group or the terminal carbon favors the head-to-tail configuration.

4. Termination of propagating macroradicals may take place by coupling or disproportionation. The rate of termination is proportional to the square of the concentration of macroradicals.

5. The degree of polymerization (DP) is inversely proportional to the square root of the concentration of initiator and decreases as temperature increases.

6. Since growing chains continue to propagate until a high molecular weight product is formed the concentration of monomer decreases steadily and approaches zero at the end of the reaction. At all times prior to the end of the polymerization, the composition of the system consists of monomer and high molecular weight polymers.

7. Polymerization will not take place above the characteristic ceiling temperature.

8. Chain transfer, in which the macroradical abstracts a weakly bonded atom, causes branching when chain transfer with polymer occurs. Chain transfer with solvent or some other additive results in a dead polymer and a new free radical. If the latter does not serve as an initiator for further propagation, it is called a retarder or inhibitor.

9. Vinyl monomers may be polymerized without other additives except free radicals in bulk polymerization. When the monomer is polymerized while suspended in a stirred aqueous medium, the process is called suspension, or pearl, polymerization. Polymerization may also take place in good or poor solvents. In the former case, the viscosity continues to increase, and in the latter, the macroradicals precipitate.

10. When the system is viscous, the termination step is hindered but propagation continues. Thus, this so-called Trommsdorff or gel effect produces high molecular weight polymers.

11. Monomers may also be polymerized by a water-soluble initiator while dispersed, by agitation, in a concentrated soap solution. In this emulsion polymerization process, initiation takes place in the aqueous phase and propagation takes place in the soap micelles. Since the growing macroradicals are not terminated until a new free radical enters the micelle, high molecular weight products are obtained in a relatively short time.

12. The rate of polymerization and the degree of polymerization in the emulsion process are proportional to the number of activated micelles.

13. The polyfluorocarbons are resistant to heat, solvents, and corrosives. The resistance is greatest in the regularly structured polytetrafluoroethylene and decreases as the geometry is upset by substitution of larger or smaller groups for the fluorine atoms.

14. Low-density polyethylene, poly(vinyl chloride), polystyrene, and neoprene are made in large quantities by free radical chain polymerization.

- Cationic Chain-Growth Polymerization

Readily undergo radical polymerization alkenes having the double bond with an aryl, an ester, a nitrile group or a halogen atom, as these groups are capable of stabilizing intermediately formed radicals.

Homologues of ethylene, particularly propylene and isobutylene are polymerised by a radical mechanism with difficulty. For them, the most typical are cationic and 	ionic-coordinate polymerization.

Cationic polymerization goes by a mechanism comprising intermediate formation of carbocations, usually in the presence of acid (Н2SO4, H3PO4, HF, BF3, AlCl3, etc.). By this mechanism polymerize alkenes, which are formed from relatively stable carbocations: isobutylene, styrene, vinyl ethers ( Scheme 4.1)

)

Scheme 4.1 Cationic polymerization

Note! The process is the principle of joining the “head to tail”!

Cationic polymerization is rarely used for industrial polymers, but is used for the dimerization and trimerization related alkenes.

In particular, an example of oligomerization is the dimerization of isobutylene, which goes in presence of Н2SO4 at 60% (the reaction firstly studied by Butlerov A.M.):

Mechanism of dimerization of alkenes presented below (Scheme 4.2)

Stage 1 - the accession of a proton to an alkene to form a carbocation:

Stage 2 - reacting the carbocation with an alkene:

Stage 3 - the stabilization of the carbocation with elimination of a proton:

Scheme 4.2 Mechanism of dimerization of alkenes

Catalytic hydrogenation of the resulting mixture gives 2,2,4-trimethylpentane (isooctane), used as a standard for determining octane number of gasoline.

A drawback of ionic and radical polymerization is the formation of non-stereospecific polymer (atactic) polymer, i.e. polymers, which don’t have a certain orientation in space of the side groups attached to the main chain.

Such polymers have low performance (strength, storage stability).

Polymerization of isobutylene (2-methylpropene) by traces of strong acids is an example of cationic polymerization. The polyisobutylene product is a soft rubbery solid, Tg = - 70º C, which is used for inner tubes. This process is similar to radical polymerization, as demonstrated by the following equations. Chain growth ceases when the terminal carbocation combines with a nucleophile or loses a proton, giving a terminal alkene (as shown here) (Figure 4.4)

.

Figure 4.4

# Monomers bearing cation stabilizing groups, such as alkyl, phenyl or vinyl can be polymerized by cationic processes. These are normally initiated at low temperature in methylene chloride solution. Strong acids, such as HClO4 , or Lewis acids containing traces of water (as shown above) serve as initiating reagents. At low temperatures, chain transfer reactions are rare in such polymerizations, so the resulting polymers are cleanly linear (unbranched).

- Anionic and ionic-coordinate polymerization

- Anionic Chain-Growth Polymerization

Anionic vinyl polymerization is a method of making polymers from small molecules containing carbon-carbon double bonds. It is a type of vinyl polymerization. In anionic polymerization, the process is begun by an initiator. In this case, the initiator is an anion; that is, an ion with a negative electrical charge. There are a lot of different initiators used in anionic vinyl polymerization, but the most often used is an unassuming little molecule called butyl lithium

Now a little bit of the butyl lithium will always fall apart. It falls apart to form a positive lithium cation and a negative butyl anion. We call an anion like this where the negative charge is on a carbon atom a carbanion.

A pair of electrons from the butyl anion will be donated to one of the double bond carbon atoms of the monomer. Now this carbon atom already has eight electrons in its outer shell which it shares with the atoms to which it is bonded, so one pair of these electrons, specifically a pair in the carbon-carbon double bond, will leave the carbon atom, and settle on the other carbon atom of the carbon-carbon double bond. This forms a new carbanion, with the negative charge resting on that carbon. The process in which the butyl lithium falls apart, and the butyl anion reacts with a monomer molecule is called initiation.

The carbanion now reacts with another monomer molecule in just the same manner as the initiator reacted with the first monomer molecule; another carbanion is generated. This keeps happening, and each time another monomer is added to the growing chain, a new anion is generated allowing another monomer to be added. In this way the polymer chain grows. This adding of monomer after monomer is called propagation.

Summary.Treatment of a cold Tetrahydrofurane (THF) solution of styrene with 0.001 equivalents of n-butyllithium causes an immediate polymerization. This is an example of anionic polymerization, the course of which is described by the following equations. Chain growth may be terminated by water or carbon dioxide, and chain transfer seldom occurs. Only monomers having anion stabilizing substituents, such as phenyl, cyano or carbonyl are good substrates for this polymerization technique. Many of the resulting polymers are largely isotactic in configuration, and have high degrees of crystallinity. (Figure 4.5)

Figure 4.5

# Species that have been used to initiate anionic polymerization include alkali metals, alkali amides, alkyl lithiums and various electron sources. A practical application of anionic polymerization occurs in the use of superglue. This material is methyl 2-cyanoacrylate, CH2=C(CN)CO2CH3. When exposed to water, amines or other nucleophiles, a rapid polymerization of this monomer takes place.

- Olefin Polymerization with Ziegler-Natta Catalyst

# (https://chem.libretexts.org)

Extremely important practical application has ion coordination polymerization, which also takes place under the influence of metal-organic compounds, usually of the Ziegler-Natta catalyst and is used in particular for producing HDPE and polypropylene.

Scheme 4.3

Here M - a fragment of a Ziegler-Natta catalyst

In the early 1950s, Karl Ziegler in the GDR and John. Natta in Italy independently studied this type of polymerization. For

| The Nobel Prize in Chemistry 1963 was awarded jointly to Karl Ziegler and Giulio Natta "for their discoveries in the field of the chemistry and technology of high polymers" |  |
| --- | --- |
| Karl Ziegler was testing possible new catalysts that could drive reactions to create neater chains, when he accidentally discovered that compounds containing aluminium and carbon in the presence of trace amounts of a transition metal element could achieve the task. Acting upon his fortuitous observation, Ziegler systematically tested a range of related compounds, until he arrived at a combination that could link together the small chemical monomer ethylene to form polyethylene chains that were longer and had fewer branches, and crucially could achieve this under less intense temperatures and pressures than the methods used at the time. | Giulio Natta looked at ways of developing this catalyst to stitch other monomers together. For instance, linking the monomer propene also created unwanted chemical attachments pointing in different directions, which made it difficult for these polymer chains to fit neatly on top of each other. Natta solved this problem by designing a variation of the catalyst in which the space through which a growing polymer chain progresses is shaped in such a way that it can only accept attachments aligned (выравненный) in a particular direction. |
| Thanks to Ziegler and Natta's breakthroughs, the plastics business saw one of its most significant periods of innovation. Many new plastics were created, from the man-made fibers in clothes to the plastic bottles that we drink from, and for the first time chemists could create the type of complex polymers present in nature, most notably synthetic versions of rubber. |  |

An important advantage of ionic-coordinate polymerization is the stereospecificity; in its course formed stereospecific (isotactic) polymers. The polymers obtained in these conditions are of high quality. Low pressure polyethylene has a higher density and melting point as compared with the high-pressure polyethylene. In the case of propylene we mean the formation of polymer in which all methyl groups are arranged on one side of the polymer main chain.

The Ziegler-Natta (ZN) catalyst, named after two chemists: Karl Ziegler and Giulio Natta, is a powerful tool to polymerize α-olefins with high linearity and stereoselectivity (Figure 4.6)

A typical ZN catalyst system usually contains two parts: a transition metal (Group IV metals, like Ti, Zr, Hf) compound and an organoaluminum compound (co-catalyst). The common examples of ZN catalyst systems include TiCl4+ Et3Al and TiCl3+ AlEt2Cl.

Figure 4.6 The generic reaction equation for polymerization of α-olefins.

In 1953, German chemist Karl Ziegler discovered a catalytic system able to polymerize ethylene into linear, high molecular weight polyethylene which conventional polymerization techniques could not make.( Ziegler, K.; Holzkamp, E.; Breil, H.; Martin, H., Polymerisation Von Athylen Und Anderen Olefinen. Angew Chem Int Edit 1955, 67 (16), 426-426.1)

The system contained a transition metal halide with a main group element alkyl compound (Figure 4.7)

Figure 4.7 Linear polyethylene obtained by Ziegler’s catalytic system (20-70 ).

Following the catalytic design, Italian chemist Giulio Natta found that polymerization of α-olefins resulted in stereoregular structures, (2) either syndiotactic or isotactic, depending on the catalyst used (Figure 3). Because of these important discoveries, Karl Ziegler and Giulio Natta shared the Nobel Prize in Chemistry in 1963. (Figure 4.8).

Figure 4.8 The ZN catalytic polymerization of linear polypropene with two different stereoregular structures.

Atactic polypropylene is polymer having the substituents randomly oriented along the carbon backbone of an elongated polymer chain.

Syndiotactic polypropylene is polymer having the substituents alternating from one side of the backbone of an elongated polymer chain to the other.

Isotactic polypropylene is polymer having all the substituents on the same side of the carbon backbone of an elongated polymer chain.

Advantages over traditional polymerization method

Traditionally, polymerization of α-olefins was done by radical polymerization (Figure 4). Problem with this technique was that the formation of undesired allylic radicals leaded to branched polymers.For example, radical polymerization of propene gived branched polymers with large molecular weight distribution. Also, radical polymerization had no control over stereochemistry. Linear unbranched polyethylene and stereoregulated polypropylene could not be fabricated by free radical polymerization. This technique largely limited the potential applications of these polymeric materials. (Figure 4.9).

low molecular weight oils

Figure 4.9 The radical polymerization of propylene using traditional method.

The invention of ZN catalyst successfully addressed these two problems. The catalyst can give linear α-olefin polymers with high and controllable molecular weights. Moreover, it makes the fabrication of polymers with specific tacticity possible. By controlling the stereochemistry of products, either syndiotactic or isotactic polymers can be achieved.

- Mechanism of Ziegler-Natta catalytic polymerization

Activation of Ziegler-Natta catalyst

It is necessary to understand the catalyst’s structure before understanding how this catalyst system works. Herein, TiCl4+AlEt3 catalyst system is taken as an example.

The titanium chloride compound has a crystal structure in which each Ti atom is coordinated to 6 chlorine atoms. On the crystal surface, a Ti atom is surrounded by 5 chlorine atoms with one empty orbital to be filled. When Et3Al comes in, it donates an ethyl group to Ti atom and the Al atom is coordinated to one of the chlorine atoms. Meanwhile, one chlorine atom from titanium is kicked out during this process. Thus, the catalyst system still has an empty orbital (Figure 4.10)

The catalyst is activated by the coordination of AlEt3 to Ti atom.

Figure 4.10 The activation of ZN catalyst system by coordination of AlEt3 to Ti atom.

Initiation step

The polymerization reaction is initiated by forming alkene-metal complex. When a vinyl monomer like propylene comes to the active metal center, it can be coordinated to Ti atom by overlapping their orbitals. As shown in Figure 6, there is an empty dxy orbital and a filled dx2-y2 orbital in Ti’s outermost shell (the other four orbitals are not shown here). The carbon-carbon double bond of alkene has a pi bond, which consists of a filled pi-bonding orbital and an empty pi-antibonding orbital. So, the alkene's pi-bonding orbital and the Ti's dxy orbital come together and share a pair of electrons. Once they're together, that Ti’s dx2-y2 orbital comes mighty close to the pi-antibonding orbital, sharing another pair of electrons. (Fig. 4.10)

Figure 4.10 Molecular orbitals representation of monomer coordinating to metal center.

The formed alkene-metal complex (1) then goes through electron shuffling, with several pairs of electrons shifting their positions: The pair of electrons from the carbon-carbon pi-bond shifts to form Ti-carbon bond, while the pair of electrons from the bond between Ti and AlEt3’ ethyl group shifts to form a bond between the ethyl group and the methyl-substituted carbon of propylene (Figure 4.11). After electron shuffling, Ti is back with an empty orbital again, needing electrons to fill it (2)

Figure 4.11 The formation process of alkene-metal complex.

Propagation step

When other propylene molecules come in, this process starts over and over, giving linear polypropylene (Figure 4.12).

Figure 4.12 Propagation towards polymeric chains.

Termination step

Termination is the final step of a chain-growth polymerization, forming “dead” polymers (desired products). (Figure 4.13) illustrates several termination approaches developed with the aid of co-catalyst AlEt3.4

Figure 4.13 Three termination approaches: (a) β-elimination from the polymer chain, forming metal hydride; (b) β-elimination with hydrogen transfer to monomer; (c)hydrogenation.

Regio- and stero-selectivity

Regio-selectivity

For propene polymerization, most ZN catalysts are highly regioselective, favoring 1,2-primary insertion [M-R + CH2=CH (Me) = M-CH2-CH (Me) (R)] (Figure 4.14), due to electronic and steric effects.7

Figure 4.14 Primary insertion occurs in ZN-catalytic system to give regioselective products.

Stereo-selectivity

Stereochemistry of polymers made from ZN-catalyst can be well regulated by rational design of ligands. By using different ligand system, either syndiotactic or isotactic polymers can be obtained (Figure 4.15).

The relative stereochemistry of adjacent chiral centers within a macromolecule is defined as tacticity. Three kinds of stereochemistry are possible: isotactic, syndiotactic and atactic. In isotactic polymers, substituents are located on the same side of the polymer backbone, while substituents on syodiotactic polymers have alternative positions. In atactic polymers, substituents are placed randomly along the chain.

Figure 4.15 Tacticity of macromolecules

Choice of ZN catalyst regulates the stereochemistry. We use propylene polymerization as an example here. Recall the mechanism section, a monomer approaches the metal center and forms a four-membered ring intermediate. The binding of a monomer to the reactive metal-carbon bond should occur in from the least hindered site.As shown in (Figure 4.16), the trans-complex in which methyl on the growing chain is trans to the methyl group on the incoming monomer, should be energetically favored than the cis-complex, as the trans-complex experience less steric effect.

Figure 4.16 The active state a (trans) is more stable than b (cis) due to less steric effects of methyl groups.

Following the trans- complex, the methyl group on the newly added monomer is trans to that on the previous monomer. The step repeats so that a syndiotactic polypropylene is obtained (Figure 4.17a). However, if the metal center is coordinated with bulky ligands (e.g. –iBu, -Et2 groups), as denoted by Y in (Figure 4.17b), the incoming monomer will adopt a cis-conformation to avoid serious steric effect with the bulky ligand. Thus, at the presence of bulky ligand, the propylene monomer is cis to the growing chain. This results in a isotactic product.

Figure 4.17 a. Trans-intermediate avoids 1,3-strain of methyl groups, producing syndiotactic polypropylene; b. at the presence of bulky ligand Y, a cis-intermediate is adopted, generating isotactic polypropylene.

Applications

ZN catalysts can catalyze α-olefins to produce various commercial polymers, like polyethylene, polypropylene and Polybutene-1.

Substrate scope and limitations

ZN catalysts are effective for polymerization of α-Olefins (ethylene, propylene) and some dienes (butadiene, isoprene). However, they don’t work for some other monomers, such as 1.2 disubstituted double bonds. Vinyl chloride cannot be polymerized by ZN catalyst either, because free radical vinyl polymerization is initiated during the reaction. Another situation that ZN catalysts don’t work is when the substrate is acrylate. The reason is that ZN catalysts often initiate anionic vinyl polymerization in those monomers.11

Summary. Ziegler-Natta polymerization is a method of vinyl polymerization.. It's important because it allows one to make polymers of specific tacticity. Ziegler-Natta catalysis is especially useful, because it can make polymers that can't be made any other way, such as linear unbranched polyethylene and isotactic polypropylene. Free radical vinyl polymerization can only give branched polyethylene, and propylene won't polymerize at all by free radical polymerization. So this is a pretty important polymerization reaction, this Ziegler-Natta stuff.

A key step in the process that determines the stereospecificity of ionic-coordinate polymerization is the introduction of coordinatively connected polymer to σ – bond Ti-C (Scheme 4.4)

Scheme 4.4 Ionic-coordinate polymerization

- Polymerization techniques

Methods of synthesizing polymers include the following types:

The first type is Emulsion polymerization:

Scheme 4.5 Emulsion polymerization

Emulsion polymerization is a widely used technique industrially to synthesize the following materials: - synthetic rubber latexes - butadiene-styrene, acrylonitrile-butadiene, polybutadiene, polychloroprene and polyisoprene; - coating latex - polyacrylates, polyvinyl acetate, polyvinyl chloride and polyethylene copolymers; - plastisol resins (a resin mixed with a plasticizer to make a paste) polyvinyl chloride; - specialty latexes - polyethylene and polytetrafluroethylene. Emulsion polymerization has a number of technical advantages. The use of water as the dispersion medium is environmentally friendly (compared to using volatile organic solvents) and also allows excellent heat dissipation during the course of the polymerization. Similarly, the low viscosity of the emulsion allows access to high weight fractions of polymer not readily accessible in solution or bulk polymerization reactions.

The second type is Solution polymerization:

Scheme 4.6 Solution polymerization

Solution polymerization is a method of industrial polymerization. In this procedure, a monomer is dissolved in a non-reactive solvent that contains a catalyst.High-density polyethylene (HDPE), Low-density polyethylene (LDPE), Polypropylene, Polystyrene, cis-1,4-isoprene and cis-1,4-butadiene Rubbers, ethylene-propylene and butyl Rubbers, styrene- butadiene thermoplastic and Rubbers with statistic distribution of unit monomers are produced by this method. The advantages of solution polymerization are better heat control, comparatively little heat liberation, light movement of products withing polymerization system, and easiness of dozation. All these factors allow using continuous process line with automatic regulation of its parameters. Industrial solution polymerization processes are commonly used to produce polymers with special characteristics. Addition polymerizations are usually carried out bulk and solution polymerizations.

The third type is Bulk polymerization:

| - Monomer - Polymerization Starter Scheme 4.7 Bulk polymerization |  |  |
| --- | --- | --- |
| The bulk addition polymerization is the simplest of all polymerization processes. The polymerization of a liquid monomer in the absence of solvents or diluents is called bulk polymerization.The bulk addition polymerization is a homogeneous system with an organic initiator. If the polymer is insoluble in monomer, then initiation, propagation, and termination might happen in the monomer phase. If the polymer is soluble in the monomer, then the concentration of monomer decreases continuously and the viscosity changes. Producing of the pure polymeris an advantage of one. For example, Poly (ethylene terephthalate) films, Low-density polyethylene ( LDPE), Sodium Butadiene Rubber are obtained by bulk polymerization. Addition polymerizations are usually carried out bulk and solution polymerizations. |  |  |
| Chapter5 |  |  |
|  |  | Copolymerization |

Copolymerization is a process wherein unlike molecules join together in random sequences or alternating sequences

While the mechanism of copolymerization is similar to that discussed for the polymerization of one reactant (homopolymerization), the reactivities of monomers may differ when more than one is present in the feed, i.e., reaction mixture. Copolymers may be produced by step reaction or by chain reaction polymerization. It is important to note that if the reactant species are M1 and M2, the composition of the copolymer is not a mixture or blend [M1]n + [M2]n.

Most naturally occurring polymers are largely homopolymers, but both proteins and nucleic acids are copolymers. While many synthetic polymers are homopolymers, the most widely used synthetic rubber (SBR) is a copolymer of styrene (S) and butadiene (B). A widely used plastic (ABS) is a copolymer or blend of polymers of acrylonitrile, butadiene, and styrene. A special fiber called Spandex is a block copolymer of a stiff polyurethane and a flexible polyester.

The following examples refer to a two component system, in which one monomer is designatedAand the otherB.

| Statistical Copolymers. | Also called random copolymers. Here the monomeric units are distributed randomly, and sometimes unevenly, in the polymer chain: ~ABBAAABAABBBABAABA~ |
| --- | --- |
| Alternating Copolymers. | Here the monomeric units are distributed in a regular alternating fashion, with nearly equimolar amounts of each in the chain: ~ABABABABABABABAB~.. |
| Block Copolymers | Instead of a mixed distribution of monomeric units, a long sequence or block of one monomer is joined to a block of the second monomer: ~AAAAA-BBBBBBB~AAAAAAA~BBB~.. |
| Graft Copolymers | As the name suggests, side chains of a given monomer are attached to the main chain of the second monomer: ~AAAAAAA(BBBBBBB~)AAAAAAA(BBBB~)AAA~.. |

- Block copolymers

Block copolymers (BCPs) are a specific class of copolymers, in which the chemically distinct monomer units are grouped in discrete blocks along the polymer chain. (Figure 5.1) illustrates a few of the many architectures of BCPs, which can be configured into linear, branched (graft and star), and cyclic molecular architectures. Thanks to the advancement of polymer synthetic strategies and techniques, e.g., controlled polymerization techniques along with facile post-polymerization functionalization, BCPs with precisely controlled molecular weights and defined macromolecular architectures can be prepared. The extraordinary structural and compositional versatility of BCPs has facilitated an explosion in the discovery and implementation of innovative synthetic strategies capable of generating previously unattainable levels of man-made architectural complexity

Figure 5.1 Representative architectures of linear block terpolymers, “comb” graft polymers, miktoarm star terpolymers, and cyclic block terpolymers.

- Addition Copolymerization

Most direct copolymerizations of equimolar mixtures of different monomers give statistical copolymers, or if one monomer is much more reactive a nearly homopolymer of that monomer. The copolymerization of styrene with methyl methacrylate, for example, proceeds differently depending on the mechanism. Radical polymerization gives a statistical copolymer. However, the product of cationic polymerization is largely polystyrene, and anionic polymerization favors formation of poly(methyl methacrylate). In cases where the relative reactivities are different, the copolymer composition can sometimes be controlled by continuous introduction of a biased mixture of monomers into the reaction.

Formation of alternating copolymers is favored when the monomers have different polar substituents (e.g. one electron withdrawing and the other electron donating), and both have similar reactivities toward radicals. For example, styrene and acrylonitrile copolymerize in a largely alternating fashion.Depending on the nature of the monomers, the type of initiating

systems it is possible to carry out copolymerization of radical andionic mechanism.

Block Copolymerization

Several different techniques for preparing block copolymers have been developed, many of which use condensation reactions. In the anionic polymerization of styrene a reactive site remains at the end of the chain until it is quenched. The unquenched polymer has been termed a living polymer, and if additional styrene or a different suitable monomer is added a block polymer will form. This is illustrated for methyl methacrylate in the following diagram. (Figure 5.2)

Figure 5.2

Production.The process can be carried out in bulkmonomers, in a solvent, in an emulsion or suspension.

SUMMARY

1. Unlike homopolymers, which consist of chains with identical repeating units, copolymers are macromolecules with more than one repeating unit in the same molecule. These repeating units may be randomly arranged or they may alternate in the chain. Block copolymers are linear polymers that consist of long sequences of repeating units in the chain, and graft copolymers are branch polymers in which the branches consist of sequences of repeating units that differ from those in the backbone.

2. Strongly electrophilic or nucleophilic monomers will polymerize exclusively by anionic and cationic mechanisms. Those like styrene and methyl methacrylate, which are neither strong electrophiles nor nucleophiles, also polymerize by free radical mechanisms. Since these two monomers also polymerize by ionic mechanisms, the reactivity ratios for all three systems may be compared.

3. The principal copolymers are SBR, butyl rubber, poly(vinyl chloride-co-vinyl acetate), Saran, ionomers, and Acrilan fibers.

4. Block and graft copolymers differ from mixtures but having the properties of each component. Thus, block copolymers may be used as thermoplastic elastomers and graft copolymers with a flexible backbone may be used for highimpact plastics.

5. Block and graft copolymers may be produced by step reaction polymerization and by chain reaction polymerization.

6. The principal graft copolymers are ABS, HIP, polyester plastics, and grafted starch and cellulose.

| Chapter6 |  |
| --- | --- |
|  | Step-Reaction Polymerization or Polycondensation Reactions |

Introduction

While condensation polymers account for only a small percentage of all synthetic polymers, most natural polymers are of the condensation type. The first all-synthetic polymer,Bakelite, was produced by the stepwise condensation of phenol and formaldehyde, andmany of the other synthetic polymers available before World War II were produced usingstepwise polycondensations of appropriate reactants.

As shown by Carothers in the 1930s, the chemistry of condensation polymerizationsis essentially the same as classic condensation reactions leading to the formation of monomeric esters, amides, and so on. The principal difference is that the reactants used forpolymer formation are bifunctional instead of monofunctional.The kinetics for stepwise polycondensation reactions and the kinetics for monofunctional aminations and esterifications, for example, are similar. Experimentally, both kineticapproaches are found to be essentially identical. There is a large overlap between the terms addition polymers and chain-growth kinetics and the terms condensation polymers and stepwise kinetics (Table 6.1).

Table 6.1 Comparison of Stepwise and Chainwise Polymerizations

| Chain | Step |
| --- | --- |
| Growth occurs by addition of one unit at a time Monomer concentrations decrease steadily throughout the polymerization Polymer chains are formed from the beginning of the polymerization and throughout the process Average chain length for reacted species remains approximately constant throughout the polymerization As reaction time is increased, polymer yield increases but molecular weight remains about the same Reaction mixture contains almost only unreacted monomer, polymer, and very little growing polymer chain | Any two molecular units can react Monomer disappears early in the reaction Polymer chain length increases steadily during the polymerization Average molecular weight for the reaction (for the reacted species) increases throughout the polymerization High “extents” of reaction are required to obtain high chain lengths Reaction system contains various stages, chain lengths, of product present in a calculable distribution |

This is in agreement with the slowness of stepwise processescompared with radical chain processes. The rate constant of individual polycondensationsteps is essentially independent of chain length, being similar to that of the “small-molecule” condensation. This is responsible for the stepwise growth pattern of polycondensations, since addition of a unit does not greatly increase the reactivity of the growing end,whereas for radical and ionic vinyl polymerizations the active radical and ionic site istransmitted to the growing chain end, giving a reactive end group.

- Polycondensation is a step process going through the mechanism

substitutions, intermediate products at separate stages can be

- formation of reaction centers,

  - formation of macromolecules (step chain growth),

  - termination of chain growth.

Most polycondensation processes are catalytic. The catalyst in them is either one of the original components (for example, dicarboxylic acid), or specifically injected substances.

According to the mechanism of action of catalysts (the mechanism Education Active Centers) V.V. Korshak suggested classify polycondensation processes into four main type:

  - cationic polycondensation;

  - anionic polycondensation;

  - ion coordination polycondensation;

  - free radical polycondensation

The cationic mechanism of polyesterification reactions occur and polyamidation. Ion coordination mechanism is characteristic of processes polycondensation of dicarboxylic acid dichlorides biphenols in the presence of tertiary amines.

Description of process

A large number of important and useful polymeric materials are not formed by chain-growth processes involving reactive species such as radicals, but proceed instead by conventional functional group transformations of polyfunctional reactants. These polymerizations often (but not always) occur with loss of a small byproduct, such as water, and generally (but not always) combine two different components in an alternating structure.

The polyester Dacron and the polyamide Nylon 66, shown here, are two examples of synthetic condensation polymers, also known as step-growth polymers. In contrast to chain-growth polymers, most of which grow by carbon-carbon bond formation, step-growth polymers generally grow by carbon-heteroatom bond formation (C-O & C-N in Dacron & Nylon respectively). Although polymers of this kind might be considered to be alternating copolymers, the repeating monomeric unit is usually defined as a combined moiety.

Examples of naturally occurring condensation polymers are cellulose, the polypeptide chains of proteins, and poly(β-hydroxybutyric acid), a polyester synthesized in large quantity by certain soil and water bacteria. (Figure 6.1)

Figure 6.1

Characteristics of Condensation Polymers

Condensation polymers form more slowly than addition polymers, often requiring heat, and they are generally lower in molecular weight. The terminal functional groups on a chain remain active, so that groups of shorter chains combine into longer chains in the late stages of polymerization. The presence of polar functional groups on the chains often enhances chain-chain attractions, particularly if these involve hydrogen bonding, and thereby crystallinity and tensile strength. The following examples of condensation polymers are illustrative.

Note that for commercial synthesis the carboxylic acid components may actually be employed in the form of derivatives such as simple esters. Also, the polymerization reactions for Nylon 6 and Spandex do not proceed by elimination of water or other small molecules. Nevertheless, the polymer clearly forms by a step-growth process.

Table 6.2 Some Condensation Polymers.

The difference in Tg and Tm between the first polyester (completely aliphatic) and the two nylon polyamides (5th & 6th entries) shows the effect of intra-chain hydrogen bonding on crystallinity. The replacement of flexible alkylidene links with rigid benzene rings also stiffens the polymer chain, leading to increased crystalline character, as demonstrated for polyesters (entries 1, 2 &3) and polyamides (entries 5, 6, 7 & 8). The high Tg and Tm values for the amorphous polymer Lexan are consistent with its brilliant transparency and glass-like rigidity. Kevlar and Nomex are extremely tough and resistant materials, which find use in bullet-proof vests and fire resistant clothing.

Many polymers, both addition and condensation, are used as fibers The chief methods of spinning synthetic polymers into fibers are from melts or viscous solutions. Polyesters, polyamides and polyolefins are usually spun from melts, provided the Tm is not too high. Polyacrylates suffer thermal degradation and are therefore spun from solution in a volatile solvent. Cold-drawing is an important physical treatment that improves the strength and appearance of these polymer fibers. At temperatures above Tg, a thicker than desired fiber can be forcibly stretched to many times its length; and in so doing the polymer chains become untangled, and tend to align in a parallel fashion. This cold-drawing procedure organizes randomly oriented crystalline domains, and also aligns amorphous domains so they become more crystalline. In these cases, the physically oriented morphology is stabilized and retained in the final product. This contrasts with elastomeric polymers, for which the stretched or aligned morphology is unstable relative to the amorphous random coil morphology.

This cold-drawing treatment may also be used to treat polymer films (e.g. Mylar & Saran) as well as fibers. (Figure 6.2)

Figure 6.2

Step-growth polymerization is also used for preparing a class of adhesives and amorphous solids called epoxy resins. Here the covalent bonding occurs by an SN2 reaction between a nucleophile, usually an amine, and a terminal epoxide. In the following example, the same bisphenol A intermediate used as a monomer for Lexan serves as a difunctional scaffold to which the epoxide rings are attached. Bisphenol A is prepared by the acid-catalyzed condensation of acetone with phenol. (Figure 6.3)

Figure 6.3

| Polyamides are polymers where the repeating units are held together by amide links. An amide group has the formula - CONH2. An amide link has this structure: | #### Nylon-6,6 |
| --- | --- |
|  | ### Nylon-6 is made from a monomer called caprolactam. |
|  | When this molecule polymerizes, the ring opens, and the molecules join up in a continuous chain |
|  | ### KevlarThe two monomers are benzene-1,4-dicarboxylic acid and 1,4-diaminobenzene |
| A polyester is a polymer (a chain of repeating units) where the individual units are held together by ester linkages. |  |
| A polyester is made by a reaction involving an acid with two -COOH groups, and an alcohol with two -OH groups. In the common polyester drawn below. |  |

SUMMARY

1. Many naturally occurring and some synthetic polymers are produced by condensation reactions which are described kinetically by the term step-reaction polymerization. Since a high fractional conversion (p) is required, only a relatively few useful linear polymers, such as polyesters, polycarbonates, polyamides, polyurethanes, polyureas, polysulfides, polyoxides, and polysulfones, may be synthesized by step reactions. However, this technique may be used to produce network polymers even when the fractional conversion is relatively low. Phenolic, epoxy, urea, and melamine resins are produced by step-reaction polymerization.

2. Since the fractional conversions are very high, useful polymers may be produced by the stepwise condensation of a bifunctional acyl or sulfonyl chloride with a diamine or glycol. The rate constant k for these second- and third-order reactions is similar to corresponding reactions of monofunctional reactants and is essentially unchanged as the reactions proceed through dimers, tetramers, octamers, oligometers, and higher molecular weight polymers. This rate constant increases with temperature in accordance with the Arrhenius equation.

3. The crosslinking of polyesters produced from phthalic anhydride and glycerol may be controlled using relatively low-temperature conditions under which the secondary hydroxyl group is not esterified until the temperature is increased. The crosslinking of unsaturated polyesters such as alkyds occurs by so-called drying reactions in which crosslinking occurs in the presence of oxygen and a heavy metal catalyst.

4. High molecular weight polyamides, such as nylon-66, may be produced by the thermal decomposition of pure salts of the diamine and dicarboxylic acid reactants. The melting point of these polyamides is decreased as the number of methylene groups in the reactants is increased or if pendant groups are present. The introduction of stiffening groups such as phenylene groups increases the melting point. Polyamides, polybenzimidazoles, polyquinoxaline, and spiroketal polymers have many stiffening groups in the chains and are useful at high temperatures.

5. Polyurethanes and polyureas are produced by the room temperature reaction of a diisocyanate with a dihydric alcohol or a diamine, respectively. When water is present in the reactants, unstable carbamic acids are produced, there decompose to form carbon dioxide, which serves as a blowing agent for foam production.

6. Flexible and rigid polysulfides are produced by a Williamson condensation of aliphatic reactants and a Wurtz condensation of aromatic reactants, respectively. Rigid polyoxides are produced by the low-temperature oxidative coupling of hindered phenols. Stable rigid aromatic polysulfones are produced by the Friedel-Crafts condensation of phenyl sulfonyl chlorides.

7. Low molecular weight epoxy resins are produced by the condensation of epichlorohydrin and dihydroxy compounds such as bisphenol A. These prepolymers, which contain hydroxyl pendant groups and epoxy end groups, may be cured at room temperature by the reaction of polyamines and at elevated temperature by the reaction with cyclic anhydrides.

8. Linear phenolic and amino resins may be produced by the condensation of formaldehyde with phenol, urea, or melamine under alkaline conditions at moderate temperatures. These A-stage resole resins may be advanced almost to incipient gelation (B stage) by heating and cured to the C stage by heating at higher temperatures or by the addition of acids. Novolac resins may be produced under acid conditions by condensing formaldehyde with an excess of phenol. These A-stage linear resins are advanced to the B stage by heating with hexamethylenetetramine under moderate conditions and cured to the C stage in a mold at higher temperatures.

9.When the functionality of phenol, urea, or melamine is reduced to 2 by the incorporation of substituents, the condensation with formaldehyde yields soluble thermoplastics.

| Chapter 7 |  |
| --- | --- |
|  | Polymer Structure (Morphology) |

Introduction

The size and shape of polymers are intimately connected to their properties. The shape of polymers is also intimately connected to the size of the various units that make up the macromolecules and the various primary and secondary bonding forces that are present within the chain and between chains. This chapter covers the basic components that influence polymer shape or morphology. We describe the structure of both synthetic and natural polymers in terms of four levels of structure.

- The primary structure

The primary structure describes the precise sequence of the individual atoms that compose the polymer chain. For polymers where there is only an average structure, such as proteins, polysaccharides, and nucleic acids, a representative chain structure is often given.

The structure can be given as a single repeat unit such that the full polymer structure can be obtained by simply repeating the repeat unit 100, 500, or 1,000 times, depending on the precise number of repeat units in the polymer chain. For poly(vinyl chloride), PVC, this is

Or some fuller description of the primary structure may be given such as that below for three repeat units of PVC where the particular geometry about each chiral carbon is given.

| The repeat unit for cellulose is |  |
| --- | --- |

- The secondary structure

The secondary structure describes the molecular shape or conformation of the polymer chain. For most linear polymers this shape approaches a helical or “pleated skirt” (or sheet) arrangement depending on the nature of the polymer, treatment, and function. Examples of secondary structures appear in Figures 7.1 and 7.2.

| In general, polymers (both natural and synthetic) “emphasize” two general shapes—helical and pleated (Figures 7.3, 7.1) |  |  |
| --- | --- | --- |
| The intermolecular bonds in many polyamides and some fibers, including β-keratin, produce strong pleated sheets. These and many other polymers, including nucleic acids, may form helices. Ribonucleic acid (RNA) exists as a single helix, whereas deoxyribonucleic acid (DNA) exists as a doublehelix. |  |  |
|  | (a) α-helix and (b) β-pleated Sheet structure |  |
| The secondary structure of synthetic polymers are: |  |  |
| Figure 7.3 Typical hydrogen bonding between hydrogen and oxygen or nitrogen atoms in nylon66. (From Modern Plastics Technology, by R. Seymour, 1975, Reston Publishing Company, Reston, Virginia. Used with permission.) |  |  |
| It is important to note that the high melting point of nylon-66 (2650C, Figure 7.3) is the result of a combination of London, dipole–dipole, and hydrogen bonding forces between the polyamide chains. The hydrogen bonds are decreased when the hydrogen atoms in the amide groups in nylon are replaced by methyl groups and when the hydroxyl groups in cellulose are esterified. | Figure 7.1 Ball-and-stick structure of polystyrene in the helical conformation | Figure 7.2 Helical conformations of isotactic vinyl polymers. [From N. Gaylord, in Linear and Stereoregular Addition Polymers (N. Gaylord and H. Mark, eds.), Wiley Interscience, New York, 1959. With permission from the Interscience Division of John Wiley and Sons, Publishers |

Atoms in individual polymer molecules are joined to each other by relatively strong covalent bonds. The bond energies of the carbon–carbon bonds are on the order of 80–90 kcal/mol (320–370 kJ/mol). Further more polymer molecules, like all other molecules, are attracted to each other (and for long-chain polymer chains even between segments of the same chain) by intermolecular, secondary forces.

Secondary forces, frequently called van der Waals forces because they are the forces responsible for the van der Waals corrections to the ideal gas relationships, are of longer distance in interaction, in comparison to primary bond lengths, generally having significant interaction between 2.5 and 5 A˚ (0.25–0.5 nm).

Many physical properties of polymers are indeed quite dependent on both the conformation (arrangements related to rotation about single bonds) and configuration (arrangements related to the actual chemical bonding about a given atom), since both affect the proximity one chain can have relative to another. Thus, amorphous polypropylene is more flexible than crystalline polypropylene (compare linear polymers a (left) and b of (Figure 7.4).

Figure 7.4 Representation of an amorphous polymer and representation of folded polymer chains in polymer crystals. (From Modern Plastics Technology by R. Seymour, 1975, Reston Publishing Company, Reston, Virginia. Used with permission.)

- The tertiary structure

The tertiary structure describes the shaping or folding of the polymer. Examples of this are found in (Figures 7.4, 7.5 and 7.9–7.10).

Polymers typically contain combinations of ordered (crystalline) regions and structures and less ordered (amorphous) regions and structures. These different structures profoundly influence the chemical and physical properties of the material and products derived from them. Chains can be connected to one another through physical entanglement similar to what happens when a kitten gets a hold of a ball of yarn. Chains can be connected through formation of chemical linkages that chemically hold one chain to another chain. Some polymers, such as the traditional rubbers of our automobile tires, are highly interconnected through chemical bonds, whereas other polymers have only a small amount of chemical interconnections, such as are often present in so-called “permanent press” dress shirts. These two types of interconnections, physical and chemical, are referred to as crosslinks, and the extent of crosslinking referred to as the crosslink density. Further, some structures are composed of a maze of crosslinking and have a high crosslink density, forming a complex interlocking structure that offers only an average overall structure.

Figure 7.5 Model representation of a folded chain lamellar crystal for polyethylene at the surface of a single crystal. (From P. Geil and D. Reneker, J. Appl. Phys. 31:1921 (1960). With permission from the American Institute of Physics.)

Crystalline portions are represented by structures such as (Figures 7.5, 7.6) while historically important amorphous-crystalline representations are given in (Figures. 7.7, 7.82.19) with both structures building upon helical and pleated structures (Figures 7.3, 7.6, 7.2).

Figure 7.6 Maltese cross–like pattern for spherulites viewed under a polarizing microscope with crossed Nicol prisms in a silicone-like polymer. The large and small spherulites are the result of crystallization occurring at different temperatures. [From F. Price, in Growth and Perfection of Crystals (R. Doremus, B. Roberts, and D. Turnbull, eds)]. John Wiley, New York, 1958, p. 466. With permission.]

Figure 7.7 Schematic two-dimensional representations of models of the fold surface in polymer lamellae: (a) sharp folds, (b) switchboard model, (c) loops with loose folds, (d) buttressed loops, and (e) a combination of these features.

Figure 7.9 Steps in the formation of a spherulite from the bulk.

Figure 7.10 (a) Spherulite structure showing the molecular-level lamellar chain-folded platelets and tie and frayed chain arrangements. (b) A more complete description of two sets of three lamellar chain-folded platelets formed from polyethylene. Each platelet contains about 850 ethylene units as pictured here.

- The quaternary structure

Finally, the quaternary structure represents the overall shape of groups of the tertiary structures where the tertiary structures may be similar or different. Examples are found in (Figures 7.9–7.10)

For linear polyethylene, the initial structure formed is a single crystal with folded chain lamellae as shown in (Figure 7.5) and depicted in (Fig. 7.9a).These quickly lead to the formation of sheaf-like structures (Figure 7.9d) called axialites or hedrites. As growth proceeds, the lamellae develop on either side of a central reference plane. The lamellae continue to fan out, occupying increasing volume sections through the formation of additional lamellae at appropriate branch points. The result is the formation of spherulites as pictured in (Figures 7.6, 7.9, and 7.10). While the lamellar structures present in spherulites are similar to those present in polymer single crystals, the folding of chains in spherulites is less organized. Further, the structures that exist between these lamellar structures are generally occupied by amorphous structures including atactic chain segments, low molecular material, and impurities.

SUMMARY

1. Polymers, or macromolecules, are high molecular weight compounds with chain lengths greater than the critical length required for the entanglement of these chains. There is an abrupt change in melt viscosity and other physical properties of high molecular weight compounds when the chain length exceeds the critical chain length.

2. While some naturally occurring polymers, such as proteins, are monodisperse, i.e., all have the same molecular weight, other natural and synthetic polymers, such as cellulose and polyethylene, are polydisperse, i.e., they consist of a mixture of polymer chains with different molecular weights. Hence, one uses the term DP to indicate an average degree of polymerization, where DP is equal to the number of mers (repeating units) in the polymer chain.

3. Many polymers, such as cellulose and HDPE, are linear polymers consisting of long, continuous, covalently bonded atoms. Others, such as amylodextrin and LDPE, have branches or chain extensions from the polymer backbone and hence have greater volume and lower density than linear polymers. Both linear polymers and those with branches are thermoplastics. In contrast, network polymers such as ebonite, in which individual chains are joined to each other by covalently bonded crosslinks, are infusible thermoset polymers.

4. Functional groups in the polymer backbone, such as the methyl group in polypropylene and hevea rubber, are called pendant groups.

5. Many rubber-like polymers are flexible because the free rotation of carbon–carbon single bonds allows the formation of many different shapes, or conformations. This segmental motion is restricted by bulky pendant groups, by stiffening groups in the polymer chains, and by strong intermolecular forces. Hydrogen bonding, which is the strongest of these intermolecular forces, is essential for most strong fibers.

6. Free rotation of covalently bonded atoms is also prevented by the presence of double bonds. Thus, stable trans and cis configurations are possible for polymers such as polyisoprene. The cis and trans isomeric forms of polyisoprene are known as flexible hevea rubber and hard plastic gutta percha, respectively.

7. When a chiral center is present in a polymer such as polypropylene, many different configurations or optical isomers are possible. The principal configurations with ordered arrangements of the pendant groups are high-melting, Copyright © 2003 by Marcel Dekker, Inc. All Rights Reserved. strong molecules known as isotactic and syndiotactic isomers. Lower melting isomers in which the pendant groups are randomly oriented in space are known as atactic polymers.

8. The temperature at which segmental motion occurs because of free rotation of the covalent bonds is a characteristic temperature called the glass transition temperature. To be useful as plastics and elastomers, the polymers must be at a temperature below and above the glass transition temperature, respectively.

9. Since the specific volume, index of refraction, gas permeability, and heat capacity increase because of the onset of segmental motion at Tg, abrupt changes in these properties may be used to determine Tg.

10. The first-order transition, or melting point (Tm), is 33–100% greater than Tg, which is sometimes called the second-order transition. The greatest difference between Tm and Tg is demonstrated by symmetrical polymers like HDPE.

11. A polymer chain stretched out to its full contour length represents only one of the myriad of conformations present in a polymer at temperatures above Tg. Hence, the chain length is expressed statistically as the root-mean-square distance  which is about 7% of the full contour length of the polymer chain.

12. Since branched chains like LDPE have many chain ends, it is customary to use the radius of gyration (S), which is the distance of a chain end from the polymer’s center of gravity, instead of r.

13. The flexibility, which is related inversely to the orientation time (), increases as the temperature increases and may be calculated from the Arrhenius equation:

14. Fibers and stretched elastomers are translucent because of the presence of spherulites consisting of organized crystallites or regions of crystallinity.

15. Since single-lamellar crystals consisting of folded chains of symmetrical polymers can be prepared, it is now assumed that crystalline polymers may be represented by a switchboard model consisting of crystalline and amorphous domains.

16. Additional orientation of crystalline polymers occurs and physical properties are improved when films are biaxially oriented or when fibers are stretched.

17. The principal differences between elastomers, plastics, and fibers are the presence and absence of stiffening groups in the chain, the size of the pendant groups on the chain, and the strength of the intermolecular forces. Elastomers are usually characterized by the absence of stiffening groups in the polymer backbone, the presence of bulky pendant groups, and the absence of strong intermolecular forces. In contrast, fibers are characterized by the presence of stiffening groups in the polymer backbone and of intermolecular hydrogen bonds and the absence of branching or irregularly spaced pendant groups. The structure and properties of plastics are between these two extremes.

| Chapter 8 |  |
| --- | --- |
|  | ADVANCED METHODS FOR IDENTIFICATION |

Introduction

The complete and reliable identification of a polymeric material is a complex and complex task, requiring a long time and based on a deep understanding of analytical chemistry, experience and the use of modern equipment. Polymeric materials are often copolymers, blends and contain various additives. Modifying a material changes its fundamental characteristics used for identification, such as the color of smoke and smell, which makes simple identification methods inapplicable. Moreover, very small amounts of material are often available, so that polymer identification is possible only using modern methods described later in this chapter. Just a few milligrams of a substance is needed in order to perform studies using spectroscopy, thermal analysis, microscopy or chromatography.

To identify polymers and additives contained in compositions based on them, use the following modern analytical methods (Table 8.1):

Table 8.1 Modern analytical methods of identification of polymers

| Method | Area of application |
| --- | --- |
| Liquid chromatography | Distribution of macromolecules by size |
| Gelpermeation chromatography | Studying of mixtures, phosphorites, plasticizers, lubricants |
| Gas chromatography | Residual monomers Non-polymer components Plasticizers |
| Infrared spectroscopy | Polymer type Nature of additives |
| Thermal analysis | Fillers Lubricants Polymer molecular weight |
| X- ray diffraction analysis | Fillers Fire retardant additives Stabilizers |
| Nuclear magnetic resonance | Polyethers organosilicon compounds Phenolic resins |
| Chemical analysis | Lubricants Fire retardant additives Catalysts |

- IR-Spectroscopy in Polymer Science

IR-spectroscopy is probably the oldest of the spectroscopic methods used in polymer science. It is basing of the analysis of molecular vibrations. It can be subdivided into near-infrared (NIR), medium-infrared (MIR), and Raman-spectroscopy.

20

is ideally suited to qualitative analysis of polymer starting materials and finished products as well as to quantification of components in polymer mixtures and to analysis of in-process samples. IR spectroscopy is reliable, fast and cost-effective. This application note describes several approaches to themeasurement and analysis of IR spectra of typical polymer samples, and applies the techniques to the identification of some industrial polymer samples.

When identifying polymeric materials, as a rule, first analyze the presence of absorption bands in the region stretching vibrations of the double bond (1680–1640 cm – 1) and the region of deformation vibrations of these bonds (990–660 cm – 1). If they are in the IR spectrum, the polymer can be classified as unsaturated polymers. Next, using the characteristic frequency tables, make a complete assignment of other absorption bands to certain

atomic groups that make up the link macromolecules. The interpretation of the spectrum is complicated by the fact that the absorption bands different groups may overlap or shift as a result a number of factors. Using the method of IR-spectroscopy can also be determined and study intermolecular and intramolecular hydrogen communications, since their formation leads to a shift of the characteristic band towards lower frequencies; to broadening and increasing the intensity of the band corresponding to the valence vibration of the group involved in the formation of hydrogen bonds. For the study of hydrogen bonds, spectra of polymers are usually taken at several concentrations in a non-polar solvent. An important role in the analysis of polymers is played by structurally sensitive bands in the IR spectra. These include bands crystallinity, regularity, conformation-sensitive stripes, as well as stripes due to wrinkling in crystallites of polymers.

Mid Infrared Spectroscopy. The positions of absorption bands in the spectrum give information about the presence or absence of specific functional groups in a molecule and as a whole the spectrum constitutes a “fingerprint” that can be used to determine the identity of the sample. The absorption band positions in the spectrum provide data regarding the absence or presence of certain functional groups within a molecule. Samples containing different components can be identified through a variation between two spectra. The IR spectra of a number of standard polymers, such as polytetrafluoroethylene (PTFE), polystyrene (PS), polypropylene (PP), and polyethylene (PE), are shown in (Figure 8.1).  Visual analysis of the obvious variations between the spectra makes it easy to distinguish the materials.

Figure 8.1 Mid-IR spectra of common polymers.

Further spectral interpretation can provide structural data, for instance, while observing the C–H stretch region around 2950cm- 1, it is possible to view the difference between PP and PE because of the differing ratios of CH3 and CH2 groups. With bands over 3000cm-1, PS suggests the presence of aromatic groups, while C–H groups are not found in PTFE, and hence, the existing weak bands could be the result of surface contamination or impurities.

Fast infrared spectroscopy in the near spectral region has become especially popular lately. The sample is irradiated in the near infrared region, lying in the wavelength range from 800 to 200 nm. Macromolecules absorb radiation in different ways, which ultimately gives a unique spectrum, which allows identifyingof the polymer under study.

The technology of measuring the spectrum in the near infrared region is an inexpensive high-speed method that has become an alternative to the method of Fourier-infrared spectroscopy.Also in connection with the development of a new generation of consoles that allowed to reduce the sample preparation time and expand the functionality of the method. Therefore, there are practically no restrictions on the type of sample, i.e. IR spectra of opaque, dark, colored polymer samples, dark and viscous liquids, polymer

granules, cables and other materials that cannot be analyzed by transmission.

- Fourier Infrared spectroscopy

Significant advances in IR spectroscopy are due in recent time with the advent of high-resolution instruments - Fourier spectrometers, which record the spectrumin a very short time (1-2 minutes), with high resolution (up to 10–2 cm – 1) and are characterized by high sensitivity-sensitive stripes, as well as stripes due to wrinkling in crystallites of polymers.

The given analysis based on the use of the Fourier transform of the Infrared spectrum  (IR-spectrum )is currently one of the most widely used methods, both by practitioners and scientists, for the identification of polymers. The resulting infrared spectrum is the same individual reflection of the polymer as fingerprints. The results of the analysis are displayed in graphical form on the display. Since no two individual structures give completely identical spectra, the obtained spectrum is compared with known standards for previously studied materials, which allows us to uniquely identify the polymer being analyzed.

Analysis Fourier transform infrared (FTIR) analysis is by far the most widely used and accepted technique for plastics identifi cation by the professionals and scientists. The test is conducted simply by passing an infrared beam through a prefabricated sample, whereby some of the infrared radiation is absorbed or transmitted. The resulting spectrum, like a fi ngerprint unique to a particular polymer, is graphically displayed on a computer screen. Since no two unique molecular structures produce the same infrared spectrum, the resulting spectra can be compared with known material spectra and the material can be positively identifi ed. Fast identifi cation of polymers using near-infrared spectroscopy (NIR) has gained popularity in recent years. The specimen to be identifi ed is illuminated with a near-infrared wavelength ranging from 800 to 2000 nms. Polymer molecules absorb this radiation in different ways, generating unique spectra allowing one to quickly identify a particular polymer. NIR technology offers plastics recyclers lowcost, high-speed alternative to traditional FTIR methods.

- Thermogravimetric Analysis

In thermogravimetric analysis (TGA), changes in the weight of a specimen are recorded as the specimen is progressively heated. The test procedure is quite simple. A typical apparatus consists of an analytical balance, a programmable electrical furnace, and a recorder. TGA is very useful in characterizing polymers containing different levels of additives and fi llers by measuring the degree of weight loss. For example, the percentage of glass fi ber or mineral fi ller in a polymer can be determined by completely combusting the polymer in an inert atmosphere such that the remaining residue is only glass or inert fi ller. TGA is also used to identify the ingredients of blended compounds according to the relative stability of individual components.

- Differential scanning calorimetry (DSC)

Differential scanning calorimetry (DSC) measures the amount of energy absorbed or released in terms of heat by a sample as it is heated or cooled or held at a constant temperature. DSC is one of the most powerful techniques available for determining melting profi les of polymers including glass transition temperature, melting point, crystallization temperature, and degradation temperature. In the case of a semicrystalline polymer, many important physical properties are dependent upon crystallinity. DSC measurements provide important information concerning percent crystallinity along with rate of crystallization. The presence or absence of anti-oxidant in a polymer along with oxidative stability can be determined with this technique. DSC can be used to determine the ratio of polymer in a blend, block, or random copolymer through measuring the thermal characteristics of the melting region. Many applications requiring quantitative determination of additives such as mold release agents, antistats, UV stabilizers, and impact modifi ers can be achieved through the use of DSC technique. By studying a typical DSC thermogram, one can characterize a polymer by studying (a) the behavior of the material all the way from glass transition temperature to degradation temperature and (b) any changes that take place between the two extremes.

- Thermomechanical Analysis (TMA)

TMA is designed to measure the physical expansion or contraction of the material, or changes in its modulus or viscosity, as a function of temperature. It is used to identify softening points and characterize viscoelastic performance over a temperature range. Thermomechanical analysis is fairly simple, and it consists of applying a constant force with a probe and measuring dimensional changes in vertical direction as the sample is heated under a no-load or fi xed-load condition. TMA is very useful in polymer characterization, to determine properties such as melting point, glass transition temperature, crosslink density, degree of crystallization, and coeffi cient of expansion accurately.

- Nuclear Magnetic Resonance (NMR)

NMR spectroscopy is a very powerful analytical technique for identifying organic molecules and determining their chemical structures. Some of the nuclei in a molecule possess the property of spin, which can be in one of two orientations. If a magnetic fi eld is applied to the molecule, these differences in spin cause the nuclear energy level to split. The molecule is then subjected to an additional weak, oscillating magnetic fi eld. At a precise frequency the nuclear magnets resonate, and it is this that is recorded and amplifi ed (3). NMR provides characterization of compound structure as well as absolute identifi cation of specifi c ingredients in simple mixtures. The technique can also provide a general characterization by functional group that cannot be obtained by other analytical methods (4). In the plasticspolymer fi eld, carbon-13 NMR is most widely used for identifi cation analysis. Identifi cation of monomeric substances such as plasticizers, stabilizers, and lubricants from their NMR spectra is relatively simple and straightforward.Nuclear magnetic spectroscopy is a powerful analytical method for identifying organic molecules and determining their structure. The nuclei of some atoms in a molecule can be in different positions with respect to the orientation of their spin. If a magnetic field is imposed on such a nucleus, the difference in the spins leads to a splitting of the energy levels. Further, the molecule is additionally affected by a weak oscillating magnetic field. At some specific and precisely defined frequencies, a resonance of oscillations occurs and this effect is recorded and amplified.

The method of nuclear magnetic resonance gives a complete description of the structure of a chemical compound, as well as reliable identification of ingredients in mixtures. This method allows you to define the structure of functional groups, which cannot be established by other analytical methods.

In the study of polymers, C13 atoms are most often used to identify a material. The determination of low molecular weight compounds, such as plasticizers, stabilizers, lubricants, is very easily and directly determined by their NMR spectra.

- Chromatography

Chromatography is an analytical technique used to separate the components of a mixture, which fl ow at different rates along some separating medium. The fi xed material over which the mixture passes is called the stationary phase and is usually solid or gel. The moving fl uid, often a liquid but sometimes a gas, is called moving phase. The mixture is dissolved in a solvent called eluent and passed through a column or series of columns. The different strengths of the interatomic force between the molecules being separated and the molecules of the stationary phase and the eluent are responsible for the separation of the mixture. The different components may be identifi ed and in some cases may be determined quantitatively (5). Both gas chromatography (GC) and liquid chromatography (LC) are used for identifi cation analysis. However, gel permeation chromatroghy (GPC) is most used and accepted in the plastics industry.

- Mass Spectrometry (MS)

A mass spectrometer is a very useful tool in obtaining detailed structural information about a polymeric compound from very minute quantity of material. The molecular weight and atomic composition can be determined by studying and evaluating the spectra of organic compounds, and additives are positively identifi ed. The combined use of GC (gas chromatography) and MS (mass spectrometry), called GCMS, provides even more powerful tool for identifi cation analysis. In mass spectrometry the substance to be analyzed is heated and placed in a vacuum. The resulting vapor is exposed to a beam of electrons which causes ionization to occur, either of the molecules or their fragments; the ions thus produced are accelerated by an electric impulse and then passed through a magnetic fi eld, where they describe curved paths whose direction depend on the speed and mass-to- charge ratio of the ions. This has the effect of separating the ions according to their mass (electromagnetic separation). Because of their greater kinetic energy, the heavier ions describe a wider arc than the lighter ones and can be identifi ed on this basis. The ions are collected in appropriate devices as they emerge from the magnetic fi eld (6).

- X-Ray Fluorescence

X-ray fl uorescence spectrometry is primarily used for qualitatively and quantitatively identifying the additives used in a variety of polymers, determining the presence of impurities and contaminants in a compound, and detecting and determining trace elements in polymers and monomers. Two types of instruments are available for X-ray fl uorescence spectrometry: wavelength-dispersive (WDXRF) and energy-dispersive (EDXRF)

- Microscopy

Optical microscopy (OM) excels in providing information about surface morphology, identifying contaminants and impurities, and analyzing polyblends and alloys. The technique is used extensively for study of elemental composition in thin fi lms. Optical microscopy is further divided into two classes, SEM (scanning electron microscopy) and TEM (transmission electron microscopy), the latter being capable of providing greater resolution capabilities. The image can be magnifi ed over 100,000 times from the original object. SEM image is produced by scanning a fi nely focused electron beam over a surface and using the scattered secondary electrons to create highly magnifi ed image of the material surface (7). By contrast, transmitting the electrons through the specially prepared specimen produces a TEM image. In special cases, more advance techniques such as SPM (scanning probe microscopy) and AFM (atomic force microscopy) are used.

| Chapter 9 | BIOPOLYMERS |
| --- | --- |
|  | POLYLACTIC ACID (PLA) |

- History of Polylactic acid

- Manufacturingof Polylactic acid

- Use-end of Polylactic acid

- Environmental Impact and Recycling

- Summary ofPLA

The problem of protecting the environment from stable polymers has grown into one of the most pressing global challenges. After creating extremely robust polymeric materials, chemists are now concerned about the opposite problem: how to get the materials with a short period of operation and which are able to decompose under natural conditions.

Research has developed in two directions.

1.The use of biopolymers. The biopolymers are produced by living organisms and are able to decompose under natural conditions. In this case it is often said about polysaccharides (starch and cellulose).

2. Synthesis of analogs of biopolymers are capable of degradation by light and bacteria, as well as polymers soluble in water.

Polylactide is a bio-based compostable thermoplastic that is considered as one of the most promising materials for replacement of traditional volume plastics. The properties of Polylactide can be tuned to resemble Polystyrene, Poly(ethylene terephthalate) or Polyolefins by controlling the stereochemistry by copolymerization or blending.

| Poly(lactic acid) (PLA) is the first commodity polymer produced from annually renewable resources, such as corn starch or sugarcanes. Polylactic acid (PLA) is a rigid thermoplastic polymer that can be semi- crystalline or totally amorphous, depending on the stereopurity of the poly- mer backbone. ( L)-Lactic acid (2-hydroxy propionic acid) is the natural andmost common form of the acid, but (D)-Lactic acid can also be produced bymicroorganisms or through racemization and this “impurity” acts much likecomonomers in other polymers such as Polyethylene Terephthalate (PET) orPolyethylene (PE). |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| POLYLACTIC ACID (PLA) |  |  |  |  |  |
| PLA films possess flexibility, suitable for making containers, including food, as protecting the packaged goods from odors and pollution.. It is believed that the PLA could be especially perspective for the manufacture of synthetic carpets, as suitable for the manufacture of both the front side and the carpet backing. |  |  |  |  |  |
|  |  |  |  | Fiber |  |
| Leading producers of PLA are Cargill Dow (NatureWorks LLC), Shimadzu, and Dupont and they produce PLA of varying molecular weight. The molecular weight is an important parameter to consider; most often it must be higher than 100,000 g/mol to obtain a polymer with good mechanical properties. |  |  |  |  |

PLA is a unique polymer that in many ways behaves like PET, but also

performs a lot like polypropylene (PP), a polyolefin.

PLA also has excellent organolepticcharacteristics and is excellent for food contact and related packaging applications.

- History of Polylactic acid

PLA is not new to the world of polymers. Carothers investigated the production of PLA from the cyclic dimer (lactide) of Lactic acid as early as 1932. Even before that, low molecular weight dimers and oligomers were detectedwhen water was removed from an aqueous solution of lactic acid.

Theannouncement of the formation of a new company, Cargill Dow LLC, in 1997brought two large companies together to focus on the production and marketing of PLA with the intention of significantly reducing the cost of production and making PLA a large-volume plastic.In today’s world of green chemistry and concern for the environment,PLA has additional drivers that make it unique in the marketplace. The starting material for the final polymer, lactic acid, is made by a fermentationprocess using 100% annually renewable resources. The polymer will alsorapidly degrade in the environment and the by-products are of very low toxicity, eventually being converted to carbon dioxide and water.

- Manufacturingof Polylactic acid

PLA can be prepared by both direct condensations of lactic acid and by

the ring-opening polymerization of the cyclic Lactide dimer, as shown in

(Figure 9.1)

Figure 9.1 Polymerization routes to polylactic acid.

Because the direct condensation route is an equilibrium reaction,difficulties of removing trace amounts of water in the late stages of polymerizationgenerally limit the ultimate molecular weight achievable by thisapproach. Most work has focused on the ring-opening polymerization of Lactide,although other approaches, such as azeotropic distillation to drive theremoval of water in the direct esterification process, have been evaluated.

Cargill Dow LLC has developed a patented, low-cost continuous process

for the production of Lactic acid-based polymers. The process combines thesubstantial environmental and economic benefits of synthesizing both Lactideand PLA in the melt rather than in solution and, for the first time, provides a commercially viable biodegradable commodity polymer made from renewableresources. The process starts with lactic acid produced by fermentation ofdextrose, followed by a continuous condensation reaction of aqueousLactic acid to produce low molecular weight PLA prepolymer (Figure 9.2).

Figure 9.2 E 42 Schematic of PLA production via prepolymer and Lactide.

Next, the low molecular weight oligomers are converted into a mixture of

Lactide stereoisomers using a catalyst to enhance the rate and selectivity of theintramolecular cyclization reaction. The molten Lactide mixture is then purifiedby vacuum distillation. Finally, PLA high polymer is produced using anorgano tin-catalyzed, ring-opening Lactide polymerization in the melt, completelyeliminating the use of costly and environmentally unfriendly solvents.After the polymerization is complete, any remaining monomer is removedunder vacuum and recycled to the beginning of the process (Scheme 9.1).

Scheme 9.1 Nonsolvent process to prepare Polylactic acid.

In any case they are not yet comparable to the global nature of the environmental problems, which created by environmental modern polymers.However, initial results indicate that chemists are on the way to solve them.

As of June 2010,Nature Workswas the primary producer of PLA (bioplastic) in the United States. Other companies involved in PLA manufacturing arePURAC Biomaterials(The Netherlands) and severalChinese manufacturers. The primary producer of PDLLA is PURAC, a wholly owned subsidiary ofCSMlocated in the Netherlands.

GalacticandTotalPetrochemicalsoperate a joint venture,Futerro, which is developing a second generation Polylactic acid product. This project includes the building of a PLA pilot plant in Belgium capable of producing 1,500tonnes/year.

PLA is a high strength and high modulus thermoplastic which can be processed by conventional processing techniques used for thermoplastics like injection molding, blow molding, and extrusion. PLA has, in comparison with many other bio-based materials, good properties and it is a promising candidate to replace petroleumbased plastics. The stiffness and strength are high, comparable to polystyrene at least at room temperature.

- Use-end of Polylactic acid

Polylactic acid (PLA) is the most common bioplastic in use today. First, corn or other raw materials are fermented to produce lactic acid, which is then polymerized to make Polylactic acid (PLA). Bioplastics are expected to make major contributions to environmental protection, because they reduce CO2and because they are biodegradable.

PLA is a highly versatile material suitable for a range of applications.Due to the high cost PLA was originally used mainly in biomedicalapplications. Through variations of the stereochemical composition,copolymerization and blending, properties similar to commercialthermoplastics like PP, PS and PET can be obtained. Currentapplications, thus, cover everything from biomedical applicationsto packaging, disposable items, fiber and agricultural applications.Possible future applications are numerous, ranging from automotive parts to housing for electric appliances.The range of applications for bioplastics is growing, from materials used in automobile interiors to packaging for foods and cosmetics, to agricultural sheeting, to household appliances (Pie-diagram 9.1).

Pie-diagram 9.1 Application of PLA

Biomedical Applications.Polylactide and its copolymers are among the most well-knownand studied bioresorbable biomedical materials and have beenused in biomedical applications since 1980s. The applicationsinclude resorbable sutures, implants and supports in human bodysuch as bone screws and plates, stents, drug delivery devices and tissue engineering. Polylactide has been shown to have good or satisfactorybiocompatibility and degrades in the body to nonharmful natural metabolites i.e. Lactic acid. The degradation time in the body can be modified over a wide span ranging from lessthan one year to several years depending on the L/DL composition,porosity and degree of crystallinity.

Being able to degrade into innocuous Lactic acid, PLA is used as medical implants in the form of anchors, screws, plates, pins, rods, and as a mesh. Depending on the exact type used, it breaks down inside the body within 6 months to 2 years. This gradual degradation is desirable for a support structure, because it gradually transfers the load to the body (e.g. the bone) as that area heals. The strength characteristics of PLA and PLLA implants are well documented.

Packaging.PLA is approved by the Food and Drug Administration (FDA)for use as food contact material.

Global bioplastics packaging demand is forecast to reach 885 kt by 2020 and a 24.9% compound annual growth rate (CAGR) is expected from 2010–15 slowing to 18.3% in the five years to 2020 (Pira International, 2010).

In packaging applications PLA is suitablefor cups, bottles, films and containers. Applications include rigid thermoforms such as trays and lids, bottles for water, milkor oil, clamshells for food packaging, shrink wraps for packaging, candy and flower wraps, disposable salad cups and cold drink cups. However, due to PLA's relatively low glass transition temperature, PLA cups cannot hold hot liquids. PLLA/PDLA stereocomplex,however, has higher glass transition temperature as wellas better thermal and hydrolytic stability and has potential also inapplications such as microwavable trays and hot-fill applications.Another advantage of stereocomplex PLA in packaging applicationsis the special crystal structure, which makes the products transparentdespite of high crystallinity. A limiting factor for wider use of stereocomplex materials is the poor availability of PDLA. PLAexhibits good aroma barrier properties and could prevent flavor loss in packaged food. One study showed that the quality of tomatoesin a Polylactide perforated paperboard tray remained as goodas the quality of tomatoes stored in LDPE bags. Another studyshowed that PLA container prolonged the blueberry shelf life comparedto the commercial vented petroleum based clamshell containers. Poly-L-lactide and poly-L-lactide-co-polycaprolacone havealso been tested for use in cheese packaging applications.

PLA can also be used as a decomposable packaging material, either cast, injection-molded, or spun.Cups and bags have been made from this material. In the form of a film, it shrinks upon heating, allowing it to be used in shrink tunnels. It is useful for producing loose-fill packaging, compost bags, food packaging, and disposable tableware. In the form of fibers andnon-woven textiles, PLA also has many potential uses, for example asupholstery, disposable garments,awnings, feminine hygiene products, anddiapers.

Fiber and Textile Applications.Polylactide and especially its more heat resistant stereocomplex aresuitable for textile fiber applications due to the low moisture absorption,low flammability and smoke generation. Polylactide isalso highly resistant to ultraviolet light and is, thus, suitable foroutdoor applications. The fiber applications include shirts, furnituretextiles, carpets, pillows, wipes, beddings, table clothes, curtains,mattresses, underwear and sports' clothes. Heat resistantPLA is also used in automobile textiles. In addition to the specificadvantages of Polylactide fibers described above, the quality of Polylactide fibers was considered to be at the same level compared to other chemical fibers. Polylactide fibers could, thus, successfullybe used as a replacement for existing chemical fibers.

Other Applications.Polylactide has high potential in agricultural applications such as mulchfilms either in pure form or blended with other polymerssuch as thermoplastic starch. In addition, Polylactide is used incompostable yard bags and dog poop bags. Lactic acid based hotmeltadhesives have also been developed. Foamed PLA couldbe used as structural protective foams, loose-fill packaging andinsulation material as an alternative for expanded polystyrene(EPS). While packaging is currently the high volume applicationfor PLA, in the future it is predicted that approximately half of PLAproduction would go to textile fibers and fabrics. Other important future applications are predicted to be in transportation and building, electrical appliances and electronics.

- Environmental Impact and Recycling

Organic waste materials from biodegradable and compostable bioplastics packaging can be treated, along with food, agricultural and garden/park waste, to produce carbon-rich compost (humic material). The biomass-origin of Polylactide together with its goodproperties, degradability, compostability and recyclability are, thus, increasingly important advantages. The possibility to tune the properties and degradation rate by e.g. stereochemical engineering or blending are further driving the development of PLAfor packaging and other commodity applications. Bioplastics packaging enables food waste to be composted without removing the packaging.

PLA lifecycle (Figure 9.3).The lifecycle of Poly Lactic Acid (PLA) is based on a closed loop system. Instead of simply reducing negative environmental impacts, PLA looks to actually create a positive impact. How? By re-using and recycling products as much as possible and thereafter, at their end-of-life, using various reintegration options to transform them back into feedstock for a new product lifecycle.

The end-of-life options for PLA include reusing, recycling, renewable energy recovery (incineration), compost/biodegradation, anaerobic digestion and feedstock recovery. By closing the loop in this way, consumers, brandowners and manufacturers can use resources more efficiently – securing the return of a valuable material stream and reducing waste.Instead of products having a linear, straight cradle-to-grave approach, lifecycles instead become circular and self-renewing.

Figure 9.3

PLA lifecycle

Summary ofPLA

PLA - aliphatic polyester, which is obtained by polycondensation of Lactic acid or by polymerizing a cyclic dimer Lactide (Figure 9.4 )

Figure 9.4 Biodegradable polymers organization based on structure and occurrence PLA is easily decomposed under natural conditions or hydrolyzed to Lactic acid, which can be re-converted to polymer

PLA can be processed by extrusion, injection molding, film and sheet casting, 3d printing, and spinning, providing access to a wide range of materials.

Bioplastics technology is rapidly advancing to improve cost competitive performance and provide materials with properties and processing similar to common plastics, such as PE, PP, PS, PVC and PET.

Significant proportions of biodegradable plastics now have renewable rather than petrochemical origins (www.european-bioplastics.org).

Figure 9.5 illustrates Evolution of PLA Production Capacities world 2011-2020

| Chapter 10 |  |
| --- | --- |
|  | Smart Polymers |

Introduction

Smart materials have been with us for some time, though the term is relatively new. Some of the first smart materials were piezoelectric materials, including poly(vinylene fluoride), that emit an electric current when pressure is applied and change volume when a current is passed through them. Most smart materials are polymeric in nature or have polymers forming integral parts of the “smart material” system.

Smart Polymers are composed of a wide range of macromolecules that reacts to a small change in the environment. They are also known as stimuli responsive polymers or intelligent materials. These polymers not only exhibit sensitive changes to environment but also return to their original state.

Smart materials are materials that react to an externally applied force—electrical, stress/strain (including pressure), thermal, light, and magnetic. A smart material is not smart simply because it responds to external stimuli, but it becomes smart when the interaction is used to achieve a defined engineering or scientific goal. Thus, most materials, including ceramics, alloys, and polymers, undergo volume changes as they undergo phase changes. While the best known phase changes are associated with the total changes in matter state such as melting/freezing, many more subtle phase changes occur.

Smart polymers  undergo large reversible changes, either physical or chemical, in their properties as a consequence of small environmental variations.

They can respond to a single stimulus or multiple stimuli such as temperature, pH, electric or magnetic field, light intensity, biological molecules, etc., that induce macroscopic responses in the material, such as swelling/collapse or solution-to-gel transitions, depending on the physical state of the chains.

Linear and solubilized smart macromolecules will pass from monophasic to biphasic near the transition conditions giving rise to reversible sol–gel hydrogels.

Smart cross-linked networks undergo chain reorganization at the transition conditions where the network passes from a collapsed to an expanded estate.

Smart surfaces change their hydrophilicity as a function of a stimulus-providing, responsive interface.

The important trends and factors which are promoting the market confidently are strong, resilient, durable and reliable nature. Due to these features, they are used in various applications such as biotechnology and medicine, electrical & electronics, automotive, drug delivery systems, and others.  These polymers are strong, resilient, durable, ecofriendly and reliable nature. Owing to these attributes, they are used in various applications such as biotechnology and medicine, drug delivery systems, and others (Figure 10.1).

Figure 10.1 Uses of smart polymers in biotechnology and medicine.

From Galaev, I.Y., Mattiasson, B. ‘Smart’ polymers and what they could do in biotechnology and medicine. Trends Biotechnol 17, 335_340.

Figure 10.2 schematically represents the uses of smart polymers in biotechnology and medicine. Biotechnology and biomedicine were the initial uses and nowadays continue to be the most diffuse applications. This fact is a consequence of the smart polymers’ behavior which initially was mainly observed in water (Galaev and Mattiasson, 1999) and, occasionally, in polymer blends (Sato et al., 1998) and in organic solvents (Osada and Gong, 1998).

- Types of “Smart polymers”

The Polymers that respond to temperature changes and, more specifically, those that undergo a phase transition in aqueous solution are currently gaining special attention due to their potential applications in the biomaterials fi eld (Bajpai, 2010 ), architecture (Yang et al. , 2013) or water-recovery strategies (Yang et al. , 2013) amongst others.

Moreover, analyzing the previous results related to the reviews published so far on smart polymers,four different classes of smart materials can be summarized. Not only hydrogels, but also shape memory polymers and nanocomposites, self-healing polymers and nanocomposites, as well as polymers and nanocomposites for smart packaging, can be evidenced, as summarized in (Figure 10.2).

Figure 10.2 Four different classes of smart materials.

- Polymer hydrogels

| Polymer hydrogelsplay a key role in the development of new biomaterials as their high level of hydration and 3D structure resemble natural tissue. | Aqueous polymer solutions that are transformed into gels by changes in environmental conditions, such as temperature and pH, thus resulting in in situ hydrogel formation, have recently attracted the attention of many investigators for scientific interest and for practical biomedical or pharmaceutical applications. When the hydrogel is formed under physiological conditions and maintains its integrity for a desired period of time, the process may provide various advantages over conventional hydrogels. Because of the simplicity of pharmaceutical formulation by solution mixing, biocompatibility with biological systems, and convenient administration, the pharmaceutical and biomedical uses of the water-based sol–gel transition include solubilization of low-molecular-weight hydrophobic drugs, controlled release, labile biomacromolecule delivery, such as proteins and genes, cell immobilization, and tissue engineering. When the formed gel is proven to be biocompatible and biodegradable, producing non-toxic degradation products, it will provide further benefits for in vivo applications where degradation is desired. |
| --- | --- |
| Polymeric systems of natural or modified natural polymers are N-isopropylacrylamide copolymers, poly(ethylene oxide)/poly(propylene oxide) block copolymers, and poly(ethylene glycol)/poly(d,l-lactide-co-glycolide) block copolymers.N-isopropylacrylamide copolymers, poly(ethylene oxide)/poly(propylene oxide) block copolymers, and poly(ethylene glycol)/poly(d,l-lactide-co-glycolide) block copolymers. |  |
| Mechanisms of Hydrogel | Hydrogels consist of a polymersolvent system. The polymer has to be cross-linked, physically or chemically, so that a three-dimensional network that is submerged in water is formed, swells, and retains some of the water within its structure. This requires that the polymer chain possesses hydrophilic groups. The temperature sensitive hydrogels are those that change their swelling properties when subjected to temperature changes. Two types of hydrogels with different behavior versus temperature exist—the “lower critical solution temperature” (LCST) and the “high critical solution temperature” (HCST). As the temperature increases LCST decrease swelling while HCST increase in swelling. |
| Application.A typical example of stimuli-sensitive hydrogel is a cross-linked waterswollennetwork with environment-sensitive groupsable to change their affinity with water. They areable to form additional cross-linking points uponstimulation. In this case, stimuli-sensitive hydrogelsshow only nonprogrammable shape transformationbetween swollen states and shrunken states.Stimuli-sensitive hydrogels have been extensivelystudied for drug delivery, cell culture, fluid control,separation, and sensing applications, not onlybecause of their stimuli sensitivity, but also becauseof their unique softness, high hydrophilicity, biocompatibility,and ability for rapid diffusion of molecules(Drury and Mooney, 2003; Chung et al., 2012).The first example of shape memory hydrogel wasreported by Osada and coworkers in the mid 1990s(Osada and Matsuda, 1995; Kagami et al., 1996).A thermally triggered shape memory hydrogel wasformed by water swelling of a polymer networkobtained by copolymerizing of acrylic acid, stearylacrylate, and methylenebisacrylamide (the crosslinker)(Zhao et al., 2015). In this case they used thecrystalline/melting transition as the switching segmentswhile the cross-linker set the permanent shape. The presence of water in hydrogels creates evenmore opportunities for designing shape memoryhydrogels using molecular switches. Theoretically, the same principle can be applied to organogelsalthough not much has been reported in the literature(Zhao et al., 2015). |  |
| However, despite the superior performance of hydrogels, they present several limitations mainly due to their poor controllability, actuation and response polymers. |  |
| Several advances have been made in this sense by the use of smart polymers in the preparation of hydrogels (Ravichandran et al. , 2012). For example, magnetically responsive polymer gels and elastomers are composites based on magnetic nanoparticles dispersed in a high elastic polymeric matrix. |  |
| Magnetic field quickly deforms the polymer matrix with no noise, heat evolution or exhaustion which makes these materials ideal for the preparation of sensors, micromachines, energy transducing devices, controlled delivery systems or even artifi cial muscles (Li et al. , 2013). |  |
| Macroscopic transitions can also be triggered by ‘biology-to-material’ interactions in the so-called biointeractive polymers . These materials incorporate receptors for biomolecules which, when stimulated, cause localized or bulk modifi cations in the material properties. |  |
| Those polymers that respond to selective enzyme catalysis are known as enzyme responsive. These materials represent an important advance in the integration of artificial materials with biological entities as they link together the polymer properties with specific biological processes controlled naturally by either regulating enzyme expression levels or availability of cofactors (Huet al., 2012b). Enzyme responsive polymers can also display reversible and dynamic responses to a stimulus, thus being of great interest in the formulation of new biomaterials such as cell supports, injectable scaffolds or drug delivery systems (de la Rica et al. , 2012). - Shape memory polymers |  |
| Shape memory polymers represent one of the most active areas in material science due to their easier processability and lower cost when compared with shape memory metals or ceramics; This kind of smart polymers have the ability to recover their (permanent) predefi ned shape when stimulated by an external stimulus (Figure 10.3).. Figure 10.3 Shape memory effect in polymers. A stable network and a reversible switching transition of the polymer are the two pre-requisites for shape memory effect. The stable network is responsible for the original shape, and reversible switching transition fixes the temporary shape, which can be crystallization/melting transition, liquid crystal anisotropic/isotropic transition, reversible molecule cross-linking (such as photodimerization, Diels – Alder reaction, oxidation/ redox reaction of mercapto groups), and supramolecular association/disassociation (such as hydrogen bonding, self-assembly metal–ligand coordination and self-assembly of β -cyclodextrin). In addition to the reversible switches mentioned, other stimuli that change chain mobility can also trigger shape memory effect, such as light, pH, moisture, electric fi eld, magnetic fi eld, pressure, etc. (Pretsch, 2010). Shape memory polymers allow large, recoverable strains; however, they normally present poor mechanical properties and do not support great shape-recovery stresses. As a result, great efforts are being made in the development of shape memory composites with reinforced properties. Shape memory polymers present numerous actual and potential applications in medicine, aerospace, textiles, engineering, microfl uidics, lithography and household products (Meng and Li, 2013). |
| The first shape memory effect in polymers was reported in the 1960s (Rainer et al ., 1964). This polymer consisted of a matrix of polyethylene irradiated with gamma radiation; the result was a material able to memorize its initial shape. |  |

- Self-healing polymers

Self-healing or restoration of lost functionalities without external help is a dream come true with self-healing polymers (Aïssa et al. , 2012).; Healing mechanisms can be extrinsic (the healing compound is isolated from the polymer matrix in capsules, fi bers or nanocarriers) or intrinsic (the polymer chains temporarily increase mobility and flow to the damaged area) (Billiet et al. , 2013) and are responsible for restoration of properties such as structural integrity (White et al. , 2001), surface aesthetics (Yao et al. , 2011), electrical conductivity (Tee et al. , 2012), hydrophobicity and hydrophilicity (Ionov and Synytska, 2012), mechanical properties (Jones et al. , 2013), etc.. When speaking about self-healing polymers it is worth distinguishing between those able to recover their material properties fully autonomously and those that require the application of an external stimulus, such as heat or UV-light, to initiate the recovery process (Hillewaere and Du Prez, 2015). Within the autonomous ones it is possible to distinguish two different categories of self-healing polymers, namely, external and internal self-healing polymers (Hillewaere and Du Prez, 2015). Yuan et al. (2008) and later many other groups worldwide (Hager et al., 2010; Blaiszik et al., 2010; Murphy and Wudl, 2010; Garcı´a et al., 2011; Guimard et al., 2012) refer to these two categories as extrinsic and intrinsic materials. Zhong et al. (Zhong and Post, 2015) reported an interesting review on composites with intrinsically self-healing polymeric matrices, summarizing their mechanisms, schematically reported in Fig. 6.14. Hillewaere et al. (Hillewaere and Du Prez, 2015) named them as external and internal, a definition we also adopt. In particular, external refers to the materials able to show its self-healing capabilities by adding supplementary healing agents in any kind of container (capsules, vascular network, etc.) while internal refers to materials where the self-healing capability is due to its own chemical nature. As examples of internal self-healing polymers we can take into account the work of Herbst et al., where they studied self-healing polymers obtained via supramolecular forces (Herbst et al., 2013). Another example is presented by Billiet et al. (2013) where they reported a study on the chemistry of cross-linking processes for self-healing polymers. Moreover, there are different material functions that can be recovered, obtaining the so-called functional self-healing polymers. Recently, there have been publications on the recovery ability of the material functions, such as corrosion protection or conductivity (Garcı´a et al., 2011; Hughes et al., 2010; Amendola and Meneghetti, 2012). Hillewaere et al. (Hillewaere and Du Prez, 2015) recently reviewed external self-healing polymers. They reported different self-healing chemistries and for each one they highlighted if there is a catalyst required, the different types of damage, and the efficiency of each system (Table 6.1). In particular, they reported that for the selfhealing chemistry based on the ring-opening metathesis polymerization of dicyclopentadiene (DCPD) and 5-ethylidene-2-norbornene (ENB) the use of catalyst is required and considered as the drawback of the system. Moreover, the choice of the catalyst is strongly influenced by the final selfhealing application temperatures, Fig. 6.15.. - Temperature-responsive polymers

Temperature-responsive polymers are especially interesting since variations in temperature can be applied externally in a non-invasive manner.; Furthermore, spontaneous temperature fl uctuations also occur in nature, for example, during day and night cycles as well as the increased temperature of infl amed tissue.. The three main classes of temperatureresponsive polymers are: 1. shape-memory materials; 2. liquid crystalline materials; 3. responsive polymer solutions.. Temperature-sensitive polymers present low critical solution temperature (LCST) or upper critical solution temperature (UCST) depending on their transition behavior from monophasic to biphasic when temperature is raised or, on the contrary, from biphasic to monophasic when temperature is raised, respectively. LCST polymers have been widely investigated whereas UCST polymers are quite rare. Most common LCST polymers are the poly( N -substituted acrylamide), poly(vinyl amide) and poly(oligoethylene glycol (meth)acrylate) families.. The most commonly studied and fi rst reported thermoresponsive polymer in aqueous solution is poly( N -isopropylacrylamide) (PNIPAM) (Figure 10.4). Figure 10.4 Structures of poly( N -isopropylacrylamide) (PNIPAM) and poly( N - vinyl caprolactam) (PVCL).. The polymerization of both the N -isopropylacrylamide (NIPAM) and N -vinylcaprolactam (VCL) monomers can be achieved by free radical polymerization of the vinyl group using a common radical initiator, such as azobisisobutyronitrile (AIBN). In recent years, the controlled radical polymerization (CRP) of both monomers has also been developed resulting in polymers of defi ned and narrow molecular weight distribution and defi ned end-groups..

- pH-sensitive polymers

pH-sensitive polymers can be defined as polyelectrolytes that include in their structure weak acidic or basic groups that either accept or release protons in response to a change in the environmental pH.; A polyelectrolyte is a macromolecule that can dissociate to give polymeric ions when dissolved in water or other ionizing solvents. Because of the repulsion between charges on the polymer chain, the system expands when it is ionized in a suitable solvent.. However, if the solvent prevents ionization of the polyelectrolyte, the dissolved chain remains in a compact, folded state (Fig. 3.1). If the polyelectrolyte chains are hydrophobic when unionized in a poor solvent, they collapse into globules and precipitate from solution. The interplay between hydrophobic surface energy and electrostatic repulsion between charges dictates the behavior of the polyelectrolyte. Since the degree of ionization of a weak polyelectrolyte is controlled by pH and the ionic composition of the aqueous medium, pH-sensitive polymers dramatically change conformation in response to minute changes in the pH of the aqueous environment. Medium pH controls polybase conformation changing from an expanded state to a folded state depending on the ionization degree of the pH-responsive polymer. (Figure 10.5) Figure 10.5 Polybasic states depending of the ionization of the ionic chain groups of the pH-responsive polymer..

pH-sensitive polymers bear weak polyacidic (poly(acrylic acids) or poly(methacrylic acids)) or polybasic (poly( N -dimethylaminoethyl methacrylate), poly( N -diethylaminoethyl methacrylate), poly(ethyl pyrrolidine methacrylate)) moieties in their structure that protonate or deprotonate as a function of the surrounding pH. Drug delivery systems, gene carriers (Pezzoli and Candiani, 2013) or glucose sensors (Kost and Langer 2012) are three of the multiple applications described for this kind of smart polymer.

There are such polymeric structures, as homopolymers (Tian et al ., 2012), block copolymers (Yao et al ., 2011; Yuan et al ., 2011), microgels, hydrogels (HGs) (Ram í rez et al ., 2011; Wu et al ., 2011), micro- and nanoparticles (NP) (Yang and Liu, 2013) and polymer brushes (Lee et al ., 2010) . The ‘intelligent’ properties of these pH-responsive polymeric systems are attractive for applications in life sciences and the chemical industry, providing potential applications, such as in controlled drug delivery, personal care, industrial coatings, oil exploration, water remediation, etc. (Brun-Graeppi et al ., 2011; Calder ó n et al ., 2010; Ho et al ., 2011; Luzinov et al ., 2004; Wever et al ., 2011; Zhao et al ., 2011). et al ., 2011; Luzinov et al ., 2004; Wever et al ., 2011; Zhao et al ., 2011).

Total Conclusion.Thermoresponsive polymers have gained significant interest in the past decade, especially those that undergo a temperature-induced phase transition in aqueous solutions. Water-soluble polymers generally undergo an LCST phase transition in water and, thus, the majority of reports focus on such LCST polymers. In recent years, the gold standard of LCST polymers, namely PNIPAM, has lost terrain to other alternative thermoresponsive polymers of which the TCP can be more easily tuned and that show less hysteresis between heating and cooling cycles, including POEG(M)As and poly(2-oxazoline)s. In contrast to LCST polymers, there is only a relatively small number of polymers reported that undergo a UCST transition in aqueous solution. Recent progress includes the development of UCST polymers with primary amide side chains that strongly interact by hydrogen bonding, but the UCST transition is strongly affected by minor ionic impurities as well as the ionic strength of the solution. Therefore, the major challenge in this fi eld is the development of polymers with a robust UCST transition in aqueous solution. The large application potential of LCST polymers is currently being explored for a wide variety of smart materials, ranging from biomedical applications, to sensors, water collection and energy effi cient buildings. However, further in-depth studies are required before such materials will be able to enter the market.

- Photo-sensitive polymers

Photo-sensitive polymers undergo a reversible or irreversible change in conformation, polarity, amphiphilicity, charge, optical chirality, conjugation, etc., in response to a light stimulus.; Reversible chromophores or reversible molecular switches (e.g., azobenzenes, spiropyran, diaryl ethane or coumarin) undergo a reversible isomerization upon light irradiation (Wang and Wang, 2013) while irreversible chromophores are cleaved from the polymer chain upon light exposure (e.g ., ο -nitrobenzylphotolabile protecting group) or induced reactivity resulting in the coupling of two species (e.g ., 2-naphthoquinone-3-methides).. Both molecular switches and irreversible chromophores have been applied in multiple applications such as drug delivery systems, functional micropatterns, responsive hydrogels, photodegradable materials or photoswitchable liquid crystalline elastomers for remote actuation (Ohm et al. , 2010)...

- The use of smart materials as sensing devices and shape-changing devices has been enhanced due to the increased emphasis on composite materials that allow the introduction of smart materials as components (Figure 10.6).

A typical smart material assembly might contain:

- Sensor components containing smart materials that monitor changes in pressure, temperature, light, current, and/or magnetic field

- Communications network that relays changes detected by the sensor components via fiberoptics or conductive “wire” (including conductive polymer channels)

- Actuator part that reacts to the action command.

Figure 10.6 Applications enabled by Ultra-thin chips

The actuator part may also be a smart material such as a piezoelectric bar placed in a wind foil that changes orientation according to a current “ordered” by the computer center to allow better handling and more fuel-efficient operation of a machine such as an automobile. Thus, the smart material may act as a sensor component, as an actuator part, or by itself as described earlier. The smart material may act on a molecular level, as in sensors, or as bulk material, such as in wind foils.

We are aware that muscles contract and expand in response to electrical, thermal, and chemical stimuli. Certain polymeric materials, including synthetic polypeptides, are known to change shape on application of electrical current, temperature, and chemical environment. For instance, selected bioelastic smart materials expand in salt solutions and may be used in desalination efforts.

They are also being investigated in tissue reconstruction, as adhesive barriers to prevent adhesion growth between surgically operated body parts, and in controlled drug release where the material is designed to behave in a predetermined manner according to a specified chemical environment. The molecular design can be tailored, giving materials with varying biodegradabilities.

Most current efforts include three general types of smart materials: piezoelectric, magnetostrictive (materials that change their dimension when exposed to a magnetic field), and shape memory alloys (materials that change shape and/or volume as they undergo phase changes).

Conductive polymers and liquid crystalline polymers can also be used as smart materials, since many of them undergo relatively large dimensional changes when exposed to the appropriate stimulus such as an electric field. New technology is being combined with smart materials called micromachines, i.e., machines smaller than the width of a human hair, of the order of micrometers. Pressure and flow meter sensors are being investigated and commercially made.

Summary. Smart Polymers are composed of a wide range of macromolecules that reacts to a small change in the environment. They are also known as stimuli responsive polymers or intelligent materials. These polymers not only exhibit sensitive changes to environment but also return to their original state. The important trends and factors which are promoting the market confidently are strong, resilient, durable and reliable nature. Due to these features, they are used in various applications such as biotechnology and medicine, electrical & electronics, automotive, drug delivery systems, and others. The characteristics of polymers which are determined by a change in environment factors such as pH, temperature, and others are known as smart polymers. They are also called stimuli response polymers or intelligent materials. These polymers are strong, resilient, durable, ecofriendly and reliable nature. Owing to these attributes, they are used in various applications such as biotechnology and medicine, drug delivery systems, and others.

Figure 10.7   illustrates Smart Polymers Market Forecasts to 2023

Figure 10.7 Smart polymers market forecast 2018 to 2023

| Chapter 11 |  |
| --- | --- |
|  | Recycling Plastic and Disposal |

Introduction

Plastic Problems: Waste and Health Plastic’s reputation fell further in the 1970s and 1980s as anxiety about waste increased. Plastic became a special target because, while so many plastic products are disposable, plastic lasts forever in the environment. It was the plastics industry that offered recycling as a solution. In the 1980s the plastics industry led an influential drive encouraging municipalities to collect and process recyclable materials as part of their waste-management systems. However, recycling is far from perfect, and most plastics still end up in landfills or in the environment. Grocery-store plastic bags have become a target for activists looking to ban one-use, disposable plastics, and several American cities have already passed bag bans. The ultimate symbol of the problem of plastic waste is the Great Pacific Garbage Patch, which has often been described as a swirl of plastic garbage the size of Texas floating in the Pacific Ocean. The reputation of plastics has suffered further thanks to a growing concern about the potential threat they pose to human health. These concerns focus on the additives (such as the muchdiscussed bisphenol A [BPA] and a class of chemicals called phthalates) that go into plastics during the manufacturing process, making them more flexible, durable, and transparent. Some scientists and members of the public are concerned about evidence that these chemicals leach out of plastics and into our food, water, and bodies. In very high doses these chemicals can disrupt the endocrine (or hormonal) system. Researchers worry particularly about the effects of these chemicals on children and what continued accumulation means for future generation

The same desirable characteristics that make polymers popular materials for consumer products— durability, strength, and lack of reactivity—also contribute to environmental problems. Polymers do not degrade readily, and as a result, billions of pounds of polymers end up in landfills every year. Estimates suggest that synthetic polymers comprise 11% of solid municipal waste, 30% of which comes from packaging materials.

Two solutions to address the waste problem created by polymers are recycling existing polymer types to make new materials, and using biodegradable polymers that will decompose in a finite and limited time span.

The most environmentally friendly alternative for plastic waste disposal - is the process by which we can re-utilize the energy content of the polymer in an ecologically acceptable way. The other two alternatives are Land filling, and Incineration, which have, amongst others, the following constraints, especially because of increasing rapid accumulation of plastic wastes:

|  | - Lack of adequate and suitable sites for landfilling. |
| --- | --- |
|  | - The feared toxic emissions from inadequate equipment and inappropriate incineration conditions, and the resultant public resistance. |

There are some ISO standards that pertain to recycling too.For environmental management control there is ISO 14001:2004 and for plastics there is ISO 15270:2008.

- History of Recycling

Recycling is not a new concept. The practice of recycling has been around for thousands of years. However, it has been affected predominantly by supply and demand, much as it is today. Recycling has a history that dates back to the historic times. As early as 400 BC (and even earlier), people have been recycling.

For example, archaeological evidence indicates that glass from the imperial Byzantine times was being recycled in the ancient city of Sagalassos, located in current day Turkey. There is also evidence that early Romans recycled bronze coins into statues that could be sold at a higher monetary value than the original coins. In hard times (eg. wartime), metals from everything like jewelry and coins were being melted for weapons or other necessary goods. Pottery recycling operations have been uncovered as well. Archaeologist also deduced from waste remnants about the history of recycling – that recycling was a popular practice during times of distress. For example, less waste remains were found where there were also other indicators of distress such as famine, war and widespread illness. During these times of distress, new materials might have been scarce, making the recycling of waste necessary.

As for the history of recycling prior to the industrial revolution, recycling and general household re-using was actually a common place practice.  For example, evidence shows that scrap bronze and other metals were collected in Europe and melted down for perpetual reuse. In Britain, dust and ash from wood and coal fires were being downcycled as a base material in brick making.

In other words, during these times in the history of recycling, recycling was mainly motivated by the economic benefits of using recycled feedstock instead of virgin material. The history of recycling took a turn during the times of industrialization. A highlight in the history of recycling was during World War II.

During the war, financial constraints and massive material shortage due to war efforts made it necessary for our ancestors to reuse goods and recycle materials.

When the war ended, resource conservation programs established during the war were continued in some countries without an abundance of natural resources, such as Japan. However, for other countries such as the USA, recycling efforts were largely forgotten. In the 1940s and 1950s, when landfilling became a cheap way to dispose trash, recycling was less popular.

Nevertheless, in the 1970s, recycling became more popular again and drop-off recycling centers were established. Theenvironmental movementhad started since 1960s, and there was greater public awareness and rising environmental consciousness. The increased interest in recycling in the 1970s was also a result of rising energy costs. Significant saving was achieved through recycling.

- Plastic Identification Code

| A milestone in the history of recycling was the introduction of the universal symbol for recycling (Plastic Identification Code) (Figure 11.1). |  |
| --- | --- |
|  | In the form of a Mobius strip, the symbol was designed by Gary Anderson in the late 1960s, after a Chicago-based recycled-container company sponsored an art contest to raise environmental awareness. Since then, the triangle has been used to represent the recycling hierarchy of reduce, reuse, and recycle. |

This number will be found inside a recycling symbol, (a triangle of arrows), on the container. The symbol with a number inside indicates what kind of plastic resin the container is made from.

Figure 11.1 Plastic Identification Codes

The plastic found in water bottles is numbered as 1. This is a PET type plastic.

Type 2 is HDPE, hard plastic found in dishware.

Type 3 is PVC that is normally found in shampoo bottles or credit cards. Type 4 is LDPE that is commonly found in tote bags and shopping bags.

Type 5 is PP found in bottles, straws and the popular Tupperware too. Type 6 is PS found in compact disk cases.

Type 7 includes all the rest which can range from bulletproof plastics to sunglasses.

Although thousands of different synthetic polymers have now been prepared, six compounds, called the “Big Six”. Each polymer is assigned a recycling code (1–6) that indicates its ease of recycling; the lower the number, the easier to recycle.

Table 11.1 lists these six most common polymers, as well as the type of products made from each recycled polymer. Recycling begins with sorting plastics by type, shredding the plastics into small chips, and washing the chips to remove adhesives and labels. After the chips are dried and any metal caps or rings are removed, the polymer chips are melted and molded for reuse.

Table 11.1 Recyclable Polymers

| Recycling code | Polymer name | Structure | Recycled product |
| --- | --- | --- | --- |
| 1 | PET Polyethylene terephthalate |  | Fleece jackets carpeting plastic bottles |
| 2 | HDPE High-density polyethelene |  | Tyvek insulation sports clothing |
| 3 | PVC Poly (vinyl chloride) |  | Floor mats |
| 4 | LDPE Low-density Polyethelene |  | Trash bags |
| 5 | PP Polypropylene |  | Furniture |
| 6 | PS Polystyrene |  | Molded trays trash cans |

Of the Big Six, only the polyethylene terephthalate (PET) in soft drink bottles and the highdensity polyethylene (HDPE) in milk jugs and juice bottles are recycled to any great extent.

Since recycled polymers are often still contaminated with small amounts of adhesives and other materials, these recycled polymers are generally not used for storing food or drink products.

Recycled HDPE is converted to Tyvek, an insulating wrap used in new housing construction, and recycled PET is used to make fibers for fleece clothing and carpeting.

An alternative recycling process is to re-convert polymers back to the monomers from which they were made, a process that has been successful with acyl compounds that contain C – O orC– N bonds in the polymer backbone. For example, heating polyethylene terephthalate with CH3OH cleaves the esters of the polymer chain to give ethylene glycol (HOCH2CH2OH) and dimethyl terephthalate. These monomers then serve as starting materials for more PET.

The ease of recycling the various types of plastic differs.

| Type 1 plastic (PET, or PETE) and | are easy to recycle and poses low risk of leaching breakdown products. |
| --- | --- |
| Type 2 plastic (HDPE) |  |
| Type 3 plastic (PVC) | contains chlorine, and hence, in its manufacture, as well as its disposal (eg. incineration), highly dangerous and toxic gases are released. Hence, type 3 plastic is rarely recycled. |
| Type 4 plastic (LDPE) | are historically not accepted by most American curbside recycling programs. Nevertheless, more and more communities are starting to accept it these days. |
| Type 5 plastic (PP) | are also gradually becoming more accepted by recyclers. |
| Type 6 plastic (PS), such as Styrofoam | leach toxins and are very difficult to recycle. |
| Given the high cost of recycling, type 3 to 7 plastics are rarely recycled. |  |

- Plastic Recycling Process

The 5-Step Process for Plastic Recycling is shown on (Figure 11.2).

- Collection– The recycling facilities gather available recyclable plastic material in their area, such as from roadsidecollections, special recycling bins, or even directly from industries. In this way, both post-consumer and post-industrial plastic items are collected.

- Manual sorting– All plastic items that are collected are then sorted according to the various plastic types indicated by theplastic recycling symbols and codeson them. Unwanted non-plastic materials found in the piles are promptly taken out.

Figure 11.2 The 5-Step Process for Plastic Recycling

- Chipping– After sorting, the sorted plastic products are prepared for melting by being cut into small pieces. The plastic items are fed into a machine which has sets of blades that slice through the material and break the plastic into tiny bits.

- Washing– At this step in the process of recycling plastic, all residue of products originally contained in the plastic items and various other ‘contaminants’ (e.g. paper labels, dirt) are removed. A particular wash solution consisting of an alkaline, cationic detergent and water is used to get rid of all the contaminants effectively on the plastic material, making sure that all the plastic bits are clean and ready for the final step.

During washing, the wash tank agitator serves as an abrasive, stripping the adhesive off any labels and shredding any paper mixed in with the plastics. The alkaline, cationic detergent (which is similar to the formulas used in shampoos and fabric softeners) is used because plastic materials have a positive surface charge, and only positively-charged chemical compounds (which in this case are cationic detergents) can properly clean them, and effectively remove dirt and grease from the positively charged plastic surfaces.

- Pelleting– The cleaned and chipped pieces of plastic are then melted down and put through a machine called an ‘extruder’ in this stage of the recycling plastic process. The extruder shapes the melted plastic into thin noodle-like tubes. Then the plastic tubes are cut into small pellets by a set of rotating knives. The pellets are then ready to be reused and remade into new items.

Processing of Reusable Plastics: The reusable and more homogenous material is finally packed and piled before being forwarded to appropriate processing plants. There are two essential prerequisites for high-quality recycling of plastics: according to the plastic type: 1) the material has to be sorted properly and 2) it has to be free of contaminants.

Before being introduced back into the production line for the assemblage of new packaging material, it is shredded into tiny pellets and according to its colour separated automatically. Based on the qualitative requirements, a distinct fraction is mixed with prime material to maintain the qualitative properties of the final product; i.e. in general not more than 50% of recycled plastics are mixed to the virgin plastic; doing so avoids major changes in the chemo-physical properties of the product (Figure 11.3).

Figure 11.3 Processing Plant of Recycled Plastic

When plastics cannot be sustainably recycled such non-recyclable plastics provides a valuable energy resource for advanced thermal process; contributing to energy security and displacing virgin fossils fuels (Figure 11.4).

Figure 11.4 Minicipal Solid Waste (MSW) Co-combustion Process

- Summary of Recycling. Ten 10 Reasons to Recycle are:

- Recycling saves trees.

- Recycling protects wildlife habitat and biodiversity.

- Recycling lowers the use of toxic chemicals.

- Recycling helps curb global warming.

- Recycling stems the flow of water pollution.

- Recycling reduces the need for landfills.

- Recycling reduces the need for incinerators.

- Recycling creates jobs and promotes economic development.

- Cities may profit by selling recyclables.

- Buying recycled products contributes to the demand for more recycled products.

References

- Sepour / Carraher's Polymer Chemistry: Sixth Edition, Revised and Expanded, Charles E Carraher, Jr, 2003, by Marcel Dekker, Inc., 902 p.

- Urazbayeva K.A. Selective chapters of organic chemistry: polymer chemistry: study guide / K. A. Urazbayeva, S. K. Iskakova. - Shymkent: Alem, 2015. - 196 с.

- Тасанбаева Н.Е., Мамытова Г.Ж., Сақыбаева С.Ә., Полимерлердің химиясы мен физикасы. – Шымкент.: М.Әуезов атындағы ОҚМУ, 2005ж. -208б.

- Тасанбаева Н.Е., Мамытова Г.Ж., Сакибаева С.Ә., Полимерлердің химиясы мен физикасы. 2 бөлім. Шымкент.: М.Әуезов атындағы ОҚМУ, 2014ж. -200б.

- Сутягин В.М., Бондалетова Л.И. С 90 Химия и физика полимеров: Учебное пособие. – Томск: Изд-во ТПУ, 2003. – 208 с.

- Кулезнев В.Н., Шершнев В.А. Химия и физика полимеров.- 2-е изд., перераб. и доп. - М.: КолосС,2007. -367с.

- Киреев В.В. Высокомолекулярные соединения: учебник для бакалавров. - М.: Издательство Юрайт, 2013. -602с.

- Тагер А.А. Физикохимия полимеров,4-е изд., перераб. и доп. Учеб. пособие для хим. фак. ун-тов / А. А. Тагер; под ред. А. А. Аскадского. - М.: Научный мир, 2007. - 573с.

- Аскадский А.А.  Введение в физикохимиюполимеров: учебник для студ. и аспирантов физических и химических спец. / А. А. Аскадский, А. Р. Хохлов. - М.: Научный мир, 2009. - 384 с.: 163 ил.

- Тасекеев М.С.  Производство биополимеров как один из путей решения проблем экологии и АПК / М. С. Тасекеев, Л. М. Еремеева; Нац. центр научно- тех. информации. - Алматы: НЦ НТИ, 2009. - 200

- Ф. Ш. Вильданов, Ф. Н. Латыпова, П. А. Красуцкий, Р. Р. Чанышев Биоразлагаемые полимеры – современное состояние и перспективы использования / Башкирский химический журнал. 2012. Том 19. № 1 С.135-139

- Курманбаева К Биоразлагаемая упаковка как один из путей решения проблем экологии/ Вопросы студенческой науки Выпуск №4 (20), апрель 2018- С.17-21

- Katarzyna Leja, Grażyna LewandowiczPolymer Biodegradation and Biodegradable Polymers - a Review/ Polish J. of Environ. Stud. Vol. 19, No. 2 (2010), 255-266

- Handbook of Biodegradable Polymers, 2nd Edition A complete guide to the subject of biodegradable polymers / Edited by Catia Bastioli, Novamont published 2014 704 pages.

- Applied plastic engineering handbook. Processing and Materials /Edited by Myer Kutz -2011, Elsevier Inc

- Encyclopedia of chemistry. Don Rittner and Ronald Bailey, 2005

- Smith, Janish G. Organic chemistry/ Janish G. Smith. -3nd ed. - 2011 by The McGraw-Hill Companies, Inc.

- Jan W. Gooch (Ed.) Encyclopedic Dictionary of Polymers: With 710 Figures and 38 Tables, 2007, Springer Science+Business Media, LLC. - 1256 p

- Giulio Natta and the Development ofStereoselective Propene PolymerizationVincenzo Busico Adv Polym Sci (2013)

- Bioplastics: Its Timeline Based Scenario & Challenges.Swati Pathak,. CLR Sneha, Blessy Baby Mathew.  // Journal of Polymer and Biopolymer Physics Chemistry, 2014, Vol. 2, No. 4, 84-90

- Basics of Polymers: Fabrication and Processing Technology Copyright © Momentum Press®, LLC, 2015.

- Polylactic Acid TechnologyDavid E. Henton, Patrick Gruber, Jim Lunt, and Jed RandallB Natural Fibers, Biopolymers, and Biocomposites Natural Fibers

- Aguilar MR, Elvira C, Gallardo A, Vázquez B, Román JS. Smart polymers and their applications as biomaterials / Topics in Tissue Engineering, Eds. N Ashammakhi, R Reis & E Chiellini. - 2007;3. - 27p

- L. Peponi, M.P. Arrieta, A. Mujica-Garcia, D. López. 6 Smart Polymers / Modification of Polymer Properties – Chapter – 2017. P.131-154

- Ipsita Roy and Munishwar Nath Gupta. Smart Polymeric Materials: Emerging Biochemical Applications. Review / Chemistry & Biology, Vol. 10, Issue 12. December 2003. -  P. 1161–1171

- Sera Erkeçoğlu, Ali Demir Sezer and Seyda Bucak. Smart Delivery Systems with Shape Memory and Self-Folding Polymers. Chapter 1/ Smart Drug Delivery System – Chapter, 2016. - 31 p.

Appendices

Appendix 1 – CLOSSARY of POLYMERS

| Полимерлеу реакциясы нәтижесінде түзілген жоғары молекулалы қосылыстарды полимерлер дейді. | Polymer is a large molecule composed of smaller monomer units covalently bonded to each other in a repeating pattern. | Полимер -высокомолекулярные соединения, образующиеся при полимеризации. |
| --- | --- | --- |
| Мономерлер – полимерлеу реакциясына түсетін молекула. | Monomers are small organic compounds that can be covalently bonded to each other (polymerized) in a repeating pattern. | Мономер - молекула, вступающая в реакцию полимеризации. |
| Полимерлеу деп қанықпаған көмірсутектер молекулаларының π-байланыстарының үзілу нәтижесінде бір-бірімен қосылып жаңа -байланыс түзетін химиялық процессті айтады. | Polymerization is formation of high molecular substance (polymer) molecules by repeated addition of low-molecular substance (monomer) to the active centers in the growing polymer molecule. | Полимеризация - химический процесс, в котором молекулы ненасыщенного углеводорода присоединяются одна к другой за счет разрыва π-связей и образования новых -связей. |
| Ионды -координациялық полимерлеуде металорганикалық қосылыстардың әрекетімен жүреді, көбірек Циглер-Натта катализаторы - (C5H5)3Al + TiCl4 қолданылады. | Coordination polymerization. A polymerization reaction that uses a homogeneous catalyst that is soluble in the reaction solvents typically used. | Ионно-координационная полимеризация также протекает под действием металлорганических соедине- ний, чаще всего катализатора Циглера-Натта (C5H5)3Al + TiCl4. |
| Аддициондық полимер – қанықпаған қосылысты полимер тізбегінің өсіп келе жатқан аяғына қосу арқылы түзілетін полимер. | Addition polymer is a polymer prepared by a chain reaction that adds a monomer to the growing end of a polymer chain. Addition polymers are also called chain-growth polymers. | Аддиционный полимер – полимер, получаемый по цепной реакциипоследовательным присоединением ненасыщенного соединения к растущему концу полимерной цепи. |
| Атактикалық полимер – орынбасарлары негізгі полимер тізбегінің екі жағына тәртіпсіз (жүйесіз) орналасқан полимер; стереоретсіз полимер. Радикальды және ионнды полимерлеуде кездеседі. | Atactic polymer is polymer having the substituents randomly oriented along the carbon backbone of an elongated polymer chain. | Атактический полимер – полимер, в котором заместители расположена беспорядочно по обе стороны основной полимерной цепи; нестреорегулярный полимер. Встречается в радикальной и ионной полимеризации. |
| Синдиотактический полимер – негізгі полимер тізбегінің көміртек атомдарынын орынбасарлары кезектесіп тізбектің екі жағына бірдей орналасқан. | Syndiotactic polymer is polymer having the substit uents alternating from one side of the backbone of an elongated polymer chain to the other. | Синдиотактический полимер - это полимер, в котором заместители у атомов углерода основной полимерной цепи расположены регулярно попеременно то по одну, то по другую сторону цепи. |
| Изотактикалық полимер – орынбасарлары полимер тізбегінің бір жағына орналасқан полимер; стереоретті полимер ионнды-координациялық полимерлеуде кездеседі. | Isotactic polymer is polymer having all the substituents on the same side of the carbon backbone of an elongated polymer chain. | Изотактический полимер – полимер, в котором заместители расположены по одну сторону полимерной цепи; стереорегулярный полимер. Встречается в ионно-координационной полимеризации. |
| Конденсациялық полимер - екі әртүрлі бифункционалды органикалық қосылыстардың конденсациялау реакциясынан түзілген полимер | Condensation polymer is polymer formed when monomers containing two functional groups come together with producing by-products such as water or HC1. Condensation polymers are also called step-growth polymers. | Конденсационный полимер – полимер, образованный по реакции конденсации из двух различных бифунциональных органическихсоединений. |
| Гетерополимер - әр түрлі мономерлерден алынған полимер. | Heteropolymer (orCopolymer) is polymer prepared from different monomers. | Гетерополимер – полимер, полученный из различных мономеров. |
| Гомополимер – екі бірдей мономерлерден алынған полимер. | Homopolymer is polymer prepared from a single monomer. Homopolymerization is identical polymerization of the monomers; | Гомополимер – полимер, полученный из одинаковых мономеров. |
| Биоыдырау полимері – қалыпты жағдайда микроорганизмдердің әрекетінен ыдырауға ыңғайлы полимер. | Biodegradable polymer is polymer that can be degraded by microorganisms naturally present in the environment. | Биоразлагаемый полимер – полимер, которыйспособен разлагаться в природных условиях под действием микроорганизмов. |

Appendix 2 HISTORY of PLASTICS

### Timeline Precursors

1839– Natural Rubber- method of processing invented by Charles Goodyear

1843–Vulcunite- Thomas Hancock 1843 - Gutta-Percha - William Montgomerie

1856 - Shellac - Alfred Critchlow, Samuel Peck 1856 - Bois Durci("hardened wood") - Francois Charles Lepage

### Timeline - Beginning of the Plastic Era with Semi Synthetics

1839–Polystyreneor PS discovered - Eduard Simon

1862 - Parkesine - Alexander Parkes

1863 - Cellulose Nitrate or Celluloid - John Wesley Hyatt

1872 – Polymer Polyvinyl Chlorideor PVC - first created by Eugen Baumann

1894 –Viscose Rayon- Charles Frederick Cross, Edward John Bevan

### Timeline - Thermosetting Plastics and Thermoplastics

1908 –Cellophane- Jacques E. Brandenberger

1909 - First true plastic Phenol-Formaldehyde tradenamed Bakelite - Leo Hendrik Baekeland

1926 –Vinyl or PVC- Walter Semon invented a plasticized PVC

1927- Cellulose Acetate -DuPont Company began production of acetate fibre in the United States.

1933 –Polyvinylidene chloride or Saran also called PVDC - accidentally discovered by Ralph Wiley, a Dow Chemical lab worker

1935 - Low-density polyethylene or LDPE - Reginald Gibson and Eric Fawcett

1936 - Acrylic or Polymethyl Methacrylate-Imperial Chemical Industries (ICI), now Lucite International began the first commercially viable production of acrylic safety glass

1937–Polyurethanes tradenamed Igamid for plastics materials and Perlon for fibers. - Otto Bayer and co-workers discovered and patented the chemistry of polyurethanes

1938 –Polystyrenemade practical 1938 - Polytetrafluoroethylene or PTFEtrade named Teflon- Roy Plunkett

1939 Nylon and Neoprene considered a replacement for silk and a synthetic rubber respectively Wallace HumeCarothers

1941 –Polyethylene Terephthalateor Pet - Whinfield and Dickson

1942- Low Density Polyethylene 1942 – Unsaturated Polyesteralso called PET patented by John Rex Whinfield and James Tennant Dickson

1951 – High-density polyethylene or HDPE trade nasme Marlex- Paul Hogan and Robert Banks 1951 – Polypropylene or PP- Paul Hogan and Robert Banks

1953– Saran Wrap introduced by Dow Chemicals

1954 – Styrofoam a type of foamed polystyrene foam was invented by Otis Ray McIntire for Dow Chemicals

### Hermann Staudinger: Father of Macromolecular Chemistry. Hermann Staudinger (1881-1965) German chemist. ### Nobel Prize Laureate ### for Chemistry (1953 ). Hermann Staudinger’s pioneering theorieson the polymer structures of fibers and plastics and his later research on biological macromolecules formed the basis for countless modern developments in the fields of materials science and biosciences and supported the rapid growth of the plastics industry. For his work in the field of polymers, Staudinger was awarded the Nobel Prize for chemistry in 1953.. In 1920, Hermann Staudinger, then professor of organic chemistry at the Eigenössische Technische Hochschule in Zurich, created a stir in the international chemical community when he postulated that materials such as natural rubber have very high molecular weights. In a paper entitled "Über Polymerisation," Staudinger presented several reactions that form high molecular weight molecules by linking together a large number of small molecules. During this reaction, which he called "polymerization," individual repeating units are joined together by covalent bonds. Hermann Staudinger early in his career. This new concept, referred to as "macromolecules" by Staudinger in 1922, covered both synthetic and natural polymers and was the key to a wide range of modern polymeric materials and innovative applications. Today, the molecular architectures of synthetic polymers and biopolymers are tailored with high precision to meet the demands of modern technology.The products of polymer chemistry are diverse, from food packaging, textile fibers, auto parts and toys, to membranes for water desalination, carriers used in controlled drug release and biopolymers for tissue engineeringStaudinger's concept, however, represented a strong challenge to his contemporaries. The scientific community was very reluctant to admit the existence of extremely large compounds with molecular weights exceeding 5000. Instead, micelle-type aggregates, as observed for soap molecules, were considered to account for the unusual properties of such materials. Moreover, some scientists were convinced that the size of a molecule could never exceed the size of the unit cell, as measured by X-ray crystallography. Staudinger, following the scientific tradition of classical organic chemistry, presented sound experimental evidence to support the existence of high molecular weight polymers. He selected natural rubber as the model system because Carl Harries and Rudolf Pummerer had suggested independently that natural rubber consisted of aggregated small cyclic polyisoprene units via "partial valencies" associated with the double bonds. Such aggregates should have been destroyed when the double bonds were removed by hydrogenation. Staudinger's hydrogenation experiments showed that hydrogenated rubber was very similar to normal unsaturated rubber. During the late 1920s, Staudinger provided additional evidence based on viscometry to confirm that molecular weights remained unchanged during chemical modification of polymers. Despite the impressive experimental evidence, Staudinger continued to encounter very strong opposition from leading organic chemists for nearly two decades. For instance, Heinrich Wieland, 1927 Nobel laureate in chemistry, wrote to Staudinger, "Dear colleague, drop the idea of large molecules; organic molecules with a molecular weight higher than 5000 do not exist. Purify your products, such as rubber, then they will crystallize and prove to be low molecular compounds!" In his autobiography, Staudinger commented: "My colleagues were very skeptical about this change, and those who knew my publications in the field of low molecular chemistry asked me why I was neglecting this interesting field and instead was working on a very unpleasant field and poorly defined compounds, like rubber and synthetic polymers. At that time the chemistry of these compounds often was designated, in view of their properties, as Schmierenchemie ('grease chemistry')." Staudinger never ceased to promote his concepts of polymer sciences, despite his colleagues' mistrust of many of his methods and results. In lively discussions, he eloquently defended his ideas against all attacks using his ingenuity, persistence and pronounced enthusiasm. By the end of the 1920s and during the 1930s, Staudinger's macromolecular concept found increasing acceptance by other chemists. Although some of his opponents still maintained their objections, his concept was already being applied in industrial processes. At long last, on December 10, 1953, Staudinger received his reward for the concept of macromolecules and his prolonged effort to establish the science of large molecules when he was awarded the Nobel Prize for chemistry.. 1955 - First production of high density polyethylene in UK 1956 - Reliant Regal 111, first commercially successful all glass-reinforced-plastic bodied car goes on sale 1956 - DuPont files patents for first acetals (POM) 1957 - First production of polypropylene by Montecatini using Ziegler-Natta catalysts 1958 - First production of polycarbonates (Bayer and General Electric) 1958 - Lego patents its stud and block coupling system and produces toys of cellulose acetate, later Acrylonitrile- butadiene-styrene polymer. 1959 - Barbie Doll unveiled by Mattel at American International Toy Fair Early 1960s - introduction of water based acrylic paints 1960 - Ethylene-vinyl acetate co-polymers launched by DuPont 1962 - DuPont launches polyimide films and varnishes 1962 - Silicone gel breast implants pioneered successfully 1964 – Polyimide 1965 - Styrene-butadiene block copolymers 1965 - Kevlar® is first developed by DuPont 1966 - Blow moulding of fuel tanks introduced 1966 - Liquid crystals 1967 - Polyvinyl chloride (PVC) ‘Blow’ chair designed by Scolari, De Pas and Lomazzifor manufactured by Znaotta 1969 - Neil Armstrong plants a nylon flag on the moon. 1970 - Poly(butylene terephthalate) 1970 – Thermoplastic Polyesterthis includes trademarked Dacron, Mylar, Melinex, Teijin, and Tetoron 1970 - First Yellow HDPE pressure pipes for gas introduced into UK by Wavin/British Gas. 1973 - Polyethylene terephthalate beverage bottles introduced 1974 - Polyacetylene 1976 - Plastics in its great variety of forms becomes the most used type of material in the world 1977 - Polyaryletheretherketone (PEEK) was first prepared by ICI 1978 - Linear Low Density Polyethylene 1979 - Introduction of first commercial mobile/ portable ‘phones 1979 - First PVC-U double glazed windows installed 1980s & 90s - High Performance Plastics 1980 - First production of linear low density polyethylene 1980 - First Blue HDPE pressure pipes for potable water introduced into UK. 1982 - First artificial heart made mainly of polyurethane, introduced implanted in a human. 1983 - The slim plastic Swatch watch made of 51 mainly plastic components 1983 - ICI and Bayer launch PEEK, PPS (polyphenyene sulphide), and PES (polyether sulphone) 1987 - BASF in Germany produces a polyacetylene that has twice the electrical conductivity of copper. 1988 - Introduction of triangular recycling symbols relating to plastic 1989 - First light-emitting polymers (poly-ethyne) discovered in Cambridge 1989 - The Gravimetric Batch Blender is invented by Steve Maguire revolutionising the industry and bringing affordable gravimetric blending to processors 1990 - ICI launches Biopol, the first commercially available biodegradable plastics 1991 - Dyson’s vacuum cleaner launched in Japan 1994 - Smart car with lightweight flexible integrally coloured polycarbonate panels introduced 1998 - Free standing Zanussi Oz fridge, with insulation and outer skins made in one process from polyurethane foam introduced 2000 - 2010 - Nano Technology, Airbus A380, iPod 2000s Nano-Technology applied to polymer and composit applications 2000 - First commercial metallocene catalysed polyolefins introduced. 2001 - iPod dreamed up by Tony Fadell, an independent inventor, developed by Apple Computers 2005 - NASA explores the advantages of a polyethylene based material RFX1, as the material for the spaceship that will send man to Mars 2005 - Polycond project established to look at the potential of conductive polymers 2008 - Airbus 380, comprising 22% carbon-fibre reinforced plastics flies into Heathrow 2009 - Boeing 787 (nicknames 'Boeing's Plastic Dream') comes into service, its skin is made up of 100% Plastic composites with plastic making up 50% of all materials in the plane. 2010 + - Plastics fit for the Future Bullet Proof Polymer - Scientists at Rice University, Texas have created a new super polymer material that can stop a 9mm bullet and seal the hole behind it Plastics Blood - Developed by the University of Sheffield to mimic haemoglobin, for use in trauma situations where blood is needed quickly Plastic Solar Cells - A polymer solar cell that can produce electricity from sunlight by the photovoltaic effect provides a lightweight, disposable and inexpensive alternative to traditional solar panels Implantable Polymers - Medical grade and implantable biomaterials such as PEEK will be used in neurological applications to help control epilepsy, Parkinson’s disease and brain trauma Commercial - Space Flights Lightweight carbon composite materials will be crucial in the realisation of sub-orbital tourist spaceflights 3D Printed - Body Parts Using plastic materials such as PMMA car parts can be printed at home and doctors can produce replica livers or kidneys for transplant patients Flexible Plastic Screens - Organic light-emitting diodes are placed on plastic foil to create electronic devices with flexible displays Driverless Cars - In the future all driverless vehicles will be almost entirely constructed from plastic parts due to the light weighting properties they provide. (from https://www.bpf.co.uk/plastipedia/plastics_history/Default.aspx)

Appendix 3 – NOMENCLATURE of POLYMERS

rational nomenclature, or

Nomenclature, based on the monomer name

Most polymer names used by polymer scientists are source-based; i.e., they are based on the common name of the reactant monomer, preceded by the prefix “poly.”

For example, polystyrene is the most frequently used name for the polymer derived from the monomer 1-phenylethene, which has the common name styrene.

The vast majority of polymers based on the vinyl group (CH2=CHX) or the vinylidene group (CH2=CX2) as the repeat unit are known by their source-based names. For example, polyethylene is derived from the monomer ethylene, poly(vinyl chloride) from the monomer vinyl chloride, and poly(methyl methacrylate) from methyl methacrylate:

Many condensation polymers are also named in this manner. In the case of poly(ethylene terephthalate), the glycol portion of the name of the monomer, ethylene glycol, is used in constructing the polymer name, so that the name is actually a hybrid of a sourcebased and a structure-based name.

In the case of poly(ethylene terephthalate), the glycol portion of the name of the monomer, ethylene glycol, is used in constructing the polymer name, so that the name is actually a hybrid of a sourcebased and a structure-based name.

This polymer is well known by trade names, such as Dacron, or its common grouping, polyester.

So, Name is formed:

- Prefix "poly" + name of monomer (polystyrene, polypropylene, etc.)

- The name of the polymer is written together or in parentheses (if the name of the monomer is a compound word - (poly (vinyl acetate), poly (methyl methacrylate), etc.).

However, this nomenclature is not very successful, since one and the same monomer can form polymers of different structures, and the same polymer can be formed from monomers of different structures.

Examples: The name "poly (ethylene oxide)" can reflect the following structures:

The macromolecule of a polymer, commonly called polyethylene, can be obtained not only by polymerization of ethylene (path 1), but also by a number of other reactions (paths 2-4).

Copolymers are composed of two or more monomer units. Source-based names are conveniently used to describe copolymers by using an appropriate term between the names of the monomers. Any of a half dozen or so connecting terms may be used, depending on what is known about the structure of the copolymer. When no information is specified about the sequence of monomer units in the copolymer, the connective term co is used in the general format poly(A-co-B), where A and B are the names of the two monomers. An unspecified copolymer of styrene and methyl methacrylate would be called poly[styrene-co-(methyl methacrylate)]. Kraton, the yellow rubber-like material on the bottom of many running shoes, is an example of a copolymer about which structural information is available. It is formed from a group of styrene units, i.e., a “block” of polystyrene, attached to a group of butadiene units, or a block of polybutadiene, which is attached to another block of polystyrene forming a triblock copolymer. The general representation of such a block copolymer is —AAAAABBBBBAAAAA—, where each A or B represents an individual monomer unit. The proper source-based name for Kraton is polystyrene-block-polybutadiene-blockpolystyrene, with the prefix “poly” being retained for each block.

Random nomenclature:Trade (and/or brand) names

There are no regularities in names formation.For examples:

- Lavsan, in USSR (Terylene,in Great Britain; Dacron, in the USA;Mylar, corporation DuPont) - poly (ethylene terephthalate)

- Vinyl plastic (PVC) - poly (vinyl chloride)

- Teflon, corporation DuPont (fluoroplast-4) - poly (tetrafluoroethylene)

-Plexiglas (organic glass) -poly (methyl methacrylate)

- Profax, Polyurgo (USA); Danlay, Donbond (Japan), and the United Kingdom (Polypropylene).

Trade (and/or brand) names and abbreviations are often used to describe materials. They may be used to identify the product of a manufacturer, processor or fabricator and may be associated with a particular product or with a material or modified material. Trade names, Brand names, and Abbreviations is presented in Table  .

Table  Abbreviations for Selected Polymeric Materials

Copyright © 2003 by Marcel Dekker, Inc. All Rights Reserved.

Trade names are used to describe specific groups of materials that are produced by a specific company or under licence of that company. Abbreviations, generally initials in capital letters, are also employed to describe materials. Table  contains a listing of some of the more widely employed abbreviations and the polymer associated with the abbreviation.

Appendix 4 – POLYMERS CONCEPT MAP

From: Chem1General Chemistry Virtual Textbook → States&Solids → Polymers

Appendix 5 Uses of Plastics

| Polymer name | Polymer formula |  | Use-end |
| --- | --- | --- | --- |
| Application area: House cosiness |  |  |  |
| Polyvinylchloride |  |  | Windows, doors, shutters |
| Polystyrene |  |  | Wall Insulation |
| Polystyrene |  |  | Boxes for CDs |
| Polypropylene body, |  |  | Markers |
| Nylon rod |  |  |  |
| Polypropylene |  |  | Carpet covering |
| Acrylic (ACM) (alkyl acrylate copolymer) |  |  |  |
| Nylon |  |  |  |
| fiber PET |  |  |  |
| Filler- foamed Polystyrene |  |  | Beanbag chair |
| Polyurethane foam |  |  | Mattress |
| Latex |  |  |  |
| Polyester fibers |  |  | Filler for blankets, pillows |
| Application area: Tourism and Active relaxation |  |  |  |
| Rubber |  |  | Bicycle tires |
| PET |  |  | Water bottles |
| Polyamide |  |  | Sportswear |
| fiber PET |  |  |  |
| Inside-Polystyrene |  |  | Helmet |
| outside -ABS-plastic |  |  |  |
| Polyuretane, termoelasts |  |  | Shoes |
| Polyamide |  |  | Backpack |
| Polyamide |  |  | Sleeping bag |
| Polyester |  |  |  |
| Polyethylene foam |  |  | Rug tourist |
| Nylon, |  |  | Tent |
| Polyurethane |  |  |  |
| Application area: Movement and comfort |  |  |  |
| Polypropylene |  | Elements of interior casing of rugs, battery cases |  |
| Elastic Polyurethane foam, |  | Car seat |  |
| PVC |  |  |  |
| ABS-plastic |  | Dashboard |  |
| Nylon |  | Airbags |  |
| Rubber |  | Tires |  |
| Thermoplastic polymeric additive to bitumen, plasticizers |  | Asphalt |  |
| Polypropelene |  | Road embankment |  |
| Termoplastic |  | Carriageway marking |  |
| PVC |  | Light reflectors |  |
| Application area: Working and connection |  |  |  |
| Nylon |  |  | Inner trim the plane |
| ABS-plastic |  |  |  |
| PVC |  |  |  |
| Polystyrene, , |  |  | Flight Catering (package) |
| PET |  |  |  |
| BOPP film |  |  |  |
| Etylene glycol |  |  | Deicing fluid |
| Acrylic (ACM) (alkyl acrylate copolymer) |  |  | Illuminators |
| Polystyrene, |  |  | The body of the computer and phone |
| ABS-plastic |  |  |  |
| Application area: Working and connection |  |  |  |
| Nylon |  |  | Inner trim the plane |
| ABS-plastic, |  |  |  |
| PVC |  |  |  |
| Polystyrene, |  |  | Flight Catering (package) |
| PET |  |  |  |
| BOPP film |  |  |  |
| Etylene glycol |  |  | Deicing fluid |
| Acrylic (ACM) (alkyl acrylate copolymer) |  |  | Illuminators |
| Polystyrene, |  |  | The body of the computer and phone |
| ABS-plastic |  |  |  |
| Application area: Storage of food products |  |  |  |
| Polypropylene composite |  |  | The body of the refrigerator |
| Polysterene |  |  | Shelves |
| Polycarbonate |  |  | Boxes for fruits and vegetables |
| Polypropylene film |  |  | Packaging of bread |
| Polyethylene |  |  | Packages for vegetables |
| PET |  |  | Plastic bottles |
| Polystyrene |  |  | Disposable cups, trays |
| Polypropylene laminates |  |  | Flexiblepackaging ketchup, mayonnaise |
| Why Are Plastics Used in Packaging? | Because they are light, resistant, air- and watertight, and inert, i.e. they do not react with the bodies they are in contact with. Plastics can be soft or stiff, formable or brittle, clear or opaque depending on the needs. Additionally, plastics are also easy to process. |  |  |
| Application area: Agriculture |  |  |  |
| Cellular polycarbonate |  |  | Greenhouse |
| Polypropylene |  |  | drain fiber |
| Polyethylene |  |  | Covering materials |
| Polypropylene |  |  | Pots for seedlings |
| Polyethylene/ PVC | / |  | Pipes of irrigation system |
| PVC, Polyethylene | / |  | Hoses |
| PVC or |  |  | Rubber boots, gloves |
| Synthetic rubber |  |  |  |
| Polyethylene |  |  | Drums, cans, containers, watering cans, buckets |
| Polypropylene |  |  |  |
| Application area: Science and medicine |  |  |  |
| ABS-plastic |  |  | Cases of devices |
| Polyethylene |  |  | Disposable tubes |
| Polypropylene |  |  | The body of the dispenser |
| Polycarbonate |  |  | Protective glasses |
| Synthetic latex |  |  | Gloves |
| Polystyrene |  |  | Rack for tubes |
| PET fiber |  |  | protective gown |
| Polyethylene |  |  | Shoe covers, protective caps |
| Application area: Sports |  |  |  |
| Polyethylene |  |  | The body of kayak |
| PVC |  |  | Kayaking protective skirt |
| PVC |  |  | The body of raft, kayak |
| Polyethylene |  |  | The blades of the paddles |
| Polyamide, |  |  | Life jacket |
| Foamed polystyrene |  |  |  |
| Casing helmet- Polycarbonate composite |  |  | Helmet |
| Helmet lining-Polystyrene foam, |  |  |  |
| Polyurethanes |  |  |  |
| Neoprene, |  |  | Wetsuit |
| Polyurethane |  |  |  |
| PET fiber |  |  | Sport Insulated clothing |

Appendix 5 BIOPLASTIC LIFECYCLE

Svetlana ISKAKOVA

Saule SAKIBAYEVA

gulnara Mamutova

Aziza Issa

CHEMISTRY and PHYSICS of POLYMERS

STUDYGUIDE

Signed to print

Paper size 60 * 84 1/16

Typographical paper. Offset printing. The volume of 11,0  p.p.

Circulation ___. Copies. Order number ____

__

© Edition of M. Auezov South Kazakhstan State University

Publishing Center of M.Auezov SKSU, Shymkent, 5 Tauke Khan Ave