F. 7.03- 03

MINISTRY OF EDUCATION AND SCIENCE OF THE REPUBLIC OF KAZAKHSTAN

M. AUEZOV SOUTH KAZAKHSTAN STATE UNIVERSITY

High School of Chemical Engineering and Biotechnology

Department of Chemical Technology of Inorganic Substances

Таubayeva А.S., Kambarova G.A

lecture notes to the discipline

«Theoretical bases of processing of mineral and technogenic raw materials»

for students of a specialty 5В072000 – Chemical technology of inorganic substances (6B071 Engineering and engineering work, EP 6B07160- Chemical Technology of Inorganic Substances)

Shymkent, 2019

MINISTRY OF EDUCATION AND SCIENCE OF THE REPUBLIC OF KAZAKHSTAN

M.AUEZOV SOUTH KAZAKHSTAN STATE UNIVERSITY

higher school “Chemical Engineering and Biotechnology”

Chair “Chemical technology of inorganic substances”

Таubayeva А.S., Kambarova G.A

METHODICAL INSTRUCTIONS

lecture notes to the discipline

«Theoretical bases of processing of mineral and technogenic raw materials»

for students of a specialty 5В072000 – Chemical technology of inorganic substances (6B071 Engineering and engineering work, EP 6B07160- Chemical Technology of Inorganic Substances)

Shymkent, 2019

UDК 631.812;893.

BBК

Composers: Таubayeva А.S., Kambarova G.A., discipline «Theoretical bases of processing of mineral and technogenic raw materials» for students of a specialty 5В072000 – Chemical technology of inorganic substances (6B071 Engineering and engineering work, EP 6B07160- Chemical Technology of Inorganic Substances) / Lecture notes. – Shymkent: M.Auezov South Kazakhstan State University, 2019. – 96 p.

The methodical instructions to collection of lectures compiled in accordance with the requirements of the curriculum and the discipline program of the discipline "Theoretical bases of processing of mineral and technogenic raw materials" and include all the necessary information on the implementation of the lectures of the course.

The reviewers: Kadyrbayeva A.A. - cand.techn.scie., department "Chemical technology of inorganic substances".

Abduova A.A.– cand.techn.scie., department "Ecology".

The methodical instructions in the "Chemical technology of inorganic substances" of the department meeting (The report №     from «    » «    »   20    ) and “Chemical engineering and biotechnology” higher school education innovative technologies and methodical to ensure the meeting of the committee (The report №     from «    »  «    »   20    ) were considered and recommended for printing.

It is recommended to the edition by methodical council of M. Auezov SKSU, the report №   from «   »  «   »   20

@ М.Auezov South Kazakhstan State University 2019

Responsible for release:  Taubayeva A.S

CONTENTS

| Introduction | 7 |
| --- | --- |
| Lecture 1. Introduction. Purpose and tasks of the course "Theoretical bases of processing of mineral and technogenic raw materials". Characteristic of mineral and technogenic raw materials. | 9 |
| Lecture 2. The value of theoretical methods of analysis of real technological systems to substantiate the technological mode of production. | 11 |
| Lecture 3. General information about the mineral and technogenic raw materials. Technogenic raw materials as a result of mining operations. The concept of technogenic deposits, features and prospects of development. | 15 |
| Lecture 4. Mineral and technogenic raw materials used for the production of mineral salts, fertilizers and acids. | 18 |
| Lecture 5. Secondary mineral raw materials. Characteristics of secondary mineral raw materials, the rationale for the need and the possibility of its disposal. | 21 |
| Lecture 6. Creating wasteless technology. The main problems of the processing of secondary mineral raw materials. Types of waste, methods of disposal of valuable components. | 26 |
| Lecture 7. Waste recycling as secondary material resources. Processing of technogenic raw materials depending on their aggregative state. | 30 |
| Lecture 8. The basic principles of the choice of technology for processing technogenic raw materials, depending on the physico-chemical composition and properties. | 30 |
| Lecture 9. Typical processes of chemical technology of inorganic substances and their legitimacy. The theoretical basis of the processes of dissolution of solids and crystallization from solutions. | 34 |
| Lecture 10. Filtration of suspensions. Extraction methods from aqueous solutions. | 38 |
| Lecture 11. Hygroscopic properties of crystalline substances. Hygroscopic point. Sorption isotherm and solubility. Moisture absorption rate. Coefficient of hygroscopicity. | 41 |
| Lecture 12. Caking bulk materials. Causes of loss of flowability. Ways to prevent caking of raw materials and finished products. | 42 |
| Lecture 13-14. Theoretical foundations of the granulation process. Structural granulation in the presence of a liquid phase. The formation of granules. Granulation methods. Granulation of powders by pressing. Pelleting granulation. | 44 |
| Lecture 15-16. Thermodynamic analysis of processes in the technology of inorganic substances. Chemical thermodynamics. Calculation of the thermodynamic probability of the processing of technogenic raw materials. | 48 |
| Lecture 17-18. Hess law and its consequences. Methods for calculating the heat of formation and heat capacity of inorganic compounds. | 52 |
| Lecture 19. Temperature dependence of the thermodynamic characteristics of substances. | 59 |
| Lecture 20. Kirchhoff equation. | 61 |
| Lecture 21-22. The effect of temperature and pressure on the properties of substances and chemical systems. The equation of heat balance of chemical-technological processes. | 65 |
| Lecture 23-24. Methods for calculating thermodynamic characteristics. Application of comparative calculation methods in chemical thermodynamics. Calculation of heat capacity of substances. Calculation of the entropy of substances and its changes in various processes. | 67 |
| Lecture 25. Calculation of the heat of formation of substances and the thermal effect of the reactions of processing of industrial waste. | 71 |
| Lecture 26. Calculation of the Gibbs energy change (ΔGoT) of chemical reactions occurring in real technological systems. | 73 |
| Lecture 27. Calculation of properties of solutions. Application of additivity rule to multicomponent solutions. | 75 |
| Lecture 28. Calculation of the properties of the solution by comparative methods. | 78 |
| Lecture 29. The role of chemical interactions in changing the physicochemical properties of the solution. Entropy analysis of interactions. | 80 |
| Lecture 30. Thermodynamic characteristics of mixed solutions of sulfuric and phosphoric acids. System HNO3-H2O. System H2SO4-H2O. H3PO4-H2O system. The final lecture on the theoretical foundations | 82 |
| Assessment criteria | 91 |
| The list of recommended literature | 94 |

Introduction

The discipline "Theoretical bases of processing of mineral and technogenic raw materials" refers to the cycle of basic disciplines (BD) and elective component (EC) for students of a specialty 5В072000 – Chemical technology of inorganic substances (6B071 Engineering and engineering work, EP 6B07160- Chemical Technology of Inorganic Substances).

Problems of complex use of natural raw materials, improve product quality, increase the volume of their output, processing and recycling of waste. Possible solutions to the problems of technology of inorganic substances.

The purpose of study of the discipline "Theoretical bases of processing of mineral and technogenic raw materials" is the formation of students' knowledge of the theoretical foundations of the processing of mineral and technogenic raw materials, to formulate the general laws governing the processing of mineral raw materials and chemical waste.

The task of studying the discipline is:

- the study of the theoretical bases of the processing of mineral and technogenic raw materials;

- the study of typical processes in the technology of inorganic substances;

- acquisition of skills for calculating thermodynamic potentials;

- the study of methods for determining thermodynamic probability process flow.

Pre-requisites: Chemistry, Inorganic Chemistry, Introduction to the specialty

Post-requisites: Theory and technology gallurgy productions, Technology of mineral fertilizers, Chemistry and technology of inorganic substances.

After students have completed to study this course, they must be able to:

- to formulate the general laws governing the processing of mineral raw materials and chemical waste;

- determine the values of heat capacity, entropy, heat of formation and combustion of chemical compounds;

- use the main physico-chemical and thermodynamic characteristics of the state of the system to determine the likelihood and direction of the processes;

- reasonably summarize the results of theoretical studies of chemical transformations;

- make decisions on the optimization and improvement of existing technologies for the processing of mineral and technogenic raw materials and evaluate their effectiveness.

Discipline «Theoretical bases of processing of mineral and technogenic raw materials» consists of a course of lectures, practical classes and independent work. Independent work involves the study of lecture material, independent study of individual sections of the course, problem solving, the development of presentations and other types of ERIW.

The final control of mastering the discipline is recommended in the form of an exam.

Competences: to be able to use information to solve problems in the chemical technology of inorganic substances and materials; apply logical and critical thinking to solve the problems of processing mineral and man-made materials; apply thermodynamic and thermophysical properties of substances to calculate the main parameters of heat-using devices of chemical technology; know the basic physico-chemical and thermodynamic characteristics of the state of the system to determine the probability and direction of the processes.

Practical classes are conducted according to the syllabus and include topics for each class. Independent practical tasks for students are given in these guidelines.

Lecture 1. Introduction. Purpose and tasks of the course "Theoretical bases of processing of mineral and technogenic raw materials". Characteristic of mineral and technogenic raw materials.

Lesson plan: give students an explanation about the mineral and technogenic raw materials.

Lesson purpose: to acquaint students with mineral raw materials base of the Republic of Kazakhstan

Theoretical part:

The purpose of study of the discipline "Theoretical bases of processing of mineral and technogenic raw materials" is the formation of students' knowledge of the theoretical foundations of the processing of mineral and technogenic raw materials, to formulate the general laws governing the processing of mineral raw materials and chemical waste.

The task of studying the discipline is:

- the study of the theoretical bases of the processing of mineral and technogenic raw materials;

- the study of typical processes in the technology of inorganic substances;

- acquisition of skills for calculating thermodynamic potentials;

- the study of methods for determining thermodynamic probability process flow.

Meaning:

Mineral raw materials – Natural mineral formations extracted from the bowels of the earth in the process of exploitation of mineral deposits.

Тechnogenic raw materials - wastes formed at the stages of production and processing of metals, which can serve as a source for the reproduction of raw materials, as well as waste from mining and metallurgical industries (dumps of poor ores, tailings, sludge, dust, scrap, slag, etc.) containing non-ferrous, rare and noble metals. Production waste is usually quite significant and due to its features.

Mineral raw material sources are the general sector of Kazakhstan economics and the real base of development all industrial production. Significant power supplies have been established in the Republic for processing important types of mineral raw materials, such as ores of iron, manganese, chrome, copper, lead, zinc, uranium, bauxites, and other Republic valuable components, which allows not only provide intestinal necessities of the Republic, but also exported a large part of marketable products. Kazakhstan is one of the world leader in area of amount and variety of mineral raw material sources. The Republic has unique resources of ferrous, non-ferrous, precious metals and energy feedstocks. Also, mineral resources of the country include phosphorites, barytes, fiber rocks, kaolin, potassium salts and other types of ore and non-metallic materials.

Recommendations to students in preparation for lesson

The student must be prepared for lesson. Preparation consists of studying materials from lecture notes, textbooks and training manuals. Homework is performed in accordance with the topic of training. Each student's homework is given to the teacher at the next lesson.

Task and order of performance lecture lesson in the audience

1. Students make the determination of the prevalence of chemical elements in the earth's crust.

2. Students determine the geographical location of mineral raw materials in Kazakhstan

Technical and tooling facilities: multimedia board

List and types of homework: Determine the role of mineral raw materials in the innovative development of the Republic of Kazakhstan.

Сontrol questions:

The main terms used in the technology of inorganic substances.

- What does mean mineral raw materials?

- What does mean technogenic raw materials?

Tasks to ERIW

I. Variant (simple)

1. Characteristics of mineral and technogenic materials.

2. How is industrial raw materials classified?

II. Variant (medium difficulty)

Man-made raw materials as a result of mining

III. Variant (complicated)

Complex use of mineral raw materials.

Main literature:

1. Erdman S.V., Frolova I.V., Korobochkin V.V. Chemical technology of inorganic substances: a training manual. –Tomsk: Publishing House of Tomsk Polytechnic University, 2011. - 194 p.

2. Shirokov Yu.G. Theoretical foundations of technology of inorganic substances: a manual / GOU VPO Ivan. State Chemical Chemistry Technological University, Ivanovo, 2009-376 p.

Lecture 2. The value of theoretical methods of analysis of real technological systems to substantiate the technological mode of production.

Lesson plan: give students an explanation about the mineral and technogenic raw materials.

Lesson purpose: to acquaint students with mineral raw materials base of the Republic of Kazakhstan

Theoretical part:

Raw material - Basic substance in its natural, modified, or semi-processed state, used as an input to a production process for subsequent modification or transformation into a finished good.

Raw materials are materials intended for further processing.

Figure 1. Classification of raw materials

- Mineral raw materials. Useful fossil, extracted from the earth's crust.

Mineral resource classification is the classification of mineral deposits based on their geologic certainty and economic value (figure).

Mineral deposits can be classified as:

Mineral resources that are potentially valuable, and for which reasonable prospects exist for eventual economic extraction.

Mineral reserves or Ore reserves that are valuable and legally and economically and technically feasible to extract

Figure 2. Classification of minerals

The starting materials for the production of industrial products are raw materials, half-products and secondary raw materials.

The first of the mentioned initial substances are basic, they are called raw materials.

Raw materials (raw materials) - natural materials used in the manufacture of industrial products.

- Mineral raw materials are minerals extracted from the earth's interior, which at a given level of technological development can be economically processed in the industry into the required products. Mineral raw materials can be divided into three types: ore, non-metallic and combustible.

Mineral resources by use:

- combustible (oil, gas, coal);

- ore (aluminum, copper, tin);

- non-metallic (asbestos, graphite, marble).

Mineral resources can vary in status and are divided into:

- liquid (oil, mineral water);

- solid (salt, coal, marble);

- gaseous (methane, helium, combustible gases).

Ore mineral raw materials are rocks from which metals are obtained. During the processing of many types of ore raw materials, along with metals, chemical products are also produced. A classic example is the production of sulfuric acid in the production of copper, zinc, and nickel.

Non-metallic minerals are rocks used in the manufacture of chemical, construction and other non-metallic materials and are not the starting material for the production of metals. Halite (sodium chloride NaCI) - non-metallic raw materials in the production of caustic soda NaOH and chlorine, sulfur pyrite (pyrite FeS) and sulfur - in the production of sulfuric acid, apatite and phosphorite [a group of phosphorus-containing minerals, for example Ca10 (PO4) 6F2] - in the production of phosphoric acid.

Combustible mineral raw materials contain carbon, therefore it is also called carbon containing. This type of raw materials include coal, oil, oil shale, natural gas.

Combustible (fuel) minerals are divided into liquid (oil), solid (coal, peat) and gaseous (natural and associated gas) by their state.

Oil and gas serve as a source of energy and heat: thanks to them the engines of machines work, the rooms are heated.

Coal is the main source of energy used in production.

Peat is used as a fuel and as thermal insulation.

Combustible minerals are the most important type of minerals.

Technogenic minerals

- Waste generated during the production and processing of metal and waste from the mining, metallurgical, chemical industries containing non-ferrous and precious metals is a technogenic mineral raw material.

Mineral raw materials for chemical industry

Mineral reserves in the chemical industry are divided into two groups:

- Balance - with a high content of useful components.

- Off-balance - with a low content of useful components. Such a group, if any conditions change, can move to a balance group.

Recommendations to students in preparation for lesson

The student must be prepared for lesson. Preparation consists of studying materials from lecture notes, textbooks and training manuals. Homework is performed in accordance with the topic of training. Each student's homework is given to the teacher at the next lesson.

Task and order of performance lecture lesson work in the audience

1. Students make the determination of the prevalence of chemical elements in the earth's crust.

2. Students determine the geographical location of mineral raw materials in Kazakhstan

Technical and tooling facilities: multimedia board

List and types of homework: Determine the role of mineral raw materials in the innovative development of the Republic of Kazakhstan.

Сontrol questions:

1. What does mean raw material?

2. Classification of raw material

3. What is technogenic minerals?

Tasks to ERIW

I. Variant (simple)

1. Characteristics of mineral and technogenic materials.

2. How is industrial raw materials classified?

II. Variant (medium difficulty)

Man-made raw materials as a result of mining

III. Variant (complicated)

Complex use of mineral raw materials.

Main literature:

1. Erdman S.V., Frolova I.V., Korobochkin V.V. Chemical technology of inorganic substances: a training manual. –Tomsk: Publishing House of Tomsk Polytechnic University, 2011. - 194 p.

2. Shirokov Yu.G. Theoretical foundations of technology of inorganic substances: a manual / GOU VPO Ivan. State Chemical Chemistry Technological University, Ivanovo, 2009-376 p.

Lecture 3. General information about the mineral and technogenic raw materials. Technogenic raw materials as a result of mining operations. The concept of technogenic deposits, features and prospects of development.

Lesson plan:

- General information about the mineral and technogenic raw materials.

- Technogenic (techno-genetic) raw materials

Lesson purpose: to acquaint students with characteristic of mineral and technogenic raw materials, technogenic waste

Theoretical part:

- Mineral raw materials - it is useful mineral, which are used in the production sphere, it plays an important role in the national economy, especially in industry. Minerals provide almost 75% of the raw materials for production.

- Technogenic mineral raw materials-Waste generated during the production and processing of metal and waste from the mining, metallurgical, chemical industries containing non-ferrous and precious metals is a technogenic mineral raw material.

Technogenic mineral raw materials are divided into groups, depending on their affiliation with certain industrial sectors.

There are raw materials:
     -mining enterprises;
     -processing plants;
     -metallurgical plants;
     -chemical industry;
     -fuel energy.

Technogenic mineral raw materials are widely used in construction (production of cement, concrete), during road works (backfilling of quarries, filling of dams), in the production of mineral fertilizers.

- technogenic (techno-genetic) raw materials - waste generated during the production and processing of metals, which can serve as a source of raw material reproduction, as well as waste from mining and metallurgical industries (dumps of poor ores, tailings, sludge, dust, scrap , slags, etc.), containing non-ferrous, rare and noble metals. Production waste is usually quite significant and due to its features.

The main sources of multi-tonnage waste are:

- -ore mining processing, metallurgical, chemical, timber and woodworking, textile industries;

- -energy complex;

- -building materials industry;

- -agro-industrial complex;

- -household human activity.

All technogenic wastes can be divided into two large groups: mineral and organic.

Mineral waste is of primary importance, there are more of them, they are better studied and have the greatest value for the production.

Technogenic raw materials are characterized by a complex internal structure, differ in density, particle size of debris, material composition, content of useful components and technological properties of mineral raw materials.

The bulk of mining waste in Kazakhstan is formed in mining enterprises (72.5%) with overburden and mining operations, much less at concentrating factories (25.7%) and metallurgical plants (1.8%).

Technogenic mineral objects according to belonging to certain industries, enterprises of mining production and methods of formation are divided into five types:

1) Technogenic mineral objects of mining enterprises, represented by dumps of overburden and ore-bearing rocks, off-balance sheet and substandard ores;

2) Technogenic mineral objects of the processing plants are dumps (tailings) of enrichment;

3) Technogenic mineral objects of metallurgical plants, represented by metallurgical slags;

4) Technogenic mineral objects of the chemical industry are waste chemical processing (sludge, etc.);

5) Technogenic mineral objects of fuel energy are ash and slag waste from thermal power plants

Slags of ferrous metallurgy is a by-product in the smelting of cast iron and iron ores (blast furnaces, marten, ferromanganese).

The slag yield is very pure and ranges from 0.4 to 0.65 tons per 1 ton of cast iron.

They include up to 30 different chemical elements, mainly in the form of oxides. The main oxides are: SiO2, Al2O3, CaO, MgO. FeO, MnO, P2O5, and TiO2 are present in smaller amounts.

In the production of building materials used 75% of the total amount of blast furnace slag. The main consumer is the cement industry. It consumes millions of tons of granulated blast furnace slag annually.

Slags of nonferrous metallurgy are extremely diverse in composition.

The most promising direction of their use is complex processing: preliminary extraction of non-ferrous and rare metals from slag; release of iron; the use of silicate residue slag for the production of building materials.

A byproduct in aluminum production is bauxite slurry, a loose, loose material of red color. When alumina is produced from nepheline raw materials, as a by-product is formed nepheline slime.

Alumina is produced from high aluminate clays, as a by-product is formed kaolin slime, etc. The main application of all these sludges are found in cement production.

Mining waste. Overburden rocks - mining waste, mining waste of various minerals. A particularly large amount of this waste is formed during open pit mining. According to approximate estimates, over 3 billion tons of waste are generated annually in the country, which are an inexhaustible source of raw materials for the building materials industry. However, at present they are used only by 6-7%. Overburden and waste rock are used depending on their composition (carbonate, clay, marl, sand, etc.).

Mining and concentrating mills dump into dumps a large number of flotation tailings, formed in particular during the processing of non-ferrous metal ores. Waste of coal mining and coal beneficiation are formed in coal preparation plants. For coal waste is characterized by the constancy of the composition, which distinguishes them from other types of mineral waste.

Gypsum wastes from the chemical industry are products containing calcium sulphate in one form or another. Scientific studies have shown the complete replacement of traditional gypsum raw materials with chemical industry wastes.

Phosphogypsum - waste in the production of phosphate fertilizers from apatite and phosphate. It is CaSO4-2H2O with admixtures of undecomposed apatite (or phosphate) and unwashed phosphoric acid.

Fluorine gypsum (fluoride hydride) - a by-product in the production of hydrofluoric acid, anhydrous hydrogen fluoride, fluoride salts. According to its composition, it is CaSC> 4 with admixtures of the original undecomposed fluorite. It may also contain unwashed sulfuric acid.

Electrothermophosphorus slags - waste production of phosphoric acid, but obtained electrothermal method. In the granulated form contain 95-98% glass. The main oxides included in their composition are SiO2 and CaO. They are a valuable raw material in the production of binders.

Technogenic raw materials can be used to extract useful components, as building materials, mineral fertilizers, etc.

The greatest practical interest is the waste of enrichment of metallurgical production, which contains non-ferrous, rare and noble metals. Waste enrichment of ores, metallurgical and sludges are mainly used as ore raw materials.

As mining raw materials use tailings, metallurgical slags, ash and slag waste of thermal power plants and waste of the chemical industry. They are used for the extraction of valuable components (barite, asbestos, graphite, fluorite, mica, talc, etc.) and the production of flux, molding and refractory materials.

Technogenic mineral raw materials (slags, ash and slag waste, tailings, etc.) are widely used in the construction industry for the production of concrete, cements, building materials.

Mining wastes are used for backfilling of pits, dumping of dams of tailing dumps, as a filling material when sinking underground mines, during road construction.

Control questions:

1. What is meant by man-made mineral formations?

2. What technogenic mineral formations are technogenic deposits?

3. What are the signs of the classification of man-made mineral objects?

4. Where is applied technogenic minerals?

Main literature:

1. Tleuova S.T., Tleuov A.S., Zhuldyzbaeva S.E., Altybaev Zh.M., Nazarbek U.B. Resource-saving technologies for processing industrial waste. Tutorial. - Shymkent: SKSU named after M. Auezova, 2016 .-262 p.

2. Pozin M.E. The technology of mineral fertilizers. - M: Chemistry, 1983, - 335 p.

3. Erdman S.V., Frolova I.V., Korobochkin V.V. Chemical technology of inorganic substances: a training manual. –Tomsk: Publishing House of Tomsk Polytechnic University, 2011. - 194 p.

Lecture 4. Mineral and technogenic raw materials used for the production of mineral salts, fertilizers and acids

Lesson plan:

1. Mineral and technogenic raw materials used for the production of mineral salts.

2. Mineral and technogenic raw materials used for the production of mineral   fertilizers.

3. Mineral and technogenic raw materials used for the production of mineral acids.

Lesson purpose: to acquaint students with characteristic of mineral and technogenic raw materials, technogenic waste

Theoretical part:

Mineral salts - the most large-tonnage type of chemical products used in agriculture, industry, medicine and home. The largest quantities are produced and consumed compounds of sodium, phosphorus, potassium, nitrogen, aluminum, iron, sulfur, copper, chlorine, fluorine, etc. Salts used as mineral fertilizers and pesticides are produced on the largest scale.

Huge quantities of mineral salts are used in the chemical industry, which is not only a manufacturer, but also one of the largest consumers of mineral salts.In industry use a variety of mineral salts.The chemical industry is not only a manufacturer, but also one of the largest consumers of mineral salts. Sodium salts are especially widely used.Sodiumsalt is the most valuable raw material in the production of soda, chlorine, caustic soda, hydrochloric acid, metallic sodium.

Sodium sulfate is a raw material for the production of sodium sulfide, cellulose, paper and glass.

Many sodium salts (sulfites, sulfides, bichromates, fluorides, phosphates, etc.) are widely used in the manufacture of synthetic fibers, dyes and plastics, various chemical reagents, catalysts, detergents and skin treatments, as well as in a number of other productions.

The metallurgical industry uses some mineral salts as additives and fluids in the smelting of metals, in the enrichment and hydrometallurgical processing of ores.

In the production of glass in large quantities consumedsodium sulfate and soda, salts and oxides of lead, zinc and boron.Cement production is based on the use of limestone - calcium carbonate.

Simple fertilizers, depending on what kind of battery they contain, are divided into nitrogen, phosphate and potash.

Nitrogen fertilizers. The raw materials for the production of nitrogen fertilizers are ammonia and nitric acid, synthesized from atmospheric nitrogen or utilized from waste gases of various industries.

Nitrogen fertilizers - inorganic and organic substances containing nitrogen, which are applied to the soil to increase yields. Mineral nitrogen fertilizers include amide, ammonia and nitrate.

Types of nitrogen fertilizers:

- Ammonia fertilizers:

•	Ammonium sulfate

• Ammonium Chloride

• Ammonium carbonate

• Ammonium sulfide

• Ammophos and diammophos

- Nitrate fertilizers:

o Sodium Nitrate

o Calcium nitrate

o Potassium nitrate

- Ammonium nitrate fertilizers:

 Ammonium nitrate

 Calcium ammonium nitrate

- Amide fertilizers:

 Urea (carbamide)

 Calcium cyanamide

Phosphate fertilizers - mineral fertilizers, calcium salts and ammonium phosphoric acid. Phosphoric ores and products their processing are used as fertilizers. Phosphorites and apatites serve as raw materials for phosphate fertilizers.

Phosphate fertilizers include superphosphate, double superphosphate, ammophos, diammophos, orthophosphate, potassium metaphosphate, precipitate, tomasshlak, phosphate rock, bone meal, etc.

Potash fertilizers are a type of mineral fertilizers designed to fill the need of plants for potassium. As a rule, they are presented in the form of water-soluble salts, sometimes with the addition of other compounds containing potassium. Potassium fertilizers, as a rule, are used in combination with nitrogen and phosphate fertilizers.

Types of potash fertilizers: potassium chloride, potassium sulfate, potassium salt, potassium nitrate.

The main raw materials for the production of potassium chloride are natural potassium salts (sylvinite and carnallite - salts with a pure substance content of 12-15% with admixtures of sodium and magnesium salts).

The raw materials for the production of salts and mineral fertilizers are natural minerals, semi-products of the chemical industry and waste products of some industries.

The basis of the production of salts from chemical intermediates are neutralization reactions. In this way, most nitrogenous fertilizers are made from acids and alkalis (ammonium sulfate, ammonium nitrate, sodium and potassium). Many salts are formed as by-products of other industries. So, when obtaining alumina from nepheline, soda and potash K2CO3 are emitted as by-products.

In the production of hydrochloric acid by the sulfate method, the side is sodium sulfate. Sodium nitrate or calcium get captured soda or lime milk waste nitrous gases in the production of nitric acid. In the production of titanium dioxide and sulfuric acid etching of metals in large quantities, iron vitriol FeSO4 О 7H2O is formed.

Recommendations to students in preparation for lesson

The student must be prepared for lesson. Preparation consists of studying materials from lecture notes, textbooks and training manuals. Homework is performed in accordance with the topic of training. Each student's homework is given to the teacher at the next lesson.

Task and order of performance lecture lesson in the audience

- Give characterize to mineral fertilizers

- Describe the main types of nitrogen fertilizers.

- Which fertilizers more effective?

Technical and tooling facilities: multimedia board

List and types of homework: Determine the role of fertilizers to plants.

Control questions:

- Give the classification of mineral fertilizers.

- Describe the main types of nitrogen fertilizers.

- List the main types of phosphate and complex mineral fertilizers based on phosphorus.

- What is the raw material in the production of Nitrogen fertilizers?

- What is the raw material in the production of phosphate fertilizers and phosphoric acid?

- What is the raw material in the production of Potash fertilizers?

Tasks to ERIW

I. Variant (simple)

1. Nitrogen fertilizers.

2. Potash fertilizers

3. Phosphate fertilizers

II. Variant (medium difficulty)

Complex use of fertilizers

III. Variant (complicated)

Prospects for use fertilizers

The list of recommended literature:

1. Dmitrevsky B.A. Properties, production and use of mineral fertilizers. - SPb .: Prospect of Science, 2013. 326 p.

2. Akhmetov, T.G., Porfir'ev, R.T., Gaisin, L.G., Akhmetova, L.T., Karimov, Y.M. Chemical technology of inorganic substances: -M .: Higher School, 2002. - 688 p.

Lecture 5. Secondary mineral raw materials. Characteristics of secondary mineral raw materials, the rationale for the need and the possibility of its disposal

Lesson plan:

1. Characteristics of secondary raw materials

2. Types of secondary raw materials

Lesson purpose: to acquaint students with secondary mineral raw materials and types of secondary raw materials

Theoretical part:

- Secondary raw materials - substances and materials used in the production that are unclaimed in other industries.

Secondary raw materials are called only those production and consumption wastes, which by their nature are material resources and which can and should be used again as raw materials or products directly or after additional processing.

Secondary material resources - Production and consumption waste generated in the national economy, for which it is possible to reuse directly or after additional processing.

Their sources are waste production and waste of consumption.

- Waste production - raw material residues and supporting materials that have lost their original qualities, as well as products that are not the aim of the production process (additional products).

- Waste Consumption   - used substances and products, the recovery of which is not economically feasible.

When we talk about secondary raw materials, we are usually talking about such material resources that can be reused.

Classification of secondary raw materials is clear and simple. Conventionally, it can be divided into several separate groups:

- 1. Secondary raw materials that can be used as a full or partial replacement of primary raw materials.

- 2. Waste, acting as a source product for the manufacture of primary raw materials.

- 3. Waste in the form of used raw materials, which can be used in a fundamentally new technological cycle during processing.

- 4. Wastes that serve as a source for ore raw materials and the extraction of various metals.

The main ways of their use in industrial production are as follows:

- 1) extraction, regeneration of unreacted raw materials and materials and return to production;

- 2) extraction of valuable components as products of production;

- 3) the selection of components and giving them with the help of special operations of commercial value;

- 4) the use of waste as precursors and materials in other industries or other industries.

Secondary raw materials partially or even completely replace the primary in any production;

On the basis of secondary raw materials is created а new chemical and technological process, good other than used in production the same product based on primary raw materials.

Secondary material resources - a set of production and consumption wastes that can be used as the main or auxiliary material for the production of target products.

In the creation of non-waste technology, the following four principles were defined:

1. development and implementation of various drainless technological schemes and water circulation cycles based on effective cleaning methods (for example, in electroplating);

2. development and introduction of fundamentally new technological processes, excluding the formation of any types of waste;

3. the creation of territorial industrial complexes, i.e. economic regions in which a closed system of material flows of raw materials and waste within the complex is implemented;

4. widespread use of waste as secondary material and energy resources.

In general, to solve the problems of waste utilization, it is necessary to focus on the following areas:

- the use of waste as a secondary raw material for the production of products from ferrous, non-ferrous and precious metals, as well as cellulose, plastics, glass, rubber, wood;

- disinfection, storage and heat treatment;

- the use of large industrial waste mining and processing of minerals.

Classification based on the sources of secondary raw materials:

- in metallurgical production: slags formed in ferrous and non-ferrous metallurgy (blast-furnace, ferroalloy, etc.);

- in the fuel energy and fuel industries: ashes, fuel slags, ore dressing wastes, etc .;

- in the chemical industry: waste containing iron, lime, gypsum, secondary polymer products, etc .;

- in the mining industry: overburden rocks and passing minerals;

- in the production of building materials: dust with different chemical composition, screenings, glass breakage, etc .;

- in the processing of wood and other plant materials: sawdust, shavings, straw, fiber, rags, etc .;

- secondary raw materials of urban economy and human activity: glass, rubber, remains of building structures, plastic, etc.

Classification of secondary raw materials toxicity:

Secondary raw materials contain various chemicals that can dangerously affect biological objects. Classification according to the class of toxicity allows you to safely make further processing:

- secondary raw materials of the first class of hazard contain highly toxic substances (mercury, mercuric chloride, mercuric chloride, arsenic compounds, cyanides and other substances);

- the second class of hazard implies the presence of less toxic substances (copper chloride, nickel chloride, lead nitrate and other substances);

- the third hazard class indicates the content of even less toxic substances (copper sulphate, oxaloaceous copper, lead oxide and other substances);

- the secondary raw materials of the fourth hazard class contain the least hazardous simple chemical substances (manganese, phosphates and other substances).

Depending on the class of toxicity of secondary raw materials they are subjected to neutralization and processing. Secondary raw materials of the first two hazard classes require careful attention. Recycling is done without further transportation and production costs are high.

According to the method of use as a secondary raw material, all types of waste can be divided into the following groups: a) waste, as secondary raw materials, which are used as an additive or instead of primary raw materials;

b) waste, as an initial product for the production of secondary raw materials, which is intended to be used partially or completely instead of primary raw materials;

c) wastes that are generated in the form of raw materials or materials used in the main technological process - as secondary raw materials for use in another technological cycle;

d) waste as raw materials and materials, characterized by new properties, which are absent in primary raw materials;

e) waste as a source of ore raw materials for the extraction of various kinds of metals.

As soon as a person learned to extract metal from ore, he had a need to reuse production waste and consumer waste.

In principle, the metal from the ore and the metal from the waste, ultimately, has no differences. However, the energy costs for obtaining metal from ore are much higher than in obtaining metal from waste.

At present, on the basis of waste from various industries, building materials enterprises produce products and materials of adequate quality, and with lower production costs than with the use of primary raw materials, because it excludes costs for the extraction, transportation, processing of raw materials.

In modern conditions, one of the most important tasks is the widespread use of secondary raw materials. The building materials industry has gained positive experience in using waste as a raw material for the production of efficient building materials that are not inferior in quality to the products obtained using primary raw materials. However, it should be remembered that the use of certain types of secondary raw materials is still cheaper than the processing of primary raw materials.

In modern conditions, the problem of wider involvement in the production of waste generated is of particular importance for the effective development of the national economy, which makes it possible to expand the resource base and reduce environmental pollution. Quite efficiently and in significant volumes, the generated waste can consume such industries as construction and building materials industry.

Types of secondary raw materials.

- · Waste paper: paper, cardboard, newspapers, textiles, Tetra Pak;

- · Glass: glassware, cullet;

- · Scrap metal: black, color, precious;

- · Chemicals: acids, alkalis, organics;

- · Oil products: oils, bitumen, asphalt;

- · Electronics: products, boards, batteries, mercury lamps, wire;

- · Plastics: polyethylene terephthalate (PET), polyvinyl chloride (PVC), high pressure polyethylene (LDPE) and low polyethylene (HDPE), ABS plastic, polystyrene (PS)

- · Rubber: tires, rubber;

- · Biological: food waste, grease, sanitation;

- · Wood: boughs, shavings, leaves

- · Construction: brick, concrete;

- ·       Wastewater.

As an example of the identity of the use of various raw materials and wastes, the fact that the overburden produced in the extraction of mining and raw materials, stone, brown coal and a number of ferrous metals can be widely used for the production of various building and binding materials. Technical hydrolysis lignins and some types of coal waste can be used as fuel, carbonaceous reducing agents.

Complex use of raw materials and waste is also important because it involves solving the problem of creating waste-free and environmentally friendly industrial technologies. The development and development of waste-free technologies are important for chemical, mining, microbiological, metallurgical, coal, construction and other resource-intensive industries.

Recommendations to students in preparation for lesson

The student must be prepared for lesson. Preparation consists of studying materials from lecture notes, textbooks and training manuals. Homework is performed in accordance with the topic of training. Each student's homework is given to the teacher at the next lesson.

Task and order of performance lecture lesson in the audience

- Give characterize to secondary raw materials

- Describe the main types of secondary raw materials

Technical and tooling facilities: multimedia board

List and types of homework: Determine the role of secondary raw materials in industry

Control questions:

1. What is secondary raw materials?

2. What types of secondary raw materials do you know?

3. Does the use of secondary raw materials benefit?

4. Characteristics of secondary raw materials.

5. The use of waste metallurgical industry in the production of cement and other binders.

Tasks to ERIW

I. Variant (simple)

Give characterize to secondary raw materials

II. Variant (medium difficulty)

The main ways of using secondary raw materials in industrial production

III. Variant (complicated)

The value of secondary raw materials for the production of building materials and the environment.

The list of recommended literature:

1. Taymasov B.T. Production technology of portland cement. - Shymkent, SKSU. 2004.-293 p

2. Electronic resource. Secondary raw materials. https://encyclopedia2.thefreedictionary.com/Secondary+Raw+Material

Lecture 6. Creating wasteless technology. The main problems of the processing of secondary mineral raw materials. Types of waste, methods of disposal of valuable components

Lesson plan:

1. The concept of non-waste technology

2. Requirements for non-waste production

Lesson purpose: to acquaint students with definition of non-waste technology

Theoretical part:

Non-waste technology means such a process of management of the national economy, or a region, or an industry, or a particular enterprise, which provides for the rational utilization of all the components of raw materials and energy in a complete cycle, namely, virgin raw materials - production - comsumption - secondary raw materials, without at the same time upsetting the ecological balance.

Low-waste technology is an intermediate stage on the way to non-waste technology.

Low-waste technology is an intermediate stage in waste-free technology and differs from waste-free technology in that losses are not completely eliminated, i.e., the coefficient of utilization of material resourccs should be 0.8-0.9, and thercupon attainment of established limiting allowable norms for discharges and runoff of harmful substances into the atmosphere and watet resources are assured, and also limiting altowable concentrations in working areas.

"Non-waste technology is a method of production in which all raw materials and energy are used most rationally and comprehensively in a cycle: raw materials - production - consumption - secondary resources, and any environmental impact does not violate its normal functioning."

The general principle of creating non-waste production is also the rationality of its organization. Determining here is the requirement to use all components of raw materials reasonably, to minimize the energy, material and labor intensity of production and to search for new environmentally sound raw materials and energy technologies, which is largely due to the reduction of the negative impact on the environment and damage to it, including related sectors of the people's economy economy. The ultimate goal in this case should be considered the optimization of production at the same time for energy, economic and environmental parameters.

The main way to achieve this goal is to develop new and improve existing processes and industries. One example of this approach to the organization of wasteless production is the utilization of pyrite cinders - a waste of sulfuric acid production. At present, pyritic cinders are completely used for the production of cement. However, the most valuable components of pyritic cinders - copper, silver, gold, not to mention iron, are not used. At the same time, an economically advantageous technology for processing pyritic cinders (for example, chloride) has been proposed to produce copper, noble metals and the subsequent use of iron.

Requirements for non-waste production

On the way of improving existing and developing fundamentally new technological processes, it is necessary to comply with a number of general requirements:

- the implementation of production processes with the minimum possible number of technological stages (apparatus), since waste is generated on each of them, and raw materials are lost;

- application of continuous processes that allow the most efficient use of raw materials and energy;

- increase (up to optimum) of unit capacity of units;

- intensification of production processes, their optimization and automation;

- creation of energy-technological processes. The combination of energy with technology makes it possible to use the energy of chemical transformations more fully, to save energy resources, raw materials and materials and to increase the productivity of aggregates.

Wasteless technology (cascade) - chain processes where the waste of production become a raw material for another (assuming the use of this raw material without remainder).

Low-waste technology allows obtaining a technically achievable minimum of solid, liquid, gaseous and thermal waste and emissions. It is not possible to achieve complete energy waste even theoretically, since the energy flow is unidirectional and all its quantity eventually turns into heat. In the global totality, the energy efficiency of technologies, apparently, can not be higher than the achieved biosphere - about 1% of the energy involved (in the case of the biosphere - coming from the Sun). For all specific technological processes there is a calculated, theoretically achievable low-waste maximum, unfortunately not yet calculated.

Waste-free technology is an environmental strategy for the entire industrial production, providing products with a small amount of waste, and in the future, without waste.

Non-waste technology is understood as such a principle of organization of production, in which the cycle "primary raw materials - production - consumption - secondary raw materials" is built with the rational use of all components of raw materials, all types of energy and without disturbing the ecological balance. Waste-free production can be created within the framework of the plant, industry, region, and ultimately for the entire national economy.

Non-waste technology is also understood as such a production method that ensures the most complete use of the processed raw materials and the resulting waste.

Waste-free production is a combination of organizational and technological measures, technological processes, equipment, materials that ensure maximum and integrated use of raw materials and minimize the negative impact of waste on the environment.

Secondary materials and resources are production and consumption wastes that at this stage of the development of science and technology can be used in the national economy both at the enterprise where they were formed and beyond. Secondary material resources do not include recyclable production wastes that are reused as raw materials of the technological process in which they are generated.

By-products and waste are possible raw materials for other industries. By-products can be planned and profit from their sale or use. Waste is an undesirable but inevitable product.

Secondary material resources are classified according to the following criteria:

1. By industry or where the waste comes from;

2. In technological processes;

3. By types of resources

4. According to the degree and possibility of use.

5. According to the state of aggregation.

Depending on the possibility of use, secondary material resources are subdivided:

1.Really possible to use, i.e. there are effective conditions for processing and use;

2. Potentially possible to use secondary materials, the use of which is not yet economically and technically feasible.

According to the sources of its appearance, there are secondary material resources:

1. Wastes from industrial production and construction - residues of raw materials, materials or semi-finished products suitable for use as raw materials, auxiliary materials or finished products.

2. Wastes from sphere consumption:

- waste of means of production that have become unsuitable for further use

- waste items consumption- products unsuitable for their intended use, but potentially suitable as secondary raw materials

- solid household wastes, formed by the population in the process of life and are unlikely to have suitability

3. Waste from the sphere of circulation, ie materials that have fallen into disrepair due to careless transportation, storage and handling.

In addition, secondary material resources can be used in places of their education or in other sectors of the economy.

Low-waste and non-waste technologies, as a rule, are focused on the most important sectors of the national economy: the production and rational use of metals, building materials, wood, and minerals.

Recommendations to students in preparation for lesson

The student must be prepared for lesson. Preparation consists of studying materials from lecture notes, textbooks and training manuals. Homework is performed in accordance with the topic of training. Each student's homework is given to the teacher at the next lesson.

Task and order of performance lecture lesson in the audience

- Give сlassification of secondary material resources

- Describe about non-waste technology

List and types of homework: Determine the main role of technogenic raw materials in industry

Control questions:

- What is non-waste technology?

- Definition of non-waste technology

- By-products, secondary resources

- Tell about the main requirements for non-waste production

- What does mean wasteless technology?

Tasks to ERIW

I. Variant (simple)

Give characterize to technogenic raw materials

II. Variant (medium difficulty)

Classification of technogenic raw materials depending on their aggregative state III. Variant (complicated)

The main value of technogenic raw materials

The list of recommended literature:

1. Laskorin B.Ch. et al. Non-waste technologies for processing mineral raw materials. - M.: Nedra, 1984.

2. Halperin A.M., Ferster V., Chef H.Yu. Man-made arrays and environmental protection .- M.: Moscow Publishing House. state mountain university, 1997.- 534 p.

3. R. G. Melkonyan., O. V. Suvorova., D. V. Makarov. Use of Technogenic Raw Materials of the Mining Plants of Murmansk Region for Manufacturing Glass and Glassy-Crystalline Materials// Glass Physics and Chemistry. May 2018, Volume 44, Issue 3, pp 244–250

Lecture 7-8. Waste recycling as secondary material resources. Processing of technogenic raw materials depending on their aggregative state. The basic principles of the choice of technology for processing technogenic raw materials, depending on the physico-chemical composition and properties.

Lesson plan:

1. Wastes as secondary raw materials

2. Processing of technogenic raw materials depending on their aggregative state

Lesson purpose: to acquaint students with secondary mineral as waste

Theoretical part:

Waste is the product of human activity in everyday life, in transport, in industry, not used directly in the places of its formation and which can be actually or potentially used as raw materials in other sectors of the economy or during regeneration.

- Production wastes are residues of materials, raw materials, semi-finished products, formed in the process of manufacturing products and have lost all or part of their useful physical properties.

- Production waste may be considered products resulting from the physico-chemical processing of raw materials, mining and mineral processing, the production of which is not the goal of this production.

- Consumption waste, unsuitable for further use for its intended purpose and written off in the prescribed manner of machinery, tools, household products.

Secondary materials and resources - waste production and consumption, which at this stage of development of science and technology can be used in the national economy as an enterprise where they were formed, and beyond.

- Processing (processing) of waste - the implementation of any technological operations associated with changing the physical, chemical or biological properties of waste, in order to prepare them for environmentally safe storage, transportation, recycling or disposal.

- o Recycling - the use of waste as secondary material or energy resources.

- o Waste disposal - carrying out any waste operations that do not lead to their disposal.

- o Neutralization of waste - reducing or eliminating the hazard of waste by mechanical, physicochemical or biological treatment.

- o Burial Waste- final disposal of waste when it is disposed of in designated areas or at facilities in such a way that the long-term harmful effects of waste on the environment and human health do not exceed the established standards.

- Processing of secondary raw materials - a set of technological operations for the preparation of secondary raw materials for its subsequent use.

- Sorting of secondary raw materials - the separation of secondary raw materials according to certain characteristics into classes, groups, types.

Different approaches to waste classification are based on the following classification criteria:

- Place production of waste (industry);

- stage of the production cycle; type of waste;

- the degree of damage to the environment and human health;

- direction of use;

- efficiency of use;

- the size of the stock and the volume of production;

- degree of knowledge and development of recycling technologies.

Waste can be divided into two groups - primary and By-products.

The main (primary ) ones are solid waste materials used directly for the manufacture of commercial products. This is metal, metal-containing (scale, sludge, slag, etc.) and non-metal (wood, plastics, rubber, textiles, glass, etc.) waste.

By-products include waste of technological materials and substances used or generated during the technological processes. Side waste may be solid (ash, abrasives, refractory materials), liquid (coolant, mineral oils and other petroleum products, electroplating waste) and gaseous (waste gases).

Wastes from the production of phosphorus, phosphoric acid and phosphate fertilizers are the most large-tonnage waste of the chemical industrial complex. The largest share in the phosphorus industry accounts for the production of phosphate fertilizers - superphosphate.

Fertilizer production

Phosphate fertilizers include superphosphate, precipitate, phosphoric flour

The main waste produced during the manufacture of fertilizers from phosphate raw materials is fluorine and ammonia compounds. They are separated from dryers, evaporators and reactors, with effluents from flushing gases and equipment, with solid waste (phosphogypsum) and fertilizers. The most toxic are hydrogen fluoride and silicon fluoride.

Used gas cleaning equipment allows you to capture most of the fluoride compounds. They are then processed into fluorides and silica-fluorides of various metals and ammonium for subsequent use in nuclear power, non-ferrous metallurgy, the glass industry, and organic synthesis.

Wastes from the production of extraction phosphoric acid

Main wastes:

- Wastewater (acidic, depending on the type of technology varies from 2.9 to 28.4 m3 per tonne of P2O5.

They contain fluorine and phosphorus compounds in significant concentrations.

When neutralizing wastewater is formed fluorophosphate sludge containing in terms of dry matter 25% P2O5 and 5-10% fluorine.)

- phosphogypsum (calcium sulfate with phosphate impurities). Up to 5.8 tons of phosphogypsum is produced per ton of acid.

With the extraction method of processing apatite and phosphate concentrates receive extraction phosphoric acid and phosphate fertilizers-superphosphate, as well as solid waste - calcium sulfate (phosphogypsum).

Figure 3. Superphosphate

Depending on the conditions of phosphoric acid production, waste is generated in the form of Ca2S04 * 2H20 dihydrate, Ca2S04 * 0.5H20 hemihydrate or anhydrous calcium sulfate. This waste is a gray crystalline lumpy powder with a moisture content of 25--40%. They contain unreacted phosphates, compounds of fluorine, strontium, unwashed phosphoric acid, organic substances, compounds of rare-earth elements, uranium. The bulk of the phosphogypsum formed is dumped into dumps, in which millions of tons of phosphogypsum have accumulated.

Comparison of the composition of phosphogypsum with natural gypsum raw materials showed that phosphogypsum is a potentially high-quality raw material for the production of various binders.

When using it, additional cleaning from impurities is required. The volumes of phosphogypsum produced exceed the demand for specially mined gypsum raw materials.

Developed and tested technologies for producing gypsum binders from phosphogypsum. To reduce the content of impurities and neutralize it is washed, then dried, fired and crushed. This technology produces high-strength gypsum that meets the requirements of the standard. Phosphogypsum binders can be used as additives to cements to regulate the setting time.

From phosphogypsum binders can be obtained partition plates, blocks, gypsum sand brick, decorative acoustic plates. On the basis of phosphogypsum binders, it is possible to obtain a decorative material - artificial marble. Knitting for such materials is obtained by roasting the raw material mixture consisting of phosphogypsum, silicofluoride salts, calcium oxide. Phosphogypsum can be used as a raw material for cement production with simultaneous production of sulfuric acid. The essence of this method is the decomposition of calcium sulfate in a reducing environment.

Thermal processing of phosphorus concentrate is carried out in electric furnaces at a temperature of 1300--1500 ° C using carbon (coke) with the introduction of silica as a flux into the mixture, resulting in the formation of phosphorus and slag melt. Per 1 ton of phosphorus accounts for 10-- 12 tons of slag. The possibilities of using phosphoric slags in the production of building materials.

Control questions:

- What is waste?

- What does mean Secondary materials?

- Wastes from the production of extraction phosphoric acid

- Describe highly hazardous industrial waste

- The effect of phosphates on the human body

- Classification of industrial wastes

The list of recommended literature:

1. Laskorin B.Ch. et al. Non-waste technologies for processing mineral raw materials. - M.: Nedra, 1984.

2. Halperin A.M., Ferster V., Chef H.Yu. Man-made arrays and environmental protection .- M.: Moscow Publishing House. state Mountain University, 1997.- 534 p.

3. Maksimov I.E. The state and prospects of using environmental protection systems in solving waste problems // Municipal and industrial waste: methods of disposal and recycling - analytical reviews. - Novosibirsk, 1995.- P.75-86.

4. Tleuov A.S. Recycling of phosphorus industry enterprises. Tutorial. –Shymkent: South Kazakhstan State University named after M. Auezova, 2015.176 s.

Lecture 9. Typical processes of chemical technology of inorganic substances and their legitimacy. The theoretical basis of the processes of dissolution of solids and crystallization from solutions.

Lesson plan:

1. Chemical-technological process

2. Technological regime

Lesson purpose: to acquaint students with chemical-technological process

Theoretical part:

The industry of inorganic substances covers extremely wide area of productions. Productions of speciality «Chemical technology of inorganic substances» are processes of obtaining sulphuric, phosphoric, nitric acids; ammonia, hydrogen, sulphur dioxide and other industrial gases; alkalis, soda, alumina, nitrates, carbamide; fertilizing, technical and mineral food phosphates; compounds  of potassium, chrome and halogens; reactive salts; in wide assortment - mineral fertilizers.

Its importance in national economy is great, the need in inorganic products grows permanently. Together with intensification and output and unit capacity of aggregates increasing, the operating technological processes are permanently perfected, the tasks of product quality raising and waste utilization are solved. For acceptance of new engineering decisions, processes management and optimization of technological modes it is required deep knowledge of chemical technology, methods of raw material processing, physical-chemical regularities of process course.

The primary value in choice of the rational technological scheme of production has a theoretical basing of the process. The physical-chemical bases of production are developed for this purpose. These permit to determine optimal parameters of the process for the product high quality production with maximal productivity and the least expenses, to select a reasonable method of complex raw material processing and waste utilization. The methods of physical chemistry allow estimating in detail equilibrium in complex conditions of real processes, to install presence and degree of deviation of the system from equilibrium.

Thus, the knowledge of theoretical bases of the technology of inorganic substances gives possibility of effective management of industrial production, allows to solve problems of intensification of technological processes.

Chemical-technological process is a set of operations that allow to obtain the End product from the initial raw materials. All these operations are part of the three main stages, characteristic of almost every chemical process:

- preparation of initial reagents for carrying out a chemical reaction;

- chemical interaction;

- selection of the product (s)

Preparation of initial reagents may include several operations:

Appropriately prepared reagents in the next stage are subjected to chemical interaction, which may consist of several stages. In between these stages, it is sometimes necessary to re-use cooling, heating, gas compression, or other physical processes.

As a result of chemical reactions, a mixture of products and unreacted reagents is obtained. At the last stage of the conducting operations associated with the separation of this mixture and the selection of End products.

Typical scheme of technological production chemical products.

Thus, the chemical-technological process as a whole is a complex chemical-technological system consisting of separate interconnected processes and interacting with the environment.

The elements of the chemical-technological system are the processes of heat and Mass exchange, hydrodynamic, mechanical, chemical, etc.

A chemical process is one or more chemical reactions, accompanied by phenomena transmission of heat, mass, and impulse, influencing each other and the course of a chemical reaction.

In a reacting system, there are usually several sequential (and sometimes parallel) chemical reactions leading to the formation of the main product, as well as a series of side By-product reactions between the main initial substances and admixtures, contained in raw materials.

As a result, in addition to the main produced by-products or waste production.

The state of the process is characterized by technological parameters, which include temperature, pressure, expenditure, concentration, etc.

The set of technological parameters that determine the operating conditions of the equipment or equipmentes systems it called technological regime.

The physical-chemical bases of inorganic technology are based on the chemical-technological analysis of processes with application of a number of the fundamental laws, concepts and regularities about mass and energy transfer (conservation laws). The chemical thermodynamics studies the application of thermodynamics laws to chemical and physical-chemical phenomena. The following  questions are considered in it:

Single processes take place in various apparatuses - chemical reactors, absorption and rectification columns, heat exchangers, etc. Separate apparatuses are connected to the technological scheme of process.

Technological scheme is a rationally constructed system of single apparatuses, connected by various types of bonding, which allows to obtain a given product of a given quality.

An industrial enterprise (plant, combine) consists of a number of productions united by the same type of chemical and physicochemical processes, common sources of raw materials and energy, and the possibility of using End products of one production as raw materials on another.

The development and construction of a rational technological scheme is an important task of chemical technology. The process of creating chemical production consists of the following steps:

- development of chemical technological process;

- drawing up project documentation;

-construction of the manufactory, building construction, installation of equipment, placement of control devices and regulation.

Chemical and technological methods produce tens of thousands of products. With the development of chemical technology, chemical processes and reactors are increasingly typed.

Chemical process systems with similar processes and reactors have been developed, which can be used in the production of many chemical products, taking into account unprincipled specifics.

Therefore, engineers- technologists- chemists it is necessary to know the general laws of chemical technology, the most typical chemical-technological processes and reactors, principles of creating rational chemical-technological systems.

Control questions:

1. What is chemical-technological process?

2. What does mean raw material?

3. Classification of raw material

4. What is chemical process?

The list of recommended literature:

1. Shirokov Yu.G. The theoretical basis of the technology of inorganic substances: a training manual / GOU VPO Ivan. State Chemical and Technological University, Ivanovo, 2009-376 p.

2. Bugenov E.B., Dzhusipbekov U.Zh. Theoretical foundations of chemical technology. - Almaty, 2003 .- 244 p.

3. Censkaya V.V., Cherkasova T.G., Tsalko E.V. Theoretical Foundations of Technology inorganic substances. Tutorial. - Kemerovo, 2010 .-- 203 p.

Lecture 10. Filtration of suspensions. Extraction methods from aqueous solutions

Lesson plan:

1. Filtration methods

2. Types of filters

Lesson purposes: to acquaint students with filtering process

Theoretical part:

Filtration is any of various mechanical, physical or biological operations that separate solids from fluids (liquids or gases) by adding a medium through which only the fluid can pass. The fluid that passes through is called the filtrate. In physical filters oversize solids in the fluid are retained and in biological filters particulates are trapped and ingested and metabolites are retained and removed. However, the separation is not complete; solids will be contaminated with some fluid and filtrate will contain fine particles (depending on the pore size, filter thickness and biological activity). Filtration occurs both in nature and in engineered systems; there are biological, geological, and industrial forms. For example, in water treatment and sewage treatment, undesirable constituents are removed by absorption into a biological film grown on or in the filter medium, as in slow sand filtration.

FILTERING (from lat. Filtrum - felt), separation of inhomogeneous systems liquid - solid particles (suspensions) and gas - solid particles in special apparatus - filters, equipped with porous filter partitions, which pass liquid or gas, but delay the solid phase.

Filtration is a process used to separate solids from liquids or gases using a filter medium that allows the fluid to pass, but not the solid. The term "filtration" applies whether the filter is mechanical, biological, or physical. The fluid that passes through the filter is called the filtrate. The filter medium may be a surface filter, which is a solid that traps solid particles, or a depth filter, which is a bed of material that traps the solid.

Filtration is typically an imperfect process. Some fluid remains on the feed side of the filter or embedded in the filter media and some small solid particulates find their way through the filter. As a chemistry and engineering technique, there is always some lost product, whether it's the liquid or solid being collected.

### Filtration Methods

There are different types of filtration. Which method is used depends largely on whether the solid is a particulate (suspended) or dissolved in the fluid.

- General Filtration: The most basic form of filtration is using gravity to filter a mixture. The mixture is poured from above onto a filter medium (e.g., filter paper) and gravity pulls the liquid down. The solid is left on the filter, while the liquid flows below it.

- Vacuum Filtration: A Büchner flask and hose are used to pull a vacuum to suck the fluid through the filter (usually with the aid of gravity). This greatly speeds the separation and can be used to dry the solid. A related technique uses a pump to form a pressure difference on both sides of the filter. Pump filters do not need to be vertical because gravity is not the source of the pressure difference on the sides of the filter.

- Cold Filtration: Cold filtration is used to quickly cool a solution, prompting the formation of small crystals. This is a method used when the solid is initially dissolved. A common method is to place the container with the solution in an ice bath prior to filtration.

- Hot Filtration: In hot filtration, the solution, filter, and funnel are heated to minimize crystal formation during filtration. Stemless funnels are useful because there is less surface area for crystal growth. This method is used when crystals would clog the funnel or prevent crystallization of the second component in a mixture.

Sometimes filter aids are used to improve flow through a filter. Examples of filter aids are silica, diatomaceous earth, perlite, and cellulose. Filter aids may be placed on the filter prior to filtration or mixed with the liquid.

Types of filters:

- Drum Vacuum Filters

-Belt filter

-Leaf filters

- Рlate filters

-Disk filters

- Rotary filters

### Equipment’s are classified based on the application of external force.

- Pressure filters: plate and frame filter press and metafilter

- Vacuum filters: filter leaf

- Centrifugal filters

Filter partitions should have good retention capacity, low hydraulic resistance, physical and mechanical strength, chemical resistance, high porosity and uniform distribution of pores in size, maintain permeability during repeated filtration, easy to regenerate, and when filtering with clogging of pores - be sufficiently “mud-intensive”. Main filtration characteristics: type of material, water permeability, air diffusivity, porosity, strength, working pressure, mass 1 m2, linear dimensions.

Recommendations to students in preparation for lesson

The student must be prepared for lesson. Preparation consists of studying practical materials from lecture notes, textbooks and training manuals. Homework is performed in accordance with the topic of training. Each student's homework is given to the teacher at the next lesson.

Task and order of performance lesson work in the audience

1. Filtration methods

2. Types of filters

Technical and tooling facilities: multimedia board

List and types of homework: Determine the main role of filtration

Control questions

- What is filtration?

- Which types of filters do you know?

Tasks to ERIW

I. Variant (simple)

Describe about filtration methods

II. Variant (medium difficulty)

Which types of filters do you know?

III. Variant (complicated)

Which types of filters more effective, how do you think?

The list of recommended literature:

1."Filtration Methods". University of Calgary. University of Calgary. Retrieved 4 June 2015.

2. Electronic resource. Article on "Water treatment solution: Filtration", retrieved on 15 October 2013 from http://www.lenntech.com/chemistry/filtration.htm

Lecture 11. Hygroscopic properties of crystalline substances. Hygroscopic point. Sorption isotherm and solubility. Moisture absorption rate. Coefficient of hygroscopicity.

Lesson plan:

1.Hygroscopicity

2.Hygroscopic properties of crystalline substances

3.Hygroscopic point

Lesson purposes: to acquaint students with hygroscopicity

Theoretical part:

The ability of substances to absorb moisture from the air is called hygroscopicity.

All hydrophilic solids are hygroscopic. Initially, moisture is adsorbed on the surface, then gradually fills the capillaries. With an increase in relative humidity of air is growing and moisture of substance.

Hygroscopy is the phenomenon of attracting and holding water molecules from the surrounding environment, which is usually at normal or room temperature. This is achieved through either absorption or adsorption with the adsorbing substance becoming physically changed somewhat. This could be an increase in volume, boiling point, viscosity, or other physical characteristic or property of the substance, as water molecules can become suspended between the substance's molecules in the process. If a compound absorbs enough moisture so that it dissolves, then it is classed as hydrophilic.

The ratio of the equilibrium pressure of water vapor over the moisture-containing substance to the pressure of saturated water vapor at the same temperature, or, equivalently, the relative humidity of the air at which the substance does not absorb or lose water, is called a hygroscopic point of the substance.

The higher the hygroscopic point, the less hygroscopicity substance.

Characteristics of the hygroscopicity of wet water-soluble salts can practically serve hygroscopic points of their saturated solutions φ=(PH/PB)·100

- PH and PB      vapor pressure saturated solution and water

Substances with a hygroscopic point below 50% belong to very highly hygroscopic, from 50% to 60% to highly hygroscopic, from 60 to 70% to hygroscopic, from 70 to 80% to weakly hygroscopic, from 80 to 85% - to almost non-hygroscopic and above 85% - practically non-hygroscopic.

Finely crystalline and granular materials have a Loose the ability to flow freely under the action of gravitational forces. Many of them during storage lose this valuable quality, turning into a solid mass in which the individual grains are more or less firmly linked to each other. This makes them difficult to transport and use.

Definition of Hygroscopic

A hygroscopic substance is able to absorb or adsorb water from its surroundings. Typically, this occurs at or near ordinary room temperature. Most hygroscopic materials are salts, but many other materials display the property.

When water vapor is absorbed, the water molecules are taken into the molecules of the substance, often resulting in physical changes, such as increased volume. Color, boiling point, temperature, and viscosity can also change. When water vapor is adsorbed, the water molecules remain on the surface of the material.

Control questions:

1. What is Hygroscopicity?

2. What does mean hygroscopic point?

The list of recommended literature:

1. Moskvichev, Yu. A. Theoretical Foundations of Chemical Technology / Yu. A. Moskvichev, A. K. Grigorichev, O. S. Pavlov. - M.: Academy, 2005. - 272 p.

2. Pozin, M.E., Zinyuk R.Yu. Physical and chemical foundations of inorganic technology / M.E. Pozin, R. Yu. Zinyuk. - L.: Chemistry, 1993. - 437 p.

Lecture 12. Caking bulk materials. Causes of loss of flowability. Ways to prevent caking of raw materials and finished products.

Lesson plan:

1. Caking (Conglomeration).

2. Ways to prevent caking of raw materials and finished products.

Lesson purposes: to acquaint students with ways to prevent caking of raw materials

Theoretical part:

The main most common cause of loss of flowability is сonglomeration water-soluble crystalline and granular materials, ie, turning them into compacted compressed mass.

Conglomeration is caused by the formation of phase contacts at the points of contact of the particles — solid salt bridges causing the particles to adhere and agglomerate the material.

Increased moisture salt is one of the main factors contributing to its сonglomeration (caking). The ability to сonglomeration is greater, the greater the solubility of salt in water. The more the solubility of a substance changes with a change in temperature, the сonglomeration is also greater, because even in this case a large mass of substance crystallizes than when its solubility varies little with temperature. For example, potassium chloride, the effect of temperature on the solubility of which is quite significant, compresses more than sodium chloride, the solubility of which does not depend much on temperature.

To reduce сonglomeration hygroscopic fertilizers, they are sometimes produced in the form of compositions with less hygroscopic. For example, ammonium nitrate is produced in the form of alloys with ammonium sulfate (ammonium sulfate-nitrate), with potassium chloride (potassium-ammonium nitrate).

The reduction of ammonium nitrate сonglomeration is achieved by additives that slow down polymorphic transformations or lead to metastable transformation with less volumetric deformation. Addition of magnesium nitrate, which forms Mg(NO3)2·6H2O,  crystalline hydrate, binds the hygroscopic moisture of ammonium nitrate.

As surface modifying or conditioning additives, reducing caking of crystalline or granular mineral fertilizers, water-insoluble inert hydrophilic mineral powders, organic hydrophobic and polymeric substances, surface active substances are used.

Ways to prevent Conglomeration

1) Мaking products in the form of large crystals. Finely crystalline products should be monodisperse whenever possible;

2) The output of granular products with high static strength of granules;

3) Good drying and cooling of products to a temperature close to the ambient temperature before their supply to the storage;

4) Кeeping in a closed storage with constant humidity and air temperature

5) Кeeping in sealed waterproof containers (bags made of polyethylene and other films, kraft or impregnated with hydrophobic substances paper, drums from roofing iron) or in another container (jute bags, boxes, barrels, cardboard boxes). When storing in bulk, the heaps should be low and the product should be mixed periodically.

6) The use of modifying or conditioning additives.

Recommendations to students in preparation for lesson

The student must be prepared for lesson. Preparation consists of studying practical materials from lecture notes, textbooks and training manuals. Homework is performed in accordance with the topic of practical training. Each student's homework is given to the teacher at the next practical lesson.

Task and order of performance work in the audience

1. Definition of Hygroscopic

2. How store hygroscopic materials

Technical and tooling facilities: multimedia board

List and types of homework: Determine about conglomeration

Control questions:

1. What does mean сonglomeration

2. Which ways to prevent сonglomeration do you know?

Tasks to ERIW:

I. Variant (simple)

Describe about Hygroscopicity

II. Variant (medium difficulty)

Which ways to prevent of сonglomeration more effective?

III. Variant (complicated)

Give examples which hygroscopic materials more effective

The list of recommended literature:

1. "Hygroscopic compounds". hygroscopiccycle.com. IBERGY. Retrieved April 7, 2017.

2. Moskvichev, Yu. A. Theoretical Foundations of Chemical Technology / Yu. A. Moskvichev, A. K. Grigorichev, O. S. Pavlov. - M.: Academy, 2005. - 272 p.

3.Pozin, M.E., Zinyuk R.Yu. Physical and chemical foundations of inorganic technology / M.E. Pozin, R. Yu. Zinyuk. - L.: Chemistry, 1993.- 437 p.

Lecture 13-14. Theoretical foundations of the granulation process. Structural granulation in the presence of a liquid phase. The formation of granules. Granulation methods. Granulation of powders by pressing. Pelleting granulation.

Lesson plan:

1. Granulation methods.

2. Types of granulators.

Lesson purposes: to acquaint students with ways to prevent caking of raw materials

Theoretical part:

Granulation (from the Latin. Granulum-grain), the formation of solid particles (granules) of certain sizes and forms with given properties.

- Granular products in many cases have advantages than powdered ones. For example, water-soluble mineral fertilizers in granular form have better physical properties, - they keep their flowability well over time, more efficiently used by plants.

The size of the granules depends on the type of material, the method of its further processing or use, and is usually (mm): for mineral fertilizers 1-4, thermoplast 2-5, rubbers and rubber mixtures 15-25 or more, drugs (tablets) 3-25. The formation of granules with a size of less than 1 mm is sometimes called microgranulation.

Granulation can be based on compaction of powdered materials (with or without using binders), dispersion and subsequent crystallization of melts or solutions, or breakage of large pieces in crushers.

- Main indicators of granulation efficiency:

-granulometric composition;

-оutput of marketable fractions;

-the quality of the obtained granules (form, strength, piled up mass) ;

-uniformity granulemetric composition;

-granule porosity;

- conglomeration.

- Granulation methods:

Rolling includes the following stages: wetting of the material particles with a binder (water, sulfite-alcohol barda, lime water mixtures. clays, slags and other binding materials), resulting in the formation of individual nubbins - agglomerates of particles and (or) happens layering of small particles on larger ones; compaction of agglomerates in the material layer.

The process is carried out in

- drum,

- plate,

- speed and

- vibration granulators.

The principle of operation of the drum (figure 4) and plate (figure 5) granulators is based on the rotation of the drum, respectively installed horizontally or at an angle of 1-3 ° (rotation frequency 5-20 min -1), and special plates, placed at an angle of 45-55 ° (rotation frequency 5-50 min-1), within which a layer of material moves. The degree of filling them apparatus can vary from 10 to 15%. Rolling around in the drum granulator occurs on the side cylindrical surface, in the plate - mainly on the surface of the bottom plate.

Figure 4. Drum granulator

Figure 5. Plate granulator (on the left is shown the trajectory of the particle of material during the rotation of the plate).

Figure 6. Speed granulator.

For the intensification of rolling, high-speed and vibration granulators are used, in which pellets are more dense and uniform in size. In the high-speed granulator (Fig. 6), the layer of material is strongly mixed by means of a screw (rotational speed 1000-2500 min-1) and a shaft with pins or plates mounted on it. The housing of the vibration granulator - horizontal rectangular or trapezoidal box - is mounted special. springs to the base plate and using a vibrator are subjected to mechanical vibrations (frequency 5-50 Hz, amplitude 2-5 mm), due to which the material is well mixed and compacted.

Making the form of granules improves the conditions of their storage and transportation, allows to mechanize and automate the process of subsequent use of products, increases productivity and improves working conditions, reduces the loss of raw materials and finished products.

Recommendations to students in preparation for lesson

The student must be prepared for lesson. Preparation consists of studying materials from lecture notes, textbooks and training manuals. Homework is performed in accordance with the topic of training. Each student's homework is given to the teacher at the next lesson.

Task and order of performance lesson work in the audience

1. Definition of granulation, Types of granulators.

2. Main indicators of granulation efficiency

Technical and tooling facilities: multimedia board

List and types of homework: Determine about granulation

Control questions:

1. What is Granulation?

2. Which main indicators of granulation efficiency do you know?

Tasks to ERIW

I. Variant (simple)

Preparation of mineral raw materials.

II. Variant (medium difficulty)

Describe about other methods:

Crushing.

Grinding.

Screening.

III. Variant (complicated)

Ore preparation of mineral raw materials.

The list of recommended literature:

1. Dhenge, Ranjit M.; Washino, Kimiaki; Cartwright, James J.; Hounslow, Michael J.; Salman, Agba D. (2012). "Twin screw granulation using conveying screws: Effects of viscosity of granulation liquids and flow of powders". Powder Technology. 238: 77–90.

2. Sau L. Lee; Thomas F. O’Connor; Xiaochuan Yang; Celia N. Cruz; Sharmista Chatterjee; Rapti D. Madurawe; Christine M. V. Moore; Lawrence X. Yu; Janet Woodcock (2015). "Modernizing Pharmaceutical Manufacturing: from Batch to Continuous Production". Journal of Pharmaceutical Innovation. 10 (3): 191–199.

3. QDevelopment. "Wet Granulation". Retrieved 28 March 2016.

Lecture 15-16. Thermodynamic analysis of processes in the technology of inorganic substances. Chemical thermodynamics. Calculation of the thermodynamic probability of the processing of technogenic raw materials.

Lesson plan:

1. Chemical thermodynamics

2. Thermodynamic analysis of processes in the technology of inorganic substances

Lesson purposes: to acquaint students with chemical thermodynamics

Theoretical part:

The physical-chemical bases of inorganic technology are based on the chemical-technological analysis of processes with application of a number of the fundamental laws, concepts and regularities about mass and energy transfer (conservation laws). The chemical thermodynamics studies the application of thermodynamics laws to chemical and physical-chemical phenomena.

The following  questions are considered in it:

- Heat balances of processes, including heat effects of physical and chemical processes;

- Phase equilibriums;

- Chemical equilibrium.

The thermodynamic analysis of chemical and phase changes includes researching dependences of thermodynamic properties and functions of the system from intensive and extensive parameters change. It is possible to solve many important tasks in industry, project engineering and scientific research without experiment by means of thermodynamic and mass calculations:

1. Determination of conditions for the process to be possible.

2. Determination of substance stability in certain conditions.

3. Choice of  process optimal mode (temperature, pressure, concentration).

4. Suppression or elimination of side reactions.

5. Calculation of  substances properties in wide range of conditions.

The first law of  thermodynamics

The first law of thermodynamics is a particular case of energy conservation and transformation law in application to processes with heat emission, absorption or conversion. According to the first law of thermodynamics, the heat supplied to the system, is spent on change (increase) of internal energy

and on overcoming of resistances prohibitive to change of a system state, i.e. on work doing:    Q=ΔU+A

The second law of  thermodynamics

The second law is concerned with the direction of natural processes.It asserts that a natural process runs only in one sense, and is not reversible. For example, heat always flows spontaneously from hotter to colder bodies, and never the reverse, unless external work is performed on the system. The explanation of the phenomena was given in terms of entropy. Total entropy (S) can never decrease over time for an isolated system because the entropy of an isolated system spontaneously evolves toward thermodynamic equilibrium: the entropy should stay the same or increase.

Recommendations to students in preparation for lesson

The student must be prepared for lesson. Preparation consists of studying materials from lecture notes, textbooks and training manuals. Homework is performed in accordance with the topic of training. Each student's homework is given to the teacher at the next lesson.

Task and order of performance lesson work in the audience

1. Laws of thermodynamics

2. Units of measurement of heat capacity.

Technical and tooling facilities: multimedia board

List and types of homework: Describe the first law of thermodynamics. Describe the second law of thermodynamics

Control questions:

- Chemical thermodynamics

- The first law of  thermodynamics

- The second law of  thermodynamics

Tasks to ERIW

I. Variant (simple)

1. Temperature dependence of the heat capacity of substances

2. Calculate the heat capacity of substances depending on temperature

II. Variant (medium difficulty)

Units of measurement of heat capacity. Relations between different units of measurement.

III. Variant (complicated)

1. Calculate the enthalpy change of substances with temperature

2. Describe modern methods for calculating the heat capacity of substances.

The list of recommended literature:

1. Karapetyants M.Kh. Chemical thermodynamics. -M.: Chemistry, 1975.- 584 p.
2. Zinyuk R.Yu., Pozin M.E Thermodynamic analysis of chemical systems in the technology of inorganic substances. Tutorial.-L.:1977, 83 p.

Lecture 17-18. Hess law and its consequences. Methods for calculating the heat of formation and heat capacity of inorganic compounds.

Lesson plan:

1. The law of Hess and its consequences

2. Methods for calculating the heat of formation of inorganic compounds

3. Methods for calculating the heat capacities of inorganic compounds

Theoretical part:

The independence of process heat effect from its course was installed by practical consideration by Russian academician H.I. Hess’s in 1836. The Hess’s law sometimes is called as the law of constant heat summation, it is stated so:

The process heat effect does not depend on intermediate stages, and it is determined only by initial and final states of the system.

The Hess's law is the basic law of thermochemistry, which is formulated as follows: The thermal effect of a chemical reaction carried out in isobaric-isothermal or isochoric-isothermal conditions depends only on the type and state of the starting materials and products of the reaction and does not depend on the way it proceeds.

There are isobaric processes in chemical technology more often, therefore we shall consider only isobaric heat effects, i.e. It is possible to make of the Hess’s law following conclusions:

1. The formation heat of compounds from initial substances does not depend on reaction path.

2. The decomposition heat of compound up to the same initial substances is equal on value and is opposite on the sign to the formation heat of compound from the same substances.

3. If from two different systems as a result of different processes the identical products will be obtained, the difference between values of process heat effects is equal to transition heat of the first system into the second one. If the transition from identical initial states to different final is made, the difference between values of process heat effects is equal to transformation heat of the first final products into others. Two important consequences can be resuming, which have wide application:

4. The reaction heat effect is equal to the algebraic sum of formation heats of reagents from simple substances, i.e. the sum of formation heats of reaction products minus the sum of formation heats of initial substances:

5. The reaction heat effect is equal to the algebraic sum of combustion heats of reagents up to the identical products, i.e. the sum of combustion heats of initial substances minus the sum of combustion heats of reaction products:

In all cases the stoichiometric coefficients are taken into account, and it is meant, that all heat effects concern to identical aggregate states of simple substances. On the basis of the Hess’s law it is possible to calculate heat effects of reactions unavailable to immediate measurement, or such reactions, the realization which in heater is connected with different difficulties.

Hess law.

If the process is thermodynamically irreversible and at constant volume or pressure, and the resulting products have the same temperature as the original substances, then the heat released or absorbed during this process is called the thermal effect.

The Hess law states that the thermal effect of the process does not depend on intermediate stages, but is determined only by the initial and final states of the system. It is understood that the only work done by the system is to work against external pressure forces. Pressure or volume throughout the process remains unchanged. The process is thermodynamically irreversible.

The following conclusions can be drawn from the Hess law:

1. The heat of formation of a compound from the starting materials does not depend on the way this compound is obtained.

2. The heat of decomposition of a compound to the same starting materials is equal in value and opposite in sign to the heat of formation of a compound from the same substances.

3. If identical products are formed from two different systems as a result of different processes, then the difference between the values of the thermal effects of these processes is equal to the heat of transition of the first system to the second.

If, on the contrary, there is a transition from the same initial states to different final states, then the difference between the values of the thermal effects of the processes is equal to the heat of transformation of one final product into another. This results in two important consequences that are widely used:

- The thermal effect of the reaction is equal to the algebraic sum of the heats of formation of reagents from simple substances., i.e. the sum of the heats of formation of the reaction products minus the sum of the heats of formation of the starting materials:

ΔН = Σ(ΔНобр)прод - Σ(ΔНобр)исх.в 		                        (2.1)

2. The heat effect of the reaction is equal to the algebraic sum of the heat of combustion of the reactants to the same products, i.e. the sum of the heat of combustion of the original substances minus the sum of the heats of combustion of the reaction products:

ΔН = Σ(ΔНсгор)исх.в - Σ(ΔНсгор)прод 		          		        (2.2)

The dependence of the thermal effect of a chemical reaction on temperature (with constant pressure or volume) determined by Kirchhoff’s equation in the integral form:

(2.3)

The equation makes it possible to calculate the thermal effects of reactions at any temperature T, if the dependence of the heat capacities of all the reagents in the considered temperature range and the heat effect of the reaction at any one temperature is known.

After integrating the equation (2.5) we obtain the dependence of the thermal effect on temperature in general:

(2.4)

where - integration constant, which is usually determined by the experimental thermal effect obtained at a standard temperature Т = 298К according to the ratio of the form:

(2.5)

The equation (2.4) only valid for that temperature range, for which the empirical equation holds (1.4) for heat capacities of the substances involved in the reaction.

Substituting into an integral equation (2.4)  given the integration from T1 to T2, we obtain the final calculated expression in the form:

(2.6)

Where the index 1 usually corresponds to standard temperature 298 К, but index 2 some given final temperature Т2 in kelvins.

The Hess’s law and its consequences.

The independence of process heat effect from its course was installed by practical consideration by Russian academician H.I. Hess’s in 1836. The Hess’s law sometimes is called as the law of constant heat summation, it is stated so:

The process heat effect does not depend on intermediate stages, and it is determined only by initial and final states of the system.

Example 1. Calculate heat effect of reaction at standard conditions using standard formation heats of compounds:

Fe2O3(S) +3CO(G)=2Fe(S)+3CO2(G)+,

The heat effects of reaction depend on temperature practically always, therefore  standard values of heat effects  are used in thermochemical calculations. In thermodynamics standard values of heat effects are those at pressure 1atm (1.013 *105 Па) and temperature 250С=298К.

Calculation methods of formation heats of inorganic compounds.

Because of deficit of calorimetric data it is possible to find heat effects of few reactions only on the basis of formation and combustion heats immediately. At absence of data about formation or combustions heats of substances the heat effect of reaction can be calculated using methods of approximate calculation of heat effects.

One of such methods is calculation on the basis of chemical bonds energies. For this purpose decomposition of the initial simple substances on atoms (sequential transition them in monoatomic gases), and then formation of them of final gaseous compound mentally will be carried out. The first stage is connected with energy consumption on break of bonds Еin in the initial simple substances, and the second one - with energy emission of foundation of new bonds Еprod. Therefore according to the Hess’s law formation heat of gaseous substance is determined by the equation:

=                                                                                (16),

where n – the number of bonds of this type, n ' – the number of atoms of solid elements,  - heat of sublimation of solid or liquid element.

Energy of chemical bond is fraction of absorbed energy for entire dissociation of a molecule on free atoms.

The calculation of formation heats of inorganic compounds by Kapustinsky method is based on that the formation heat of compound of one element with other ones divided to one gram-equivalent is a linear function of log of ordinal number of this element. This regularity installed by Kapustinsky A.F. (1948), is expressed as the equation:

/w = a lgz+b                                                                                                          (17),

where w – active valency, z - ordinal number, a and b - empirical constants. The dependence (17) allows estimating formation heats approximately.

The approximate calculation of  of inorganic compounds some classes can be realized by method of chemically similar substances (method of comparative calculation) – using the experimental data about properties of similar substances and parameters of one-type reactions, using the additive property. All components of compared reactions should be in an identical aggregate state and should have identical stoichiometric coefficients. It is necessary to install degree of similarity at comparing, which predetermines an accuracy of result. Hereby linear dependence is used more often.

The calculation  by means of the 3-d law of thermodynamics is based on usage of equilibrium constant.

Examples of tasks:

Exercise 1. 	Determine the thermal effect of the reaction

2NaCl + H2SO4            Na2SO4 + 2HCl

under standard conditions for temperature 2980К on the basis of the first investigation of the Hess law, using the heat of formation of substances included in this reaction

Exercise 2. To derive the temperature dependence of the thermal effect of the reaction

N2(г) + O2(г) = 2NO(г)

if the dependence of the molar heat capacities of the reactants on temperature is expressed by the equations:

= 29,58 + 3,85·10-3 Т – 0,59·105 Т-2Дж/моль·град

= 27,87 + 4,27·10-3 Т Дж/моль·град

= 31,46 + 3,39·10-3 Т – 3,77·105 Т-2Дж/моль·град

Exercise 3. 	Calculate the thermal effect of the reaction

С(т) + Н2О(г)) = СО(г) + Н2(г)

at 10000К, if the molar heat capacities of the reaction participants are expressed by the equations:

= 11,19 + 10,95·10-3 Т – 4,89·105 Т-2Дж/моль·град

= 28,41 + 4,10·10-3 Т – 0,46·105 Т-2Дж/моль·град

= 30,00 + 10,71·10-3 Т + 0,33·105 Т-2Дж/моль·град

= 27,28 + 3,26·10-3 Т + 0,502·105 Т-2Дж/моль·град

Exercise 4. 	Calculate the thermal effect of the reaction of formation of thermal phosphoric acid at 3500К.

Exercise 5. Calculate the thermal effect of the reaction of the formation of extraction of phosphoric acid at 3700К.

Recommendations to students in preparation for lesson

The student must be prepared for lesson. Preparation consists of studying practical materials from lecture notes, textbooks and training manuals. Homework is performed in accordance with the topic of training. Each student's homework is given to the teacher at the next lesson.

Task and order of performance lesson work in the audience

- The theoretical essence of the first law of thermodynamics.

- Thermochemical patterns.

Technical and tooling facilities: multimedia board

List and types of homework:

- The laws of Hess.

- The thermal effect of the process.

- The influence of external factors on the thermal effect of the process.

- The effect of temperature on the thermal effect of the process.

Control questions:

1. The theoretical essence of the first law of thermodynamics.

2. Thermochemical patterns.

3. Laws of Lavoisier-Laplace.

4. The laws of Hess.

5. The thermal effect of the process.

6. The influence of external factors on the thermal effect of the process.

7. The effect of temperature on the thermal effect of the process.

Tasks to ERIW

I. Variant (simple)

Calculation of the heats of formation of substances by the energy of crystal lattices, examples of calculations.

II. Variant (medium difficulty)

Calculation of the heats of formation of substances by the binding energies, examples of calculations.

III. Variant (complicated)

Calculation of the heats of formation of complex compounds, examples of calculations.

The list of recommended literature

- Karapetyants M.Kh. Examples and problems in chemical thermodynamics. -M.: Chemistry, 1974.- 302 p.

- Pozin, M.E., Zinyuk R.Yu. Physical and chemical foundations of inorganic technology / M.E. Pozin, R. Yu. Zinyuk. - L.: Chemistry, 1993.- 437 p.

Lecture 19. Temperature dependence of the thermodynamic characteristics of substances

Lesson plan:

1. Isobaric heat capacity

2. Isochoric heat capacity

3. The dependence of thermodynamic characteristics on temperature

Theoretical part:

Calculations of thermal effects of reactions based on consequences of the Hess Act using reference thermodynamic data is limited to standard conditions (P = 1 atm; T = 298 K).

The thermal effects of chemical reactions depend on temperature, as the temperature changes, the heat capacities of the substances change - participants reaction.

Heat capacity - the amount of heat required to heating 1 mole or 1 gram (1 kg) of substance for one degree.

С - molar heat capacity, J / (mol • K)

Суд- specific heat capacity, J / (g • K) or J / (kg • K)

Ср- isobaric heat capacity

Сv- isochoric heat capacity

Average heat capacities are measured at a certain temperature range.

True heat capacities correspond to infinitely small temperature changes.

- Isobaric heat capacity (p=const)

- Isochoric heat capacity (V=const)

The dependence of thermodynamic characteristics on temperature

The internal energy of a substance is composed of several components:

U= Utrans+ Urot+ Uvib+ U intraat

The first two components – translational Utrans and rotational Urot energy - do not depend on temperature; vibrational energy Uvib significantly dependent on temperature; the value of the last component - intra-atomic - the temperature affects in different ways: at 273÷1500 К- few, at high (> 1500K) - strongly.

Given the equation of enthalpy of matter

H=U+PV= Utrans+ Urot+ Uvib+ U intraat+PV

Enthalpy dependence from temperature is realized through heat capacity. Heat capacity C is the amount of heat δQ (J) needed to change the temperature of a unit mass or amount of substance (kg, kmol) by 1 K.

Distinguish between true heat capacity (T2≈T1), average (in the range from T2 to T1), specific (per 1 kg of mass), atomic (per 1 kmol of atoms), molar (per 1 kmol of substance), and isochoric (Сv at V = const) and isobaric (Сp at Р = const).

For ideal gases, the calculation formulas of the main characteristics of the polytropic process are expressed by the equations:

C=CvδQdU

V(Cp/Cv)-1T=exp (const/Cv)

PVn=const

Table 1. Equation indicators politrops

| Process | n | C | PVn |
| --- | --- | --- | --- |
| Isobaric | 0 | Cp | P |
| Isothermal | 1 | ∞ | PV |
| Adiabatic | Y=Cp/Cv | 0 | PVCp/Cv |
| Isochoric | ∞ | Cv | PV∞ |

The table shows the values n, C and PVn equations V(Cp/Cv)-1T=exp (const/Cv) and PVn=const.

Whereas  Cv= ∂U∂Tv and Cp=∂H∂Tp, then the temperature dependences of the characteristic functions of substances without their phase transformations in the range from the base temperature T1 to the desired T2 will be

UT2=UT1+T1T2CvdT;        ST2=ST1+ T1T2Cp/T dT

HT2= HT1+ T1T2CpdT

For the stability temperatures of atoms and molecules without ionization in the gaseous state, Cp at low (near standard) pressures is associated with Cv by a simple equality, and the heat capacity values are taken only for the first three components of the equality

Cp=Cv+R=Cvtrans+ Cvrot+ Cvvib+R

It can be seen from the above equalities that if there is information about the basic values of internal energy, enthalpy, entropy (UT1, HT1, ST1), translational and rotational components, the temperature dependence of the vibrational component, you can calculate the values of the characteristic functions and entropy for a given temperature. More often, changes in characteristic functions are calculated in the range from the base temperature to the desired temperature. When calculating the temperature effect, specific data are needed on the relationship of both the individual components and the specific heat as a whole with the temperature of substances in different state of aggregation (solid, liquid or gaseous).

Control questions:

- How calculate the dependence of thermodynamic characteristics on temperature?

- Write equation of enthalpy of matter

The list of recommended literature:

- Karapetyants M.Kh. Examples and problems in chemical thermodynamics. -M.: Chemistry, 1974.- 302 p.

- Pozin, M.E., Zinyuk R.Yu. Physical and chemical foundations of inorganic technology / M.E. Pozin, R. Yu. Zinyuk. - L.: Chemistry, 1993. - 437 p.

Lecture 20. Kirchhoff equation.

Lesson plan: Kirhgoff equation

Lesson purposes: teach to students to calculate thermal reactions by Kirchhoff methods

Theoretical part:

Dependence of heat capacity from temperature is expressed usually in practice by empirical formula as a power series:

с = а + в Т + сТ2 +dТ3

or  с =  = а + в Т + сэТ-2                                                                                                       (1)

where а ,в, с, d –  empirical coefficients true for the given temperature range.

There are values of  temperature coefficients for many substances used in inorganic technology in critical tables. The true heat capacity for isobaric process is determined as:

(2)

So reaction heat effect is described by the formula:

(2)

Then temperature dependence of reaction heat effect is determined by Kirhgoff equation:

(4)

where  is a difference of sums of products and reagents molar heat capacities with account of stoichiometric coefficients.

The integral form of Kirhgoff equation is expressed as

(5)

It is possible to calculate reaction heat effects at any temperature by means of (5) equation, if temperature dependences of heat capacities and reaction heat effect at some temperature are known. Because of  equation temperature dependence of reaction heat effect is resumed after integration of (5):

(6)

where  is an integration constant determined by practical heat effect at one temperature.

The last time there are data about hyperthermal components (НТ – Н298) more often in the tables. It is possible to calculate reaction heat effect using these data under the formula:

(7)

Kirchhoff's law: the temperature coefficient of the thermal effect of a chemical reaction is equal to the change in the heat capacity of substances as a result of this process.

Kirchhoff equation in differential form:

The temperature coefficient of the thermal effect is a quantity that shows how the thermal effect of a chemical reaction changes when the temperature changes by 1 K.

Kirchhoff equation and its integration

Kirchhoff's law for chemical reaction

The dependence of the enthalpy of a chemical reaction on temperature is expressed by the Kirchhoff law.

- For chemical reaction:

This expression applies to each substance in the reaction:

Kirchhoff's law for chemical reaction

Kirchhoff's equation can be written for the dependence of the internal energy of a chemical reaction from temperature

For chemical reaction:

Kirchhoff's law for chemical reaction

Recommendations to students in preparation for lesson

The student must be prepared for lesson. Preparation consists of studying practical materials from lecture notes, textbooks and training manuals. Homework is performed in accordance with the topic of training. Each student's homework is given to the teacher at the next lesson.

Task and order of performance lesson work in the audience

1. Thermal effect

2. Kirchhoff equation

Technical and tooling facilities: multimedia board

List and types of homework: Calculation of the thermal effect by the Kirchhoff equation

Control questions:

- Write Kirhgoff equation

- Kirchhoff's law for chemical reaction

Tasks to ERIW

I. Variant (simple)

1.What is thermal effect?

2.Kirchhoff equation

II. Variant (medium difficulty)

Calculation of the thermal effect using the exact Kirchhoff equation

III. Variant (complicated)

Prove that Kirchhoff's law is a consequence of the first law of thermodynamics. Under what conditions does the heat effect of the reaction not depend on temperature? What is the physical meaning of in terms DH0

The list of recommended literature:

1. Calculations on the technology of inorganic substances. / Ed. Pozina M.E. -L .: Chemistry, 1977. -496s.

2. Haywood R. Thermodynamics of equilibrium processes. -M .: Mir, 1983.-491s.

3. Kasenov B.K., Aldabergenov M.K., Pashinkin A.S. Thermodynamic methods in the chemistry of metallurgy. - Almaty.: "Rauan" "Demeu", 1994.-256 p.

4. Bugenov E.S., Dzhusipbekov U.ZH. Theoretical foundations of chemical technology. - Almaty .: 2003. -244 p.

5. Ravdel Handbook of physico-chemical quantities, edited by -M .: Chemistry, 1987.- 348c.

6. Pozin, M.E., Zinyuk R.Yu. Physical and chemical foundations of inorganic technology / M.E. Pozin, R. Yu. Zinyuk. - L.: Chemistry, 1993. - 437 p.

Lecture 21-22.   The effect of temperature and pressure on the properties of substances and chemical systems. The equation of heat balance of chemical-technological processes.

Lesson plan: The effect of temperature and pressure on the properties of substances and chemical systems

Lesson purposes: teach to students to calculate heat balance of chemical-technological processes.

Theoretical part:

Effect of pressure on enthalpy and heat capacity

Differentiation enthalpy H=U+PV at a constant temperature, a very important form of the relation between enthalpy and pressure ∂H∂PT with full volume V and volume derivative with respect to temperature at constant pressure ∂V∂TP

∂H∂PT  =V-T∂V∂TP                                         (1)

Taking into account the coefficient of thermal expansion βP=1V∂V∂TP transform the equation (1)

∂H∂PT  =V(1-βT)

Integrating the equation (1) in the range of standard pressure Ро -final pressure P, we obtain

HP, T=HOPo,T+PoPVdP-TPoP(∂V∂T)PdP

First addendum HoPo,T calculated according to Kirchhoff’s law as a function of temperature

HoPo,T=Ho298+298TCopdT

The second and third terms are represented by integrals, which take into account the dependence of V on pressure and temperature.

Joint consideration of equations (∂z∂T)P= - PVRT2+PRT(∂V∂T)P= - PRT2[V-T(∂V∂T)p] and (1) leads to equality    (∂z∂T)P= - PRT2[V-T(∂V∂T)p]= - PRT2(∂H∂P)T

After a small rearrangement (∂H∂P)T= - RT2P(∂z∂T)P

Substitution in the last equality P=πPкр and Т=τТкр integration and transformation lead to the equation by which the enthalpy is calculated as a function of pressure

HP,T-HP,ToTкр= -Rτ2πoπ(∂z∂τ)πdInπ                                      (2)

In directories provide dependency graphs (HPo, To – HP,T)/Tкр=φ(π,τ) constructed by Koldbach and Tyne, but with a sign opposite to the sign obtained by the equation (2).

In accordance with the correction of the change in enthalpy at elevated pressure, the heat of formation ΔHf,P,T substances at high pressures are calculated by the formula ΔHf,P,T= ∆Hf, Po,To- [(HPo,To-HP,T)/Tкр]Ткр

The dependence of the specific heat on the pressure is calculated after finding the correction ΔСР,Т

ΔСР,Т= СР,Т-СPo,Tо=PoP(∂V∂T)P-T(∂2/V∂T2)PdP

which is summed with the specific heat at standard pressure РО and temperature T

CP,T=CPo,To+∆CP,T

Recommendations to students in preparation for lesson

The student must be prepared for lesson. Preparation consists of studying materials from lecture notes, textbooks and training manuals. Homework is performed in accordance with the topic of practical training. Each student's homework is given to the teacher at the next lesson.

Task and order of performance lesson work in the audience

Thermochemical equations.

Thermochemical calculations.

List and types of homework: Thermochemical equations and calculations

Control questions:

1. What is the thermal effect of a chemical reaction?

2. List the factors that influence the thermal effect of a chemical reaction.

3. Which reactions are called exothermic and endothermic? Give examples.

4. Effect of pressure on enthalpy and heat capacity

The list of recommended literature:

Pozin, M.E., Zinyuk R.Yu. Physical and chemical foundations of inorganic technology / M.E. Pozin, R. Yu. Zinyuk. - L.: Chemistry, 1993. - 437 p.

Lecture 23-24.  Methods for calculating thermodynamic characteristics. Application of comparative calculation methods in chemical thermodynamics. Calculation of heat capacity of substances. Calculation of the entropy of substances and its changes in various processes.

Lesson plan:

1. Application of comparative calculation methods in chemical thermodynamics

2. Calculation of heat capacity of substances

Lesson purposes: teach to students to calculate heat capacity of substances

Theoretical part:

Application of comparative calculation methods in chemical thermodynamics

Theoretical and practical aspects of the use of comparative methods are adequately reflected in the monographs of M. Kh. Karapetyants and V. A. Kireev. These methods allow, using previously established experimentally or theoretically thermodynamic data on the properties of similar (similar, chemically similar) substances and parameters of similar reactions, to calculate the thermodynamic properties for substances and reactions for which these data are not available.

To compare the chemical similarity of the same type of inorganic simple substances and compounds, a periodic table of the elements of Mendeleev is used. Compounds with a similar structural formula, which differ by only one element that belongs to a common subgroup or a number of elements of the periodic system and has a characteristic identical valence state, are usually considered to be of the same type. As for the chemical reactions of the same type, they include two (or more) reactions in which each component of one reaction corresponds to the same type (chemically similar) component of the other reaction. Important common features of the reactions of the same type are the same state of aggregation and the same stoichiometric coefficients.

Comparison of similar substances, series of compounds and reactions can be carried out by different forms of direct comparison. There are a lot of such forms of comparison. Consideration, for example, of the difference in the heat of formation for sulfates (the first similar series) and sulfites (the second similar series) of alkaline elements of group I of the periodic system allows us to establish the features of the dependence of this difference Δ on a specific functional indicator - the element serial number, atomic mass, atom radius, etc. This dependence can be illustrated both graphically and in the form of very simple mathematical laws. Hence, the possibility arises of estimating the heat of formation of sulfate or sulfite of an element, which occupies an intermediate place in terms of a functional indicator among the indicators used to construct the dependencies.

For a series of similar compounds, the values of two properties can be compared under constant conditions. A comparison of these two properties can be carried out in the form of a difference, if their dimension is the same, or in the form of a ratio. The comparison result is also presented in the form of mathematical dependencies with the establishment of constant coefficients inherent in this series of similar compounds. In general terms, the direct relationship between the two properties (M1 and M2) is displayed by the equation:

М2=αM1+λ

A straightforward relationship means the proportionality of the increments (ΔM) of both properties for a number of substances:

ΔМ2/ΔМ1=α

The proportionality coefficient α can reflect not only the relationship of M2 and M1 but also of other properties, most often associated with Mi,. Sometimes the equation expresses the relationship between the same property for two substances of the same type of the series (AX and BX) with some constant parameter:

МАх =αМвх +λ

In particular, the Kireev equation for the logarithms of saturated vapor pressure is represented in the form:

lgPАХ=αlgPВХ+λ

In the equation underlying the construction of the nomogram for finding the pressure of saturated vapor of liquids, the coefficient α is equal to the ratio of the heats of evaporation of the compared and standard liquids.

Let us dwell on the two methods of comparison, already mentioned above, - the method of differences and the method of relations.

The method of differences consists in a single and double comparison of the thermodynamic properties of substances of the same type or reaction parameters by subtracting a smaller value from a larger value, ensuring that the difference is minimal (λ → 0), but positive (λ>0)

λ2,1=М2-М1

Four substances or four reactions can be involved in the comparison. For this, in addition to the first comparison, another second is used: λ4,3=М4-М3

When comparing varieties of single comparisons (difference of differences or double comparison), four reactions are already involved in one mathematical equality

λ4,3- λ2,1≥0

or λ4,3= λ2,1

The desired value of the property or parameter is included in the last equality in the one-time difference λ2,1 or λ4,3.

The relationship method is also possible with a single (α2,1) and double (α4,3 / α2,1) comparisons. The maximum accuracy of the calculation of the desired value is achieved when selecting the comparison conditions, when

α2,1=(М2/М1)≥1 at   α2,1   →1

Similarly, α4.3≥1 for α4.3→ 1. The double ratio should also meet these two conditions:  (α4,3/α2,1)≥1

According to the equality, subject to the conditions, the ratio (М4/М3)=(М2/М1)

From which it is easy to find the desired property or parameter. The methods of relations and differences are very convenient when calculating the properties of substances and reaction parameters at high temperatures.

Calculation of the heat capacity of substances

The heat capacity of substances can be calculated by exact, theoretically justified methods, by semi-empirical rules and formulas, by approximate dependencies. To solve various problems using the values of isobaric or isochoric heat capacity at a given temperature (СоР, Т or Cv, T), average heat capacity in the temperature range from T1 to T2 (СоР  or Cv), true value of specific heat at ΔТ=Т2-Т1 ≈0 (СоР ,true), specific heat at specific temperature and non-standard pressure (СР, Т or Cv, T).

The temperature dependence of isobaric heat capacity is presented for inorganic substances in the form of an equation:

СоР = a +bT+c/T2                                                           (1)

As already noted, the full value of the isobaric heat capacity of a gas at a pressure close to the standard consists of four terms:

СоР = Соtrans+ Соrot+ Соvib+R

Соtrans=1,5 R; Соrot and Соvib are determined by the structure and complexity of the structure of gaseous molecules. For diatomic and linear polyatomic molecules Соrot= R; at complication of structure Соrot=1,5 R. To find the vibrational component by the equalities

Соvib=3n-5CE (θE/T)i  or Соvib=3n-6CE (θE/T)i

necessary knowledge of the molecular structure, the number of atoms n in the gas molecule, Einstein characteristic temperature θE. For simple linear structures, the number of degrees of freedom (number terms of heat capacity CE-functions relationship θE/T) constitute (3n-5), and for complex molecular configurations and for complex molecular configurations (3n-6).

For a chemical reaction, it is calculated according to the rules of the algebraic sum system heat capacity change ΔСоР by equality

ΔСоР=viСоР, i, finite - viСоР, i, primary= via i, finite - via i, primary+T (vibi, finite - vib i, primary) + 1T2 (vic i, finite - vic i, primary)= Δai +ΔbiT+Δci/T2                     (2)

if the substance is stable in a narrow temperature range 298К÷Т then its heat capacity is not described by the equation (1). In this case, when calculating the algebraic sum Δai instead ai and Δci count without bi and ci for this substance.

Applying the formula Dulong and Pti it is possible to quickly calculate the estimated heat capacity of solid and liquid substances at 298 K from the statistically established average values of atomic isobaric heat capacities C p, I , 298 and the number of atoms of each kind ni

СоР, 298=niСР, i, 298

Significance СР, i, 298 for most atoms in compounds, according to experimental data, are for solids substances 26,0 – 26,8 J/(mol ·K) and for liquid 33,5 J/(mol ·K).

Calculation of the entropy of substances and its changes in various processes

The total entropy of the substance from absolute zero to a temperature exceeding the boiling point is described by the equation:

ST= 0TI-IICp,TB,ITdT+ℷ  I-IITf, I-II+Tf,I_IITmeltingCp, s,IITdT+ℷ mTm+TmTbCp lTdT+ℷbTm+TbTCp,gTdT

The equation is based on Planck's postulate: at absolute zero, the entropy of an ideal crystal is zero. Hence the origin of the entropy is absolute zero. The equation includes:

1) the change in entropy during isobaric heating of an ideal crystal — modification I of a solid — from absolute zero to the transition temperature of modification I to modification II (T I-II);

2) the change in entropy as a result of a phase transition at constant temperature and pressure with the expenditure of heat λ I-II

3) the change in entropy during isobaric heating of modification II of a solid substance to the melting temperature (Tm)

4) the change in entropy during melting with the heat of phase transition λm

5) change in entropy during isobaric heating of a liquid substance up to the boiling point (Tb)

6) the change in entropy upon boiling of a substance with a phase transition heat λb

7) change in entropy during isobaric heating of a gaseous substance (for isochoric heating ΔS=TbTCv,gTdT); modification changes can also occur in gas.

The total entropy of gas S consists, without taking into account the internal rotation of electrons, of three terms

SoT=Sоtrans+ Sоrot+ Sоvib

Control questions:

1. Where use comparative calculation methods in chemical thermodynamics

2. How calculate of the heat capacity of substances?

3. How calculate of the entropy of substances and its changes in various processes?

The list of recommended literature:

1. Karapetyants M.Kh. Thermodynamic properties of inorganic and organic substances, 1968 – 472 p.

2. Pozin, M.E., Zinyuk R.Yu. Physical and chemical foundations of inorganic technology / M.E. Pozin, R. Yu. Zinyuk. - L.: Chemistry, 1993.- 437 p.

Lecture 25.  Calculation of the heat of formation of substances and the thermal effect of the reactions of processing of industrial waste.

Lesson plan:

1. Calculation of the heats of formation of substances and the thermal effect of reactions

2. Calculation of heat of formation of substances

Lesson purposes: teach to students to calculate heats of formation of substances and the thermal effect of reactions

Theoretical part:

The heats of formation of complex substances from simple ones at basic temperatures of 0 (ΔНof, 0) or 298 K (ΔНof, 298) can be calculated using several methods that give different discrepancies between the calculated values ​​and the experimental values. Conventionally, the heats of formation of simple substances in their most stable aggregate state at a base temperature are taken as zero. Sometimes the heat of formation of a complex compound is calculated using the heat of not simple, but complex substances. The value of the heat of formation of a complex compound calculated by this method differs from ΔНof by the sum of the heats of formation of the starting materials, referred to 1 mol (kmol) of the target substance. Typically, this calculation path is specifically indicated in the notes on the enthalpy values.

According to Hess's law, the thermal effect ΔHoT of obtaining, under the same initial and final conditions, certain chemical products from the same starting materials is a constant value that does not depend on the way chemical transformations are carried out. This means that the heat of chemical transformation, fixed for one of the possible ways, can be used as a known result of the algebraic addition of the heats of formation or combustion (decomposition) of substances for any other way of the process. When calculating the thermal effect of the reaction of the formation of a substance from simple and complex initial structures, as well as any other chemical reaction (decomposition, neutralization, substitution, exchange of ion groups, etc.), the sum of the heats of formation of the starting materials is subtracted from the sum of the heats of formation of the final products, taking into account stoichiometric coefficients vi:

ΔHoT=vi∆Hf,T,i ocont-(vi∆Hf,T,io) initial

When calculating ΔHoT according to the heats of combustion (decomposition) - the reverse course of calculation:

ΔHoT=vi∆HT,combustion,i oinitial-(vi∆HT,combustion,io)cont

The unknown value of the heat of formation (∆Hf,T,i o) of the i- component of the reaction can be included in the sum of the enthalpies of the starting or final substances.

From the law of Hess, the following consequences arise:

1. The heat of formation of the compound from the starting materials does not depend on the method of its preparation.

2. The heat of decomposition of the compound to the starting materials is numerically equal and opposite in sign to its heat of formation from the same substances with the same initial and final state parameters of the systems.

3. If the same substance is obtained from different starting materials in two possible ways, respectively, with thermal effects ∆HT1 oand ∆HT2 o, the difference between these thermal effects (ΔH=ΔHoT2 - ΔHoT1) characterizes the difference between the amounts heat of formation of starting materials.

So, the thermal effect of the reaction is equal to the algebraic sum of the heats of formation

ΔHoT=vi∆Hf,T,i o

In accordance with the individual temperature dependence of the heats of formation of each component, the thermal effect of the reaction is also a function of temperature (and pressure):

ΔHo f,T,i = ΔHof,298,i+298TCp,idT

ΔHoT = ΔHo298 +298TΔCpdT

In the presence of calculated integrals and equality, the temperature dependence can be represented as:

ΔHo f,T > 298, i = ΔHof,298,i  +(HT - H298)i

ΔHo f,T < 298, i = ΔHof,298,i  -(H298 – HT)i

Hence the thermal effect of the reaction:

ΔHoT=ΔН298о+viHT-H298i

ΔHoT=ΔН298о-viH298-HTi

Control questions:

- Hess law

- How calculate ΔHoT according to the heats of combustion?

The list of recommended literature:

1. Karapetyants M.Kh. Thermodynamic properties of inorganic and organic substances, 1968 – 472 p.

2. Pozin, M.E., Zinyuk R.Yu. Physical and chemical foundations of inorganic technology / M.E. Pozin, R. Yu. Zinyuk. - L.: Chemistry, 1993.- 437 p.

Lecture 26.  Calculation of the Gibbs energy change (ΔGoT) of chemical reactions occurring in real technological systems.

Lesson plan:

1. Calculation of changes in Gibbs energy (ΔGoT) of chemical reactions

Lesson purposes: teach to students to calculate Gibbs energy change

Theoretical part:

The Gibbs-Helmholtz equation for a chemical reaction takes into account the thermal effect (ΔHoT) and the change in entropy (ΔSoT)

ΔGoT= ΔHoT- ТΔSoT

ΔGoT chemical reactions can be calculated using various methods

1. According to standard data for a base temperature of 298 K

ΔGo298= ΔHo298- 298ΔSo298

Using this equation, the possibility of a spontaneous chemical reaction or phase transformation is evaluated under the assumption that for the reaction the sum of the changes in the specific heat ΔCoP is close to zero and does not depend on temperature. Such an estimate can be made for the temperature range from 298 K to the temperature of the change in the state of aggregation of at least one component of the reaction. Neglecting the ΔCoP value when the temperature changes from 298K leads to a certain deviation from the true ΔGoT values. The error allowed in this case depends on the ratio of ΔGo298 and the difference in the integrals of the equation.

2. In a wide temperature range of 298 ÷ T, the temperature dependence ΔGoT=φТ is taken into account in the form of the equality:

ΔGoT= ΔНoT+298Т∆СpodT-T∆S298o-T298T∆CpoTdT

This equation can be solved by several methods:

a) according to average heat capacities ΔСoT for the interval 298 ÷ T

ΔGoT= ΔНo298+ ΔСoР (Т-298) - Т ΔSo298 – T ΔСoP  ln (T/298)

The possibility of error arises due to the fact that the curvilinear dependences of the specific heat on temperature are replaced by straight-line ones, which is correspondingly reflected in the value ΔСoр

b) by the method of disclosing the integrals included in the equation

298T∆CpodT=298T(∆a+∆b*T+∆c,/T2) dT

298T∆CPoTdT=298T∆a+∆bT+∆c,T2TdT

The exclusion of the integral quantities Δс'/Т2 or ΔbT+ Δс'/Т2 somewhat simplifies the calculation, but the error increases.

c) by the Temkin-Schwartzman method, according to which the equation for inorganic substances is presented in a rearranged form:

ΔGoT= ΔНo298-TΔSo298  - T (ΔaMo+ΔbM1+Δc'M-2)

Here Mo, M1 and M-2 factors determined only by temperature (given in the corresponding Temkin-Schwartzman tables)

d) by the method of high-temperature (Т> 298) and low-temperature (Т <298) components of enthalpy

298Т∆CpodT=vi(HT-H298)i

and entropy

298Т∆CPoTdT=viSTo-S298oi

The dependence ΔGoT=φТ is written for this calculation method in the form of equality:

ΔGoT=ΔHo298 +viHT-H298i-T∆S298o-Tvi(STo-S298o)i

When using reference data, the speed of calculation using this method using improvised calculation tools (microcomputers, arithmometers, slide rules, etc.) is higher than by the methods described in paragraphs b and c.

The accuracy of the solution for all these methods is close to each other and quite close to the experimentally found values.

3. The ΔGoT values of the reactions are found as the algebraic sum ΔGoT, i for the components, taking into account stoichiometric coefficients for them:

ΔGoT= vi∆GT,io

4. The calculation of ΔGoT reactions can be performed by the method of Ф* - potential (absolute entropies, reduced thermodynamic potentials)

ΔGoT=∆HT1o+Tvi(GTo-HT1o)/Ti

In contrast to equality, the thermal effect in the formula is calculated not for temperature T, but for the base temperature T1 (most often T1 = 0 K), from which the value Фi* of the potential is calculated for temperature Т

Фi*= - (GTo-HT1o)/Ti

If there are no data on the heats of formation at Т1 (ΔHof,T1), but there are those for temperature T (including for T = 298 K), then the equality is transformed into the equality:

ΔGoT=∆HTo-vi(HTo-HT1o)+Tvi(GTo-HT1o)/Ti

Or for two base temperatures of 298 K and 0 K

ΔGoT=∆HTo-vi(HTo-H298o)i-vi(H298o-H0o)+Tvi(GTo-H0o)/Ti

5. For the corresponding series of chemical reactions in a certain temperature range, the entropy factor

TΔSoT≈const.

Hence, knowing TΔSoT for one corresponding or for a series of corresponding reactions, as well as the value of the thermal effect of the reaction under study, we can calculate for it ΔGoT.

Control questions:

1. The Gibbs-Helmholtz equation

2. How calculate average heat capacities ΔСoT?

3. Temkin-Schwartzman method

The list of recommended literature:

1. Karapetyants M.Kh. Thermodynamic properties of inorganic and organic substances, 1968 – 472 p.

2. Pozin, M.E., Zinyuk R.Yu. Physical and chemical foundations of inorganic technology / M.E. Pozin, R. Yu. Zinyuk. - L.: Chemistry, 1993.- 437 p.

Lecture 27.  Calculation of properties of solutions. Application of additivity rule to multicomponent solutions.

Lesson plan:

- Calculation of properties of solutions.

- Application of additivity rule to multicomponent solutions.

Lesson purposes: teach to students with Zdanovsky rule

Theoretical part:

Application of additivity rule to multicomponent solutions

In the calculations, first of all, the relationship between the concentration in binary (mi*) and multicomponent (mi) solutions and the desired properties is established according to the Zdanovsky rule at the same temperature and pressure and, very importantly, at the same water activity in binary solutions and in their mixtures.

For concentrations of mixed and binary solutions, for example, for a four-component system consisting of water and three salts with a common ion, the mathematical interpretation of the Zdanovsky rule is displayed by the equation below. This equation includes the mass fraction of mixed solutions, calculated as the ratio of concentrations mi /mi*

m1 /m1*+m2 /m2*+m3/m3*…..=1

Isopietes (lines of equal vapor pressure) and water isoactivates of binary and mixed solutions in the composition - property diagram are characterized in this case by the equalities:                            Р1=Р2=Pi=Pcm.p

a1=a2=ai=acm.p

Deviation from the Zdanovsky rule of concentrations and mass fractions of mixed solutions having the same values of aH2O, i can be estimated by the value Δ, expressed as a percentage:

Δ =(m1/m1*+m2/m*+m3/m3* - 1)100

Graphically, the Zdanovsky rule for a four-component system, for example, NaCl-KCl-LiCl-H2O (figure 7), is illustrated in the form of straight lines — isoactivate (aH2O = const) D'C'; D''C''; B'C'; B''C'' if you measure the concentration in the molar and molar scales. The segments of isoactivates inside the regions of OBE1C and OCE2D are characteristic of saturated solutions, and the isoactivates of saturated and supersaturated solutions are located at the intersection points of the isoactivate with the solubility lines (l and m) and above them (segments lC'' and mC''). It should be noted that with a strict consideration of the issue, the isoactivates should have some curvature (see the dashed lines C'D') - this is due to the interaction of electrolyte particles (their structuring). Therefore, Kirgintsev and Lukyanov proposed an amendment to the isoactivate equation with the introduction of the coefficient b (b= -0,047÷0,016):

m1/m1*+m2/m2*=1-[bm1m2/(m1+m2)]

The value of b depends not only on the nature of the components of the solution, but also on aH2O and the ratio m1/ m2. In a thermochemical study of the mixing of solutions with aH2O = const, deviations from additivity are well traced by the values of the change in heat and entropy of mixing.

According to Zdanovsky, to determine the properties of a mixed solution by the properties of binary isopiestic solutions, it is necessary to choose a value of aH2O for which the equation is satisfied:

х1/х1*+х2/х2*+….+xi/xi*=1

The construction necessary to determine the composition of binary solutions (xi*) is performed in the coordinates aH2O-xi (figure 8). For this, from the literature data on the point aH2O = 1 (xi = 0), the dependence aH2O = φ (xi*) is constructed for each component of the mixed solution. After application, the polyactivate as a function of concentration parallel to the x axis is carried out isoactivate aH2O, cm.p, corresponding to the activity of water in the mixed solution.

Figure 7. Isoactivates of water in the projection of a simple four-component system NaCl-KCl-LiCl-H2O

Figure 8. Graphic finding of the compositions of isoactivate solutions

Perpendiculars are lowered from the points of intersection of the isoactivates with the lines of polyactivate to determine the composition of binary solutions with water activity equal to the activity in a mixed solution. Using the formulas below, the numerical value of the properties of the mixed solution is calculated, such as heat capacity C, density ρ, coefficient of volume expansion α/ρ, kinematic yield coefficient ρ/η, molar volume of solution V, etc.

C=C1x1/x1*+C2x2/x2*+ …..+Cixi/xi*

ρ=1/[x1(x1* ρ1)+x2/(x2* ρ2)+ ……+xi/(xi* ρi)]

ρ=ρ0(1-φiCi/1000)+Mici/1000

αρ=α1ρ1x1x1*+α2ρ2x2x2*+……+αiρi(xixi*)

ρη=ρ1η1x1x1*+ρ2η2x2x2*+……+ρiηixixi*

V=N0φ0+φiNi

Where, ρо- density of water; φi and φ0- apparent molar volumes of electrolyte and water; ci- molar concentration of electrolyte; Mi is the molecular weight of the electrolyte; N0 and Ni is the number of moles of water and electrolyte.

Control questions:

1. Zdanovsky rule

2. Zdanovsky rule for a four-component system

The list of recommended literature:

1. Karapetyants M.Kh. Thermodynamic properties of inorganic and organic substances, 1968 – 472 p.

2. Pozin, M.E., Zinyuk R.Yu. Physical and chemical foundations of inorganic technology / M.E. Pozin, R. Yu. Zinyuk. - L.: Chemistry, 1993.- 437 p.

Lecture 28.  Calculation of the properties of the solution by comparative methods.

Lesson plan:

- Comparative calculation methods

- Calculate the density ρt

Lesson purposes: teach to students with calculation of the properties of the solution by comparative methods

Theoretical part:

Comparative calculation methods are also applicable to solutions. It has been established that the ratio of temperature coefficients of viscosity, density, vapor pressure and electrical conductivity of a solution to similar values of a solvent or a standard solution is almost constant over a wide temperature range.

To calculate the density ρt of any solution with concentration m, it is necessary and sufficient to obtain experimental data on density polyconcentrates for two temperatures - ρt2 and ρt1; to build graphical dependences ρt = f(ρot) of the density of the solution on the density of the solvent; calculate the ratio of temperature density gradients (Δρt/∆ρot) solution (Δρt= ρt2- ρt1) and solvent (Δρ0t= ρ0t2- ρ0t1) and build its dependence on concentration:

Δρt∆ρt0=1-Bpm

Here is the Bp - ratio of temperature gradients for a standard solution with a concentration of m = 1.

It is believed that this ratio is approximately constant at different temperatures and decreases with increasing concentration.

The temperature dependence of the density of water is depicted in this case by the equation:

ρto=ρH2Oo+3*10-5t-4,5*10-6t2+5*10-9t3+2*10-13t4

Here ρH2Oo-is the density of water at 0°C; t- in oC.

Using this equation, the density of water is calculated with an accuracy of ± 0.2% for the interval 0-240°C and 0.5% at 250-300°C.

A kink in the straight line may indicate the formation of chemical compounds in the solution from the corresponding concentration range. Due to the fact that the equation does not take into account the compressibility factor of the solution and changes in its structure with increasing temperature, the error in calculating the density at 250-300°C will be -2 and -6%, respectively.

Using a similar sequence of reasoning, a peculiar relationship was obtained between the temperature coefficients of dynamic viscosity and concentration:

Δηt/Δηt0=1+Bηm2

When calculating the pressure of water vapor over aqueous solutions of electrolytes, you can apply the equation:

ΔPt/ΔP0t=1+Bpm

Table 2. Coefficients of activity γо  at 25 ° C of electrolytes, differing in temperature ranges, in which the maximum electrical conductivity is located.

| I group;100÷120 оС |  | II group;160÷250 оС |  |  |  | III group; >260 оС |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| electrolyte | γо | electrolyte | γо | electrolyte | γо | electrolyte | γо |
| CdSO4 | 0,037 | CoCl2 | 2,48 | BaCl2 | 0,45 | KNO3 | 0,23 |
| ZnSO4 | 0,048 | NiCl2 | 4,80 | Na2CrO4 | 0,45 | NaCl | 1,00 |
| CuSO4 | 0,036 | NaAlO2 | - | NaOH | 31,2 | KCl | 0,58 |
| FeSO4 | - | KAlO2 | - | KOH | 55,4 | Na3PO4 | 0,097 |
| MnSO4 | 0,045 | Na2MoO4 | - |  |  |  |  |
| MgSO4 | 0,05 | Na2SO4 | 0,15 |  |  |  |  |
| CoSO4 | - | MgCl2 | 31,6 |  |  |  |  |
| NiSO4 | 0,037 | CaCl2 | 41,2 |  |  |  |  |
| FeCl3 | 1,57 | SrCl2 | 1,5 |  |  |  |  |

Somewhat different are the calculation of the electrical conductivity of electrolyte solutions. For comparison, take temperatures t* at which there are absolute maxima of electrical conductivity. In this case, electrical conductivity isotherms are constructed for t1 <t * and t2> t *. It is believed that the appearance of a maximum of electrical conductivity coincides with a decrease in the dielectric constant of water. In our opinion, each of the three temperature ranges for the maximum values ​​of electrical conductivity (at t*) can also be characterized by the activity coefficients of compounds in a saturated solution, using γo even at 25°C, and not at t*. The possibility of such a connection is especially evident for the first group of electrolytes (in the table), in which the maximum electrical conductivity of the compounds lies in the temperature range 100 ÷ 120°C.

Based on the values of γo (at 25°C), the first group contains electrolytes, the constituent parts of which form mostly dissolved complexes. In the second and third groups, as a rule, electrolytes are presented, which form ion pairs or hydrates in saturated solutions at 25°C.

Control questions:

1. How calculate the ratio of temperature density gradients?

2. Coefficients of activity γо

3. Write the equation the temperature dependence of the density of water

The list of recommended literature:

1. Karapetyants M.Kh. Thermodynamic properties of inorganic and organic substances, 1968 – 472 p.

2. Pozin, M.E., Zinyuk R.Yu. Physical and chemical foundations of inorganic technology / M.E. Pozin, R. Yu. Zinyuk. - L.: Chemistry, 1993.- 437 p.

Lecture 29. The role of chemical interactions in changing the physicochemical properties of the solution. Entropy analysis of interactions.

Lesson plan:

1. Calculation of the entropy change of a chemical reaction

2. Entropy analysis of interactions

The purpose of the lesson: - to teach students the calculations of the entropy of isobaric processes.

Theoretical part:

Entropy analysis of interactions.

It was previously noted that in the absence of chemical interactions between the particles that form the solution, the additivity rule is quite applicable in calculating its properties. Chemical interactions complicate the method of calculating the properties of a solution, while the most difficult is to evaluate the effect of chemical interactions for infinitely diluted and supersaturated solutions. However, this becomes possible if a substance or group of substances in a dissolved state is compared with a change from small concentration values ​​to saturation with compared and other components. In particular, such an assessment can be carried out by analyzing the entropy changes in the solution components. Of all the thermodynamic functions, entropy (and its change ΔSfull) is determined to the greatest extent by the structure of the solution.

The change in the entropy of the system ΔSfull consists of the change in the entropies of the ideal ΔS (due to a change in concentration) and non-ideal (excess) ΔS (due to chemical interactions of the solution particles)

ΔSfull= ΔSideal+ΔSexcess

Accordingly, for each i component of the solution (solvent and dissolved substances), the relative partial molar entropies are calculated by the equalities:

∆Gi=Li-T∆Si, full

ΔSi,full= ΔSi,ideal+ΔSi,excess

For solvent:

ΔS1,excess= ΔS1,full – ΔS1,ideal

Moreover

ΔS1,full=(L1-ΔG1)/T=(L1-RTlna1)/T

ΔS1,ideal=-RLnx1

L1=λo-λp

Here λo and λp is the enthalpy of evaporation of the solvent, respectively, from pure water and solution.

Substituting expressions into the equation, we obtain

ΔS1,excess=(L1-RTlna1x1)/T=(L1-RTlnγ1)/T

Thus, by calculating the ΔS value of any component, we can judge the directions of chemical interactions in which not only the solvent but also other components of the solution take part.

Recommendations to students in preparation for lesson

The student must be prepared for lesson. Preparation consists of studying practical materials from lecture notes, textbooks and training manuals. Homework is performed in accordance with the topic of training. Each student's homework is given to the teacher at the next practical lesson.

Task and order of performance work in the audience: Calculation of entropy change

List and types of homework: do exercises to determination of entropy change

Control questions:

1. The theoretical essence of the second law of thermodynamics.

2. The theoretical essence of the third law of thermodynamics, Planck's postulates.

3. On the essence of the entropy index of processes.

4. Characteristic changes in entropy for processes proceeding in a given direction.

5. Characteristic changes in entropy for processes proceeding in the opposite direction.

6. Characteristic changes in entropy for processes in equilibrium.

7. The relationship of entropy with the main thermodynamic parameters and parameters.

8. The effect of temperature on entropy.

9. Methods for calculating changes in entropy.

Tasks to ERIW

I. Variant (simple)

Second thermodynamics. Entropy

II. Variant (medium difficulty)

Entropy changes with temperature and as a result of phase transition

III. Variant (complicated)

Calculation of changes in isobaric-isothermal potential

The list of recommended literature

1. A.B.Remizov. Thermodynamic calculations of chemical-technological processes. The text of the lectures / Remizov AB; Kazan.Technol.un-t. Kazan, 2006. 140 p.

2. Karapetyants M.Kh. Thermodynamic properties of inorganic and organic substances, 1968 – 472 p.

3. Pozin, M.E., Zinyuk R.Yu. Physical and chemical foundations of inorganic technology / M.E. Pozin, R. Yu. Zinyuk. - L.: Chemistry, 1993.- 437 p.

Lecture 30. Thermodynamic characteristics of mixed solutions of sulfuric and phosphoric acids. System HNO3-H2O. System H2SO4-H2O. H3PO4-H2O system. The final lecture on the theoretical foundations

Lesson plan:

1. Thermodynamic characteristics of mixed solutions of sulfuric and phosphoric acids

2. System HNO3-H2O.

3. System H2SO4-H2O.

4. System H3PO4-H2O

The purpose of the lesson: - to teach students the Systems HNO3-H2O; H2SO4-H2O; H3PO4-H2O.

Theoretical part:

Thermodynamic characteristics of mixed solutions of sulfuric and phosphoric acids

Consider mixed solutions of sulfuric and phosphoric acids as an example. Since they are dealt with in some chemical industries, this necessitates studying the physicochemical properties of solutions of the H3P04—H2S04—Н20 ternary system in wide concentration and temperature ranges. Data on the pressure and heat of vaporization of water vapor, boiling points and thermochemical characteristics of phosphoric acid solutions are of practical value in the development of new processes for the production of concentrated phosphoric acid and phosphoric fertilizers with controlled distribution of heat and water according to the main stages, when solving problems associated with the solubility of salts, phase transformations of calcium sulfate, evaporation of systems containing phosphoric acid.

Suggest the presence of an acid-base interaction between phosphoric and sulfuric acids, similar to that observed in their anhydrous mixture. This allows us to expect a significant mutual influence of dissolved sulfuric and phosphoric acids when they are mixed, which is reflected in the dependences of the physicochemical properties of the ternary system on its composition.

Table 3. Water activity in solutions of the Н3РО4-H2SO4-Н20 system at 25–90°С

| Mass ratio of acids | Composition mixture |  |  | Water activity at temperature |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | H2O, mol.share | H3PO4, % | H2SO4, % | 25°С | 60°С | 90°С |
| 155 | 0,92 0,881 0,765 0,65 | 31 42,5 62 74 | 0,2 0,28 0,4 0,48 | 0,870 0,745 0,475 0,269 | 0,885 0,760 0,490 0,308 | 0,905 0,735 0,505 0,508 |
| 15,5 | 0,92 0,87 0,735 0,62 | 31 42,5 62,2 74 | 2 2,74 4,1 4,8 | 0,860 0,680 0,430 0,140 | 0,855 0,710 0,440 0,165 | 0,850 0,730 0,464 0,187 |
| 5,6 | 0,92 0,86 0,76 0,62 | 27 41 53 65,5 | 4,8 7,3 9,35 11,6 | 0,848 0,750 0,400 0,147 | 0,856 0,715 0,431 0,172 | 0,863 0,695 0,460 0,193 |
| 2 | 0,92 0,855 0,76 0,62 | 21,4 32 41,85 51,3 | 10,5 16,1 21 25,4 | 0,850 0,615 0,346 0,100 | 0,850 0,635 0,382 0,130 | 0,850 0,670 0,405 0,157 |
| 0,23 | 0,92 0,855 0,76 0,62 | 6,4 9,0 11,8 14,4 | 28 39 51,2 62,5 | 0,745 0,430 0,147 0,004 | 0,725 0,452 0,178 0,01 | 0,718 0,479 0,208 0,016 |

The thermodynamic properties of solutions of the Н3РО4-H2SO4-Н20 system were studied [75] in the temperature range from 25 to 90°С with a mass or molar ratio Н3Р04: H2S04 (Д) from 155 to 0.23 and a water content from 0.92 to 0.62 mol.share, that is, in the field of concentrations used in the production of simple and double super ¬ phosphate and extraction phosphoric acid. The obtained data were used to calculate some thermodynamic characteristics aH2O, γH2O, ΔSH2O

The lack of data on acid dissociation in ternary system solutions did not allow, when calculating the molar fraction of water xH2O, to take into account the degree of dissociation, i.e., xH2O was calculated from the ratio:

xH2O= nH2O/( nH2O+nН3РО4+nH2SO4)

As can be seen from the table. 3 data, the activity of water in phosphoric acid solutions decreases with a decrease in the molar fraction of water and increases with increasing temperature; the latter is especially characteristic for mixtures containing from 0.76 to 0.62 molar fractions of H2O.

The activity coefficient of water depends on the ratio of D acids in the mixture with a constant water content (Fig. 9). For a constant content of the total amount of acids, with an increase in the proportion of phosphoric acid γH2O grows, and this is especially sharp in the interval D from 0.23 to 2. This is possibly a consequence of the redistribution of water between the components in the studied concentration range.

The presence of a water distribution between the structural groups of sulfuric and phosphoric acids in a mixed solution is indicated by the obtained dependences of the experimental heats of mixing of the starting materials on the composition. As can be seen in fig. 10, the exothermicity of the heat of mixing solutions of sulfuric and phosphoric acids decreases with an increase in the acid component. This addiction, and also the dependence of water activity on temperature is characteristic of type 1 electrolytes according to the classification of Mishchenko and Pronina, during the formation of which the hydration effect dominates over all the others.

Figure 9. Dependence γH2O from D and temperature at xH2O=0.62 share of units

Figure 10. The effect of the final total molal concentration mΣ sulfuric and phosphoric acids on ΔНm at 25°С

In fig. 11, the effect of the concentration of phosphoric acid on the thermal effect of the dissolution of sulfuric acid is clearly traced. It is seen that when mixing binary solutions, the degree of hydration characteristic of a solution of sulfuric acid in water with the same molarity as in the resulting mixtures is not achieved. For example, when sulfuric acid is dissolved in a phosphoric solution with a concentration of 62% Н3Р04, the thermal effect of mixing is 38–39% less than the thermal effect of the dissolution of sulfuric acid in water.

From the data on the vapor pressure, using equations ΔS1,excess= ΔS1,full – ΔS1,ideal and ΔS1,excess=(L1-RTlna1x1)/T=(L1-RTlnγ1)/T, the excess (non-ideal) fractions of the relative partial molar entropies are calculated ΔSH2O. For the average temperatures of the studied range (from 25 ° С to the boiling point), the values ΔSH2O depend (Fig. 12) on the water content and the ratio of acids D. At xH2O=0,76 for almost all D values ΔSH2O are negative.

mH3PO4, mol per 1000 g H2O

Figure 11. The effect of molar concentration of phosphoric acid mH3PO4 on thermal effect ΔHm dissolving sulfuric acid

Line А - heat of dissolution without influence H3PO4. mH2SO4 in a mixed solution, mol per 1000 g H2O: 1-1,03; 2- 0,55; 3- 0,13.

Figure 12. Character of change ΔSH2O, in solutions systems Н3РО4-H2SO4-Н20

xH2O share of units: 1-0,62; 2-0,76; 3-0,86; 4-0,92.

For region D from 1 to 31, positive and negative extremes are observed, indicating the formation of stable hydrates. Negative extrema characterize the preferential binding of water with phosphoric acid to strong hydrates, which are destroyed by an increase in sulfuric acid content (positive extrema).

Thermodynamic analysis showed the complexity of the processes occurring in mixed solutions of sulfuric and phosphoric acids, which prevents the a priori calculation of a number of physicochemical properties of the ternary system Н3Р04 - Н2S04 – Н20 according to the data on binary systems.

System HN03—Н20

Nitric acid solutions of various compositions are used in the synthesis of inorganic and organic substances. As follows from the data

excess fractions of the OРM of the entropy of water (ΔSH2O) and nitric acid (ΔSHNO3) at 40°C change significantly depending on the content of HNO3.

When water is added to the HNO3 – H20 system (Fig. 13), its first portions, added to the solution with xHNO3 > 94%, where the main condition is the self-dehydration equilibrium with the formation of NO2+  +   + NO3- ions, shift this reaction to the left.

At xHNO3 < 94% ions NO2+ practically no, but hydrates are formed (HNO3)2·  Н20 and HNO3 ×  ×Н20. System is ordered and values ΔSH2O and ΔSHNO3 are decreasing.

Figure 13. The equilibrium of particles in a solution of nitric acid

Beginning with xHNO3≈90%, the values ΔSH2O sharply decrease, but ΔSHNO3 - pass through a minimum of about xHNO3≈5,7%. From Figure 14. shows that due to a decrease in the H20 content with increasing xHNO3, the proportion of H3О+ monotonically reaches an infinitely small value (above ~ 90% HNО3). A decrease in the degree of electrolytic dissociation (simultaneously with the formation of hydrates) leads to a decrease in vapor pressure and (almost simultaneously with this) to an increase in viscosity. The specific electrical conductivity of the solution reaches its maximum value at xHNO3≈30%, and then decreases to vanishingly small values in the concentrated solution.

For the density of nitric acid solutions, the expression is obtained:

∆ρt/∆ρto=1+0,081m  (for m≤13)

System H2SO4—Н2O

The applied value of sulfuric acid is unusually high. Its solutions have been thoroughly studied. A diagram of the equilibrium concentrations of particles in a solution (H2SO4, HSO4-, SO42-), according to Jung, is presented in Fig. 15.

Figure 14. Change in the molar fraction of various particles (axis A) and physicochemical properties (axis B) at 20°C depending on the content HNО3

Particles: 1- H3O+ and NO3-; 2- undissociated HNО3; 3- HNО3·3H2O and HNО3·H2O; 4- HNО3·3H2O. Properties: 5- pressure vapors P·10-3, Pa; 6- viscosity η·10-3,Pa sec; 7- specific electric conductivity ϰ·10-3, cm / m

Figure 15. The diagram of equilibrium concentrations of particles contained in a solution of sulfuric acid at 25°C

Table 4. Properties of sulfuric acid hydrates

| Hydrate formula | Distectic temperature, °C | Concentration H2SO4 (%)at distectic temperature | Heat of melting, kJ / mol |
| --- | --- | --- | --- |
| H2SO4 H2SO4·H2O H2SO4·2H2O H2SO4·3H2O H2SO4·4H2O H2SO4·6,5H2O | 10,3 8,48 -39,5 -36,4 -24,3 -52,9 | 100 84,5 73,1 65,8 57,6 45,6 | 10,7 19,4 18,2 24,0 30,6 34,2 |

For sulfuric acid solutions characteristic of equilibrium with dissociation degrees α1  and α2:

2H2O+ H2SO4 α1  2H3O++ SO42-                             (A)

H2SO4+ H2O α2 H3O++ HSO4-	   (B)

According to various sources, it can be concluded that the reaction of complete dissociation (A) proceeds completely (α1≈1) only in solutions with a concentration of up to 0.3 mol/L. At CH2SO4 from 0.3 to about 14 mol/L, the formation of dissolved particles occurs in both reactions, and as the concentration increases, the reaction with the formation of the hydrosulfate ion (B) prevails. At CH2SO4> 14 mol/L, the content of hydroxonium ions of H3O+ and the HSO4- anion sharply decreases (at CH2SO4=18 mol/L, α2 = 0.04). At the same time dissociation ceases sulfuric acid molecules.

The formation of hydrates is typical for sulfuric acid solutions (Table 4), and with a change in the number of water molecules in the hydrate, the properties of the H2SO4·nH20 molecules abruptly change.

System Н3Р04—Н20

Phosphoric acid solutions are widely used in the production of mineral fertilizers, phosphate feed and industrial salts. Typically, phosphoric acid is classified as medium strength acid - the constant of the first stage of dissociation at 25°C is 7.3 •10-3. Therefore, even in weak solutions, the H3PO4 molecule dissociates only partially, unlike HNO3 or H2SO4, which completely dissociate in weakly concentrated solutions.

As follows from fig. 16, a, an increase in the concentration of H3PO4 leads to the accumulation of hydrogen ions (pH decreases). This is explained by the fact that the monomeric H3PO4 molecules combine into dimers (and into more complex associates), which dissociate to a greater extent than monomers:

nH3PO4→ (H3PO4)n+H2O→(H2PO4)nn-+ nH3O+

An increase in temperature decreases the degree of dissociation and activity of hydrogen ions. According to fig. 16, b at 25–80°С the coefficient of activity of water becomes less than 1 at a concentration 18-30% Н3РО4, that is, all free water is bound by accumulating protons in Н30+.

Figure 16. The effect of temperature on pH (a) and the coefficient of activity of water (b) in a solution of * phosphoric acid

The dependence of the solubility of many sparingly soluble compounds on the concentration of Н3РО4 is expressed by a curve with a maximum. On the ascending part of the curve, the increase in solubility with increasing Н3РО4 concentration is explained by an increase in the activity of hydrogen ions, and on the descending (after the maximum), by a decrease in the content of free water.

Recommendations to students in preparation for lesson

The student must be prepared for lesson. Preparation consists of studying practical materials from lecture notes, textbooks and training manuals. Homework is performed in accordance with the topic of training. Each student's homework is given to the teacher at the next practical lesson.

Task and order of performance work in the audience: Calculation of entropy change

List and types of homework: do exercises to determination of entropy change

Control questions:

1. Thermodynamic characteristics of mixed solutions of sulfuric and phosphoric acids

2. System HNO3-H2O.

3. System H2SO4-H2O.

4. System H3PO4-H2O

Tasks to ERIW

I. Variant (simple)

System HNO3-H2O.

II. Variant (medium difficulty)

System H2SO4-H2O.

III. Variant (complicated)

System H3PO4-H2O

The list of recommended literature

1. A.B.Remizov. Thermodynamic calculations of chemical-technological processes. The text of the lectures / Remizov AB; Kazan.Technol.un-t. Kazan, 2006. 140 p.

2. Karapetyants M.Kh. Thermodynamic properties of inorganic and organic substances, 1968 – 472 p.

3. Pozin, M.E., Zinyuk R.Yu. Physical and chemical foundations of inorganic technology / M.E. Pozin, R. Yu. Zinyuk. - L.: Chemistry, 1993.- 437 p.

Assessment criteria

| LetterGrade | Points in numbers | %-percentage | Assessment in traditional system | Criterion of education receiver’s knowledge assessment |
| --- | --- | --- | --- | --- |
| А | 4,0 | 95-100 | Excellent | The student demonstrates: - a deep and lasting assimilation of program material - complete, consistent, competent and logically presented answers for all types of activities; - Ability to freely cope with the tasks; - correct, well-founded decisions, - skills in the use of information from basic and additional specialized literature in the study of discipline, - Ability to work with foreign literature and information resources of the Internet; - Timely and high-quality execution of all types of tasks. |
| А- | 3,67 | 90-94 |  | The student demonstrates: - Deep assimilation of program material; - complete, consistent and logically presented answers for all activities; - ability to cope with the tasks; - the right decisions, - skills of using special literature in the study of discipline, - the ability to self-systematize the program material; - Timely execution of all types of tasks. |
| В+ | 3,33 | 85-89 | Good | The student demonstrates: - assimilation of program material; - complete, consistent, literate, without significant inaccuracies, an account of the answers for all kinds of tasks; - correct application of theoretical knowledge - Possession of necessary skills in the performance of applied tasks - skills in using recommended literature in the study of discipline, - skills of systematization of program material; - Possession of skills and techniques for performing all types of tasks; - Timely execution of all types of tasks. |
| В | 3,0 | 80-84 |  | The student demonstrates: - assimilation of program material; - a consistent presentation of the answers for all types of tasks with non-essential errors; - skills in applying theoretical knowledge under the guidance of a teacher; - Possession of necessary skills in performing practical tasks - skills in using recommended literature in the study of discipline, - skills of systematization of program material under the guidance of a teacher; - mastering the skills of performing all kinds of tasks; - the ability to independently correct mistakes made; - the timely execution of all types of tasks with the elimination of errors. |
| В- | 2,67 | 75-79 |  | The student demonstrates: - assimilation of program material; - Ability to present answers with non-essential errors; - skills in applying theoretical knowledge under the guidance of a teacher; - Possession of techniques in the performance of practical tasks - skills in using recommended literature under the guidance of a teacher - skills of generalization of program material under the guidance of a teacher; - the ability to correct mistakes made with the help of a teacher; - the timely execution of all types of tasks with the elimination of errors. |
| С+ | 2,33 | 70-74 | Good | The student demonstrates: - mastering of the main material; - Inadequate formulations when responding to all kinds of tasks; - violation of the sequence in the presentation of the program material; - difficulties in self-fulfillment of practical tasks; - Possession of individual techniques in the performance of practical tasks - skills in using the literature recommended by the teacher; - skills of generalization of separate sections of program material under the guidance of a teacher; - the ability to correct major mistakes made with the help of a teacher; - execution of all types of tasks with elimination of errors. |
| С | 2,0 | 65-69 | satisfactorily | The student demonstrates: - mastering of the main material; - Inadequate understanding of formulations when answering all types of assignments; - lack of consistency in the presentation of the material; - difficulties in self-fulfillment of practical tasks; - Possession of separate receptions at performance of tasks - difficulty in using the literature recommended by the teacher; - difficulties in generalizing the individual sections of the material studied; - the ability to correct major mistakes made with the help of a teacher; - execution of all types of tasks with elimination of errors. |
| С- | 1,67 | 60-64 |  | The student demonstrates: - mastering of the main material; - Inadequate understanding of formulations when answering all types of assignments; - lack of consistency in the presentation of the material; - significant difficulties in the independent implementation of practical tasks; - Inadequate possession of individual methods in the performance of assignments - significant difficulties in using the literature recommended by the teacher; - significant difficulties in the generalization of individual sections of the material studied; - the ability to correct major mistakes made with the help of a teacher; - execution of all types of tasks with elimination of errors. |
| D+ | 1,33 | 55-59 |  | The student demonstrates: - mastering of separate sections of the main material; - lack of consistency in the presentation of the material; - significant difficulties in the independent implementation of practical tasks; - significant difficulties in the application of individual methods of performing tasks; - significant difficulties in using the literature recommended by the teacher; - significant difficulties in the generalization of individual sections of the material studied; - difficulties in correcting the mistakes made by the teacher; - untimely execution of all types of tasks with elimination of errors. |
| D- | 1,0 | 50-54 |  | The student demonstrates: - difficulties in mastering individual sections of the main material; - misunderstanding of formulations when answering all types of assignments; - lack of consistency in the presentation of the material; - significant difficulties in the independent implementation of practical tasks; - Inability to apply individual methods of performing tasks; - significant difficulties in using the literature recommended by the teacher; - Inability to generalize the individual sections of the material studied; - significant difficulties in correcting the mistakes committed by the teacher; - untimely execution of all types of tasks with elimination of errors. |
| FX | 0,5 | 25-49 | unsatisfactory | The student demonstrates: - lack of understanding of the wording in the answers for all types of tasks; - inability to use individual methods of performing tasks; - late performance of all types of tasks with the elimination of errors. |
|  |  |  |  | The student demonstrates: - ignorance of program material, - at performance of all types of tasks gross errors are allowed; - lack of skills in the use of individual techniques for performing tasks; - Failure to comply with the tasks provided by the forms of current, intermediate and final control. |
| F | 0 | 0-24 |  |  |

The list of recommended literature

Main literature:

1.Эрдман С.В., Фролова И.В., Коробочкин В.В. Химическая технология неорганических веществ: учебное пособие. –Томск: Изд-во Томского политехнического университета, 2011. – 194 с.

2. Широков Ю.Г. Теоретические основы технологии неорганических веществ: учебное пособие/ГОУ ВПО Иван. гос.хим.-технол.ун-т, Иваново, 2009-376 с.

3. Ченская В.В., Черкасова Т.Г., Цалко Е.В. Теоретические основы технологии

неорганических веществ. Учебное пособие. -  Кемерово, 2010. – 203 с.

4. Бестереков У. Теоретические основы технологии неорганических веществ: учебник для студ.спец. 5В072000 – Химическая технология неорганических веществ/У.Бестереков .-Шымкент:ЮКГУ,2014.-163с.

Additional literature:

- Бугенов Е.Б., Джусипбеков У.Ж. Теоретические основы химической технологии. – Алматы, 2003. – 244 с.

- Царева, З. М. Теоретические основы химической технологии / З. М.    Царева, Е. И. Орлова. – Киев :Высш. шк., 1986.–  271 с.

- Москвичев, Ю. А. Теоретические основы химической технологии / Ю. А.

Москвичев, А. К. Григоричев, О. С. Павлов. – М. : Академия, 2005. – 272 с.

- Позин, М. Е., Зинюк Р.Ю. Физико-химические основы неорганической

технологии / М. Е. Позин, Р. Ю. Зинюк. – Л. : Химия, 1993. – 437 с.

- Дмитревский Б.А. Свойства, получение и применение минеральных удобрений. – СПб.: Проспект Науки, 2013. 326 с.

- Ахметов Т.Г., Порфирьев Р.Т., Гайсин Л.Г., Ахметова Л.Т., Каримов Я.М. Химическая технология неорганических веществ: -М.: Высшая школа, 2002. – 688 с.

- Карапетьянц М.Х.Термодинамические   свойства неорганических и органических веществ, 1968 - 472с.

- Абрамов А.А. Переработка, обогащение и комплексное использование твердых полезных ископаемых: учебник Т.1 Обогатительные процессы и аппараты/А.А.Абрамов,-2-е изд. Стереотип, Москва: МГГУ, 2006-470 с

- Абрамов А.А. Технология переработки и обогащения руд цветных металлов: учеб. пособие.  Т.3 Кн.1. Рудоподготовка и Сu, Сu-РyСu-Fе, Мо, Сu-Мо, Сu-Zn руды /А.А. Абрамов, Москва:МГГУ,2005-575 с.

- Мельник Б.Д. Инженерный справочник по технологии неорганических веществ. – М.: Химия, 1975, 544с.

- Киреев Р.А. Методы практических расчетов в термодинамике химических реакций. -М.: Химия, 1977.-288с.

- Краткий справочник физико-химических величин./Под ред. Равделя А.А. – Л.: Химия, 1983. -232с

- Киреев Р.А. Методы практических расчетов в термодинамике химических реакций. -М.: Химия, 1977.-288с.

- Карапетьянц М.Х. Химическая термодинамика. -М.: Химия, 1975.- 584с.

Electronic textbooks, teaching materials, slides, video films, animations, computer programs, presentations (numbers, full names by module)

EMCD on the educational portal on www.asu.ukgu.kz

Таubayeva А.S., Kambarova G.A

Methodical instructions

lecture notes to the discipline

«Theoretical bases of processing of mineral and technogenic raw materials»

for students of a specialty 5В072000 – Chemical technology of inorganic substances (6B071 Engineering and engineering work, EP 6B07160- Chemical Technology of Inorganic Substances)

It has been signed for the publication.

Paper size 60x84  1/16.

Writing paper. Offset publication. The volume of 5 printed sheets.

The circulation of copies.

Order №

Publication of  M. Auezov South Kazakhstan State University

M. Auezov SKSU publishing center, city. Shymkent, Tauke Khan avenue 5.