F. 7.03- 03

Таubayeva А.S

METHODICAL INSTRUCTIONS

on carrying out of laboratory works on discipline

«Technogenic chemical waste»

for students of a specialty 5В072000 – Chemical technology of inorganic substances, (6B071 Engineering, EP 6B07161-Processing of mineral and technogenic raw materials)

Shymkent, 2021

MINISTRY OF EDUCATION AND SCIENCE OF THE REPUBLIC OF KAZAKHSTAN

M.AUEZOV SOUTH KAZAKHSTAN UNIVERSITY

higher school “Chemical Engineering and Biotechnology”

Chair “Chemical technology of inorganic substances”

ТаubayevaА.S

METHODICAL INSTRUCTIONS

on carrying out of laboratory works on discipline

«Technogenic chemical waste»

for students of a specialty 5В072000 – Chemical technology of inorganic substances (6B071 Engineering, EP 6B07161-Processing of mineral and technogenic raw materials)

Shymkent, 2021

UDC536.7:54 (0.75)

Composers: ТаubayevaА.S. Methodical instructions to laboratory works on discipline «Technogenic chemical waste» for students of a specialty 5В072000-«Chemical technology of inorganic substances», (6B071 Engineering EP 6B07161-Processing of mineral and technogenic raw materials) – Shymkent: M. Auezov SKSU, 2021. – 40 p.

The methodical instructions to laboratory works compiled in accordance with the requirements of the curriculum and the discipline program of the discipline "Technogenic chemical waste" and include all necessary data on carrying out of laboratory works of a course.

The reviewers: Anarbaev A.A. - doctor.techn.scie.,Professor., department "Chemical technology of inorganic substances".

The methodical instructions in the "Chemical technology of inorganic substances" of the department meeting (The report №     from «    » «    »   20    ) and “Chemical engineering and biotechnology” higher school education in novative technologies and methodical to ensure the meeting  of the committee (The report №     from «  »  «    »   20    ) were considered and recommended for printing.

It is recommended to the edition by methodical council of M. Auezov SKSU, the report №    from « »   «  »   20

@ М.Auezov South Kazakhstan University 2021

Responsible for release:  Taubayeva A.S

Content

| Introduction | 6 |
| --- | --- |
| Safety measures in the chemical laboratory | 8 |
| Theme of laboratory lesson 1: Determination of solid materials granulometric composition and bulk density | 10 |
| Theme of laboratory lesson 2: Waste analysis in the production of sulfuric acid. Analysis of the insoluble residue in the cinder | 11 |
| Theme of laboratory lesson 3: Analysis of the residual sulfate content in the cinder | 13 |
| Theme of laboratory lesson 4: Determination of iron by the complexometric method | 14 |
| Theme of laboratory lesson 5: The use of phosphorus production wastes in order to obtain sulfuric acid. Obtaining sulfuric acid from gypsum and phosphogypsum. | 16 |
| Theme of laboratory lesson 6: Determination of sulfur content | 19 |
| Theme of laboratory lesson 7: Determination of speed and degree of burning. | 20 |
| Theme of laboratory lesson 8: Analysis of wastewater chemical enterprises. | 21 |
| Theme of laboratory lesson 9: Determination of oxidizability. | 21 |
| Theme of laboratory lesson 10: Analysis of wastewater chemical enterprises. Determination of total hardness. Determination of carbonate hardness. | 23 |
| Theme of laboratory lesson 11: Determination of zinc and lead in zinc concentrate, cinder, dust, copper-cadmium cake. | 25 |
| Theme of laboratory lesson 12: Methods of analysis of products of lead production. Determination of lead in agglomerate, matte, speise and dust (complexometric method). Methods of analysis of products of lead production. | 28 |
| Theme of laboratory lesson 13: An accelerated method for determining mercury. | 30 |
| Theme of laboratory lesson 14: Determination of bismuth in bismuth lead (complexometric method) | 31 |
| Theme of laboratory lesson 15: Determination of calcium oxide in the agglomerate | 33 |
| Criteria for assessing the knowledge | 35 |
| The list of recommended literature | 38 |

Introduction

The discipline "Technogenic chemical waste" refers to the cycle of profile disciplines (PD) and elective component (EC) for students of the specialty 5В072000 - Chemical technology of inorganic substances. Studying the course "Technogenic chemical waste" is: deep study by students of various methods of integrated waste-free processing of technogenic materials and industrial products in the production of mineral fertilizers.

The purpose of study of the discipline "Technogenic chemical waste" is to form an idea of the modern processes of processing and disposal of industrial waste and industrial products of mineral raw materials of the chemical industry, taking into account the increased complexity of the use of mineral and secondary resources and the organization of non-waste technology.

Tasks of studying the discipline:

- to study the composition of technogenic gas-liquid waste production of mineral fertilizers;

- get acquainted with the environmental standards for the production of inorganic substances and materials, develop new technologies for processing industrial waste into multicomponent mineral fertilizers;

- be able to use advanced methods for the disposal of industrial waste in order to ensure the complexity and non-waste processing and disposal of secondary raw materials;

- be able to carry out work on a feasibility study on the introduction of innovative waste management technologies when using them in the production of complex mineral fertilizers.

Pre-requisites: Chemical technology of inorganic substances; Introduction to the specialty; Mineral raw materials of Kazakhstan

Post-requisites: Technology of mineral fertilizers, Complex processing of technogenic waste, Pre-diploma practice

Learning outcomes:

- Knowledge:  large-scale technogenic chemical waste at chemical  enterprises of Kazakhstan, the volumes of their production and disposal;

-Abilities: identify the composition of technogenic chemical wastes by chemical and physicochemical methods of analysis; - assess the quality of technogenic chemical waste containing useful components for the production of mineral fertilizers;

- Skills: to apply acquired knowledge and skills in future production activities; to make conclusions about the possibility of using solid waste in inorganic technology.

After education receiver’s have completed to study this program, they must be able to:

- evaluate the most large-scale types of technogenic chemical wastes at the enterprises of Kazakhstan, their production volumes;

- apply resource and energy-saving technologies for the processing of industrial waste;

- identify the composition of technogenic chemical wastes by chemical and physico-chemical methods of analysis;

- evaluate the quality of industrial chemical wastes containing useful components for the production of mineral fertilizers;

- draw conclusions about the possibility of using solid waste in inorganic technology.

Safety measures in the chemical laboratory

1. Suction of acids, alkalis and other caustic liquids into the pipette by mouth is strictly FORBIDDEN. The selection of acids and alkalis is made only by pears.

2. All dry chemical reagents and especially caustic alkalis should be taken with porcelain spoons or spatulas. It is strictly FORBIDDEN to take caustic alkalis with your hands.

3. Flasks with bromine, hydrogen peroxide, hydrofluoric acid and other caustic liquids must be opened in such a way that the neck of the flask is not directed towards the opening one.

4. Work with acids, alkalis and other poisonous and toxic substances only under the hood with the ventilation on.

5. It is strictly forbidden to throw liquids and solids immiscible with water, as well as strong poisons into the sink.

6. It is strictly prohibited to use reagents without labels or with questionable labels.

7. It is forbidden to work with flammable substances near switched on electrical appliances.

8. Vessels with hot liquids should be carried only with two hands: one hand holds by the throat, the other - supports under the bottom of the vessel.

9. Collect broken dishes with a dustpan and a broom, you can not collect them with your hands

10. For burns caused by acids, alkalis, and other caustic substances, you should:

a) wash the affected area immediately with a large amount of water, then with acid burns -10% soda solution; for burns with alkalis - 3-4% acetic acid solution and 3% boric acid solution;

b) in case of redness, rinse the burned area with a 2% manganese solution;

c) after providing first aid, in serious cases, immediately consult a doctor;

d) when cutting glass with simultaneous exposure to acid or alkali, first of all, wash the wound immediately with a large amount of water and make sure that there are no glass fragments in the wound, then lubricate the edges of the wound with iodine solution and bandage the cut;

e) if sulfuric acid gets on the skin, wash it off with plenty of water, and then neutralize it with a weak solution of soda and apply a bandage soaked in KMnO4, consult a doctor.

11.If acid spills: dilute the acid with water, then neutralize with baking soda and scoop. If sulfuric acid is spilled, then it must be diluted with water, and then covered with sand or washed off with plenty of water, and then neutralized with soda.

12.In case of an alkali spill, wash it off with water and then neutralize it with a weak acid (acetic, boric).

13.When washing dishes with a chromium mixture, it is poured into the same dish where it was. Do not pour chrome mixture into the sink

14.When heating a substance in a chemical container, consider the following:

- for heating to a temperature not exceeding 100°C, use a water bath

- to temperatures above 100°С - oil

- up to temperatures above 200°С - sand

15. It is strictly FORBIDDEN to heat glassware over an open fire.

16.When heating, it is strictly FORBIDDEN to take hot dishes with unprotected hands.

17.After working in the laboratory, you should wash your hands and rinse your mouth with water.

Laboratory work №1

Determination of solid materials granulometric composition and bulk density

The purpose of the work: acquiring skills in determination of granulometric composition and bulk density of solid granular materials.

The brief theoretical information

Solid granular materials are widely applied as initial raw materials in many branches of chemical industry. Granular structure and volumetric density describing porous structure of analyzed substance concerns to basic technical and industrial characteristics of solid materials which determine their properties and indicators of quality.

Determination of materials bulk density

Bulk density is mass of 1 m3 of granular material in natural condition taking into account its transparency. Determination of bulk density is carried out three times and arithmetic mean of three results is taken.

Volumetric density in the condensed condition is determined as follows: the used material fed into a volumetric vessel, is condensed by knocking of the vessel about solid surface up to constant volume. The determination is carried out three times.

The technique of work carrying out

At determination of grinding fineness of fine-disperse materials the sample of previously dried analyzing substance in amount 50-100 g is fed on the appropriate sieve attached in tray. At the experience finishing the control sieving is carried out above paper at the taken off tray. The sieving is considered completed if through a sieve during 1 minute no more than 0.1% of an analyzed material passes. The fineness of grinding is expressed in percentage and it is determined by weighing the rest of an analyzed material on the appropriate sieve.

The grading test of analyzed material is carried out also with set of sieves using depending on necessary amounts of fractions. The set of appropriate sieves is placed between a cover and a tray so that the finest sieve is above the tray, and the largest one is under the cover.

The sample of dry material is weighted (in amount of 1 kg with accuracy 0.1 g) and then it is placed on the top sieve. The cover is closed and the sieving is carried out manually or mechanically.

The bulk density is determined under the formula:

ρH=M1-M2/V

where ρH is bulk density, g/cm3

M1 is mass of the vessel with material, g

M2 is mass of empty vessel, g

V is volume of vessel, cm3

Control questions:

- What do granular composition and density of solid materials characterize?

- How is bulk density calculated?

Laboratory work №2

Waste analysis in the production of sulfuric acid. Analysis of the insoluble residue in the cinder

The purpose and tasks of the work: Mastering analysis methods and acquiring skills for controlling the quality of sulfur-containing products.

Characteristics of the process

The main raw materials for the production of sulfuric acid are sulfur pyrite (sulfur-containing materials), elemental sulfur and exhaust gases, containing SO2 and H2S. Sulfuric acid is obtained in two ways: contact and nitrous. Sulfuric acid production by contact method consists of the following stages:

1. obtaining sulfur anhydride by bake sulfur-containing raw materials,

2. oxidation of SO2 to SO3 oxygen air

3. absorption of sulfuric anhydride with water or sulfuric acid solutions.

The main waste in the production of sulfuric acid is cinder and selenium sludge (when the system is operating on pyrites), exhaust gases containing SO2 and H2SO4 fog, as well as acid effluents.

As a result of pyrite firing, about 18-20 million tons of cinder, which is a valuable raw material, is formed for the metallurgical industry. The composition of the precipitation formed depends on the nature of the raw materials used and the oxidized agent, the burning temperature and the design of the furnaces (fluidized bed, cyclone).

The pyrite combustion process can be represented by the general equation

4FeS2+11O2=2Fe2O3+8SO2

and during the formation of protoxide- oxide iron

3FeS2+8O2=Fe3O4+6SO2

Usually, sulfur does not burn out completely in pyrites, and a small amount of undecomposed pyrites passes into the cinder.

Thus, a cinder, consisting mainly of iron oxide, may contain Fe3O4, FeS, and a number of sulfates of the corresponding metals, the oxides of which are always present in sulfur pyrite. Impurities accompanying pyrites also pass into the cinder: SiO2, CaSO4, etc.

EQUIPMENT, TECHNICAL AND INSTRUMENTAL TOOLS:
Analytical balance
Electric stove
Muffle furnace
Desiccator
Burettes for titration 
Conical flasks
pipet(te)
beaker (Chemical glasses)
Funnel
Filter paper (blue ribbon)
Pear

PERFORMANCE ORDER
1.1. Analysis of the insoluble residue in the cinder

The insoluble phosphate residue contains silicon containing minerals insoluble in mineral acids (mainly silica and sparingly soluble silicates).

Reagents:
Hydrochloric acid, concentrated and diluted (1: 1)
Nitric acid, concentrated and diluted (1: 2)

Analysis progress

0.5-1.0 grams of cinder are weighed with an error of not more than 0.0002 g on an analytical balance, placed in a beaker with a capacity of 200-250 ml, moistened with a small amount of water, mixed until a homogeneous gruel, with a glass stirring. Leave the stirring in a beaker. Add 45 ml of dilute hydrochloric acid (1:1), 10 ml of nitric acid (1:2), cover with a watch glass and dissolve at boiling for 30 minutes, stirring the contents from time to time. Wash the watch glass over the beaker with a small amount of water.

The residue is filtered through an ashless filter (blue ribbon) with a small amount of paper mass into a 500 ml volumetric flask (the main solution is W), the beaker and glass stirring are carefully wiped with ashless filter paper, transferred to the filter, the residue on the funnel is washed 6-7 times with a warm wash solution and 2-3 times with warm distilled water.

The filter with the residue is placed in a pre-calcined and weighed porcelain crucible, carefully incinerated and calcined in a muffle furnace to a constant weight at a temperature of 700-800 ° C (40-50 minutes). Then it is cooled in a desiccator and weighed (insoluble residue).

The volumetric flask with the washing liquid is cooled, diluted with water to the mark, and thoroughly mixed (the main solution is W). Calcium, magnesium, iron, and aluminum are determined from the solution.

Calculation. The content of the insoluble residue (I. o.) as a percentage is calculated using the formula

insoluble residue =a∙100m, %

where а- mass of calcined insoluble residue, g.

m- mass of weight cinder

Control questions: 
1. What raw materials are used to produce sulfuric acid?
2. The essence of the contact method for the production of sulfuric acid.
3. The main stages of the process for producing sulfuric acid from pyrites.
4. The main stages of the process for producing sulfuric acid from sulfur.
5. What waste is generated in the production of sulfuric acid?
6. Methods of disposal of cinder.
TASK: Conduct a chemical analysis of sulfuric acid production wastes and process the results.

Laboratory work №3

Analysis of the residual sulfate content in the cinder

The purpose and tasks of the work: Mastering analysis methods and acquiring skills for controlling the quality of sulfur-containing products.

Characteristics of the process

The sulfate ion is determined by weight method based on its deposition in the form of barium sulfate in a hydrochloric acid medium:

Na2SO4+BaCl2=2NaCl+BaSO4

The barium sulfate residue is filtered, calcined, cooled, and weighed.

Reagents:

Barium chloride, 20% solution

Ashless filter (blue ribbon)

Silver nitric acid 1% solution

Concentrated hydrochloric acid

Analysis progress

For analysis, 50 cm3 of the basic solution is selected, transferred to a glass beaker with a capacity of 300 cm3, diluted with water to 200 cm3, neutralized with hydrochloric acid according to methyl red, 3 ml of hydrochloric acid is added, heated to a boil and with continuous stirring, 10 ml of barium chloride solution heated to a boil is poured in a thin stream. The solution with the BaSO4 precipitate is boiled for 5 minutes with constant stirring, then the beaker is placed on a water bath or tile (88°C) and kept for 2 hours. Or leave the glass beaker with the sediment for 16-18 hours. Filtered through a single filter, the clear liquid over the sediment is filtered through a filter. The BaSO4 residue from the walls is carefully removed with a piece of an ashless filter using a glass stirring and attached to the filter on a funnel. The washing of the residue is repeated until complete removal of chlorine ions in the wash water. The completeness of washing is checked in the following way: 2 ml of the filtrate was acidified with a few drops of a 10% HNO3 solution and two drops of a silver nitrate solution were added. The lack of turbidity indicates the completeness of laundering from chlorine ions. The filter cake is washed with hot water (distilled), the filter cake is transferred to a crucible, dried, ashed and calcined to constant weight at 800°C. The crucible with residue is cooled in a desiccator and weighed. Through the entire course of the analysis, a blank test is carried out. The found correction is taken into account when calculating the results of the analysis.

The residual sulfate content in the cinder is determined by the formula:

where m1- weight crucible with residue BaSО4, g

m- empty crucible mass,g

0,412 – gravimetric coefficient recount with BaSО4 on SО42-

g – cinder weight, g

а – aliquot of the analyzed solution, ml

Control questions: 
1. What raw materials are used to produce sulfuric acid?
2. The essence of the contact method for the production of sulfuric acid.
3. The main stages of the process for producing sulfuric acid from pyrites.
4. The main stages of the process for producing sulfuric acid from sulfur.
5. What waste is generated in the production of sulfuric acid?
6. Methods of disposal of cinder.

TASK: Conduct a chemical analysis of sulfuric acid production wastes and process the results.

Laboratory work №4

Determination of iron by the complexometric method

The purpose and tasks of the work: Mastering analysis methods and acquiring skills for controlling the quality of sulfur-containing products. Determination of iron by the complexometric method

The essence of the method. At pH = 1.5-1.8, Trilon B forms a slightly dissociated stable complex with ferric ions. Trilon titration of iron is carried out in the presence of sulfosalicylic acid as an indicator. To increase the rate of complexation, it is recommended to heat the solution to 40 - 50°C.

Reagents:

Aqueous ammonia (25% solution) diluted 1:1
Rifan paper (indicator) with an interval of pH = 0.3 - 2.2
Iron Electrolytic 
Nitric acid (density 1.36 g/cm3), diluted 1:3
Sulfosalicylic acid, 20% aqueous solution

Standard solution of iron nitrate: 0.3497 g of electrolytic iron or Armco type iron wire is dissolved in 100 ml of nitric acid solution (1:3), boiled to remove nitrogen oxides and diluted to 500 ml with water (1 ml of the resulting solution contains 1 mg of Fe2О3). For colorimetric determination, 25 ml of the stock solution is diluted to 500 ml of 0.2N. nitric acid solution (1 ml of the resulting solution contains 50 mkg Fe2О3).

Trilon B, 0.02 M solution (see definition of calcium). The titer of the solution according to Fe2О3 is set under the conditions described in the analysis.

Analysis progress

In a conical flask with a capacity of 250 ml, 50 ml of the main solution is taken, diluted with water to approximately 100 ml, set with an ammonia solution (1:1) pH = 1.5 - 1.8 according to the Rifan indicator paper. Then the solution is heated to 40-50°C, 0.5 ml of sulfosalicylic acid solution is added and titrated dropwise with Trilon B until the color changes from red-violet to lemon yellow or colorless (with a low iron content).

Calculation. The iron content in terms of iron oxide (III) (in%) is determined by the formula:

where Vтp - the quantity of 0.02 M solution of trilon B, consumed for the titration of the iron, ml;

ТТР/Fe2О3- titer of 0.02 M solution of trilon B for iron oxide, established by a standard solution of iron nitrate, g / ml;

W- quantity main solution, ml;

а - weight of cinder, g;

b - aliquot of the main solution, ml.

When the sample contains 1-5% Fe2O3, the relative determination error is 10-5%.

Control questions: 
1. What raw materials are used to produce sulfuric acid?
2. The essence of the contact method for the production of sulfuric acid.
3. The main stages of the process for producing sulfuric acid from pyrites.
4. The main stages of the process for producing sulfuric acid from sulfur.
5. What waste is generated in the production of sulfuric acid?
6. Methods of disposal of cinder.

TASK: Conduct a chemical analysis of sulfuric acid production wastes and process the results.

Laboratory work №5

The use of phosphorus production wastes in order to obtain sulfuric acid. Obtaining sulfuric acid from gypsum and phosphogypsum

The purpose and tasks of the work: To master the research methods of phosphorus production wastes in order to obtain sulfuric acid and methods of analysis of raw materials and sulphur gas.

Characteristics of the process

Obtaining sulfuric acid from gypsum and phosphogypsum

Any sulfur-containing natural ores or secondary resources can serve as raw materials for the production of sulfuric acid: elemental sulfur, sulfide raw materials (sulfides of zinc, iron, lead, copper, nickel, etc.), among which pyrite sulphide occupies a special place, the main substance of which is pyrite, FeS2, as well as sulfates, hydrogen sulfide, and waste products from the extraction of phosphoric acid.

For the production of sulfuric acid, several varieties of calcium sulfate are used: anhydrite, or anhydrous calcium sulfate CaS04, gypsum or the two-water salt CaS04-2H20 and phosphogypsum, which is a waste of the production of phosphoric fertilizers, i.e. a mixture of gypsum with fluorine compounds, phosphorus oxides, S02 and other impurities remaining in the gypsum after washing it.

In the production of extraction of phosphoric acid per 1 ton of Р2О5 phosphoric acid is formed from 3.6 to 6.2 tons of phosphogypsum in terms of dry matter (or from 7.5 to 8.4 tons of wet phosphogypsum in terms of dihydrate).

Phosphogypsum (in terms of dry matter) contains up to 94% CaSO4, as well as impurities undecomposed phosphate, unwashed phosphoric acid, one-and-a-half oxide, strontium compounds, various trace elements (rare earth elements: molybdenum, cobalt, manganese, copper, zinc), compounds fluorine and others.

During the thermal processing of gypsum, crystallization water is first released:

CaSO4·2H2O= CaSO4+2H2O

Then the anhydrite decomposes according to the reaction:

CaSO4=CaO+SO2+0.5O2-566,2 kilojoule (kj)

The gas formed during the firing of anhydrite is processed into sulfuric acid according to the usual (classical) scheme.  The difference lies in the fact that in the wash compartment is installed only one stage of wet electric filters, and in the contact compartment increases the surface of the heat exchangers.

The exclusion of additional stages of electrofilters is due to the fact that the firing gas does not contain arsenic and contains very little SO3, so a small amount of mist is formed during the cooling and washing of the gas. The increase in the heat exchange surface in the contact compartment is due to a lower concentration of SO2 in the gas produced by firing anhydrite than when combustion pyrite.

The processing of gypsum is less economical than the processing of anhydrite, since in the first case additional heat is expended to remove the water released during decomposition CaSO4·2H2O, and the concentration decreases SO2 in the resulting gas.

Before burning, phosphogypsum is dried in rotary kilns at 600-800°C so that the bulk of the fluorine is transferred to the exhaust gases. These gases are subjected to special purification from fluorine, which is then used.

When CaO is added, fluoride emission decreases both during: drying of phosphogypsum and during its subsequent combustion.

Description of the installation

1 - tubular electric furnace, 2- connection tube, 3- absorption flask, 4- thermoregulator, 5- thermo steam, 6- thermoregulator, 7- millivoltmeter, 8 - amperemeter, 9- porcelain tube.

Figure 1. Installation schemes for burning sulfur-containing raw materials

The phosphogypsum burning unit consists of a tubular electric furnace (1) that allows heating up to 700-800°C. To control the temperature, the furnace is equipped with a chromel-alumel connection tube (2), a millivoltmeter (3), the set temperature is maintained by a temperature regulator - thermal relay MKU-2 (4), in the center of the furnace there is a reaction porcelain tube (5) in which the boat (6) is placed with the sample weight. On one side, the tube is open for air access, and through the second, the generated gas is discharged into the absorption vessels (7) and (8), in the first three-necked flask, the alkali is titrated with a burette (9), and the second sanitary flask is designed for control absorption. The gas is drawn through the system by means of a water-jet pump (10). 100 are poured into the absorption flask (7), and 50 ml of an aqueous solution of hydrogen peroxide with a concentration of 5-10%, which is neutralized with an alkali solution according to the methyl orange indicator, is poured into the flask (8).

EQUIPMENT, TECHNICAL AND TOOLS:

-Installation for the burning of sulfur-containing raw materials

-Chemical vessels

-Analytical balance

Procedure for performance

1) Check the entire system for leaks.

2) Turn on the electric furnace in the network, set the preset temperature on the device.

3) At the same time prepare a sample of sulfur-containing raw materials 0.5-1 g, weighed on an analytical balance. When the set temperature is reached, the water-jet pump is turned on, the boat with phosphogypsum is placed in the electric furnace using forceps and kept for 30-60 minutes.

The formed sulfur dioxide, when passed through a flask with a solution of hydrogen peroxide, forms a solution of H2SO4

SO2+H2O2 ↔ H2SO4

the obtained sulfuric acid is titrated with a solution of NaOH with a concentration of 0.1, 0.5 or 1M, depending on the temperature of the experiment and the weight of pyrite.

Titration is carried out in the presence of the indicator methyl orange, the transition from pink to yellow means the end of the titration.

The amount of evolved SO2 is determined by the formulas:

СSO2 = 0.032 V - during titration with 1M NaOH solution,

СSO2 = V · 0.016 - 0.5M NaOH solution,

СSO2 = V · 0.0032 - 0.1M NaOH solution,

where V is the amount of NaOH solution used for titration, ml.

Control questions:

1. Chemistry of the process of burning sulfur-containing raw materials.

2. Factors affecting the speed and degree of firing.

3. Determination of the speed and degree of firing.

4. Technique of the experiment and analysis.

5. Types of raw materials for the production of sulfuric acid, their characteristics, requirements for the composition.

6. Reactions of obtaining sulfur dioxide from various types of raw materials.

7. Maximum (theoretical) concentration of SO2 in sulfur dioxide.

8. Justification of the upper limit of the process temperature limitation.

9. Features of the oxidation of iron sulfates and non-ferrous metals.

10. The main stages of the production of sulfuric acid.

11. Types of furnaces used for burning sulfur-containing raw materials ..

12. How is the utilization of the heat of sulphurous pyrite firing in an industrial environment?

TASK: Get sulfuric acid from the waste of phosphoric production. Determine the acid concentration and the main indicators of the process.

Laboratory work №6

Determination of sulfur content

The purpose and tasks of the work: To master the research methods of phosphorus production wastes in order to obtain sulfuric acid and methods of analysis of raw materials and sulphur gas.

Analysis progress

A weight of 0.2 g of phosphogypsum is weighed with an error of not more than 0.0002 g and distributed in a thin layer along the length of the boat. They are placed in the center of the furnace and burned in a stream of air at a temperature of 700-800°C for 30-60 minutes. Exhaust gases pass at a speed of 2-3 bubble/sec through a solution of hydrogen peroxide (10%), titrate the resulting H2SO4 with a 0.1 M NaOH solution until the color of the methyl orange indicator changes from pink to yellow. The sulfide sulfur content is calculated by the formula:

where, V - the volume of caustic soda solution used for titration, ml;

Т - titer solution of caustic soda, expressed in grams of sulfur;

g - weight of phosphogypsum, g.

For the reliability of the data it is necessary to conduct parallel experiments.

Control questions:

- Chemistry of the process of burning sulfur-containing raw materials

- The main stages of sulfuric acid production

- Types of furnaces used for burning sulfur-containing raw materials

- How is the heat of burning of sulfur pyrite utilized in an industrial environment?

TASK: Obtain sulfuric acid from phosphorus wastes. Determine the acid concentration and key process indicators.

Laboratory work №7

Determination of speed and degree of burning

The purpose and tasks of the work: To master the research methods of phosphorus production wastes in order to obtain sulfuric acid and methods of analysis of raw materials and sulphur gas.

Analysis progress

The rate of the firing process at a given temperature is determined by the amount of SO2 released per unit time g/min (g-mol/min). For this, the solution in the absorption vessel must be titrated continuously throughout the entire time of the experiment (after 1; 3; 5; 10; 15; 30, etc. minutes) the calculated amount of absorbed SO2 is divided into the corresponding time intervals and the average firing rate in this time lapse. The degree of firing is defined as the ratio of the actually released amount of SO2 over a certain time to the theoretical amount of SO2:

where GSО2 actual – the amount of SO2 obtained in the experiment,

where СSО2 theory - the amount of SO2, which should theoretically be allocated in accordance with the total equation of the firing reaction;

Ст - sulfur content in phosphogypsum;

m- mass of phosphogypsum.

Depending on the task, the degree and speed of firing is determined at different temperatures, for different particle size distribution of the raw material, and then the dependence of these indicators on the process conditions is established.

Control questions:

1. Chemistry of the process of burning sulfur-containing raw materials.

2. Factors affecting the speed and degree of firing.

3. Determination of the speed and degree of firing.

4. Technique of the experiment and analysis.

5. Types of raw materials for the production of sulfuric acid, their characteristics, requirements for the composition.

6. Reactions of obtaining sulfur dioxide from various types of raw materials.

7. Maximum (theoretical) concentration of SO2 in sulfur dioxide.

8. Justification of the upper limit of the process temperature limitation.

9. Features of the oxidation of iron sulfates and non-ferrous metals.

10. The main stages of the production of sulfuric acid.

11. Types of furnaces used for burning sulfur-containing raw materials ..

12. How is the utilization of the heat of sulphurous pyrite firing in an industrial environment?

TASK: Get sulfuric acid from the waste of phosphoric production. Determine the acid concentration and the main indicators of the process.

Laboratory work № 8-9

Analysis of wastewater chemical enterprises. Determination of oxidizability

Purpose and tasks of work: Mastering the analysis of wastewater by various methods.

CHARACTERISTIC OF THE PROCESS

To develop effective measures for wastewater treatment, it is necessary to know exactly what pollution is in wastewater and in what quantities. These tasks are solved by analyzing water.

Industrial water is used in various chemical industries. Water should not cause corrosion of boilers, equipment, pipes, contain an excess of suspended solids clogging the pipes of the cooling system; it regulates the content of salts that form scale.

The waters used in the production may contain mechanical suspensions and dissolved acids, alkalis, salts in various combinations. The waters of organic matter production often contain phenol and other toxic substances that are dangerous to living things. For each enterprise, sanitary norms are established for the maximum content of harmful and poisonous pollution, as well as the size of the reservoir into which the water flows.

Wastewater from non-ferrous metallurgy plants containing ions of copper, lead, nickel, zinc and other metals is purified by precipitation of cations in the form of insoluble compounds, followed by filtration or the use of ion exchangers.

An important national economic task is the development of more advanced wastewater treatment methods and the construction of treatment facilities at chemical plants that provide a high degree of purification.

Wastewater treatment methods are divided into physical-mechanical (sedimentation, filtration, etc.), physical-chemical (adsorption, extraction of harmful impurities, their distillation with water vapor, etc.), thermal (evaporation and burning of the organic part of the dry residue), chemical (neutralization of harmful substances, their translation into an inactive harmless form, etc.) and biochemical.

EQUIPMENT, TECHNICAL AND INSTRUMENTAL TOOlS:

Electric stove

Titration Burettes

Conical flasks

Dropper

Chemical beakers

Pear

PERFORMANCE ORDER

Determination of oxidizability

Oxidation of water shows the presence in the water of organic and easily oxidized inorganic substances capable of reacting with oxidizing agents. Most of the organic substances of wastewater have the ability to decompose and create a nutrient medium for various microorganisms, many of which are harmful to human health.

Reagents:

Sulfuric acid, 25% solution

Potassium permanganate, 0.01 N solution

Oxalic acid, 0.01 N. solution

Determination method

In a conical flask pipette pour 10-100 ml of the test water, depending on the concentration of substances dissolved in it, bring to a total solution of 100 ml of distilled water, add 5 ml of 25% solution of sulfuric acid. The solution on the tile is brought to a boil. Then add to it from the burette 10 ml of 0.01N. solution of potassium permanganate and boil for 10 minutes from the moment of the first bubble of steam. After boiling, the liquid should have a red color, which guarantees the necessary excess of oxidation. If the color disappears, you should repeat the definition, taking a smaller amount of test water for analysis. To the hot liquid is poured from a burette 10 ml of 0.01 n. solution of oxalic acid, while the solution is discolored. Excess oxalic acid is titrated with 0.01n. solution of potassium permanganate until pink color appears.

In parallel, 5 ml of 25% sulfuric acid solution is poured into the flask, 100 ml of distilled water, and then the determination is carried out in the same way as for the test water.

Oxidability X (mg/l) is calculated by the formula:

where V1 and V2 - volume of 0.01 N. solution of potassium permanganate, which went to titrate the excess solution of oxalic acid, respectively, in the main and in the control experiment, ml;

0.08-the amount of oxygen equivalent to 1 ml exactly 0.01 N. solution of potassium permanganate;

V - volume of the test water, ml.

Control questions:

1. Give the concept of temporary, permanent and total water hardness.

3. What is water oxidizability, water reaction?

4. Methods of water softening (lime, soda, phosphate).

5. Methods of wastewater treatment.

TASK: Conduct a chemical analysis of wastewater from chemical enterprises and process the results.

Laboratory work № 10

Analysis of wastewater chemical enterprises. Determination of total hardness. Determination of carbonate hardness

Purpose and tasks of work: Mastering the analysis of wastewater by various methods.

Reagents:

Trilon B, 0.1N

Buffer solution, pH = 9.18

Indicator solution. Eriochromic black T in an amount of 0.5 g is dissolved in 20 ml of ammonia buffer solution and diluted with ethyl alcohol to 100 ml.

Determination method

The titration result is good when no more than 0.5 mEq of calcium and magnesium ions are in the taken volume of water. Therefore, depending on the expected hardness, it is necessary to take the following volumes of water samples:

Water hardness, mEq/L ………..0,5-5,0        5-10        10-50

Sample volume, ml ……………50             25            10

A sample of the test water is poured into a conical flask and diluted with distilled water to 100 ml. Then add 5 ml of ammonia buffer solution and after mixing 5-8 drops of the indicator solution. With vigorous stirring, titrate 0.1 N. Trilon B solution until the appearance of red-violet staining, after which the titration is continued very slowly, pouring 1 drop of Trilon B solution until the blue staining appears. From the addition of excess Trilon B, the color of the solution does not change.

During titration, the color of the analyzed solution can be compared with a “witness”, which is prepared in a conical flask of 100 ml of distilled water, 5 ml of ammonia buffer solution, 5-8 drops of indicator solution. The Witness is blue in color.

The total hardness HTotal (mEq/l) is calculated by the formula:

HTotal =

where V1 is the volume of 0.1N Trilon B solution used for titration of the sample, ml;

V2 - the volume of water samples taken for titration, ml;

C is the normality of Trilon B.

Determination of carbonate hardness.

Reagents:

Hydrochloric acid, 0.1 N. solution

Indicator - methyl orange, 0.1% solution

Determination method

In a conical flask pipette pour 10 ml of test water and dilute with distilled water to 100 ml. Add 2-3 drops of methyl orange, titrate 0.1 n. hydrochloric acid solution until the appearance of a weak pink staining and boil for 3 minutes. If the solution becomes yellow when boiling, add more hydrochloric acid to a weak pink color and boil again for 2 minutes.

Carbonate hardness Hcarb (mEq / l) calculated by the formula:

Hcarb  =

where V- volume of 0.1 n of hydrochloric acid solution used for titration, ml

C- the exact concentration of hydrochloric acid.

Control questions:

1. What is water hardness, hardness units.

2. Give the concept of temporary, permanent and total water hardness.

3. What is water oxidizability, water reaction?

4. Methods of water softening (lime, soda, phosphate).

5. Methods of wastewater treatment.

Task: Conduct a chemical analysis of wastewater from chemical enterprises and process the results.

Laboratory work №11

Definition of zinc and lead in zinc concentrate, in cinder, in dust, copper-cadmium cake

THE PURPOSE AND TASKS OF WORK: Study and development of methods for the analysis of solid metal waste with the determination of the content of metal components.

EQUIPMENT, TECHNICAL AND INSTRUMENTAL TOOLS:

Electric stove

Burettes for titration

Conical flasks

Pipettes

Beaker

Funnel

Filter paper

Pear

PROCEDURE FOR PERFORMING THE WORK

Complexometric method

The method is based on the formation of a strong complex of zinc with Trilon B at pH = 5-6. At an equivalent point, the color of the solution changes from raspberry-violet, due to the complex compound of zinc with the xylenol orange indicator, to yellow-lemon.

Interfering with the determination of zinc, copper, lead and iron are removed from the solution by sequential analysis. The addition of ammonium fluoride to the analyzed solution eliminates the interfering effect of aluminum, calcium, and magnesium present in the solution.

If the sample contains a significant amount of manganese, it is removed by oxidizing with ammonium persulfate to dioxide, which precipitates. To do this, after separation of copper, add 3 g of ammonium persulfate and boil the solution until a precipitate of manganese dioxide:

MnSO4 + (NH4)2S2O8 + 2H2O = MnO2 + (NH4)2SO4 + 2H2SO4

The residue is filtered out and washed 3-4 times with hot water, acidified with sulfuric acid.

Reagents:

1.19 hydrochloric acid

Sulfuric acid with a density of 1.84

1.4 nitric acid

Ammonia, 25% solution

Ammonium Fluoride

Xylenol orange indicator, solution

Trilon B, titrated solution

Buffer solution, pH = 5 (500 g of ammonium acetate, 20 ml of glacial acetic acid and water up to 1 liter).

Analysis progress

A 0.5 g sample of the sample is placed in a 100 ml conical flask, 10-20 ml of aqua regia is added, and after the violent reaction ceases, it is placed on a hot plate and boiled, evaporated to a volume of 5 ml, allowed to cool. 10 ml of hydrochloric acid and hot water are added to a volume of 50-60 ml, the insoluble residue is boiled and filtered through a funnel, into the cone of which a cotton swab is placed, and a filter paper mass is placed on top. The filter residue is washed with hot hydrochloric acid (1: 4) until the reaction to heavy metals is negative (sample with Na2S).

The filtrate was evaporated to a volume of 10 ml, 8-7 ml of sulfuric acid was added and the solution was evaporated until a thick white vapor of sulfuric anhydride was liberated. Cool and add a small amount of water along the walls of the flask. If a brown cloud of nitrogen oxides is formed at the moment of touching it, 10 ml of water are added and the solution is again evaporated to vapor of sulfuric anhydride to completely remove nitric acid, which gives a rather strong compound, nitrosylsulfuric acid, with sulfuric acid. Sometimes even double evaporation of the solution to the vapor of sulfuric anhydride is not enough, and you have to repeat this operation three times.

The solution is cooled and 50-60 ml of water is added, boiled for 2-3 minutes until all soluble sulfates are completely transferred to the solution and cooled for 1 hour.

The precipitate of lead sulfate is filtered through a dense filter with filter paper. The filter cake is washed first twice with cold water, acidified with sulfuric acid, and then with pure water until a negative reaction for SO42- ion (sample with barium chloride) is obtained. The filtrate is stored to determine iron.

The precipitate together with the filtrate is transferred to a conical flask, in which the precipitation was carried out, 10-15 ml of ammonium acetate are added, diluted to 150-180 ml with water and heated, without boiling, for 1 h until complete leaching. The volume of the solution before titration should be at least 100-120 ml.

10 ml of xylenol orange indicator solution is added to the cooled solution and titrated with Trilon B solution until the color changes from violet-raspberry to yellow.

The lead content is calculated by the formula:

where V - volume of the Trilon B solution used for titration

T - titer of the solution of Trilon B for lead, g / ml; (0,01035)

a – sample weight, g.

Filtrate after separation of lead is cooled by adding 0.5 g of ammonium fluoride, add 10 ml of Xylenol orange indicator solution and neutralize excess sulfuric acid with ammonia (1:2) until the color of the solution changes from yellow-lemon to orange. Pour 30 ml of buffer solution (pH=5-6), while the solution is colored in a crimson-purple color, and titrate with intensive mixing with a solution of Trilon B until the color of the solution turns yellow-lemon color. The clarity of the color transition at the equivalent point depends on how correctly and thoroughly the solution was neutralized with ammonia before adding the buffer solution.

The zinc content is calculated using the formula:

,

where     V  - volume of the Trilon B solution used for titration

Т – titer of the solution of Trilon B for zinc, g/ml;

а – sample weight, g.

Control questions:

1. Classification of metal waste.

2. What are cupcakes?

3. what are the complexometric methods of analysis based on?

4. Complexometric method for determining lead.

5. Complexometric method for determining zinc.

TASK: Conduct a chemical analysis of solid metal waste from metallurgical industries and process the results.

Laboratory work №12

Methods of analysis of products of lead production. Determination of lead in agglomerate, matte, speise and dust (complexometric method). Methods of analysis of products of lead production.

Purpose and tasks of the work: Study and development of methods for analysis of products of lead production with determination of the content of metal components.

EQUIPMENT, TECHNICAL AND INSTRUMENTAL TOOLS:

Analytical balance

Electric stove

Titration Burettes

Conical flasks

Dropper

Chemical glasses

Funnel

Filter paper

Pear

PERFORMANCE ORDER

Determination of lead in the agglomerate, the Stein, speise and dust (complexometric method)

According to this method, the sample is sequentially decomposed with acids, lead is separated from other elements by precipitation as sulfate, then it is dissolved in ammonium acetic acid and titrated with Trilon B in an acetate buffer solution at pH=5.5 with an orange Xylenol indicator.

A distinctive feature of these products is the increased content of arsenic and antimony in them, which significantly complicates the determination of the main elements.

Reagents:

Hydrochloric acid with a density of 1.19

Sulfuric acid with a density of 1.84

Nitric acid with a density of 1.4

Ammonium fluoride

Xylenol orange indicator

Trilon B, titrated solution (0.05 n. solution)

Sodium sulphate

Potassium bromide

Ammonium acetic acid, a 30% solution containing 3 ml of hydrochloric acid with a density of 1.19 per 1 liter.

Analysis progress

The 0.5 g suspension material is placed in a conical flask with a capacity of 250 ml, moistened with water, pour 15-20 ml of hydrochloric acid, 1-2 g of sodium sulfite and 1-2 g of ammonium fluoride, boil for 5-10 minutes, add 5 ml of nitric acid and heat until the suspension is completely decomposed by reactions:

PbS + 2HCI = PbCI2 + H2S                                                                         (1)

CuS + 4HNO3 = Cu(NO3)2 + S + 2NO2 + 2H2O                                          (2)

PbSiO3 + 6HCI + 4NH4F = PbCI2 + SiF4 + 4NH4CI + 3H2O                      (3)

Pb3(AsO4)2 + 12HCI + 2Na2SO3 = AsCI3 + 2Na2SO4 + 3PbCI2 + 6H2O          (4)

Pb3(SbO4)2 + 12HCI + 2Na2SO3 = SbCI3 + 2Na2SO4 + 3PbCI2 + 6H2O        (5)

Then add 7-10 ml of sulfuric acid and heat until abundant release of sulfur anhydride vapors. Cool, wash off the edges of the flask with a minimum amount of water (10 ml), and again evaporate to thick white vapors. Add 1-2 g of potassium bromide to completely remove antimony from the sample in the form of a compound with bromine. This operation is repeated 2 times. The reaction proceeds according to the equation:

2HSbO2 + 6KBr + 3HSO4 = 2SbBr3 + 3K2SO4 + 4H2O                   (6)

Pour 50-60 ml of water, boil until the soluble sulphates are completely dissolved. The solution is cooled in running water for 1 hour. The precipitate of lead sulphate is filtered through a filter with a filter paper mass, washed 2-3 times with cold water, acidified with sulfuric acid, then with cold water until a neutral reaction of the wash water (a sample with methylorange). The precipitate with the filter is transferred to the flask in which the precipitation was carried out, add 25-35 ml of ammonium acetic acid, bring water to a volume of 150 ml and leach at a temperature close to the boiling point for 30 minutes. The volume of the solution before titration should not be less than 100-120 ml.

To the cooled solution, add 10 ml of the Xylenol orange indicator solution and titrate with a solution of Trilon B until the color changes from purple-crimson to yellow.

The lead content is calculated using the formula:

where    V – volume of the Trilon B solution used for titration,

Т – titer of the solution of Trilon B for lead, g/ml; (0,01035)

а  - weight, g.

Control questions:

1. What are metal slags, what compounds are included in the composition of slags.

2. What is sludge, methods of their analysis.

3. What are mattes, speises and what compounds are included in the composition.

4. Complexometric method for the determination of lead in agglomerate, matte, speise.

5. Accelerated method for the determination of mercury.

6. Determination of bismuth in bismuth lead.

7. Determination of calcium oxide in the agglomerate.

TASK: Conduct a chemical analysis of lead production waste and process the results.

Laboratory work №13

An accelerated method for determining mercury.

The accelerated method for determining mercury is based on the decomposition of mercury compounds with sulfuric acid containing potassium permanganate:

Bivalent mercury is titrated with potassium thiocyanate.

Reagents:

Sulfuric acid with a density of 1.84

Potassium permanganate

Hydrogen peroxide, 30% solution

Iron-ammonium alum, 10% solution

Rodanium potassium, 0.1 N solution.

Analysis progress

The sample weight of 0.5-5 g is placed in a flask with a capacity of 500 ml, cover the flask with a funnel, pour 25-35 ml of concentrated sulfuric acid and pour 1-2 g of finely grated potassium permanganate. Dissolution is carried out in the cold, from time to time shaking the flask. After complete dissolution of potassium permanganate, the flask is heated, gradually increasing the temperature until the release of sulfuric acid vapors, and at this temperature, it is maintained for 10-15 minutes. After cooling carefully pour 100-200 ml of water and add hydrogen peroxide drop by drop until the reduction of potassium permanganate and the released manganese dioxide by reaction:

2KMnO4 + 5H2O2 + 3H2SO4 = 2MnSO4 + K2SO4 + 8H2O + 5O2                    (1)

MnO2 + H2O2 + H2SO4 = MnSO4 =2H2O + O2                                            (2)

Then the solution is boiled until the main salts are dissolved and the excess hydrogen peroxide is destroyed. To the cooled sulphuric acid solution, add 2-3 ml of 10% solution of iron-ammonium alum and titrate 0.1 n. or 0.01 n. with a solution of potassium rhodanide:

HgSO4 + 2NH4CNS = Hg(CNS)2 + (NH4)2SO4                                         (3)

The mercury content is calculated using the formula:

where   V -  volume of potassium rhodanide solution used for titration,

Т -  titer of potassium rhodanide solution by mercury, g / ml,

а – sample weight, g.

Laboratory work №14

Determination of bismuth in bismuth lead (complexometric method)

Determination of bismuth in bismuth lead (complexometric method)

The method of complexometric determination of bismuth is based on the formation of a strong bismuth complex with Trilon B in an acidic medium pH=0.5-1.5. The end of titration is determined by the Xylenol orange indicator.

Reagents:

Nitric acid (1: 1)

Wine acid

Vitamin C

Xylenol orange

Ammonia diluted 1: 1

Trilon B, titrated solution

Analysis progress

The sample weight of 5 g is placed in a 250 ml flask, 3-4 g of tartaric acid is added and dissolved in 30 ml of nitric acid 1:3. the Solution is transferred to a 500 ml measuring flask, diluted with water to the mark and mixed well. If the sample contains a large amount of bismuth, then when diluting the solution with water, a white precipitate is released, which is dissolved by adding nitric acid, diluted 1:3, drop by drop.

From the resulting solution take aliquot part of 50 ml, placed in a conical flask 500 ml, add 0.1-0.2 g ascorbic acid and diluted with water to a volume of 200 ml, add 0.1 g of the indicator and titrated with a solution of Trilon B before the solution colour from raspberry red to lemon yellow. The bismuth content is calculated from the amount of Trilon B used for titration:

where  V -  Trilon B solution volume used for titration,

Т -  titer of bismuth solution of Trilon B, g / ml,

а – sample weight, g.

Control questions:

1. What are metal slags, what compounds are included in the composition of slags.

2. What is sludge, methods of their analysis.

3. What are mattes, speises and what compounds are included in the composition.

4. Complexometric method for the determination of lead in agglomerate, matte, speise.

5. Accelerated method for the determination of mercury.

6. Determination of bismuth in bismuth lead.

7. Determination of calcium oxide in the agglomerate.

TASK: Conduct a chemical analysis of lead production waste and process the results.

Laboratory work №15

Determination of calcium oxide in the agglomerate

The method is based on the formation of a strong complex with Trilon B by calcium ions at a solution pH of 10-11.

The determination is carried out in the presence of the indicator murexide.

Reagents:

Hydrochloric acid with a density of 1.19 and 1: 1

Hydrofluoric acid

Caustic soda, 4n. Solution

Trilon B, titrated solution 0.05N.

Murexid – indicator

Analysis progress

A weighed sample of 0.1 g is placed in a flask with a capacity of 250 ml, moistened with water and decomposed in a mixture of acids (15 ml of aqua regia and 1-2 ml of hydrofluoric acid), followed by evaporation of the solution to dryness. After evaporation, the walls of the flask are washed with 10 ml of hydrochloric acid and again evaporated to dryness. This operation is repeated one more time with 5 ml of hydrochloric acid to completely remove the nitric acid.

The dry residue is dissolved by heating in 4-5 ml of hydrochloric acid (1:1), diluted with 50 ml of water and boiled for 1-2 minutes to dissolve the chloride salts. After cooling the solution, 100-120 ml of water, 5 ml of a 50% solution of triethanolamine, 30 ml of sodium hydroxide are added and titrated with Trilon B in the presence of 0.2 g of an indicator - murexide on a photoelectric titrimeter of the FET type.

Calcium oxide content is calculated by the formula:

where V is the volume of the titrated solution of Trilon B, which went into

titration,

T - titer of Trilon B solution in terms of CaO, g/ml,

a - sample portion, g.

Control questions:

1. What are metal slags, what compounds are included in the composition of slags.

2. What is sludge, methods of their analysis.

3. What are mattes, speises and what compounds are included in the composition.

4. Complexometric method for the determination of lead in agglomerate, matte, speise.

5. Accelerated method for the determination of mercury.

6. Determination of bismuth in bismuth lead.

7. Determination of calcium oxide in the agglomerate.

TASK: Conduct a chemical analysis of lead production waste and process the results.

Criteria for assessing students' knowledge

| Evaluation by letter system | Numeral equivalent of points | %- content | Evaluation according to the traditional system | Criteria for assessing students' knowledge |
| --- | --- | --- | --- | --- |
| А | 4,0 | 95-100 | Excellent | The student demonstrates: - a deep and lasting assimilation of program material - complete, consistent, competent and logically presented answers for all types of activities; - Ability to freely cope with the tasks; - correct, well-founded decisions, - skills in the use of information from basic and additional specialized literature in the study of discipline, - the ability to self-systematize the program material; - Possession of versatile skills and methods of performing all types of tasks; - Ability to work with foreign literature and information resources of the Internet; - Timely and high-quality execution of all types of tasks. |
| А- | 3,67 | 90-94 |  | The student demonstrates: - Deep assimilation of program material; - complete, consistent and logically presented answers for all activities; - ability to cope with the tasks; - the right decisions, - skills of using special literature in the study of discipline, - the ability to self-systematize the program material; - Possession of skills and techniques for performing all types of tasks; - Timely execution of all types of tasks. |
| В+ | 3,33 | 85-89 | Good | The student demonstrates: - assimilation of program material; - complete, consistent, literate, without significant inaccuracies, an account of the answers for all kinds of tasks; - correct application of theoretical knowledge - Possession of necessary skills in the performance of applied tasks - skills in using recommended literature in the study of discipline, - skills of systematization of program material; - Possession of skills and techniques for performing all types of tasks; - Timely execution of all types of tasks. |
| В | 3,0 | 80-84 |  | The student demonstrates: - assimilation of program material; - a consistent presentation of the answers for all types of tasks with non-essential errors; - skills in applying theoretical knowledge under the guidance of a teacher; - Possession of necessary skills in performing practical tasks - skills in using recommended literature in the study of discipline, - skills of systematization of program material under the guidance of a teacher; - mastering the skills of performing all kinds of tasks; - the ability to independently correct mistakes made; - the timely execution of all types of tasks with the elimination of errors. |
| В- | 2,67 | 75-79 |  | The student demonstrates: - assimilation of program material; - Ability to present answers with non-essential errors; - skills in applying theoretical knowledge under the guidance of a teacher; - Possession of techniques in the performance of practical tasks - skills in using recommended literature under the guidance of a teacher - skills of generalization of program material under the guidance of a teacher; - the ability to correct mistakes made with the help of a teacher; - the timely execution of all types of tasks with the elimination of errors. |
| С+ | 2,33 | 70-74 | Good | The student demonstrates: - mastering of the main material; - Inadequate formulations when responding to all kinds of tasks; - violation of the sequence in the presentation of the program material; - difficulties in self-fulfillment of practical tasks; - Possession of individual techniques in the performance of practical tasks - skills in using the literature recommended by the teacher; - skills of generalization of separate sections of program material under the guidance of a teacher; - the ability to correct major mistakes made with the help of a teacher; - execution of all types of tasks with elimination of errors. |
| С | 2,0 | 65-69 | satisfactorily | The student demonstrates: - mastering of the main material; - Inadequate understanding of formulations when answering all types of assignments; - lack of consistency in the presentation of the material; - difficulties in self-fulfillment of practical tasks; - Possession of separate receptions at performance of tasks - difficulty in using the literature recommended by the teacher; - difficulties in generalizing the individual sections of the material studied; - the ability to correct major mistakes made with the help of a teacher; - execution of all types of tasks with elimination of errors. |
| С- | 1,67 | 60-64 |  | The student demonstrates: - mastering of the main material; - Inadequate understanding of formulations when answering all types of assignments; - lack of consistency in the presentation of the material; - significant difficulties in the independent implementation of practical tasks; - Inadequate possession of individual methods in the performance of assignments - significant difficulties in using the literature recommended by the teacher; - significant difficulties in the generalization of individual sections of the material studied; - the ability to correct major mistakes made with the help of a teacher; - execution of all types of tasks with elimination of errors. |
| D+ | 1,33 | 55-59 |  | The student demonstrates: - mastering of separate sections of the main material; - misunderstanding of formulations when answering all types of assignments; - lack of consistency in the presentation of the material; - significant difficulties in the independent implementation of practical tasks; - significant difficulties in the application of individual methods of performing tasks; - significant difficulties in using the literature recommended by the teacher; - significant difficulties in the generalization of individual sections of the material studied; - difficulties in correcting the mistakes made by the teacher; - untimely execution of all types of tasks with elimination of errors. |
| D- | 1,0 | 50-54 |  | The student demonstrates: - difficulties in mastering individual sections of the main material; - misunderstanding of formulations when answering all types of assignments; - lack of consistency in the presentation of the material; - significant difficulties in the independent implementation of practical tasks; - Inability to apply individual methods of performing tasks; - significant difficulties in using the literature recommended by the teacher; - Inability to generalize the individual sections of the material studied; - significant difficulties in correcting the mistakes committed by the teacher; - untimely execution of all types of tasks with elimination of errors. |
| FX | 0,5 | 25-49 | unsatisfactory | The student demonstrates: - lack of understanding of the wording in the answers for all types of tasks; - inability to use individual methods of performing tasks; - late performance of all types of tasks with the elimination of errors. |
|  |  |  |  | The student demonstrates: - ignorance of program material, - at performance of all types of tasks gross errors are allowed; - lack of skills in the use of individual techniques for performing tasks; - Failure to comply with the tasks provided by the forms of current, intermediate and final control. |
| F | 0 | 0-24 |  |  |

The list of recommended literature

Main literature:

1. Yeskendirova M.M. Methodological guidelines to laboratory works for the discipline "Techology of mining and preparation of mineral and secondary raw material"  for students of the specialty 050720- "Chemical technology of inorganic substances"/ M. M. Yeskendirova, K. T. Zhantasov. – 2012.

2. Алтыбаев Ж.М., Тлеуова С.Т. МУ к лабораторным занятиям по дисциплине «Безотходная технологи».-Шымкент, ЮКГУ им. М. Ауезова, 2015.

Additional literature:

- Химические методы анализа. Уч.пос. для хим.-тех. вузов /В.И.Посыпайко, Н.А.Козырева и др. –М.: Высш.шк., 1989.

- С.А.Крашенинников и др. Технический анализ и контроль в производстве неорганических веществ. –М.: Химия, 1989.

- Наркевич И.П., Печковский В.В. Утилизация и ликвидация отходов в технологии неорганических веществ. – М.: Химия, 1984.

- Равич Б.М. Комплексное использование сырья и отходов. – М.: Химия, 1988.

- Торочешников Н.С., Родионов А.И. и др. Техника защиты окружающей среды. -М.: Химия, 1981.

- Проскуряков В.А., Шмидт Л.И. Очистка сточных вод в химической промышленности. –М.-Л: Химия, 1077.

- Очистка и рекуперация промышленных выбросов. /Под общ. Ред. Максимова В.Ф. и Вольфа Н.В. – М.: Химия, 1981.

- Кузнецов И.Е., Троицкая Т.М. Защита воздушного бассейна от загрязнения вредными веществами химических предприятий. –М.: Химия, 1979.

- Методы анализа продуктов предприятий свинцовоцинковой промышленности. Глотко Е.Д., Гейнрихс К.Я., Баркова А.А. Изд. «Металлургия», 1969.

- Анализ цветных металлов и сплавов. Степин В.В., Силаева Е.В. и др. –М., «Металлургия», 1974.

Electronic textbooks, teaching materials, slides, video films, animations, computer programs, presentations (numbers, full names by module)

EMCD on the educational portal on www.asu.ukgu.kz

Таubayeva А.S

Methodical instructions

on carrying out of laboratory works on discipline

«Technogenic chemical waste»

for students of a specialty 5В072000 – Chemical technology of inorganic substances, (6B071 Engineering EP 6B07161-Processing of mineral and technogenic raw materials)

It has been signed for the publication.

Paper size 60x84  1/16.

Writing paper. Offset publication. The volume of 3 printed sheets.

The circulation of copies.

Order №

Publication of M. Auezov South Kazakhstan University

M. Auezov SKU publishing center, city. Shymkent, Tauke Khan avenue 5.