RYSDAULETOV RAIMBERDI

MOMINOVA SAULE

PHYSICAL CHEMISTRY OF BUILDING MATERIALS

TEXTBOOK

RYSDAULETOV RAIMBERDI

MOMINOVA SAULE

PHYSICAL CHEMISTRY OF BUILDING MATERIALS

TEXTBOOK

Shymkent, 2021

UDC 69(075.8)

ҚБЖ 38я73

Reviewers:                             assistant professor, PhD in Engineering Science

of M.Auezov South Kazakhstan University

Каlshabekova Ye.N.

Professor, PhD in Engineering Science of

Zhangir Khan WKATU

Montayev S.А.

assistant professor, PhD in Engineering Science

of Korkyt ata Kyzylorda State University

Baitasov K.N.

Rysdauletov R.A., Mominova S.M. Physical Chemistry of Building Materials:Textbook/

Rysdauletov R.A., Mominova S.M. – Shymkent, М.Auezov SKU. 2021-112p.

ISBN 978-601-327-314-3

The proposed textbook is written in accordance with the standard curriculum of the discipline «Chemistry of building materials» and includes fundamentals of physical chemistry, thermodynamic conditions of the system and their application in production management of building materials.

The textbook is developed for of the educational programs as 5В073000 «Production of building materials, products and structures» and 5В075300 «Chemical technology of heat resistant nonmetals and silicates».

The textbook has been discussed and proposed for publication at the meetings of the chair of «Construction and construction materials» (minutes No.18 dated from June 02, 2021) andthe Methodical commission of the faculty of «Architecture, Construction and Transport» (minutes No.11 dated from June 17, 2021).

The textbook has been proposed for publication by Educational and Mehodical subdivision on Chemical Engineering specialty of M.Auezov SKU of REMC ofMES RK (minutes No. dated from , 2021) .

ISBN 978-601-327-314-3

М. Auezov South Kazakhstan University, 2021.

Content

Introduction.........................................................................................................7

ICrystal chemistry of solid materials…………………………………............8

  - Physical form of substance  ............................................................................8

1.2 The order of the chemical bond in building materials………………...........10

1.3 Structure of building materials......................................................................14

1.4Crystal structure of building materials..........................................................15

1.4.1Description of building materials by crystalline state................................16

1.4.2 Types of crystal lattices..............................................................................18

1.4.3 Principal law of crystal chemistry…..........................................................19

1.4.4 Formation rules of ionic crystal lattices.....................................................21

1.4.5 The structure of building materials............................................................23

1.4.6 Defects in crystal lattice.............................................................................24

1.4.7 Structure of silicates…………...................................................................27

II Physico-chemical properties of water and aqueous solutions...................33

2.1 Properties and structure of water...................................................................33

2.2 Physico-chemical characteristics of water….................................................33

2.3 Water is universal solvent.............................................................................34

2.4 Solutions and their significance……............................................................35

2.5 Electrolytic dissociation of water…………..................................................37

2.6 Hydrogen ion exponent (рН).........................................................................38

2.7 Salt hydrolysis…...........................................................................................39

2.8 The main components in the composition of natural water..........................40

2.9 Ways of industrial water treatment…………………………………............44

IIIElements of chemical thermodynamics and thermochemistry

ofmaterials.........................................................................................................48

3.1 Basics of thermodynamics.............................................................................48

3.2 Hess's  law............................................ 55

3.3 Dependence of the thermal effect on temperature. Kirchhoff's equation..... 58

3.4 Application of the second law of thermodynamics to physicochemical processes..................................................................................................................... 59

3.5 Application of the third law of thermodynamics to physicochemical processes..................................................................................................................... 61

3.6 Gibbs energy and chemical equilibrium ………...........................................61

3.7 Calculation of equilibrium constants of chemical reactions by thermodynamic functions……………………………................................................65

IV Main rules of chemical kinetics………………………............................ 67

4.1 General law of chemical kinetics……......................................................... 67

4.2 Consecutive and parallel reactions….......................................................... 69

4.3  Catalysts……….......................................................................................... 72

4.4 Chain reactions…….....................................................................................74

V Chemistry of binders………………………................................................ 77

5.1 Classification of binders……………….......................................................77

5.1.1 Gypsum binders…………….....................................................................78

5.1.2 Air-hardening lime.....................................................................................79

5.1.3 Magnesia cement……………………........................................................80

5.1.4 Alkali-silicate binder……………………..................................................80

5.2 The process of hydration hardening of binders……………........................ 81

5.3 Portland cement............................................................................................ 83

5.3.1 Cement production methods.......................................................................84

5.3.2 Composition of Portland cement clinker....................................................86

5.3.3 Specification of clinker minerals………....................................................86

5.3.4 Properties of clinker minerals…………......................................................87

5.3.5 Interaction of clinker minerals with water………......................................89

5.4 The theory of the hardening of binders………............................................ 91

5.5 Impurity Portland cement............................................................................. 95

VI Corrosion of construction materials........................................................ 97

6.1 Corrosion of cement and concrete, and methods of their prevention........ 100

6.1.1 Physical corrosion of concrete……........................................................ 100

6.1.2 Chemical corrosion of concrete................................................................101

6.1.3 Methods of protecting concrete from corrosion.......................................102

6.2 Metal corrosion……................................................................................... 104

References........................................................................................................109

INTRODUCTION

Chemical engineering is based on the fundamental laws of physical chemistry, therefore, a construction technologist must be able to apply the laws of chemical kinetics and thermodynamics to thermal, chemical processes, phase changes occurring in the production of building materials, products and structures. Physical chemistry provides  means for determination of the optimal, energetically sustainable conditions for conducting technological processes, prediction of their results, mastering the theory of processes, management of processes and determination of the prospects for the production of new building materials. Mechanical, hydromechanical, heat and mass transfer, chemical and physicochemical processes, which are determined by the laws of physics, chemistry, mechanics, hydraulics, heat transfer, chemical thermodynamics and kineticsare used in the production of building materials. The main goal of physical chemistry is a comprehensive study of chemical, physicochemical processes and reactions in the production of building materials. Each building material is a system consisting of body or a group of bodies, conceptualy isolated from the external environment. The system has a certain boundary and is characterized by certain parameters (temperature, pressure, volume, concentration, etc.) and properties. It is believed that if one parameter of the system changes, then a thermodynamic process occurs in the system, a change in its chemical composition is the result of a chemical reaction, and a change in a certain physical parameter is the result of a physical process. In most cases, a change in chemical composition in materials is followed by a change in physical properties.The main elements of physico-chemical processes are their stages. Simple processes take place in one stage, complex ones –in several stages. Physico-chemical processes are subdivided into periodic and sequential. The sequence of processes occurring in the production of building materials can be shown by the following scheme: preparation of the initial components of raw materials, grinding and mixing of raw materials, mix preparation, heat treatment, etc.In accordance with the theoretical basics of physical chemistry aconstruction process engineer calculates the composition and physico-chemical composition of materials, material and heat balances of processes, determines the capacity and optimal conditions for heat treatment. Therefore, to know and correctly apply the laws of physical chemistry in the production of building materials gives a process engineer an opportunity to control processes, predict and set the properties of products.

The history of physical chemistry of building materials

The term «physical chemistry» was introduced by M. Lamonosov in 1741, according to his formulation, physical chemistry is «the science that explains the processes occurring in mixed bodies during chemical operations based on experiments and the rules of physics». M. Lamonosov made a great contribution to the technology and theoretical foundations of such a building material as glass. He is the founder of scientific glass production in Russia.Only a hundred years later, N.N. Beketov began teaching physical chemistry at Kharkiv University in 1865. D. Mendeleev made a great contribution to the development of physical chemistry. He made aninvaluable contribution to the hydration theory of solutions, the kinetic theory of gases, and the theory of the glass structure. D. Mendeleev's major work was the discovery of the periodic table of elements in 1869. In the works «Chemical composition and structure of silicon compounds» and «Principles of chemistry» he outlined new conclusions about the structure of silicate compounds and showed that silica in the composition of aluminosilicates can be replaced with alumina, and also made a contribution to the theory of cement hardening.Geochemist and mineralogist V.I. Vernadsky developed the theory of complex aluminosilicate acids and anhydrides and made a contribution to the chemistry of silicates. N.S. Kurnakov introduced DTA method for study of silicates, E.S. Fedorov developed the theory of the crystalline state of substance and identified the possible types of structure.N.V. Belov took a close look at these structures. A great contribution to the study of the physical chemistry of silicates and alloys was made by O. A. Esin, N.A. Toropov and K. S. Evstropiev. The physico-chemical foundations of the theory of the hardening of binding agents were developed by A. Le Chatelier (1887), V. Michaelis (1902), A. A. Baikov (1923-1931). A great contribution to the physical chemistry of silicates among scientists of the Soviet era was made by P.A. Rebinder, V.N. Yung, V.F. Zhuravlev, O.P. V. Timashev, M. M. Sychev, L. G. Shpynova. A. I. Avgustinik (1947), D. S. Belyankin, V. V. Lapin, N. A. Toropov (1954), D. K. Botvinkin (1955) Kukolev (1966), V. Eitel (1962), K.S. Evstropiev and N.A. Toropov (1956), V.I.Babushkin, T.M. Matveev and O.P. Mchedlov-Petrosyan (1962), N. M. Bobkova (1977), V. S. Gorshkov, V. G. Saveliev, N. F. Fedorov (1988), A. A. Pashchenko (1986), O. P. Mchedlov-Petrosyan (1971,1988 ), T. V. Kuznetsova, I. V. Kudryashov, V. V. Timashev (1989), N. M. Bobkova, L. M. Silich and I. M. Tereshchenko (1990). They published  textbooks and tutorials on physical chemistry of silicates.The production of building materials, products and structures provides for the production and processing of small and large fillers for mortars and concretes from non-metallic raw materials, the production of all types of binding agents (lime, gypsum, cement, etc.) and building materials, in particular ceramic materials (building ceramics , porcelain, earthenware, chemically resistant ceramics, refractory and technical ceramics), materials based on molten silicates (glass, glass-crystalline materials, glaze, enamel). The physical chemistry of building materials lays the foundation for studying the technological features of the production of building materials, products and structures.

I CRYSTAL CHEMISTRY OF SOLID MATERIALS

  - Physical form of substance

(O, Si, A1) are the most commonly used on the Earth, they make up 82.58% of the total mass of the Earth, and 12 elements (O, Si, Al, Fe, Ca, Na, Mg, K, H, Cl, C, Ti) – 99.29%, and the percent of other elements is less than 1%.

Тable1.1– Distribution of chemical elements in the earth's crust

| р/с | Element name | Number,% | n/o | Element name | Number,% |
| --- | --- | --- | --- | --- | --- |
| 1 | Oxygen | 47,20 | 7 | Magnium | 2,24 |
| 2 | Silicon | 27,60 | 8 | Potassium | 2,28 |
| 3 | Aluminium | 8,08 | 9 | Tutanium | 0,37 |
| 4 | Ferrum | 5,10 | 10 | Hydrogen | 0,95 |
| 5 | Calcium | 3,60 | 11 | Carbon | 0,19 |
| 6 | Sodium | 2,43 | 12 | Chlorine | 0,21 |

In the earth's crust, elements are occurred mainly in the form of natural compounds such as minerals with a certain composition and properties that form rocks. The following minerals are widespread in the earth's crust, by weight content,%:

Fieldspar – 55;

Silica fume (silica and so on)– 12;

Water – 9;

Alkali iron – 3;

Mica– 3.

A quarter of minerals isclassified as minerals that make up nine-tenths of the earth's crust.

Physical form of substance. There are three physical forms of substances: solid, liquid and gas. A solid substance retains both its shape and volume, a substance in a liquid form can only retain a volume, gassubstances cannot keep either a shape or a volume, and completely acquire a target volume.There are two types of solid forms of substance: crystalline and noncrystolline. Atoms, ions and molecules in crystals are arranged in the form of a crystal lattice. Substances of the crystalline type have a lower surface and internal energy in comparison with noncrystalline substances, therefore they are stable.The properties of crystals vary in different directions depending on their anisotropic structure. The arrangement of particles in substances with a noncrystalline structure is random, therefore their physical properties are the same in all directions (isotropy). The noncrystalline form of substances can transform into a crystalline form under certain conditions. Systems consisting of solid and liquid substances, or consisting of two phases at the same time, are called condensingsystems.

The transition of a liquid melt to a crystalline or noncrystalline glassy form is investigated on the basis of heating and cooling lines (Figure 1.1). When theliquid melt or liquid is cooled in (a) position, a horizontal platform is formed on the line.This delay occurs due to the heat released as a result of structural changes that occur during the transformation of a liquid substance with a low energy into a crystal. If the rate of internal changes is low, then the liquid isgradually cooling, i.e., the liquidis gradually transforming into glass (case b).The glassy form of substance is a thermodynamically unstable state. Glass can spontaneously go into a crystalline form, and at this time an excess amount of energy is released, and the property of the substance changes very rapidly. A crystalline substance can turn into a glassy form only by rapid cooling of the liquid melt.Solids pass into a gas form by thermal dissociation according to the following scheme: solid-liquid (alloy) - gas (evaporation). Solids retain their shape under external deforming forces, being in a stable physical form. The physicochemical, mechanical and thermal properties of solids are determined by the nature of the chemical bond and the energy magnitude of these bonds.

а                                                       б

а –crystalline form;б –noncrystalline or glassy form.

Figure 1.1 - «Temperature-time» curve of liquid melt or liquid under cooling

  - The order of the chemical bond in building materials

There are several types of chemical bonds between particles of a solid: covalent, ionic, metallic and hydrogen. The bond strength is determined by the chemical bond energy, which is equal to the energy expended to separate the substance into its constituent elements. The stronger the bond is, the more stable its connection and the more costs it spends on changing the substance during the technological process, the higher its strength, stiffness and melting point.

The atoms, which are constituent of compounds, are capable of forming a positive ion - a cation, giving up an electron or receiving a negative charge through the formation of an ion - anion. This ability  is called electronegativity, or similarity to an electron. The relative electronegativity of the elements is shown in Table 1.2.

Table 1.2 - The relative electronegativity of the elements

| I | II | III | IV | V | VI | VII |
| --- | --- | --- | --- | --- | --- | --- |
| Н-2,1 | Ве-1,5 | В-2,0 | С-2,5 | N-3,0 | 0-3,5 | F - 4,0 |
| Li-1,0 | Mg-1,0 | А1 -1,5 | Si - 1,8 | Р -2,1 | S - 2,5 | С1 - 3,0 |
| Na-0,9 | Са~1,0 | Fe- 1,25 |  |  |  | Вг - 2,8 |
| К-0,8 |  |  |  |  |  |  |

In the above table, the electronegative value of fluorine is taken equal to four, the electronegative value of lithium is equal to one. Elements of groups I and II give an electron, starting from group III the elements can add an electron. When atoms with different electronegativity begin to combine, for example, in sodium chloride, the sodium atom turns into a cation by giving an electron, and a chlorine atom turns into an anion by linking an electron.The electrostatic force of attraction between different charged ions forms anionic bond. The electrostatic field of an ion has the shape of a ball, so the ionic bond will not be directed. The fields of two different charged ions cannot make equal each other, so they retain the ability to attract other ions, and a deficiency of ionic bond occurs. In specific ionic lattices, the condition for the association of electrons is preserved, i.e., the formation of a fraction of covalent link.

Figure 1.2– Diagram of ionic bond formation

The ionic bond is considered as a saturated polar chemical bond, and the charge of the atoms in it is close to counting numbers (1,2,3,4, etc.). The fraction of the ionic bond or the degree of ionization of the compound is determined by the Pauling's equation:

Р=(1-е (-∆Х^2)/4) ≈ К (Х1-Х2)2 (1.1)

where P is the percent of the ionic bond; ∆X = X1 - X2 is the difference in the values of the electronegativity of the element in the compound; k-constant.

The percent of ionic bonds in the crystal lattices of some oxides is presented in Table 1.3.

The table shows that the percent of ionic bonds in alkali and alkaline earth metals reaches 75-85%, the percent of ionic bonds in elements of III and IV groups reaches 50-65%. It is possible to determine the effective charge of the ion depending on the percent of this ionic bond.

For example: the effective charge of Si4 + in Si02 silicon oxide = +4 • 0.5 = +2; and the effective charge of О2- = -2 • 0.5 = -1

The effective charge of Ca2 + in CaO calcium oxide is = +2 • 0.8 = +1.6; and the effective charge of O2-= -2 • 0.8 = -1.6

Table 1.3 – The percent of ionic bonds in some oxides

| Index | Element |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Na | Ca | Mg | Fe | Mn | Al | Ti | Si | B | P |
| electronegativity Х | 0,9 | 1 | 1,2 | 1,25 | 1,25 | 1,5 | 1,6 | 1,8 | 2 | 2,1 |
| ∆Х=3,5-Х | 2,6 | 2,5 | 2,3 | 2,25 | 2,25 | 2,0 | 1,9 | 1,7 | 1,5 | 1,4 |
| the percent of ionic bonds | 82 | 80 | 73 | 72 | 72 | 63 | 56 | 50 | 44 | 30 |

Ionic bond is standard for most crystals. Under the strong electrostatic interaction between ions, the bond in ionic crystals is characterized by high strength, while crystals are characterized by high strength and melting point. In ionic crystals, the energy of the crystal lattice can be calculated based on the attraction energy of non-homogeneously charged ions and the repulsion energy of same charged ions. It is convenient to calculate the energy of crystallization by A.F. Kapustinskii  equation, the energy of a crystal and its properties are determined by the number of its structural units, sizes, valence and charging properties:

∪=1202,9Za *Zbra-rk (1-0,395ra-rk)                              (1.2)

where U is the energy of the crystal lattice, кJ/mol; Za, Zb - cationic and anionic charges; rk, ra - the radiuses of the cation and anion, A0.

The crystal lattice energies of CaO, SiO2 and A12O3, calculated by A.F. Kapustinskii equation, are equal to 3432, 13247, and 15353 kJ/mol, respectively. The strength improvement of the chemical compounds allows to increase the strength of the mineral on the Mohs scale up to 3 (CAO), 7 (Si02), 9 (A12O3), respectively.

Crystals with an ionic bond consisting of different charged particles f are called heteropolar compounds. However, crystal lattices are also formed from uncharged particles. Such compounds are called homeopolar, and the compounds between particles are called covalent. The formation of a compound between uncharged atoms occurs through the formation of an electron pair common to both atoms.

Figure 1.4– Diagram of covalent compound formation

The atoms in hydrogen molecules - H2, fluorine - Cl2 are linked by such a covalent bond. The theory of the covalent bonding is complex. When forming a covalent chemical bond, the orbital arrangement of electrons is taken into account. Atomic orbits have a definite shape, when two atoms interact, they overlap each other, which leads to the directivity of covalent compounds. According to the direction of overlapping atomic orbital, the compounds are subdivided into π and σ.

σ figure of bounding formation р figure of bounding formation

Figure 1.5- σand р figure of boundings formation

When figuring the structure of an atom, electron atmospheres (S, p, d - atmospheres) and electron numbers in the outer layer and empty  atmospheres which affect the properties of the atom are displayed.

Table 1.4 - Electron configuration of atoms Si, Al, Oand types of hybridity

| Element | Electron configuration | Groups | types of hybridity | Distribution of orbitals in space |
| --- | --- | --- | --- | --- |
| O | 1s2 2s2 2p4 | - | sp | linear |
| Si | 1s2 2s2 2p6 3s2 3p2 | [SіO4] | sp3 | tetrahedra |
| Al | 1s2 2s2 2p6 3s2 3p1 | [AIO4] [А1О6] | sp3 sp3d2 | tetrahedra octahedra |

Table 1.4 shows that  due to the distribution of the sp - hybrid orbitals of the silicon atom in space in the form of a tetrahedron, the stability of the Si-0 bond angle (109°) is observed in the elementary tetrahedral group [SiO4]. In comparison with many metals that make up silicates, silicon has a higher electronegativity; therefore, the degree of ionic bond between the metal and oxygen is higher than the degree of ionic bond between silicon and oxygen.

Aluminum, which has a hybridization of sp3- and sp3d2, is of particular importance in the silicates. In the first case, it corresponds to the tetrahedral bond arrangement, and in the second case, to the octahedral one and forms the groups of  [AlO4] and [A1O6], which are the most common in aluminosilicates. The semipolar mechanism is also involved in the formation of the A1-O bond, which proceeds by transferring the oxygen electron pair to the free P-orbital of the aluminum atom. Since the electronegativity of aluminum is lower than that of silicon, in comparison with the Si-O bond the Al-O bond has a higher degree of ionization (up to 63%, in silicon 50%).

Hydrogen and metallic bondings. A hydrogen bonding is formed between a positively charged hydrogen atom and negatively charged oxygen, fluorine, and nitrogen atoms. A positively polarized hydrogen atom has unique properties: it is very small in size and does not have an inner electron layer. Consequently, it can penetrate into the electron layer of a negatively polarized atom of a neighboring molecule.A bond is formed between two molecules, which, on the one hand, has an electrostatic character (ionic bond), and on the other hand, has a semipolar character (covalent). For example, the electron pair H-F is displaced towards the fluorine atom in the molecule, , and a hydrogen bond is formed between the molecules. The special properties of water are characterized by the presence of a hydrogen bond between molecules that form associations [Н2О]п. The energy of the hydrogen bond is 8-40 kJ/mol and is lower compared to the energies of the ionic and covalent bonds.

Figure 1.6– Figure of hydrogen bond formation

The «free electron model» is used to explain the metallic bond. According to this model, densely spaced positively charged metall ions are located in metal lattice points, which are «immersed» in an electron gas formed from unused valence electrons. In this case, a valence electron with a low ionization energy moves freely along the orbitals of all atoms, providing a bond between neighboring atoms.The stability of the crystal is ensured by the attractive force between the positively charged ions and the electron gas. The motion of an electron gas is subjected to the classical laws of particles motion in an ideal gas. The metal bond can be formed by elements with fewer valence electrons and more orbitals that are empty in the outer layer. 4/5 of the elements of Mendeleev's periodic system are composed of metals. In construction, metals such as Al, Fe and their alloys are widely used.

1.3 Structure of building materials

The structure of building materials is studied at three levels: macrostructure - the visual structure of the material; microstructure - the structure of a material under a microscope; internal structure of the studied material at the molecular-ionic level (physicochemical research methods - electron microscopy, DTA, X-ray structural analysis, and other methods).

The macrostructure of solid building materials (with the exception of rocks that have their own geological classification) is divided into the following groups: conglomerate, porous, finely porous, fibrous, sandwich and granular (powdery). Artificial conglomerates have a large group, they are various concretes, ceramic and other materials.The cellular structure of the material is distinguished by the presence of macropores typical for foam concrete, gas silicate concrete, etc. The fine-porous structure is specific to ceramic materials obtained as a result of combustion of introduced organic substances. The fibrous structure is typical for wood, mineral wool products. The sandwich structure is typical for sheet, plate and roll materials. Granular materials are various concretes with heat and sound insulation, fillers for mortars.

The microstructure of building materials can be crystalline and amorphous. These structures often represent different states of just one substance, such as different changes in the types of quartz and silica. The crystalline form is always constant.Autoclave curing with saturated vapors is used at a temperature of 175°C and a pressure of 0.8 MPa for the formation of  the chemical interraction between silica sand and lime in the production of silicate bricks, and when terra silicea hardens (a noncrystalline change in the type of silica dioxide) with lime and water at normal temperature 15...25°C, calcium hydrosilicate is formed. The noncrystalline structure of a substance can transform into a more stable crystalline structure.

A crystalline structure is a structure caused by the crystallization of a solid phase and the gradual combination of crystals into a mono - or polycrystalline aggregate. During crystallization under normal conditions, structural particles form a crystal lattice from a solution or liquid molt located in a certain order in space. Each type of chemical bond corresponds to a certain type of crystal lattice: atomic, molecular, ionic and metallic.

а                                         b

cd

Figure 1.7 – Types of crystal lattices (а – atomic, b –molecular, c – ionic, d - metallic)

However, the structure of certain crystals constantly deviates  from ideal conditions, and this affects the properties of the material.

Coagulation structure is a structure resulted from Van der Waals forces, weak intermolecular forces acting through a layer of a liquid medium. A liquid medium, in contrast to a solid lattice frame, forms a special fluent space lattice. Under the action of this fluent surface, materials with a coagulation structure take on the thixotropy character. Thixotropy is the property of a material to restore its structure and properties after its liqueation from various external mechanical forces (mixing, shaking up, vibration, etc.) with the subsequent transition to a rest.

A condensation structure is a structure caused by direct interaction of particles or under the action of covalent and ionic bonds.

  - Crystall structure of building materials

Crystal chemistry studies the relationship between the internal structure of solids and their physical and chemical properties. V. Goldschmidt defined the basic law of this science and said: «The crystal structure is determined by the number of its structural parts, the ratio of sizes and their polarization properties». The structural elements of crystalline bodies (ions, atoms, molecules) are located in space correctly and periodically, forming a spatial lattice. The crystal structure theory (the theory of the spatial lattice) was developed by Ye.S.Fedorov in 1875. A diagram of a three-dimensional lattice in space is shown in Figure 1.8.

Figure 1.8– A diagram of a three-dimensional lattice in space

a, b, c parts  between  lattice points close to each other are called lattice constant. Knowing the lattice constant, the atomic or ionic radius of an element can be determined: it is equal to half the minimum distance between particles in the lattice. The second characteristic of the crystal lattice is the presence of three angles between the parts.A primitive unit cell is the minimum amount that can be extracted from a crystal. Since the crystal net is formed by the migrating of primitive  unit cells in space, it can be considered that the cells can completely describe the lattice. The types of primitive unit cells are shown in Figure 1.9. There are seven types of primitive unit cells in total, if you include Bravais cells, there will be fourteen.

Figure 1.9– Types of primitive unit cells

1.4.1 Description of building materials by crystalline state

Many building materials and raw materials being used, such as silicate compounds, vitrifications, are in a crystalline state. The crystalline state of substance is characterized by the arrangement of atoms, ions and molecules in a certain order in space.A crystal lattice is formed in a specific sequence from the arrangement of the particles that make up the substance in space (three-dimensional space) (Figure 1.10). Structural elements (atoms, ions, molecules)  are located in the points of the crystal lattices. Primitive unit cells form the crystal lattices. A primitive unit cell is its smallest part, separated from the crystal lattice and retaining all its properties.

Figure 1.10–Structure of crystal lattice

The primitive unit cell along the segments a, 2a, 3a ... along the OX axis are repeated for obtaining a crystal lattice and thus segments b, 2b, 3b ... and c, 2C, 3c ... along the OY and OZ axes are obtained (Fig. 1.11).

Figure 1.11 - Primitive unit cell

vectors a, b, c are called vectors with the smallest repetition, and their absolute values are called axes. The parallelepiped formed by vectors a, b, c in the figure is called a primitive unit cell.

The primitive unit cells that form the crystal lattice have the one-type shape and size, and the sides and bounds of the cell are equivalent to each other. To describe the primitive unit cells, it is necessary to indicate its three directions (a, b, c) and three angles between them (α, β, γ). These sizes are called crystal lattice parameters.

1.4.2 Types of crystal lattices

Crystalline lattices are classified according to their structure into three types: coordination, complex and sandwich.

- Coordination lattices can be charged (ionic crystal lattice), uncharged (atomic crystal lattice), formed by one or different structural elements (Figure 1.12 a).

Figure 1.12–Crystall lattices а) coordination; b) complex; c) sandwich.

In lattices formed by different elements, each ion (or atom) is surrounded by an oppositely charged ion (or atom). The number of ions (or atoms) surrounding this ion (or atom) is called the coordination number. The ratio of the coordination numbers of various ions in the crystal lattice is equal to the inverse ratio of the number of elements in the formula of the substance. For example: the coordination number of Si+4 in the crystal latticeSiO2 is equal to 4, the coordination number of O2 is 2. Their ratio is 2: 1, the ratio of Si+4 and O2 in the formula SiO2 is equal to 1:2, i.e., they are opposite to the coordination numbers elements in the lattice.

2. Complex crystal lattices. Molecules or complex ions are located at the points of such lattices (Figure 1.12 b).

3.Sandwich crystal lattices. Such lattices are formed as a result of a one-sided ionization process, due to which the distances between ions differ depending on different directions. Three-dimensional «packs» are formedin sandwich silicates, they are generated from polar cations located inside the polarized ions. Packs can be connected endlessly on a floor. Inside flat floors (molecules), valence forces act, and Van der Waals forces arise in the interlayer floors, leading to the unification of crystals with each other (Figure 1.12 c).

A lot of building materials, including the crystal lattices of silicate materials, form a lattice similar to the lattices between ionic, coordination and complex anionic crystal lattices.

There are also characteristic features of 3 different crystal latticesin the structures of silicate crystal lattices with a sandwich structure.

1.4.3 Principallawofcrystal chemistry

In accordance with this law, the structure of crystal lattices depends on the ratio of the numbers and sizes of an atom, ion, or atomic groups in the structure and on the properties of polarization. This law is called Goldschmit's law.

Crystal chemistry introduces the concept of the effective ionic and atomic radius by describing the ions and atoms in crystals in the form of solid globe. The effective ionic radius is the distance between the centers of ions and atoms. Consequently, to determine the effective ionic and atomic radius, the distance between the centers of ions and atoms in the crystal is determined. In this case, if a solid sphere is drawn through the centers of the ions and atoms at a distance equal to the radius of the effective ion, they should be in contact with each other. The position of cations and anions in the crystal becomes more solidat a low potential energy of the crystal lattices, and in this case the sphere of different charged ions only intertlaced with one another.

When a sphere of same charged ions in a structure links together, its strength decreases. If the spheres of the same charged ion in the structures intersect, and the spheres of different charged ions do not touch, then the structure loses its strength and collapses (Figure 1.13).

а                                      bc

Figure 1.13–Stability level. Figure of different structures (а -stable; б -medium; в –unstable)

From the figures in the geometric representation, one can determine the upper and lower bounds of rkravalue for two-component joints. For coordination numbers 3, 4, 6 and 8, the bounds of this interval are as follows: 0,15-0,22; 0,22-0,41; 0,41-0,73 и >0,73. These coordination numbers lead to the formation of structures in the form of a triangle, tetrahedra, octahedra and cube (Figure 1.14).

а bc

def

Figure 1.14–Coordination multi-facet polyhedral (а -dumb-bell; b–triangle;c- tetrahedra; d - octahedra; e - cube; f – cubic octahedra)

Table 1.5 – Coordination number of some cations in bulding materials structures

| Cations | Groups | Coordination numbers | Examples of structures |
| --- | --- | --- | --- |
| B3+ | triangle [BO3] tetrahedra[BO4] | 3 4 | hambergite |
| Be2+ | tetrahedras [BeO4] | 4 | and other compounds |
| Si4+ | tetrahedras[SiO4] | 4 | silicates, SiO2modifiers, silica glass |
| Al3+ | tetrahedras[AlO4] octahedras[AlO6] | 4 5 6 | silimanite groups, aluminosilicate,kaolin |
| Ti4+ | octahedras[TiO6] | 6 | rutile, titanit |
| Fe3+ | tetrahedras[FeO4] | 4 | iron-orthoclase |
| Mg2+ | [MgO4] | 4 | spinelles |
| Fe2+ | [FeO4] |  | cross-stone |
| Zr4+ | [ZrO6] | 6 | lavenite |
| Ca2+ | [CaO6], [CaO8] | 6, 8 | monticellite,amphibole |
| Ba2+ | [BaO6] | 6 | benitoite |

An example is  the structure SiO2. rkra=0,39:1,36=0,29is for Si4+ and O2- and has the shape of a tetrahedra. As the coordination number increases, the oxidation state of the central cation decreases. As a result of polarization, the shape of the ions changes, their radius and distance between the ions decrease, when this distance reaches a certain value, the coordination number decreases, and the structure of the crystal lattice transforms into a different form. The larger the cation, the higher its coordination number is.

Thus, the ratio of the coordination numberrkra, the type of cation (oxidation state), is determined by the composition of the compound, temperature, pressure, and the medium pH during crystallization. As the coordination number of the cation increases, the refractive property and the density of the crystals increase.

    - Formationrulesofioniccrystallattices

The formation rules of crystal lattices are developed in accordance with the Pauling’s theory. His theory is based on the potential energy of ionic lattices. When the potential energy of an ionic crystal lattice decreases, its stability increases. Pauling described 5 rules to explain the structure of ionic crystal lattices.

Rule 1. Each cation is surrounded by anions located at the top of the multi-facet polyhedra. The distance between the centers of cations and anions is equal to the sum of their radius. The coordination number of the cation is equal to the number of polyhedron tops, and therkraratio will be somewhat disrucpted.

Rule 2. Rule of electrostatic valence. In accordance with this rule, in crystals with a constant ionic structure, the valence of each anion is equal to the sum of the electrostatic bond forces of the same anion and simultaneously adjacent cations. The bond strength is based on the ratio of the bond strength of the cation to the coordination number. To check this rule, it is necessary to determine the ratio of the coordination number of the cation to the number of anions and the ratio of anions to the number of cations; from the result obtained later, equality is obtained.

For example: in the spinelle structure MgAl2O4, the oxygen atom is surrounded by cations 3Al3+ и 1Mg2+. The total electrostatic bonding forces corresponds to the oxygen atom and it will be equal to 2/4 = 2for the spinelle structure 3 +3/6 +1, i.e., the rule is met the conditions, and in this case the electrostatic bond is equal to 2. In the structure of the perofskitemineralCaTiO3, the coordination number 2 of valence calcium Ca2+ is equal to 12, the strength of bond with oxygen O2 isequal to 2/12 = 1/6 (Figure 1.15).

The valence of the titanium atom is equal to 4, the coordination number is 6, and the strength of the bond in it is 4/6. Each oxygen atom is surrounded by 4 calcium atoms and 2 titanium atoms, the strength of electrostatic bonding is equal to 4 + 1/6 + 2 4/6 = 2, i.e., it is equal to the valence of oxygen atoms. According to rule 2, in the structures of complex silicate compounds, the difference between the total forces of electrostatic bonding and valence is equal to

1/6.

Figure 1.15 - Crystal lattice of perofskitemineralCaTiO3

Rule 3. The presence of common sides in coordination polyhedra reduces the stability of the structure. In this case, as different charged cations approach each other, the repulsive forces increase, and the potential energy of the crystal decreases, and the structure remains unstable. This rule applies to cations with high valence and low coordination number. For example, Figure 1.16 shows the brining into association of tetrahedra SiO4with each other. When tetrahedrasSiO4join each other through the combination sides, if the distance between the Si+4 ions is taken to be equal to 1, then when the tetrahedra join through the combination sides, the distance is 0,58, and when the tetrahedra join through the combination sides, the distance decreases again and equals 0,33. For a number of octahedra, this distance will be equal to the following criteria: 0,71 and 0,58.

Figure 1.16–Varoius ccombination of tetrahedras SiO4(а- with points (stable system); б –with sides (unstable system); в –with edges)

It can be seen in the structures that on the top of each cation, surrounded by a multi-facet polyhedron, is located an anion. The distance between the cation-anion centers is equal to the sum of their ionic radius. The coordination number of cations is equal to the number of polyhedron tops and is determined by the ratio rkra.

Rule 5. If the crystal contains several types of cations, the cations with a low coordination number and high valence try to be located inside polyhedra with smaller common tops.

Rule 6. Rule of lean. According to the basics of crystal chemistry, an atom in a crystal acts to reduce the number of various atoms and ions.

    - The structure of building materials

The building materials formula can be expressed in three ways. In the first way their formula is written in the form of oxides with increasing cationic charge. For example: K feldspar –K2O · Al2O3 · 6SiO2, monticellite –CaO · MgO · SiO2. In the second way, in ascending order of the cationic charge, followed by silicon and finally oxygen. The formula for potash feldspar is written as follows: K2Al2Si6O16or KАlSi3O8. But the formulas of materials written in the first and second ways cannot fully reflect their structures. According to the third way, the lattices of silicon oxygen or alumino-oxygen groups are enclosed in square brackets, and isomorphic exchange cations are enclosed in roud brackets.For example: potash feldspar- (K, Na) [AlSiO3O8]. Silicates formed by medium or metasilicic acids are called ortho or metasilicates. For example:CaO:SiO2:2SiO2is a monosilicate, where the number of oxygen atoms bonded to silicon is equal to the number of oxygen atoms bonded to calcium and aluminum; 2MgO · SiO2 - magnesium orthosilicate; MgO · SiO2 - magnesium metasilicate; K2O·Al2O3•4SiO2- potassium disilicate (leucite); Na2O·Al2O3·6SiO2is called sodium trisilicate.The structures of silicates began to be clearly defined after the method of X-ray diffraction analysis was applied. For example: the formula of copper orthosilicate H2Cu[SiO4]was determined by N. Belov. He wrote its formula in crystalline form in the form of metasilicate Cu[Si6O18]·6Н2О. Therefore, it does not define silicon oxygen tetrahedra with a silicon to oxygen ratio ¼.

Consequently, the ratio of the coordination numbers of different ions is opposite to the ratio in the substance formula:

rkra=2:1                                           (1.3)

As the ratioof the radiusrkraof the upper and lower cation and anion increases, which can be determined for two-component compounds, the anions can expand and form a new anion around the cation:

For example: Si4+= г(k)=0,39;

O2-= г(а)=1,36 ;

rkra=0,39:1,36=0,29≈0,3tetrahedra

For example: Al2O3→Al3+=r(k)=0,57

    - Defects in crystal lattice

Crystalline lattices can be perfect or real. In perfect crystals, the atoms are arranged correctly. The atoms located at the lattice points of such crystals are stationary, the electrons are at low temperatures. There may be deviations or damages in the perfect crystals. The structures formed such damages are called crystal lattice defects. Many properties of perfect crystals such as mechanical, electrically conductive, magnetic, and others depend on the effect of crystal lattice defects. These properties are called structure-dependent properties.

Crystal lattice defects are classified into point, linear, plane and volumetric, depending on the geometric principle.

1. Point defects. They are also classified into:

а) energy defects;

б) atomic defects;

в) electronic defects.

2. Linear defects:

а) linear defects;

б) dislocations.

3. Plane defects. They are classified into:

а) non-dislocation defects;

б) dislocation defects.

4. Three-dimentional defects. Such defects joined point, linear and plane defects.

Point atomic defects in ionic crystals.Ya. Frenkel and V. Schottky defects. The atoms in Frenkel defect structure are situated in closely located crystal lattices, i.e., in crystals, the distance between the points of which corresponds to the size of the atoms. A defect that is a pair consisting of a vacancy and an interstitial atom (ion) is called a Frenkel defect. The Frenkel defect is formed by cations in many crystals of the ion, because the cations are smaller than the anions and can be freely located in the points. When atoms or ions which form a vacancy leave their place and move to the surface of the structure, forming positive and negative vacancies, a Schottky defect is formed (Fig. 1.17).

а                                              б

Figure 1.17–Crystal lattice defects (а -Frenkel defect; b -Schottky defects)

Atomic defects. Such defects arise as a result of the entrance of an additional number of atoms into the composition structure. The atoms entered into the structure can be of two types:

- an additional atom by its chemical nature does not differ from the main atom in the points of the structure (Fig. 1.18 b);

-an atom enteredinto a structure differs in chemical nature from the main atom (Fig. 1.18 c).

The atom entered into the structure is located between the points of the crystal lattice.

Figure 1.18–Аtomic defects (а – free point (vanacy); b –atom itself between points; c – other atom)

Energy defects. Point defects are troubles in the crystal lattice that have arisen at certain points in the structure. These defects are formed as a result of the vibrational action of the atom, ion and molecules in the lattice.

When a certain force of action is applied on these lattices in perfect crystal lattices, the energy of the vibrational forces can move these atoms from place, each atom from the action of vibrations moves to a certain distance. In this case, an energy defect arises. The vibrations of atoms are called phono. Each phono has its own energy, amplitude and vibration frequency.

Dislocations. Dislocations arise in crystal lattices under the influence of the latticebindings. In this case, one part of the crystal lattice is displaced in comparison with the other. Three floors can be distinguished in the plane of deformation: the first has no displacement, the second has deformation, but the atoms in the lattice are located correctly one after the other and form the boundary between the deformed crystal lattice.This limit is called the line of dislocation. The shift of locations is caused by abnormal growth of the crystal lattice, the formation of cavities at low temperatures, and various thermal and mechanical changes. Linear dislocations are classified into external and screw dislocations.

Such a defect is called an external dislocation, and the formed half-plane is called an extra-plane, if the crystal lattice is interrupted once by parallel planes during the formation of a plane then a half-plane is formed in the crystal lattice (Figure 1.19).

а                                              б

Figure 1.19- a) External (linear) dislocation; b – extra-plane

In this figure, the lower part of the crystal lattice dislocation is screwed, the upper part of the dislocation is streched, so the number of planes in the upper part of the figure is more. The lattice defect decreases with distance from the dislocation point. The spot of plane break is indicated by a perpendicular sign.In the figure, an external (linear) dislocation appears in the area marked by the dotted line. External dislocations are conventionally divided into positive and negative dislocations. The situation that we see relates to positive dislocations. Equally charged dislocations are repelled from each other, differently charged dilocationsare attracted to one another.

A screw dislocation is a topological defect of a crystal lattice. If one moves around the dislocation, the lattice plane shifts by one layer (or more layers), like a spiral staircase(Fig. 1.20).

Figure 1.20–Screw dislocation: а – figure of screw dislocation formation; b –arrangements of atoms in the crystal lattice during screw dislocation;

In a screw dislocation, the crystal lattice is formed not in the form of parallel planes, but in the form of one screwed-in plane. A row of points located horizontally is split and vertically offset by one parameter. If we depict the deformation of the planes along the arrow, then the deformation will be the same as if we were moving along a helical line. Dislocations affect the strength of solids, resulting in reduced strength.

Structureofsilicates

In the illustration of silicates in the crystal lattice, [SiO4]4-- silicon oxygenrefers to the way oxygen tetrahedra are bonded to each other.

Based on this illustration, silicates are divided into the following types (nesosilicate):

- silicates in the form of guano, consisting of separated tetrahedrons;

- chain silicates formed by finite-dimensional radicals;

- ribbon silicates;

- tectosilicate silicates;

- spherical silicates.

Figure 1.21–Structural types of silicates: а – silicates in the form of guano, consisting of separated tetrahedrons; b – silicates in the form of double guanos; c - linear; d– ribbon; e – leaf shaped; f– tectosilicate alumosilicates; g – spherical

Nesosilicates

Structural groups, complexes or radicals in silicate formulas are written in square brackets. For example [Si2O7] 4-∞, [Si4O11]6-∞. The infinity sign ∞ after the brackets indicates that the radical is in infinite dimension. If the structure of silicates is sandwich, that is, it is 2-dimensional, then the numeral 2 is added above the infinity sign (2∞), if the structure of silicate is dense, that is, 3-dimensional, then the numeral 3 is written above the sign ∞. For example: pyroxene dioxide Ca, Mg[SiO6]1∞, enstatype - Mg[SiO6]1∞, augite Ca (Mg, Fe)[SiO6]1∞.  Cations are written in round brackets, they exchange isomorphic with each other.

Nesosilicates include orthosilicates, in which the distances between atoms in structural groups have different meanings. For example: the distance between silicon and oxygen atoms in a quartz crystal is equal to 1,62 Å. 4 oxygen atoms form a -4-guano group around the silicon atom [SiO4]-4. Nesosilicates also include silicates of the forsterite group Mg2SiO4, fayalite Fe2SiO4, olivine (Mg,Fe)2[SiO4]. Orthosilicates also include clinker minerals Ca3SiO5, Ca2SiO4(Figure 1.22).

Figure 1.22–Structure of forsterite. Mg2+on illustration plane; Mg2+on2-1/2а side; Mg2+on3-4 – central position; О2-on 5 - 3/4а side; oxygen on 6- 1/4 а side; lattice values along the а-х axis

Silicates consisting of chain or complex groups are linear silicates.

These silicates are formed from two -, three -, four -, six-layer silicon-oxygen tetrahedral and are characterized by the formulas [Si2O7]6-, [Si3O9]6-, [Si4O12]8-и [Si6O16]12-(Figure 1.22).

In this case, oxygen atoms which are common to 2 silicon-oxygen tetrahedron do not bind with other cations. The remaining oxygen atoms form a crystalline structure, spending one valence on the bond with silicon, and the other valence on the connection of silicon-oxygen radicals with the cation. [Si2O7]6-radical melilite occurs in rankinite silicate groups, such as: Са3[Si2O7] - rankinite, Ca2Al[AlSiO7]- helenite, Ca2Mg[Si2O7] - okermanite.

Figure 1.23–Complex groups formed from tetrahedron guano and[SiO4] tetrahedrons.

These minerals are found in titanium and high-aluminous rocks. Radical silicates [Si2O7]6-are called diorthotopic silicates (Figure 1.24).

Figure 1.24–Types of finite-dimensional tetrahedrons groups

Silicates (ribbon) formed from infinite-dimensional radicals

They are composed of [SiO4]4-tetrahedra and form continuous ribbon silicates through shared oxygen atoms. Ribbon silicates have stable Si-O-Si silaxane bonds. Endless ribbons formed by the radical [SiO3]2-1∞are formed by the formation of pyroxene-type metasilicates.

For example: in an oxygen ribbon, silicon dioxide Ca, Mg[Si2O6]corresponds to two free oxygen valences to each tetrahedron that bind the cations. The most important cations are Mg2+и Ca2+.Since Ca, Mg cations are capable of isomorphic exchange, clinoenstatite is formed, which exchanges Mg2+and Ca2+. If it exchanges with ions Mg2+и Ca2+ , Al3+ и Zn2+, then the mineral spodumene is formed.

If two ribbons are bonded by common oxygen ions, then secondary ribbons are formed and written in the form of the radical [Si4O11]6-1∞ . These radicals are mainly found in the form of the asbestos mineral. Asbestos is obtained by ore cleaning. 1 ton of oregives 3% asbestos. Depending on its acid solubility, asbestos is classified into chrysotile and amphibole.

Amphibole and chrysotile asbestos. The structure of amphiboles [Si4O11]6-is formed from tetrahedra. Here, 2 pyroxene ribbons together form an amphibiol ribbon. 2 xonotlite ribbons [Si6O17]10-1∞are formed from the compound of wollastonite ribbons such as the compound of the oxygen and calcium atoms. Xonotlite ribbons are radicals peculiar to calcium hydrosilicates.Calcium hydrosilicates, formed in the frame structure belonging to the tobermorite group, are the main mineral of Portland cement and other binders. Their structure is based on xonotlite ribbons. Calcium hydrosilicates have strengthened the binders.

а                                                   b

c                              d

Figure 1.25 -  Amphibole (a, b) and chrysotile (c,d) asbestos

Skeletal structure of silicates

The skeletal structure of silicates is typical for minerals such as soil minerals, specular stone, talc, chlorite, and tobermorite. They combine into six, eight, and five-cornered skeletons across three common SiO4points of silicon-oxygen tetrahedra. In this case, [Si4O10]4-1∞ layers are linked by oxygen atoms. Intermediate layers form Al(OH)3; Mg(OH)2orMg2+, Al3+, potassium ions, hydroxyl groups.

Skeleton silicates also include silicates formed from two- or three-layer packets. A two-layer packet consists of one tertahedral and one octahedral layers. The tetrahedral layer is formed by a silicon-oxygen tetrahedron. Polar cations are located in the packeage layers in the middle part of the tetrahedral layer, and polar oxygen anions are located outside the layer. In addition to oxygen atoms, there are hydroxyl ions on the outer side of the octahedral layer,  andAl3+ cations in the middle part. For example: the formula of kaolinite is Al4[Si4O10]2∞(ОН)3. There one layer is bonded with[Si2O5],the other layer with Al2(OH)6. The packet consists of 5 layers: there are О2- ionson the first layer, [SiO4]4-ionson the second, О2 ions alternate with OH ionson the third, Al3+ ionson the fourth, OH- ionson the fifth. There is a hydrogen bond between the hydroxyl ions of one packet and the oxygen ions of the other packet, therefore, kaolins formed from two packets do not have the property of inturgescence (Figure 1.26).

Figure 1.26–Packets formed bytertahedral and one octahedral layers

The layer formed by octahedra in three-layer packets consists of cations Al3+ and anions О2- and ОН-, they are located between the layers Al3+и О2-, ОН-, two Si4+и О2-tetrahedrons. Three packets minerals include montmorillonite, hydromica, talc, pyrophyllite, and mica.

The layer connects two [Si2O5]2-tetrahedral layers in the formula of montmorillonite Al2[Si4O10](ОН)2∞nH2O[Al2(OH)3]. Oxygen ions are located in the outer part of the three-layer packets; therefore, the intermediate bonds between the packets are weaker. There is water between the packets and they are tied by the forces of Vander Waals. In a humid environment, the amount of intermediate water between the packets and the distance between the packets increases and montmorillonite turgesces.

Solid silicates

Ifoxygen ions, located at all four points, are located between two adjacent silicon atoms as a result of linking together silicon-oxygen tetrahedra, three-dimensional infinite solid silicates are formed. The ratio between silicon and oxygen is 1: 2. Such a solid  structure is considered electrically neutral and is characteristic of the structural modification of silica. If as a result of the structure of the layers, common oxygen atoms in a solid structure are the center of symmetry for a couple of tetrahedra, then a high-temperature α-cristobalite modification of quartz is formed (Figure 1.27, b).

If a plane of symmetry passes through the common oxygen atom, then a high-temperature hexagonal α-tridymite is formed. The Si2O5partitions form a free space passing through the crystal (Figure 1.27, c).

а

б                                                             в

Figure 1.27–Methods of linking together [SiO4]4- tetrahedras from modifications SiO2 а) α-silica; b) α-cristobalite; c) α-tridymite.

In cristobalt, these spaces will be equal to the height of three stories. These structures do not follow the law of close spacing, and the structure remains free. In these empty spaces, there are K+ ,Na+ , Ca2+cations with a low charge, which fill the volume of free space and scatter the charge of the solid structure. Solid silicates include the following aluminosilicates:

- feldspar–albite Na[AlSi3O8]- Na2O·Al2O3·2SiO2

- anorthite – Ca[Al2Si2O8] - CaO·Al2O3·2SiO2

- orthoclase – K[AlSi3O8] - K2O·Al2O3·6SiO2.

ІІPHYSICO-CHEMICAL PROPERTIES OF WATER AND AQUEOUS SOLUTIONS

2.1Properties and structure of water

It is known that a pure water molecule consists of 88.8% oxygen and 11.,2% hydrogen, i.e. 2 hydrogen atoms and 1 oxygen atom (Fig. 2.1, and hydrogen atoms are bonded to an oxygen atom at an angle of 1050). Positive and negative charges in it are located at 2 poles. Dipole moment µ = 1.85 Debye.

а                         б

Figure 2.1 – Water molecule

The arrangement of electrons in the oxygen atom is as follows: 1s22s22p4. Six electrons at the energy level participate in the formation of 2 water molecules, that is, they can be represented in the form of H: O: H. The other two electron pairs, adjacent to 2, will be directed towards  H atoms that form the water molecule. They participate in the formation of hydrogen bonds between associated molecules, forming a negatively charged electron cloud (- O .... H -) (Fig. 2.1, b). The hydrogen bond is 4.5 kcal per 1 kg of atoms.

Due to the fact that the pole water molecules are in an associated state, the hydrogen bond occupies a special place.

Thus, a long-chain molecule is formed on the basis of a hydrogen bond. In addition, there is a scientific understanding that two water molecules combine with each other to form a dimer and pass into a more stable state. Water molecules in this particular state are located relatively densely. A different arrangement of molecules, somehow, leads to the presence of defects. For example, the mutual arrangement of molecules in the state of icecan be identified: in this case, the oxygen atom connects two «corresponding» (located in the direction of 0.99 A0) and two other – «another’s» (located at a distance of 1.78 A0) hydrogen atoms. Thus the formed «water» structureacquires a crystalline state (ice) with defects (Fig.2.2).

As the temperature rises, the degree of water association continues to decrease. It was found that at a water evaporation temperature of 1000C, the association becomes very low, and the molecular weight is 18, which means that there is no association at all in water vapor. The most interesting thing is that the density of ice (00C) is 0.92 g/cm3, the density of water at 40C is equal to the maximum value of 1.0 g/cm3. That is, the process of dimerization in water in this state will be high. In science, it is called an ab-normal  phenomena due to the density of the water.

Figure 2.2– Arrangement of water molecules in various physical conditions (а – vapor condition, b– liquid condition, c – solid condition)

2.2 Physico-chemical characteristics of water

In comparison with a number of other substances, the heat capacity of water is higher. For example, the heat capacity of water is 3100 times higher than that of air (there are even more different salts in melt water). This property directly depends on the associative properties of water molecules. Because the heat supplied from the outside is spent not only on increasing its temperature, but also on separating water molecules from each other.

Water compounds in the state of water vapor, contained in the atmosphere, are actively involved in the formation of the thermal balance of our plante surface. Water moleculeslike CO2 transmit a large amount of energy from sunlight to the earth and, conversely, hold in themselves the thermal energy that rises from the earth.

Not only liquid water evaporates, but also ice. But at lower temperatures, the vapor pressure on ice is very low:

Table 2.1–Vapor pressure on ice in various temperature

| Т0С | -20 | -10 | 0 | 10 | 20 | 30 | 50 | 75 | 100 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| mm. Hg | 0,8 | 1,9 | 4,0 | 9,2 | 17,5 | 31,8 | 92,5 | 289,1 | 760 |

When the water pressure is equal to the pressure of the external atmosphere, the water boils. Therefore, the boiling point of water depends on pressure:

Table 2.2–Dependence of boiling point of water to the its pressure

| Р atm. | 1 | 2 | 5 | 10 | 20 | 50 | 100 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Тof boiling at 0С | 100 | 150 | 151 | 179 | 211 | 263 | 310 |

Compared to the same volume of water in the water + ice system in equilibrium, the volume of ice + ice will be larger.

According to Le Chatelier's principle, in case of excess above the equilibrium pressure, the left side shifts in the direction of liquid water, and vice versa, in the direction of ice, if the pressure drops. Indeed, each atmospheric pressure (based on practical results) reduces the ice melting temperature by 0.0080C.

The electrical conductivity of pure water is very low. For example, 180C (at room temperature) is equal to 0,04·10-6ОМ-1см-1. Among the methods used to determine the physico-chemical properties of water, the most sensitive and clear methods are those based on electrical conductivity.

Water has some surface traction depending on other liquid substances (72.7 ergscm2at 200С). If water contains surface-active material, its surface traction decreases. It is possible to determine the surface tractionof water in practice, to draw a conclusion about purity or impurity based on the energy consumption for water supply, the degree of water moistening of solids during flotation, as well as the rise of water in capillaries.

Also of great importance is the determination of the viscosity of water. As the temperature rises, force of gravity and viscosity rapidly decrease. For example, at 00C it is equal to 1.789 fgv; at 200Сis equal to 1.002 fgv.

2.3Water is universal solvent

This property is widely used in the preparation of various solutions. Therefore, its composition in different parts of the Earth and in each place of water bodies differs from each other. In addition, water reacts with various chemical compounds and, due to the reactivity, we can talk about the purity or impurity  of the water.

Water is one of the most widely used compounds in the production of building materials and products. For example, hardening and setting of inorganic binders occurs as a result of their hydration process, that is, water is one of the main components of building materials and products made on the basis of inorganic binders. In this case, water and a humid environment are one of the factors of the reverse (aggressive) impact on the service life of building materials. Therefore, the relation of building materials to water and the protection of materials from the aggressive effects of water is one of the main issues when extending the service life of building materials and products.

2.4 Solutions and their significance

A liquid or homogeneous system consisting of two or more components is called a solution. It is usually used for widespread liquid solutions.

Solutions are of great importance in nature and construction practice. Chemical additives used in the production of building materials and products are used in the form of working concentration solutions.

Solubility of the substancein water

The dissolubility property of substances in 100 grams of a certain solvent is called solubility. The solubility of substances (i.e., the concentration of a saturated solution) depends on the nature of the solute and solvent, as well as on temperature and pressure.

The mass of a particular substance dissolved in 100 g of solvent at a given temperature and forming a saturated solution is called its solubility coefficient.

The solubility of some substances in water is shown below.

Table 2.3– Water solubility of some mineral binders and their hydration products

| Substance | Temperature, 0С | Solubility, mol/l |
| --- | --- | --- |
| Domestic salt NaCl | 20 | 8,641 |
| Hemihydrate of calcium sulfate СаSO4·0.5Н2О | 20 40 60 | 0,06 0,05 0,04 |
| Tricalcium aluminate 3СаО·Аl2O3 | 20 40 60 | 0.0071 0.0076 0.0078 |
| Tricalcium silicate 3CaO·SiO2 | 10 20 | 0.0015 0.0015 |
| Belit β 2CaO·SiO2 | 20 40 | 0,0011 0,0012 |
| Gypsum СаSO4·2Н2О | 20 40 | 0,0153 0,0154 |
| Hillebrandite2CaO·SiO2·nН2О | 20 | 0.0011 |
| XonotliteCaO·SiO2· nН2О | 25 | 0.0002 |
| Tobermorite5CaO·6SiO2· nН2О | 25 | 0.0002 |

Theoretically, there are no absolutely insoluble substances. However, as can be seen from the table, the water solubility of mineral binders and their hydration products is significantly lower than the solubility of sodium salt.

The water solubility of solids increases with increasing temperature. In gases, on the contrary, the solubility decreases with increasing temperature.

Heat effect of solution

When substances dissolve, heat is absorbed or released. The amount of heat released or absorbed during the dissolution of one mole of a substance is called the heat of dissolution of this substance and is denoted by the symbol K. If heat is absorbed during dissolution of a substance, then K is indicated by a negative sign, and when heat is released, it is indicated by positive one.

For example, the dissolution temperature of  is equal to -6.32 kcal (-26.5 kJ), and the dissolution temperature of KOH- is +13.3 kcal (K 55.7 kJ).

There are various ways to express the composition of a solution by a numerical value: mass fraction of a solute, molar concentration, percentage, etc.

The mass fraction of a solute is a dimensionless physical quantity equal to the ratio of the mass of the solute to the total mass of the solution:

ω = mе.s. / ms(2.1)

whereω – massfractionofasolute, mmm.s. – mass of a solute, ms. –mass of the solution.

Percentage is a value equal to multiplying the mass of the solute by 100% and divided by the mass of the solution:

С% = mе.s.* 100%/ ms(2.2)

For example: calculate the mass of calcium chloride required to prepare 200 g of a calcium chloride solution with a mass fraction of 0.05 or 5%.

Solution: according to the given task ω = 0.05 or 5%, and ms = 200g. According to the formula:

mе.s. = ω * mm.s.or  С% = ms.* 100% / ms.

Ms. = 0,05 * 200g= 10g or ms. = 5% * 200g / 100% = 10g

Molar concentration or molarity is a value equal to the amount of solute per volume of solution:

С(з) = n (з) / V(2.3)

whereС(з) – molarconcentration, n(з) – amountofsolute(mole), V – volume of solute (m3).

For example: How many grams of sodium nitrate is needed to prepare 200ml 0.3 mole solution?

Solution: according tothe problem situation, C (NaNO3) = 0.3 mol/l, V = 0.2 l. These values are found by the formula:

n (з) = С(з)*V= 0,3mol/l * 0,2l = 0,06mol

m = n * М

М(NаNО3) = 23+14+16*3=85g/mol

m = 0,06 mol * 85g/mol= 5,1g

2.5 Electrolytic dissociation of water

Pure water as weak electrolyte is dissociated into ions:

During the dissociation of one water molecule, one and one are formed, when mole of  dissociates in 1 liter of water, hydrate ion and hydrate ion are formed.

Equilibrium constant for water dissociation under the law of interacting mass:

If the amount of dissociated molecules in water is greater than [Н+] and  [ОН-], the amount of [H2O] can be considered unchanged, 1 liter of water contains 1000/18 = 55.56 mol of water.

Therefore, this constant is called the ionic product of water and is written as .

Thus, the concentration of [Н+] and  [ОН-] in 1 liter of water is also equal to . Consequently, the ionic product of water at 220C is equal to and does not change at this temperature.

In pure water [Н+]·[ОН-]is equal to 10-14, i.e., the concentration of ions [H+] and [OH-], therefore water is a neutral substance. [H+] and [OH-] can vary in different water solutions, but their product remains unchanged.

Ifthe concentrations of [H+] and [OH-] ions are equal when a certain substance is dissolved in water,a solution is neutral. If acid is added to the water, the concentration of [H+] will increase. But since the product of the [H+] and [OH-] concentrations does not change, with an increase in the [H+] concentration, the [OH-] concentration decreases. In this case, the concentration of [H+] will be greater. The environment of such a solution will be acidic.

[Н+] = [ОН-] – neutral environment

[Н+] >[ОН-] – acid environment

[Н+] < [ОН-] – alkaline environment

To determine solution environment which contains [Н+]·[ОН-]=10-14, it is enough to know the concentration of [H+] or [OH-]. It is customary to depict a solution environment mainly with a concentration of [H+].

[Н+] = 10-7– neutralenvironment

[Н+] > 10-7– acidenvironment

[Н+] < 10-7– alkalineenvironment

If in solution [H+] = 10-5, then the value of [OH-] can be determined: [OH-] = 10-9, then the solution environment is acidic.

If in solution [H+] = 10-9, then [OH-] = 10-5, the solution environment is an alkaline.

2.6 Hydrogen ion exponent (рН)

Since the above numbers are difficult to use in calculations, a negative decimal algorithm of [Н+] ion concentration is used, and it is called the pH and is denoted by the pH symbol.

рН=-lg[Н+]                                   (2.4)

For example: if [H+] = 10-7, then the pH is equal to -lg [10-7] =-(-7) = 7, which indicates a neutral environment. If [H+] = 10-3, then the  pH =-lg[10-3]=-(-3)=3, it means the environment is acidic. If [Н+] = 10-9, then the рН=-lg[1093]=-(-9)=9, the environment will be alkaline.

If in some solutions рН=5, then рОН=9.

In the study of solutions, general chemical reactions, the reaction environment (pH) has particular importance. For example, the reaction of hydration of mineral binders proceeds well in weakly basic media. Corrosion of concrete and reinforced concrete products occurs intensively in an acidic environment. Thus, it is possible to control the processes, knowing the environment of its behavior.

The pH of solutions is determined using a special pH meter or ionomers.

Figure 2.3–Ionomer (рН meter)

2.7 Salt hydrolysis

When water is used as a solvent, an exchange reaction occurs between the solute and water and the substances decompose.

This process is called the hydrolysis process. In this case, the molecule of the solute disintegrates and reacts with water ions[Н+] или [ОН-], as a result of which the equilibrium between the molecules and water ions is disturbed, and the dissociation of water continues.

When salt ions combine with water ions [H+], the concentration of water ions [OH-] in the solution increases, as a result of which the environment becomes alkaline.

If, on the contrary, the solution environment will be acidic. Some salts do not hydrolyze, that is, do not interact with water.

The reactions that take place between salt and water and lead to the formation of a weak electrolyte (weak acid, weak base, and acidic or alkaline salt) are called salt hydrolysis. As a result of hydrolysis, the dissonant equilibrium of water shifts to the positive side:

The hydrolysis of salts depends on the strength of the acid and base that form them.

- The salt formed by a strong base and a weak acid hydrolyzes in water and forms an alkaline environment:

In this case,interacts with [OH-] water ions. The formation of a strong electrolyte NaOH is necessary, but only in the state of ions in solution. However, the acetate ion of the salt interacts with the water ions [H+].

It is a weak electrolyte with less dissociation. As a result, an alkaline environment is formed, in which the [OH-] ions in the solution exceed the [H+] ions:

- The salt formed by a weak base and a strong acid hydrolyzes in water to form an acidic environment.

Ionic equation

3. Salts formed by a weak acid and a weak base are hydrolyzed. In this case, the solution environment has a weak acidity or a weak base depending on how strong the acid or base is. The solution environment is neutral if the degree of dissociation of acid and base is equal.

Ionic equation

4. Salts formed by a strong base and a strong acid do not hydrolyze.

2.8The main components in the composition of natural water

No natural water H2Oisfound in its pure form. Speaking about natural water, it must be borne in mind that it contains dissolved solids, liquid and gaseous substances. It has been established that there are compounds of more than half of the elements of the periodic system of D.I.Mendeleevin the composition of natural waters.

All components in water are present in two forms: dissolved and undissolved. According to scientific data, natural water contains mainly various ions, mineral salts, organic and biogenicdebrises and dissolved gases. At the same time, there are many undissolved solutes. Concentrations of dissolved substances in natural waters are designated Cs (g/m3 or mg/l) and indicate the mixing rate of water. If the total volume of water consumption is denoted by Q, then it can be shown by the following equation

(2.5)

At the same time, the dependence of the mass of material particlesflowing through running water on the flow rate (U) is determined by the Erie law and can be described by the following equation

(2.6)

where A is the constant of proportionality. As can be seen from the equation, the water flow rate of the total dissolved substance in the river directly depends on the amount of water flow. The presence of dissolved substances in natural waters is the result of water erosion by various layers of the earth's crust. It was found that the more layers of the earth's crust were eroded, the more dissolved components.

Conversely, the Earth erosionis associated with the resistance of the earth layers to washout and the energy of the water flow E, which flows at a right angle.

(2.7)

This equation calculates the value of E. Where Q is the amount of water (m3/s or t/s); Н - height or low level of the channel of the flowing water source. Thus, the erosion of the earth's crust in the mountains or on the hills proceeds quickly, on flat areas - slowly. In mountainous areas, the flow of water is composite type, and also erodes and runs off the layers of the earth. The content of dissolved substances in water depends on the seasons, climate, conditions and other factors.

Various microorganisms and water plants in some natural waters, as well as insoluble plankton, are the main sources of organic material. Since there are favorable conditions for the growth of plankton in the summer, it has been established that the content of organic material increasesin the water.

As a result of the breakdown of organic compounds contained in water, some stable substances are formed, such as humus, which multiplies in local soil layers. According to the quality indicators of the content of various substances in the water, the color of natural waters will also differ.

Natural waters depend on the salts dissolved in them. Depending on the content of dissolved salts (mineralization), waters can be classified as follows:

- freshwater, percentage of salt in it is 1 g/l;

- соленая вода, percentage of salt in it is 1-25 г/л;

- горькой воды, содержание солей в них будет более 25 г/л.

- fresh water, salt content in it up to 1 g / l;

- salt water, the salt content in it is up to 1-25 g / l;

- bitter water, the salt content in them will be more than 25 g / l.

It is known that the content of dissolved salts in fresh water of the earth's crust is 200 mg/g, in «medium waters» 200-500 mg/l and in highly mineralized waters (but considered drinking) 500-1000 mg/l, i.e. 1 kg/l.

The most common cations in water are given below:

H, Nа, К, NH4, Cа2, Мg2, Fе2, Мn2, Аl3

as well as anions:

ОH-, HCО3-, CО3-2, Cl-, SО42-, HS-, NО3-, NО2-, F-, PО3-4, Br- J-, HSiО3-

Themostcommon7 ionsare: Nа, К, Cа2, Мg2, HCО3-, SО42-, Cl-.

According to the amount of the above ions, natural waters are classified into 3 groups: hydrocarbonate (carbonate), sulfate and chloride (hazardous for reinforced concrete products). Each of them, in turn, is classified into 3 more types, for example, bicarbonate (carbonate) water, itcontains calcium, magnesium and sodium salts.

The above types of water, depending on the relative low content of ions in the composition (mg-equ/L), are classified into 3 more groups:

1. HCО3-> Cа2 Мg2

2. HCО3-< Cа2 Мg2< HCО3- SО42-

3. HCО3- SО42-< Cа2 Мg2

As shown above, groundwater is generally more mineralized and contains a higher content of sodium, sulfate and chloride ions. They are formed mainly from the dissolution of the corresponding water-soluble salts. In the territory of Central Asia and Kazakhstan, waters of this composition are most widespread.

In addition to the above, natural waters contain biogenic substances and various microelements. These include such elements  as Cu, Zn, Mn, B.

The solubility of gases in water depends on many physicochemical conditions, in particular on the nature of the gaseous substance, the partial pressure of vapor, temperature and other conditions. The solubility of a gas in water under certain conditions is expressed by the following equation, characterized by the familiar Henry's law in science.

С  К·Р                            (2.8)

where C is the gas solubility in water (ml/l); P is the partial pressure of the gas (atm); K is a proportional constant (it has a certain value for each gas). This equation can be used to determine the solubility of any gas at a pressure of 1 atm at a given temperature. Table 2.4 shows the data characterizing the dependence of the solubility of gases on temperature (determined experimentally).

Table 2.4–Solubility of gases in water at different temperatures

| Temperature of water, 0С | Solubility, mgl |  |  |
| --- | --- | --- | --- |
|  | СО2 | О2 | Н2 |
| 0 10 25 50 100 | 3350 2310 1450 700 0 | 69.5 53.7 39.3 26.6 0 | 7070 5110 3380 1680 0 |

The concentration of dissolved gas in water, i.e., the amount of dissolved gas, depends on the interdependence of this gas with the potential gas pressure on the water surface (due to the tendency towards equilibrium), continuous sorption-desorption processes take place in the gas-water system. They are found mainly in the surface water sheets, and as a result of a gradual diffusion process, dissolved gas molecules can also be found in the lower layers. It is obvious that the content of free gas is low in deep water sheets(depending on the factors p, T).

The content of gases in water is different depending on temperature, pressure and other physicochemical indicators of solubility, different seasons of the year, different times of the day. At the same time, the purity or impurity of the water also affects the solubility of gases.

Basicityofwater

The overall concentration of some salts like ОH-, HCО3-, CО32-, PО43-, SiО32-and weak organic acids in water is called the total basicity of water (Bw) and is expressed in millimoles (mmol/l) in a liter of water. Because all of these substances interact with acids, which means that the total water content is determined by the amount of acid consumed for titration with a methyl indicator. Depending on the type of anions such ashydrocarbonate Нhc(HCО3-), carbonate Нc (CО32-), silicate Нs (SiО32-), hydrate Нh (ОH-), phosphate Нph (Н2РО4-, НРО42-, РО43-), they are subdivided for substantiations. The total substantiation will be equal to Нж Нhc Нc Нs Нh Нph.

In natural waters, most often, hydrocarbonate ions are found in relatively large quantities, therefore, Нж Нhc is characteristic of such waters.

Waterhardness

Water hardness is one of the indicators of its quality. The hardness of natural waters depends on the presence of calcium and magnesium salts in them. It is expressed by the total millimolar amount ofСа2+and Мg2+ions in a liter of water. Hardness is classified into two groups: temporary and permanent.

The temporary (carbonate) hardness of Hw is mainly characterized by the presence of calcium and magnesium gyrocorbanates Са(НСО3)2, Мg(НCО3)2in water, whichturn into insoluble salts and precipitate as a solid precipitate when boiling water:

Са(НСО3)2 СаСО3 СО2 Н2О

Мg(НСО3)2 МgСО3 СО2 Н2О

The constant (non-carbonate) hardness Hc is determined by the amount of chlorides, sulfates, calcium and magnesium nitrates in water, which are in a dissolved state in solution even when water is boiled.

The sum of the temporary and permanent water hardness gives the total hardness.

Natural waters are classified according to their total hardness into: soft (Hw2); medium (Hw210) and hard (Hw 10) waters.

Water oxidability

Water oxidability is substances contained in water and are mainly determined by the mass of oxygen (based on mg/l) required for the oxidation of organic substances and small amounts of iron compounds, hydrogen sulfide, nitrates. Its value is used to mentally describe the concentration of organic impurities in water. The oxidizability of artesan waters is usually 1-3 mg/l, clean lake waters - 5-8 mg/l, peat waters - 400 mg/l of O2.

2.9 Waysofindustrial water treatment

When water is precipitated, impurities in water are separated mainly by the precipitation method. This method is also called the reagent method because it separates precipitate impurities with special reagents. Processes used in water precipitation include methods of coagulation, liming, and purification of magnesia silicon.

Coagulation, as a physicochemical process, occurs through the fusion of colloidal particles, the formation of coarse microphases (follicles). Аl2(SО4)3, Fе2(SО4)3are mainly used as reagents called coagulants. Flocculants (polyacrylamide, active silicic acid, etc.)are used to increase the efficiency of coagulation. At this time, the formation of sediments is accelerated and their structure improves.

The sediment, consisting mainly of aluminum and iron hydroxides and other impurities, is released from water in special sedimentation tanks, open filters, contact sedimentation tanks of granular material (silica sand, crushed anthracite, keramzit, etc.), as well as in flotation machines, hydrocyclones. Various microfilters are usedto get rid of coarse impurities.

Liming.The water is treated with limefor reduction of the hydrocarbonate content. In the process the hardness, the salt content, the concentration of coarse impurities, the content of iron compounds and silicic acid are reduced.

Slaked lime Са(ОН)2is a reagent for this process. It is put into water in the form of a suspension (lime cream). In order to increase the efficiency of the loss of silicic acid, caustic magnesite (70-80% MgO) is added to the water

These processes are carried out mainly simultaneously and in one sedimentary tank. It is necessary to filterfor complete sediment detachment.

Silica sand, crushed anthracite, cellulose, perlite, volcanic slags, keramzit, etc. are mainly used as filtering materials.

Desaltation. Removing calcium and magnesium compounds that make water hard is called desaltation. One of the most effective ways of desaltation is the combination of the lime-soda method with the phosphate method. The desaltation process is based on the following reactions:

To remove temporary hardness, iron ions and СО2binding by slaked lime treatment:

Са(НСО3)2 Са(ОН)2 2СаСО3 2Н2О

Мg(НСО3)2 2Са(ОН)2 2СаСО3 Мg(ОH)2 2Н2О

FеSО4 Cа(ОH)2Fе(ОH)2 CаSО4

CО2 Cа(ОH)2 CаCО3H2О

1) caustic ash treatment for removal the permanent water hardness:

2) trisodium phoshate treatment for complete sedimentation of Cа2and Мg2ions:

3Са(НСОз)2 2Nа3PО4  Cа3(РО4)2 6NаHCО3

3МgCl2 2Nа3PО4 Мg3(PО4)2 6NаCl

The phosphate method is effective since the solubility of calcium and magnesium phosphates is very low.

Currently, the ion-exchange method is widely used for desaltation, salt elimination and water sterilization. The method is confined in that ions of a positive and negative charge in a solution of a solid - an ion exchanger - an electrolyte are replaced by other ions with the same charge in an equivalent amount. Depending on the type of charge, the replaced ions are divided into ion exchangers – cationidsand anionids.

Cationidsare mainly insoluble substances present in insoluble anionic salts or acids; cationids in the ion exchanger (sodium or hydrogen) react with cations in solution under certain conditions. Such cations are called Na-cationids or H-cationids.

Anionids are insoluble bases or cation salts. Anionids contain an active OH group (OH-anionids).

The following aluminosilicates are used as Na-cationids: glauconite, zeolite, permutite, etc.; synthetic resinsare used as H-cationids. Synthetic resins with a complex composition are usedfor OH-anionids, it is, for example, carbamide.

Ion exchange between a solution and an ionis is a chemical reaction that is heterogeneous. Impurities in water purified by an ion-exchange method do not form a precipitate, and such treatment does not require constant addition of components.

One of the main characteristics of ionids is called the cation exchange capacity, which indicates the absorption of ions of a certain size by the ionids under certain conditions. The cation exchange capacity is determined by the duration of the working cycle of ionid filters. As soon as the ionid exchange capacity reaches a certain limit, the process of its recovery takes place (by carrying out the ion exchange process in the opposite composition).

The cation desaltation process is based on the reaction of exchange of sodium and hydrogen ions in cationids for Са2and  Мg2ions. The exchange of sodium ions is called Na-cationization, the exchange of hydrogen ions–H-cationization:

2RNа Cа2  R2Cа2 Nа

2RNа Мg2  R2Мg2 Nа

here R – complex matrices and functional groups that do not participate in the ion exchange reaction (obtained as monovalent).

During H-cationization, cation exchange occurs according to the following reaction:

2RН Cа2R2Cа2 Н

2RН Мg2R2Мg2 Н

RНNаRNaН

After the cationid exchange capacity reaches the limit, they are deoxidized by washing with solutions of NaCl or sulfuric acid H2SО4.

When the cationid is deoxidized with NaCl solution, the following reactions occur:

R2Cа2 nNа  2RNа Cа2 (n - 2)Nа

R2Мg2 nNа  2RNа Мg2 (n - 2)Nа

here (n – 2) – NaCl taken more when comparing stoichilmetric volume.

The recovery of the H-cationic filter occurs with a 1-1.5% solution of sulfuric acid in accordance with the following reactions:

R2Cа2nН  2RН Cа2 (n - 2)Н

R2Мg2nН  2RН Мg2 (n - 2)Н

RNаnНRНNа (n - 1)Н

When water is filtered through the layers of anionids, sorption of anions occurs, which occurs in accordance with the reaction below:

RОH- Cl-  RCl-ОH-

2RОН-SО42-R2SО42- 2ОH-

Recovery of anionids filters is carried out mainly with  4% NaOH solution in accordance with the following reaction:

RCl- nОH-  RОH- Cl- (n – 1)ОH-

R2SО42- nОH-  2RОH- SО42- (n – 2)ОH-

The diagram of the installation, which goes one after the other with the use of H-cation exchange and OH-anion exchange, is shown in Fig. 2.4. When water passes through the cationid in the H-cation exchanger filter (1), it is purified from calcium and magnesium ions, then in the anion exchanger filter (2) it is purified from anions. Then the water passes through the degasser (3), where it is purified from oxygen and carbon dioxide and is sent to the consumer through the storage device (4). A solution of sulfuric acid is usedfor restoration of the filter (1), a sodium hydroxide is used for restoration of the second filte.

1 – cation exchange filter; 2 – anion exchange filter; 3 – degasser; 4 – water storage device

Figure2.4– Installation diagram of water desaltation

ІІІELEMENTS OF CHEMICAL THERMODYNAMICS AND THERMOCHEMISTRY OF MATERIALS

3.1 Basics of thermodynamics

Chemical thermodynamics as a theoretical basis for the technology of building materials allows to determine the direction and energetics of the processes, heat balances, stability of the products, equilibrium concentrations of reaction products and determine the optimal order of the reactions.

Chemical thermodynamics considers a system of bodies interacting with each other and, in this regard, a change in the properties of systems. The system of factors influencing the system is called the external environment. If the system is intimate throughout its volumeit is called homogeneous, and if the system consists of several phases with a superficial difference from each other it is called  heterogeneous.

The state of the system is determined by its properties. The quantities characterizing the state of the system are called system parameters or thermodynamic parameters. System pressure, temperature, intrinsic volume, concentration, internal energy, entropy, enalpy can be parameters that characterize the system.

A chemical change in a substance is called a reaction, and a physical change is called a process. The thermodynamic process can take place through heat release or heat absorption. Thus, chemical thermodynamics, using the three basic laws of thermodynamics, investigates the possibility and direction of chemical reactions.

The first law of thermodynamics is a mathematical expression of the law of energyconservation: energy does not exist and does not disappear from non-existence, but only passes from one type to another. Energy balances of chemical reactions are calculated on the basis of the first law of thermodynamics.

In thermodynamics, the following designations are used: work-A; heat - Q; internal energy-U; enthalpy-H; heat capacity - Cp or Cv.

The system state function is called parameters on which only the initial and final state of the system depends, and not the path of the system transition from one state to another. For example: for this purpose can be obtained the internal energy of the body (potential+kinetic energy) or liquid water at a temperature of + 20°C and water vapor in equilibrium with it. The water-steam system has specific parameters: pressure, volume.If we heat water, all of the water turns into steam. The resulting water vapor is characterized by other parameters (temperature, pressure, volume). The internal energy of water molecules at this time changes and is determined by the final state. The participation of the system in certain processes leads to  ΔU-change in its internal energy. But the value of ΔU does not depend on whether these changes are carried out by: U1 - a - U2 or U1 - c - U2, but depends only on the initial internal energies of the system U1 and the final U2:

ΔU=U2 - U1 (3.1)

Therefore, it is sufficient to know the value of its internal energy in various statesto describe the internal energy of a system. For closed processes leading to the return of the system to its original state, the value of ΔU is equal to zero.

In addition to internal energy, the concepts of work and heat are used in thermodynamics.

Heat is movement that is transmitted based on the random movement of microparticles. Another work is that macroscopic masses, made up of very large numbers of particles, are a form of sequential motion caused by a certain force. Generally, Q is a heat and A is a work. They cannot be the system state function, since it depends on the path of change. For example: an increase in gas equal to the multiplication of its pressure (p) and the increased volume.

A=pV (3.2)

The equation of several principles of thermodynamics is a mathematical representation of the law of conservation of energy:

Q=ΔU+A  (3.3)

or in differential equation:

δQ = δU+δA  (3.3а)

that is, the heat given to the system is spent on changing its internal energy and the operation of the system.

It can be seen from the above formulas that heat and work cannot be a function of the state of the system, since these two quantities correspond to the process, and not to the system.

But in both cases, heat can become a function of the state of the system, that is, it depends only on the initial and final state of the system, regardless of the ways of the transition of the system from one state to another:

- the first case is an isochoric process, i.e. in a process when the volume is constant:

if V=const; thenA=pΔV=0.

that is, the heat given to the system is spent only on changing the internal energy:

Q=ΔU   (3.4)

For example, compressed gas in a cylinder will not work until we start to release gas from the cylinder. Gas heating in a closed volume leads to an increase in pressure and, accordingly, to an increase in internal energy.

- secondly, the isoboric process, that is, during processes proceeding at constant pressure:

If p=const, then A=p(V2 – V1)

that is, the work depends only on the initial and final state of the system, and not on the way of changing its state. In this case, equation 3.3 is described as follows:

Qp = U2 – U1 + pV2 – pV1                              (3.5)

hereU+pV=H. The new function of the system state is called enthalpy. I.e.:

Q= H2 – H1 =∆H

According to Hess's law, the thermal effect of chemical reactions does not depend on the intermediate stages of the process, but only on the initial and final state of the active substances. This law is the applicability of the first law of thermodynamics for all processes occurring under conditions of constant volume or constant pressure. In thermochemical equations, chemical symbols describe not only the amount of a substance, but also the supply of their internal energy for processes occurring under constant volume conditions, or the enthalpy for processes occurring at constant pressure.

Accordingly, for processes proceeding at constant pressure, the thermal effect is denoted by Qv, and for processes proceeding at constant pressure, the thermal effect is denoted by Qp. At low temperatures, the volume in liquids and solids changes insignificantly, therefore:

Qр - Qv=pΔV=0                              (3.6)

This dependence is also proper to reactions proceeding in the presence of gases, in which the initial number of moles and the number of moles after the reactions do not change.

There is the following relationship between enthalpy and reaction heat:

ΔH = - Q   (3.7)

As a standard state at ΔH=0, the values of the enthalpy of elements were obtained under a pressure of 1 atm and a temperature of 25°C (2980K). If there are several derated modifications of a substance, then the value of its most stable modification is taken as the standard value. And for the rest of the modifications, ΔH has a negative value, since energy is consumed for their transition from the standard state.

In this regard, in chemistry opposite symbols are used to the symbols which are used in chemical thermodynamics,where enthalpy has a negative value for the processes while formation of compound (exothermic) during heat formation. When using the standard enthalpy value, attention must be paid to the state of aggregation of substances.

Common thermodynamic values for some substances commonly used by builders are shown in Table 3.1.

Table 3.1–Values of common  thermodynamic quantities of some substances

| Substances | State of aggregation | ∆Н0 298, кJ/mol | S0298, J/ (mol deg.) | ∆Z, кJ/ mol |
| --- | --- | --- | --- | --- |
| Na | crystal | 0 | 51,12 | 0 |
| Cl2 | gas | 12,65 | 165,34 | 105,55 |
| C | crystal | 0 | 56,98 | 0 |
| CO2 | gas | - 394,07 | 213,94 | -394,95 |
| CH4 | gas | -75 | 186,46 | -50,87 |
| H2O | gas | -242,18 | 188,97 | -228,94 |
| H2O | liquid | -286,26 | 70,06 | -237,53 |
| H2O | crystal | -292,25 | 39,39 | -234,43 |
| NaCl | crystal | -411,58 | 72,49 | -384,50 |
| SiO2 | crystal | -860,63 | 41,49 | -806,16 |
| Silica | crystal |  |  |  |
| SiO2 | glass-like | -848,47 | 46,93 | -799,87 |
| Fe2O3 | crystal | -822,08 | 90,08 | -742,05 |
| Al2O3 | crystal | -1672,23 | 51,08 | -1578,67 |
| Alumina | crystal |  |  |  |
| CaO | crystal | -636,46 | 39,81 | -605,04 |
| CaCO3 | crystal | -1208,61 | 93,02 | -1130.38 |
| calcite | crystal |  |  |  |
| Ca(OH)2 | crystal | -988 | 76,26 | -898,04 |

Example 1. It is necessary to calculate the reaction heat ofCaO(c) + СО2(2) → СаСО3(c).

Solution: It is necessary to find the standard enthalpies of the initial and final substancesin the table.

The valueΔH of any reaction is equal to the difference of the heat (enthalpies) of formation of the reaction products (CaCO3(c)) and the initinal materials (СаО(c); СО2(g))

ΔH= ∑ΔH(reaction products) - ∑ΔH(initial substances)

next:

ΔH=-1208,61 – (-636,46 + -394,07) = -178,07 кJ

Reactions with negative enthalpy values are exothermic, and reactions with positive enthalpy are endothermic. Exothermic processes occur spontaneously, while for endothermic reactions, energy must be supplied from the outside.

Example 2. It is necessary to determine the amount of heat required to heat 1 kg of silica  from 20 to 1000°C.

Solution: It is necessary to determine the molar heat capacity of silica from the evaluation of physicochemical quantities:

Ср = 47,01 +34,36· 10-3Т - 11,31 · 105Г-2.

The desired temperature range is:

Т2-Т1 = (1273-293)К.

The amount of heat spent on heating 1 mole of silica is calculated by the formula:

Н2 -Н1=Т1Т2СрdT=a(T2-T1)+b(T22-T12)/2+C(T2-T1)/T2T1 (3.8)

∆Q = ∆Н = 47,01 (1273-293) + 34,36 ·10-3 /2 (12732-2932) - 11,31·105х

х(1273-293)/ (1273-293) = 69464 J/mol.

Let's calculate the number of moles in 1 kg of silica:

n= 1000/60 =16,6.

Answer: the amount of heat spent on heating 1 kg of silica is

∆Q = 69464·16,6 = 1153102,4 J = 115,31 кJ.

The value of the bond energy directly depends on the chemical compounds in which it is formed. For example, the average O – H bond energy in water is 458 kJ/mol, and in alcohol - 438.7 kJ/mol.

Knowledge of the energy of the crystal lattice makes it possible to characterize the hardness, strength and heat resistance of a material. At the same time, knowing the energy of the crystal lattice, one can understand the important characteristics of a substance about the possibility of its hydration and proximity to solvents.

The energy of the crystal lattice of tricalcium silicate (alite) and dicalcium silicate (belite), which are the main constituents of cement, is 10768 and 7240 kJ/mol, respectively, and the crystal lattice energy of CaO of lime is much lower - 3528 kJ/mol.

Knowing the exact information about the energy of the crystal lattice is of great importance not only for science, but also for practice. Because, it helps to calculate in advance the energy spent on processing the material.

In addition to isochoric and isobaric processes, knowledge of isothermal processes occurring at a constant temperature is of great importance for technologists.

When t=const, the work of the system is defined by the following formula:

(3.8а)

where R – a constant gas, T – the absolute temperature, n – the number of molecules. If the change in concentration or pressure during the reaction is known, then it is solved as follows, depending on the parameters:

(3.8 b)

(3.8c)

These dependencies are often used to determine the centers of crystallization during the crystallization process.

The thermochemical calculations considered above are based on the application of the first law of thermodynamics. However, there are also known chemical reactions and processes proceeding in accordance with the law of conservation of energy, which are also difficult to implement from a practical point of view.

Therefore, another law is needed that characterizes the direction and possibility of the process. Such processes are described by the second law of thermodynamics.

Observation of the processes shows that they are moving in the direction of equilibration. This equilibrium is inherent in any system, and the processes occurring in the system necessarily tend to a state of equilibrium. For example, mixing cement with water necessarily leads to hydration of the cement, since the cement hardens during hydration, which corresponds to the equilibrium state of the system. Heat passes from a hot body to a cold body only until the temperatures of these bodies become equal, etc.

The problem of equilibrium is of great importance in chemical reactions. So that better to start from the explaination of what equilibrium or state of equilibrium is.

The equilibrium state of the system is characterized by the following features:

- the stability of the state regardless of the time when the conditions of the external environment are stable;

- dynamic mobility (it returns to its original statein case of imbalance);

If the equilibrium state is characterized on the basis of the rates of reactions of the forward and reverse directions, then it means that the reactions do not stop, but their rates are equal.

The change in the internal energy of the system can be depicted through the corresponding state parameters as follows:

dU = TdS + pdV + Ede + μdm ...,(3.9)

here T - temperature; S - entropy; p - pressure; V - volume; E - electric potential; e - electric charge; μ - the chemical potential; m - the mass.

Heat capacity is widely used in thermodynamics. Heat capacity is the amount of heat spent on heating 1 g (specific heat capacity) or 1 mol (molar heat capacity) of a substance to a temperature of 1°C.

The average heat capacity is determined by the formula:

Ĉ = Q/T2–T1= Q/∆T or Q= Ĉ∆T                 (3.10)

Manuals basically indicate the true heat capacity, which is the limit (zero) of the average heat capacity by reducing the minimum temperature range:

∁=limt2-t1Ĉ (3.11)

Heat capacity is divided into heat capacity at constant volume (Cv) and at constant pressure (Cp). Since silicate systems are condensed systems without a gas phase, an increase in the external pressure and volume of the system can also be ignored, then:

Ср≈ Cv = С      (3.12)

Taking into account (3.10) and (3.12), the relationship between the real heat capacity and the average heat capacity can be depicted as follows:

Ср = dQ/dT = d(Cp ∆t)/dT = (dH/dT)p         (1.13)

here dH –increase of enthalpy.

Considering that Ср =Т1Т2CpdT / Т2-Т1; Ср = dH/dT       (3.14)

thenusing integration, the equation below can be obtained:

Н2-Н1 = Т1Т2CpdT      (3.15)

Using the integral regression equation that are used in formulas (3.14) and (3.15), which are used mainly for organic substances, you can solve:

Ср = а + bТ+сТ2+...,(3.16)

And also using the below equation which is mainly applied to inorganic substances

Ср = а + bТ+сТ-2 +...,   (3.17)

The values of the coefficients a, b, c of the heat capacity of all substances are presented in thermodynamic manuals.

The value of the average heat capacity can be solved by the values of constants  of 3.17equation and by solving the integralТ1Т2CpdT in 3.14 equation.

Ср = а + b/2 (Т1+ Т2) + с/Т1Т2        (3.18)

Example 1. Calculate the average heat capacity of silica in the temperature range of 298-1000K.

Solution: It is necessary to find the coefficients in the manuals and compose the equation for the molar heat capacity of α-silica:

For more information, see original text

Ср = а + bТ – сT-2 = 47,01+34,36·10-3Т - 11,31·105T-2

according to equation 3.14:

Ср = 1/ Т2–Т1Т1Т2(a+bT-cТ-2 )dT

Using the integration, we get the following formula:

Ср = а + b/2 (Т1+ Т2) + с/Т1Т2 = 47,01 + 34,36·10-3/2 (1000-298) -11,31·105/(1000·298)= 55,28 J/mol.

Answer: the average heat capacity of silica in the temperature range 298-1000K is 55.28 J/mol.

3.2 Hess's  law

Hess’s law. Hess's Law was discovered in 1840 and has a form of the application of the first law of thermodynamics to specific cases. All chemical reactions take place through heat release or heat absorption, and this is the basis for heat balances of chemical reactions and thermotechnical calculation.

According to Hess's law, the enthalpy of the reaction does not depend on the intermediate stages of the reaction, and is a quantity that is determined by the initial and final state of the system:

∆Нt 0=Vi ∆Hti0                           (3.20)

here ∆Нt 0 – Т is the enthalpy of formation of compounds of simple substances at temperature, Vі is the number of moles during chemical reactions of substances (for reaction products - +Vі; for initial substances – -Vі), ∆H°Ті– enthalpy of formation of substances participating in the reaction.

Example 3. Calculate the heat effect of sodium silicate formation by the following reaction:

Nа2О + SiО2 = Na2Si03

Solution. It is necessary to find by determinants:

∆Н°298 (Nа2О) = -416,16 кJ/mol;

(Si02) = - 911,55 кJ/mol;

(Na2Si03) = -1562,47 кJ/mol.

Determine the following using Hess's Law:

∆Н°298 = ∆Н°298Na2Si03 -∆Н°298Na20 -∆H°298Si02 = -1562,47+416,16+911,55= -234,76кJ/mol.

Answer: the thermal effect of the formation of Na2Si03is equal to 234.76 kJ/mol.

Reactions with negative enthalpy values are exothermic, and reactions with positive enthalpy are endothermic. Exothermic processes occur spontaneously, while for endothermic reactions, energy must be supplied from the outside.

Example 4. Determine the heat formation Ca(OH)2 based on the following reaction:

1) СаСО3 = СаО + С02

2) СаО + Н20 = Са(ОН)2

Solution. According to the standard enthalpy values given in the manuals, the heat effects of the first and second reactions are equal:

∆Н°298(1)=∆Н°298СаО + ∆Н°298С02-∆Н°298СаС03 = +177,83 кJ/mol;

∆Н°298(2)=∆Н°298Са(ОН)2-∆Н°298СаО -∆Н°298Н20= -65,20 кJ/mol.

The first reaction occurs only when energy is transferred from the outside, and the second occurs  spontaneously. The total energy of formation of Ca(OH)2 is equal to:

∆Н°298 = ∆H°1 + ∆Н°2 = 177,83-65,20 = +113,61 кJ/mol.

Answer. The heat of formation of Ca(OH)2 is equal to +113.61 kJ/mol.

3.3 Dependence of the thermal effect on temperature. Kirchhoff's equation

The thermal effect of chemical reactions depends on temperature. The change in the heat effect of the reaction is calculated from the difference in the heat capacity of the reaction products and the initial materials, taking into account the stoichiometric coefficients.

The dependence is described by the Kirchhoff's equation:

For more information, see the original text

[d(∆H) /dT]p = [dH/dT]p = ∆Ср = ΣViCpi                     (3.21)

here ∆Ср is the difference in molar heat capacities (molar numbers), provided that stoichiometric coefficients are taken into account, at ∆Ср> 0, the heat effect of the reaction increases due to an increase in temperature, at ∆Ср = 0, it does not depend on temperature, and at ∆Ср <0, it decreases.

The difference in molar heat capacities is calculated in accordance with the equation ∆Ср (3.13):

∆Ср = ∆а + ∆bТ + ∆сТ-2.

Using the value of ∆Ср in the equation (3.22) and integrating it, we find the thermal effect of ∆HT - reaction:

∆НТ = ∆Н0 + ∆аТ + 1/2 ∆ЬТ2 - ∆с/Т (3.22)

In this equation ∆H0 is constant integration, unknown quantity. It is found by determining a known ∆HT value at a given temperature.

Example 5. If the heat of dissociation of calcite at a temperature of T=173K is equal to 178.07 kJ/mol, it is necessary to find the equation ∆HT=fT and determine the heat spent on the breakdown of 1 kg of calcium carbonate at a temperature of 1000°C.

Solution:

СаСО3 = СаО+СО3

We find the equation for the molar heat capacity of the reactants from the determinants:

СрСаСОз = 104,5+21,92·10-3Т - 25,94·105Т-2;

СрСаО = 49,63 +4,52·10-3Т- 6,95·105Т-2;

СрС02 = 44,14 + 9,04·10-3Т- 8,53·105Т-2.

The calculations will be carried out according to equation (3.22). First, the general coefficients ∆а, ∆b, ∆с will be calculated.

∆а =Σаproduct–Σаinitial materials,

∆а = аСО2+ аСаО - аСаСОз = 49,63 + 44,19 - 104,5 = -10,73.

Likewise:

∆b = bС02 + bСа0 - bCаCOз = 9,04·10-3 + 4,52·10-3 – 21,92·10-3 = -8,36·10-3;

∆с = 8,53·105 + 6,95·10-5 – 25,94·105 = -10,46·105.

The equation for the heat effect of the reaction:

∆НТ = ∆Но- 10,73Т - 8,36·1031/2 Т2 + 10,46·105Г-1.

In problem situation: ∆Н1173=178,07 кJ/mol= 178070 J/mol,

here

∆Но = 178070 + 10,73·1173 + 8,36·103·11732 - 10,46·105·1173-1 =191141,49.

Equation ∆HT=f (T) of the decorbanization reaction

∆НТ= 191141,49- 10,73Т-8,36·10-3Т2+ 10,46·105Т-1.

It is necessary to use this value in the above equation for determination of the heat effect of this reaction at 1000°C=1273K:

∆НТ = 191141,49- 10,73 · 1273-8,36•10-3 ·12732 + 10,46·105·1273'1= 164755,76 J/mol= 164,75 кJ/mol.

The molecular weight of CaCO3 is equal to 100.09, the number of moles per 1000g:

n=1000/100,09=9,99.

Answer: The thermal effect of breakdown of 1 kg of calcite at a temperature of 1000°C is equal to

∆НТ = = 1646,02 кJ/kg.

3.4 Application of the second law of thermodynamics to physicochemical processes

The processes are classified as reversible, irreversible, and equilibrium. Reversible processes do not lead to a change in the parameters in the reaction environment and in the system, while irreversible processes change both the environment and the system. Reversible processes are sometimes called an equilibrium process. The study of the system taking into account the time factor is carried out by the thermodynamics of irreversible processes.

The second law of thermodynamics. M. Lomonosov said: «Heat cannot independently pass from a cold body to a warm body»; Clausius mentioned: «There cannot be a process in which heat passes from a cold body to a warm one». From the point of view of a static approach: the probability of self-carrying processes goes from low to high. The first law of thermodynamics is enthalpy, it embeds the functions of statelike internal energy, the second law of thermodynamics is entropy, it introduces the function of state.Clausiusentropy is the ability to change, and it is related to the heat of the process (Q/T). For a system, an increase in entropy means a transition of the system from a state with high consistency to a state with low consistency. If the system transitions from a low consistency state to a high consistency state, the entropy decreases. Hence, absolute zero has complete consistency in an ideal crystal, and entropy is zero.Actual crystals always have impurities, crystal lattice defects, therefore, the entropy of solids is not zeroeven at low temperatures. Since the value of infeasibilityincreases with increasing temperature, the energy of the system increases as well.For any substance, entropy increases in the solid-liquid-gas series. For example, the entropy of ice, water and water vapor is 39.3; 69.9; 188.7 J/(mol• К), respectively. For reversible processes, the increase in entropy is determined by the ratio of a very small amount of heat, supplied to the system, to the temperature:

dS= dQ/T (3.23)

Heat change is related to molar heat capacity:dQ =CpdT.

Then dQ =CpdT /T                                         (3.24)

It can be seen from the equation (3.24)that the value of entropy coincides with the value of heat capacity: J/(mol• К). By integrating the temperature from 298K to T, we get the equation below:

S°T - S°298 = a In Т/298 + b (Т-298) + с/2 (Т2-2982)/(Т2 »2982) (3.25)

the values S°298 of the coefficients a, b, c are found in the reference book of thermodynamic quantities. The entropy of a system is an additive quantity, therefore, it is necessary to find the algebraic sum of the entropies of the interacting substancesfor  calculation of the entropy of chemical reactions,.

∆S=ΣSreact. product. –ΣSinital material             (3.26)

Then the formula for calculating the entropy will be the following:

∆S°T=∆S°298 + ∆а In Т/298 + ∆b (Т-298) + ∆с/2 (Т2-2982)/(Т2•2982)    (3.27)

From the second law of thermodynamics, it follows that if a system is isolated, then during reversible processes its entropy does not change, and during irreversible processes it increases. If an irreversible process brings an isolated system into equilibrium, then its entropy reaches its maximum value. Consequently, the entropy is a measure of the direction of the process at ∆S>0, and it is a measure of equilibriumat ∆S=0, if ∆S <0, the process does not occur in an isolated system. However, reversible and irreversible processes can also occur through a decrease in entropyin some parts of non-isolated systems.

The change in the total entropy during the transition from state A to state B is determined as follows:

∆S = SB - SAor ∆S°T= ΣVі S°Ti            (3.28)

Due to phase changesmodification changes, melting, gasification and other changes occur at a constant temperature, the entropy change is calculated from the definite values of the heat and temperatures of these changes, for example:

∆Smelting= ∆Н/Тmelting       (3.29)

3.5 Application of the third law of thermodynamics to physicochemical processes

In 1906, Nernst concluded that the change in the entropy of a chemical reaction around the absolute zero can also be ignored. In 1912, M. Planck showed that the crystal lattice of a substance is in an ideal stateat an absolute zero temperature, therefore its entropy should be also equal to zero. If we take the energy of the absolute zero temperature of a substance in the crystalline state equal to zero, then this substance has a positive entropy valueat high temperatures. But there are also substances that do not follow the third law of thermodynamics, they are substances with a disordered structure: these are glass, amorphous substances with S°0≠0.

The entropy of a substance is calculated according to the above formula (3.28), using the standard value of S°298 at 298K, the absolute value of entropy at 0K is not indicated, because it is calculated using a special method.

3.6 Gibbs energy and chemical equilibrium

Gibbs (1878), Helmholtz (1884) and Van Hoff (1885) proposed to describe the performance of the system by the isobaric-isothermal potential or Gibbs energy. Gibbs energy is determined by the ratio:

TdS = dU + pdV - μdm           (3.30)

here TdS is the bound energy, dU is the change in internal energy, pdV is the mechanical work, μdm is the chemical work. Moving the values in place, we get the following formula:

G = H-TS                  (3.31)

here G - Gibbs energy, H - enthalpy, S - entropy, T - temperature.

Separate products (dG/dT)р=-S and (dG/dp)T=V indicate that Gibbs energy is a characteristic function that determines the quantitative relations of the system with the environment, i.e., it can also have internal energy.

For isothermal process(Т-const) or reaction:

∆GT = G2– G1 = ∆НТ – T∆ST                       (3.32)

For standard cases:

∆G°298 = ∆Н°298 - T∆S°298 (3.33)

In the standard case, the Gibbs energy, associated with the formation of an ideal gas, pure liquid or solid under a pressure of 0.1 Mpa, is called the standard Gibbs energy of formation, it is denoted ∆G0ƭ and is indicated in the reference book of physical quantities.

The Gibbs energy decreases and acquires a minimum valuefor any processes that occur spontaneously at constant temperature and pressure.

If: ∆G р;Т< 0 –a reaction takes place,

∆G р;Т = 0 –chemical equilibrium is formed,

∆G р;Т> 0 –the process cannot happen by itself.

The integration method of the molar heat capacity equation described by the temperature series is usedfor calculation of the Gibbs energy and its application in analyzing the probability of reactions in various systems. For the calculation,the initial data are taken from the table of thermodynamic properties of substances in the standard state: enthalpy - ∆H°298, entropy - ∆S°298, Gibbs energy - ∆G°298, and coefficients a, b, c from the heat capacity equation.

The calculation is carried out in the following order:

1.Define enthalpy reaction:

∆Н 298=∑∆Н°298(r.p.) -∑∆Н°298(i.m.)

2.Define reaction of Gibbs energy:

∆G°298=∑∆G°298(r.p.) -∑∆G°298(i.m.)

3. Define ∆Ср =ƭ(Т) for reaction:

∆Ср = ∆а + ∆bТ - ∆сТ-2

And for ∆а =∑a(r.p.)-∑a(i.m.), ∆band ∆с as well.

4.By integrating the obtained equation of heat capacity, and puttingthe value of ∆Н298 in it (according to equation 3.22), we determine the constant ∆Н°298 at T=298K:

∆Н0 = ∆Н°298 - ∆а 298 –1/2∆b (298)2 + ∆с (298)-1

5.Gibbs energy at any temperature is expressed by the following equation:

∆G°T = ∆Н0 - ∆аТ lnТ - ∆b /2 Т2 - ∆с/2 Т-1 + JT

here J-integration constant, determined by putting the known values of ∆G°298 and T=298K into this equation.

6. Determine the integration constants ∆Н0 and J and calculate ∆G°T:

∆G°т = ∆Но - ∆аТ InT - ∆b/2 Т2 - ∆с/2 Т-1 + JT

The value of the Gibbs energy is determinedby setting different temperatures, the dependence ∆GT=f(T) (at ∆G°t>0) allows to determine the temperature interval in which the reaction does not take plcae, (at ∆G°f=0) happens the beginning of the reaction and its behavior.

Example 6. Conduct a thermodynamic analysis of the formation of calcium monoaluminate Са0А1203from the original raw materials СаО, Са(ОН)2. СаС03.

Solution. From the maual on thermodynamic quantities, we find the values ∆G°298, ∆H°298, the coefficients a, b, c of the molar heat capacity of the original materials and reaction products (Table 3.2):

1.СаO+Al2O3= СаOAl2O3

2. Са(OH)2+Al2O3= СаOAl2O3+H2O

3. СаCO3+Al2O3= СаOAl2O3+CO2

Table 3.2–Thermodynamic characteristics of compounds

| Compounds | ∆Н°298, кJ/mol | ∆G°298, кJ/mol | ∆Ср = ∆а + ∆bТ - ∆сТ-2 |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | a | b•103 | c•105 |
| СаO | -635,55 | -604,17 | 48,83 | 4,53 | -6,53 |
| Са(OH)2 | -986,59 | -896,76 | 82,80 | 43,72 | 12,30 |
| СаCO3 | -1206,87 | -1128,76 | 104,52 | 21,92 | -25,94 |
| Al2O3 | -1669,83 | -1576,53 | 114,77 | 12,80 | -35,44 |
| СаOAl2O3 | -2221,28 | -2202,04 | 150,67 | 41,76 | -33,30 |
| H2O (г) | -241,83 | -228,59 | 30,00 | 10,71 | 0,33 |
| CO2 (г) | -393,51 | -394,38 | 44,14 | 9,04 | -8,54 |

For the 1 reaction:

∆Н°298=∆Н°298СА- ∆Н°298СаО-∆Н°298А1203= - 2321,28 -(-635,55) - (-1869,83) = =-15,9 кJ/mol

∆G°298 = -2202,04 - (-604,17) - (- 1576,33) = -21,34 кJ/mol

∆а = ∆аса - ∆а СаО-∆аAl2O3 == 150,67 - 48,83 -114,77 = -12,93

∆b = (41,76-4,52-12,80)* 10-3 = 24,44·10-3

∆с = (-33,3 - (-6,530 - (-25,94))• 105 = - 0,83·105

Find theintegration constant ∆Н°:

∆Но - ∆Н°298 - ∆а 298 - ∆b/2 2982 + ∆c 298-1= -1590 + 12,93·298 –

-24,44·103/2·298 – 0,83·105·298-1 = - 13410,56

We define the integration constant J from the dependence ∆GT=f (T) at T=298K:

∆G°T = ∆Н0 - ∆аТlnT - ∆b/2 Т2 - ∆с/2 T-1 + JT =-21340 = -13410 + 12,93·298·ln 298 – 24,44·10-3/2 2982 + 0,83·105/2· 298-1 + J·298

From this equation, we define that J=-97.13. The thermodynamic functions and values are defined for same reactions 2 and 3.

Basedonthe findings we calculate the equation ∆GТ = f(T) :

Reaction (1): ∆G°T = -13410 + 12,93·Т lnT-12,22+0,41 · 105T-1 - 97,13T

Reaction  (2): ∆G°T = 95228 + 16,90 T lnT + 2,03·10-3Т2 + 4,91·105Т-1

Reaction (3): ∆G°T= 175048 + 24,48T lnT - 8,04·10-3T2- 9,77·105 Т-1–

- 348,20Т

We determine the values of ∆G°T at temperatures of 1000 and 1500K, the values of ∆G°T are shown in Table 3.3.

Table 3.3 - Calculations of the thermodynamic characteristics of the synthetic reaction of СаOAl2O3

| Reactions | ∆Н°298, кJ/mol | ∆G°298, кJ/mol | ∆Ср = ∆а + ∆bТ - ∆сТ-2 |  |  | Integral constants |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | ∆a | ∆b•103 | ∆c•105 | ∆Н0 | J |
| 1 | -15900 | -21340 | -12,93 | 24,44 | -0,83 | -13410,50 | -97,13 |
| 2 | 93310 | 42660 | -16,90 | -4,05 | -9,83 | 95228,00 | -278,87 |
| 3 | 161910 | 108870 | -24,48 | 16,08 | 19,54 | 175048,00 | -348,20 |

The calculation data shows that the synthetic reaction from СаО+А1203oxides takes place in the investigated temperature range, and Са(ОН)2 + А1203reaction happens at 600K(∆G°t=0) and СаС03 + А1203reaction begins at 920K.

Table 3.4- The value of the Gibbs energy at different temperatures of the synthetic reaction of СаОА1203

| Reactions | ∆G°T, кJ/mol |  |  |
| --- | --- | --- | --- |
|  | 298 | 1000 | 1500 |
| СаO+Al2O3 | 21,34 | -33,4 | -44,73 |
| Са(OH)2+Al2O3 | 42,66 | -64,38 | -135,82 |
| СаCO3+Al2O3 | 108,88 | -13,07 | -97,45 |

Thus, the calculations of the Gibbs energy of synthetic reactions from various materials containing calcium СаОА1203allow us to draw the following conclusions:

- the type of the raw materials has a significant impact on the reaction behavior;

- the probability of  Са0+А1203reaction is high among other reactions.

The studied raw materials, depending on their activity, can be arranged as follows:

СаО > Са(ОН)2> СаС03

3.7 Calculation of equilibrium constants of chemical reactions by thermodynamic functions

Equilibrium constant is a value that characterizes the relationship between the activity, concentration and partial pressure of the reaction components in an equilibrium state.

The reaction should take place according to the following scheme:

Formoreinformationseeoriginal text

аА(қ) +bВ(г) →сС(қ) +dD(г)

The equilibrium constant calculated for the equilibrium vapor pressure of each component (p) is equal to:

Ка = РсСРdD/РаАРbВ

If the substance is solid, then its equilibrium vapor pressure is equal to 1. Then for this reaction:

Ка = РdD/РbВ

For example, in the following reactions will be:

FeO+CO↔Fe+C02Ка = РC02/РCO

СаС03↔  СаО + С02Ка = РС02.

The CO2 pressure in CaCO3calcining nreaction is called the dissociation pressure. The temperature where CO2 pressure reaches 0.1 MPa (1 atm) is called the decomposition point.

The equilibrium constant can be calculated from known Gibbs energies using the formula below:

In Ка = - ∆G°T/RT = - 0,052 ∆G°T/T

∆GT-F (T) determines the value of the Gibbs energy taking into account the equation of molar heat capacity Cp=f(T). The equilibrium constant increases due to thereaction  heat and a temperature reduction.

The determined values of the equilibrium constant can be used to calculate the pressure of equilibrium vapors of gaseous components (Н20, СО, С02, S02, 02 and, etc.).

IVMAINRULESOFCHEMICAL KINETICS

Civil engineersmore frequently use the laws of chemical kinetics among all branches of physical chemistry.

Chemical kinetics is the science of the rate of chemical reactions, that is, of the processes that are constantly influenced by the time factor, which differs from thermodynamics. Consequently, the subject of chemical kinetics research is processes that develop over time, such as processes that were important for civil engineers, hardening of building materials, deterioration of organic materials, corrosion of building products and structures, stability of gels and emulsions.

However, civil engineers are still applying the laws of chemical kinetics, since the study of the mechanism of chemical reactions is also included in the task of chemical kinetics.

Two interrelated phenomena are considered when considering the mechanism and rate of chemical processes in chemical kinetics:

-macroscopic changes in a chemical reaction, independent of external factors (temperature, pressure, concentration), and these changes consist of certain chemical stages;

-specific microscopic chemical event leading to chemical reactions, that is, processes occurring in the microworld.

The mechanism of chemical reactions, that is, the sequence and content of elementary steps, consists of processes happening at the atomic and molecular scales.

Chemical processes are divided into homogeneous (occurring only in the volume of single phase) and heterogeneous (occurring between several phases with a surface difference) processes. Homogeneous reactions in construction include: polymerization and polycondensation reactions during polymer production, neutralization reactions between calcium hydroxide and acid in concrete pores. Heterogeneous reactions include: hardening of binding agents, corrosion of concrete, corrosion of reinforced concrete, etc.

4.1 General law of chemical kinetics

It is necessary to represent some definitions,which are necessary for synthesis of principal laws of chemical kinetics.

The speed of a homogeneous chemical reaction is determined by the change in the concentration of one of the active substances per unit of time.

ортСt(4.1)

here:СС1-С2

tt1-t2

Since there is a relationship between the concentration change of the reacting substances, it is sufficient to determine theconcentration change of one of the components when determining the reaction speed.

For example:

Н2SO4+2NaOHNa2SO4+2H2O

2H++SO2-4+2Na++2OH-2Na++SO2-4+2H2O

2H++2OH-2H2O

As follows from equation, two molecules of sodium hydroxide are required for deacidification of one molecule of dibasic sulfuric acid, and along with this two molecules of water are formed. Consequently, the speed of this reaction can be determined either by a decrease in hydrogen or hydroxyl ions, or by an increase in the concentration of a water molecule. Other chemical processes are calculated in a same way.

Figure 4.1–The ratio of reaction speed to concentration

Sometimes the speed of a chemical reaction can be determined by a change in certain physical parameters directly related to chemical acts, for example, a change in the coverage and electrical conductivity of a solution.

Norwegian scientists K. Guldberg and P. Waage formulated the basic law of chemical kinetics, which establishes the dependence of the rate of a chemical reaction on the concentration of reacting substances, and independently of them. The Russian scientist N.I. Beketov made independently the similar conclusion.

According to the basic law of chemical kinetics, the rate of the chemical reaction is in direct proportion to the product of the reacting substances concentrations.

For example, the mathematical equation of the basic law of kinetics for the reaction nA+mB=xC+yD, which occurs according to the following scheme, is written in the  following form:

kCna•Cmb(4.2)

Here k-chemical reaction constant;

Са and Сb-concentration of reacting agents;

nand m  - coefficients;

by this means for the above reaction:

R C(H2SO4)•С2(NaOH)

it means, the rate of a chemical reaction increases with increase of the concentration of reacting agents. And the reaction constant k does not depend on the concentration of substances; it shows the rate of the process if the concentration of the interacting substances is equal to one.

The value of this kinetic characteristic can be explained by the fact that at a constant temperature it does not change until the end of the process, and the concentrations of the interacting substances change per time unit. Consequently, the rate constant does not depend on the concentrations of the interacting substances; it describes the ability of their interaction with each other.

However, the above equation cannot describe the reaction mechanism. In most cases, the number of particles reacting in specific chemical elementary acts does not correspond to the number described by the above equation. Therefore, the kinetic equation (4.2) shows only the order of the reaction, that is, the sum of the exponents of the degrees of concentrations of the interacting substances included in this equation, which can be determined experimentally. Equation 4.2 shows that the rate constant depends on the order of the reaction.

For the simplest first-order reactions, the rate constant is characterized by the dimension of 1/c:

kC                             (4.3)

4.2 Consecutive and parallel reactions

Chemical reactions can be consecutive and parallel, depending on the mechanism of the process. The division of reactions into consecutive and parallel allows to have a better grip of the order of the reactions and the mechanism of their process, regardless of whether the reaction is homogeneous or heterogeneous.

Consecutive reactions have intermediate stages, when the product of the previous stage serves as aninitial material for the next one. One example is the processes of dissolution of a binder and crystallization of new growths, which ensure the hardening of cement. The rate of such reactions is determined by the rate of the slowest stage.

Multi stepis typical for homogeneous and heterogeneous reactions. For specific homogeneous reactions, a chemical reaction does not occur as a result of the direct interaction of all the initial molecules with each other, but as a result of several successive stages. The analysis of reactions is thus effective due to the need for collision of a small number of particles, which increases the likelihood of their collision for the implementation of elementary acts.

Parallel chemical reactions are called reactions where the same initial substances can simultaneously form different reaction products.

A diagram of consecutive, parallel and consecutive-parallel reactions is shown below:

а)  А→ C→ D→ Sconsecutive reactions;

b

б) А                            Dparallel reactions;

а

S

в) А → Bconsecutive-parallel reactions.

E

The rate of parallel reactions is determined by the following formula:

k1С+k2C+k3C+...knC(k1+k2+...kn)С        (4.4)

In general, the rate of a parallel reaction is determined by the change in the concentration of the initial substances and is equal to the sum of all the reaction rates that make it up. If the number of reactions is not large and it is known that the rate of one reaction is much higher than that of others, then the rate of a parallel reaction is determined by the fastest rate of reaction. This feature of parallel reactions from consecutive ones shows that the resulting product is in ratio to the reaction rate.

υ1υ2=k1Сk2С=k1k2  (4.5)

Consequently, parallel reactions differing from consecutive ones can be considered as rival reactions with each other and determine the direction of the general process, a reaction with a high speed.

Let us analyze why the rate of chemical reactions increases due to an increase in temperature.

Since the concentration of substances does not depend on temperature, the reaction rate in this case occurs due to an increase in the rate constant k, i.e., due to a change in the properties of molecules of various substances. For example, civil engineers are aware of substances that are in a liquid state under cold conditions and at normal room temperature and, when heated, quickly harden due to the acceleration of the reaction.

To understand why a change in temperature has such an effect on the kinetics of a chemical reaction, let us turn to the basic principles of chemical thermodynamics. The fact that a chemical reaction is a process of changing molecules was mentioned above. The atoms of the elements in the composition of substances keep close each otherwith a chemical bond. The type of chemical bond depends on the distribution of electron density in the molecule (covalent, heteropolar or intermediate).

As a result of a chemical reaction, energy rationality is achieved. But for its implementation, it is necessary to spend a certain amount of energy in order to break and regroup some of the old bonds, that is, to go through a certain potential energy barrier.

It is known that the molecules of any substance move at different speeds, it means they have different energy. Under normal conditions, only a small part can pass through this energy barrier, which is proportional to the concentration of common molecules in the reaction volume. Accordingly, the rate of a chemical reaction, which is proportional to the number of such molecules, will also be very low, that is, in some cases, such reactions do not occur.

To increase the speed of the process, it is necessary to expend the energy necessary to overcome a potential energy barrier. This energy is called the activation energy of a chemical reaction. It can transfer energy by heating the body or from other sources of energy: mechanical (vibration), electrical, radiation, etc.

The physical meaning of "activation energy" can be shown in the following figure.

Figure 4.2–Scheme of potential energy barrier

Y-axis shows the total energy Einitialbefore the reaction of the system and Econt.after the reaction. Thus, the difference Еа=Еinit-Еcont  describes the thermodynamic state necessary for the spontaneous behavior of a chemical reaction. But there is E energy barrier on the reaction route, and it is possible to carry out this reactiononly by overcoming this barrier. Consequently, activation energy is the amount of excess energy required to start a reaction. In general, this energy can be compared to the energy expended to push a ball up a hill, that is, it rolls down a hill by itself. The temperature incresase allows this energy barrier to be overcome.

As the temperature rises, the reaction rate increases exponentially

υ=υ0е-ЕRT(4.6)

Here υ0–reaction rate at a continuous high temperature, Т – absolute temperature, Е –activation of effective energy, R – gas constant, е – basis of natural logarithm.

Since the rate constant changes due to temperature changes, equation 4.6 at constant concentration can be represented as follows:

k=k0е-ЕRT(4.7)

It can be seen from these formulas that the number of molecules participating in the reaction and, accordingly, the rate of chemical changes are proportional to the activating factor е-ЕRT. At temperature change, the rate of a chemical reaction depends on it.

It is experimentally impossible to estimate the real activation energy of a chemical act; basically, the total energy of several elementary acts is determined.

The effective activation energy can be determined in a simple way, that is, by determining the reaction rate and measuring the rate constants at different temperatures and plotting the coordinateslgk-1Т or lgυ-1Т. In this case, the value of E can be calculated by measuring the tangent of the angle drawn by the experimental line to X-axis.

In most cases, the dependence of the rate of a chemical reaction on temperature is also estimated by the temperature coefficient γ, which shows how many times the rate increases with an increase in temperature by 100C. There is a relationship between E and γ.

Generally, the activation energy of a chemical reaction can be high or lowindependent of ∆E. In other words, knowledge of the thermodynamic characteristics of the primary and final products of the interaction does not allow to determine exactly rate of the reaction and changes depending on the temperature rise.

4.3 Catalysts

It can be seen from Figure 4.2 above that the rate of a chemical reaction can also be accelerated by reducing the activation energy. It is the effect of catalysts - substances that increase the reaction rate, but by themselves are not included in the final products. The processes that take place in the presence of a catalyst are called catalysis.

The mechanism of action of catalysts can be understood by referring to the concepts of consequitive and parallel reactions.

It has now been proven that catalysts are involved only in certain chemical acts. It was said above about the multi step of major reactions. Catalysts increase the overall rate of a chemical reaction not by increasing the rate of that stage of the reaction, which was before the addition of the catalyst, but by forming in its presence a new stage with a low activation energy and a high rate. For example, if the final product without the participation of a catalyst can be obtained according to the scheme A → b → D and the activation energy EA, then in the presence of a catalyst it is possible to obtain the activation energy EAK according to the scheme A → c → D. In this case, the reaction occurs in the second direction and at a high speedbecause EAK<EA.

Figure 4.3–Effect of the catalyst on the activation energy

Civil engineers are found the effect of catalysts when working with polymerizing agents and using solidification accelerators.

It is important that catalysts affect the kinetics of the process, but they do not affect their thermodynamics, i.e., the thermodynamic characteristics of the initial and final products. This is their main feature over other substances that accelerate the rate of a chemical reaction. For example, the introduction of electrolytes into the reaction accelerates the setting and hardening of cement, but they cannot be called catalysts for this action. Because in the process of effect, they not only increase the reaction rate, but also change the thermodynamic characteristics of the initial and final products.

The main advantages of using catalysts are in their selective effect.

If the rate of all reactions (both desirable and undesirable) increases with increasing temperature, then the rate of only the required reaction can be increasedwith the correct selection of catalysts.

Another advantage of using catalysts is that the reaction rate can be increased at relatively low temperatures, which, in turn, provides economic (by reducing heat loss) and technological efficiency.

In heterogeneous catalysis, the reaction happens on the catalyst surface, the efficiency of which is determined by the physicochemical characteristics of the catalyst surface and the supply of reactants to it. For example, in heterogeneous catalysis, it is important that the base materials are adsorbed on the catalyst.

4.4Chain reactions

Knowledge and understanding of the mechanism of chain reactions allows technologists to purposefully control such processes as polymerization, slow oxidation and combustion of organic substances, destruction of polymers. In general, it can be said that most of the homogeneous processes occur by a chain mechanism.

Chain reactions belong to a special category of reactions consisting of intermediate stages.

Free atoms of all elements, except for inert gases, have one or more unpaired free electrons in an excited state, and the molecules of substances formed by them do not have such electrons: and valences are saturatedduring a chemical reaction.

These unpaired electrons determine the chemical activity of free atoms. Free radicals (particles with unpaired electrons) are also highly chemical activity. Thus, there is a similarity between free atoms and free radicals, both of which are unsaturated in valence due to the presence of unpaired electrons and therefore react chemically.

N. Semenov made an enormous contribution to the discovery of the mechanism of chain reactions. According to his theory, chain reactions consist of three stages: emergence, development of an active center, and chain break. There are several options for the formation of a chain: under the influence of light or radioactive radiation; as a result of chemical reactions with the formation of free radicals; under the action of a catalyst, high temperatures, electric discharge, etc. For example, two hydroxyl radicals can be formed from one hydrogen molecule and one oxygen moleculeon the surface of silicaat a temperature of 5000C: Н2 + О2 = 2ОН*, under the action of light two free chlorine atom can be formed from a chlorine molecule: Cl2 + hν= 2 Cl*.

There are a lot of such examples, and the activation energy has also been determinedfor most of them. For such reactions, it is advisable to compare certain activation energies with the activation energies of reactions occurring between saturated valence molecules and ions that do not have unpaired electrons.

Such comparisons show that in the interaction of active centers or them with other molecules, the activation energies of homogeneous reactions proceeding through the formation of new free atoms and radicals are very low: most often it does not exceed 40 kJ/mol (in the case of an endothermic reaction, it is slightly higher - up to 150 kJ/mol), and when valence saturated molecules and ions interact, the activation energy is not less than 170-200 kJ/mol. This circumstance makes chain reactions energetically efficient.

In general, of the above three stages, the most energetically complex is the formation of free atoms and radicals, which contribute to the development of the chain, and after the formation of the chain, its further development proceeds easily.

In general, the formation of free atoms and radicals are most complex stage among the above-mentioned 3 stages, because it effects the chain development, however its further development goes easier after the chain formation.

There are two types of chain reactions, they are branching chain reactions and unbranching chain reactions. The first type includes reactions  where one active center interacts with a molecule of the initial substance in each cycle, forming only one new active center which is  a free radical, except for the final product.

One example is the reaction of obtainingchlorinated hydrocarbon, which is the main raw material of polymerization for civil engineers:

In this case, a free chlorine atom is obtained by light effect on chlorine molecule. The loss of one active center during an unbranching chain reaction (free chlorine atom Cl*) leads to the formation of only one active center (methyl radical CH3*). Therefore, the methyl radical leads to the formation of a free chlorine atomduring the next cycle, and this process continues until the chain is broken.

In addition, each active center gives the rise to the formation of several active centersin branching chain reactions. One example of branching chain reactions is the reaction of water formation. It has now been proven that the well-known equation 2Н2 +О2 = 2Н2О describes only the beginning and end of the process, and the mechanism of its occurrence at low pressure and temperature 5000C can be described by the following elementary acts:

Н2+О2→2ОН*

2ОН*+2Н2Н2О+2Н*

2Н*+2О22ОН*+2О*

2О*+2Н22НО*+2Н*

In this chain the first act is the stage of chain formation. As a result of the interaction of each OH* radical with a hydrogen atom,a water molecule and one active center – a hydrogen atom are formed.

But the next two acts lead to a change in the process - each of them forms two active centers at once - when a free hydrogen atom interacts with an oxygen molecule, OH* radical and O* atom with two unpaired electrons are formed, this free atom forms two more active centers: a hydroxyl radical and a hydrogen atom, and each of them contributes to the formation of a new chain in accordance with the scheme below:

Let’s consider the third stage of chain reactions - chain break. Above, during the analysis of the formation of active centers, we talked about the emergence of new active centers during the interaction of active centers with a molecule. If the process developed in this way, then the chain length, i.e., the number of cycles before the formation and breaking of the chain, would be determined only by the concentration of the initial substance.

This means that polymers of any length can be obtained by way of coaservationof certain organic free radicals with the main molecule forpolymerization reactions.

V Chemistry of binders

5.1 Classification of binders

A binder is any material or substance that holds or draws other materials together to form a cohesive whole mechanically, chemically, by adhesion or cohesion.

Binders are loosely classified as organic and inorganic. Organic binders are high molecular mass compounds that, when heated or dissolved in organic solvents, enter into a plastic state. These include bitumens, asphalts, adhesives, and various polymers.

The plastic state of inorganic binders  happens by adding a liquid medium (water, glycerin, alcohol, etc.) to them, For example:

Artificial stone

Binding paste

Binding powder

+Н2О

Binding powder interacts with water, forming new chemical compounds containing bound water. One of the conditions ensuring the activity of the binder in relation to water is its high dispersion (since the reaction is heterogeneous).

When a binder is mixed with water, a plastic mass (binder paste) is formed. The plasticity of the mass is called deformation without scratches from mechanical influences and the preservation of a given shape in the absence of external influences. All mineral binders are produced artificially by thermal (sometimes chemical) treatment of the raw material input.

The main characteristics of inorganic binders are:

– hydrophilic property (wetting);

- the ability to form easily deformable mass when mixed with water;

- the ability to become solid in the absence of external influence.

According to freezing conditions and water resistance of freezing products, inorganic binders are classified as air-setting and hydraulic.

Air-setting binders are substances that only harden in air and remain firm. These include gypsum, lime, magnesia and alkali silicate binders.

Hydraulic binders are substances that harden both in air and in water (after the initial stage of hardening and aging) and remain firm in both water and air. These include Portland cement, mixed binders based on them, alumina cement, hydraulic lime.

5.1.1 Gypsum binders

The following materials are used as raw materials for the production of gypsum binders:

– rock gypsum CaSO4 · 2Н2О;

– anhydrate CaSO4;

–phosphogypsum that are wastes from the production of phosphoric acid and the production of phosphates containing CaSO4 · 2Н2О;

–artificial gypsum material is used (contains 90% CaSO4 · 2Н2О), derived by neutralizing flue gases of thermal power plants with alkaline solutions or solid alkalis.

Let’s consider the process of gypsum binders production. Upon the application of heat to calcium sulfate dihydrate to 120-170°C (at atmospheric pressure), a dehydration reaction happens:

CaSO4· 2Н2О  → CaSO4· 0,5H2O + 1,5Н2О(120-1700С )

In this case, the β-modification is obtained –gypsum plaster CaSO4 · 0,5Н2О.

A product (calcium sulfate dihydrate) with a high free surface energy and a water interaction is produced from water resistantcalcium sulfate dihydrate.

The mechanism and kinetics of the dehydration process of calcium sulfate dihydratevaries depending on the technological conditions of its implementation. If the dehydration reaction is carried out in a closed high-pressure apparatus saturated with water vapor, water is separated from the gypsum in a liquid spray and gypsum of the α-modificationCaSO4 · 0,5Н2О (high-strength medical gypsum) is formed:

CaSO4· 2Н2О →CaSO4· 0,5H2O + 1,5Н2О (105-1200С)

The specific surface area of the β-modification particles is 2.5-5 times higher than that of the α-modification, therefore, the water demand is also higher, but the strength of the hardened product (after hydration) is lower. The compressive strength of the product CaSO4 · 0,5Н2О of the α-modification can reach 60-70 MPa.

Anhydrite binder is produced with high-temperature firing of gypsum rock (600 - 800°C):

CaSO4· 2Н2О → CaSO4 + 2Н2О(600-8000С)

This substance can also be obtained by grinding natural anhydrite and adding hardening activators.

Estrich gypsum (calcined gypsum) can be obtainedwhen firing in a reducing environment at a temperature of 900-1000°C. In this case,the main part of CaSO4 does not change, and a small part (10-20%) turns into calcium oxide (on the CaSO4 surface).

CaSO4+С→  CaO + SО2 + CO(900-10000С)

5.1.2 Air-hardening lime

For the production of air-hardening lime, boracium, limestone, dolomite (СаСО3·MgCO3) and marble production waste with a clay impurity content of no more than 6% are used. Limestone consists mainly of calcium carbonate CaCO3. Limestone firing is carried out at a temperature of 900-1200°C.

CaCO3 ↔ CaО + CO2;    ΔH = 179 кJ

During firing, the mass decreases by about 2 times, since M(CaCO3)=100g/mol, M(CaO)=56g/mol. Therefore, the fired product has a porous structure, an excess amount of energyactively interacts with water.

The slaking happens according to the following reaction:

СаО + Н2О = Са(ОН)3 + 15,5 kkal

The transition of calcium oxide to calcium hydroxide occurs through structural changes. Whereas the process is exothermic, a highly dispersed product is obtained (the volume of hydrated lime is higher than that of quicklime).

For obtaining obtain loose lime, Н2Оis required about 60-80% of the mass of lime. Lime paste in the form of a suspension contains up to 50% of Ca(OH)2 particles.

In construction, air-hardening lime is used in the form of loose lime mixed with sand and water, and lime paste added to the sand. In both cases, lime structural clay is taken.

Air-hardening structural clay:

–due to drying and crystallization of Ca(OH)2;

- hardens due to the carbonization process (under the influence of carbon dioxide).

Са(ОН)2 + СО2 = СаСО3 + Н2О

Са(ОН)2 + SiО2 = CaO·SiО2·H2О

Sand is added to reduce the shrinkage process, the cost of the mixture and improve lime hardening (facilitates the penetration of CO2 into the binder).

5.1.3 Magnesia cement

Magnesia cement are obtained by firing magnesite (in some cases, dolomite) at a temperature of 750 – 850°С:

MgCО3 = MgO+CО2

Magnesia cement is a powdered caustic magnesite. When caustic magnesite interacts with water, the hydration process carries out slowly and the hardening stone does not have high strength. Magnesia cement are generally hardened by water containing magnesium salts, such as magnesium chloride, which is believed to form 3MgO · MgCl2 · 6Н2Оneoplasms.

Since magnesia cement adhere well topyrolignite of lime upon hydration, they are widely used in the production of xylene, fibrolite.

5.1.4 Alkali-silicate binder

Alkaline silicate binders are also air-hardening binders. The composition of soluble glass can be described by the formula Me2O · nSiO2, where the N-modulus of soluble glass, often equal to Me = Na, n = 3. The solubility decreaseswith an increase in the number of modules, but the binding property increases.

Soluble glass is obtained by the interaction of silica sand and soda:

Nа2CO3 + 3SiО2 = CO2↑ + Nа2O·3SiО2

Or by interaction of silica sand with sodium sulfate:

Nа2SO4 + 3SiО2 + C = CO↑ + SO2↑+ Nа2O·3SiО2,(t = 1350-14000С)

The derived product is cooled and glass particles are removed.

In construction, soluble glass is used in liquid form. The derived silicate is ground and dissolved at a temperature of 160-170°C and a pressure of 0.6-0.7 MPa. The solution contains 50-70% of water.

If the base binder of the thin protective layer hardens in air, its hardening can be shown by the equation below:

Nа2O·3SiО2+ CO2 + 6Н2О= Nа2CO3 + 3(SiО2·2Н2О)

The gel of extractive silicic acid has binding properties.

To accelerate the solidification of liquid glass, sodium fluorosilicate Na2SiF6is added to it:

2(Nа2O·3SiО2)+ Nа2SiҒ6 + 14Н2О = 6NаҒ + 7(SiО2·2Н2О)

This process is used when working with large amount of materials.

5.2 The process of hydration hardening of binders

Hydration hardening of stucco can be described by the following reaction:

CaSO4· 0,5Н2О + 1,5Н2О → CaSO4· 2H2O

Aswas mentioned above, partially calcinated gypsum (CaSO4 · 0,5Н2О) has excess surface free energy, therefore it has a high ability to interact with various substances (for example, with water).

As a result of interaction with water, it becomes a stable hydrated newgrowths with low free energy.

Academician A. A. Baikov proposed to divide the hydration hardening of binders into three stages. Subsequently, his views on the hardening mechanism were developed by P.A.Rebinder.

Saturation period (water saturation). It lasts several minutes. At this stage, the binder mixes with water and forms a plastic mixture. Particles of β-modification CaSO4 · 0,5Н2Оbegin to dissolve in water from the surface, and its saturated solution in water is formed. At the same time, hydration begins:

CaSO4· 0,5Н2О + 1,5Н2О → CaSO4· 2H2O

Setting strength period (colloidization). Since the solubility of calcium sulfate dihydrate in water (2 g/L) is lower than the solubility of calcium sulfate dihydrate in water (8 g/L), the saturated solution associated with the hemihydrate gypsum is more saturated than the two resulting water gypsum. An excess of calcium sulfate dihydrate begins to precipitate in the form of crystals (sizes no more than 0.001 microns).These particles attract a water molecule to their surface, and some of the water molecules pass from a free state to a bound one. The system gradually begins to lose plasticity. Particles of newfrowths are connected to each other by directed water molecules in the surface of CaSO4 · 2Н2Оcrystals, as a result of which a coagulated structure is formed.The setted paste still has low strength. The colloidal period lasts several minutes.

Curing period (crystallization). Further splitting of CaSO4 · 2Н2Оleads to an increase in dehydrate crystals of calcium sulfate, and the penetration of water molecules into their composition leads to a gradual thinning of the hydration layer between them - as a result, to a violation of the colloidal state of the substance. As a result, a new spatial crystal structure, an artificial stone, and mechanical strength are formed.

Inorganic binders harden as a result of interaction with water, that is, as a result of the hydration process. The hydration hardening process is determined by the following factors:

- the solubility of dry or partially dehydrated substances should not be higher (not more than 10 g/l), but it must be higher than in hydrated newgrowths. In this regard, an excessive saturation of the solution is carried out in comparison with the products of hydration and conditions are created for the separation of hydrated newgrowths from the solution (that is, their crystallization occurs);

- the rate of dissolution of dry or partially dehydrated binders should be higher than the rate of crystallization of hydrated nwgrowths, and only in this case the solution is saturated until the end of solidification;

- the higher the saturation value, the faster the hardening process takes place.

The interaction of dry anhydride ofdry calcium sulfate CaSO4 with water happens in the following reaction:

CaSO4+ 2Н2О → CaSO4· 2H2O

To increase the solubility of anhydrite cement in water (to accelerate the setting time), calcium oxide or hydroxide (lime) is added to the composition in an amount of 5-10%. The same efficiency can be achieved by adding 0.5-1.5% soluble salts Na2SO4, NaHSO4, K2SO4to the water composition.

The composition of calcined gypsum (estrich gypsum) contains 5-15% of CaO, which increases the solubility of CaSO4.

Advantages and disadvantages of structural gypsum:

- for the production of 1 ton of gypsum, fuel and energy resources are consumed 4.5 times less than for the production of 1 ton of cement;

– high fire resistance;

- the possibility of increasing the volume during hardening;

- high air permeability of gypsum fence structures;

- early hardening, the time of the initial setting is less than 2 minutes, the end is not more than 15 minutes;

- low water resistance, this disadvantage can be increased by adding a water repellent in an amount of 4-8% by weight of the binder (absorption decreases from 30-40% to 7%);

- low strength of hardening products, this disadvantage can be increased by introducing superplasticizers and by reducing the ratio of water during hardening: gypsum (W/G).

Gypsum binders are used to obtain gypsum, gypsum concrete and gypsum board products: panels, internal walls, dry gypsum plaster mixes, plugging cements, gypsum finishing materials, gypsum-cement-pozzolanic binders, gypsum-lime-slag binders, fiber-reinforced binders. This new composite material consists of 25% of ash from the regional power station, 2% of lime, 4-6% of fiberglass and the rest of gypsum binder.

Тампонажные цементы применяют для бетонирования нефтяных и газовых скважин.Oil well cements are used for concreting oil and gas wells.

5.3 Portland cement

Portland cement is a silica cement. This binder was first patented by the English bricklayer Joseph Aspdin in 1824. Portland cement is widely used in the production of concrete and reinforced concrete products.

Portland cement production scheme:

Figure 5.1–Portland cement production scheme

Most often, an artificial mixture is used in the manufacture of Portland cement, which consists of limestone (СаСО3– 75-78 wt%) and clay (Аl2О3 · 2SiO2 · 2H2O – kaolinite, the main clay mineral - 22-25%).

Sometimes, wastes are usedinstead of clay or for its partial replacement,such as: blast-furnace slag (the remainder of the iron production), nepheline slime (the remainder of alumina production) containing 25-30% of SiO2 and 50-55% of CaO.

For the formation of the required composition of the raw mixture, property-altering additives are added: silica sand (SiO2), roasted pyrite (Fe2O3).

Marl (a mixture of limestone and clay) can be used as a raw mix. It is necessary to grind the raw mixturefor activation of the reactions during firing.

5.3.1 Cement production methods

There are two known methods of cement production: dry and wet. Rotary kilns widespread in Kazakhstan have a length of 185 m, a diameter of it is 5-7 m, its rotation frequency is 0.8-1.2 rpm, an inclined arrangement is equal to 2-5° (Figure 5.2).

Figure 5.2–Scheme of the rotary kiln

The principle of approach flow is applied. The rawmixture flows out of the upper part of the kiln, and the hot gases resulting from the combustion of the fuel (coal dust, natural gas) drain against the raw material and burn it.

The processes taking place in the kiln space can be divided into sixzones.

In the first zone, water is evolved in a free state. The kiln charge is heated to 200-250°C.

The second zoneis the dehydration zone (500-800°C). Chemically bound water is released in this area. The following chemical equation can be writtenfor one of the minerals (clay, kaolinite):

Al2O3·2SiO2· 2Н2О →Al2O3·2SiO2 + 2Н2О↑(500-8000С)

The third zone is the zone of decorbanization (900-1000°C). In this area, oxides of calcium, aluminum, silicon dioxide are formed:

CaCO3 ↔ CaО + CO2

Al2O3·2SiO2→Al2O3+ 2SiO2

In this area, the reaction between oxidants begins, but the reaction rate is still slow.

The fourth zone is the zone of solid-phase reactions (1100-1300°C). In this area, exothermic reactions of the synthesis of minerals from oxides happen:

CaО + SiO2→ CaО·SiO2

CaО + CaО·SiO2→ 2CaО·SiO2(belit)

CaО + Al2O3→ CaО· Al2O3

2CaО+ CaО· Al2O3 → 3CaО· Al2O3(tricalcium aluminate)

2CaО+Fe2O3 → CaО·Fe2O3

CaО·Fe2O3 + 3CaО· Al2O3 → 4CaО·Al2O3·Fe2O3(tetracalcium aluminoferrite)

Several parts of CaO remain free.

The rate of reactions in the solid state is influenced by defects in the structure and crystal lattices of the initial substances, the area of the contact surfaces of the interacting substances, which increases with an increase in the degree of dispersion.

As the temperature rises, the vibrational motion of the elementary particles that form the crystal lattice increases, and they acquire the diffusion capacity.

The fifth zone is the curing zone (1300-1500°C) at 1300°C, here a liquid phase is formedas a result of melting of 3СаО · Аl2О3and 4СаО · Аl2О3 · Fe2O3. As a result of complex physicochemical processes in the presence of a liquid phase, small crystals of tricalcium silicate - alite are formed:

2CaО·SiO2→ 3CaО·SiO2(alite)

In this area, the kiln charge cures in the form of particles with a size of 4 - 20 mm, which are called clinkers. Clinker is a product of the burning mechnism.

The sixth zone is the cooling zone. The clinker temperature drops to 1000°C. When removing from the kiln, it is necessary to quickly cool the clinker in special coolers so that it does not stick with large particles. A clinker that does not cool too quickly has a low reactivity due to water.

After curing for 1-2 weeks, calcium sulfate dehydrateand other mineral and organic additives are added to the clinker in an amount of 3.5-6% to regulate the setting time.

5.3.2 Composition of Portland cement clinker

A cement clinker is a system consisting of several artificial minerals formed during the firing of a raw mixture.

Table5.1– Compound composition of clinker

| Mineral name | Formula | Symbolic notation | Content in clinker, % |
| --- | --- | --- | --- |
| Tricalcium silicate - alite | 3CaO · SiO2 | C3S | 40-65 |
| Dicalcium silicate - belite | 2СаО · SiO2 | C2S | 15-40 |
| Tricalcium aluminate | 3СаО · Аl2О3 | С3А | 5-15 |
| Tetracalcium aluminoferrite - cellite | 4СаО · Аl2О3 · Fe2O3 | C4AF | 10-20 |

There may be other minerals in small quantities, for example: 8СаО · 3 Аl2О3 Fe2O3, 2CaO · Fe2O3.

The clinker chemistry  is determined by the proportion of oxides (wt%): 63-66 CaO, 21-24 SiO2, 4-8 Al2O3, 2-4 Fe2O3. Their total proportion is 95-97%. MgO, Na2O, K2O, SO3, TiO2, Cr2O3can be foundin a small amount as a mixture.

5.3.3 Specification of clinker minerals

Cement clinker, as a result of firing the raw mix, has the form of a system of several natural minerals. Comparison with granite, which is composed of certain natural minerals, can give a general idea of clinker as a polymineral system. But unlike granite, individual parts of clinker cannot be distinguished with the naked eye, since clinker consists of very fine-grained crystalline as well as amorphous phases.

The names as alite, belite come from the ancient Greek word "lithos", it means stone, and the original letters of the Latin alphabet.

It should be noted that the composition of alite is more complex than the formula indicated in the table, but for the simplicity, this difference between alite and tricalcium silicate is often ignored.

The quantitative content of minerals significantly affects the properties of cement. However, there are alumoferites and calcium alumoferites, and in small amountsin the composition of clinker. In clinker, amorphous substances are also present in the form of non-crystallized glass (1-3%)along with the crystalline phase.

The clinker also contains a small amount of magnesium oxide(no more than 5%). This is an unnecessary, but temporary mixture, since the lime sediment used in the manufacture of the raw mixture contains calcium carbonate and magnesium carbonatein small quantities. As we said earlier, there should be no free calcium oxide in the clinker, but it does occur occasionally, indicating that the clinker has not been completely burnt.

The clinker can also contain a certain amount of compounds (up to 1-2%) formed by alkali oxide of  and . These oxides penetrate into clinker from raw materials and solid fuel ash.

5.3.4 Properties of clinker minerals

Knowing the properties of individual clinker minerals and determining their amount in clinker, it is possible to describe the main features of the cement obtained from this clinker thanks to certain devices.

Tricalcium silicate () is reactive when it reacts with water. This is evidenced by the amount of heat release during hydration, especially in the first three days (Table 5.2). Tricalcium silicate is capable of rapid hardening and increasing the strength, therefore, the presence ofin the clinker should be higher, since it affects the rapid hardening progress and the increase in the strength characteristics of the cement.

Table 5.2–The amount of heat generated during the hydration of clinker minerals

| Mineral name | Amount of generated heat |  |
| --- | --- | --- |
|  | When fully hydrated, J/g/kkаl/g | During 3 days, % as the result of complete generation of heat |
| Tricalcium silicate | 120 (500) | 75-80 |
| Dicalcium silicate | 60 (250) | about 10 |
| Tricalcium aluminate | 200 (840) | not less than 10 |
| Tetracalcium aluminoferrite | 100 (420) | about 20 |

The activity of dicalcium silicate (С2Ѕ) is much slower than that of tricalcium silicate, which indicates a low thermal effect during hydration. A mineral that has hardened during the first weeks, months, has a lower strength compared to others, although after a few years the strength increases continuously when favorable conditions for hardening are created (i.e., in the presence of moisture and heat).

Thus, so-called alite cements (which contain high quantity of ) are more active than belite cements (which contain relatively high amounts of ) when they react with water.

Tricalcium aluminate () is the most rapidly hydrated clinker mineral. Its total heat is more than twofold, and 80% of heat of hydration is releasedwithin three days. hardens quickly even in the first hours after immersion of cement in water. If the cement did not contain gypsum, which retards hardening, then cement would be obtained, which would harden when mixing the concrete mixture and pouring it into the mold. Hardened has low strength.

Tetracalcium alumoferrite () takes place among the tricalcium and dicalcium silicates in terms of the amount of heat released and the rate of hardening during hydration. Its strength is lower than the strength of the hydration product , and higher than the strength of -.

The indicated brief characteristics of clinker minerals, their quantitative content in clinker indicate that they have a significant effect on the properties of cement.

Therefore, clinker with a high content of  and is used to obtain fast-hardening cement, which is necessary for the manufacture of precast concrete products, in order to reduce the time of their production. Cement with a high content of tricalcium silicate and tricalcium aluminate is also requiredfor concrete work carried out in the autumn-winter period. In a structure,concrete, insulated from heat loss due to the high hydration heat of such cement, can harden even in cold weather.However, in most cases, cement with less hydration heat will be required. For example, in solid concrete structures, in hydraulic structures. If the heat transfer of the freezing cement is high, thermal expansion of the concrete occurs. It is especially noticeable in the inner part of solid concrete, and its relative increase is less on the outer part, which is subject to natural cooling of air and water. Under the influence of volumetric deformations, temperature fluctuations, cracks are formed in concrete, which, in turn, can lead to emergency destruction of the structure.

Magnesium oxide can be mixed only in limited quantities, since the interaction of cement and water increases the volume of slowly formed magnesium hydroxide compared to the original magnesium oxide. This creates internal pressure in the material used and in some cases can lead to cracking.

It was found that silica in the form of opal, i.e., amorphous aqueous silicon dioxide (), which previously did not attach importance to potassium and sodium oxides contained in clinker in various chemical compounds, but characterized by a high reactivity to basic oxides in stone concrete aggregates, causes destruction of concrete due to interaction with alkalis in cement. In this regard, when testing aggregates for concrete, in a number of cases, it is imperative to check for the presence of amorphous, highly active silica.

The above examples show that in order to select the cement required for use in a particular area, it is necessary to know the mineralogical and chemical composition of clinker.

5.3.5 Interaction of clinker minerals with water

Minerals in cement clinker react with water and generate hydrated compounds. Clinker minerals are poorly soluble in water, and their hydrated products, except for calcium hydroxide, are practically insoluble.

Hydrated compounds obtained under influence of water on clinker minerals are generated as a result of their hydrolysis and hydration.

In clinker, in terms of quantity, lime silicates prevail, formed by a strong base and a weak acid salt, capable of hydrolysis decomposition, enriching the aqueous solution with hydroxide ions.

As any chemical exchange between ions, hydrolysis is a reversible process, the equilibrium of which depends on all factors affecting the equilibrium state of the reactions of general ion exchange. With an increase in temperature, which occurs during warm-wet processing of a product, the degree of hydrolysis also increases.

The hydration reaction consists in the interaction of clinker minerals with a water molecule and the formation of hydrated complex compounds. It should be noted that the composite complexes obtained for hydration, in most cases, have a variable composition. Therefore, the water formed by the clinker minerals listed below in the formulas of the compounds is conditional.

When exposed to water on tricalcium silicate, the product of its hydrolysis is hydrated. Then the complex is rearranged in the hydrated complex compounds in the solution, as a result of which tetracalcium calcium silicate hydrate is hardly released from the solution.

The equation describes that lime hydrate in free state is also generated together with calcium hydrosilicate tetrahydrate.

The content of calcium oxide in dicalcium silicate is less than in tricalcium silicate, i.e., it is lower in comparison with it, therefore, the hydrolysis of dicalcium silicate practically largely depends on the external conditions of hydration, for example, the concentration of calcium hydroxide in solution. Under normal temperature conditions for the preparation of concretes and mortars, dicalcium silicate practically does not form a hydrolysis product, but only hydrates:

But while avtoclave treatment of sand-cement products, dicalcium silicate is hydrolyzed with the release of free calcium hydroxide. The latter reacts with the silica contained in the sand to generate calcium hydrosilicate.

As for tricalcium aluminate, its hydration can be described by the following equation:

Tricalcium aluminate reacts with water in different ways where gypsum is present. Let's discuss this issue in detail as it is important for the following reasons. Firstly, gypsum dihydrate is always present in cement in small amounts as an additive introduced to control the setting time of cement when grinding clinker. Secondly, if an aqueous solution of calcium sulphate gets into concrete with hardening water, sulphate corrosion of concrete can occur (see below «Corrosion of Portland cement stone»).

Due to the high reactivity of tricalcium aluminate, bound with water, due to the very rapid freezing of cement without a gypsum mixture, the resulting six-calcium aluminate contributes to the formation of an excessively early structure in the cement paste. This complicates the mixing, placing and compacting the concrete mixture, and sometimes does not allow to operate.

The reaction is slowed down by the introduction of gypsum:

It can be seen from this equation that as a result of the reaction of gypsum with tricalcium aluminate, calcium hydrosulfoaluminate is released from the crystallization of ettringite containing 31-32 water molecules. This compound is poorly soluble. Thus, at the first stage, the calcium hydroaluminateis in contact with hydrated cacium aluminate after mixing the cement with water. Only after a few hours, that is, after the complete consumption of all the gypsum in the solution, calcium hydroaluminate is formed and the cement begins to set.

That is, the gypsum mixture serves as a "barrier", preventing a certain amount of tricalcium aluminate from reacting with water in the freshly mixed concrete at the initial stage.

As shown above, the second reason for our consideration of the interaction of tricalcium aluminate in an aqueous medium, where gypsum is present, is the ability of the cement stone to rust.

During the generation,calcium hydrosulfoaluminate with the addition of a large amount of water takes up more space than the initial reagents and water. If a solid hydrated complex salt (ettringite) is generated in the middle of the cement paste, which still retains its plasticity, the increase in volume will not have bad consequences. But an increase in volume is dangerous if the formation of this salt occurs in cement, cured under the action of sulfate ions in aggressive media, i.e., therefore, during sulfate corrosion of concrete, strong internal pressures arise, leading to the formation of cracks in the concreteand loss of strength.

Let us now consider the reaction of tetra-calcium alumoferrite with water. This clinker mineral, reacting with water, degenerates to form six-calcium aluminate and calcium hydroferrite.

4СаО·Al2O3·Fе2О3+ 10Н2О + 2Са(ОН)2=

3СаО·Al2O3·6Н2О + 3СаО·Fе2О3·6Н2О

5.4 The theory of the hardening of binders

In 1882, Le Chatelier proposed a crystalline hardening theory, in which the more soluble anhydrous minerals of Portland cement clinker, which are more soluble than hydration products, form saturated and supersaturated solutions of hydrated phases. Crystallized phases are separated in the form of crystalline hydrates of various compositions, in which crystals increases gradually. When the dissolved anhydrous crystals are hydrated, their concentration in the solution gradually decreases, and a new portion of the anhydrous substance enters the solution.Crystalline hydrates of new growths are used either for the growth of initial crystals, or for the formation of new growths of this phase. They joint to each other, as a result, of crystal growth, and generate the frame structure of the cement stone. This theory can correctly explain the hardening of some binders, such as gypsum, but cannot explain the mechanism for the strength development of the cement paste.

It’s about saturated and supersaturated new growths in solution (the presence of an exceptional concentration of a substance in a solution (exceeding its solubility), that is, supersaturated (SS)SS=S-S0, here S0 is solubility, and S is the concentration of a soluble substance at a given temperature Investigation of the refractive indices of supersaturated solutions showed that at a high degree of saturation close to the critical point, and the optical properties of the solution under study change rapidly.In the given conditions, this reflects the formation of independently generated new growths of phase. In this case, the solution is in an unstable, metastable state. The separation of the solid phase from it does not occur spontaneously, but only with the introduction of seeds in the form of very small crystals. The transition from a stable state to a metastable one can be carried out by cooling or evaporating the solution, as well as introducing an additional amount of a dissolved solids into it. Supersaturated solutions are unstable. If the supersaturation exceeds a certain limit, a spontaneous crystallization process begins. It begins with an increase in the probability of associative reaction between dissolved particles and the formation of small quasicrystals near colloids. At first, such quasicrystals have low stability, they sometimes degenerate, or are formed at another point in the solution under the action of thermal convection. At a certain degree of supersaturation, such quasicrystals grow to a certain limiting size and serve as the beginning of crystallization.

The dependence of the degree of supersaturation on the initiation criterion of in the equilibrium state is determined by the Thomson formula:

lnCC0=σμρrRT                                          (5.1)

here σ is the specific surface energy at the phase boundary; ρ is the density of the crystallizing substance; C0is solubility of large crystals; C is the solubility of crystals of r value; μ is the molar mass.

It can be seen from this equation that the lower the value of the constant initiation, the higher the saturation of the solution. With the emergence and growth of initiation between the new and the old phases, a phase boundary forms, on which energy is spent.

Currently, opinions about the nature of the emergence of intiations is different. Apparently, they are formed as a result of combining crystal blocks of different sizes under the influence of Brownian motion, forces of contact with each other. The collision and coaservation of at least two large blocks can lead to the formation of a larger particle than the original initiators.

Crystalline initiators can also appear in another way. Initially, a gel-like globule is formed with a size of no less than a critical one, and subsequently its structure can be corrected in the same way as in a crystal.

The formation of new phase initiators can be controlled by changing the temperature, adding various additives, and physical impact.

The peculiarities of the formation of a solid phase from the above supersaturated solutions must be taken into account when considering the mechanism of hardening of mineral binders.

In 1893, the Swedish scientist Michaelis developed and proposed a unique colloidal theory from Le Chatelier's theory. Michaelis paid special attention to colloidal-chemical phenomena during hardening of hydrogels and binders formed during hydration. He considered the formation of crystalline hydrates auxiliary and noted that it can have a negative effect on some features of the cement stone.

According to Michaelis, the formation of strength, water resistance and other important properties of a multicomponent system of hardening cement depends on the presence of hydrogels of silicates, alumoferrites and aluminoferrites of calcium. In the structure of hydrogels, strength is formed due to the involvement of most of the original solid particles in the hydration reaction and the formation of coagulation sealing new growths. Michelis explains the drying of gels by the fact that when the gels are compressed, water is sucked out through the capillaries. The released water reacts with non-interacting particles, which affects the further compaction of the system.

During 1925-1927,Russian scientist A.A.Baikov proposed a theory on the hardening of binders by a combination of crystallization and colloidal processes. In his understanding, the hardening of binders consists of certain periods and stages. As far as is known the hardening of binders has two periods - setting and real hardening. Setting occurs due to condensation and loss of plasticity of the system. Over time, the binder paste becomes stiff and turns into a solid that does not yet have the necessary strength. This indicates the end of the setting and the beginning of the hardening process. These stages begin with the fact that the mineral binder does not dissolve in water and chemicallyreact with it. This is the main feature of the theories of Baikov and Le Chatelier.According to Baikov, despite the fact that the final product of the hydration process will be a crystalline body, it will be a colloidal stage in the process of hydration and hardening of binders. Baikov identified three stages in the process of hardening binders.

The first stage (saturation) begins from the reaction of the binder with water, when the minerals and the generated hydrates dissolve to a saturated state. Hydrated new growth in such solutions, being in a colloidal-dispersed state in the form of a gel, do not dissolve further. When solubility of the gel is very low, repeated recrystallization can happen from an aqueous solution in contact with it.

The second stage (colloidization) consists in the generation of a colloidal-dispersed structure. As noted above, a saturated solution in relation to colloidal particles is more saturated in relation to large crystals. It should be borne in mind that the gel is polydisperse, that is, it consists of globules of different sizes and is more saturated in relation to large particles.As a result, small particles become solution and large particles are generated from them. Polymineral binders such as Portland cement can contain gels of varying solubility, so cement stone can be composed of crystals bonded to each other and a gel phase. Crystals consist of Ca(OH)2 free limestone, and the gel is in the form of calcium hydrosilicates.During this period, thetemperature of the paste rises, since the hydration of minerals happens when water reacts with the surface of the crystal. The generated heat raises the temperature of the paste, as a result of which the reaction rate increases, and a gel film forms on the surface of the crystals. During this period, the binder loses its plasticity, setting begins and a coagulation structure is formed, which does not yet have mechanical strength.Calcium hydrosilicates are released as a constant mass. Calcium hydroxide formed during the hydrolysis of C3S dissolves in water and forms a saturated solution. First, undercomposed tricalcium silicate and other components of Portland cement clinker react with water. New portions of Ca(OH)2 cannot become solution, since they are in a saturated state. The colloidal phase formed by hydrosilicates and calcium hydroxide determines the setting and hardening of cement and concrete.Gel-like products formed during the setting and hardening of clinker minerals become stable and are not able to greatly change their volume upon drying, that is, to lose the dispersed medium. At this point, although the gel has a porous structure, the lattice does not change. At second wetting, water is absorbed and fills its pores without changing the volume of the gel.The dried gel has a porosity and a high specific surface, which makes easier the diffusion of gases and solution in its pores. Over time, gels age, become denser by separating the dispersed medium and change their structure, decreasing in volume. This process is called syneresis. An increase in temperature accelerates the aging of colloidal systems.Mechanical effects – transformation of a sol or colloidal solution into a gel while stirring, shaking is called thixotropy. It is used to impart a binder to partially hardened cement paste by mixing or shaking. After the termination of mechanical effect, the colloidal solution again forms a coagulation structure.

Gels have a cellular structure, as a result of which they are able to retain a large amount of a dispersed medium, while maintaining the properties of a solid. The formation of such a structure occurs due to the presence of asymmetric hydrated colloidal particles, molecules and ions in the gel. During the formation of a gel, the particles bind to each other, forming internal cavities or cells filled with a dispersed medium or colloidal solution. When dry, these cells remain intact and form pores.

The third stage of hardening of binders is followed by recrystallization of gel-like hardening products and the formation of crystalline compounds in the form of accretions, which contribute to an increase in the strength of the system. At this time, heat generation decreases. A condensation structure of the cement stone is formed. Its strength depends not only on the chemical and mineralogical composition and density of the binder, but also on the conditions for the development of its internal stresses, the formation of compounds in polycrystalline material, determined by the kinetics of crystallization of new formations.

Such scientists as Yu.But, V.Timashev, P.Rebinder, O.Mchedlov-Petrosyan, D. Jeffrey, J. Bernal made contribution in formation of modern theory of binders hardening. Although the division of the hardening process into several stages is conditional, it helps to reveal the essence of the phenomena taking place. And in real conditions, the processes of dissolution, crystallization, gelation proceed in parallel, and the hardening process can take years. So, the setting of Portland cement occurs within 10-15 hours, and the process of compressive strength generation according to the brand takes about a month.

Figure 5.3–Hardening of Portland cement crystals

5.5 Impurity Portland cement

Additives help to regulate the basic properties of binders and have become widely used in recent years. Their diversity and insufficient knowledge of the mechanism of action make it difficult to correctly apply this simple and cost-effective approach to improve the quality of binders.

Let’s consider the chemical effect of the additives used on the constituent elements of the cement. According to V. Ratinov, additives can be classified into four groups:

- additives that change the solubility of the binder and do not react with it;

- additives that generate sparingly soluble or slightly dissociating compounds with the binder;

- additives that are centers of crystallization;

- additives adsorbed on binder particles.

The additives of the first group include additives that do not contain the same ions with the binding agent. Such additives bounded with alite and belite include sodium salt, potassium sulfate and chloride, sodium nitrate and other salts. These additives do not hydrolyze and do not change the alkalinity of the medium, although they accelerate their strengthening by increasing the solubility of calcium silicate. Secondly, this group includes compounds containing same ions with binding ones, for example, СаСl2, Ca(NO3)2. It reduces the solubility of the binder when exposed to small amounts of compounds of gypsum, alit, belit and increases the rate of crystallization of hardening products.

Additives of the second group can be divided into several subgroups: additives that reduce the alkalinity of the medium; chemically reacting into the exchange of Ca(OH)2 and forming poorly soluble products; reacting compounds to form hydrated double salts. These include salts formed with a strong base and a weak acidic residue, for example, iron (III) sulfate and ferric chloride, aluminum sulfate, which accelerate the hardening of concrete and reduce its permeability.At the same time, this group includes potash К2СО3 (orNa2CO3)sodium aluminate and sodium fluoride, which chemically react into exchange of Ca(OH)2 and form poorly soluble products. These additives increase the alkalinity of the cement mortar. Their introduction accelerates the hardening of the cement. When using mixtures of this group, it is necessary to apply various measures to protect steel reinforcement against corrosion (decrease in pH) and active silica aggregate (increase in degree of acidity or alkalinity). Practically, potash and sodium aluminate are widely used as a sealing mixture to reduce the freezing point of water during concrete work in the cold season.

Additives of the third group include additives in which the components of the cement clinker form poorly soluble complex salts such as С3А and C4AF- hydrates. This group includes СаСl2, CaSO4, Ca(NO3)2. It should be borne in mind that these salts can also be classified into the first group in terms of the effect on the silicate phases of Portland cement. The reaction of C3A with calcium chloride can be described by the following equation:

3CaО· Al2O3 +CaCl2+ 10H2O→ 3CaО·Al2O3·CaCl2·10H2O

calcium hydrochloride aluminate

Similar ferriferous clinker minerals with sodium, potassium and calcium sulfates generate hydrosulfoaluminoferrite calcium:

3CaО·Al2O3(Fe2O3)·CaSO4·31H2O

These complex salts, which are dissociated into simple ions on dissolving, have a low stability constant. They can be considered as salts close to double salts. The reaction of aluminoferrite with other additives happens in a similar way.

When the simultaneous presence of additives in the cement, there is a «struggle» between them for reaction with С3А and С4АF. Since calcium hydrosulfoaluminate with a high crystallization rate and low solubility salts with a similar composition are formed with these minerals, the action of calcium sulfate is optimal. Other additives, which are added during hardening, remain unchanged in the liquid phase of the cement paste and act as additives of the first group. Over time, these additives (СаСl2, Ca(NO3)2and others) react with cement minerals like calcium sulfate.

Alkali metal carbonates (soda, potash) Ca(OH)2 form the CaCO3 salt, which is poorly soluble in water. Under the influence of these additives, the hardening and compaction of the cement stone is accelerated, the filtration of liquids and gases through concrete and diffusion processes decreases. These additives also include alkali metal fluorides that form CaF2, poorly soluble in water and some other solvents.

The third group of additives includes salts that form crystallization centers. The additives of this group include powdered gypsum CaSO4· 2Н2О, which is an effective accelerator used to accelerate processes.

When it is necessary to impart acid-and heat-resistant properties to concrete, for example, in the production of autoclave silicate binders, calcium hydrosilicates are widely used. These additives are introduced empirically, in the amount of 3-5% by weight of the cement.

Additives of the fourth group mainly slow down the hardening of concrete, the main purpose of their use is to give the cement paste plastic, hydrophobic properties. This effect is due to the surfactant action of the additives in relation to the binder. These include sulfite-cellulose liquor (containing calcium lignosulfonates), sodium abietate, high molecular weight fatty acids and their salts with alkali metals. These compounds contain polar functional groups SO3H, –СООН, –СООМе and non-polar radicals.Polar groups form a thin film that reduces friction between particles, focusing on the hydrophilic surface of the binder. At the same time, the content of cement decreases, its plasticity increases, as a result of which the strength, durability and frost resistance of buildings increase. Such surfactants are added in an amount of 0.15 - 0.25% by weight of the cement to ease the grinding process. The adsorption of molecules of organic compounds by binding particles hinders the diffusion of water from the new-forming layer, reduces the rate of setting and hardening.

The search and development of new additives, the study of their influence on the construction and technological properties of concretes allow to create new binders with the required properties. Such substances, called plasticized, hydrophobic, expanding Portland cements, are widely used in the construction of monolithic buildings, in the manufacture of precast concrete and reinforced concrete structures. Their use is especially effective in regions with a variable level (repetition of freeze and thaw cycles, wetting and drying cycles), as well as in road construction.

VI CORROSION OF CONSTRUCTION MATERIALS

Any construction materials or structures are in constant touch with the environment during operation, that is, the materials used in the construction of this building react with the components of the external environment. If such reaction decreases the strength of a building structure or reduces the service life, then environmental factors are called aggressive, depending on the material used.

The interaction of material and environmental factors depends on physical conditions: temperature, phase composition of an aggressive medium, contact conditions, pressure of a liquid or gaseous medium, and other factors. Chemical or physicochemical phenomena leading to the destruction of the material are called the corrosion process.

The main building and structural materials have the ability to chemically react with the components of the gaseous medium, water and substances dissolved in water. From a chemical point of view, these can be neutralization or exchange reactions. The direction of the corrosion process depends on the properties of the reactants and reaction products. Ifwater-soluble products are formed as a result of corrosion reactions, then the intensity of the process increases. Ifa substance insoluble in water is formed as a result of the reaction, then the rate of the corrosion process and its negative effect on the material decrease.

The corrosion-resistance of various building materials depends primarily on their chemical composition and reactivity.

V.Moskvin classifies the corrosion process in concrete into three main types:

Corrosion process happens due to the dissolution of the  cement components in water, especially calcium hydroxide Ca(OH)2. The rate of a heterogeneous reaction occurring at the interface between a common solid phase and a liquid phase depends on the rate of diffusion of aggressive components in the cement stone or against the aggressive component Ca(OH)2. Under general normal conditions, the solubility of Ca(OH)2 in water is 1.3 g/l (per CaO).

First, Ca(OH)2 begins to dissolve in waterin the outer concrete, and then hydrosilicates and calcium hydroaluminates are gradually hydrolyzed. Thus, a film of corrosion products forms on the concrete surface. If this film is stable, then due to the diffusion resistance of corrosion products, the rate of the corrosion process decreases sharply. And if the corrosion products are washed off the concrete surface, then due to the diffusion rate of Ca(OH)2, the corrosion process begins to develop even more intensively.Studies have shown that if the content of Ca(OH)2 in Portland cement decreases by 20% of its initial amount, then hydrolysis of calcium hydrosilicate begins, which forms the basis of the strength of the cement stone. Destruction is especially intense in the most stressed areas of the cement stone. In practice, the first type of corrosion occurs when concrete is exposed to soft waters.

2. Corrosion process happenswith the formation of water-soluble products between the cement componentsand the environment. In general, the cement stone has an alkaline environment, therefore, the aggressive effect of the products formed as a result of the reaction of acids and Ca(OH)2 in the cement composition on them is also different. If poorly soluble salts are formed, then they are deposited on the pores of the cement stone and prevent the corrosion process, and if highly soluble salts are formed, then the process begins to proceed intensively.

а) Н2SiF6+3Ca(OH)2→3CaF2↓+SiO2↓+H2O

CaF2 and SiO2 gels formed as a result of the reaction are poorly soluble, therefore, the action of these acids reduces the corrosion rate:

b) 2HCl + Ca(OH)2→ CaCl2 + H2O

c) СH3COOH + Ca(OH)2→ (CHCOO)2Ca + 2H2O

as a result of the reaction of these two acids of Ca(OH)2, a very soluble substance in water is formed, therefore these acids are very aggressive for concrete.

d) Carbon dioxide is the most widespread in nature, which reacts on concrete in all buildings, both in water and in air. If its size is smaller, then

Са(ОН)2 + СО2 → СаСО3↓ + Н2О

but if the amount of CO2 increases, then the reaction will be  as follows:

СаСО3 + СО2 + Н2О ↔ Са(НСО3)2

Here in a system consisting of СаСО3; СО2; Са(ОН)2, an unstable equilibrium is formed and it will depend on the concentration of CO2.

Moreover, natural waters contain a solution of various salts. Some of them are not corrosive to concrete, and some are very corrosive. Salts of the first group include, for example, NaCl solution.

NaCl + Ca(OH)2↓ ↔ NaOH + CaCl2

that is, such salts do not actively react with the cement component.

Waters containing sulfuric acid saltsare especially dangerous for concrete. As a result of such aggressive action, concrete swells and cracks appear on the structure.

3СаО∙Al2O3 + 3CaSO4 + 31H2O = 3CaO∙Al2O3∙3CaSO4 ∙31H2O

As a result of the formation of calcium hydrosulfoaluminate, the volume of the solid phase increases 2.6 times and cracks appear on the concrete, then it collapses. Sulfate resistance of cement depends on the content of tricalcium aluminate in it. The content of tricalcium aluminate in such cements should not exceed 5%.

3.The third type of corrosion happens as a result of the aggressive action of salts accumulating in the pores, capillaries and cracks of concrete.

а) carbonization

Са(ОН)2 + СО2 → СаСО3↓ + Н2О

b) оcratation

Са(ОН)2 + SiF4 → 2CaF2↓ + SiO2↓ +        4H2O

c) fluatation

Н2SiF6 + 3Ca(OH)2 → 3CaF2↓ + SiO2 + 4H2O

6.1 Corrosion of cement and concrete, and methods of their prevention

Concrete, an artificial stone-like mass, is the composite material that is created by mixing binding material (cement or lime) along with the aggregate (sand, gravel, stone, brick chips, etc.), water, admixtures, etc in specific proportions.

Environmental factors cause the gradual destruction of cement stone and concrete. Under the influence of corrosive destruction, the service life of concrete and reinforced concrete structures is reduced. Portland cement-based concretes are of particular importance in modern construction.

Portland cement clinker consists of the following components:Са(ОН)2, alite 3СаО ∙ SiO2 (C3S), belite 2CaO ∙ SiO2(С2S), tricalcium aluminate 3СаО ∙ Al2O3(C3A) and tetracalcium alumoferrite 4СаО ∙ Al2O3∙ Fe2O3 (C4AlF).

6.1.1 Physical corrosion of concrete

When water (soft water)reacts on concrete, Ca(OH)2 is washed off from the concrete. As a result of a decrease in its concentration, the state of stability of highly basic hydroaluminates and gyrosilicates is disturbed. Other components of the cement stone begin to deterioratewith a decrease in its concentration by 1.1 g/l. For example,

The gradual transition of Ca(OH)2 into the external environment leads to irreversible processes leading to a decrease in the strength of concrete.

The strength of cement stone is reduced to 15-30%by decreasing the content of Ca(OH)2to 40-50% and this process is intensified when the cement stone is exposed to soft water or water under high pressure.

6.1.2Chemical corrosion of concrete

Carbon dioxide corrosion. An excess of carbon dioxide (excess of CO2 content in water over the equilibrium state) leads to the dissolution of calcium corbanate on the concrete surface:

Са(ОН)2 + СО2 → СаСО3↓ + Н2О

СаСО3 + СО2 + Н2О ↔ Са(НСО3)2

As a result of its gradual washing out of concrete, the porosity and permeability of the concrete increases.

Magnesia corrosion.Magnesium salts (MgSO4, MgCl2) are found in sea and ground waters. When such waters expose on concrete, the following reactions happen:

Mg(OH)2 - (large bulk weight) precipitates in the form of a water-permeable shell, CaCl2, in seawater CaSO4 · 2H2O,are also washed off with water.

Magnesium salts can react with the cement components:

As a result, the cement stone turns into a loose mass.

Sulfate corrosion.Sulfate corrosion happens when water containing calcium, magnesium, sodium and other sulfates expose on concrete:

3CaO · Al2O3 · 6H2O + 3CaSO4 + (25-26)H2O =

= 3CaO · Al2O3 · 3CaSO4 (31-32)H2O

Ettringite

If sodium sulfate is present in water, then it reacts primarily with Ca(OH)2:

As a result of the reaction of calcium with the sulfate ion,the equilibrium in the reaction shifts to the left (see sulfate corrosion).

Acid corrosion.It occurs under the influence of acids present in wastewater and groundwater of industrial enterprises:

Other components of the cement stone can also be destroyed by the acids effect.

All methods of protecting concrete from corrosion can be classified into the following groups:

– adequate cement;

– high density concrete mix design;

– use of protective concrete layers;

– control of corrosive medium (for example, neutralizing of acid water contacting with concrete).

6.1.3 Methods of protecting concrete from corrosion

Several protective measures are carried outfor preventing the harmful effects of corrosion,the main of which are:

1. The content of C3S and C3Adecreasesin Portland cement clinker. During the hydrolysis of C3S, Са(ОН)2is formed, which reacts with various components contained in water in large quantities. C2SH2transforms into a low-basic hydrosilicate CSH(B) and passes into a solution of Ca(OH)2.Calcium aluminate C3Ahydrates and recrystallizes to С3АН6and other products. In this case, the presence of sulfate ions in water leads to the generation of ethiringite (cement bacillus), which leads to the formation of internal pressure in concrete and cracks in cement stone. An example would be the corrosion that occurs when gypsum plaster is applied to concrete substrates.When watering, gypsum passes into the concrete in the form of a solution and generates gypsum-trisulfate –ettringite. At the same time, when assessing their influence on the properties of concrete, it is necessary to take into account the exchange reactions leading to the crystallization of hydrochloaluminates, calcium hydrocarboaluminates and other double salts.

2. When grinding cement, gypsum is added to cement composition in such an amount that during the first 1-2 days it is completely contacted with ettringite.

3. Puzzolanic (active SiO2) mixtures are added to the composition of Portland cement in an amount of 20% by weight of cement in order to reduce the growth of Ca(OH)2 crystals by transferring them into low-basic hydrosilicates with low solubility of CSH by reacting with SiO2 and compacting the solid phase.

4. When choosing a concrete composition, the required ratio of cement, coarse and fine aggregatesare selected, the W/C ratio is reduced by the introduction of the necessary additives, and the mobility of the concrete mixture and the density of concrete are increased.

5. In products used in precast reinforced concrete structures, heat treatment is used, which makes it possible to form a dense crystalline structure and accelerate the hardening process; the surface of the products is covered with a thin film of cement, the surface of the concrete is covered with various waterproofing materials. If the integrity of the waterproofing layer is damaged, corrosion can also occur under this layer.

6. The stability of concrete can also be increased by carrying out the process of natural or artificial carbonization and treatment with electrolyte solutions such as H2[SiF6] – silicon hydrofluoric acid, Н2С2О4–ethane acid, Са(Н2РО4)2–monocalcium phosphate. Practically, fluorination of cement is widely used, i.e., treatment with a solution of silicon hydrofluoric acidwith the generation of poorly soluble products together with calcium compounds:

In construction, concrete protection from corrosion are carried out by choosing methods of protection from corrosion in accordance with the results of studies aimed at determining the degree and type of aggressive environmental impact on concrete. Most often in construction practice, we are faced with special reagents that destroy steel structures. For example, these are organic acids and their vapors - oils, glycerin, fatty acids, mineral fertilizers, special compounds used in medicine, pharmaceuticals, food industry, agriculture, as well as waste products from these industries.

The first place should be given to the methods of choosing cements and their additivesof the above methods for protecting concrete, excluding or allowing to reduce the aggressive effect of the environment.

For example, plastic mix is used to protect from acid corrosion, as well as products based on acid-resistant and aluminous cements. Sulfate-resistant cements with С3А content of not more than 5% by weight are used for sulfate corrosion control. This prevents the accumulation of calcium hydrosulfoaluminate in the pores of the concrete.

When waterexposes with a low content of dissolved mineral salts, it is necessary to use puzzolanic cements containing silica additives. Such mixtures include tripolite, diataomite, etc. It is recommended to use blast-furnace cement containing slags in the form of blast furnace and phosphoric slags, belite sludge or waste in the form of ash, dust and slags formed during fuel combustion at regional power station, thermal power station.Such slags do not bind free lime well in comparison with puzzolan. The content of Са(ОН)2in the composition of the hardened cement stone based on these additives is much less than in cement stone based on a simple Portland cement base, as a result of which the stability of concrete based on hydraulic additives increases.Waste products in the form of smoke and other gaseous products containing acid oxides (SO2, NO2, СО2), as well as water vapor at high temperatures (above 200°C) also have a negative effect on concrete. This can damage both the cement frame and the aggregates. To work in such aggressive environments, special concrete compositions are used as a coarse aggregates, in which strong corbanate rocks are precipitated.

6.2 Metal corrosion

Metal corrosion, which differs from the corrosion of building materials, is characterized by a redox reactionin all cases. Civil engineers are mainly faced with electrochemical corrosion of metals. Electrochemical corrosion is characterized by the following main features

- the reaction of a metal with an aggressive medium consists of two independently occurring processes: anodic (metal dissolution) and cathodic (oxidation of atoms or ions of the external environment).

- most often, anodic and cathodic processes occur in different areas of the metal surface.

During metal corrosion, as in chemical cells, only hydrated positively charged ions pass into the solution, and an excess of electrons accumulates on the outer surface of the metal.

-    -

-    -

-    -

-    -

-    -

-    -

-    -

Fe + nH2O     -2е-        Fe2+∙ nH2O	+	+

+              +

Fe + nH2O     -3e-Fe3+∙nH2O+             +

+             +

Therefore, when positively charged ions passes into the liquid phase, an electrode potential arises at the metal-solution interface. During the transition of ions into the solution, the negative potential of the metal and the kick of potential at the interface increase. But the accumulation of metal ions slows down further dissolution. At a certain value of the potential, a mobile equilibrium is generated:

Fe ↔ Fe+2 ∙ nH2O

The transition of many metals to the ionic state is a thermodynamically efficient process and leads to a decrease in the free energy of the system.

The value of the total standard electrode potential is a relative value. The electrode potential of hydrogen is takenfor the value of the standard electrode potential equal to 0.

Table6.1–Standard electrode potentialof some metals

Zn                     Cu                                  В0Zn / Zn+ = -0,76

В0Cu / Cu+ = +0,52

CuSО4ep

ZnSО4  ep

anode                                       cathode

Zn → Zn+2 + 2e         Cu+2 + 2e → Cu0

In such a chemical cell, the active (with low potential) metal is oxigenized by its electron loss, and metal ions with low activity (with high potential) are reduced. In this case, electrons move through the conductor, and ions move through the solution.

In metal structures, consisting of a very complex composition of microcathodes and microanodes, the corrosion process carries somewhat differently. The main factors causing electrochemical corrosion in such structures are: impurities in the structure, heterogeneity of the structure, porosity of the metallic and non-metallic protective layer, internal tension, and point damage on the metal surface.

In this case, damaged or somewhat tensed areas of the metal surface turn into an anode, i.e., they begin to dissolve according to the above scheme, and atoms or ions with a positive charge are oxidizedin areas with low activity. As a result, the concentration of hydrogen ions decreases due to the occurrence of one of the following processes in the zones close to the cathode.

2Н+ + 2е → Н2 (in acid zone)

О2 + Н2О + 4е → 4ОН- (in neutral zone)

Consequently, the cathodic process neutralizes acids and facilitates the formation of OH-ions. As a result of the reaction of metals dissolved in the anode with the products of the cathodic process, poorly soluble substances (M:Fe(OH)2 and Fe(OH)3) are formed, which can form a layer that protects the metal from corrosion. Consequently, in addition to the primary reactions happening in the cathode and anode, the corrosion process is also influenced by secondary reactions that form poorly soluble substances.

In construction practice, corrosion of metal piles installed between soils or in water is common. Due to the uneven supply of oxygen and electrolytes to the metal surface in different zones of the pile, due to the lack of oxygen in the zones of the pile in the soil, the metal zones act as an anode, and the rest of the metal zones act as a cathode.

R

Fe – 2e → Fe2+

Reinforcement in general reinforced concrete products can be protected by creating a protective layer of metal on its surface. The metal protective layer can be cathodic or anodic.

А.Metals with a lower negative electrical value (with higher potential) than iron are used as the cathodic protective layer. If such a protective layer is damaged in a certain area, the intensity of localized corrosion will increase. A potential difference arises between iron and copper, the surface of which is exposed in the damaged zone, and iron begins to play the role of an anode, and a protective layer plays the role of cathode.

В.Compared to this, the protective layers of the anode metal (zinc, aluminum) better protect the base metal. In this case, the steel begins to act as a cathode and retains its stability until the outer protective layer dissolves. This principle is most applicable in cathodic protection.

anode, electrode

basicmetal – cathode

Analogical cathodic protection is used as well.

- flow of direct current

- metal

Recently, aluminum and its casting have been widely used in construction.

As shown above, aluminum is a corrosive metal due to its standard electrode fluidity (-1.67). But under normal conditions, aluminum and its casting are resistant to corrosion, since on its outer layer there is an anode layer that is poorly soluble and resistant to the effects of the atmosphere and fresh water. But this stability (aluminum and zinc) changes rapidly in acidic and alkaline environments.

а) acid medium

2Al + 6HCl → 2AlCl3 + 3H2↑           Zn + HCl → ZnCl2 + H2

Al2O3 + 6HCl → 2AlCl3 + 3H2О       ZnO + 2HCl → ZnCl2 + H2O

б) alkaline medium

2Al + NaOH → 2Na3AlO3 + 3H2↑             Zn + 2NaOH → Na2ZnO2 + H2

Al2O3 + 6NaOH → 2Na3AlO3 + 3H2О    ZnO + 2NaOH → Na2ZnO2 + H2O

Aluminumincontactwithplainconcretecancorrode.

2Al + 3Сa(OH)2 + 6 H2O → Сa3(AlO3)2 ∙ 6H2О + 3Н2

But this process stops over time, since the generated six aqueous calcium hydroaluminates are insoluble in water.

The main corrosion prevention methods ofmetal structures are:

- normally, if there is a sufficient protective layer of concrete (10-15mm) on the reinforcement surface and there are no defects,the reinforcement doesn’t corrode;

- under normal conditions, the pH of concrete is 12-13. At this pH, the reinforcement does not oxidize even in contact with water in the pores and capillaries of concrete. That is, itstays passive. Passivity is the resistance of a metal to corrosion. Substances that increase the passivity of the metal are called passivators or inhibitors (Ca(NO2)2, NaNO2, NaCrO4, KCrO4);

-the water diffusion and corrosion products is poor in dense concrete. Therefore, the corrosion of the reinforcement is slow;

-the use of additives that reduce the permeability of concrete (putty mixtures);

-coating of reinforcement with special protective layers (grease, paint), etc.

References

- Pashenko А.L. Fizicheskaya khimiya silikatov.-М.: VSh.1986,368p

- Boldyrev А.I. Fizicheskaya I kolloidnaya khimiya. .-М.: VSh.1983,346p

- Golikov G.А. Rukovodstvo po fiz.khimii. .-М.: VSh.1988,384p

- Frolov Yu.G. Kurs kolloidnoi khimii. .-М.:Khimiya.1989,275p

- Rarinov V.B. Khimiya v stroitelstve. – М.: Stroiizdat.1977.325p

- Kostornykh L.I. Dobavki v betony I stroitelnye rastvory. – RnD.: Izdatelstvo «Finiks». 2007. 221p

- YegemberdiyevaG.А. Polimeryvd/o. Uchebnoeposobie, Almaty, КazGASA,2004,108p

- KarieevV.А. Kratkiikursfiz.khimii.-М.: Khimiya,1978,622p

- RabukhinА.I., SavelevV.G. Fizicheskaya khimiya tugoplavkikh I silikatnykh soedinenii. Uchebnik. - М.: INFRA-М, 2004. – 304p.

- AnfilogovV.N.Silikatnyerasplavy / V.N.Anfigolov, V.N.Bykov, А.А. Osipov; In-tmineralogiiUroRAN. - М.: Nauka, 2005 – 357p.

- MolyukovaN.I., YegemberdiyevaG.А., NurgozhaevК.Kh. Analiticheskayakhimiya. Kachestvennyi analiz. Almaty, КаzGASA, 2000,27p.

- TravenV.F.Organicheskayakhimiya.-М.: INU«Akademkniga», 2004,1-kniga, 727p., 2-kniga,282p.

Rysdauletov Raimberdi

Mominova Saule

PHYSICAL CHEMISTRY OF BUILDING MATERIALS

Textbook

Approved for publication___  ____ 2021

(date, month, year)

Paper size 60х84 1/16,Offset. Volume 7,0p.sh.

Printed copies 500 exemplar. Order №_____

@ М.Auezov South Kazakhstan University